Etosha 22 CrySub 4-10 cm S1 REPLICATE

Graphics

Graphics

Graphics

Quantitative Results

Phase Sodium Aluminum Silicate Hydrate

Weight fraction/ %	22.0

Phase Calcium Carbonate

Weight fraction/ %	10.0

Phase Sodium Chloride

Weight fraction/ %	10.0

Phase Potassium Sodium Aluminum Silicate

Weight fraction/ %	11.0

Phase Potassium Magnesium Aluminum Silicate Fluoride Hydroxide

Weight fraction/ %	13.0

Phase Sodium Magnesium Silicon Oxide Hydrate

Weight fraction/ %	4.0

Phase Potassium Hydronium Magnesium Aluminum Silicon Oxide Hydroxide

Weight fraction/ %	29.0

Multiple Quantitative Results

Scans vs Phases Matrix

| Scan name | Sodium Aluminum Silicate Hydrate | Calcium Carbonate | Sodium Chloride | Potassium Sodium Aluminum Silicate | Potassium Magnesium Aluminum Silicate Fluoride Hydroxide | Sodium Magnesium Silicon Oxide Hydrate | Potassium Hydronium Magnesium Aluminum Silicon Oxide Hydroxide |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 10R ETOSHA 22 CRYSUB 4-10CM S1 REPLI | 22.0 | 10.0 | 10.0 | 11.0 | 13.0 | 4.0 | 29.0 |

Anchor Scan Data

| Pos. [°2θ] | Iobs [cts] | Icalc [cts] | Iback [cts] |
| --- | --- | --- | --- |
| 5.0064 | 8504.0000 | 8503.3818 | 8504.0000 |
| 5.0174 | 8588.2670 | 8488.4795 | 8487.0387 |
| 5.0284 | 8451.1632 | 8471.5267 | 8470.0775 |
| 5.0394 | 8529.3673 | 8454.5739 | 8453.1162 |
| 5.0504 | 8331.8191 | 8437.6212 | 8436.1550 |
| 5.0614 | 8373.2684 | 8420.6685 | 8419.1937 |
| 5.0724 | 8449.6785 | 8403.7160 | 8402.2325 |
| 5.0834 | 8229.5418 | 8386.7635 | 8385.2712 |
| 5.0944 | 8452.6775 | 8369.8111 | 8368.3100 |
| 5.1054 | 8312.0708 | 8352.8588 | 8351.3487 |
| 5.1164 | 8356.3618 | 8335.9065 | 8334.3875 |
| 5.1274 | 8165.7906 | 8318.9544 | 8317.4262 |
| 5.1384 | 8227.3038 | 8302.0023 | 8300.4650 |
| 5.1494 | 8115.5025 | 8285.0503 | 8283.5037 |
| 5.1604 | 8307.3382 | 8268.0984 | 8266.5425 |
| 5.1714 | 8171.7773 | 8251.1466 | 8249.5812 |
| 5.1824 | 8222.2045 | 8234.1948 | 8232.6200 |
| 5.1934 | 8140.4621 | 8217.2432 | 8215.6587 |
| 5.2044 | 8182.8496 | 8200.2916 | 8198.6975 |
| 5.2154 | 8073.9228 | 8183.3401 | 8181.7362 |
| 5.2264 | 7927.3363 | 8166.3887 | 8164.7750 |
| 5.2374 | 8008.1947 | 8149.4374 | 8147.8137 |
| 5.2484 | 8019.5103 | 8132.4862 | 8130.8525 |
| 5.2594 | 8012.1770 | 8115.5351 | 8113.8912 |
| 5.2704 | 7992.5723 | 8098.5841 | 8096.9300 |
| 5.2814 | 7906.4312 | 8081.6332 | 8079.9687 |
| 5.2924 | 7927.5998 | 8064.6823 | 8063.0075 |
| 5.3034 | 7871.3053 | 8047.7316 | 8046.0462 |
| 5.3144 | 7887.4415 | 8031.0220 | 8029.0850 |
| 5.3254 | 7902.9110 | 8019.1441 | 8012.1237 |
| 5.3364 | 7824.2360 | 8002.3931 | 7995.1625 |
| 5.3474 | 7719.9154 | 7988.0757 | 7978.2012 |
| 5.3584 | 7874.1770 | 7971.2466 | 7961.2400 |
| 5.3694 | 7872.8997 | 7954.4203 | 7944.2787 |
| 5.3804 | 7774.2822 | 7937.5969 | 7927.3175 |
| 5.3914 | 7759.7399 | 7920.7765 | 7910.3562 |
| 5.4024 | 7736.1416 | 7903.9592 | 7893.3950 |
| 5.4134 | 7783.3446 | 7887.1451 | 7876.4337 |
| 5.4244 | 7751.4789 | 7870.3342 | 7859.4725 |
| 5.4354 | 7678.3613 | 7853.5267 | 7842.5112 |
| 5.4464 | 7679.8201 | 7836.7227 | 7825.5500 |
| 5.4574 | 7737.1499 | 7819.9223 | 7808.5887 |
| 5.4684 | 7765.7876 | 7803.1256 | 7791.6275 |
| 5.4794 | 7789.6047 | 7786.3326 | 7774.6662 |
| 5.4904 | 7677.5319 | 7769.5437 | 7757.7050 |
| 5.5014 | 7684.5841 | 7752.7588 | 7740.7437 |
| 5.5124 | 7772.2271 | 7735.9780 | 7723.7825 |
| 5.5234 | 7649.6917 | 7719.2017 | 7706.8212 |
| 5.5344 | 7623.4159 | 7703.3738 | 7689.8600 |
| 5.5454 | 7706.4995 | 7693.4703 | 7680.7066 |
| 5.5564 | 7822.3284 | 7684.5157 | 7671.5531 |
| 5.5674 | 7717.8864 | 7675.5659 | 7662.3997 |
| 5.5784 | 7705.2832 | 7666.6213 | 7653.2463 |
| 5.5894 | 7651.7261 | 7657.6820 | 7644.0929 |
| 5.6004 | 7697.8850 | 7648.7482 | 7634.9394 |
| 5.6114 | 7636.1067 | 7639.8200 | 7625.7860 |
| 5.6224 | 7595.0777 | 7630.8977 | 7616.6326 |
| 5.6334 | 7519.7316 | 7621.9815 | 7607.4792 |
| 5.6444 | 7653.2399 | 7613.0716 | 7598.3257 |
| 5.6554 | 7728.9769 | 7604.1682 | 7589.1723 |
| 5.6664 | 7690.7021 | 7595.2716 | 7580.0189 |
| 5.6774 | 7611.5211 | 7586.3820 | 7570.8655 |
| 5.6884 | 7650.9636 | 7577.4997 | 7561.7121 |
| 5.6994 | 7734.2699 | 7568.6250 | 7552.5586 |
| 5.7104 | 7709.7355 | 7559.7581 | 7543.4052 |
| 5.7214 | 7681.2227 | 7550.8994 | 7534.2518 |
| 5.7324 | 7538.2832 | 7542.0491 | 7525.0984 |
| 5.7434 | 7635.2896 | 7533.2077 | 7515.9449 |
| 5.7544 | 7615.3599 | 7524.3754 | 7506.7915 |
| 5.7654 | 7504.2301 | 7515.5527 | 7497.6381 |
| 5.7764 | 7495.4641 | 7506.7399 | 7488.4847 |
| 5.7874 | 7628.7724 | 7497.9374 | 7479.3312 |
| 5.7984 | 7512.6017 | 7489.1457 | 7470.1778 |
| 5.8094 | 7613.4366 | 7480.3652 | 7461.0244 |
| 5.8204 | 7635.1858 | 7471.5964 | 7451.8710 |
| 5.8314 | 7714.3555 | 7462.8397 | 7442.7175 |
| 5.8424 | 7667.7552 | 7454.0959 | 7433.5641 |
| 5.8534 | 7558.9484 | 7445.3652 | 7424.4107 |
| 5.8644 | 7722.6903 | 7436.6485 | 7415.2573 |
| 5.8754 | 7848.4612 | 7427.9463 | 7406.1038 |
| 5.8864 | 7874.6155 | 7419.2592 | 7396.9504 |
| 5.8974 | 7832.1903 | 7410.5880 | 7387.7970 |
| 5.9084 | 7602.2272 | 7401.9334 | 7378.6436 |
| 5.9194 | 7755.4076 | 7393.2962 | 7369.4901 |
| 5.9304 | 7676.9292 | 7384.6771 | 7360.3367 |
| 5.9414 | 7647.1475 | 7376.0772 | 7351.1833 |
| 5.9524 | 7699.5015 | 7367.4973 | 7342.0299 |
| 5.9634 | 7798.8894 | 7358.9384 | 7332.8765 |
| 5.9744 | 7687.8781 | 7350.4015 | 7323.7230 |
| 5.9854 | 7676.3953 | 7341.8879 | 7314.5696 |
| 5.9964 | 7797.2743 | 7333.3986 | 7305.4162 |
| 6.0074 | 7815.4646 | 7324.9350 | 7296.2628 |
| 6.0184 | 7891.6628 | 7316.4984 | 7287.1093 |
| 6.0294 | 8011.4026 | 7308.0903 | 7277.9559 |
| 6.0404 | 7928.2163 | 7299.7122 | 7268.8025 |
| 6.0514 | 8047.6588 | 7291.3657 | 7259.6491 |
| 6.0624 | 7998.7138 | 7283.0150 | 7250.4956 |
| 6.0734 | 7829.2601 | 7274.4634 | 7241.0308 |
| 6.0844 | 7934.3628 | 7265.9115 | 7231.5659 |
| 6.0954 | 7956.7124 | 7257.3992 | 7222.1011 |
| 6.1064 | 7965.6165 | 7248.9287 | 7212.6362 |
| 6.1174 | 8040.6185 | 7240.5025 | 7203.1713 |
| 6.1284 | 8003.1387 | 7232.1234 | 7193.7065 |
| 6.1394 | 8120.4950 | 7223.7943 | 7184.2416 |
| 6.1504 | 7958.2960 | 7215.5183 | 7174.7767 |
| 6.1614 | 8001.2714 | 7207.2988 | 7165.3119 |
| 6.1724 | 8096.7247 | 7199.1394 | 7155.8470 |
| 6.1834 | 8193.1706 | 7191.0442 | 7146.3822 |
| 6.1944 | 8131.5310 | 7183.0174 | 7136.9173 |
| 6.2054 | 8102.1563 | 7175.0637 | 7127.4524 |
| 6.2164 | 8089.6274 | 7167.1881 | 7117.9876 |
| 6.2274 | 8262.3378 | 7159.3961 | 7108.5227 |
| 6.2384 | 8258.8485 | 7151.6939 | 7099.0579 |
| 6.2494 | 8257.9445 | 7144.0878 | 7089.5930 |
| 6.2604 | 8364.2183 | 7136.5851 | 7080.1281 |
| 6.2714 | 8326.1647 | 7129.1936 | 7070.6633 |
| 6.2824 | 8518.3816 | 7121.9219 | 7061.1984 |
| 6.2934 | 8537.7654 | 7114.7794 | 7051.7335 |
| 6.3044 | 8493.1495 | 7107.7764 | 7042.2687 |
| 6.3154 | 8636.2704 | 7100.9244 | 7032.8038 |
| 6.3264 | 8703.0118 | 7094.2360 | 7023.3390 |
| 6.3374 | 8751.2016 | 7087.7252 | 7013.8741 |
| 6.3484 | 8731.4720 | 7081.4073 | 7004.4092 |
| 6.3594 | 8842.3997 | 7075.2995 | 6994.9444 |
| 6.3704 | 8789.4532 | 7069.4209 | 6985.4795 |
| 6.3814 | 8830.3781 | 7063.7928 | 6976.0147 |
| 6.3924 | 9054.5930 | 7058.4390 | 6966.5498 |
| 6.4034 | 9091.3422 | 7053.3861 | 6957.0849 |
| 6.4144 | 9065.0000 | 7048.6641 | 6947.6201 |
| 6.4254 | 9140.5354 | 7044.3066 | 6938.1552 |
| 6.4364 | 9326.1220 | 7040.3518 | 6928.6903 |
| 6.4474 | 9374.7315 | 7036.8427 | 6919.2255 |
| 6.4584 | 9433.6490 | 7033.8283 | 6909.7606 |
| 6.4694 | 9608.7685 | 7031.3645 | 6900.2958 |
| 6.4804 | 9627.5929 | 7029.5150 | 6890.8309 |
| 6.4914 | 9676.7965 | 7028.3533 | 6881.3660 |
| 6.5024 | 9733.7896 | 7027.9642 | 6871.9012 |
| 6.5134 | 9920.4912 | 7028.4464 | 6862.4363 |
| 6.5244 | 10044.7699 | 7029.9163 | 6852.9715 |
| 6.5354 | 10194.0645 | 7032.5126 | 6843.5066 |
| 6.5464 | 10245.8378 | 7036.4045 | 6834.0417 |
| 6.5574 | 10322.7021 | 7041.8030 | 6824.5769 |
| 6.5684 | 10311.4975 | 7048.9800 | 6815.1120 |
| 6.5794 | 10527.5591 | 7058.2956 | 6805.6472 |
| 6.5904 | 10637.9558 | 7070.2118 | 6796.1823 |
| 6.6014 | 10670.9017 | 7085.2547 | 6786.4655 |
| 6.6124 | 10845.4327 | 7104.5546 | 6776.7487 |
| 6.6234 | 10860.7625 | 7129.5133 | 6767.0320 |
| 6.6344 | 10972.7660 | 7162.0514 | 6757.3152 |
| 6.6454 | 11009.8078 | 7204.8107 | 6747.5984 |
| 6.6564 | 11128.4248 | 7261.3306 | 6737.8816 |
| 6.6674 | 11276.6805 | 7336.1984 | 6728.1649 |
| 6.6784 | 11408.2665 | 7435.1266 | 6718.4481 |
| 6.6894 | 11432.0443 | 7564.9008 | 6708.7313 |
| 6.7004 | 11600.8506 | 7733.1378 | 6699.0145 |
| 6.7114 | 11592.0364 | 7947.8067 | 6689.2978 |
| 6.7224 | 11768.8113 | 8216.4879 | 6679.5810 |
| 6.7334 | 11692.9601 | 8545.3829 | 6669.8642 |
| 6.7444 | 11823.5300 | 8938.1151 | 6660.1474 |
| 6.7554 | 11782.3776 | 9394.3652 | 6650.4307 |
| 6.7664 | 11892.1220 | 9908.3393 | 6640.7139 |
| 6.7774 | 12043.8078 | 10466.9911 | 6630.9971 |
| 6.7884 | 11993.4779 | 11047.9293 | 6621.2803 |
| 6.7994 | 12097.2719 | 11617.3049 | 6611.5635 |
| 6.8104 | 12176.8810 | 12129.0353 | 6601.8468 |
| 6.8214 | 12226.6474 | 12528.1787 | 6592.1300 |
| 6.8324 | 12045.0718 | 12761.1959 | 6582.4132 |
| 6.8434 | 12147.7867 | 12791.6760 | 6572.6964 |
| 6.8544 | 12248.3009 | 12613.6621 | 6562.9797 |
| 6.8654 | 12186.5865 | 12253.7044 | 6553.2629 |
| 6.8764 | 12066.5830 | 11760.4804 | 6543.5461 |
| 6.8874 | 11851.2920 | 11189.3097 | 6533.8293 |
| 6.8984 | 11696.9390 | 10589.9232 | 6524.1126 |
| 6.9094 | 11710.4838 | 10000.7995 | 6514.3958 |
| 6.9204 | 11706.7935 | 9448.5820 | 6504.6790 |
| 6.9314 | 11753.3771 | 8949.7628 | 6494.9622 |
| 6.9424 | 11744.0491 | 8512.7924 | 6485.2455 |
| 6.9534 | 11555.2566 | 8139.9689 | 6475.5287 |
| 6.9644 | 11458.7679 | 7829.0614 | 6465.8119 |
| 6.9754 | 11302.3810 | 7574.7435 | 6456.0951 |
| 6.9864 | 11170.7257 | 7369.8645 | 6446.3784 |
| 6.9974 | 11186.6970 | 7206.5264 | 6436.6616 |
| 7.0084 | 10905.2644 | 7076.9234 | 6426.9448 |
| 7.0194 | 10703.1622 | 6973.9202 | 6417.2280 |
| 7.0304 | 10520.4759 | 6891.3804 | 6407.5113 |
| 7.0414 | 10443.6155 | 6824.2864 | 6397.7945 |
| 7.0524 | 10341.8141 | 6768.7059 | 6388.0777 |
| 7.0634 | 10262.7330 | 6721.6652 | 6378.3609 |
| 7.0744 | 10104.1375 | 6680.9799 | 6368.6441 |
| 7.0854 | 9808.5797 | 6645.0793 | 6358.9274 |
| 7.0964 | 9806.6991 | 6612.8488 | 6349.2106 |
| 7.1074 | 9671.9788 | 6583.5000 | 6339.4938 |
| 7.1184 | 9531.9055 | 6556.4708 | 6329.7770 |
| 7.1294 | 9376.6244 | 6531.3537 | 6320.0603 |
| 7.1404 | 9234.8141 | 6507.8450 | 6310.3435 |
| 7.1514 | 8981.3775 | 6485.7118 | 6300.6267 |
| 7.1624 | 8802.8259 | 6464.7698 | 6290.9099 |
| 7.1734 | 8659.1303 | 6444.8690 | 6281.1932 |
| 7.1844 | 8591.2920 | 6425.8849 | 6271.4764 |
| 7.1954 | 8502.8692 | 6407.7123 | 6261.7596 |

Scan List

| Vis. | Dataset Name | Start pos. [°2θ] | End pos. [°2θ] | Step [°2θ] | Meas.Date/Time |
| --- | --- | --- | --- | --- | --- |
| * | 10R ETOSHA 22 CRYSUB 4-10CM S1 REPLI | 5.0064 | 84.9874 | 0.0110 | 8/23/2023 11:50:14 AM |

Peak List

| Pos. [°2θ] | Height [cts] | FWHM Left [°2θ] | d-spacing [Å] | Rel. Int. [%] |
| --- | --- | --- | --- | --- |
| 6.8344 | 5607.63 | 0.1515 | 12.92311 | 52.04 |
| 8.7899 | 779.64 | 0.4330 | 10.05205 | 7.23 |
| 11.6491 | 403.21 | 0.2165 | 7.59045 | 3.74 |
| 13.5918 | 128.61 | 0.5196 | 6.50961 | 1.19 |
| 15.8340 | 7716.94 | 0.0866 | 5.59248 | 71.61 |
| 18.3116 | 1351.88 | 0.1299 | 4.84102 | 12.55 |
| 19.8224 | 3289.92 | 0.1948 | 4.47531 | 30.53 |
| 20.9685 | 962.06 | 0.1082 | 4.23323 | 8.93 |
| 21.4078 | 798.20 | 0.2165 | 4.14734 | 7.41 |
| 22.5237 | 118.84 | 0.1732 | 3.94433 | 1.10 |
| 23.0547 | 750.14 | 0.1082 | 3.85466 | 6.96 |
| 23.4860 | 1278.43 | 0.1515 | 3.78485 | 11.86 |
| 24.2846 | 525.48 | 0.1732 | 3.66216 | 4.88 |
| 25.9979 | 10776.04 | 0.1515 | 3.42456 | 100.00 |
| 26.8067 | 1276.65 | 0.1515 | 3.32305 | 11.85 |
| 27.0886 | 932.20 | 0.1082 | 3.28910 | 8.65 |
| 27.3547 | 1239.13 | 0.1082 | 3.25771 | 11.50 |
| 27.6051 | 904.12 | 0.1299 | 3.22873 | 8.39 |
| 29.3955 | 6835.24 | 0.1188 | 3.03602 | 63.43 |
| 29.4601 | 5987.87 | 0.0660 | 3.02951 | 55.57 |
| 29.7732 | 703.67 | 0.1584 | 2.99836 | 6.53 |
| 30.5794 | 5233.48 | 0.1188 | 2.92112 | 48.57 |
| 31.6903 | 10698.63 | 0.0792 | 2.82121 | 99.28 |
| 31.7811 | 5075.87 | 0.0396 | 2.81336 | 47.10 |
| 33.3198 | 1351.64 | 0.2112 | 2.68687 | 12.54 |
| 34.3464 | 1462.11 | 0.2112 | 2.60887 | 13.57 |
| 34.7401 | 2479.85 | 0.2376 | 2.58020 | 23.01 |
| 35.9571 | 2351.67 | 0.2112 | 2.49562 | 21.82 |
| 37.0635 | 1214.59 | 0.1320 | 2.42362 | 11.27 |
| 39.4363 | 1302.42 | 0.1320 | 2.28309 | 12.09 |
| 40.5225 | 705.63 | 0.2376 | 2.22436 | 6.55 |
| 41.5906 | 228.05 | 0.2640 | 2.16967 | 2.12 |
| 43.1526 | 888.58 | 0.2112 | 2.09468 | 8.25 |
| 45.4305 | 4892.54 | 0.0924 | 1.99481 | 45.40 |
| 45.5466 | 2754.31 | 0.0528 | 1.98999 | 25.56 |
| 47.1032 | 358.03 | 0.1584 | 1.92780 | 3.32 |
| 47.5072 | 900.33 | 0.2112 | 1.91234 | 8.35 |
| 47.8460 | 1017.44 | 0.1584 | 1.89959 | 9.44 |
| 48.4771 | 912.22 | 0.1056 | 1.87632 | 8.47 |
| 50.7571 | 92.81 | 0.4224 | 1.79726 | 0.86 |
| 52.5477 | 1243.59 | 0.1320 | 1.74015 | 11.54 |
| 53.4689 | 433.00 | 0.2112 | 1.71232 | 4.02 |
| 54.3487 | 486.68 | 0.2112 | 1.68666 | 4.52 |
| 55.2646 | 195.94 | 0.4224 | 1.66086 | 1.82 |
| 56.4299 | 924.40 | 0.0924 | 1.62929 | 8.58 |
| 57.4395 | 451.34 | 0.2112 | 1.60303 | 4.19 |
| 57.8448 | 482.02 | 0.2112 | 1.59276 | 4.47 |
| 60.6809 | 838.36 | 0.7392 | 1.52493 | 7.78 |
| 61.3792 | 800.92 | 0.3696 | 1.50925 | 7.43 |
| 62.9189 | 191.51 | 0.4224 | 1.47597 | 1.78 |
| 64.7055 | 244.10 | 0.4224 | 1.43946 | 2.27 |
| 66.1848 | 756.77 | 0.1320 | 1.41083 | 7.02 |
| 68.4733 | 95.55 | 0.3168 | 1.36915 | 0.89 |
| 69.1813 | 552.69 | 0.1584 | 1.35685 | 5.13 |
| 72.3451 | 386.76 | 0.4224 | 1.30511 | 3.59 |
| 73.8582 | 272.34 | 0.2640 | 1.28207 | 2.53 |
| 75.2567 | 926.84 | 0.0924 | 1.26168 | 8.60 |
| 78.2939 | 345.93 | 0.3168 | 1.22016 | 3.21 |
| 81.2816 | 132.85 | 0.5280 | 1.18268 | 1.23 |
| 82.6440 | 100.32 | 0.4224 | 1.16661 | 0.93 |
| 83.9301 | 492.73 | 0.1584 | 1.15197 | 4.57 |

Pattern List

| Visible | Ref.Code | Score | Compound Name | Chem. Formula | Mineral Name | SemiQuant[%] |
| --- | --- | --- | --- | --- | --- | --- |
| * | 01-075-8690 | 72 | Sodium Aluminum Silicate Hydrate | Na1.71 ( ( Al1.806 Si4.194 ) O12 ) ( H2 O )2.16 | Analcime | 22 |
| * | 01-083-1762 | 58 | Calcium Carbonate | Ca ( C O3 ) | Calcite | 10 |
| * | 01-085-8594 | 47 | Sodium Chloride | Na Cl | Halite | 10 |
| * | 01-086-0682 | 22 | Potassium Sodium Aluminum Silicate | ( K0.831 Na0.169 ) ( Al Si3 O8 ) | Sanidine | 11 |
| * | 04-013-9383 | 25 | Potassium Magnesium Aluminum Silicate Fluoride Hydroxide | K Mg3 Al Si3 O10 ( O H ) F | Phlogopite-2M1 | 13 |
| * | 01-082-8023 | 35 | Sodium Magnesium Silicon Oxide Hydrate | Na2 Mg3 ( Si6 O16 ) ( H2 O )7 | Loughlinite | 4 |
| * | 04-018-6570 | 21 | Potassium Hydronium Magnesium Aluminum Silicon Oxide Hydroxide | K0.97 ( H3 O )0.03 Mg0.4 Al2.2 Si3.4 O10 ( O H )2 | Muscovite-2M1 | 29 |

Anchor Scan Parameters

Dataset Name	10R ETOSHA 22 CRYSUB 4-10CM S1 REPLI

File name	C:\aeris_data\XRD data\Goldstein\10R ETOSHA 22 CRYSUB 4-10CM S1 REPLI.xrdml

Sample Identification	10R ETOSHA 22 CRYSUB 4-10CM S1 REPLI

Measurement Start Date/Time	8/23/2023 11:50:14 AM

Operator	Instrument

Raw Data Origin	XRD measurement (*.XRDML)

Scan Axis	Gonio

Start Position [°2θ]	5.0064

End Position [°2θ]	84.9874

Step Size [°2θ]	0.0110

Scan Step Time [s]	48.1950

Scan Type	Continuous

PSD Mode	Scanning

PSD Length [°2θ]	5.54

Offset [°2θ]	0.0000

Divergence Slit Type	Fixed

Divergence Slit Size [°]	0.4584

Specimen Length [mm]	10.00

Measurement Temperature [°C]	25.00

Anode Material	Cu

K-α1 [Å]	1.54060

K-α2 [Å]	1.54443

K-β1 [Å]	1.39225

K-A2 / K-A1 Ratio	0.50000

Generator Settings	15 mA, 40 kV

Diffractometer Type	2082464

Diffractometer Number	0

Goniometer Radius [mm]	145.00

Dist. Focus-Diverg. Slit [mm]	95.00

Incident Beam Monochromator	No

Spinning	Yes