Etosha 22 MoiSub 10-15 cm S1

Graphics

Graphics

Graphics

Quantitative Results

Phase Sodium Aluminum Silicate Hydrate

Weight fraction/ %	20.0

Phase Calcium Carbonate

Weight fraction/ %	14.0

Phase Sodium Chloride

Weight fraction/ %	6.0

Phase Sodium Magnesium Silicon Oxide Hydrate

Weight fraction/ %	5.0

Phase Potassium Aluminum Silicate

Weight fraction/ %	11.0

Phase Cobalt Iron Oxide Hydroxide

Weight fraction/ %	2.0

Phase Potassium Magnesium Aluminum Silicate Fluoride Hydroxide

Weight fraction/ %	14.0

Phase Potassium Hydronium Magnesium Aluminum Silicon Oxide Hydroxide

Weight fraction/ %	29.0

Multiple Quantitative Results

Scans vs Phases Matrix

| Scan name | Sodium Aluminum Silicate Hydrate | Calcium Carbonate | Sodium Chloride | Sodium Magnesium Silicon Oxide Hydrate | Potassium Aluminum Silicate | Cobalt Iron Oxide Hydroxide | Potassium Magnesium Aluminum Silicate Fluoride Hydroxide | Potassium Hydronium Magnesium Aluminum Silicon Oxide Hydroxide |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 11 ETOSHA 22 MOISUB 10-15CM S1 | 20.0 | 14.0 | 6.0 | 5.0 | 11.0 | 2.0 | 14.0 | 29.0 |

Anchor Scan Data

| Pos. [°2θ] | Iobs [cts] | Icalc [cts] | Iback [cts] |
| --- | --- | --- | --- |
| 5.0064 | 8219.0000 | 8213.3650 | 8219.0000 |
| 5.0174 | 8121.0737 | 8199.8600 | 8199.8600 |
| 5.0284 | 8130.2203 | 8180.7199 | 8180.7199 |
| 5.0394 | 8253.7965 | 8161.5799 | 8161.5799 |
| 5.0504 | 8133.8722 | 8142.4399 | 8142.4399 |
| 5.0614 | 7945.5590 | 8123.2998 | 8123.2998 |
| 5.0724 | 8059.9676 | 8104.1598 | 8104.1598 |
| 5.0834 | 8039.2566 | 8085.0198 | 8085.0198 |
| 5.0944 | 7951.6903 | 8065.8797 | 8065.8797 |
| 5.1054 | 7922.2478 | 8046.7397 | 8046.7397 |
| 5.1164 | 8032.7522 | 8027.5997 | 8027.5997 |
| 5.1274 | 7722.0025 | 8008.4596 | 8008.4596 |
| 5.1384 | 7761.2271 | 7989.3196 | 7989.3196 |
| 5.1494 | 7806.3555 | 7970.1796 | 7970.1796 |
| 5.1604 | 7821.9351 | 7951.0395 | 7951.0395 |
| 5.1714 | 7837.6268 | 7931.8995 | 7931.8995 |
| 5.1824 | 7957.6863 | 7912.7595 | 7912.7595 |
| 5.1934 | 7932.7630 | 7893.6194 | 7893.6194 |
| 5.2044 | 7703.8053 | 7874.4794 | 7874.4794 |
| 5.2154 | 7627.8619 | 7855.3394 | 7855.3394 |
| 5.2264 | 7687.8692 | 7836.1993 | 7836.1993 |
| 5.2374 | 7575.9115 | 7817.0593 | 7817.0593 |
| 5.2484 | 7677.9597 | 7797.9193 | 7797.9193 |
| 5.2594 | 7594.5403 | 7778.7792 | 7778.7792 |
| 5.2704 | 7629.6519 | 7759.6392 | 7759.6392 |
| 5.2814 | 7689.1190 | 7740.5487 | 7740.4992 |
| 5.2924 | 7506.6588 | 7721.9620 | 7721.3591 |
| 5.3034 | 7591.7699 | 7702.8506 | 7702.2191 |
| 5.3144 | 7660.5526 | 7683.9912 | 7683.0791 |
| 5.3254 | 7568.0492 | 7664.8570 | 7663.9390 |
| 5.3364 | 7531.4808 | 7645.7229 | 7644.7990 |
| 5.3474 | 7530.3781 | 7626.5888 | 7625.6590 |
| 5.3584 | 7460.5555 | 7607.4548 | 7606.5189 |
| 5.3694 | 7409.4410 | 7588.3208 | 7587.3789 |
| 5.3804 | 7412.8515 | 7569.1869 | 7568.2389 |
| 5.3914 | 7431.0413 | 7550.0531 | 7549.0988 |
| 5.4024 | 7433.6106 | 7530.9193 | 7529.9588 |
| 5.4134 | 7356.8191 | 7511.7856 | 7510.8188 |
| 5.4244 | 7392.6283 | 7492.6520 | 7491.6787 |
| 5.4354 | 7313.0796 | 7473.5184 | 7472.5387 |
| 5.4464 | 7268.0875 | 7454.3848 | 7453.3987 |
| 5.4574 | 7412.9602 | 7435.2514 | 7434.2586 |
| 5.4684 | 7443.1239 | 7416.1180 | 7415.1186 |
| 5.4794 | 7359.3918 | 7396.9847 | 7395.9786 |
| 5.4904 | 7304.2144 | 7377.8514 | 7376.8385 |
| 5.5014 | 7308.1903 | 7358.7182 | 7357.6985 |
| 5.5124 | 7297.0383 | 7339.5851 | 7338.5585 |
| 5.5234 | 7292.0875 | 7320.4521 | 7319.4184 |
| 5.5344 | 7375.2861 | 7304.2651 | 7300.2784 |
| 5.5454 | 7297.1047 | 7292.1927 | 7291.1449 |
| 5.5564 | 7170.0541 | 7283.0664 | 7282.0114 |
| 5.5674 | 7179.4764 | 7273.9402 | 7272.8779 |
| 5.5784 | 7265.8309 | 7264.8140 | 7263.7443 |
| 5.5894 | 7297.1372 | 7255.6879 | 7254.6108 |
| 5.6004 | 7292.0088 | 7246.5619 | 7245.4773 |
| 5.6114 | 7318.7163 | 7237.4360 | 7236.3438 |
| 5.6224 | 7247.3392 | 7228.3102 | 7227.2103 |
| 5.6334 | 7348.4174 | 7219.1844 | 7218.0768 |
| 5.6444 | 7275.4041 | 7210.0587 | 7208.9433 |
| 5.6554 | 7269.1362 | 7200.9331 | 7199.8098 |
| 5.6664 | 7352.6342 | 7191.8076 | 7190.6763 |
| 5.6774 | 7265.0364 | 7182.6822 | 7181.5428 |
| 5.6884 | 7300.3943 | 7173.5568 | 7172.4093 |
| 5.6994 | 7162.7124 | 7164.4316 | 7163.2757 |
| 5.7104 | 7345.6952 | 7155.3064 | 7154.1422 |
| 5.7214 | 7324.9125 | 7146.1814 | 7145.0087 |
| 5.7324 | 7378.6313 | 7137.0564 | 7135.8752 |
| 5.7434 | 7250.2404 | 7133.3347 | 7126.7417 |
| 5.7544 | 7252.4317 | 7124.4755 | 7117.6082 |
| 5.7654 | 7176.7360 | 7118.1958 | 7108.4747 |
| 5.7764 | 7360.7463 | 7109.3273 | 7099.3412 |
| 5.7874 | 7265.5909 | 7100.3884 | 7090.2077 |
| 5.7984 | 7278.8584 | 7091.4555 | 7081.0742 |
| 5.8094 | 7166.3579 | 7082.5290 | 7071.9406 |
| 5.8204 | 7232.1298 | 7073.6090 | 7062.8071 |
| 5.8314 | 7218.7979 | 7064.6959 | 7053.6736 |
| 5.8424 | 7300.1367 | 7055.7899 | 7044.5401 |
| 5.8534 | 7370.3560 | 7046.8915 | 7035.4066 |
| 5.8644 | 7328.9410 | 7038.0009 | 7026.2731 |
| 5.8754 | 7376.5207 | 7029.1184 | 7017.1396 |
| 5.8864 | 7209.8584 | 7020.2445 | 7008.0061 |
| 5.8974 | 7407.1106 | 7011.3796 | 6998.8726 |
| 5.9084 | 7393.7011 | 7002.5241 | 6989.7391 |
| 5.9194 | 7356.8869 | 6993.6785 | 6980.6055 |
| 5.9304 | 7401.0384 | 6984.8431 | 6971.4720 |
| 5.9414 | 7436.8766 | 6976.0186 | 6962.3385 |
| 5.9524 | 7544.9921 | 6967.2054 | 6953.2050 |
| 5.9634 | 7613.6342 | 6958.4042 | 6944.0715 |
| 5.9744 | 7640.4307 | 6949.6155 | 6934.9380 |
| 5.9854 | 7544.4695 | 6940.8400 | 6925.8045 |
| 5.9964 | 7542.7345 | 6932.0784 | 6916.6710 |
| 6.0074 | 7489.0521 | 6923.3314 | 6907.5375 |
| 6.0184 | 7478.4690 | 6914.5999 | 6898.4040 |
| 6.0294 | 7435.3997 | 6905.8846 | 6889.2704 |
| 6.0404 | 7384.3383 | 6897.1864 | 6880.1369 |
| 6.0514 | 7725.0496 | 6888.5064 | 6871.0034 |
| 6.0624 | 7626.7198 | 6879.7655 | 6861.8699 |
| 6.0734 | 7620.9651 | 6870.9332 | 6852.4648 |
| 6.0844 | 7608.5654 | 6862.0424 | 6843.0596 |
| 6.0954 | 7702.3628 | 6853.1743 | 6833.6544 |
| 6.1064 | 7721.1770 | 6844.3303 | 6824.2493 |
| 6.1174 | 7795.0649 | 6835.5119 | 6814.8441 |
| 6.1284 | 7679.9735 | 6826.7206 | 6805.4390 |
| 6.1394 | 7821.4105 | 6817.9583 | 6796.0338 |
| 6.1504 | 7708.6274 | 6809.2267 | 6786.6286 |
| 6.1614 | 7846.5428 | 6800.5279 | 6777.2235 |
| 6.1724 | 7908.1317 | 6791.8640 | 6767.8183 |
| 6.1834 | 7933.4951 | 6783.2374 | 6758.4131 |
| 6.1944 | 8034.1239 | 6774.6507 | 6749.0080 |
| 6.2054 | 7965.4027 | 6766.1066 | 6739.6028 |
| 6.2164 | 8011.5762 | 6757.6083 | 6730.1977 |
| 6.2274 | 8059.7095 | 6749.1590 | 6720.7925 |
| 6.2384 | 8139.9213 | 6740.7624 | 6711.3873 |
| 6.2494 | 8170.8333 | 6732.4224 | 6701.9822 |
| 6.2604 | 8203.4366 | 6724.1433 | 6692.5770 |
| 6.2714 | 8208.7689 | 6715.9300 | 6683.1719 |
| 6.2824 | 8309.2134 | 6707.7876 | 6673.7667 |
| 6.2934 | 8438.8982 | 6699.7220 | 6664.3615 |
| 6.3044 | 8460.2468 | 6691.7395 | 6654.9564 |
| 6.3154 | 8452.6509 | 6683.8472 | 6645.5512 |
| 6.3264 | 8376.4720 | 6676.0529 | 6636.1461 |
| 6.3374 | 8576.8088 | 6668.3653 | 6626.7409 |
| 6.3484 | 8687.0767 | 6660.7939 | 6617.3357 |
| 6.3594 | 8656.5974 | 6653.3497 | 6607.9306 |
| 6.3704 | 8732.9214 | 6646.0445 | 6598.5254 |
| 6.3814 | 8762.6091 | 6638.8920 | 6589.1203 |
| 6.3924 | 8773.3274 | 6631.9072 | 6579.7151 |
| 6.4034 | 8899.9243 | 6625.1074 | 6570.3099 |
| 6.4144 | 9013.6372 | 6618.5116 | 6560.9048 |
| 6.4254 | 9073.5015 | 6612.1420 | 6551.4996 |
| 6.4364 | 9186.9037 | 6606.0232 | 6542.0945 |
| 6.4474 | 9276.7773 | 6600.1838 | 6532.6893 |
| 6.4584 | 9317.6726 | 6594.6561 | 6523.2841 |
| 6.4694 | 9427.3801 | 6589.4775 | 6513.8790 |
| 6.4804 | 9513.7621 | 6584.6909 | 6504.4738 |
| 6.4914 | 9625.5974 | 6580.3463 | 6495.0686 |
| 6.5024 | 9704.5497 | 6576.5013 | 6485.6635 |
| 6.5134 | 9707.3741 | 6573.2237 | 6476.2583 |
| 6.5244 | 9804.3363 | 6570.5926 | 6466.8532 |
| 6.5354 | 9907.8019 | 6568.7014 | 6457.4480 |
| 6.5464 | 9863.5290 | 6567.6610 | 6448.0428 |
| 6.5574 | 10067.9072 | 6567.6033 | 6438.6377 |
| 6.5684 | 10339.8231 | 6568.6866 | 6429.2325 |
| 6.5794 | 10397.1814 | 6571.1023 | 6419.8274 |
| 6.5904 | 10473.5310 | 6574.9643 | 6410.4222 |
| 6.6014 | 10621.3702 | 6580.7008 | 6400.7974 |
| 6.6124 | 10751.3393 | 6588.5391 | 6391.1726 |
| 6.6234 | 10888.1431 | 6599.0790 | 6381.5478 |
| 6.6344 | 10900.2566 | 6613.0090 | 6371.9230 |
| 6.6454 | 10926.0978 | 6631.3185 | 6362.2982 |
| 6.6564 | 10892.3481 | 6655.3678 | 6352.6734 |
| 6.6674 | 11004.8329 | 6687.6367 | 6343.0486 |
| 6.6784 | 11343.6442 | 6731.9996 | 6333.4238 |
| 6.6894 | 11614.7744 | 6794.5282 | 6323.7990 |
| 6.7004 | 11502.1484 | 6884.6128 | 6314.1742 |
| 6.7114 | 11456.9415 | 7015.6535 | 6304.5494 |
| 6.7224 | 11516.3835 | 7205.3841 | 6294.9246 |
| 6.7334 | 11751.6348 | 7475.0168 | 6285.2998 |
| 6.7444 | 11664.4395 | 7846.7019 | 6275.6750 |
| 6.7554 | 11770.6048 | 8339.0499 | 6266.0502 |
| 6.7664 | 11785.6657 | 8960.8900 | 6256.4254 |
| 6.7774 | 11820.2601 | 9703.5662 | 6246.8006 |
| 6.7884 | 11948.8584 | 10531.5487 | 6237.1758 |
| 6.7994 | 12059.2650 | 11371.1531 | 6227.5510 |
| 6.8104 | 12134.6784 | 12102.8372 | 6217.9261 |
| 6.8214 | 12047.9085 | 12577.0047 | 6208.3013 |
| 6.8324 | 11914.5468 | 12672.0303 | 6198.6765 |
| 6.8434 | 12114.2124 | 12362.3469 | 6189.0517 |
| 6.8544 | 12028.2182 | 11730.6068 | 6179.4269 |
| 6.8654 | 11773.3894 | 10916.9168 | 6169.8021 |
| 6.8764 | 11776.6676 | 10056.3871 | 6160.1773 |
| 6.8874 | 11649.8540 | 9245.5922 | 6150.5525 |
| 6.8984 | 11714.6548 | 8539.2873 | 6140.9277 |
| 6.9094 | 11601.0182 | 7959.6039 | 6131.3029 |
| 6.9204 | 11540.8732 | 7506.2591 | 6121.6781 |
| 6.9314 | 11557.0589 | 7165.1949 | 6112.0533 |
| 6.9424 | 11326.0845 | 6915.6853 | 6102.4285 |
| 6.9534 | 11247.2728 | 6735.7805 | 6092.8037 |
| 6.9644 | 11120.6164 | 6605.8387 | 6083.1789 |
| 6.9754 | 10902.5850 | 6510.2068 | 6073.5541 |
| 6.9864 | 10797.9912 | 6437.4748 | 6063.9293 |
| 6.9974 | 10822.5796 | 6379.8904 | 6054.3045 |
| 7.0084 | 10667.4877 | 6332.4541 | 6044.6797 |
| 7.0194 | 10490.3096 | 6292.0424 | 6035.0549 |
| 7.0304 | 10156.4297 | 6256.7167 | 6025.4301 |
| 7.0414 | 10061.8279 | 6225.2483 | 6015.8053 |
| 7.0524 | 9985.7670 | 6196.8224 | 6006.1805 |
| 7.0634 | 9938.0220 | 6170.8669 | 5996.5557 |
| 7.0744 | 9594.5604 | 6146.9571 | 5986.9309 |
| 7.0854 | 9480.1371 | 6124.7643 | 5977.3061 |
| 7.0964 | 9227.6744 | 6104.0261 | 5967.6813 |
| 7.1074 | 9040.4543 | 6084.5293 | 5958.0565 |
| 7.1184 | 8972.0441 | 6066.0987 | 5948.4317 |
| 7.1294 | 8819.0886 | 6048.5885 | 5938.8069 |
| 7.1404 | 8914.4818 | 6031.8769 | 5929.1821 |
| 7.1514 | 8703.8480 | 6015.8617 | 5919.5573 |
| 7.1624 | 8535.1790 | 6000.4561 | 5909.9325 |
| 7.1734 | 8390.5608 | 5985.5866 | 5900.3077 |
| 7.1844 | 8106.6106 | 5971.1902 | 5890.6829 |
| 7.1954 | 8016.1784 | 5957.2130 | 5881.0581 |

Scan List

| Vis. | Dataset Name | Start pos. [°2θ] | End pos. [°2θ] | Step [°2θ] | Meas.Date/Time |
| --- | --- | --- | --- | --- | --- |
| * | 11 ETOSHA 22 MOISUB 10-15CM S1 | 5.0064 | 84.9874 | 0.0110 | 8/23/2023 12:51:11 PM |

Peak List

| Pos. [°2θ] | Height [cts] | FWHM Left [°2θ] | d-spacing [Å] | Rel. Int. [%] |
| --- | --- | --- | --- | --- |
| 6.8243 | 5893.82 | 0.1082 | 12.94237 | 59.67 |
| 8.7456 | 637.75 | 0.3464 | 10.10280 | 6.46 |
| 11.6746 | 363.71 | 0.2598 | 7.57396 | 3.68 |
| 13.5666 | 112.94 | 0.6927 | 6.52160 | 1.14 |
| 15.8317 | 7033.75 | 0.1082 | 5.59330 | 71.21 |
| 18.2943 | 1337.99 | 0.1082 | 4.84553 | 13.55 |
| 19.8655 | 2950.52 | 0.1948 | 4.46569 | 29.87 |
| 20.9420 | 993.94 | 0.1082 | 4.23852 | 10.06 |
| 21.4162 | 764.39 | 0.1732 | 4.14573 | 7.74 |
| 22.4874 | 125.05 | 0.1299 | 3.95061 | 1.27 |
| 23.0556 | 1020.91 | 0.1082 | 3.85451 | 10.34 |
| 23.4749 | 1246.60 | 0.1732 | 3.78660 | 12.62 |
| 24.2789 | 590.07 | 0.0866 | 3.66301 | 5.97 |
| 25.9916 | 9877.66 | 0.1299 | 3.42538 | 100.00 |
| 26.8048 | 1324.88 | 0.1299 | 3.32328 | 13.41 |
| 27.0768 | 934.16 | 0.1082 | 3.29051 | 9.46 |
| 27.3386 | 1252.61 | 0.1299 | 3.25959 | 12.68 |
| 27.6114 | 884.65 | 0.1299 | 3.22800 | 8.96 |
| 29.3794 | 9188.77 | 0.0924 | 3.03765 | 93.03 |
| 29.4493 | 7891.75 | 0.0660 | 3.03060 | 79.89 |
| 29.7969 | 785.51 | 0.1320 | 2.99603 | 7.95 |
| 30.5677 | 4830.08 | 0.1452 | 2.92221 | 48.90 |
| 31.6724 | 7010.95 | 0.0924 | 2.82276 | 70.98 |
| 33.3114 | 1383.40 | 0.0792 | 2.68753 | 14.01 |
| 34.3291 | 1390.32 | 0.2112 | 2.61015 | 14.08 |
| 34.7090 | 2287.65 | 0.3696 | 2.58244 | 23.16 |
| 35.9553 | 2475.15 | 0.0792 | 2.49574 | 25.06 |
| 37.0698 | 1101.75 | 0.1320 | 2.42322 | 11.15 |
| 39.4199 | 1397.21 | 0.2112 | 2.28400 | 14.15 |
| 40.5607 | 653.66 | 0.2112 | 2.22236 | 6.62 |
| 41.6487 | 235.65 | 0.1584 | 2.16678 | 2.39 |
| 43.1771 | 1182.51 | 0.1320 | 2.09355 | 11.97 |
| 45.4464 | 3342.13 | 0.1056 | 1.99415 | 33.84 |
| 47.0989 | 475.15 | 0.1848 | 1.92796 | 4.81 |
| 47.4782 | 1172.62 | 0.1584 | 1.91344 | 11.87 |
| 47.8559 | 957.22 | 0.1848 | 1.89922 | 9.69 |
| 48.4638 | 1079.71 | 0.1584 | 1.87680 | 10.93 |
| 50.7590 | 169.16 | 0.4224 | 1.79719 | 1.71 |
| 52.4923 | 968.54 | 0.2904 | 1.74186 | 9.81 |
| 53.4517 | 369.69 | 0.2112 | 1.71283 | 3.74 |
| 54.3524 | 460.18 | 0.1848 | 1.68656 | 4.66 |
| 55.2051 | 167.23 | 0.3168 | 1.66251 | 1.69 |
| 56.4170 | 976.36 | 0.1320 | 1.62964 | 9.88 |
| 57.3938 | 459.57 | 0.2640 | 1.60420 | 4.65 |
| 57.8360 | 430.91 | 0.2640 | 1.59298 | 4.36 |
| 60.6460 | 937.54 | 0.1584 | 1.52573 | 9.49 |
| 61.3978 | 728.50 | 0.4224 | 1.50883 | 7.38 |
| 62.8957 | 178.52 | 0.4224 | 1.47645 | 1.81 |
| 64.6603 | 359.01 | 0.2640 | 1.44036 | 3.63 |
| 66.1395 | 606.12 | 0.2112 | 1.41168 | 6.14 |
| 68.4556 | 73.03 | 0.3168 | 1.36946 | 0.74 |
| 69.2084 | 515.90 | 0.2112 | 1.35639 | 5.22 |
| 72.3129 | 362.36 | 0.4224 | 1.30561 | 3.67 |
| 73.7836 | 285.71 | 0.4224 | 1.28318 | 2.89 |
| 75.2761 | 754.91 | 0.1320 | 1.26140 | 7.64 |
| 78.3109 | 312.64 | 0.3168 | 1.21993 | 3.17 |
| 81.3772 | 139.78 | 0.8448 | 1.18154 | 1.42 |
| 82.7127 | 116.79 | 0.3168 | 1.16581 | 1.18 |
| 83.9264 | 403.81 | 0.2640 | 1.15202 | 4.09 |

Pattern List

| Visible | Ref.Code | Score | Compound Name | Chem. Formula | Mineral Name | SemiQuant[%] |
| --- | --- | --- | --- | --- | --- | --- |
| * | 01-075-8690 | 69 | Sodium Aluminum Silicate Hydrate | Na1.71 ( ( Al1.806 Si4.194 ) O12 ) ( H2 O )2.16 | Analcime | 20 |
| * | 01-086-4273 | 60 | Calcium Carbonate | Ca ( C O3 ) | Calcite | 14 |
| * | 01-085-8594 | 52 | Sodium Chloride | Na Cl | Halite | 6 |
| * | 01-082-8023 | 30 | Sodium Magnesium Silicon Oxide Hydrate | Na2 Mg3 ( Si6 O16 ) ( H2 O )7 | Loughlinite | 5 |
| * | 01-089-8572 | 19 | Potassium Aluminum Silicate | K ( Al Si3 O8 ) | Orthoclase | 11 |
| * | 04-015-8336 | 16 | Cobalt Iron Oxide Hydroxide | Fe0.9 Co0.1 O ( O H ) | Goethite, Co-bearing, syn | 2 |
| * | 04-013-9383 | 25 | Potassium Magnesium Aluminum Silicate Fluoride Hydroxide | K Mg3 Al Si3 O10 ( O H ) F | Phlogopite-2M1 | 14 |
| * | 04-018-6570 | 19 | Potassium Hydronium Magnesium Aluminum Silicon Oxide Hydroxide | K0.97 ( H3 O )0.03 Mg0.4 Al2.2 Si3.4 O10 ( O H )2 | Muscovite-2M1 | 29 |

Anchor Scan Parameters

Dataset Name	11 ETOSHA 22 MOISUB 10-15CM S1

File name	C:\aeris_data\XRD data\Goldstein\11 ETOSHA 22 MOISUB 10-15CM S1.xrdml

Sample Identification	11 ETOSHA 22 MOISUB 10-15CM S1

Measurement Start Date/Time	8/23/2023 12:51:11 PM

Operator	Instrument

Raw Data Origin	XRD measurement (*.XRDML)

Scan Axis	Gonio

Start Position [°2θ]	5.0064

End Position [°2θ]	84.9874

Step Size [°2θ]	0.0110

Scan Step Time [s]	48.1950

Scan Type	Continuous

PSD Mode	Scanning

PSD Length [°2θ]	5.54

Offset [°2θ]	0.0000

Divergence Slit Type	Fixed

Divergence Slit Size [°]	0.4584

Specimen Length [mm]	10.00

Measurement Temperature [°C]	25.00

Anode Material	Cu

K-α1 [Å]	1.54060

K-α2 [Å]	1.54443

K-β1 [Å]	1.39225

K-A2 / K-A1 Ratio	0.50000

Generator Settings	15 mA, 40 kV

Diffractometer Type	2082464

Diffractometer Number	0

Goniometer Radius [mm]	145.00

Dist. Focus-Diverg. Slit [mm]	95.00

Incident Beam Monochromator	No

Spinning	Yes