Etosha 22 Sub 0.1-10 cm S2

Graphics

Graphics

Graphics

Quantitative Results

Phase Sodium Aluminum Silicate Hydrate

Weight fraction/ %	26.0

Phase Calcium Carbonate

Weight fraction/ %	7.0

Phase Potassium Sodium Barium Calcium Aluminum Silicate

Weight fraction/ %	19.0

Phase Sodium Chloride

Weight fraction/ %	6.0

Phase Sodium Magnesium Silicon Oxide Hydrate

Weight fraction/ %	2.0

Phase Potassium Magnesium Aluminum Silicate Fluoride Hydroxide

Weight fraction/ %	13.0

Phase Potassium Hydronium Magnesium Aluminum Silicon Oxide Hydroxide

Weight fraction/ %	27.0

Multiple Quantitative Results

Scans vs Phases Matrix

| Scan name | Sodium Aluminum Silicate Hydrate | Calcium Carbonate | Potassium Sodium Barium Calcium Aluminum Silicate | Sodium Chloride | Sodium Magnesium Silicon Oxide Hydrate | Potassium Magnesium Aluminum Silicate Fluoride Hydroxide | Potassium Hydronium Magnesium Aluminum Silicon Oxide Hydroxide |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 13 ETOSHA 22 SUB 0.1-10CM S2 | 26.0 | 7.0 | 19.0 | 6.0 | 2.0 | 13.0 | 27.0 |

Anchor Scan Data

| Pos. [°2θ] | Iobs [cts] | Icalc [cts] | Iback [cts] |
| --- | --- | --- | --- |
| 5.0064 | 7803.0000 | 7805.9079 | 7803.0000 |
| 5.0174 | 7786.1598 | 7797.0293 | 7782.4218 |
| 5.0284 | 7797.4267 | 7776.6267 | 7761.8437 |
| 5.0394 | 7734.5944 | 7756.2272 | 7741.2655 |
| 5.0504 | 7723.0167 | 7735.8309 | 7720.6873 |
| 5.0614 | 7705.2291 | 7715.4380 | 7700.1092 |
| 5.0724 | 7715.5929 | 7695.0484 | 7679.5310 |
| 5.0834 | 7603.7193 | 7674.6624 | 7658.9528 |
| 5.0944 | 7544.5713 | 7654.2799 | 7638.3747 |
| 5.1054 | 7585.4602 | 7633.9011 | 7617.7965 |
| 5.1164 | 7377.0177 | 7613.5261 | 7597.2183 |
| 5.1274 | 7507.6662 | 7593.1549 | 7576.6401 |
| 5.1384 | 7379.5752 | 7572.7877 | 7556.0620 |
| 5.1494 | 7343.9336 | 7552.4245 | 7535.4838 |
| 5.1604 | 7320.0806 | 7532.0654 | 7514.9056 |
| 5.1714 | 7426.6298 | 7511.7107 | 7494.3275 |
| 5.1824 | 7272.1170 | 7491.3603 | 7473.7493 |
| 5.1934 | 7268.6559 | 7471.0143 | 7453.1711 |
| 5.2044 | 7339.2124 | 7450.6730 | 7432.5930 |
| 5.2154 | 7248.2576 | 7430.3364 | 7412.0148 |
| 5.2264 | 7211.7709 | 7410.0047 | 7391.4366 |
| 5.2374 | 7187.3510 | 7389.6779 | 7370.8585 |
| 5.2484 | 7180.9990 | 7369.3563 | 7350.2803 |
| 5.2594 | 7324.8481 | 7349.0399 | 7329.7021 |
| 5.2704 | 7266.8230 | 7328.7289 | 7309.1240 |
| 5.2814 | 7160.7950 | 7308.4234 | 7288.5458 |
| 5.2924 | 7202.2193 | 7288.1237 | 7267.9676 |
| 5.3034 | 7086.7655 | 7267.8298 | 7247.3895 |
| 5.3144 | 7024.7925 | 7247.5419 | 7226.8113 |
| 5.3254 | 6970.2571 | 7227.2602 | 7206.2331 |
| 5.3364 | 6947.2242 | 7206.9849 | 7185.6549 |
| 5.3474 | 6958.2350 | 7186.7162 | 7165.0768 |
| 5.3584 | 6930.6067 | 7166.6252 | 7144.4986 |
| 5.3694 | 6982.7286 | 7147.2772 | 7123.9204 |
| 5.3804 | 7064.5969 | 7127.1216 | 7103.3423 |
| 5.3914 | 7010.7738 | 7107.3415 | 7082.7641 |
| 5.4024 | 6920.3805 | 7087.1190 | 7062.1859 |
| 5.4134 | 6936.1052 | 7066.9044 | 7041.6078 |
| 5.4244 | 6922.8928 | 7046.6979 | 7021.0296 |
| 5.4354 | 6913.0590 | 7026.4998 | 7000.4514 |
| 5.4464 | 6920.7021 | 7006.3103 | 6979.8733 |
| 5.4574 | 6792.3314 | 6986.1297 | 6959.2951 |
| 5.4684 | 6840.6696 | 6965.9583 | 6938.7169 |
| 5.4794 | 6924.3043 | 6945.7963 | 6918.1388 |
| 5.4904 | 6818.2360 | 6925.6441 | 6897.5606 |
| 5.5014 | 6740.1947 | 6905.5020 | 6876.9824 |
| 5.5124 | 6773.0580 | 6885.3703 | 6856.4043 |
| 5.5234 | 6860.8358 | 6865.2493 | 6835.8261 |
| 5.5344 | 6863.1917 | 6851.7529 | 6815.2479 |
| 5.5454 | 6787.2055 | 6836.8473 | 6806.4763 |
| 5.5564 | 6718.5850 | 6828.5672 | 6797.7048 |
| 5.5674 | 6756.5502 | 6820.2993 | 6788.9332 |
| 5.5784 | 6775.3825 | 6812.0439 | 6780.1616 |
| 5.5894 | 6718.4459 | 6803.8016 | 6771.3900 |
| 5.6004 | 6631.2743 | 6795.5727 | 6762.6184 |
| 5.6114 | 6767.6500 | 6787.3577 | 6753.8469 |
| 5.6224 | 6836.9872 | 6779.1572 | 6745.0753 |
| 5.6334 | 6752.1327 | 6770.9716 | 6736.3037 |
| 5.6444 | 6741.5251 | 6762.8014 | 6727.5321 |
| 5.6554 | 6711.1155 | 6754.6471 | 6718.7605 |
| 5.6664 | 6698.9499 | 6746.5094 | 6709.9890 |
| 5.6774 | 6676.0079 | 6738.3889 | 6701.2174 |
| 5.6884 | 6811.2645 | 6730.2861 | 6692.4458 |
| 5.6994 | 6609.7610 | 6722.2017 | 6683.6742 |
| 5.7104 | 6536.4267 | 6714.1365 | 6674.9027 |
| 5.7214 | 6652.6421 | 6706.0910 | 6666.1311 |
| 5.7324 | 6703.0914 | 6698.0661 | 6657.3595 |
| 5.7434 | 6544.9469 | 6690.0625 | 6648.5879 |
| 5.7544 | 6586.8928 | 6682.0810 | 6639.8163 |
| 5.7654 | 6633.3791 | 6674.1226 | 6631.0448 |
| 5.7764 | 6699.2262 | 6666.1881 | 6622.2732 |
| 5.7874 | 6655.7674 | 6658.2784 | 6613.5016 |
| 5.7984 | 6728.5310 | 6650.3946 | 6604.7300 |
| 5.8094 | 6481.4901 | 6642.5376 | 6595.9584 |
| 5.8204 | 6602.0738 | 6634.7086 | 6587.1869 |
| 5.8314 | 6608.7035 | 6626.9088 | 6578.4153 |
| 5.8424 | 6650.9695 | 6619.1392 | 6569.6437 |
| 5.8534 | 6692.8029 | 6611.4012 | 6560.8721 |
| 5.8644 | 6471.6224 | 6603.6961 | 6552.1005 |
| 5.8754 | 6456.1740 | 6596.0254 | 6543.3290 |
| 5.8864 | 6495.3314 | 6588.3904 | 6534.5574 |
| 5.8974 | 6470.1150 | 6580.7928 | 6525.7858 |
| 5.9084 | 6455.6755 | 6573.2342 | 6517.0142 |
| 5.9194 | 6664.1376 | 6565.7163 | 6508.2427 |
| 5.9304 | 6524.3835 | 6558.2410 | 6499.4711 |
| 5.9414 | 6501.5260 | 6550.8102 | 6490.6995 |
| 5.9524 | 6421.2272 | 6543.4259 | 6481.9279 |
| 5.9634 | 6656.2935 | 6536.0904 | 6473.1563 |
| 5.9744 | 6437.3864 | 6528.8059 | 6464.3848 |
| 5.9854 | 6500.6293 | 6521.5749 | 6455.6132 |
| 5.9964 | 6523.8761 | 6514.4000 | 6446.8416 |
| 6.0074 | 6521.0477 | 6507.2840 | 6438.0700 |
| 6.0184 | 6624.3687 | 6500.2298 | 6429.2984 |
| 6.0294 | 6561.5634 | 6493.2407 | 6420.5269 |
| 6.0404 | 6545.0020 | 6486.3199 | 6411.7553 |
| 6.0514 | 6595.1170 | 6479.4713 | 6402.9837 |
| 6.0624 | 6433.7729 | 6472.5377 | 6394.2121 |
| 6.0734 | 6523.7729 | 6465.7191 | 6385.1530 |
| 6.0844 | 6521.6097 | 6458.8245 | 6376.0940 |
| 6.0954 | 6646.6549 | 6452.0200 | 6367.0349 |
| 6.1064 | 6590.6441 | 6445.3113 | 6357.9758 |
| 6.1174 | 6608.1721 | 6438.7047 | 6348.9167 |
| 6.1284 | 6587.9262 | 6432.2069 | 6339.8577 |
| 6.1394 | 6588.1608 | 6425.8256 | 6330.7986 |
| 6.1504 | 6591.5988 | 6419.5694 | 6321.7395 |
| 6.1614 | 6545.7537 | 6413.4479 | 6312.6804 |
| 6.1724 | 6673.0629 | 6407.4720 | 6303.6214 |
| 6.1834 | 6684.4843 | 6401.6541 | 6294.5623 |
| 6.1944 | 6702.8053 | 6396.0082 | 6285.5032 |
| 6.2054 | 6622.1617 | 6390.5503 | 6276.4441 |
| 6.2164 | 6636.5310 | 6385.2987 | 6267.3850 |
| 6.2274 | 6746.6136 | 6380.2743 | 6258.3260 |
| 6.2384 | 6738.9341 | 6375.5012 | 6249.2669 |
| 6.2494 | 6697.8333 | 6371.0069 | 6240.2078 |
| 6.2604 | 6717.3540 | 6366.8228 | 6231.1487 |
| 6.2714 | 6843.6622 | 6362.9851 | 6222.0897 |
| 6.2824 | 6785.0305 | 6359.5350 | 6213.0306 |
| 6.2934 | 6740.1017 | 6356.5194 | 6203.9715 |
| 6.3044 | 6752.9764 | 6353.9917 | 6194.9124 |
| 6.3154 | 6852.7935 | 6352.0125 | 6185.8534 |
| 6.3264 | 6838.8732 | 6350.6499 | 6176.7943 |
| 6.3374 | 6845.1790 | 6349.9808 | 6167.7352 |
| 6.3484 | 6839.4985 | 6350.0910 | 6158.6761 |
| 6.3594 | 6799.5442 | 6351.0762 | 6149.6170 |
| 6.3704 | 6859.0531 | 6353.0421 | 6140.5580 |
| 6.3814 | 6958.1185 | 6356.1052 | 6131.4989 |
| 6.3924 | 6969.8407 | 6360.3931 | 6122.4398 |
| 6.4034 | 6890.5383 | 6366.0443 | 6113.3807 |
| 6.4144 | 6910.8417 | 6373.2082 | 6104.3217 |
| 6.4254 | 6880.8982 | 6382.0448 | 6095.2626 |
| 6.4364 | 6862.8270 | 6392.7241 | 6086.2035 |
| 6.4474 | 6937.7090 | 6405.4250 | 6077.1444 |
| 6.4584 | 7104.4219 | 6420.3342 | 6068.0854 |
| 6.4694 | 7119.8166 | 6437.6443 | 6059.0263 |
| 6.4804 | 7151.8171 | 6457.5519 | 6049.9672 |
| 6.4914 | 7269.4558 | 6480.2551 | 6040.9081 |
| 6.5024 | 7238.1406 | 6505.9506 | 6031.8490 |
| 6.5134 | 7209.1549 | 6534.8306 | 6022.7900 |
| 6.5244 | 7359.5871 | 6567.0791 | 6013.7309 |
| 6.5354 | 7392.8279 | 6602.8678 | 6004.6718 |
| 6.5464 | 7346.1249 | 6642.3524 | 5995.6127 |
| 6.5574 | 7347.6608 | 6685.6673 | 5986.5537 |
| 6.5684 | 7491.6313 | 6732.9216 | 5977.4946 |
| 6.5794 | 7430.6602 | 6784.1937 | 5968.4355 |
| 6.5904 | 7438.3451 | 6839.5264 | 5959.3764 |
| 6.6014 | 7504.9720 | 6898.9214 | 5950.3174 |
| 6.6124 | 7539.8623 | 6962.3339 | 5941.2583 |
| 6.6234 | 7623.2581 | 7029.6671 | 5932.1992 |
| 6.6344 | 7692.7827 | 7100.7657 | 5923.1401 |
| 6.6454 | 7743.9056 | 7175.4098 | 5914.0810 |
| 6.6564 | 7647.3864 | 7253.3078 | 5905.0220 |
| 6.6674 | 7642.5511 | 7334.0888 | 5895.9629 |
| 6.6784 | 7715.3275 | 7417.2942 | 5886.9038 |
| 6.6894 | 7907.3894 | 7502.3692 | 5877.8447 |
| 6.7004 | 7756.1140 | 7588.6533 | 5868.7857 |
| 6.7114 | 7830.0369 | 7675.3718 | 5859.7266 |
| 6.7224 | 7873.9440 | 7761.6283 | 5850.6675 |
| 6.7334 | 7867.7030 | 7846.4001 | 5841.6084 |
| 6.7444 | 7906.5634 | 7928.5387 | 5832.5494 |
| 6.7554 | 8105.5812 | 8006.7773 | 5823.4903 |
| 6.7664 | 8109.2006 | 8079.7491 | 5814.4312 |
| 6.7774 | 7959.2345 | 8146.0179 | 5805.3721 |
| 6.7884 | 8087.8230 | 8204.1225 | 5796.3130 |
| 6.7994 | 8075.4115 | 8252.6355 | 5787.2540 |
| 6.8104 | 7907.6589 | 8290.2329 | 5778.1949 |
| 6.8214 | 8072.0103 | 8315.7701 | 5769.1358 |
| 6.8324 | 8003.4435 | 8328.3550 | 5760.0767 |
| 6.8434 | 8014.9995 | 8327.4108 | 5751.0177 |
| 6.8544 | 8021.9026 | 8312.7192 | 5741.9586 |
| 6.8654 | 7871.3398 | 8284.4363 | 5732.8995 |
| 6.8764 | 7987.6529 | 8243.0812 | 5723.8404 |
| 6.8874 | 8035.8142 | 8189.4962 | 5714.7814 |
| 6.8984 | 8023.1533 | 8124.7878 | 5705.7223 |
| 6.9094 | 7860.0290 | 8050.2536 | 5696.6632 |
| 6.9204 | 7783.4424 | 7967.3072 | 5687.6041 |
| 6.9314 | 7700.0939 | 7877.4070 | 5678.5450 |
| 6.9424 | 7743.5910 | 7781.9955 | 5669.4860 |
| 6.9534 | 7761.1224 | 7682.4529 | 5660.4269 |
| 6.9644 | 7731.4582 | 7580.0638 | 5651.3678 |
| 6.9754 | 7569.7747 | 7475.9974 | 5642.3087 |
| 6.9864 | 7397.4956 | 7371.2982 | 5633.2497 |
| 6.9974 | 7485.1966 | 7266.8842 | 5624.1906 |
| 7.0084 | 7377.6873 | 7163.5508 | 5615.1315 |
| 7.0194 | 7402.4808 | 7061.9779 | 5606.0724 |
| 7.0304 | 7332.2870 | 6962.7385 | 5597.0133 |
| 7.0414 | 7108.8491 | 6866.3074 | 5587.9543 |
| 7.0524 | 7155.3805 | 6773.0706 | 5578.8952 |
| 7.0634 | 7068.3299 | 6683.3333 | 5569.8361 |
| 7.0744 | 6980.1169 | 6597.3276 | 5560.7770 |
| 7.0854 | 6741.6459 | 6515.2196 | 5551.7180 |
| 7.0964 | 6637.9479 | 6437.1164 | 5542.6589 |
| 7.1074 | 6710.0590 | 6363.0714 | 5533.5998 |
| 7.1184 | 6645.4071 | 6292.9297 | 5524.5407 |
| 7.1294 | 6533.3097 | 6226.8511 | 5515.1942 |
| 7.1404 | 6477.0502 | 6164.5676 | 5505.8476 |
| 7.1514 | 6447.9291 | 6106.1364 | 5496.5010 |
| 7.1624 | 6334.1259 | 6051.4269 | 5487.1544 |
| 7.1734 | 6384.9404 | 6000.2873 | 5477.8079 |
| 7.1844 | 6216.3008 | 5952.5483 | 5468.4613 |
| 7.1954 | 6104.5029 | 5908.0278 | 5459.1147 |

Scan List

| Vis. | Dataset Name | Start pos. [°2θ] | End pos. [°2θ] | Step [°2θ] | Meas.Date/Time |
| --- | --- | --- | --- | --- | --- |
| * | 13 ETOSHA 22 SUB 0.1-10CM S2 | 5.0064 | 84.9874 | 0.0110 | 8/23/2023 1:17:12 PM |

Peak List

| Pos. [°2θ] | Height [cts] | FWHM Left [°2θ] | d-spacing [Å] | Rel. Int. [%] |
| --- | --- | --- | --- | --- |
| 6.8387 | 2298.25 | 0.3897 | 12.91499 | 16.68 |
| 8.8217 | 1139.79 | 0.3464 | 10.01587 | 8.27 |
| 11.5621 | 176.97 | 0.3464 | 7.64740 | 1.28 |
| 13.6127 | 369.23 | 0.1082 | 6.49963 | 2.68 |
| 15.0657 | 416.04 | 0.0866 | 5.87591 | 3.02 |
| 15.8453 | 9997.48 | 0.0974 | 5.58851 | 72.57 |
| 18.3064 | 1854.88 | 0.0866 | 4.84236 | 13.46 |
| 19.0150 | 347.13 | 0.1299 | 4.66347 | 2.52 |
| 19.7923 | 2658.45 | 0.3897 | 4.48205 | 19.30 |
| 20.9647 | 2436.42 | 0.1082 | 4.23399 | 17.68 |
| 22.5031 | 614.59 | 0.1299 | 3.94789 | 4.46 |
| 23.0262 | 678.58 | 0.1515 | 3.85936 | 4.93 |
| 23.4329 | 2563.97 | 0.0866 | 3.79330 | 18.61 |
| 24.2946 | 608.82 | 0.1299 | 3.66067 | 4.42 |
| 24.5140 | 461.06 | 0.1082 | 3.62840 | 3.35 |
| 25.0690 | 422.58 | 0.1732 | 3.54932 | 3.07 |
| 25.6753 | 2029.93 | 0.0866 | 3.46686 | 14.73 |
| 25.9985 | 13777.20 | 0.1299 | 3.42450 | 100.00 |
| 26.7816 | 4006.10 | 0.0974 | 3.32611 | 29.08 |
| 27.1020 | 2559.19 | 0.1082 | 3.28751 | 18.58 |
| 27.3766 | 2261.85 | 0.1082 | 3.25516 | 16.42 |
| 27.5802 | 3091.92 | 0.0866 | 3.23159 | 22.44 |
| 29.4231 | 5409.95 | 0.1191 | 3.03323 | 39.27 |
| 29.7565 | 1987.29 | 0.0974 | 3.00000 | 14.42 |
| 30.5883 | 6681.50 | 0.1082 | 2.92029 | 48.50 |
| 31.6812 | 7435.12 | 0.0541 | 2.82200 | 53.97 |
| 32.0272 | 927.57 | 0.1299 | 2.79230 | 6.73 |
| 32.3296 | 696.60 | 0.1082 | 2.76687 | 5.06 |
| 33.3097 | 1713.19 | 0.0649 | 2.68766 | 12.43 |
| 34.3146 | 1620.79 | 0.1299 | 2.61121 | 11.76 |
| 34.6729 | 2997.84 | 0.1948 | 2.58505 | 21.76 |
| 35.8581 | 2004.68 | 0.1056 | 2.50228 | 14.55 |
| 35.9610 | 1978.63 | 0.0792 | 2.49535 | 14.36 |
| 37.1146 | 1468.53 | 0.1320 | 2.42040 | 10.66 |
| 37.6080 | 651.33 | 0.2640 | 2.38977 | 4.73 |
| 38.6660 | 109.69 | 0.2112 | 2.32678 | 0.80 |
| 39.4144 | 731.63 | 0.2112 | 2.28430 | 5.31 |
| 40.5287 | 732.72 | 0.1584 | 2.22403 | 5.32 |
| 41.6305 | 518.08 | 0.2112 | 2.16768 | 3.76 |
| 42.4803 | 262.63 | 0.4224 | 2.12627 | 1.91 |
| 43.1656 | 643.95 | 0.1320 | 2.09408 | 4.67 |
| 43.6639 | 161.09 | 0.1584 | 2.07134 | 1.17 |
| 44.9706 | 440.84 | 0.3168 | 2.01413 | 3.20 |
| 45.4218 | 3430.20 | 0.0924 | 1.99517 | 24.90 |
| 45.5472 | 1889.39 | 0.0660 | 1.98997 | 13.71 |
| 45.9406 | 394.03 | 0.2112 | 1.97384 | 2.86 |
| 47.0239 | 396.00 | 0.3168 | 1.93086 | 2.87 |
| 47.5345 | 756.01 | 0.2112 | 1.91130 | 5.49 |
| 47.8345 | 1121.31 | 0.1320 | 1.90002 | 8.14 |
| 48.5720 | 729.37 | 0.2112 | 1.87288 | 5.29 |
| 48.8158 | 807.83 | 0.2112 | 1.86409 | 5.86 |
| 50.7775 | 647.29 | 0.3696 | 1.79658 | 4.70 |
| 52.5435 | 1485.17 | 0.1848 | 1.74028 | 10.78 |
| 53.4779 | 545.76 | 0.0792 | 1.71206 | 3.96 |
| 54.3574 | 597.00 | 0.1056 | 1.68641 | 4.33 |
| 56.4332 | 992.80 | 0.1056 | 1.62921 | 7.21 |
| 57.4174 | 279.99 | 0.2112 | 1.60360 | 2.03 |
| 57.8558 | 536.95 | 0.1848 | 1.59249 | 3.90 |
| 60.4650 | 443.95 | 0.4224 | 1.52986 | 3.22 |
| 61.4240 | 815.83 | 0.4224 | 1.50825 | 5.92 |
| 62.9327 | 198.26 | 0.4224 | 1.47567 | 1.44 |
| 63.7517 | 78.94 | 0.4224 | 1.45868 | 0.57 |
| 64.6933 | 283.74 | 0.6336 | 1.43970 | 2.06 |
| 66.1589 | 738.19 | 0.4224 | 1.41132 | 5.36 |
| 67.6931 | 110.66 | 0.3168 | 1.38302 | 0.80 |
| 68.4511 | 146.21 | 0.3168 | 1.36954 | 1.06 |
| 69.1900 | 642.89 | 0.2112 | 1.35671 | 4.67 |
| 72.3301 | 420.73 | 0.5280 | 1.30534 | 3.05 |
| 73.7930 | 309.91 | 0.3696 | 1.28304 | 2.25 |
| 75.2397 | 739.63 | 0.0792 | 1.26192 | 5.37 |
| 78.2992 | 469.47 | 0.2640 | 1.22009 | 3.41 |
| 81.3936 | 189.63 | 0.4224 | 1.18134 | 1.38 |
| 83.9305 | 506.55 | 0.1056 | 1.15197 | 3.68 |

Pattern List

| Visible | Ref.Code | Score | Compound Name | Chem. Formula | Mineral Name | SemiQuant[%] |
| --- | --- | --- | --- | --- | --- | --- |
| * | 01-075-8690 | 70 | Sodium Aluminum Silicate Hydrate | Na1.71 ( ( Al1.806 Si4.194 ) O12 ) ( H2 O )2.16 | Analcime | 26 |
| * | 01-086-2334 | 52 | Calcium Carbonate | Ca ( C O3 ) | Calcite | 7 |
| * | 01-076-0825 | 35 | Potassium Sodium Barium Calcium Aluminum Silicate | ( K0.88 Na0.1 Ca0.01 Ba0.01 ) ( Al1.005 Si2.995 O8 ) | Orthoclase | 19 |
| * | 01-085-8594 | 42 | Sodium Chloride | Na Cl | Halite | 6 |
| * | 01-082-8023 | 25 | Sodium Magnesium Silicon Oxide Hydrate | Na2 Mg3 ( Si6 O16 ) ( H2 O )7 | Loughlinite | 2 |
| * | 04-013-9383 | 25 | Potassium Magnesium Aluminum Silicate Fluoride Hydroxide | K Mg3 Al Si3 O10 ( O H ) F | Phlogopite-2M1 | 13 |
| * | 04-018-6570 | 21 | Potassium Hydronium Magnesium Aluminum Silicon Oxide Hydroxide | K0.97 ( H3 O )0.03 Mg0.4 Al2.2 Si3.4 O10 ( O H )2 | Muscovite-2M1 | 27 |

Anchor Scan Parameters

Dataset Name	13 ETOSHA 22 SUB 0.1-10CM S2

File name	C:\aeris_data\XRD data\Goldstein\13 ETOSHA 22 SUB 0.1-10CM S2.xrdml

Sample Identification	13 ETOSHA 22 SUB 0.1-10CM S2

Measurement Start Date/Time	8/23/2023 1:17:12 PM

Operator	Instrument

Raw Data Origin	XRD measurement (*.XRDML)

Scan Axis	Gonio

Start Position [°2θ]	5.0064

End Position [°2θ]	84.9874

Step Size [°2θ]	0.0110

Scan Step Time [s]	48.1950

Scan Type	Continuous

PSD Mode	Scanning

PSD Length [°2θ]	5.54

Offset [°2θ]	0.0000

Divergence Slit Type	Fixed

Divergence Slit Size [°]	0.4584

Specimen Length [mm]	10.00

Measurement Temperature [°C]	25.00

Anode Material	Cu

K-α1 [Å]	1.54060

K-α2 [Å]	1.54443

K-β1 [Å]	1.39225

K-A2 / K-A1 Ratio	0.50000

Generator Settings	15 mA, 40 kV

Diffractometer Type	2082464

Diffractometer Number	0

Goniometer Radius [mm]	145.00

Dist. Focus-Diverg. Slit [mm]	95.00

Incident Beam Monochromator	No

Spinning	Yes