Etosha 22 MoiSub 3-15 cm S3

Graphics

Graphics

Graphics

Quantitative Results

Phase Sodium Aluminum Silicate Hydrate

Weight fraction/ %	8.0

Phase Calcium Carbonate

Weight fraction/ %	11.0

Phase Sodium Magnesium Silicon Oxide Hydrate

Weight fraction/ %	5.0

Phase Sodium Chloride

Weight fraction/ %	11.0

Phase Potassium Magnesium Aluminum Silicate Fluoride Hydroxide

Weight fraction/ %	16.0

Phase Potassium Sodium Aluminum Silicate

Weight fraction/ %	12.0

Phase Sodium Aluminum Iron Silicon Oxide Hydroxide

Weight fraction/ %	7.0

Phase Potassium Hydronium Magnesium Aluminum Silicon Oxide Hydroxide

Weight fraction/ %	29.0

Multiple Quantitative Results

Scans vs Phases Matrix

| Scan name | Sodium Aluminum Silicate Hydrate | Calcium Carbonate | Sodium Magnesium Silicon Oxide Hydrate | Sodium Chloride | Potassium Magnesium Aluminum Silicate Fluoride Hydroxide | Potassium Sodium Aluminum Silicate | Sodium Aluminum Iron Silicon Oxide Hydroxide | Potassium Hydronium Magnesium Aluminum Silicon Oxide Hydroxide |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 16 ETOSHA 22 MOISUB 3-15CM S3 | 8.0 | 11.0 | 5.0 | 11.0 | 16.0 | 12.0 | 7.0 | 29.0 |

Anchor Scan Data

| Pos. [°2θ] | Iobs [cts] | Icalc [cts] | Iback [cts] |
| --- | --- | --- | --- |
| 5.0064 | 8143.0000 | 8135.2373 | 8143.0000 |
| 5.0174 | 8040.9184 | 8120.0815 | 8118.5292 |
| 5.0284 | 7957.2940 | 8095.6196 | 8094.0583 |
| 5.0394 | 8087.1150 | 8071.1577 | 8069.5875 |
| 5.0504 | 8061.9843 | 8046.6960 | 8045.1166 |
| 5.0614 | 8021.0949 | 8022.2343 | 8020.6458 |
| 5.0724 | 7992.2950 | 7997.7727 | 7996.1749 |
| 5.0834 | 7979.9970 | 7973.3112 | 7971.7041 |
| 5.0944 | 7797.9056 | 7948.8498 | 7947.2333 |
| 5.1054 | 7688.8805 | 7924.3885 | 7922.7624 |
| 5.1164 | 7709.0393 | 7899.9272 | 7898.2916 |
| 5.1274 | 7759.3314 | 7875.4660 | 7873.8207 |
| 5.1384 | 7824.8938 | 7851.0049 | 7849.3499 |
| 5.1494 | 7666.1706 | 7826.5439 | 7824.8790 |
| 5.1604 | 7615.3638 | 7804.8465 | 7800.4082 |
| 5.1714 | 7591.6770 | 7782.8712 | 7775.9373 |
| 5.1824 | 7675.4808 | 7759.8674 | 7751.4665 |
| 5.1934 | 7585.4336 | 7736.7254 | 7726.9957 |
| 5.2044 | 7466.3717 | 7712.3690 | 7702.5248 |
| 5.2154 | 7376.0236 | 7688.0147 | 7678.0540 |
| 5.2264 | 7441.4513 | 7663.6626 | 7653.5831 |
| 5.2374 | 7419.3658 | 7639.3128 | 7629.1123 |
| 5.2484 | 7482.1091 | 7614.9652 | 7604.6414 |
| 5.2594 | 7282.5929 | 7590.6201 | 7580.1706 |
| 5.2704 | 7486.3864 | 7566.2773 | 7555.6998 |
| 5.2814 | 7399.8707 | 7541.9370 | 7531.2289 |
| 5.2924 | 7355.4848 | 7517.5993 | 7506.7581 |
| 5.3034 | 7286.9380 | 7493.2643 | 7482.2872 |
| 5.3144 | 7174.3245 | 7468.9319 | 7457.8164 |
| 5.3254 | 7172.2571 | 7444.6022 | 7433.3455 |
| 5.3364 | 7140.7434 | 7420.2755 | 7408.8747 |
| 5.3474 | 7178.7665 | 7395.9516 | 7384.4038 |
| 5.3584 | 7174.9489 | 7371.6308 | 7359.9330 |
| 5.3694 | 7055.4882 | 7347.3130 | 7335.4622 |
| 5.3804 | 7042.2665 | 7322.9984 | 7310.9913 |
| 5.3914 | 7126.4189 | 7298.6871 | 7286.5205 |
| 5.4024 | 7075.2124 | 7274.3792 | 7262.0496 |
| 5.4134 | 7064.5698 | 7250.0747 | 7237.5788 |
| 5.4244 | 7126.3353 | 7225.7737 | 7213.1079 |
| 5.4354 | 7100.7183 | 7201.4765 | 7188.6371 |
| 5.4464 | 6979.0462 | 7177.1830 | 7164.1663 |
| 5.4574 | 6997.3771 | 7152.8934 | 7139.6954 |
| 5.4684 | 7049.6667 | 7128.6078 | 7115.2246 |
| 5.4794 | 6942.6770 | 7104.3263 | 7090.7537 |
| 5.4904 | 6970.0905 | 7080.0490 | 7066.2829 |
| 5.5014 | 6977.6903 | 7055.7762 | 7041.8120 |
| 5.5124 | 6912.0806 | 7031.5079 | 7017.3412 |
| 5.5234 | 6964.7439 | 7007.2442 | 6992.8703 |
| 5.5344 | 7005.5605 | 6989.4161 | 6968.3995 |
| 5.5454 | 6991.1706 | 6975.6415 | 6960.8388 |
| 5.5564 | 6880.9115 | 6968.3028 | 6953.2780 |
| 5.5674 | 6897.1165 | 6960.9695 | 6945.7173 |
| 5.5784 | 6896.1475 | 6953.6415 | 6938.1566 |
| 5.5894 | 6891.4513 | 6946.3192 | 6930.5959 |
| 5.6004 | 6900.6814 | 6939.0027 | 6923.0351 |
| 5.6114 | 6951.0526 | 6931.6923 | 6915.4744 |
| 5.6224 | 6936.7670 | 6924.3881 | 6907.9137 |
| 5.6334 | 6873.4616 | 6917.0903 | 6900.3529 |
| 5.6444 | 6868.9705 | 6909.7991 | 6892.7922 |
| 5.6554 | 6773.4759 | 6902.5149 | 6885.2315 |
| 5.6664 | 6853.7316 | 6895.2377 | 6877.6708 |
| 5.6774 | 6828.5221 | 6887.9680 | 6870.1100 |
| 5.6884 | 6848.6745 | 6880.7059 | 6862.5493 |
| 5.6994 | 6749.7212 | 6873.4517 | 6854.9886 |
| 5.7104 | 6780.7168 | 6866.2057 | 6847.4278 |
| 5.7214 | 6881.0875 | 6858.9683 | 6839.8671 |
| 5.7324 | 6898.7552 | 6851.7396 | 6832.3064 |
| 5.7434 | 6806.5914 | 6844.5201 | 6824.7457 |
| 5.7544 | 6804.5516 | 6837.3101 | 6817.1849 |
| 5.7654 | 6865.6696 | 6830.1100 | 6809.6242 |
| 5.7764 | 6991.2901 | 6822.9201 | 6802.0635 |
| 5.7874 | 6726.3839 | 6815.7409 | 6794.5027 |
| 5.7984 | 6811.5487 | 6808.5727 | 6786.9420 |
| 5.8094 | 6936.5669 | 6801.4160 | 6779.3813 |
| 5.8204 | 6967.1908 | 6794.2713 | 6771.8206 |
| 5.8314 | 6777.2596 | 6787.1390 | 6764.2598 |
| 5.8424 | 6730.1740 | 6780.0196 | 6756.6991 |
| 5.8534 | 6725.1608 | 6772.9138 | 6749.1384 |
| 5.8644 | 6656.9321 | 6765.8219 | 6741.5776 |
| 5.8754 | 6796.7360 | 6758.7448 | 6734.0169 |
| 5.8864 | 6797.0669 | 6751.6829 | 6726.4562 |
| 5.8974 | 6864.6991 | 6744.6369 | 6718.8955 |
| 5.9084 | 6823.0698 | 6737.6076 | 6711.3347 |
| 5.9194 | 6954.0491 | 6730.5956 | 6703.7740 |
| 5.9304 | 6764.3363 | 6723.6017 | 6696.2133 |
| 5.9414 | 6838.2055 | 6716.6268 | 6688.6525 |
| 5.9524 | 6923.8938 | 6709.6717 | 6681.0918 |
| 5.9634 | 6851.0782 | 6702.7374 | 6673.5311 |
| 5.9744 | 6795.0384 | 6695.8247 | 6665.9704 |
| 5.9854 | 6902.1780 | 6688.9348 | 6658.4096 |
| 5.9964 | 6861.2921 | 6682.0687 | 6650.8489 |
| 6.0074 | 6991.3033 | 6675.2276 | 6643.2882 |
| 6.0184 | 6983.4759 | 6668.4127 | 6635.7274 |
| 6.0294 | 6858.2729 | 6661.6252 | 6628.1667 |
| 6.0404 | 6830.0807 | 6654.8667 | 6620.6060 |
| 6.0514 | 6961.6706 | 6648.1385 | 6613.0453 |
| 6.0624 | 6980.2950 | 6641.3566 | 6605.4845 |
| 6.0734 | 7038.2738 | 6634.5544 | 6597.6987 |
| 6.0844 | 7032.5635 | 6627.7020 | 6589.9128 |
| 6.0954 | 7154.5177 | 6620.8869 | 6582.1269 |
| 6.1064 | 7019.4278 | 6614.1110 | 6574.3411 |
| 6.1174 | 7153.1042 | 6607.3767 | 6566.5552 |
| 6.1284 | 7216.9204 | 6600.6861 | 6558.7694 |
| 6.1394 | 7332.0556 | 6594.0418 | 6550.9835 |
| 6.1504 | 7401.9213 | 6587.4464 | 6543.1976 |
| 6.1614 | 7284.3185 | 6580.9029 | 6535.4118 |
| 6.1724 | 7102.4110 | 6574.4142 | 6527.6259 |
| 6.1834 | 7199.3806 | 6567.9837 | 6519.8400 |
| 6.1944 | 7264.2743 | 6561.6149 | 6512.0542 |
| 6.2054 | 7267.7011 | 6555.3117 | 6504.2683 |
| 6.2164 | 7391.3992 | 6549.0782 | 6496.4825 |
| 6.2274 | 7363.7360 | 6542.9188 | 6488.6966 |
| 6.2384 | 7457.8644 | 6536.8383 | 6480.9107 |
| 6.2494 | 7548.2778 | 6530.8420 | 6473.1249 |
| 6.2604 | 7527.5782 | 6524.9355 | 6465.3390 |
| 6.2714 | 7607.6632 | 6519.1250 | 6457.5531 |
| 6.2824 | 7570.8604 | 6513.4171 | 6449.7673 |
| 6.2934 | 7590.0620 | 6507.8190 | 6441.9814 |
| 6.3044 | 7696.6834 | 6502.3386 | 6434.1956 |
| 6.3154 | 7768.5054 | 6496.9846 | 6426.4097 |
| 6.3264 | 7821.3451 | 6491.7663 | 6418.6238 |
| 6.3374 | 7809.7143 | 6486.6941 | 6410.8380 |
| 6.3484 | 7855.9066 | 6481.7792 | 6403.0521 |
| 6.3594 | 7967.3776 | 6477.0340 | 6395.2663 |
| 6.3704 | 7982.4759 | 6472.4721 | 6387.4804 |
| 6.3814 | 8119.3137 | 6468.1084 | 6379.6945 |
| 6.3924 | 8139.7876 | 6463.9597 | 6371.9087 |
| 6.4034 | 8199.8019 | 6460.0440 | 6364.1228 |
| 6.4144 | 8292.8024 | 6456.3818 | 6356.3369 |
| 6.4254 | 8381.8850 | 6452.9955 | 6348.5511 |
| 6.4364 | 8391.8250 | 6449.9100 | 6340.7652 |
| 6.4474 | 8484.2282 | 6447.1533 | 6332.9794 |
| 6.4584 | 8665.8525 | 6444.7565 | 6325.1935 |
| 6.4694 | 8704.3240 | 6442.7545 | 6317.4076 |
| 6.4804 | 8768.0521 | 6441.1864 | 6309.6218 |
| 6.4914 | 8781.3097 | 6440.0965 | 6301.8359 |
| 6.5024 | 8849.6048 | 6439.5345 | 6294.0501 |
| 6.5134 | 8963.1746 | 6439.5571 | 6286.2642 |
| 6.5244 | 9074.2744 | 6440.2293 | 6278.4783 |
| 6.5354 | 9091.7055 | 6441.6254 | 6270.6925 |
| 6.5464 | 9294.0168 | 6443.8325 | 6262.9066 |
| 6.5574 | 9433.6431 | 6446.9528 | 6255.1207 |
| 6.5684 | 9400.5909 | 6451.1095 | 6247.3349 |
| 6.5794 | 9497.1583 | 6456.4533 | 6239.5490 |
| 6.5904 | 9483.1858 | 6463.0603 | 6231.7632 |
| 6.6014 | 9663.5507 | 6471.2823 | 6223.7457 |
| 6.6124 | 9859.4199 | 6481.3306 | 6215.7282 |
| 6.6234 | 9705.5988 | 6493.7457 | 6207.7108 |
| 6.6344 | 9922.1043 | 6509.1045 | 6199.6933 |
| 6.6454 | 10113.8501 | 6528.1890 | 6191.6758 |
| 6.6564 | 10250.6756 | 6552.0544 | 6183.6584 |
| 6.6674 | 10442.1898 | 6582.1113 | 6175.6409 |
| 6.6784 | 10493.5742 | 6620.2139 | 6167.6234 |
| 6.6894 | 10473.2257 | 6668.7497 | 6159.6060 |
| 6.7004 | 10605.7090 | 6730.7136 | 6151.5885 |
| 6.7114 | 10674.4966 | 6809.8319 | 6143.5710 |
| 6.7224 | 10734.1269 | 6910.2354 | 6135.5536 |
| 6.7334 | 10865.4386 | 7036.8218 | 6127.5361 |
| 6.7444 | 11002.1682 | 7194.8332 | 6119.5186 |
| 6.7554 | 11034.8112 | 7389.4455 | 6111.5012 |
| 6.7664 | 10881.3490 | 7625.5853 | 6103.4837 |
| 6.7774 | 11295.9308 | 7907.2669 | 6095.4662 |
| 6.7884 | 11190.0265 | 8237.0021 | 6087.4488 |
| 6.7994 | 11399.0585 | 8615.1171 | 6079.4313 |
| 6.8104 | 11418.2970 | 9038.9940 | 6071.4138 |
| 6.8214 | 11554.4616 | 9502.2161 | 6063.3964 |
| 6.8324 | 11294.3707 | 9993.5761 | 6055.3789 |
| 6.8434 | 11341.1510 | 10495.9643 | 6047.3614 |
| 6.8544 | 11601.4514 | 10985.3855 | 6039.3440 |
| 6.8654 | 11670.0427 | 11430.8091 | 6031.3265 |
| 6.8764 | 11545.1839 | 11796.0468 | 6023.3090 |
| 6.8874 | 11481.8274 | 12044.7418 | 6015.2916 |
| 6.8984 | 11466.1013 | 12148.1221 | 6007.2741 |
| 6.9094 | 11610.4154 | 12092.8343 | 5999.2566 |
| 6.9204 | 11476.9410 | 11884.9564 | 5991.2392 |
| 6.9314 | 11427.5697 | 11547.9688 | 5983.2217 |
| 6.9424 | 11126.3973 | 11115.9528 | 5975.2042 |
| 6.9534 | 11317.6681 | 10625.5977 | 5967.1867 |
| 6.9644 | 11150.3805 | 10110.1645 | 5959.1693 |
| 6.9754 | 11147.1912 | 9596.4952 | 5951.1518 |
| 6.9864 | 11053.6991 | 9104.4442 | 5943.1343 |
| 6.9974 | 10932.8043 | 8647.5643 | 5935.1169 |
| 7.0084 | 10780.6204 | 8234.1722 | 5927.0994 |
| 7.0194 | 10712.0088 | 7868.3841 | 5919.0819 |
| 7.0304 | 10634.2113 | 7551.0217 | 5911.0645 |
| 7.0414 | 10376.4680 | 7280.4100 | 5903.0470 |
| 7.0524 | 10280.1063 | 7053.0956 | 5895.0295 |
| 7.0634 | 10365.3986 | 6864.4955 | 5887.0121 |
| 7.0744 | 10075.5742 | 6709.4612 | 5878.9946 |
| 7.0854 | 9896.2832 | 6582.7426 | 5870.9771 |
| 7.0964 | 9811.5349 | 6479.3375 | 5862.9597 |
| 7.1074 | 9692.6155 | 6394.7247 | 5854.9422 |
| 7.1184 | 9533.2065 | 6324.8795 | 5846.9247 |
| 7.1294 | 9500.2330 | 6266.6496 | 5838.6760 |
| 7.1404 | 9332.5289 | 6217.2947 | 5830.4273 |
| 7.1514 | 9086.5664 | 6174.8612 | 5822.1785 |
| 7.1624 | 9064.1435 | 6137.7633 | 5813.9298 |
| 7.1734 | 8989.2242 | 6104.8059 | 5805.6811 |
| 7.1844 | 8887.7787 | 6075.1001 | 5797.4323 |
| 7.1954 | 8645.4232 | 6047.9891 | 5789.1836 |

Scan List

| Vis. | Dataset Name | Start pos. [°2θ] | End pos. [°2θ] | Step [°2θ] | Meas.Date/Time |
| --- | --- | --- | --- | --- | --- |
| * | 16 ETOSHA 22 MOISUB 3-15CM S3 | 5.0064 | 84.9874 | 0.0110 | 8/28/2023 1:54:13 PM |

Peak List

| Pos. [°2θ] | Height [cts] | FWHM Left [°2θ] | d-spacing [Å] | Rel. Int. [%] |
| --- | --- | --- | --- | --- |
| 6.8950 | 5533.08 | 0.1732 | 12.80968 | 49.09 |
| 8.8350 | 860.14 | 0.4330 | 10.00081 | 7.63 |
| 11.6236 | 309.10 | 0.2598 | 7.60707 | 2.74 |
| 13.6364 | 94.21 | 0.6927 | 6.48840 | 0.84 |
| 15.8724 | 6891.88 | 0.0974 | 5.57903 | 61.14 |
| 18.3464 | 1367.24 | 0.0866 | 4.83189 | 12.13 |
| 19.8069 | 3071.39 | 0.0866 | 4.47879 | 27.25 |
| 19.9228 | 2887.41 | 0.1082 | 4.45299 | 25.62 |
| 20.9609 | 1189.24 | 0.0866 | 4.23473 | 10.55 |
| 21.4234 | 718.21 | 0.2165 | 4.14434 | 6.37 |
| 22.5363 | 135.71 | 0.1299 | 3.94215 | 1.20 |
| 23.0989 | 917.72 | 0.1299 | 3.84739 | 8.14 |
| 23.4837 | 1398.50 | 0.1515 | 3.78521 | 12.41 |
| 24.2971 | 487.80 | 0.0866 | 3.66029 | 4.33 |
| 26.0212 | 10579.87 | 0.1191 | 3.42155 | 93.86 |
| 26.8160 | 1623.84 | 0.1082 | 3.32192 | 14.41 |
| 27.1176 | 1118.66 | 0.0866 | 3.28565 | 9.92 |
| 27.3649 | 1564.78 | 0.1082 | 3.25651 | 13.88 |
| 27.6487 | 1001.23 | 0.1515 | 3.22374 | 8.88 |
| 29.4140 | 7265.68 | 0.1515 | 3.03415 | 64.46 |
| 29.8263 | 765.45 | 0.0866 | 2.99315 | 6.79 |
| 30.6040 | 4918.23 | 0.1299 | 2.91883 | 43.63 |
| 31.6959 | 11271.40 | 0.0792 | 2.82073 | 100.00 |
| 31.7887 | 6147.61 | 0.0396 | 2.81271 | 54.54 |
| 33.3521 | 1287.60 | 0.1848 | 2.68434 | 11.42 |
| 34.3502 | 1482.32 | 0.1584 | 2.60859 | 13.15 |
| 34.7709 | 2406.08 | 0.2904 | 2.57799 | 21.35 |
| 35.9933 | 2174.91 | 0.1452 | 2.49319 | 19.30 |
| 37.1237 | 1165.24 | 0.1320 | 2.41983 | 10.34 |
| 39.4535 | 1336.14 | 0.1848 | 2.28213 | 11.85 |
| 40.5922 | 739.88 | 0.1320 | 2.22070 | 6.56 |
| 41.6681 | 224.62 | 0.3168 | 2.16581 | 1.99 |
| 43.1718 | 840.88 | 0.1584 | 2.09380 | 7.46 |
| 45.4205 | 5058.34 | 0.1056 | 1.99523 | 44.88 |
| 45.5489 | 3119.43 | 0.0924 | 1.98990 | 27.68 |
| 47.1260 | 398.76 | 0.2112 | 1.92692 | 3.54 |
| 47.5209 | 1039.79 | 0.1848 | 1.91182 | 9.23 |
| 47.8597 | 1043.11 | 0.1584 | 1.89907 | 9.25 |
| 48.5034 | 982.55 | 0.2112 | 1.87537 | 8.72 |
| 50.7794 | 224.63 | 0.3168 | 1.79652 | 1.99 |
| 52.5746 | 1190.08 | 0.1848 | 1.73932 | 10.56 |
| 53.5047 | 390.70 | 0.2112 | 1.71126 | 3.47 |
| 54.3935 | 453.81 | 0.1848 | 1.68538 | 4.03 |
| 55.2493 | 180.61 | 0.3168 | 1.66128 | 1.60 |
| 56.4527 | 1120.86 | 0.1320 | 1.62869 | 9.94 |
| 57.4363 | 401.91 | 0.2112 | 1.60311 | 3.57 |
| 57.9653 | 348.78 | 0.2640 | 1.58974 | 3.09 |
| 60.6739 | 817.59 | 0.3168 | 1.52509 | 7.25 |
| 61.3214 | 752.47 | 0.4224 | 1.51053 | 6.68 |
| 62.9028 | 201.48 | 0.4224 | 1.47630 | 1.79 |
| 64.6518 | 301.65 | 0.2112 | 1.44053 | 2.68 |
| 66.1879 | 736.11 | 0.1584 | 1.41077 | 6.53 |
| 68.3136 | 459.91 | 0.0792 | 1.37196 | 4.08 |
| 69.2545 | 560.64 | 0.1848 | 1.35560 | 4.97 |
| 72.3490 | 355.85 | 0.3168 | 1.30505 | 3.16 |
| 73.8431 | 278.15 | 0.3168 | 1.28229 | 2.47 |
| 75.2786 | 902.57 | 0.1584 | 1.26136 | 8.01 |
| 78.2701 | 359.85 | 0.2112 | 1.22047 | 3.19 |
| 79.8777 | 472.62 | 0.0660 | 1.19990 | 4.19 |
| 81.2958 | 156.40 | 0.6336 | 1.18251 | 1.39 |
| 82.8057 | 72.96 | 0.6336 | 1.16474 | 0.65 |
| 83.9523 | 662.34 | 0.0792 | 1.15173 | 5.88 |

Pattern List

| Visible | Ref.Code | Score | Compound Name | Chem. Formula | Mineral Name | SemiQuant[%] |
| --- | --- | --- | --- | --- | --- | --- |
| * | 00-041-1478 | 65 | Sodium Aluminum Silicate Hydrate | Na ( Si2 Al ) O6 · H2 O | Analcime | 8 |
| * | 01-086-4272 | 58 | Calcium Carbonate | Ca ( C O3 ) | Calcite | 11 |
| * | 01-082-8023 | 32 | Sodium Magnesium Silicon Oxide Hydrate | Na2 Mg3 ( Si6 O16 ) ( H2 O )7 | Loughlinite | 5 |
| * | 01-085-8594 | 55 | Sodium Chloride | Na Cl | Halite | 11 |
| * | 04-013-9383 | 22 | Potassium Magnesium Aluminum Silicate Fluoride Hydroxide | K Mg3 Al Si3 O10 ( O H ) F | Phlogopite-2M1 | 16 |
| * | 04-011-6767 | 21 | Potassium Sodium Aluminum Silicate | K0.65 Na0.35 Al Si3 O8 | Sanidine | 12 |
| * | 04-016-0560 | 13 | Sodium Aluminum Iron Silicon Oxide Hydroxide | Na0.5 Fe2 Al0.5 Si3.5 O10 ( O H )2 | Nontronite | 7 |
| * | 04-018-6570 | 21 | Potassium Hydronium Magnesium Aluminum Silicon Oxide Hydroxide | K0.97 ( H3 O )0.03 Mg0.4 Al2.2 Si3.4 O10 ( O H )2 | Muscovite-2M1 | 29 |

Anchor Scan Parameters

Dataset Name	16 ETOSHA 22 MOISUB 3-15CM S3

File name	C:\aeris_data\XRD data\Goldstein\16 ETOSHA 22 MOISUB 3-15CM S3.xrdml

Sample Identification	16 ETOSHA 22 MOISUB 3-15CM S3

Measurement Start Date/Time	8/28/2023 1:54:13 PM

Operator	Instrument

Raw Data Origin	XRD measurement (*.XRDML)

Scan Axis	Gonio

Start Position [°2θ]	5.0064

End Position [°2θ]	84.9874

Step Size [°2θ]	0.0110

Scan Step Time [s]	48.1950

Scan Type	Continuous

PSD Mode	Scanning

PSD Length [°2θ]	5.54

Offset [°2θ]	0.0000

Divergence Slit Type	Fixed

Divergence Slit Size [°]	0.4584

Specimen Length [mm]	10.00

Measurement Temperature [°C]	25.00

Anode Material	Cu

K-α1 [Å]	1.54060

K-α2 [Å]	1.54443

K-β1 [Å]	1.39225

K-A2 / K-A1 Ratio	0.50000

Generator Settings	15 mA, 40 kV

Diffractometer Type	2082464

Diffractometer Number	0

Goniometer Radius [mm]	145.00

Dist. Focus-Diverg. Slit [mm]	95.00

Incident Beam Monochromator	No

Spinning	Yes