Etosha 22 SS Sub 0.5-5 cm S4

Graphics

Graphics

Graphics

Quantitative Results

Phase Sodium Aluminum Silicate Hydrate

Weight fraction/ %	6.0

Phase Calcium Carbonate

Weight fraction/ %	11.0

Phase Silicon Oxide

Weight fraction/ %	5.0

Phase Sodium Calcium Aluminum Silicate

Weight fraction/ %	1.0

Phase Sodium Chloride

Weight fraction/ %	31.0

Phase Potassium Aluminum Silicate

Weight fraction/ %	10.0

Phase Potassium Sodium Calcium Magnesium Aluminum Iron Silicon Oxide Hydroxide

Weight fraction/ %	7.0

Phase Sodium Magnesium Silicon Oxide Hydrate

Weight fraction/ %	3.0

Phase Potassium Hydronium Magnesium Aluminum Silicon Oxide Hydroxide

Weight fraction/ %	26.0

Multiple Quantitative Results

Scans vs Phases Matrix

| Scan name | Sodium Aluminum Silicate Hydrate | Calcium Carbonate | Silicon Oxide | Sodium Calcium Aluminum Silicate | Sodium Chloride | Potassium Aluminum Silicate | Potassium Sodium Calcium Magnesium Aluminum Iron Silicon Oxide Hydroxide | Sodium Magnesium Silicon Oxide Hydrate | Potassium Hydronium Magnesium Aluminum Silicon Oxide Hydroxide |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 19 ETOSHA 22 SSSUB 0.5-5CM S4 | 6.0 | 11.0 | 5.0 | 1.0 | 31.0 | 10.0 | 7.0 | 3.0 | 26.0 |

Anchor Scan Data

| Pos. [°2θ] | Iobs [cts] | Icalc [cts] | Iback [cts] |
| --- | --- | --- | --- |
| 5.0064 | 7850.0000 | 7848.8883 | 7850.0000 |
| 5.0174 | 8033.9149 | 7844.0703 | 7830.7392 |
| 5.0284 | 7790.6706 | 7824.9591 | 7811.4784 |
| 5.0394 | 7968.9941 | 7805.8505 | 7792.2175 |
| 5.0504 | 7792.9322 | 7786.7445 | 7772.9567 |
| 5.0614 | 7915.9995 | 7767.6411 | 7753.6959 |
| 5.0724 | 7757.4395 | 7748.5405 | 7734.4351 |
| 5.0834 | 7861.4597 | 7729.4426 | 7715.1743 |
| 5.0944 | 7695.2006 | 7710.3475 | 7695.9134 |
| 5.1054 | 7585.6726 | 7691.2553 | 7676.6526 |
| 5.1164 | 7597.3697 | 7672.1661 | 7657.3918 |
| 5.1274 | 7737.5310 | 7653.0799 | 7638.1310 |
| 5.1384 | 7633.3540 | 7633.9969 | 7618.8702 |
| 5.1494 | 7747.6445 | 7614.9170 | 7599.6093 |
| 5.1604 | 7690.2507 | 7595.8403 | 7580.3485 |
| 5.1714 | 7566.4779 | 7576.7670 | 7561.0877 |
| 5.1824 | 7776.3078 | 7557.6971 | 7541.8269 |
| 5.1934 | 7419.0148 | 7538.6307 | 7522.5660 |
| 5.2044 | 7447.9558 | 7519.5679 | 7503.3052 |
| 5.2154 | 7443.7670 | 7500.5088 | 7484.0444 |
| 5.2264 | 7339.5821 | 7481.4534 | 7464.7836 |
| 5.2374 | 7399.5133 | 7462.4019 | 7445.5228 |
| 5.2484 | 7368.5202 | 7443.3544 | 7426.2619 |
| 5.2594 | 7391.9961 | 7424.3109 | 7407.0011 |
| 5.2704 | 7388.7935 | 7405.2715 | 7387.7403 |
| 5.2814 | 7379.1863 | 7386.2364 | 7368.4795 |
| 5.2924 | 7235.0285 | 7367.2057 | 7349.2187 |
| 5.3034 | 7302.0619 | 7348.1795 | 7329.9578 |
| 5.3144 | 7250.2537 | 7329.1579 | 7310.6970 |
| 5.3254 | 7248.1293 | 7310.1410 | 7291.4362 |
| 5.3364 | 7243.0354 | 7291.1289 | 7272.1754 |
| 5.3474 | 7162.3447 | 7272.1218 | 7252.9146 |
| 5.3584 | 7231.3215 | 7253.1199 | 7233.6537 |
| 5.3694 | 7137.3555 | 7234.1231 | 7214.3929 |
| 5.3804 | 7132.9381 | 7215.1318 | 7195.1321 |
| 5.3914 | 7179.4115 | 7196.1460 | 7175.8713 |
| 5.4024 | 7086.2743 | 7177.1659 | 7156.6105 |
| 5.4134 | 7046.8215 | 7158.1917 | 7137.3496 |
| 5.4244 | 7097.9695 | 7139.2234 | 7118.0888 |
| 5.4354 | 7175.7611 | 7120.2614 | 7098.8280 |
| 5.4464 | 7111.6214 | 7101.3057 | 7079.5672 |
| 5.4574 | 7071.9602 | 7082.3565 | 7060.3063 |
| 5.4684 | 7020.5605 | 7063.4140 | 7041.0455 |
| 5.4794 | 6920.6426 | 7044.4785 | 7021.7847 |
| 5.4904 | 6944.6323 | 7025.5501 | 7002.5239 |
| 5.5014 | 6930.3673 | 7006.6289 | 6983.2631 |
| 5.5124 | 6966.7581 | 6987.7154 | 6964.0022 |
| 5.5234 | 6986.1160 | 6968.8096 | 6944.7414 |
| 5.5344 | 6872.9646 | 6957.6893 | 6925.4806 |
| 5.5454 | 6908.3732 | 6941.5010 | 6916.6986 |
| 5.5564 | 6966.6254 | 6933.0988 | 6907.9167 |
| 5.5674 | 6930.0310 | 6924.7053 | 6899.1347 |
| 5.5784 | 7067.5880 | 6916.3208 | 6890.3527 |
| 5.5894 | 7012.6863 | 6907.9456 | 6881.5707 |
| 5.6004 | 6977.8142 | 6899.5800 | 6872.7888 |
| 5.6114 | 6867.8545 | 6891.2243 | 6864.0068 |
| 5.6224 | 6890.3491 | 6882.8787 | 6855.2248 |
| 5.6334 | 6896.7729 | 6874.5437 | 6846.4428 |
| 5.6444 | 6800.3058 | 6866.2196 | 6837.6609 |
| 5.6554 | 6967.1475 | 6857.9066 | 6828.8789 |
| 5.6664 | 6910.2566 | 6849.6053 | 6820.0969 |
| 5.6774 | 6768.5310 | 6841.3159 | 6811.3149 |
| 5.6884 | 6800.2498 | 6833.0389 | 6802.5330 |
| 5.6994 | 6940.7965 | 6824.7747 | 6793.7510 |
| 5.7104 | 6867.4454 | 6816.5236 | 6784.9690 |
| 5.7214 | 6832.4076 | 6808.2863 | 6776.1870 |
| 5.7324 | 6873.9941 | 6800.0630 | 6767.4051 |
| 5.7434 | 6815.6494 | 6791.8544 | 6758.6231 |
| 5.7544 | 6997.4110 | 6783.6609 | 6749.8411 |
| 5.7654 | 6789.2079 | 6775.7315 | 6741.0591 |
| 5.7764 | 6843.9430 | 6767.8370 | 6732.2772 |
| 5.7874 | 6734.3363 | 6759.8202 | 6723.4952 |
| 5.7984 | 6693.8761 | 6751.8302 | 6714.7132 |
| 5.8094 | 6856.9907 | 6743.7266 | 6705.9312 |
| 5.8204 | 6899.6480 | 6735.6417 | 6697.1493 |
| 5.8314 | 6966.5280 | 6727.5764 | 6688.3673 |
| 5.8424 | 6878.5880 | 6719.5312 | 6679.5853 |
| 5.8534 | 6757.4843 | 6711.5070 | 6670.8033 |
| 5.8644 | 6898.6401 | 6703.5046 | 6662.0214 |
| 5.8754 | 6864.2183 | 6695.5247 | 6653.2394 |
| 5.8864 | 7040.9745 | 6687.5683 | 6644.4574 |
| 5.8974 | 6907.6062 | 6679.6364 | 6635.6754 |
| 5.9084 | 6781.1888 | 6671.7297 | 6626.8935 |
| 5.9194 | 6804.0929 | 6663.8495 | 6618.1115 |
| 5.9304 | 6761.3628 | 6655.9966 | 6609.3295 |
| 5.9414 | 6809.6952 | 6648.1724 | 6600.5475 |
| 5.9524 | 6981.2429 | 6640.3778 | 6591.7656 |
| 5.9634 | 7089.8392 | 6632.6142 | 6582.9836 |
| 5.9744 | 6928.6558 | 6624.8829 | 6574.2016 |
| 5.9854 | 6816.0246 | 6617.1851 | 6565.4196 |
| 5.9964 | 6948.2566 | 6609.5225 | 6556.6377 |
| 6.0074 | 6875.5979 | 6601.8964 | 6547.8557 |
| 6.0184 | 7097.6902 | 6594.3084 | 6539.0737 |
| 6.0294 | 6879.3098 | 6586.7604 | 6530.2917 |
| 6.0404 | 6963.7945 | 6579.2539 | 6521.5098 |
| 6.0514 | 6907.4238 | 6571.7910 | 6512.7278 |
| 6.0624 | 6978.2419 | 6563.8753 | 6503.9458 |
| 6.0734 | 6942.1962 | 6556.3324 | 6494.4926 |
| 6.0844 | 6881.3658 | 6548.3411 | 6485.0394 |
| 6.0954 | 6845.1107 | 6540.4019 | 6475.5862 |
| 6.1064 | 6998.2478 | 6532.5174 | 6466.1329 |
| 6.1174 | 7044.3461 | 6524.6901 | 6456.6797 |
| 6.1284 | 7124.5782 | 6516.9228 | 6447.2265 |
| 6.1394 | 7132.2187 | 6509.2185 | 6437.7733 |
| 6.1504 | 6966.1042 | 6501.5804 | 6428.3201 |
| 6.1614 | 6954.5472 | 6494.0118 | 6418.8669 |
| 6.1724 | 6999.7591 | 6486.5162 | 6409.4136 |
| 6.1834 | 7076.0737 | 6479.0975 | 6399.9604 |
| 6.1944 | 7027.1416 | 6471.7597 | 6390.5072 |
| 6.2054 | 7105.6849 | 6464.5070 | 6381.0540 |
| 6.2164 | 7143.7601 | 6457.3442 | 6371.6008 |
| 6.2274 | 7163.3938 | 6450.2762 | 6362.1475 |
| 6.2384 | 7206.3107 | 6443.3084 | 6352.6943 |
| 6.2494 | 7191.5000 | 6436.4464 | 6343.2411 |
| 6.2604 | 7197.5959 | 6429.6965 | 6333.7879 |
| 6.2714 | 7300.7212 | 6423.0654 | 6324.3347 |
| 6.2824 | 7312.8122 | 6416.5606 | 6314.8815 |
| 6.2934 | 7291.3363 | 6410.1900 | 6305.4282 |
| 6.3044 | 7223.1780 | 6403.9625 | 6295.9750 |
| 6.3154 | 7214.3702 | 6397.8879 | 6286.5218 |
| 6.3264 | 7330.4868 | 6391.9771 | 6277.0686 |
| 6.3374 | 7385.0482 | 6386.2423 | 6267.6154 |
| 6.3484 | 7400.9430 | 6380.6972 | 6258.1622 |
| 6.3594 | 7490.2198 | 6375.3574 | 6248.7089 |
| 6.3704 | 7519.4759 | 6370.2405 | 6239.2557 |
| 6.3814 | 7468.5801 | 6365.3669 | 6229.8025 |
| 6.3924 | 7455.7257 | 6360.7600 | 6220.3493 |
| 6.4034 | 7619.5581 | 6356.4467 | 6210.8961 |
| 6.4144 | 7625.9606 | 6352.4586 | 6201.4428 |
| 6.4254 | 7675.3068 | 6348.8319 | 6191.9896 |
| 6.4364 | 7700.0314 | 6345.6094 | 6182.5364 |
| 6.4474 | 7697.8786 | 6342.8403 | 6173.0832 |
| 6.4584 | 7882.0945 | 6340.5826 | 6163.6300 |
| 6.4694 | 7993.8678 | 6338.9034 | 6154.1768 |
| 6.4804 | 7936.3589 | 6337.8808 | 6144.7235 |
| 6.4914 | 7904.6150 | 6337.6050 | 6135.2703 |
| 6.5024 | 7881.4798 | 6338.1805 | 6125.8171 |
| 6.5134 | 7983.2070 | 6339.7270 | 6116.3639 |
| 6.5244 | 8178.0178 | 6342.3816 | 6106.9107 |
| 6.5354 | 8184.0319 | 6346.3002 | 6097.4575 |
| 6.5464 | 8164.6037 | 6351.6587 | 6088.0042 |
| 6.5574 | 8130.8141 | 6358.6548 | 6078.5510 |
| 6.5684 | 8166.4464 | 6367.5086 | 6069.0978 |
| 6.5794 | 8351.1918 | 6378.4634 | 6059.6446 |
| 6.5904 | 8323.3894 | 6391.7861 | 6050.1914 |
| 6.6014 | 8505.5015 | 6407.7663 | 6040.7381 |
| 6.6124 | 8423.1691 | 6426.7154 | 6031.2849 |
| 6.6234 | 8520.9263 | 6448.9649 | 6021.8317 |
| 6.6344 | 8560.3717 | 6474.8633 | 6012.3785 |
| 6.6454 | 8536.2276 | 6504.7724 | 6002.9253 |
| 6.6564 | 8535.2183 | 6539.0626 | 5993.4721 |
| 6.6674 | 8698.6303 | 6578.1066 | 5984.0188 |
| 6.6784 | 8807.6146 | 6622.2733 | 5974.5656 |
| 6.6894 | 8886.9204 | 6671.9190 | 5965.1124 |
| 6.7004 | 8934.3914 | 6727.3791 | 5955.6592 |
| 6.7114 | 8895.5546 | 6788.9578 | 5946.2060 |
| 6.7224 | 8929.5310 | 6856.9181 | 5936.7527 |
| 6.7334 | 9092.9076 | 6931.4703 | 5927.2995 |
| 6.7444 | 9011.7433 | 7012.7603 | 5917.8463 |
| 6.7554 | 9044.1711 | 7100.8574 | 5908.3931 |
| 6.7664 | 9296.3413 | 7195.7415 | 5898.9399 |
| 6.7774 | 9166.9808 | 7297.2898 | 5889.4867 |
| 6.7884 | 9177.8761 | 7405.2632 | 5880.0334 |
| 6.7994 | 9207.0000 | 7519.2906 | 5870.5802 |
| 6.8104 | 9207.1888 | 7638.8535 | 5861.1270 |
| 6.8214 | 9218.2434 | 7763.2674 | 5851.6738 |
| 6.8324 | 9194.7414 | 7891.6628 | 5842.2206 |
| 6.8434 | 9255.5285 | 8022.9639 | 5832.7674 |
| 6.8544 | 9173.5723 | 8155.8675 | 5823.3141 |
| 6.8654 | 9158.0172 | 8288.8227 | 5813.8609 |
| 6.8764 | 9215.4051 | 8420.0162 | 5804.4077 |
| 6.8874 | 9183.6062 | 8547.3676 | 5794.9545 |
| 6.8984 | 9124.4798 | 8668.5422 | 5785.5013 |
| 6.9094 | 9019.8377 | 8780.9884 | 5776.0480 |
| 6.9204 | 8927.3393 | 8882.0081 | 5766.5948 |
| 6.9314 | 9014.2635 | 8968.8634 | 5757.1416 |
| 6.9424 | 9041.3136 | 9038.9196 | 5747.6884 |
| 6.9534 | 8836.7860 | 9089.8142 | 5738.2352 |
| 6.9644 | 8671.7179 | 9119.6347 | 5728.7820 |
| 6.9754 | 8850.1671 | 9127.0791 | 5719.3287 |
| 6.9864 | 8588.0974 | 9111.5749 | 5709.8755 |
| 6.9974 | 8573.9719 | 9073.3327 | 5700.4223 |
| 7.0084 | 8440.0944 | 9013.3258 | 5690.9691 |
| 7.0194 | 8336.3672 | 8933.1990 | 5681.5159 |
| 7.0304 | 8198.4297 | 8835.1244 | 5672.0626 |
| 7.0414 | 8109.0309 | 8721.6284 | 5662.6094 |
| 7.0524 | 7986.1062 | 8595.4167 | 5653.1562 |
| 7.0634 | 7905.7959 | 8459.2182 | 5643.7030 |
| 7.0744 | 7836.8997 | 8315.6615 | 5634.2498 |
| 7.0854 | 7767.6947 | 8167.1874 | 5624.7966 |
| 7.0964 | 7653.1336 | 8015.9978 | 5615.3433 |
| 7.1074 | 7443.4547 | 7864.0316 | 5605.8901 |
| 7.1184 | 7354.8908 | 7712.4637 | 5596.4369 |
| 7.1294 | 7309.3982 | 7563.5356 | 5586.3124 |
| 7.1404 | 7312.0078 | 7417.6053 | 5576.1880 |
| 7.1514 | 7174.0663 | 7276.1356 | 5566.0635 |
| 7.1624 | 7041.6333 | 7139.8966 | 5555.9391 |
| 7.1734 | 6987.7777 | 7009.4835 | 5545.8146 |
| 7.1844 | 6876.0797 | 6885.3355 | 5535.6901 |
| 7.1954 | 6873.7989 | 6767.7526 | 5525.5657 |

Scan List

| Vis. | Dataset Name | Start pos. [°2θ] | End pos. [°2θ] | Step [°2θ] | Meas.Date/Time |
| --- | --- | --- | --- | --- | --- |
| * | 19 ETOSHA 22 SSSUB 0.5-5CM S4 | 5.0064 | 84.9874 | 0.0110 | 8/28/2023 11:03:48 AM |

Peak List

| Pos. [°2θ] | Height [cts] | FWHM Left [°2θ] | d-spacing [Å] | Rel. Int. [%] |
| --- | --- | --- | --- | --- |
| 6.9723 | 3046.34 | 0.3464 | 12.66795 | 8.06 |
| 8.7962 | 544.64 | 0.3031 | 10.04489 | 1.44 |
| 11.6426 | 196.86 | 0.4330 | 7.59466 | 0.52 |
| 13.6573 | 73.07 | 0.5196 | 6.47850 | 0.19 |
| 15.8606 | 5949.30 | 0.1191 | 5.58315 | 15.74 |
| 18.3043 | 1209.36 | 0.0541 | 4.84291 | 3.20 |
| 19.0433 | 616.62 | 0.0866 | 4.65662 | 1.63 |
| 19.8269 | 2235.02 | 0.1082 | 4.47431 | 5.91 |
| 20.8601 | 1538.23 | 0.0649 | 4.25497 | 4.07 |
| 21.4057 | 465.77 | 0.2598 | 4.14774 | 1.23 |
| 22.5125 | 108.14 | 0.1299 | 3.94626 | 0.29 |
| 23.0798 | 1089.87 | 0.1299 | 3.85052 | 2.88 |
| 23.4992 | 1058.27 | 0.1515 | 3.78274 | 2.80 |
| 24.3025 | 337.11 | 0.1299 | 3.65950 | 0.89 |
| 25.1462 | 440.40 | 0.2165 | 3.53859 | 1.16 |
| 26.0060 | 8827.50 | 0.1299 | 3.42352 | 23.35 |
| 26.5693 | 2664.89 | 0.0396 | 3.35221 | 7.05 |
| 26.6472 | 3997.77 | 0.0325 | 3.34258 | 10.57 |
| 27.0797 | 701.79 | 0.1082 | 3.29017 | 1.86 |
| 27.3577 | 2145.84 | 0.0541 | 3.25736 | 5.68 |
| 27.5836 | 786.84 | 0.1082 | 3.23120 | 2.08 |
| 28.0565 | 364.09 | 0.0866 | 3.17780 | 0.96 |
| 29.0168 | 428.30 | 0.0866 | 3.07478 | 1.13 |
| 29.3939 | 8078.13 | 0.1624 | 3.03619 | 21.37 |
| 29.8131 | 582.28 | 0.1082 | 2.99444 | 1.54 |
| 30.5962 | 4190.46 | 0.1191 | 2.91955 | 11.08 |
| 31.6972 | 37806.74 | 0.0660 | 2.82061 | 100.00 |
| 31.7872 | 18112.26 | 0.0396 | 2.81283 | 47.91 |
| 32.1231 | 1308.79 | 0.1320 | 2.78418 | 3.46 |
| 33.3064 | 1052.21 | 0.1848 | 2.68792 | 2.78 |
| 33.8408 | 682.61 | 0.1320 | 2.64668 | 1.81 |
| 34.7350 | 1820.23 | 0.2640 | 2.58057 | 4.81 |
| 35.9758 | 1795.99 | 0.3168 | 2.49436 | 4.75 |
| 37.1657 | 677.53 | 0.2904 | 2.41719 | 1.79 |
| 39.4297 | 1373.22 | 0.2376 | 2.28346 | 3.63 |
| 40.5603 | 584.25 | 0.1320 | 2.22237 | 1.55 |
| 41.6665 | 249.57 | 0.1584 | 2.16589 | 0.66 |
| 42.4215 | 293.81 | 0.0792 | 2.12908 | 0.78 |
| 43.1376 | 911.44 | 0.2640 | 2.09538 | 2.41 |
| 45.4530 | 10452.32 | 0.0660 | 1.99387 | 27.65 |
| 45.5796 | 4697.79 | 0.0660 | 1.98863 | 12.43 |
| 47.0977 | 504.35 | 0.1584 | 1.92801 | 1.33 |
| 47.5233 | 1113.66 | 0.2640 | 1.91173 | 2.95 |
| 47.8475 | 1029.32 | 0.0792 | 1.89953 | 2.72 |
| 48.4544 | 934.74 | 0.1056 | 1.87715 | 2.47 |
| 48.7960 | 866.01 | 0.1584 | 1.86480 | 2.29 |
| 50.7975 | 160.70 | 0.3696 | 1.79592 | 0.43 |
| 52.5600 | 1055.83 | 0.1320 | 1.73977 | 2.79 |
| 53.4620 | 274.78 | 0.2112 | 1.71253 | 0.73 |
| 53.8230 | 504.28 | 0.0924 | 1.70189 | 1.33 |
| 54.3542 | 340.15 | 0.2640 | 1.68651 | 0.90 |
| 55.2623 | 133.26 | 0.3168 | 1.66092 | 0.35 |
| 56.4465 | 3783.30 | 0.0660 | 1.62885 | 10.01 |
| 56.5998 | 2082.05 | 0.0792 | 1.62481 | 5.51 |
| 57.4173 | 453.42 | 0.2640 | 1.60360 | 1.20 |
| 57.8597 | 370.80 | 0.2112 | 1.59239 | 0.98 |
| 59.9524 | 540.11 | 0.0792 | 1.54171 | 1.43 |
| 60.6410 | 769.76 | 0.3168 | 1.52584 | 2.04 |
| 61.4050 | 589.89 | 0.3168 | 1.50867 | 1.56 |
| 62.9144 | 178.22 | 0.5280 | 1.47606 | 0.47 |
| 64.6259 | 260.82 | 0.3168 | 1.44104 | 0.69 |
| 66.2128 | 2377.51 | 0.0792 | 1.41030 | 6.29 |
| 66.3914 | 1155.71 | 0.0660 | 1.40694 | 3.06 |
| 68.2912 | 262.15 | 0.0792 | 1.37235 | 0.69 |
| 69.2275 | 454.57 | 0.1584 | 1.35606 | 1.20 |
| 72.3247 | 263.53 | 0.4224 | 1.30542 | 0.70 |
| 73.0173 | 292.97 | 0.1584 | 1.29474 | 0.77 |
| 73.8922 | 159.94 | 0.4224 | 1.28156 | 0.42 |
| 75.2727 | 2713.73 | 0.0924 | 1.26145 | 7.18 |
| 75.4838 | 1466.20 | 0.0924 | 1.25844 | 3.88 |
| 78.2637 | 316.19 | 0.2112 | 1.22055 | 0.84 |
| 81.4778 | 351.83 | 0.0792 | 1.18033 | 0.93 |
| 83.9389 | 1348.33 | 0.0924 | 1.15188 | 3.57 |
| 84.2190 | 719.34 | 0.1320 | 1.14876 | 1.90 |

Pattern List

| Visible | Ref.Code | Score | Compound Name | Chem. Formula | Mineral Name | SemiQuant[%] |
| --- | --- | --- | --- | --- | --- | --- |
| * | 00-041-1478 | 61 | Sodium Aluminum Silicate Hydrate | Na ( Si2 Al ) O6 · H2 O | Analcime | 6 |
| * | 01-083-1762 | 56 | Calcium Carbonate | Ca ( C O3 ) | Calcite | 11 |
| * | 04-002-3600 | 30 | Silicon Oxide | Si O2 | Quartz | 5 |
| * | 01-078-0432 | 24 | Sodium Calcium Aluminum Silicate | ( Na0.45 Ca0.55 ) ( Al1.55 Si2.45 O8 ) | Anorthite, Na-bearing, syn | 1 |
| * | 01-075-0306 | 51 | Sodium Chloride | Na Cl | Halite | 31 |
| * | 01-070-6187 | 26 | Potassium Aluminum Silicate | K ( Al Si3 O8 ) | Microcline | 10 |
| * | 04-017-0530 | 18 | Potassium Sodium Calcium Magnesium Aluminum Iron Silicon Oxide Hydroxide | K0.8 Na0.01 Ca0.03 Mg0.44 Fe1.08 Al0.97 Si3.56 O10 ( O H )2 | Glauconite (NR) | 7 |
| * | 01-082-8023 | 15 | Sodium Magnesium Silicon Oxide Hydrate | Na2 Mg3 ( Si6 O16 ) ( H2 O )7 | Loughlinite | 3 |
| * | 04-018-6570 | 13 | Potassium Hydronium Magnesium Aluminum Silicon Oxide Hydroxide | K0.97 ( H3 O )0.03 Mg0.4 Al2.2 Si3.4 O10 ( O H )2 | Muscovite-2M1 | 26 |

Anchor Scan Parameters

Dataset Name	19 ETOSHA 22 SSSUB 0.5-5CM S4

File name	C:\aeris_data\XRD data\Goldstein\19 ETOSHA 22 SSSUB 0.5-5CM S4.xrdml

Sample Identification	19 ETOSHA 22 SSSUB 0.5-5CM S4

Measurement Start Date/Time	8/28/2023 11:03:48 AM

Operator	Instrument

Raw Data Origin	XRD measurement (*.XRDML)

Scan Axis	Gonio

Start Position [°2θ]	5.0064

End Position [°2θ]	84.9874

Step Size [°2θ]	0.0110

Scan Step Time [s]	48.1950

Scan Type	Continuous

PSD Mode	Scanning

PSD Length [°2θ]	5.54

Offset [°2θ]	0.0000

Divergence Slit Type	Fixed

Divergence Slit Size [°]	0.4584

Specimen Length [mm]	10.00

Measurement Temperature [°C]	25.00

Anode Material	Cu

K-α1 [Å]	1.54060

K-α2 [Å]	1.54443

K-β1 [Å]	1.39225

K-A2 / K-A1 Ratio	0.50000

Generator Settings	15 mA, 40 kV

Diffractometer Type	2082464

Diffractometer Number	0

Goniometer Radius [mm]	145.00

Dist. Focus-Diverg. Slit [mm]	95.00

Incident Beam Monochromator	No

Spinning	Yes