Etosha 22 HS Crt 0-0.1 cm S4

Graphics

Graphics

Graphics

Quantitative Results

Phase Sodium Aluminum Silicate Hydrate

Weight fraction/ %	24.0

Phase Calcium Carbonate

Weight fraction/ %	11.0

Phase Silicon Oxide

Weight fraction/ %	16.0

Phase Potassium Sodium Barium Calcium Aluminum Silicate

Weight fraction/ %	9.0

Phase Sodium Magnesium Silicon Oxide Hydrate

Weight fraction/ %	2.0

Phase Potassium Sodium Magnesium Aluminum Iron Fluoride Silicate Hydroxide

Weight fraction/ %	8.0

Phase Potassium Hydronium Magnesium Aluminum Silicon Oxide Hydroxide

Weight fraction/ %	20.0

Phase Iron Arsenate Hydrate

Weight fraction/ %	10.0

Multiple Quantitative Results

Scans vs Phases Matrix

| Scan name | Sodium Aluminum Silicate Hydrate | Calcium Carbonate | Silicon Oxide | Potassium Sodium Barium Calcium Aluminum Silicate | Sodium Magnesium Silicon Oxide Hydrate | Potassium Sodium Magnesium Aluminum Iron Fluoride Silicate Hydroxide | Potassium Hydronium Magnesium Aluminum Silicon Oxide Hydroxide | Iron Arsenate Hydrate |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 20 ETOSHA 22 HSCRT 0-0.1CM S4 | 24.0 | 11.0 | 16.0 | 9.0 | 2.0 | 8.0 | 20.0 | 10.0 |

Anchor Scan Data

| Pos. [°2θ] | Iobs [cts] | Icalc [cts] | Iback [cts] |
| --- | --- | --- | --- |
| 5.0064 | 7909.0000 | 7923.4238 | 7909.0000 |
| 5.0174 | 7943.3732 | 7917.4267 | 7887.9264 |
| 5.0284 | 7895.1878 | 7896.7122 | 7866.8529 |
| 5.0394 | 7971.0855 | 7876.0043 | 7845.7793 |
| 5.0504 | 7691.9980 | 7855.3031 | 7824.7058 |
| 5.0614 | 7812.3633 | 7834.6089 | 7803.6322 |
| 5.0724 | 7872.6578 | 7813.9216 | 7782.5587 |
| 5.0834 | 7788.0098 | 7793.2417 | 7761.4851 |
| 5.0944 | 7730.6735 | 7772.5691 | 7740.4116 |
| 5.1054 | 7671.7522 | 7751.9041 | 7719.3380 |
| 5.1164 | 7530.7660 | 7731.2470 | 7698.2645 |
| 5.1274 | 7619.8063 | 7710.5978 | 7677.1909 |
| 5.1384 | 7561.5900 | 7689.9568 | 7656.1174 |
| 5.1494 | 7573.6283 | 7669.3242 | 7635.0438 |
| 5.1604 | 7574.0885 | 7648.7003 | 7613.9703 |
| 5.1714 | 7402.0634 | 7628.0852 | 7592.8967 |
| 5.1824 | 7553.9321 | 7607.4792 | 7571.8231 |
| 5.1934 | 7400.5664 | 7586.8825 | 7550.7496 |
| 5.2044 | 7447.9469 | 7566.2954 | 7529.6760 |
| 5.2154 | 7331.7483 | 7545.7181 | 7508.6025 |
| 5.2264 | 7398.6037 | 7525.1509 | 7487.5289 |
| 5.2374 | 7411.3201 | 7504.5941 | 7466.4554 |
| 5.2484 | 7349.0157 | 7484.0479 | 7445.3818 |
| 5.2594 | 7267.4941 | 7463.5127 | 7424.3083 |
| 5.2704 | 7232.1593 | 7442.9887 | 7403.2347 |
| 5.2814 | 7281.6711 | 7422.4763 | 7382.1612 |
| 5.2924 | 7267.7866 | 7401.9758 | 7361.0876 |
| 5.3034 | 7205.1460 | 7381.4874 | 7340.0141 |
| 5.3144 | 7248.0138 | 7361.0117 | 7318.9405 |
| 5.3254 | 7175.4853 | 7340.5489 | 7297.8669 |
| 5.3364 | 7201.1681 | 7320.0994 | 7276.7934 |
| 5.3474 | 7224.6672 | 7299.6635 | 7255.7198 |
| 5.3584 | 7138.9312 | 7279.2418 | 7234.6463 |
| 5.3694 | 7056.3791 | 7258.8345 | 7213.5727 |
| 5.3804 | 7058.3461 | 7238.4422 | 7192.4992 |
| 5.3914 | 7013.1092 | 7218.0653 | 7171.4256 |
| 5.4024 | 7051.1150 | 7197.7042 | 7150.3521 |
| 5.4134 | 6982.4523 | 7177.3594 | 7129.2785 |
| 5.4244 | 7016.2330 | 7157.0315 | 7108.2050 |
| 5.4354 | 7001.5605 | 7136.7208 | 7087.1314 |
| 5.4464 | 7003.3717 | 7116.4281 | 7066.0579 |
| 5.4574 | 7009.5123 | 7096.1538 | 7044.9843 |
| 5.4684 | 6979.4897 | 7075.8984 | 7023.9108 |
| 5.4794 | 7003.1863 | 7055.6627 | 7002.8372 |
| 5.4904 | 7031.5300 | 7035.4473 | 6981.7636 |
| 5.5014 | 7078.8053 | 7015.2527 | 6960.6901 |
| 5.5124 | 6903.4641 | 6995.0797 | 6939.6165 |
| 5.5234 | 6910.0851 | 6974.9289 | 6918.5430 |
| 5.5344 | 6929.3746 | 6963.5056 | 6897.4694 |
| 5.5454 | 6798.1490 | 6947.1556 | 6888.8543 |
| 5.5564 | 6988.7591 | 6939.5346 | 6880.2391 |
| 5.5674 | 6942.3053 | 6931.9389 | 6871.6240 |
| 5.5784 | 6841.7001 | 6924.3696 | 6863.0088 |
| 5.5894 | 6930.1254 | 6916.8273 | 6854.3937 |
| 5.6004 | 6957.0708 | 6909.3132 | 6845.7785 |
| 5.6114 | 6909.7915 | 6901.8281 | 6837.1634 |
| 5.6224 | 6937.8043 | 6894.3731 | 6828.5482 |
| 5.6334 | 6836.3967 | 6886.9493 | 6819.9331 |
| 5.6444 | 6903.7640 | 6879.5577 | 6811.3179 |
| 5.6554 | 6969.4041 | 6872.1995 | 6802.7028 |
| 5.6664 | 6927.3274 | 6864.8760 | 6794.0876 |
| 5.6774 | 6935.4916 | 6857.5884 | 6785.4725 |
| 5.6884 | 6946.2861 | 6850.3380 | 6776.8573 |
| 5.6994 | 6929.1903 | 6843.1263 | 6768.2422 |
| 5.7104 | 6936.5860 | 6835.9546 | 6759.6270 |
| 5.7214 | 6828.9503 | 6828.8245 | 6751.0119 |
| 5.7324 | 6735.2920 | 6821.7376 | 6742.3967 |
| 5.7434 | 6830.3491 | 6814.6956 | 6733.7816 |
| 5.7544 | 6947.6087 | 6807.9109 | 6725.1664 |
| 5.7654 | 6694.6135 | 6801.2934 | 6716.5513 |
| 5.7764 | 6886.9047 | 6794.5062 | 6707.9361 |
| 5.7874 | 6792.4823 | 6787.8307 | 6699.3210 |
| 5.7984 | 6771.2301 | 6781.0469 | 6690.7058 |
| 5.8094 | 6986.3393 | 6774.3200 | 6682.0907 |
| 5.8204 | 6880.0265 | 6767.6522 | 6673.4755 |
| 5.8314 | 6757.3023 | 6761.0461 | 6664.8604 |
| 5.8424 | 6990.8712 | 6754.5042 | 6656.2452 |
| 5.8534 | 6682.4346 | 6748.0294 | 6647.6300 |
| 5.8644 | 6925.7257 | 6741.6244 | 6639.0149 |
| 5.8754 | 7032.1573 | 6735.2925 | 6630.3997 |
| 5.8864 | 6879.6411 | 6729.0368 | 6621.7846 |
| 5.8974 | 6827.2212 | 6722.8609 | 6613.1694 |
| 5.9084 | 6956.1023 | 6716.7684 | 6604.5543 |
| 5.9194 | 6972.1446 | 6710.7632 | 6595.9391 |
| 5.9304 | 7115.7846 | 6704.8496 | 6587.3240 |
| 5.9414 | 6837.0629 | 6699.0321 | 6578.7088 |
| 5.9524 | 6763.6647 | 6693.3154 | 6570.0937 |
| 5.9634 | 6934.1077 | 6687.7048 | 6561.4785 |
| 5.9744 | 6859.4887 | 6682.2059 | 6552.8634 |
| 5.9854 | 6911.1268 | 6676.8249 | 6544.2482 |
| 5.9964 | 6930.9204 | 6671.5683 | 6535.6331 |
| 6.0074 | 6985.2650 | 6666.4435 | 6527.0179 |
| 6.0184 | 6854.6706 | 6661.4584 | 6518.4028 |
| 6.0294 | 7006.2773 | 6656.6218 | 6509.7876 |
| 6.0404 | 6969.5143 | 6651.9435 | 6501.1725 |
| 6.0514 | 6963.0413 | 6647.4343 | 6492.5573 |
| 6.0624 | 6995.4808 | 6642.9789 | 6483.9422 |
| 6.0734 | 6964.7768 | 6638.7905 | 6475.1449 |
| 6.0844 | 6945.7660 | 6634.6844 | 6466.3476 |
| 6.0954 | 7172.7743 | 6630.8051 | 6457.5503 |
| 6.1064 | 7120.8761 | 6627.1715 | 6448.7530 |
| 6.1174 | 7104.3446 | 6623.8052 | 6439.9557 |
| 6.1284 | 7074.9439 | 6620.7306 | 6431.1584 |
| 6.1394 | 7034.8102 | 6617.9753 | 6422.3611 |
| 6.1504 | 7106.9656 | 6615.5703 | 6413.5638 |
| 6.1614 | 7159.5015 | 6613.5510 | 6404.7665 |
| 6.1724 | 7220.4798 | 6611.9570 | 6395.9692 |
| 6.1834 | 7244.7271 | 6610.8332 | 6387.1719 |
| 6.1944 | 7260.2389 | 6610.2301 | 6378.3746 |
| 6.2054 | 7255.7124 | 6610.2046 | 6369.5773 |
| 6.2164 | 7248.8810 | 6610.8204 | 6360.7800 |
| 6.2274 | 7279.7065 | 6612.1486 | 6351.9826 |
| 6.2384 | 7241.5467 | 6614.2688 | 6343.1853 |
| 6.2494 | 7252.2222 | 6617.2691 | 6334.3880 |
| 6.2604 | 7276.4808 | 6621.2472 | 6325.5907 |
| 6.2714 | 7253.2124 | 6626.3110 | 6316.7934 |
| 6.2824 | 7331.5457 | 6632.5786 | 6307.9961 |
| 6.2934 | 7388.3407 | 6640.1793 | 6299.1988 |
| 6.3044 | 7470.1406 | 6649.2536 | 6290.4015 |
| 6.3154 | 7520.1957 | 6659.9537 | 6281.6042 |
| 6.3264 | 7533.3953 | 6672.4429 | 6272.8069 |
| 6.3374 | 7616.6962 | 6686.8964 | 6264.0096 |
| 6.3484 | 7641.0275 | 6703.4999 | 6255.2123 |
| 6.3594 | 7630.9130 | 6722.4500 | 6246.4150 |
| 6.3704 | 7586.6814 | 6743.9525 | 6237.6177 |
| 6.3814 | 7565.8648 | 6768.2216 | 6228.8204 |
| 6.3924 | 7769.9293 | 6795.4785 | 6220.0231 |
| 6.4034 | 7909.6342 | 6825.9493 | 6211.2258 |
| 6.4144 | 7948.8476 | 6859.8632 | 6202.4285 |
| 6.4254 | 7907.3923 | 6897.4498 | 6193.6312 |
| 6.4364 | 7850.0216 | 6938.9365 | 6184.8339 |
| 6.4474 | 7994.2611 | 6984.5452 | 6176.0366 |
| 6.4584 | 8089.6224 | 7034.4888 | 6167.2393 |
| 6.4694 | 8019.5472 | 7088.9678 | 6158.4420 |
| 6.4804 | 8037.2301 | 7148.1660 | 6149.6447 |
| 6.4914 | 8127.0177 | 7212.2468 | 6140.8474 |
| 6.5024 | 8257.7375 | 7281.3479 | 6132.0501 |
| 6.5134 | 8291.9548 | 7355.5777 | 6123.2528 |
| 6.5244 | 8186.8407 | 7435.0099 | 6114.4555 |
| 6.5354 | 8407.5458 | 7519.6791 | 6105.6582 |
| 6.5464 | 8516.0000 | 7609.5752 | 6096.8609 |
| 6.5574 | 8430.9675 | 7704.6388 | 6088.0636 |
| 6.5684 | 8486.4582 | 7804.7554 | 6079.2663 |
| 6.5794 | 8486.4528 | 7909.7498 | 6070.4690 |
| 6.5904 | 8592.4868 | 8019.3804 | 6061.6717 |
| 6.6014 | 8744.3304 | 8133.3319 | 6052.8744 |
| 6.6124 | 8640.3471 | 8251.2095 | 6044.0771 |
| 6.6234 | 8903.5104 | 8372.5304 | 6035.2798 |
| 6.6344 | 8951.2468 | 8496.7161 | 6026.4825 |
| 6.6454 | 8970.9410 | 8623.0839 | 6017.6852 |
| 6.6564 | 9048.5546 | 8750.8385 | 6008.8879 |
| 6.6674 | 9021.7704 | 8879.0634 | 6000.0906 |
| 6.6784 | 9035.8378 | 9006.7146 | 5991.2933 |
| 6.6894 | 9097.1151 | 9132.6158 | 5982.4960 |
| 6.7004 | 9229.1023 | 9255.4585 | 5973.6987 |
| 6.7114 | 9282.0148 | 9373.8076 | 5964.9014 |
| 6.7224 | 9263.0649 | 9486.1152 | 5956.1041 |
| 6.7334 | 9422.7670 | 9590.7448 | 5947.3068 |
| 6.7444 | 9392.6106 | 9686.0072 | 5938.5094 |
| 6.7554 | 9287.8923 | 9770.2078 | 5929.7121 |
| 6.7664 | 9477.2803 | 9841.7064 | 5920.9148 |
| 6.7774 | 9334.2345 | 9898.9848 | 5912.1175 |
| 6.7884 | 9570.8585 | 9940.7192 | 5903.3202 |
| 6.7994 | 9414.0413 | 9965.8499 | 5894.5229 |
| 6.8104 | 9427.8093 | 9973.6416 | 5885.7256 |
| 6.8214 | 9543.9986 | 9963.7284 | 5876.9283 |
| 6.8324 | 9643.9282 | 9936.1361 | 5868.1310 |
| 6.8434 | 9537.2679 | 9891.2807 | 5859.3337 |
| 6.8544 | 9365.5044 | 9829.9425 | 5850.5364 |
| 6.8654 | 9402.1833 | 9753.2192 | 5841.7391 |
| 6.8764 | 9250.7798 | 9662.4634 | 5832.9418 |
| 6.8874 | 9361.6902 | 9559.2126 | 5824.1445 |
| 6.8984 | 9109.1593 | 9445.1170 | 5815.3472 |
| 6.9094 | 9146.7655 | 9321.8728 | 5806.5499 |
| 6.9204 | 9077.3864 | 9191.1642 | 5797.7526 |
| 6.9314 | 9085.2453 | 9054.6176 | 5788.9553 |
| 6.9424 | 9092.2626 | 8913.7668 | 5780.1580 |
| 6.9534 | 9095.9409 | 8770.0309 | 5771.3607 |
| 6.9644 | 8840.1219 | 8624.7016 | 5762.5634 |
| 6.9754 | 8807.9882 | 8478.9380 | 5753.7661 |
| 6.9864 | 8750.6549 | 8333.7675 | 5744.9688 |
| 6.9974 | 8807.4979 | 8190.0907 | 5736.1715 |
| 7.0084 | 8499.7581 | 8048.6883 | 5727.3742 |
| 7.0194 | 8482.7124 | 7910.2292 | 5718.5769 |
| 7.0304 | 8421.3480 | 7775.2794 | 5709.7796 |
| 7.0414 | 8184.3629 | 7644.3101 | 5700.9823 |
| 7.0524 | 8287.6932 | 7517.7060 | 5692.1850 |
| 7.0634 | 8231.1101 | 7395.7723 | 5683.3877 |
| 7.0744 | 8114.5742 | 7278.7422 | 5674.5904 |
| 7.0854 | 7913.6415 | 7166.7829 | 5665.7931 |
| 7.0964 | 7796.6116 | 7060.0016 | 5656.9958 |
| 7.1074 | 7736.2890 | 6958.4512 | 5648.1985 |
| 7.1184 | 7596.4601 | 6861.9676 | 5639.4012 |
| 7.1294 | 7521.6121 | 6770.8337 | 5630.4217 |
| 7.1404 | 7513.1032 | 6684.6485 | 5621.4423 |
| 7.1514 | 7370.2920 | 6603.4680 | 5612.4628 |
| 7.1624 | 7263.2330 | 6527.1508 | 5603.4834 |
| 7.1734 | 7162.5624 | 6455.5310 | 5594.5039 |
| 7.1844 | 7189.2744 | 6388.4224 | 5585.5245 |
| 7.1954 | 7210.9223 | 6325.6228 | 5576.5450 |

Scan List

| Vis. | Dataset Name | Start pos. [°2θ] | End pos. [°2θ] | Step [°2θ] | Meas.Date/Time |
| --- | --- | --- | --- | --- | --- |
| * | 20 ETOSHA 22 HSCRT 0-0.1CM S4 | 5.0064 | 84.9874 | 0.0110 | 8/28/2023 11:55:55 AM |

Peak List

| Pos. [°2θ] | Height [cts] | FWHM Left [°2θ] | d-spacing [Å] | Rel. Int. [%] |
| --- | --- | --- | --- | --- |
| 6.8096 | 3651.69 | 0.4330 | 12.97020 | 27.01 |
| 8.7862 | 571.28 | 0.3031 | 10.05627 | 4.23 |
| 11.5662 | 286.21 | 0.2598 | 7.64464 | 2.12 |
| 13.5425 | 120.74 | 0.5196 | 6.53316 | 0.89 |
| 15.8080 | 7768.23 | 0.1299 | 5.60163 | 57.46 |
| 18.2702 | 1328.43 | 0.1299 | 4.85189 | 9.83 |
| 19.8687 | 2574.99 | 0.3247 | 4.46498 | 19.05 |
| 20.9111 | 1276.58 | 0.0649 | 4.24471 | 9.44 |
| 21.3263 | 554.00 | 0.2165 | 4.16299 | 4.10 |
| 22.4955 | 141.28 | 0.1948 | 3.94921 | 1.04 |
| 23.0533 | 1233.10 | 0.1082 | 3.85490 | 9.12 |
| 23.4993 | 1168.48 | 0.1515 | 3.78273 | 8.64 |
| 24.2685 | 352.44 | 0.1299 | 3.66455 | 2.61 |
| 25.9669 | 11043.69 | 0.1407 | 3.42858 | 81.69 |
| 26.5828 | 13519.55 | 0.0541 | 3.35053 | 100.00 |
| 27.0351 | 1134.29 | 0.1299 | 3.29550 | 8.39 |
| 27.5773 | 1154.94 | 0.1082 | 3.23192 | 8.54 |
| 29.3582 | 11625.17 | 0.1515 | 3.03979 | 85.99 |
| 29.7790 | 862.04 | 0.1299 | 2.99779 | 6.38 |
| 30.5602 | 5020.34 | 0.1082 | 2.92292 | 37.13 |
| 31.9117 | 456.14 | 0.1515 | 2.80214 | 3.37 |
| 32.3109 | 178.56 | 0.1299 | 2.76843 | 1.32 |
| 33.2810 | 1356.91 | 0.1082 | 2.68991 | 10.04 |
| 34.3009 | 1475.70 | 0.1732 | 2.61223 | 10.92 |
| 34.7125 | 2381.89 | 0.2598 | 2.58219 | 17.62 |
| 35.9277 | 2786.48 | 0.0758 | 2.49759 | 20.61 |
| 37.0249 | 1200.23 | 0.1299 | 2.42606 | 8.88 |
| 39.3580 | 1881.43 | 0.1948 | 2.28745 | 13.92 |
| 40.5489 | 731.50 | 0.1515 | 2.22298 | 5.41 |
| 41.6468 | 220.22 | 0.2598 | 2.16687 | 1.63 |
| 42.4133 | 165.52 | 0.2598 | 2.12947 | 1.22 |
| 43.1060 | 1418.89 | 0.1948 | 2.09684 | 10.50 |
| 44.8354 | 181.34 | 0.3464 | 2.01990 | 1.34 |
| 45.7437 | 143.06 | 0.5196 | 1.98188 | 1.06 |
| 47.0627 | 575.88 | 0.1732 | 1.92936 | 4.26 |
| 47.4243 | 1386.84 | 0.1082 | 1.91549 | 10.26 |
| 47.8077 | 1163.64 | 0.1082 | 1.90102 | 8.61 |
| 48.4226 | 1390.22 | 0.1082 | 1.87830 | 10.28 |
| 50.8172 | 197.71 | 0.3464 | 1.79527 | 1.46 |
| 52.5207 | 1300.93 | 0.1948 | 1.74098 | 9.62 |
| 53.4212 | 398.42 | 0.2165 | 1.71374 | 2.95 |
| 54.3295 | 511.64 | 0.1732 | 1.68721 | 3.78 |
| 54.8169 | 1039.93 | 0.0792 | 1.67336 | 7.69 |
| 54.9692 | 512.84 | 0.0792 | 1.66908 | 3.79 |
| 56.5599 | 320.82 | 0.2112 | 1.62586 | 2.37 |
| 57.3661 | 630.05 | 0.1848 | 1.60491 | 4.66 |
| 57.8185 | 474.56 | 0.1584 | 1.59343 | 3.51 |
| 59.8688 | 463.49 | 0.0792 | 1.54366 | 3.43 |
| 60.6627 | 1016.11 | 0.2640 | 1.52534 | 7.52 |
| 61.3323 | 780.04 | 0.3168 | 1.51029 | 5.77 |
| 62.8987 | 196.02 | 0.3168 | 1.47639 | 1.45 |
| 63.9929 | 279.76 | 0.1188 | 1.45376 | 2.07 |
| 64.7168 | 388.48 | 0.3696 | 1.43924 | 2.87 |
| 66.0457 | 438.16 | 0.2112 | 1.41346 | 3.24 |
| 67.6848 | 296.99 | 0.1056 | 1.38317 | 2.20 |
| 68.3215 | 183.14 | 0.3168 | 1.37182 | 1.35 |
| 69.1639 | 479.59 | 0.3696 | 1.35715 | 3.55 |
| 72.3022 | 371.70 | 0.3168 | 1.30578 | 2.75 |
| 73.7549 | 293.07 | 0.2640 | 1.28361 | 2.17 |
| 75.2530 | 217.16 | 0.1584 | 1.26173 | 1.61 |
| 78.1957 | 318.15 | 0.2640 | 1.22144 | 2.35 |
| 81.4775 | 189.98 | 0.6336 | 1.18033 | 1.41 |
| 82.6450 | 124.05 | 0.3168 | 1.16659 | 0.92 |
| 83.8349 | 184.98 | 0.5280 | 1.15304 | 1.37 |

Pattern List

| Visible | Ref.Code | Score | Compound Name | Chem. Formula | Mineral Name | SemiQuant[%] |
| --- | --- | --- | --- | --- | --- | --- |
| * | 04-011-6752 | 67 | Sodium Aluminum Silicate Hydrate | Na8 Al8 Si16 O48 ( H2 O )8 | Analcime | 24 |
| * | 01-086-4273 | 49 | Calcium Carbonate | Ca ( C O3 ) | Calcite | 11 |
| * | 01-075-8320 | 28 | Silicon Oxide | Si O2 | Quartz | 16 |
| * | 01-076-0825 | 19 | Potassium Sodium Barium Calcium Aluminum Silicate | ( K0.88 Na0.1 Ca0.01 Ba0.01 ) ( Al1.005 Si2.995 O8 ) | Orthoclase | 9 |
| * | 01-082-8023 | 23 | Sodium Magnesium Silicon Oxide Hydrate | Na2 Mg3 ( Si6 O16 ) ( H2 O )7 | Loughlinite | 2 |
| * | 04-012-9908 | 25 | Potassium Sodium Magnesium Aluminum Iron Fluoride Silicate Hydroxide | K0.82 Na0.115 Mg2.28 Fe0.12 Al1.71 Si2.785 O10 ( O H )1.932 F0.068 | Phlogopite-1M | 8 |
| * | 04-018-6570 | 17 | Potassium Hydronium Magnesium Aluminum Silicon Oxide Hydroxide | K0.97 ( H3 O )0.03 Mg0.4 Al2.2 Si3.4 O10 ( O H )2 | Muscovite-2M1 | 20 |
| * | 01-070-0825 | 21 | Iron Arsenate Hydrate | Fe ( As O4 ) ( H2 O )2 | Scorodite | 10 |

Anchor Scan Parameters

Dataset Name	20 ETOSHA 22 HSCRT 0-0.1CM S4

File name	C:\aeris_data\XRD data\Goldstein\20 ETOSHA 22 HSCRT 0-0.1CM S4.xrdml

Sample Identification	20 ETOSHA 22 HSCRT 0-0.1CM S4

Measurement Start Date/Time	8/28/2023 11:55:55 AM

Operator	Instrument

Raw Data Origin	XRD measurement (*.XRDML)

Scan Axis	Gonio

Start Position [°2θ]	5.0064

End Position [°2θ]	84.9874

Step Size [°2θ]	0.0110

Scan Step Time [s]	48.1950

Scan Type	Continuous

PSD Mode	Scanning

PSD Length [°2θ]	5.54

Offset [°2θ]	0.0000

Divergence Slit Type	Fixed

Divergence Slit Size [°]	0.4584

Specimen Length [mm]	10.00

Measurement Temperature [°C]	25.00

Anode Material	Cu

K-α1 [Å]	1.54060

K-α2 [Å]	1.54443

K-β1 [Å]	1.39225

K-A2 / K-A1 Ratio	0.50000

Generator Settings	15 mA, 40 kV

Diffractometer Type	2082464

Diffractometer Number	0

Goniometer Radius [mm]	145.00

Dist. Focus-Diverg. Slit [mm]	95.00

Incident Beam Monochromator	No

Spinning	Yes