Etosha 22 MoiSub 2.5-15 cm S4

Graphics

Graphics

Graphics

Quantitative Results

Phase Sodium Aluminum Silicate Hydrate

Weight fraction/ %	22.0

Phase Calcium Carbonate

Weight fraction/ %	16.0

Phase Sodium Chloride

Weight fraction/ %	5.0

Phase Potassium Aluminum Silicate

Weight fraction/ %	12.0

Phase Sodium Magnesium Silicon Oxide Hydrate

Weight fraction/ %	3.0

Phase Calcium Sodium Aluminum Silicate

Weight fraction/ %	18.0

Phase Potassium Hydronium Magnesium Aluminum Silicon Oxide Hydroxide

Weight fraction/ %	25.0

Multiple Quantitative Results

Scans vs Phases Matrix

| Scan name | Sodium Aluminum Silicate Hydrate | Calcium Carbonate | Sodium Chloride | Potassium Aluminum Silicate | Sodium Magnesium Silicon Oxide Hydrate | Calcium Sodium Aluminum Silicate | Potassium Hydronium Magnesium Aluminum Silicon Oxide Hydroxide |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 22 ETOSHA 22 MOISUB 2.5-15CM S4 | 22.0 | 16.0 | 5.0 | 12.0 | 3.0 | 18.0 | 25.0 |

Anchor Scan Data

| Pos. [°2θ] | Iobs [cts] | Icalc [cts] | Iback [cts] |
| --- | --- | --- | --- |
| 5.0064 | 7367.0000 | 7383.4386 | 7367.0000 |
| 5.0174 | 7263.8358 | 7364.2388 | 7340.3183 |
| 5.0284 | 7329.0580 | 7337.8279 | 7313.6365 |
| 5.0394 | 7246.0634 | 7311.4215 | 7286.9548 |
| 5.0504 | 7091.0492 | 7285.0200 | 7260.2731 |
| 5.0614 | 7088.0054 | 7258.6234 | 7233.5914 |
| 5.0724 | 7038.7994 | 7232.2317 | 7206.9096 |
| 5.0834 | 7173.6642 | 7205.8452 | 7180.2279 |
| 5.0944 | 7035.9331 | 7179.4639 | 7153.5462 |
| 5.1054 | 7057.9513 | 7153.0880 | 7126.8644 |
| 5.1164 | 6969.0905 | 7126.7176 | 7100.1827 |
| 5.1274 | 7114.9061 | 7100.3528 | 7073.5010 |
| 5.1384 | 6923.6637 | 7073.9938 | 7046.8193 |
| 5.1494 | 6810.9621 | 7047.6407 | 7020.1375 |
| 5.1604 | 6932.7050 | 7021.2937 | 6993.4558 |
| 5.1714 | 6813.2124 | 6994.9528 | 6966.7741 |
| 5.1824 | 6807.6608 | 6968.6183 | 6940.0923 |
| 5.1934 | 6760.6711 | 6942.2904 | 6913.4106 |
| 5.2044 | 6833.2743 | 6915.9691 | 6886.7289 |
| 5.2154 | 6851.0423 | 6889.6546 | 6860.0472 |
| 5.2264 | 6755.7542 | 6863.3472 | 6833.3654 |
| 5.2374 | 6706.9911 | 6837.0470 | 6806.6837 |
| 5.2484 | 6596.0403 | 6810.7542 | 6780.0020 |
| 5.2594 | 6650.0595 | 6784.4689 | 6753.3202 |
| 5.2704 | 6615.2743 | 6758.1915 | 6726.6385 |
| 5.2814 | 6642.3909 | 6731.9220 | 6699.9568 |
| 5.2924 | 6572.5605 | 6705.6607 | 6673.2751 |
| 5.3034 | 6450.3142 | 6679.4079 | 6646.5933 |
| 5.3144 | 6476.5516 | 6653.1637 | 6619.9116 |
| 5.3254 | 6457.6032 | 6626.9284 | 6593.2299 |
| 5.3364 | 6358.9440 | 6600.7022 | 6566.5481 |
| 5.3474 | 6425.9184 | 6574.4854 | 6539.8664 |
| 5.3584 | 6496.0492 | 6548.2782 | 6513.1847 |
| 5.3694 | 6455.5044 | 6522.0809 | 6486.5030 |
| 5.3804 | 6417.8987 | 6495.8938 | 6459.8212 |
| 5.3914 | 6285.8378 | 6469.7171 | 6433.1395 |
| 5.4024 | 6283.4248 | 6443.5512 | 6406.4578 |
| 5.4134 | 6266.7163 | 6417.3964 | 6379.7761 |
| 5.4244 | 6206.8387 | 6391.2530 | 6353.0943 |
| 5.4354 | 6208.7861 | 6365.1213 | 6326.4126 |
| 5.4464 | 6167.4375 | 6339.0016 | 6299.7309 |
| 5.4574 | 6166.1726 | 6312.8944 | 6273.0491 |
| 5.4684 | 6250.4838 | 6286.7999 | 6246.3674 |
| 5.4794 | 6186.0496 | 6260.7186 | 6219.6857 |
| 5.4904 | 6216.6106 | 6234.6509 | 6193.0040 |
| 5.5014 | 6187.5708 | 6208.5971 | 6166.3222 |
| 5.5124 | 6053.6804 | 6182.5578 | 6139.6405 |
| 5.5234 | 6074.5010 | 6156.5332 | 6112.9588 |
| 5.5344 | 6092.0413 | 6136.1309 | 6086.2770 |
| 5.5454 | 6133.6239 | 6125.2632 | 6080.3280 |
| 5.5564 | 6056.8495 | 6120.0187 | 6074.3789 |
| 5.5674 | 6064.8628 | 6114.7910 | 6068.4299 |
| 5.5784 | 6084.8781 | 6109.5806 | 6062.4809 |
| 5.5894 | 6050.7601 | 6104.3881 | 6056.5318 |
| 5.6004 | 6041.0000 | 6099.2141 | 6050.5828 |
| 5.6114 | 6009.9036 | 6094.0591 | 6044.6337 |
| 5.6224 | 5990.1819 | 6088.9238 | 6038.6847 |
| 5.6334 | 6006.9159 | 6083.8088 | 6032.7356 |
| 5.6444 | 6010.0098 | 6078.7149 | 6026.7866 |
| 5.6554 | 5997.1224 | 6073.6427 | 6020.8375 |
| 5.6664 | 5985.6254 | 6068.5930 | 6014.8885 |
| 5.6774 | 5956.0088 | 6063.5665 | 6008.9395 |
| 5.6884 | 6043.0177 | 6058.5641 | 6002.9904 |
| 5.6994 | 5863.1548 | 6053.5865 | 5997.0414 |
| 5.7104 | 5873.5831 | 6048.6347 | 5991.0923 |
| 5.7214 | 5890.6032 | 6043.7096 | 5985.1433 |
| 5.7324 | 5927.3156 | 6038.8121 | 5979.1942 |
| 5.7434 | 6003.5271 | 6033.9433 | 5973.2452 |
| 5.7544 | 6005.4631 | 6029.1041 | 5967.2961 |
| 5.7654 | 5809.6371 | 6024.2956 | 5961.3471 |
| 5.7764 | 5777.5811 | 6019.5191 | 5955.3980 |
| 5.7874 | 5854.7945 | 6014.7756 | 5949.4490 |
| 5.7984 | 5899.6283 | 6010.0664 | 5943.5000 |
| 5.8094 | 5994.6219 | 6005.3929 | 5937.5509 |
| 5.8204 | 5885.8505 | 6000.7564 | 5931.6019 |
| 5.8314 | 5764.3023 | 5996.1583 | 5925.6528 |
| 5.8424 | 5873.6333 | 5991.6002 | 5919.7038 |
| 5.8534 | 5852.6613 | 5987.0836 | 5913.7547 |
| 5.8644 | 5808.8171 | 5982.6101 | 5907.8057 |
| 5.8754 | 5905.0703 | 5978.1815 | 5901.8566 |
| 5.8864 | 5731.0088 | 5973.7997 | 5895.9076 |
| 5.8974 | 5975.8983 | 5969.4666 | 5889.9586 |
| 5.9084 | 5844.5821 | 5965.1841 | 5884.0095 |
| 5.9194 | 5917.5969 | 5960.9544 | 5878.0605 |
| 5.9304 | 5902.9322 | 5956.7798 | 5872.1114 |
| 5.9414 | 6045.3471 | 5952.6627 | 5866.1624 |
| 5.9524 | 5942.5782 | 5948.6055 | 5860.2133 |
| 5.9634 | 5877.0575 | 5944.6109 | 5854.2643 |
| 5.9744 | 5778.3009 | 5940.6818 | 5848.3152 |
| 5.9854 | 6018.3756 | 5936.8211 | 5842.3662 |
| 5.9964 | 6018.3894 | 5933.0320 | 5836.4171 |
| 6.0074 | 5968.6868 | 5929.3180 | 5830.4681 |
| 6.0184 | 5840.0394 | 5925.6826 | 5824.5191 |
| 6.0294 | 5919.1121 | 5922.1299 | 5818.5700 |
| 6.0404 | 5816.2163 | 5918.6640 | 5812.6210 |
| 6.0514 | 5953.2621 | 5915.2894 | 5806.6719 |
| 6.0624 | 6002.8702 | 5911.9147 | 5800.7229 |
| 6.0734 | 5888.4892 | 5908.5439 | 5794.4832 |
| 6.0844 | 6020.5664 | 5905.1841 | 5788.2436 |
| 6.0954 | 6061.3672 | 5901.9383 | 5782.0040 |
| 6.1064 | 5983.3314 | 5898.8133 | 5775.7643 |
| 6.1174 | 6010.4140 | 5895.8172 | 5769.5247 |
| 6.1284 | 6015.4631 | 5892.9583 | 5763.2850 |
| 6.1394 | 5974.7527 | 5890.2465 | 5757.0454 |
| 6.1504 | 5938.9322 | 5887.6923 | 5750.8058 |
| 6.1614 | 6078.4793 | 5885.3079 | 5744.5661 |
| 6.1724 | 6091.6510 | 5883.1066 | 5738.3265 |
| 6.1834 | 6161.5089 | 5881.1037 | 5732.0869 |
| 6.1944 | 6185.5664 | 5879.3163 | 5725.8472 |
| 6.2054 | 6182.0521 | 5877.7638 | 5719.6076 |
| 6.2164 | 6136.4553 | 5876.4679 | 5713.3679 |
| 6.2274 | 6178.1328 | 5875.4534 | 5707.1283 |
| 6.2384 | 6241.8613 | 5874.7482 | 5700.8887 |
| 6.2494 | 6214.0556 | 5874.3839 | 5694.6490 |
| 6.2604 | 6338.8201 | 5874.3961 | 5688.4094 |
| 6.2714 | 6362.6445 | 5874.8249 | 5682.1697 |
| 6.2824 | 6399.4563 | 5875.7156 | 5675.9301 |
| 6.2934 | 6442.7124 | 5877.1188 | 5669.6905 |
| 6.3044 | 6395.9449 | 5879.0914 | 5663.4508 |
| 6.3154 | 6388.9612 | 5881.6967 | 5657.2112 |
| 6.3264 | 6423.6342 | 5885.0052 | 5650.9715 |
| 6.3374 | 6422.3127 | 5889.0953 | 5644.7319 |
| 6.3484 | 6508.4818 | 5894.0533 | 5638.4923 |
| 6.3594 | 6565.3850 | 5899.9742 | 5632.2526 |
| 6.3704 | 6626.6323 | 5906.9620 | 5626.0130 |
| 6.3814 | 6542.7964 | 5915.1301 | 5619.7734 |
| 6.3924 | 6509.7080 | 5924.6015 | 5613.5337 |
| 6.4034 | 6651.1200 | 5935.5085 | 5607.2941 |
| 6.4144 | 6756.6755 | 5947.9934 | 5601.0544 |
| 6.4254 | 6809.6918 | 5962.2076 | 5594.8148 |
| 6.4364 | 6853.9135 | 5978.3113 | 5588.5752 |
| 6.4474 | 6903.5570 | 5996.4733 | 5582.3355 |
| 6.4584 | 6985.9971 | 6016.8694 | 5576.0959 |
| 6.4694 | 6944.2959 | 6039.6819 | 5569.8562 |
| 6.4804 | 7004.4612 | 6065.0980 | 5563.6166 |
| 6.4914 | 7028.3761 | 6093.3081 | 5557.3770 |
| 6.5024 | 7085.5458 | 6124.5038 | 5551.1373 |
| 6.5134 | 7206.8004 | 6158.8756 | 5544.8977 |
| 6.5244 | 7330.2360 | 6196.6109 | 5538.6580 |
| 6.5354 | 7347.8717 | 6237.8907 | 5532.4184 |
| 6.5464 | 7405.5880 | 6282.8867 | 5526.1788 |
| 6.5574 | 7419.2714 | 6331.7582 | 5519.9391 |
| 6.5684 | 7521.5821 | 6384.6487 | 5513.6995 |
| 6.5794 | 7519.3613 | 6441.6823 | 5507.4599 |
| 6.5904 | 7660.2124 | 6502.8535 | 5501.2202 |
| 6.6014 | 7575.3721 | 6568.2347 | 5494.6611 |
| 6.6124 | 7751.9244 | 6637.8696 | 5488.1020 |
| 6.6234 | 7898.9735 | 6711.8714 | 5481.5429 |
| 6.6344 | 7844.0069 | 6790.2077 | 5474.9838 |
| 6.6454 | 7977.4774 | 6872.8022 | 5468.4246 |
| 6.6564 | 7895.7935 | 6959.5297 | 5461.8655 |
| 6.6674 | 8059.8850 | 7050.2117 | 5455.3064 |
| 6.6784 | 8205.6077 | 7144.6108 | 5448.7473 |
| 6.6894 | 8200.1062 | 7242.4254 | 5442.1882 |
| 6.7004 | 8216.6421 | 7343.2834 | 5435.6291 |
| 6.7114 | 8307.7011 | 7446.7354 | 5429.0700 |
| 6.7224 | 8269.2950 | 7552.2483 | 5422.5108 |
| 6.7334 | 8419.3294 | 7659.1977 | 5415.9517 |
| 6.7444 | 8441.3619 | 7766.8609 | 5409.3926 |
| 6.7554 | 8265.4586 | 7874.4108 | 5402.8335 |
| 6.7664 | 8332.3924 | 7980.9110 | 5396.2744 |
| 6.7774 | 8435.8225 | 8085.3142 | 5389.7153 |
| 6.7884 | 8508.3717 | 8186.4646 | 5383.1561 |
| 6.7994 | 8568.4321 | 8283.1064 | 5376.5970 |
| 6.8104 | 8403.4651 | 8373.9002 | 5370.0379 |
| 6.8214 | 8372.1578 | 8457.4493 | 5363.4788 |
| 6.8324 | 8444.9036 | 8532.3346 | 5356.9197 |
| 6.8434 | 8401.6284 | 8597.1617 | 5350.3606 |
| 6.8544 | 8516.3274 | 8650.6143 | 5343.8015 |
| 6.8654 | 8455.0979 | 8691.5144 | 5337.2423 |
| 6.8764 | 8502.8564 | 8718.8821 | 5330.6832 |
| 6.8874 | 8256.8717 | 8731.9900 | 5324.1241 |
| 6.8984 | 8328.6017 | 8730.4069 | 5317.5650 |
| 6.9094 | 8213.5487 | 8714.0239 | 5311.0059 |
| 6.9204 | 8225.3126 | 8683.0620 | 5304.4468 |
| 6.9314 | 8073.2659 | 8638.0574 | 5297.8877 |
| 6.9424 | 7937.9922 | 8579.8288 | 5291.3285 |
| 6.9534 | 8080.2359 | 8509.4295 | 5284.7694 |
| 6.9644 | 7955.8387 | 8428.0907 | 5278.2103 |
| 6.9754 | 7841.5909 | 8337.1606 | 5271.6512 |
| 6.9864 | 7735.5044 | 8238.0467 | 5265.0921 |
| 6.9974 | 7603.9906 | 8132.1641 | 5258.5330 |
| 7.0084 | 7547.7532 | 8020.8926 | 5251.9739 |
| 7.0194 | 7437.9011 | 7905.5450 | 5245.4147 |
| 7.0304 | 7260.4601 | 7787.3441 | 5238.8556 |
| 7.0414 | 7205.7753 | 7667.4095 | 5232.2965 |
| 7.0524 | 7168.6135 | 7546.7510 | 5225.7374 |
| 7.0634 | 6995.0157 | 7426.2678 | 5219.1783 |
| 7.0744 | 6958.4818 | 7306.7513 | 5212.6192 |
| 7.0854 | 6875.5575 | 7188.8905 | 5206.0601 |
| 7.0964 | 6791.7227 | 7073.2787 | 5199.5009 |
| 7.1074 | 6694.8717 | 6960.4203 | 5192.9418 |
| 7.1184 | 6674.6047 | 6850.6561 | 5186.3827 |
| 7.1294 | 6596.1514 | 6744.3331 | 5179.5768 |
| 7.1404 | 6459.3264 | 6641.7321 | 5172.7708 |
| 7.1514 | 6375.8584 | 6543.1521 | 5165.9649 |
| 7.1624 | 6344.9567 | 6448.7534 | 5159.1589 |
| 7.1734 | 6325.2694 | 6358.6443 | 5152.3530 |
| 7.1844 | 6227.4247 | 6272.8862 | 5145.5471 |
| 7.1954 | 6054.4611 | 6191.4977 | 5138.7411 |

Scan List

| Vis. | Dataset Name | Start pos. [°2θ] | End pos. [°2θ] | Step [°2θ] | Meas.Date/Time |
| --- | --- | --- | --- | --- | --- |
| * | 22 ETOSHA 22 MOISUB 2.5-15CM S4 | 5.0064 | 84.9874 | 0.0110 | 8/28/2023 2:46:16 PM |

Peak List

| Pos. [°2θ] | Height [cts] | FWHM Left [°2θ] | d-spacing [Å] | Rel. Int. [%] |
| --- | --- | --- | --- | --- |
| 6.8909 | 3043.25 | 0.4330 | 12.81737 | 25.23 |
| 8.7603 | 741.22 | 0.4330 | 10.08599 | 6.15 |
| 11.6037 | 299.23 | 0.3031 | 7.62006 | 2.48 |
| 13.6129 | 272.35 | 0.1299 | 6.49955 | 2.26 |
| 15.0708 | 237.57 | 0.1299 | 5.87392 | 1.97 |
| 15.8309 | 8297.87 | 0.0974 | 5.59356 | 68.80 |
| 18.2984 | 1478.06 | 0.0758 | 4.84446 | 12.25 |
| 19.0199 | 524.22 | 0.0866 | 4.66229 | 4.35 |
| 19.6854 | 2560.77 | 0.1515 | 4.50614 | 21.23 |
| 19.7967 | 2875.93 | 0.1082 | 4.48107 | 23.84 |
| 20.9488 | 1808.23 | 0.0974 | 4.23716 | 14.99 |
| 21.4106 | 456.68 | 0.2598 | 4.14679 | 3.79 |
| 22.4681 | 415.67 | 0.0866 | 3.95395 | 3.45 |
| 23.0518 | 1455.03 | 0.1191 | 3.85514 | 12.06 |
| 23.4674 | 1941.29 | 0.1299 | 3.78781 | 16.10 |
| 24.2644 | 567.42 | 0.1082 | 3.66515 | 4.70 |
| 24.5764 | 329.89 | 0.1299 | 3.61934 | 2.74 |
| 26.0155 | 10839.25 | 0.1082 | 3.42229 | 89.87 |
| 26.7520 | 2523.50 | 0.0649 | 3.32972 | 20.92 |
| 27.0792 | 1726.81 | 0.1082 | 3.29023 | 14.32 |
| 27.3427 | 1652.54 | 0.0866 | 3.25911 | 13.70 |
| 27.5832 | 1871.52 | 0.1299 | 3.23124 | 15.52 |
| 28.0212 | 360.52 | 0.1732 | 3.18172 | 2.99 |
| 29.4021 | 12061.29 | 0.1407 | 3.03535 | 100.00 |
| 29.7728 | 1336.37 | 0.1082 | 2.99840 | 11.08 |
| 30.5896 | 5597.64 | 0.1515 | 2.92018 | 46.41 |
| 31.6760 | 7706.31 | 0.0974 | 2.82245 | 63.89 |
| 32.3455 | 407.18 | 0.1299 | 2.76555 | 3.38 |
| 33.3288 | 1490.91 | 0.1299 | 2.68616 | 12.36 |
| 34.3912 | 1681.90 | 0.1732 | 2.60558 | 13.94 |
| 34.7192 | 2665.89 | 0.2165 | 2.58171 | 22.10 |
| 35.9593 | 2822.49 | 0.0649 | 2.49547 | 23.40 |
| 37.0792 | 1155.09 | 0.1515 | 2.42263 | 9.58 |
| 39.4108 | 1975.23 | 0.0974 | 2.28451 | 16.38 |
| 40.5524 | 630.13 | 0.1082 | 2.22279 | 5.22 |
| 41.5841 | 345.77 | 0.1515 | 2.17000 | 2.87 |
| 42.4221 | 204.69 | 0.2598 | 2.12905 | 1.70 |
| 43.1638 | 1517.32 | 0.0866 | 2.09417 | 12.58 |
| 45.3980 | 3785.56 | 0.0866 | 1.99616 | 31.39 |
| 47.0907 | 698.57 | 0.1299 | 1.92828 | 5.79 |
| 47.4957 | 1695.54 | 0.0758 | 1.91278 | 14.06 |
| 47.8329 | 1081.74 | 0.1299 | 1.90008 | 8.97 |
| 48.4950 | 1642.35 | 0.1515 | 1.87567 | 13.62 |
| 50.8074 | 491.65 | 0.1299 | 1.79560 | 4.08 |
| 52.5723 | 1341.79 | 0.1515 | 1.73939 | 11.12 |
| 53.4811 | 466.41 | 0.1732 | 1.71196 | 3.87 |
| 54.3457 | 474.54 | 0.2598 | 1.68675 | 3.93 |
| 55.2860 | 199.56 | 0.1732 | 1.66027 | 1.65 |
| 56.4274 | 1044.96 | 0.0866 | 1.62936 | 8.66 |
| 57.3832 | 651.19 | 0.1299 | 1.60447 | 5.40 |
| 57.8601 | 481.83 | 0.1732 | 1.59238 | 3.99 |
| 60.6520 | 870.23 | 0.1732 | 1.52559 | 7.22 |
| 61.4150 | 888.20 | 0.1732 | 1.50845 | 7.36 |
| 63.0139 | 187.19 | 0.3031 | 1.47397 | 1.55 |
| 64.6644 | 474.30 | 0.2165 | 1.44028 | 3.93 |
| 66.1718 | 710.32 | 0.1082 | 1.41107 | 5.89 |
| 69.1813 | 554.73 | 0.3031 | 1.35685 | 4.60 |
| 70.1347 | 103.31 | 0.3464 | 1.34072 | 0.86 |
| 72.3559 | 360.12 | 0.4330 | 1.30494 | 2.99 |
| 72.9706 | 354.03 | 0.2598 | 1.29546 | 2.94 |
| 73.8175 | 322.21 | 0.3464 | 1.28267 | 2.67 |
| 75.2552 | 806.19 | 0.1191 | 1.26170 | 6.68 |
| 78.2930 | 331.48 | 0.2598 | 1.22017 | 2.75 |
| 81.4921 | 203.74 | 0.5196 | 1.18016 | 1.69 |
| 83.9345 | 537.10 | 0.3031 | 1.15192 | 4.45 |

Pattern List

| Visible | Ref.Code | Score | Compound Name | Chem. Formula | Mineral Name | SemiQuant[%] |
| --- | --- | --- | --- | --- | --- | --- |
| * | 01-075-8689 | 68 | Sodium Aluminum Silicate Hydrate | Na1.71 ( ( Al1.806 Si4.194 ) O12 ) ( H2 O )2.16 | Analcime | 22 |
| * | 01-083-1762 | 59 | Calcium Carbonate | Ca ( C O3 ) | Calcite | 16 |
| * | 01-075-0306 | 37 | Sodium Chloride | Na Cl | Halite | 5 |
| * | 01-080-2107 | 36 | Potassium Aluminum Silicate | K ( Al Si3 O8 ) | Sanidine | 12 |
| * | 01-082-8023 | 26 | Sodium Magnesium Silicon Oxide Hydrate | Na2 Mg3 ( Si6 O16 ) ( H2 O )7 | Loughlinite | 3 |
| * | 01-076-0766 | 16 | Calcium Sodium Aluminum Silicate | Ca0.8 Na0.2 Al1.77 Si2.23 O8 | Anorthite, Na-bearing | 18 |
| * | 04-018-6570 | 20 | Potassium Hydronium Magnesium Aluminum Silicon Oxide Hydroxide | K0.97 ( H3 O )0.03 Mg0.4 Al2.2 Si3.4 O10 ( O H )2 | Muscovite-2M1 | 25 |

Anchor Scan Parameters

Dataset Name	22 ETOSHA 22 MOISUB 2.5-15CM S4

File name	C:\aeris_data\XRD data\Goldstein\22 ETOSHA 22 MOISUB 2.5-15CM S4.xrdml

Sample Identification	22 ETOSHA 22 MOISUB 2.5-15CM S4

Measurement Start Date/Time	8/28/2023 2:46:16 PM

Operator	Instrument

Raw Data Origin	XRD measurement (*.XRDML)

Scan Axis	Gonio

Start Position [°2θ]	5.0064

End Position [°2θ]	84.9874

Step Size [°2θ]	0.0110

Scan Step Time [s]	48.1950

Scan Type	Continuous

PSD Mode	Scanning

PSD Length [°2θ]	5.54

Offset [°2θ]	0.0000

Divergence Slit Type	Fixed

Divergence Slit Size [°]	0.4584

Specimen Length [mm]	10.00

Measurement Temperature [°C]	25.00

Anode Material	Cu

K-α1 [Å]	1.54060

K-α2 [Å]	1.54443

K-β1 [Å]	1.39225

K-A2 / K-A1 Ratio	0.50000

Generator Settings	15 mA, 40 kV

Diffractometer Type	2082464

Diffractometer Number	0

Goniometer Radius [mm]	145.00

Dist. Focus-Diverg. Slit [mm]	95.00

Incident Beam Monochromator	No

Spinning	Yes