Etosha 22 Crt 0-0.1 cm S5

Graphics

Graphics

Graphics

Quantitative Results

Phase Sodium Chloride

Weight fraction/ %	21.0

Phase Calcium Carbonate

Weight fraction/ %	13.0

Phase Calcium Magnesium Carbonate

Weight fraction/ %	15.0

Phase Silicon Oxide

Weight fraction/ %	13.0

Phase Sodium Sulfate

Weight fraction/ %	10.0

Phase Sodium Aluminum Silicate Hydrate

Weight fraction/ %	10.0

Phase Potassium Aluminum Silicate

Weight fraction/ %	9.0

Phase Iron Arsenate Hydrate

Weight fraction/ %	6.0

Phase Potassium Magnesium Manganese Iron Aluminum Silicate Hydroxide

Weight fraction/ %	3.0

Phase Sodium Magnesium Silicon Oxide Hydrate

Weight fraction/ %	1.0

Multiple Quantitative Results

Scans vs Phases Matrix

| Scan name | Sodium Chloride | Calcium Carbonate | Calcium Magnesium Carbonate | Silicon Oxide | Sodium Sulfate | Sodium Aluminum Silicate Hydrate | Potassium Aluminum Silicate | Iron Arsenate Hydrate | Potassium Magnesium Manganese Iron Aluminum Silicate Hydroxide | Sodium Magnesium Silicon Oxide Hydrate |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 23 ETOSHA 22 CRT 0-0.1CM S5 | 21.0 | 13.0 | 15.0 | 13.0 | 10.0 | 10.0 | 9.0 | 6.0 | 3.0 | 1.0 |

Anchor Scan Data

| Pos. [°2θ] | Iobs [cts] | Icalc [cts] | Iback [cts] |
| --- | --- | --- | --- |
| 5.0064 | 6415.0000 | 6747.6589 | 6415.0000 |
| 5.0174 | 6516.3854 | 6796.5549 | 6390.9083 |
| 5.0284 | 6467.8358 | 6824.5301 | 6366.8166 |
| 5.0394 | 6502.1799 | 6840.8942 | 6342.7249 |
| 5.0504 | 6533.7375 | 6838.7392 | 6318.6332 |
| 5.0614 | 6535.2173 | 6813.6872 | 6294.5415 |
| 5.0724 | 6347.8909 | 6765.9727 | 6270.4498 |
| 5.0834 | 6427.9857 | 6700.3093 | 6246.3581 |
| 5.0944 | 6239.7660 | 6623.6774 | 6222.2664 |
| 5.1054 | 6367.3274 | 6542.8526 | 6198.1747 |
| 5.1164 | 6351.5742 | 6463.0525 | 6174.0830 |
| 5.1274 | 6153.9415 | 6387.7044 | 6149.9913 |
| 5.1384 | 6112.9617 | 6318.7269 | 6125.8996 |
| 5.1494 | 6201.4130 | 6256.8966 | 6101.8079 |
| 5.1604 | 6133.7925 | 6202.1674 | 6077.7162 |
| 5.1714 | 6029.2448 | 6153.9422 | 6053.6245 |
| 5.1824 | 5961.5152 | 6111.3077 | 6029.5328 |
| 5.1934 | 6044.7773 | 6073.2303 | 6005.4411 |
| 5.2044 | 5937.1416 | 6038.7027 | 5981.3494 |
| 5.2154 | 5976.9464 | 6006.8372 | 5957.2577 |
| 5.2264 | 5920.8614 | 5976.9090 | 5933.1660 |
| 5.2374 | 5968.0280 | 5948.3624 | 5909.0743 |
| 5.2484 | 5909.8417 | 5920.7924 | 5884.9826 |
| 5.2594 | 5894.2497 | 5893.9157 | 5860.8909 |
| 5.2704 | 5845.5428 | 5867.5397 | 5836.7992 |
| 5.2814 | 5873.3373 | 5841.5352 | 5812.7075 |
| 5.2924 | 5665.0020 | 5815.8160 | 5788.6158 |
| 5.3034 | 5626.5443 | 5790.3231 | 5764.5241 |
| 5.3144 | 5628.6568 | 5765.0152 | 5740.4324 |
| 5.3254 | 5586.8820 | 5739.8618 | 5716.3407 |
| 5.3364 | 5676.1947 | 5714.8398 | 5692.2490 |
| 5.3474 | 5599.8014 | 5689.9309 | 5668.1573 |
| 5.3584 | 5500.0747 | 5665.1202 | 5644.0656 |
| 5.3694 | 5479.3083 | 5640.3955 | 5619.9739 |
| 5.3804 | 5518.2684 | 5615.7463 | 5595.8821 |
| 5.3914 | 5511.5133 | 5591.1640 | 5571.7904 |
| 5.4024 | 5438.7876 | 5566.6410 | 5547.6987 |
| 5.4134 | 5350.2616 | 5542.1712 | 5523.6070 |
| 5.4244 | 5361.7660 | 5517.7489 | 5499.5153 |
| 5.4354 | 5414.1490 | 5493.3694 | 5475.4236 |
| 5.4464 | 5455.9400 | 5469.0287 | 5451.3319 |
| 5.4574 | 5406.8510 | 5444.7232 | 5427.2402 |
| 5.4684 | 5332.7434 | 5420.4499 | 5403.1485 |
| 5.4794 | 5310.9317 | 5396.2060 | 5379.0568 |
| 5.4904 | 5282.8368 | 5371.9891 | 5354.9651 |
| 5.5014 | 5318.0575 | 5347.7973 | 5330.8734 |
| 5.5124 | 5341.2153 | 5323.6287 | 5306.7817 |
| 5.5234 | 5230.8623 | 5299.4817 | 5282.6900 |
| 5.5344 | 5240.1357 | 5284.4024 | 5258.5983 |
| 5.5454 | 5278.3186 | 5264.7042 | 5247.9635 |
| 5.5564 | 5217.2940 | 5254.0713 | 5237.3287 |
| 5.5674 | 5130.9572 | 5243.4554 | 5226.6939 |
| 5.5784 | 5087.4130 | 5232.8557 | 5216.0591 |
| 5.5894 | 5175.8053 | 5222.2715 | 5205.4243 |
| 5.6004 | 5180.2035 | 5211.7021 | 5194.7895 |
| 5.6114 | 5143.4798 | 5201.1470 | 5184.1547 |
| 5.6224 | 5135.6234 | 5190.6057 | 5173.5199 |
| 5.6334 | 5056.5339 | 5180.0778 | 5162.8851 |
| 5.6444 | 5116.3874 | 5169.5630 | 5152.2503 |
| 5.6554 | 5008.9656 | 5159.0610 | 5141.6155 |
| 5.6664 | 4984.9735 | 5148.5716 | 5130.9807 |
| 5.6774 | 5016.2434 | 5138.0946 | 5120.3459 |
| 5.6884 | 5038.2409 | 5127.6299 | 5109.7111 |
| 5.6994 | 4921.4292 | 5117.1773 | 5099.0763 |
| 5.7104 | 4913.5320 | 5106.7369 | 5088.4415 |
| 5.7214 | 4973.7286 | 5096.3087 | 5077.8067 |
| 5.7324 | 4928.5929 | 5085.8925 | 5067.1719 |
| 5.7434 | 4893.5890 | 5075.4886 | 5056.5371 |
| 5.7544 | 5002.6677 | 5065.0970 | 5045.9023 |
| 5.7654 | 4868.1047 | 5054.7179 | 5035.2675 |
| 5.7764 | 4954.4297 | 5044.3513 | 5024.6327 |
| 5.7874 | 4945.0747 | 5033.9976 | 5013.9979 |
| 5.7984 | 4877.2832 | 5023.6568 | 5003.3631 |
| 5.8094 | 4778.3781 | 5013.3294 | 4992.7283 |
| 5.8204 | 4853.4966 | 5003.0154 | 4982.0935 |
| 5.8314 | 4828.8142 | 4992.7154 | 4971.4587 |
| 5.8424 | 4798.9105 | 4982.4296 | 4960.8239 |
| 5.8534 | 4893.5339 | 4972.1584 | 4950.1891 |
| 5.8644 | 4833.8082 | 4961.9023 | 4939.5543 |
| 5.8754 | 4891.2016 | 4951.6616 | 4928.9195 |
| 5.8864 | 4810.4041 | 4941.4369 | 4918.2847 |
| 5.8974 | 4835.8805 | 4931.2288 | 4907.6499 |
| 5.9084 | 4885.6696 | 4921.0377 | 4897.0151 |
| 5.9194 | 4840.1298 | 4910.8643 | 4886.3803 |
| 5.9304 | 4658.0030 | 4900.7093 | 4875.7455 |
| 5.9414 | 4834.6735 | 4890.5733 | 4865.1107 |
| 5.9524 | 4794.1819 | 4880.4571 | 4854.4759 |
| 5.9634 | 4933.3141 | 4870.3615 | 4843.8411 |
| 5.9744 | 4766.4277 | 4860.2873 | 4833.2062 |
| 5.9854 | 4811.8550 | 4850.2355 | 4822.5714 |
| 5.9964 | 4869.5044 | 4840.2070 | 4811.9366 |
| 6.0074 | 4793.7345 | 4830.2028 | 4801.3018 |
| 6.0184 | 4760.2999 | 4820.2241 | 4790.6670 |
| 6.0294 | 4740.1298 | 4810.2719 | 4780.0322 |
| 6.0404 | 4683.2714 | 4800.3477 | 4769.3974 |
| 6.0514 | 4668.5325 | 4790.4527 | 4758.7626 |
| 6.0624 | 4729.6490 | 4783.1814 | 4748.1278 |
| 6.0734 | 4873.0039 | 4774.6130 | 4741.3499 |
| 6.0844 | 4807.8889 | 4768.6715 | 4734.5720 |
| 6.0954 | 4739.0310 | 4762.7656 | 4727.7941 |
| 6.1064 | 4816.8328 | 4756.8971 | 4721.0162 |
| 6.1174 | 4829.0349 | 4751.0681 | 4714.2382 |
| 6.1284 | 4816.5427 | 4745.2808 | 4707.4603 |
| 6.1394 | 4733.0433 | 4739.5376 | 4700.6824 |
| 6.1504 | 4764.4002 | 4733.8410 | 4693.9045 |
| 6.1614 | 4797.2714 | 4728.1939 | 4687.1266 |
| 6.1724 | 4810.3490 | 4722.5992 | 4680.3486 |
| 6.1834 | 4772.3206 | 4717.0606 | 4673.5707 |
| 6.1944 | 4837.0797 | 4711.5815 | 4666.7928 |
| 6.2054 | 4854.1096 | 4706.1663 | 4660.0149 |
| 6.2164 | 4863.3855 | 4700.8196 | 4653.2370 |
| 6.2274 | 4880.3761 | 4695.5466 | 4646.4590 |
| 6.2384 | 4790.9361 | 4690.3533 | 4639.6811 |
| 6.2494 | 4768.3333 | 4685.2464 | 4632.9032 |
| 6.2604 | 4752.7434 | 4680.2336 | 4626.1253 |
| 6.2714 | 4752.9430 | 4675.3240 | 4619.3474 |
| 6.2824 | 4777.3953 | 4670.5277 | 4612.5694 |
| 6.2934 | 4791.3584 | 4665.8568 | 4605.7915 |
| 6.3044 | 4785.3097 | 4661.3251 | 4599.0136 |
| 6.3154 | 4795.4843 | 4656.9489 | 4592.2357 |
| 6.3264 | 4831.6578 | 4652.7469 | 4585.4578 |
| 6.3374 | 4800.8481 | 4648.7412 | 4578.6798 |
| 6.3484 | 4816.0108 | 4644.8047 | 4571.9019 |
| 6.3594 | 4863.8570 | 4640.9172 | 4565.1240 |
| 6.3704 | 4963.4995 | 4637.5386 | 4558.3461 |
| 6.3814 | 4952.0437 | 4634.6292 | 4551.5682 |
| 6.3924 | 4915.6814 | 4632.0914 | 4544.7902 |
| 6.4034 | 4893.3908 | 4629.9774 | 4538.0123 |
| 6.4144 | 5031.5114 | 4628.3471 | 4531.2344 |
| 6.4254 | 5019.2522 | 4627.2680 | 4524.4565 |
| 6.4364 | 5001.9253 | 4626.8157 | 4517.6786 |
| 6.4474 | 5040.7974 | 4627.0750 | 4510.9006 |
| 6.4584 | 5036.7345 | 4628.1395 | 4504.1227 |
| 6.4694 | 5060.5801 | 4630.1120 | 4497.3448 |
| 6.4804 | 5076.2350 | 4633.1043 | 4490.5669 |
| 6.4914 | 5062.8363 | 4637.2368 | 4483.7890 |
| 6.5024 | 4941.5024 | 4642.6379 | 4477.0111 |
| 6.5134 | 5081.5881 | 4649.4428 | 4470.2331 |
| 6.5244 | 5133.0147 | 4657.7922 | 4463.4552 |
| 6.5354 | 4983.5186 | 4667.8306 | 4456.6773 |
| 6.5464 | 5080.3570 | 4679.7037 | 4449.8994 |
| 6.5574 | 5178.5841 | 4693.5561 | 4443.1215 |
| 6.5684 | 5175.1121 | 4709.5283 | 4436.3435 |
| 6.5794 | 5133.3918 | 4727.7528 | 4429.5656 |
| 6.5904 | 5188.2124 | 4748.3510 | 4422.7877 |
| 6.6014 | 5105.5314 | 4771.4285 | 4416.0098 |
| 6.6124 | 5176.3117 | 4797.0713 | 4409.2319 |
| 6.6234 | 5329.4720 | 4825.3408 | 4402.4539 |
| 6.6344 | 5280.5496 | 4856.2693 | 4395.6760 |
| 6.6454 | 5282.9528 | 4889.8551 | 4388.8981 |
| 6.6564 | 5212.7581 | 4926.0570 | 4382.1202 |
| 6.6674 | 5343.6554 | 4964.7893 | 4375.3423 |
| 6.6784 | 5234.2910 | 5005.9159 | 4368.5643 |
| 6.6894 | 5309.9779 | 5049.2439 | 4361.7864 |
| 6.7004 | 5219.4326 | 5094.5168 | 4355.0085 |
| 6.7114 | 5291.1755 | 5141.4070 | 4348.2306 |
| 6.7224 | 5322.9351 | 5189.5080 | 4341.4527 |
| 6.7334 | 5317.5624 | 5238.3251 | 4334.6747 |
| 6.7444 | 5324.5359 | 5287.2686 | 4327.8968 |
| 6.7554 | 5349.8112 | 5335.6464 | 4321.1189 |
| 6.7664 | 5317.1701 | 5382.6623 | 4314.3410 |
| 6.7774 | 5514.7085 | 5427.4187 | 4307.5631 |
| 6.7884 | 5404.0265 | 5468.9304 | 4300.7851 |
| 6.7994 | 5497.0929 | 5506.1489 | 4294.0072 |
| 6.8104 | 5520.9793 | 5538.0023 | 4287.2293 |
| 6.8214 | 5335.7272 | 5563.4488 | 4280.4514 |
| 6.8324 | 5462.5005 | 5581.5421 | 4273.6735 |
| 6.8434 | 5409.4179 | 5591.5001 | 4266.8955 |
| 6.8544 | 5510.2684 | 5592.7710 | 4260.1176 |
| 6.8654 | 5303.5575 | 5585.0822 | 4253.3397 |
| 6.8764 | 5383.6903 | 5568.4663 | 4246.5618 |
| 6.8874 | 5509.8716 | 5543.2581 | 4239.7839 |
| 6.8984 | 5395.1406 | 5510.0627 | 4233.0059 |
| 6.9094 | 5415.3717 | 5469.7018 | 4226.2280 |
| 6.9204 | 5466.2713 | 5423.1469 | 4219.4501 |
| 6.9314 | 5285.8495 | 5371.4501 | 4212.6722 |
| 6.9424 | 5251.0993 | 5315.6814 | 4205.8943 |
| 6.9534 | 5298.6976 | 5256.8779 | 4199.1164 |
| 6.9644 | 5256.5025 | 5196.0079 | 4192.3384 |
| 6.9754 | 5269.2031 | 5133.9480 | 4185.5605 |
| 6.9864 | 5283.5929 | 5071.4728 | 4178.7826 |
| 6.9974 | 5248.8196 | 5009.2525 | 4172.0047 |
| 7.0084 | 5240.6725 | 4947.8570 | 4165.2268 |
| 7.0194 | 5181.4720 | 4887.7620 | 4158.4488 |
| 7.0304 | 5173.1209 | 4829.3573 | 4151.6709 |
| 7.0414 | 5035.0432 | 4772.9553 | 4144.8930 |
| 7.0524 | 5004.5163 | 4718.7990 | 4138.1151 |
| 7.0634 | 5088.2413 | 4667.0691 | 4131.3372 |
| 7.0744 | 4954.9538 | 4617.8910 | 4124.5592 |
| 7.0854 | 5000.2301 | 4571.3408 | 4117.7813 |
| 7.0964 | 5012.3648 | 4527.4513 | 4111.0034 |
| 7.1074 | 4985.4601 | 4486.2168 | 4104.2255 |
| 7.1184 | 4930.8348 | 4447.3176 | 4097.4476 |
| 7.1294 | 4922.1548 | 4411.1120 | 4090.2514 |
| 7.1404 | 4800.4080 | 4377.0846 | 4083.0552 |
| 7.1514 | 4672.0693 | 4345.4072 | 4075.8591 |
| 7.1624 | 4618.3186 | 4315.9561 | 4068.6629 |
| 7.1734 | 4679.1500 | 4288.5967 | 4061.4667 |
| 7.1844 | 4763.4956 | 4263.1875 | 4054.2705 |
| 7.1954 | 4668.9375 | 4239.5836 | 4047.0744 |

Scan List

| Vis. | Dataset Name | Start pos. [°2θ] | End pos. [°2θ] | Step [°2θ] | Meas.Date/Time |
| --- | --- | --- | --- | --- | --- |
| * | 23 ETOSHA 22 CRT 0-0.1CM S5 | 5.0064 | 84.9874 | 0.0110 | 8/28/2023 12:47:58 PM |

Peak List

| Pos. [°2θ] | Height [cts] | FWHM Left [°2θ] | d-spacing [Å] | Rel. Int. [%] |
| --- | --- | --- | --- | --- |
| 5.0513 | 465.89 | 0.1299 | 17.48038 | 1.86 |
| 6.8531 | 1190.58 | 0.3464 | 12.88790 | 4.76 |
| 8.7940 | 276.88 | 0.4330 | 10.04732 | 1.11 |
| 15.8543 | 3739.33 | 0.0974 | 5.58538 | 14.96 |
| 18.3083 | 548.87 | 0.1082 | 4.84188 | 2.20 |
| 19.0462 | 3085.63 | 0.0974 | 4.65592 | 12.34 |
| 19.9048 | 754.04 | 0.4330 | 4.45697 | 3.02 |
| 20.8548 | 1347.11 | 0.0758 | 4.25604 | 5.39 |
| 21.9947 | 105.40 | 0.1299 | 4.03798 | 0.42 |
| 23.0698 | 1316.76 | 0.1299 | 3.85218 | 5.27 |
| 23.4906 | 739.91 | 0.1299 | 3.78412 | 2.96 |
| 24.0368 | 643.96 | 0.1082 | 3.69935 | 2.58 |
| 24.3238 | 170.60 | 0.1082 | 3.65635 | 0.68 |
| 25.1529 | 223.22 | 0.1948 | 3.53766 | 0.89 |
| 26.0145 | 5005.27 | 0.1299 | 3.42242 | 20.02 |
| 26.6382 | 8990.74 | 0.0660 | 3.34368 | 35.97 |
| 26.7131 | 4136.18 | 0.0396 | 3.33448 | 16.55 |
| 27.3578 | 3171.73 | 0.0792 | 3.25734 | 12.69 |
| 28.0553 | 5964.28 | 0.0396 | 3.17793 | 23.86 |
| 28.1318 | 2471.42 | 0.0396 | 3.16947 | 9.89 |
| 28.9884 | 1138.24 | 0.0660 | 3.07772 | 4.55 |
| 29.3872 | 9185.18 | 0.0924 | 3.03686 | 36.74 |
| 29.4515 | 10425.67 | 0.0924 | 3.03038 | 41.71 |
| 30.5824 | 3685.06 | 0.0792 | 2.92085 | 14.74 |
| 30.8375 | 10536.71 | 0.0792 | 2.89726 | 42.15 |
| 30.9209 | 10358.76 | 0.0924 | 2.88964 | 41.44 |
| 31.6999 | 24997.13 | 0.1056 | 2.82038 | 100.00 |
| 31.7902 | 10771.63 | 0.0396 | 2.81258 | 43.09 |
| 32.1335 | 3325.85 | 0.0924 | 2.78330 | 13.30 |
| 33.3301 | 890.55 | 0.1320 | 2.68607 | 3.56 |
| 33.8480 | 1952.10 | 0.0660 | 2.64614 | 7.81 |
| 34.7205 | 1021.33 | 0.2112 | 2.58161 | 4.09 |
| 35.2061 | 639.32 | 0.2640 | 2.54711 | 2.56 |
| 35.9646 | 1561.16 | 0.0924 | 2.49511 | 6.25 |
| 36.5275 | 1008.10 | 0.0660 | 2.45795 | 4.03 |
| 37.3209 | 1206.11 | 0.1848 | 2.40749 | 4.83 |
| 38.6204 | 1201.42 | 0.0528 | 2.32942 | 4.81 |
| 39.4622 | 2799.80 | 0.1056 | 2.28165 | 11.20 |
| 39.5611 | 1775.63 | 0.0396 | 2.27617 | 7.10 |
| 40.2790 | 604.45 | 0.0660 | 2.23724 | 2.42 |
| 41.1041 | 2750.64 | 0.0660 | 2.19422 | 11.00 |
| 42.4226 | 184.11 | 0.1584 | 2.12902 | 0.74 |
| 43.1657 | 1164.34 | 0.2112 | 2.09408 | 4.66 |
| 43.7579 | 274.82 | 0.2112 | 2.06710 | 1.10 |
| 44.8947 | 1631.47 | 0.2640 | 2.01736 | 6.53 |
| 45.4223 | 10967.39 | 0.0924 | 1.99515 | 43.87 |
| 45.5553 | 5383.88 | 0.0792 | 1.98964 | 21.54 |
| 47.1067 | 533.52 | 0.2112 | 1.92766 | 2.13 |
| 47.4551 | 1201.32 | 0.1056 | 1.91432 | 4.81 |
| 47.5695 | 1390.38 | 0.1584 | 1.90998 | 5.56 |
| 48.5229 | 1105.60 | 0.1584 | 1.87466 | 4.42 |
| 48.7746 | 1681.35 | 0.0924 | 1.86557 | 6.73 |
| 50.1377 | 993.69 | 0.0924 | 1.81800 | 3.98 |
| 51.0076 | 1491.04 | 0.2112 | 1.78902 | 5.96 |
| 52.5712 | 586.31 | 0.1056 | 1.73943 | 2.35 |
| 53.8429 | 333.62 | 0.0792 | 1.70131 | 1.33 |
| 54.5452 | 500.22 | 0.1188 | 1.68105 | 2.00 |
| 54.8490 | 405.30 | 0.0528 | 1.67246 | 1.62 |
| 55.2970 | 568.54 | 0.0528 | 1.65996 | 2.27 |
| 56.4360 | 3111.50 | 0.1056 | 1.62913 | 12.45 |
| 56.5866 | 1828.58 | 0.0660 | 1.62515 | 7.32 |
| 57.4937 | 537.16 | 0.2640 | 1.60165 | 2.15 |
| 58.8095 | 180.98 | 0.2112 | 1.56891 | 0.72 |
| 59.4523 | 525.28 | 0.0660 | 1.55348 | 2.10 |
| 59.9618 | 773.30 | 0.0924 | 1.54149 | 3.09 |
| 60.1184 | 383.06 | 0.0792 | 1.53785 | 1.53 |
| 60.7828 | 423.15 | 0.3168 | 1.52262 | 1.69 |
| 61.3369 | 290.29 | 0.8448 | 1.51018 | 1.16 |
| 63.3188 | 421.79 | 0.4224 | 1.46760 | 1.69 |
| 64.6973 | 361.03 | 0.3696 | 1.43962 | 1.44 |
| 66.2060 | 1385.54 | 0.0660 | 1.41043 | 5.54 |
| 66.3924 | 645.83 | 0.0660 | 1.40692 | 2.58 |
| 67.3185 | 461.68 | 0.4224 | 1.38980 | 1.85 |
| 67.7331 | 574.52 | 0.0660 | 1.38230 | 2.30 |
| 68.1255 | 1629.70 | 0.0660 | 1.37529 | 6.52 |
| 68.3013 | 1003.77 | 0.0792 | 1.37217 | 4.02 |
| 69.1939 | 218.50 | 0.2640 | 1.35664 | 0.87 |
| 70.3749 | 142.76 | 0.6336 | 1.33674 | 0.57 |
| 72.9701 | 382.72 | 0.2640 | 1.29546 | 1.53 |
| 73.9537 | 123.26 | 0.3168 | 1.28065 | 0.49 |
| 75.2518 | 2090.14 | 0.1056 | 1.26174 | 8.36 |
| 75.4628 | 1100.87 | 0.0924 | 1.25874 | 4.40 |
| 75.6539 | 608.48 | 0.0528 | 1.25603 | 2.43 |
| 75.8672 | 215.93 | 0.0792 | 1.25303 | 0.86 |
| 76.8736 | 60.88 | 0.6336 | 1.23912 | 0.24 |
| 77.6201 | 133.65 | 0.1584 | 1.22906 | 0.53 |
| 78.3563 | 88.04 | 0.3168 | 1.21934 | 0.35 |
| 79.9266 | 136.87 | 0.4224 | 1.19929 | 0.55 |
| 81.1424 | 161.40 | 0.1848 | 1.18436 | 0.65 |
| 81.4767 | 213.38 | 0.1848 | 1.18034 | 0.85 |
| 83.9613 | 1595.49 | 0.1056 | 1.15163 | 6.38 |
| 84.2064 | 806.98 | 0.0792 | 1.14890 | 3.23 |

Pattern List

| Visible | Ref.Code | Score | Compound Name | Chem. Formula | Mineral Name | SemiQuant[%] |
| --- | --- | --- | --- | --- | --- | --- |
| * | 01-085-8594 | 52 | Sodium Chloride | Na Cl | Halite | 21 |
| * | 01-083-0578 | 58 | Calcium Carbonate | Ca ( C O3 ) | Calcite | 13 |
| * | 01-081-8227 | 52 | Calcium Magnesium Carbonate | Ca Mg ( C O3 )2 | Dolomite | 15 |
| * | 01-070-7345 | 48 | Silicon Oxide | Si O2 | Quartz | 13 |
| * | 01-074-2036 | 47 | Sodium Sulfate | Na2 ( S O4 ) | Thenardite | 10 |
| * | 01-075-8690 | 49 | Sodium Aluminum Silicate Hydrate | Na1.71 ( ( Al1.806 Si4.194 ) O12 ) ( H2 O )2.16 | Analcime | 10 |
| * | 01-084-1504 | 21 | Potassium Aluminum Silicate | K ( Al Si3 O8 ) | Sanidine | 9 |
| * | 01-070-0825 | 19 | Iron Arsenate Hydrate | Fe ( As O4 ) ( H2 O )2 | Scorodite | 6 |
| * | 04-017-4317 | 21 | Potassium Magnesium Manganese Iron Aluminum Silicate Hydroxide | K Mg0.2 Mn0.1 Fe2.4 Al1.7 Si2.6 O10 ( O H )2 | Biotite-1M | 3 |
| * | 01-082-8023 | 13 | Sodium Magnesium Silicon Oxide Hydrate | Na2 Mg3 ( Si6 O16 ) ( H2 O )7 | Loughlinite | 1 |

Anchor Scan Parameters

Dataset Name	23 ETOSHA 22 CRT 0-0.1CM S5

File name	C:\aeris_data\XRD data\Goldstein\23 ETOSHA 22 CRT 0-0.1CM S5.xrdml

Sample Identification	23 ETOSHA 22 CRT 0-0.1CM S5

Measurement Start Date/Time	8/28/2023 12:47:58 PM

Operator	Instrument

Raw Data Origin	XRD measurement (*.XRDML)

Scan Axis	Gonio

Start Position [°2θ]	5.0064

End Position [°2θ]	84.9874

Step Size [°2θ]	0.0110

Scan Step Time [s]	48.1950

Scan Type	Continuous

PSD Mode	Scanning

PSD Length [°2θ]	5.54

Offset [°2θ]	0.0000

Divergence Slit Type	Fixed

Divergence Slit Size [°]	0.4584

Specimen Length [mm]	10.00

Measurement Temperature [°C]	25.00

Anode Material	Cu

K-α1 [Å]	1.54060

K-α2 [Å]	1.54443

K-β1 [Å]	1.39225

K-A2 / K-A1 Ratio	0.50000

Generator Settings	15 mA, 40 kV

Diffractometer Type	2082464

Diffractometer Number	0

Goniometer Radius [mm]	145.00

Dist. Focus-Diverg. Slit [mm]	95.00

Incident Beam Monochromator	No

Spinning	Yes