Etosha 18 SS 0-2 cm S2

Graphics

Graphics

Graphics

Quantitative Results

Phase Sodium Aluminum Silicate Hydrate

Weight fraction/ %	12.0

Phase Sodium Calcium Aluminum Silicate

Weight fraction/ %	2.0

Phase Potassium Aluminum Silicate

Weight fraction/ %	22.0

Phase Sodium Chloride

Weight fraction/ %	3.0

Phase Potassium Magnesium Aluminum Hydroxide Fluoride Silicate

Weight fraction/ %	8.0

Phase Calcium Sulfate Hydrate

Weight fraction/ %	1.0

Phase Calcium Magnesium Carbonate

Weight fraction/ %	3.0

Phase Sodium Magnesium Silicon Oxide Hydrate

Weight fraction/ %	7.0

Phase Potassium Sodium Magnesium Aluminum Iron Silicon Titanium Oxide Fluoride Hydroxide

Weight fraction/ %	42.0

Multiple Quantitative Results

Scans vs Phases Matrix

| Scan name | Sodium Aluminum Silicate Hydrate | Sodium Calcium Aluminum Silicate | Potassium Aluminum Silicate | Sodium Chloride | Potassium Magnesium Aluminum Hydroxide Fluoride Silicate | Calcium Sulfate Hydrate | Calcium Magnesium Carbonate | Sodium Magnesium Silicon Oxide Hydrate | Potassium Sodium Magnesium Aluminum Iron Silicon Titanium Oxide Fluoride Hydroxide |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 3 ETOSHA 18 SS 0-2CM SITE 2 | 12.0 | 2.0 | 22.0 | 3.0 | 8.0 | 1.0 | 3.0 | 7.0 | 42.0 |

Anchor Scan Data

| Pos. [°2θ] | Iobs [cts] | Icalc [cts] | Iback [cts] |
| --- | --- | --- | --- |
| 5.0064 | 8627.0000 | 8626.2385 | 8627.0000 |
| 5.0174 | 8455.1465 | 8618.8204 | 8604.7184 |
| 5.0284 | 8702.9852 | 8596.6961 | 8582.4367 |
| 5.0394 | 8503.3363 | 8574.5745 | 8560.1551 |
| 5.0504 | 8479.7561 | 8552.4555 | 8537.8735 |
| 5.0614 | 8358.2011 | 8530.3393 | 8515.5919 |
| 5.0724 | 8366.2802 | 8508.2260 | 8493.3102 |
| 5.0834 | 8597.5978 | 8486.1155 | 8471.0286 |
| 5.0944 | 8357.0629 | 8464.0080 | 8448.7470 |
| 5.1054 | 8416.3982 | 8441.9035 | 8426.4654 |
| 5.1164 | 8303.6706 | 8419.8022 | 8404.1837 |
| 5.1274 | 8324.8319 | 8397.7039 | 8381.9021 |
| 5.1384 | 8258.0619 | 8375.6090 | 8359.6205 |
| 5.1494 | 8306.3412 | 8353.5173 | 8337.3389 |
| 5.1604 | 8197.1563 | 8331.4291 | 8315.0572 |
| 5.1714 | 8064.6814 | 8309.3443 | 8292.7756 |
| 5.1824 | 8079.8918 | 8287.2631 | 8270.4940 |
| 5.1934 | 8199.0747 | 8265.1856 | 8248.2124 |
| 5.2044 | 8166.7611 | 8243.1118 | 8225.9307 |
| 5.2154 | 8131.2330 | 8221.0418 | 8203.6491 |
| 5.2264 | 8238.1219 | 8198.9758 | 8181.3675 |
| 5.2374 | 8122.9911 | 8176.9138 | 8159.0858 |
| 5.2484 | 7976.3471 | 8154.8559 | 8136.8042 |
| 5.2594 | 7993.4253 | 8132.8023 | 8114.5226 |
| 5.2704 | 8070.6313 | 8110.7529 | 8092.2410 |
| 5.2814 | 7973.1268 | 8088.7081 | 8069.9593 |
| 5.2924 | 7883.9282 | 8066.6678 | 8047.6777 |
| 5.3034 | 7926.7522 | 8044.6321 | 8025.3961 |
| 5.3144 | 7909.2556 | 8022.6013 | 8003.1145 |
| 5.3254 | 7692.6539 | 8000.5754 | 7980.8328 |
| 5.3364 | 7781.9233 | 7978.5546 | 7958.5512 |
| 5.3474 | 7820.9489 | 7956.5389 | 7936.2696 |
| 5.3584 | 7746.3422 | 7934.5286 | 7913.9880 |
| 5.3694 | 7727.2670 | 7912.5238 | 7891.7063 |
| 5.3804 | 7747.4346 | 7890.5246 | 7869.4247 |
| 5.3914 | 7704.1018 | 7868.5311 | 7847.1431 |
| 5.4024 | 7730.2655 | 7846.5436 | 7824.8614 |
| 5.4134 | 7752.5624 | 7824.5622 | 7802.5798 |
| 5.4244 | 7753.3658 | 7802.5870 | 7780.2982 |
| 5.4354 | 7678.2389 | 7780.6183 | 7758.0166 |
| 5.4464 | 7602.2606 | 7758.6562 | 7735.7349 |
| 5.4574 | 7600.8501 | 7736.7009 | 7713.4533 |
| 5.4684 | 7622.2861 | 7714.7526 | 7691.1717 |
| 5.4794 | 7654.9086 | 7692.8115 | 7668.8901 |
| 5.4904 | 7529.9420 | 7670.8778 | 7646.6084 |
| 5.5014 | 7490.8540 | 7648.9518 | 7624.3268 |
| 5.5124 | 7548.0344 | 7627.0336 | 7602.0452 |
| 5.5234 | 7590.8555 | 7605.1235 | 7579.7636 |
| 5.5344 | 7506.8466 | 7592.6217 | 7557.4819 |
| 5.5454 | 7548.0998 | 7575.5681 | 7549.4399 |
| 5.5564 | 7660.5821 | 7567.9233 | 7541.3979 |
| 5.5674 | 7539.9749 | 7560.2876 | 7533.3559 |
| 5.5784 | 7541.4484 | 7552.6614 | 7525.3139 |
| 5.5894 | 7558.6858 | 7545.0448 | 7517.2718 |
| 5.6004 | 7489.2389 | 7537.4381 | 7509.2298 |
| 5.6114 | 7473.4921 | 7529.8418 | 7501.1878 |
| 5.6224 | 7531.3107 | 7522.2560 | 7493.1458 |
| 5.6334 | 7501.0546 | 7514.6813 | 7485.1038 |
| 5.6444 | 7473.7227 | 7507.1178 | 7477.0617 |
| 5.6554 | 7400.2080 | 7499.5660 | 7469.0197 |
| 5.6664 | 7389.2242 | 7492.0263 | 7460.9777 |
| 5.6774 | 7442.9843 | 7484.4990 | 7452.9357 |
| 5.6884 | 7489.4818 | 7476.9846 | 7444.8937 |
| 5.6994 | 7469.5752 | 7469.4834 | 7436.8516 |
| 5.7104 | 7498.7581 | 7461.9960 | 7428.8096 |
| 5.7214 | 7560.9297 | 7454.5229 | 7420.7676 |
| 5.7324 | 7402.0236 | 7447.0644 | 7412.7256 |
| 5.7434 | 7548.1111 | 7439.6211 | 7404.6836 |
| 5.7544 | 7495.2271 | 7432.1936 | 7396.6415 |
| 5.7654 | 7350.6357 | 7424.7824 | 7388.5995 |
| 5.7764 | 7388.2262 | 7417.3880 | 7380.5575 |
| 5.7874 | 7526.2817 | 7410.0112 | 7372.5155 |
| 5.7984 | 7491.9026 | 7402.6524 | 7364.4735 |
| 5.8094 | 7502.0477 | 7395.5907 | 7356.4314 |
| 5.8204 | 7514.9145 | 7388.8127 | 7348.3894 |
| 5.8314 | 7291.9955 | 7381.6575 | 7340.3474 |
| 5.8424 | 7299.1554 | 7374.6555 | 7332.3054 |
| 5.8534 | 7325.6067 | 7367.4069 | 7324.2634 |
| 5.8644 | 7395.0679 | 7360.1811 | 7316.2213 |
| 5.8754 | 7326.1465 | 7352.9787 | 7308.1793 |
| 5.8864 | 7351.5320 | 7345.8009 | 7300.1373 |
| 5.8974 | 7549.1239 | 7338.6484 | 7292.0953 |
| 5.9084 | 7493.4799 | 7331.5224 | 7284.0533 |
| 5.9194 | 7550.7143 | 7324.4238 | 7276.0112 |
| 5.9304 | 7395.8997 | 7317.3538 | 7267.9692 |
| 5.9414 | 7541.9553 | 7310.3136 | 7259.9272 |
| 5.9524 | 7541.7984 | 7303.3043 | 7251.8852 |
| 5.9634 | 7557.0103 | 7296.3273 | 7243.8432 |
| 5.9744 | 7578.2055 | 7289.3840 | 7235.8011 |
| 5.9854 | 7508.0231 | 7282.4756 | 7227.7591 |
| 5.9964 | 7483.2567 | 7275.6038 | 7219.7171 |
| 6.0074 | 7668.0993 | 7268.7702 | 7211.6751 |
| 6.0184 | 7584.9076 | 7261.9763 | 7203.6331 |
| 6.0294 | 7559.8407 | 7255.2240 | 7195.5910 |
| 6.0404 | 7505.8948 | 7248.5152 | 7187.5490 |
| 6.0514 | 7584.5502 | 7241.8517 | 7179.5070 |
| 6.0624 | 7636.8968 | 7235.0683 | 7171.4650 |
| 6.0734 | 7699.1087 | 7228.4157 | 7163.1693 |
| 6.0844 | 7767.9322 | 7221.6478 | 7154.8736 |
| 6.0954 | 7759.2522 | 7214.9342 | 7146.5779 |
| 6.1064 | 7773.9784 | 7208.2778 | 7138.2822 |
| 6.1174 | 7768.3092 | 7201.6812 | 7129.9866 |
| 6.1284 | 7766.9469 | 7195.1474 | 7121.6909 |
| 6.1394 | 7876.6145 | 7188.6795 | 7113.3952 |
| 6.1504 | 7792.2262 | 7182.2807 | 7105.0995 |
| 6.1614 | 7826.7655 | 7175.9547 | 7096.8038 |
| 6.1724 | 7886.7030 | 7169.7052 | 7088.5081 |
| 6.1834 | 7905.8594 | 7163.5361 | 7080.2124 |
| 6.1944 | 7966.9115 | 7157.4518 | 7071.9168 |
| 6.2054 | 7940.4081 | 7151.4566 | 7063.6211 |
| 6.2164 | 8045.1613 | 7145.5556 | 7055.3254 |
| 6.2274 | 8054.3761 | 7139.7537 | 7047.0297 |
| 6.2384 | 8082.0581 | 7134.0567 | 7038.7340 |
| 6.2494 | 8255.6667 | 7128.4703 | 7030.4383 |
| 6.2604 | 8213.6548 | 7123.0008 | 7022.1426 |
| 6.2714 | 8212.7709 | 7117.6552 | 7013.8470 |
| 6.2824 | 8287.4739 | 7112.4405 | 7005.5513 |
| 6.2934 | 8326.9735 | 7107.3647 | 6997.2556 |
| 6.3044 | 8382.4159 | 7102.4361 | 6988.9599 |
| 6.3154 | 8380.7404 | 7097.6637 | 6980.6642 |
| 6.3264 | 8459.5723 | 7093.0573 | 6972.3685 |
| 6.3374 | 8538.4405 | 7088.6274 | 6964.0729 |
| 6.3484 | 8532.5673 | 7084.3851 | 6955.7772 |
| 6.3594 | 8480.3776 | 7080.3428 | 6947.4815 |
| 6.3704 | 8524.3009 | 7076.5137 | 6939.1858 |
| 6.3814 | 8585.9376 | 7072.9120 | 6930.8901 |
| 6.3924 | 8697.6549 | 7069.5534 | 6922.5944 |
| 6.4034 | 8880.6805 | 7066.4548 | 6914.2987 |
| 6.4144 | 8892.8908 | 7063.6346 | 6906.0031 |
| 6.4254 | 8961.0635 | 7061.1130 | 6897.7074 |
| 6.4364 | 9067.1416 | 7058.9121 | 6889.4117 |
| 6.4474 | 9109.7267 | 7057.0562 | 6881.1160 |
| 6.4584 | 9116.3068 | 7055.5724 | 6872.8203 |
| 6.4694 | 9273.6594 | 7054.4906 | 6864.5246 |
| 6.4804 | 9333.4149 | 7053.8445 | 6856.2289 |
| 6.4914 | 9486.0753 | 7053.6722 | 6847.9333 |
| 6.5024 | 9589.7748 | 7054.0171 | 6839.6376 |
| 6.5134 | 9751.5556 | 7054.9292 | 6831.3419 |
| 6.5244 | 9816.7345 | 7056.4669 | 6823.0462 |
| 6.5354 | 9823.9184 | 7058.6987 | 6814.7505 |
| 6.5464 | 9979.3570 | 7061.7064 | 6806.4548 |
| 6.5574 | 10024.0723 | 7065.5882 | 6798.1592 |
| 6.5684 | 10118.8742 | 7070.4629 | 6789.8635 |
| 6.5794 | 10222.7011 | 7076.4753 | 6781.5678 |
| 6.5904 | 10224.2124 | 7083.5629 | 6773.2721 |
| 6.6014 | 10433.1058 | 7092.3924 | 6764.7059 |
| 6.6124 | 10547.8201 | 7102.7809 | 6756.1397 |
| 6.6234 | 10806.4558 | 7115.2940 | 6747.5735 |
| 6.6344 | 10782.2733 | 7130.3286 | 6739.0073 |
| 6.6454 | 10984.3123 | 7148.4077 | 6730.4411 |
| 6.6564 | 11166.5163 | 7170.0835 | 6721.8749 |
| 6.6674 | 11126.9479 | 7195.9607 | 6713.3087 |
| 6.6784 | 11300.9352 | 7226.9293 | 6704.7425 |
| 6.6894 | 11414.4115 | 7263.9150 | 6696.1763 |
| 6.7004 | 11638.4917 | 7307.9530 | 6687.6101 |
| 6.7114 | 11608.7881 | 7360.2896 | 6679.0438 |
| 6.7224 | 11711.2537 | 7422.2761 | 6670.4776 |
| 6.7334 | 11906.0094 | 7495.3877 | 6661.9114 |
| 6.7444 | 11642.1140 | 7581.2022 | 6653.3452 |
| 6.7554 | 11872.1579 | 7681.3692 | 6644.7790 |
| 6.7664 | 11992.2557 | 7797.5677 | 6636.2128 |
| 6.7774 | 12215.2646 | 7931.4525 | 6627.6466 |
| 6.7884 | 12150.6194 | 8084.5897 | 6619.0804 |
| 6.7994 | 12479.2600 | 8258.3828 | 6610.5142 |
| 6.8104 | 12269.1220 | 8453.9895 | 6601.9480 |
| 6.8214 | 12525.5147 | 8672.2315 | 6593.3818 |
| 6.8324 | 12478.1121 | 8913.4983 | 6584.8156 |
| 6.8434 | 12567.4778 | 9177.6463 | 6576.2494 |
| 6.8544 | 12423.6697 | 9463.8903 | 6567.6832 |
| 6.8654 | 12565.9331 | 9770.6875 | 6559.1170 |
| 6.8764 | 12592.5890 | 10095.6080 | 6550.5508 |
| 6.8874 | 12530.9160 | 10435.1904 | 6541.9846 |
| 6.8984 | 12725.3471 | 10784.7796 | 6533.4184 |
| 6.9094 | 12599.6642 | 11138.3595 | 6524.8522 |
| 6.9204 | 12596.3008 | 11488.4050 | 6516.2860 |
| 6.9314 | 12420.5659 | 11825.8088 | 6507.7198 |
| 6.9424 | 12460.6264 | 12139.9664 | 6499.1535 |
| 6.9534 | 12572.8687 | 12419.1230 | 6490.5873 |
| 6.9644 | 12446.1897 | 12651.0688 | 6482.0211 |
| 6.9754 | 12304.8088 | 12824.2010 | 6473.4549 |
| 6.9864 | 12312.0707 | 12928.8392 | 6464.8887 |
| 6.9974 | 12148.9200 | 12958.5404 | 6456.3225 |
| 7.0084 | 12337.1739 | 12911.0757 | 6447.7563 |
| 7.0194 | 12098.5693 | 12788.7804 | 6439.1901 |
| 7.0304 | 11946.9183 | 12598.1700 | 6430.6239 |
| 7.0414 | 11688.6986 | 12348.9466 | 6422.0577 |
| 7.0524 | 11579.2389 | 12052.6904 | 6413.4915 |
| 7.0634 | 11436.1366 | 11721.5631 | 6404.9253 |
| 7.0744 | 11355.2901 | 11367.2676 | 6396.3591 |
| 7.0854 | 11400.7919 | 11000.3657 | 6387.7929 |
| 7.0964 | 11086.1513 | 10629.9367 | 6379.2267 |
| 7.1074 | 10861.9469 | 10263.4904 | 6370.6605 |
| 7.1184 | 10788.5133 | 9907.0365 | 6362.0943 |
| 7.1294 | 10806.3913 | 9565.2286 | 6353.5281 |
| 7.1404 | 10728.8643 | 9241.5288 | 6344.9619 |
| 7.1514 | 10565.3333 | 8938.3679 | 6336.3957 |
| 7.1624 | 10327.1474 | 8657.2896 | 6327.8295 |
| 7.1734 | 10042.2226 | 8399.0793 | 6319.2633 |
| 7.1844 | 9864.2743 | 8163.8809 | 6310.6970 |
| 7.1954 | 9749.6833 | 7951.3048 | 6302.1308 |

Scan List

| Vis. | Dataset Name | Start pos. [°2θ] | End pos. [°2θ] | Step [°2θ] | Meas.Date/Time |
| --- | --- | --- | --- | --- | --- |
| * | 3 ETOSHA 18 SS 0-2CM SITE 2 | 5.0064 | 84.9874 | 0.0110 | 8/22/2023 12:00:22 PM |

Peak List

| Pos. [°2θ] | Height [cts] | FWHM Left [°2θ] | d-spacing [Å] | Rel. Int. [%] |
| --- | --- | --- | --- | --- |
| 6.9916 | 5822.49 | 0.2598 | 12.63290 | 47.31 |
| 8.8417 | 868.12 | 0.3031 | 9.99327 | 7.05 |
| 11.6870 | 441.54 | 0.2598 | 7.56591 | 3.59 |
| 13.5760 | 111.75 | 0.6927 | 6.51715 | 0.91 |
| 15.8527 | 8455.37 | 0.1299 | 5.58592 | 68.71 |
| 17.6147 | 196.78 | 0.2598 | 5.03092 | 1.60 |
| 18.2865 | 1536.24 | 0.0541 | 4.84760 | 12.48 |
| 19.9026 | 3370.95 | 0.1948 | 4.45747 | 27.39 |
| 20.9779 | 1104.88 | 0.1299 | 4.23134 | 8.98 |
| 21.3556 | 864.97 | 0.2598 | 4.15735 | 7.03 |
| 22.4902 | 83.79 | 0.1299 | 3.95012 | 0.68 |
| 23.0462 | 714.29 | 0.1082 | 3.85606 | 5.80 |
| 23.4810 | 1327.88 | 0.1515 | 3.78563 | 10.79 |
| 24.2888 | 592.74 | 0.0866 | 3.66153 | 4.82 |
| 26.0070 | 12305.92 | 0.1407 | 3.42339 | 100.00 |
| 26.7918 | 1643.15 | 0.1299 | 3.32486 | 13.35 |
| 27.0913 | 1130.94 | 0.0866 | 3.28878 | 9.19 |
| 27.3563 | 1402.97 | 0.0325 | 3.25752 | 11.40 |
| 27.6232 | 908.74 | 0.0866 | 3.22666 | 7.38 |
| 29.4221 | 6560.19 | 0.1515 | 3.03334 | 53.31 |
| 30.5827 | 5597.54 | 0.1082 | 2.92082 | 45.49 |
| 31.6983 | 1728.50 | 0.0649 | 2.82052 | 14.05 |
| 31.9949 | 570.55 | 0.1082 | 2.79504 | 4.64 |
| 33.3170 | 1631.77 | 0.1732 | 2.68709 | 13.26 |
| 34.2967 | 1482.65 | 0.1732 | 2.61254 | 12.05 |
| 34.7499 | 2731.51 | 0.3464 | 2.57950 | 22.20 |
| 35.9472 | 2388.67 | 0.2165 | 2.49628 | 19.41 |
| 37.1068 | 1377.84 | 0.1732 | 2.42089 | 11.20 |
| 39.4000 | 1351.46 | 0.1082 | 2.28511 | 10.98 |
| 40.5546 | 773.08 | 0.1515 | 2.22267 | 6.28 |
| 41.6720 | 235.69 | 0.2165 | 2.16562 | 1.92 |
| 43.1362 | 739.85 | 0.1082 | 2.09544 | 6.01 |
| 45.4197 | 1032.80 | 0.0866 | 1.99526 | 8.39 |
| 45.7857 | 630.85 | 0.0528 | 1.98016 | 5.13 |
| 47.1026 | 271.62 | 0.2598 | 1.92782 | 2.21 |
| 47.5179 | 874.39 | 0.1515 | 1.91193 | 7.11 |
| 47.8431 | 1103.14 | 0.1299 | 1.89970 | 8.96 |
| 48.5198 | 934.46 | 0.1732 | 1.87477 | 7.59 |
| 48.8392 | 674.06 | 0.1299 | 1.86325 | 5.48 |
| 50.8506 | 138.19 | 0.3031 | 1.79417 | 1.12 |
| 52.5465 | 1393.42 | 0.1515 | 1.74019 | 11.32 |
| 53.4612 | 490.59 | 0.1732 | 1.71255 | 3.99 |
| 54.3780 | 567.98 | 0.2598 | 1.68583 | 4.62 |
| 56.4405 | 1069.81 | 0.0792 | 1.62901 | 8.69 |
| 56.5896 | 756.59 | 0.0660 | 1.62507 | 6.15 |
| 57.4337 | 329.14 | 0.2112 | 1.60318 | 2.67 |
| 57.8996 | 434.10 | 0.2640 | 1.59138 | 3.53 |
| 60.5882 | 802.97 | 0.5280 | 1.52704 | 6.53 |
| 61.3727 | 889.51 | 0.2112 | 1.50939 | 7.23 |
| 62.8539 | 233.92 | 0.2640 | 1.47733 | 1.90 |
| 64.6810 | 296.20 | 0.2640 | 1.43995 | 2.41 |
| 66.0660 | 475.93 | 0.2640 | 1.41308 | 3.87 |
| 67.6830 | 108.66 | 0.3168 | 1.38320 | 0.88 |
| 68.4303 | 173.18 | 0.3168 | 1.36990 | 1.41 |
| 69.1928 | 593.78 | 0.2112 | 1.35666 | 4.83 |
| 72.3177 | 452.89 | 0.4224 | 1.30553 | 3.68 |
| 73.7917 | 318.62 | 0.3168 | 1.28306 | 2.59 |
| 75.2664 | 377.00 | 0.2112 | 1.26154 | 3.06 |
| 78.2930 | 370.21 | 0.3168 | 1.22017 | 3.01 |
| 81.3861 | 160.95 | 0.8448 | 1.18143 | 1.31 |
| 82.7596 | 96.93 | 0.6336 | 1.16527 | 0.79 |
| 83.9161 | 172.26 | 0.5280 | 1.15213 | 1.40 |

Pattern List

| Visible | Ref.Code | Score | Compound Name | Chem. Formula | Mineral Name | SemiQuant[%] |
| --- | --- | --- | --- | --- | --- | --- |
| * | 00-041-1478 | 71 | Sodium Aluminum Silicate Hydrate | Na ( Si2 Al ) O6 · H2 O | Analcime | 12 |
| * | 01-078-0432 | 30 | Sodium Calcium Aluminum Silicate | ( Na0.45 Ca0.55 ) ( Al1.55 Si2.45 O8 ) | Anorthite, Na-bearing, syn | 2 |
| * | 01-070-6187 | 26 | Potassium Aluminum Silicate | K ( Al Si3 O8 ) | Microcline | 22 |
| * | 01-085-8594 | 40 | Sodium Chloride | Na Cl | Halite | 3 |
| * | 01-073-1661 | 28 | Potassium Magnesium Aluminum Hydroxide Fluoride Silicate | K Mg3 ( Al Si3 O10 ) ( O H ) F | Phlogopite | 8 |
| * | 04-015-4421 | 13 | Calcium Sulfate Hydrate | Ca ( S O4 ) ( H2 O )2 | Gypsum | 1 |
| * | 04-013-2116 | 11 | Calcium Magnesium Carbonate | Ca0.936 Mg0.064 ( C O3 ) | Calcite, Mg-bearing | 3 |
| * | 01-082-8023 | 25 | Sodium Magnesium Silicon Oxide Hydrate | Na2 Mg3 ( Si6 O16 ) ( H2 O )7 | Loughlinite | 7 |
| * | 04-015-8225 | 19 | Potassium Sodium Magnesium Aluminum Iron Silicon Titanium Oxide Fluoride Hydroxide | K Na0.05 Mg0.07 Ti0.03 Fe0.09 Al2.92 Si2.97 O10.13 ( O H )1.8 F0.07 | Muscovite-2M1 | 42 |

Anchor Scan Parameters

Dataset Name	3 ETOSHA 18 SS 0-2CM SITE 2

File name	C:\aeris_data\XRD data\3 ETOSHA 18 SS 0-2CM SITE 2.xrdml

Sample Identification	3 ETOSHA 18 SS 0-2CM SITE 2

Measurement Start Date/Time	8/22/2023 12:00:22 PM

Operator	Instrument

Raw Data Origin	XRD measurement (*.XRDML)

Scan Axis	Gonio

Start Position [°2θ]	5.0064

End Position [°2θ]	84.9874

Step Size [°2θ]	0.0110

Scan Step Time [s]	48.1950

Scan Type	Continuous

PSD Mode	Scanning

PSD Length [°2θ]	5.54

Offset [°2θ]	0.0000

Divergence Slit Type	Fixed

Divergence Slit Size [°]	0.4584

Specimen Length [mm]	10.00

Measurement Temperature [°C]	25.00

Anode Material	Cu

K-α1 [Å]	1.54060

K-α2 [Å]	1.54443

K-β1 [Å]	1.39225

K-A2 / K-A1 Ratio	0.50000

Generator Settings	15 mA, 40 kV

Diffractometer Type	2082464

Diffractometer Number	0

Goniometer Radius [mm]	145.00

Dist. Focus-Diverg. Slit [mm]	95.00

Incident Beam Monochromator	No

Spinning	Yes