Etosha 22 Crt 0-0.1 cm S1

Graphics

Graphics

Graphics

Quantitative Results

Phase Sodium Aluminum Silicon Oxide Hydrate

Weight fraction/ %	32.0

Phase Sodium Chloride

Weight fraction/ %	27.0

Phase Calcium Carbonate

Weight fraction/ %	12.0

Phase Sodium Magnesium Silicon Oxide Hydrate

Weight fraction/ %	5.0

Phase Potassium Magnesium Aluminum Silicate Fluoride Hydroxide

Weight fraction/ %	23.0

Multiple Quantitative Results

Scans vs Phases Matrix

| Scan name | Sodium Aluminum Silicon Oxide Hydrate | Sodium Chloride | Calcium Carbonate | Sodium Magnesium Silicon Oxide Hydrate | Potassium Magnesium Aluminum Silicate Fluoride Hydroxide |
| --- | --- | --- | --- | --- | --- |
| 8 ETOSHA 22 CRUST 0-0.1CM S1 | 32.0 | 27.0 | 12.0 | 5.0 | 23.0 |

Anchor Scan Data

| Pos. [°2θ] | Iobs [cts] | Icalc [cts] | Iback [cts] |
| --- | --- | --- | --- |
| 5.0064 | 6732.0000 | 6744.8059 | 6732.0000 |
| 5.0174 | 6663.0492 | 6729.7506 | 6705.0958 |
| 5.0284 | 6665.1318 | 6703.1323 | 6678.1917 |
| 5.0394 | 6591.8481 | 6676.5191 | 6651.2875 |
| 5.0504 | 6611.3943 | 6649.9109 | 6624.3833 |
| 5.0614 | 6553.3181 | 6623.3079 | 6597.4791 |
| 5.0724 | 6438.2861 | 6596.7102 | 6570.5750 |
| 5.0834 | 6456.2453 | 6570.1180 | 6543.6708 |
| 5.0944 | 6337.4769 | 6543.5314 | 6516.7666 |
| 5.1054 | 6321.4425 | 6516.9505 | 6489.8625 |
| 5.1164 | 6500.5575 | 6490.3755 | 6462.9583 |
| 5.1274 | 6297.9086 | 6463.8065 | 6436.0541 |
| 5.1384 | 6188.2212 | 6437.2436 | 6409.1500 |
| 5.1494 | 6314.3466 | 6410.6870 | 6382.2458 |
| 5.1604 | 6209.6234 | 6384.1368 | 6355.3416 |
| 5.1714 | 6185.1165 | 6357.5933 | 6328.4374 |
| 5.1824 | 6115.6362 | 6331.0566 | 6301.5333 |
| 5.1934 | 6135.9857 | 6304.5267 | 6274.6291 |
| 5.2044 | 6058.4690 | 6278.0040 | 6247.7249 |
| 5.2154 | 6056.7483 | 6251.4886 | 6220.8208 |
| 5.2264 | 6081.5683 | 6224.9807 | 6193.9166 |
| 5.2374 | 5981.8392 | 6198.4805 | 6167.0124 |
| 5.2484 | 6020.0148 | 6171.9881 | 6140.1082 |
| 5.2594 | 6075.8402 | 6145.5039 | 6113.2041 |
| 5.2704 | 5972.1770 | 6119.0279 | 6086.2999 |
| 5.2814 | 5921.8623 | 6092.5604 | 6059.3957 |
| 5.2924 | 6035.4631 | 6066.1016 | 6032.4916 |
| 5.3034 | 5956.1372 | 6039.6519 | 6005.5874 |
| 5.3144 | 5757.7984 | 6013.2113 | 5978.6832 |
| 5.3254 | 5807.7429 | 5986.7802 | 5951.7790 |
| 5.3364 | 5836.3068 | 5960.3588 | 5924.8749 |
| 5.3474 | 5818.7620 | 5933.9474 | 5897.9707 |
| 5.3584 | 5772.8024 | 5907.5462 | 5871.0665 |
| 5.3694 | 5716.2242 | 5881.1556 | 5844.1624 |
| 5.3804 | 5722.0305 | 5854.7758 | 5817.2582 |
| 5.3914 | 5705.1736 | 5828.4071 | 5790.3540 |
| 5.4024 | 5673.5221 | 5802.0499 | 5763.4499 |
| 5.4134 | 5641.8289 | 5775.7044 | 5736.5457 |
| 5.4244 | 5676.4071 | 5749.3711 | 5709.6415 |
| 5.4354 | 5644.7758 | 5723.0502 | 5682.7373 |
| 5.4464 | 5613.7660 | 5696.7422 | 5655.8332 |
| 5.4574 | 5542.8353 | 5670.4474 | 5628.9290 |
| 5.4684 | 5505.9764 | 5644.1661 | 5602.0248 |
| 5.4794 | 5501.3766 | 5617.8989 | 5575.1207 |
| 5.4904 | 5447.1839 | 5591.6460 | 5548.2165 |
| 5.5014 | 5524.8363 | 5565.4080 | 5521.3123 |
| 5.5124 | 5456.4798 | 5539.1853 | 5494.4081 |
| 5.5234 | 5452.8270 | 5512.9784 | 5467.5040 |
| 5.5344 | 5461.9233 | 5496.2906 | 5440.5998 |
| 5.5454 | 5410.5796 | 5482.7154 | 5435.7973 |
| 5.5564 | 5413.1455 | 5478.6604 | 5430.9948 |
| 5.5674 | 5391.2994 | 5474.6232 | 5426.1923 |
| 5.5784 | 5442.4700 | 5470.6044 | 5421.3898 |
| 5.5894 | 5441.5659 | 5466.6045 | 5416.5873 |
| 5.6004 | 5367.2389 | 5462.6242 | 5411.7848 |
| 5.6114 | 5372.4484 | 5458.6642 | 5406.9823 |
| 5.6224 | 5321.2350 | 5454.7250 | 5402.1798 |
| 5.6334 | 5326.7301 | 5450.8073 | 5397.3773 |
| 5.6444 | 5292.0983 | 5446.9120 | 5392.5748 |
| 5.6554 | 5351.0438 | 5443.0396 | 5387.7723 |
| 5.6664 | 5286.6047 | 5439.1911 | 5382.9698 |
| 5.6774 | 5352.7173 | 5435.3671 | 5378.1673 |
| 5.6884 | 5308.2714 | 5431.5686 | 5373.3648 |
| 5.6994 | 5314.9735 | 5427.7964 | 5368.5623 |
| 5.7104 | 5326.3599 | 5424.0514 | 5363.7598 |
| 5.7214 | 5350.9676 | 5420.3346 | 5358.9573 |
| 5.7324 | 5366.7345 | 5416.9605 | 5354.1548 |
| 5.7434 | 5311.3550 | 5413.3760 | 5349.3523 |
| 5.7544 | 5237.9872 | 5409.9095 | 5344.5498 |
| 5.7654 | 5332.0103 | 5406.3552 | 5339.7473 |
| 5.7764 | 5452.5241 | 5402.7996 | 5334.9448 |
| 5.7874 | 5132.1514 | 5399.2789 | 5330.1423 |
| 5.7984 | 5324.5930 | 5395.7944 | 5325.3398 |
| 5.8094 | 5265.3781 | 5392.3475 | 5320.5373 |
| 5.8204 | 5116.7502 | 5388.9397 | 5315.7348 |
| 5.8314 | 5257.8673 | 5385.5725 | 5310.9323 |
| 5.8424 | 5152.3667 | 5382.2474 | 5306.1298 |
| 5.8534 | 5229.1770 | 5378.9660 | 5301.3273 |
| 5.8644 | 5322.2006 | 5375.7302 | 5296.5248 |
| 5.8754 | 5229.8717 | 5372.5418 | 5291.7223 |
| 5.8864 | 5247.6490 | 5369.4027 | 5286.9198 |
| 5.8974 | 5303.7522 | 5366.3150 | 5282.1173 |
| 5.9084 | 5379.1740 | 5363.2808 | 5277.3148 |
| 5.9194 | 5273.7906 | 5360.3025 | 5272.5123 |
| 5.9304 | 5217.8555 | 5357.3825 | 5267.7098 |
| 5.9414 | 5303.0000 | 5354.5235 | 5262.9073 |
| 5.9524 | 5301.9734 | 5351.7282 | 5258.1048 |
| 5.9634 | 5279.5236 | 5348.9995 | 5253.3023 |
| 5.9744 | 5207.2242 | 5346.3409 | 5248.4998 |
| 5.9854 | 5214.0511 | 5343.7555 | 5243.6972 |
| 5.9964 | 5148.1681 | 5341.2473 | 5238.8947 |
| 6.0074 | 5159.1849 | 5338.8203 | 5234.0922 |
| 6.0184 | 5170.3540 | 5336.4788 | 5229.2897 |
| 6.0294 | 5215.9012 | 5334.2276 | 5224.4872 |
| 6.0404 | 5367.1907 | 5332.0720 | 5219.6847 |
| 6.0514 | 5225.3884 | 5330.0178 | 5214.8822 |
| 6.0624 | 5254.1858 | 5327.5995 | 5210.0797 |
| 6.0734 | 5181.8427 | 5325.1421 | 5204.1799 |
| 6.0844 | 5226.5674 | 5322.3353 | 5198.2800 |
| 6.0954 | 5254.4823 | 5319.6596 | 5192.3801 |
| 6.1064 | 5235.9410 | 5317.1244 | 5186.4802 |
| 6.1174 | 5238.1067 | 5314.7406 | 5180.5803 |
| 6.1284 | 5357.3776 | 5312.5199 | 5174.6805 |
| 6.1394 | 5325.0885 | 5310.4757 | 5168.7806 |
| 6.1504 | 5428.6952 | 5308.6227 | 5162.8807 |
| 6.1614 | 5404.9808 | 5306.9776 | 5156.9808 |
| 6.1724 | 5441.5772 | 5305.5589 | 5151.0809 |
| 6.1834 | 5437.8909 | 5304.3875 | 5145.1810 |
| 6.1944 | 5424.3186 | 5303.4863 | 5139.2812 |
| 6.2054 | 5434.8820 | 5302.8814 | 5133.3813 |
| 6.2164 | 5476.7178 | 5302.6014 | 5127.4814 |
| 6.2274 | 5460.6829 | 5302.6785 | 5121.5815 |
| 6.2384 | 5610.5831 | 5303.1481 | 5115.6816 |
| 6.2494 | 5627.0555 | 5304.0497 | 5109.7818 |
| 6.2604 | 5606.4130 | 5305.4268 | 5103.8819 |
| 6.2714 | 5648.9720 | 5307.3274 | 5097.9820 |
| 6.2824 | 5680.4149 | 5309.8043 | 5092.0821 |
| 6.2934 | 5669.3319 | 5312.9151 | 5086.1822 |
| 6.3044 | 5685.8476 | 5316.7229 | 5080.2824 |
| 6.3154 | 5629.7222 | 5321.2963 | 5074.3825 |
| 6.3264 | 5673.9588 | 5326.7095 | 5068.4826 |
| 6.3374 | 5794.8722 | 5333.0428 | 5062.5827 |
| 6.3484 | 5763.0364 | 5340.3821 | 5056.6828 |
| 6.3594 | 5719.8584 | 5348.8198 | 5050.7829 |
| 6.3704 | 5814.6254 | 5358.4537 | 5044.8831 |
| 6.3814 | 5956.9563 | 5369.3877 | 5038.9832 |
| 6.3924 | 6027.3363 | 5381.7312 | 5033.0833 |
| 6.4034 | 6058.5364 | 5395.5989 | 5027.1834 |
| 6.4144 | 6069.4395 | 5411.1099 | 5021.2835 |
| 6.4254 | 6086.6386 | 5428.3878 | 5015.3837 |
| 6.4364 | 6071.8908 | 5447.5594 | 5009.4838 |
| 6.4474 | 6091.6077 | 5468.7539 | 5003.5839 |
| 6.4584 | 6143.0089 | 5492.1022 | 4997.6840 |
| 6.4694 | 6297.7321 | 5517.7354 | 4991.7841 |
| 6.4804 | 6328.4749 | 5545.7837 | 4985.8843 |
| 6.4914 | 6298.7035 | 5576.3748 | 4979.9844 |
| 6.5024 | 6441.3904 | 5609.6325 | 4974.0845 |
| 6.5134 | 6532.5162 | 5645.6748 | 4968.1846 |
| 6.5244 | 6564.9735 | 5684.6121 | 4962.2847 |
| 6.5354 | 6538.8687 | 5726.5456 | 4956.3849 |
| 6.5464 | 6600.3992 | 5771.5648 | 4950.4850 |
| 6.5574 | 6604.3436 | 5819.7458 | 4944.5851 |
| 6.5684 | 6675.4956 | 5871.1488 | 4938.6852 |
| 6.5794 | 6765.8825 | 5925.8162 | 4932.7853 |
| 6.5904 | 6908.4160 | 5983.3909 | 4926.8854 |
| 6.6014 | 7009.9228 | 6044.1279 | 4920.1040 |
| 6.6124 | 7072.4917 | 6107.7459 | 4913.3225 |
| 6.6234 | 6983.1519 | 6174.5707 | 4906.5410 |
| 6.6344 | 7057.2891 | 6244.5188 | 4899.7596 |
| 6.6454 | 7112.2547 | 6317.4737 | 4892.9781 |
| 6.6564 | 7291.9499 | 6393.2831 | 4886.1966 |
| 6.6674 | 7288.9061 | 6471.7556 | 4879.4152 |
| 6.6784 | 7309.9154 | 6552.6573 | 4872.6337 |
| 6.6894 | 7374.7567 | 6635.7086 | 4865.8522 |
| 6.7004 | 7301.7532 | 6720.5797 | 4859.0708 |
| 6.7114 | 7377.0807 | 6806.8875 | 4852.2893 |
| 6.7224 | 7456.6401 | 6894.1904 | 4845.5078 |
| 6.7334 | 7338.4208 | 6981.9855 | 4838.7264 |
| 6.7444 | 7494.7896 | 7069.7043 | 4831.9449 |
| 6.7554 | 7519.3142 | 7156.7105 | 4825.1634 |
| 6.7664 | 7328.6194 | 7242.2986 | 4818.3820 |
| 6.7774 | 7520.7085 | 7325.6950 | 4811.6005 |
| 6.7884 | 7693.4956 | 7406.0621 | 4804.8190 |
| 6.7994 | 7743.4941 | 7482.5057 | 4798.0376 |
| 6.8104 | 7599.2970 | 7554.0871 | 4791.2561 |
| 6.8214 | 7739.6371 | 7619.8409 | 4784.4746 |
| 6.8324 | 7631.4661 | 7678.7973 | 4777.6932 |
| 6.8434 | 7814.1671 | 7730.0094 | 4770.9117 |
| 6.8544 | 7480.8407 | 7772.5856 | 4764.1302 |
| 6.8654 | 7563.0703 | 7805.7227 | 4757.3488 |
| 6.8764 | 7534.9892 | 7828.7403 | 4750.5673 |
| 6.8874 | 7489.8009 | 7841.1119 | 4743.7858 |
| 6.8984 | 7530.2782 | 7842.4908 | 4737.0044 |
| 6.9094 | 7463.8049 | 7832.7275 | 4730.2229 |
| 6.9204 | 7543.9527 | 7811.8777 | 4723.4414 |
| 6.9314 | 7299.0201 | 7780.1992 | 4716.6600 |
| 6.9424 | 7200.0974 | 7738.1387 | 4709.8785 |
| 6.9534 | 7312.2168 | 7686.3094 | 4703.0970 |
| 6.9644 | 7357.4021 | 7625.4617 | 4696.3156 |
| 6.9754 | 7203.5702 | 7556.4506 | 4689.5341 |
| 6.9864 | 6991.3098 | 7480.2013 | 4682.7526 |
| 6.9974 | 7098.4272 | 7397.6761 | 4675.9712 |
| 7.0084 | 7061.2458 | 7309.8453 | 4669.1897 |
| 7.0194 | 6899.6754 | 7217.6618 | 4662.4082 |
| 7.0304 | 6688.8289 | 7122.0418 | 4655.6268 |
| 7.0414 | 6559.6617 | 7023.8500 | 4648.8453 |
| 7.0524 | 6436.2537 | 6923.8901 | 4642.0638 |
| 7.0634 | 6404.9789 | 6822.8991 | 4635.2824 |
| 7.0744 | 6446.5713 | 6721.5453 | 4628.5009 |
| 7.0854 | 6385.7301 | 6620.4281 | 4621.7194 |
| 7.0964 | 6286.1583 | 6520.0806 | 4614.9380 |
| 7.1074 | 6234.9946 | 6420.9722 | 4608.1565 |
| 7.1184 | 6175.1445 | 6323.5128 | 4601.3750 |
| 7.1294 | 6049.4435 | 6228.0563 | 4594.5936 |
| 7.1404 | 6036.2409 | 6134.9052 | 4587.8121 |
| 7.1514 | 5905.7300 | 6044.3142 | 4581.0306 |
| 7.1624 | 5776.1357 | 5956.4939 | 4574.2492 |
| 7.1734 | 5772.3599 | 5871.6146 | 4567.4677 |
| 7.1844 | 5705.1327 | 5789.8088 | 4560.6862 |
| 7.1954 | 5613.6907 | 5711.1753 | 4553.9048 |

Scan List

| Vis. | Dataset Name | Start pos. [°2θ] | End pos. [°2θ] | Step [°2θ] | Meas.Date/Time |
| --- | --- | --- | --- | --- | --- |
| * | 8 ETOSHA 22 CRUST 0-0.1CM S1 | 5.0064 | 84.9874 | 0.0110 | 8/22/2023 2:10:34 PM |

Peak List

| Pos. [°2θ] | Height [cts] | FWHM Left [°2θ] | d-spacing [Å] | Rel. Int. [%] |
| --- | --- | --- | --- | --- |
| 6.8953 | 2772.62 | 0.4763 | 12.80923 | 4.56 |
| 8.7596 | 407.20 | 0.3031 | 10.08680 | 0.67 |
| 11.6033 | 171.29 | 0.3464 | 7.62031 | 0.28 |
| 15.8096 | 4961.58 | 0.1191 | 5.60106 | 8.16 |
| 18.2812 | 868.90 | 0.0866 | 4.84899 | 1.43 |
| 19.7982 | 1997.92 | 0.1732 | 4.48074 | 3.29 |
| 20.7979 | 1051.59 | 0.0541 | 4.26756 | 1.73 |
| 21.3615 | 385.27 | 0.2598 | 4.15621 | 0.63 |
| 23.0031 | 1109.72 | 0.0433 | 3.86319 | 1.83 |
| 23.4322 | 1448.68 | 0.2165 | 3.79341 | 2.38 |
| 24.3011 | 216.61 | 0.1732 | 3.65971 | 0.36 |
| 25.1926 | 926.15 | 0.1732 | 3.53218 | 1.52 |
| 25.9593 | 6982.28 | 0.1082 | 3.42957 | 11.48 |
| 26.5952 | 2412.09 | 0.0433 | 3.34899 | 3.97 |
| 27.3155 | 3589.16 | 0.0866 | 3.26230 | 5.90 |
| 28.5030 | 210.60 | 0.1299 | 3.12902 | 0.35 |
| 29.3419 | 4515.44 | 0.1515 | 3.04144 | 7.43 |
| 30.5475 | 3138.05 | 0.1299 | 2.92410 | 5.16 |
| 31.6474 | 60800.97 | 0.0660 | 2.82493 | 100.00 |
| 31.7389 | 29239.10 | 0.0396 | 2.81701 | 48.09 |
| 33.2642 | 924.33 | 0.1848 | 2.69124 | 1.52 |
| 33.9120 | 967.71 | 0.2376 | 2.64129 | 1.59 |
| 34.6208 | 1950.12 | 0.1848 | 2.58882 | 3.21 |
| 35.9099 | 1291.73 | 0.3168 | 2.49879 | 2.12 |
| 37.0369 | 471.44 | 0.2112 | 2.42530 | 0.78 |
| 39.3632 | 914.10 | 0.2112 | 2.28716 | 1.50 |
| 40.5148 | 435.36 | 0.1056 | 2.22477 | 0.72 |
| 42.3577 | 140.72 | 0.3168 | 2.13213 | 0.23 |
| 43.1687 | 650.52 | 0.1848 | 2.09394 | 1.07 |
| 45.3775 | 17903.35 | 0.1056 | 1.99702 | 29.45 |
| 45.5143 | 8759.72 | 0.0660 | 1.99133 | 14.41 |
| 47.0488 | 500.09 | 0.2640 | 1.92990 | 0.82 |
| 47.4662 | 658.89 | 0.2112 | 1.91390 | 1.08 |
| 47.8265 | 806.54 | 0.2640 | 1.90032 | 1.33 |
| 48.4755 | 591.78 | 0.2640 | 1.87638 | 0.97 |
| 50.7698 | 89.33 | 0.4224 | 1.79684 | 0.15 |
| 51.6694 | 82.65 | 0.3168 | 1.76765 | 0.14 |
| 52.5084 | 753.33 | 0.1584 | 1.74136 | 1.24 |
| 53.7885 | 537.62 | 0.0792 | 1.70290 | 0.88 |
| 54.3335 | 282.54 | 0.2640 | 1.68710 | 0.46 |
| 56.3514 | 3160.66 | 0.0792 | 1.63138 | 5.20 |
| 56.4210 | 3470.92 | 0.0660 | 1.62953 | 5.71 |
| 56.5694 | 1798.51 | 0.0792 | 1.62561 | 2.96 |
| 57.3853 | 200.26 | 0.1584 | 1.60442 | 0.33 |
| 57.8358 | 201.93 | 0.2112 | 1.59299 | 0.33 |
| 59.8900 | 341.34 | 0.0792 | 1.54316 | 0.56 |
| 60.6131 | 422.79 | 0.5280 | 1.52647 | 0.70 |
| 61.2778 | 386.89 | 0.3168 | 1.51150 | 0.64 |
| 62.8845 | 112.22 | 0.4224 | 1.47669 | 0.18 |
| 64.6279 | 215.93 | 0.2112 | 1.44100 | 0.36 |
| 66.1551 | 3551.06 | 0.0660 | 1.41139 | 5.84 |
| 66.3475 | 1836.08 | 0.0792 | 1.40776 | 3.02 |
| 67.6894 | 200.42 | 0.1584 | 1.38308 | 0.33 |
| 69.1483 | 325.50 | 0.2640 | 1.35742 | 0.54 |
| 72.2842 | 129.07 | 0.4224 | 1.30606 | 0.21 |
| 72.9495 | 193.13 | 0.1584 | 1.29578 | 0.32 |
| 73.7920 | 107.98 | 0.3168 | 1.28305 | 0.18 |
| 75.1997 | 4661.22 | 0.1188 | 1.26249 | 7.67 |
| 75.4173 | 2571.82 | 0.0660 | 1.25939 | 4.23 |
| 78.2455 | 216.61 | 0.4224 | 1.22079 | 0.36 |
| 81.3555 | 114.80 | 0.3168 | 1.18180 | 0.19 |
| 83.9185 | 2107.01 | 0.1056 | 1.15210 | 3.47 |
| 84.1459 | 1112.67 | 0.1056 | 1.14957 | 1.83 |

Pattern List

| Visible | Ref.Code | Score | Compound Name | Chem. Formula | Mineral Name | SemiQuant[%] |
| --- | --- | --- | --- | --- | --- | --- |
| * | 04-012-1749 | 61 | Sodium Aluminum Silicon Oxide Hydrate | Na7.7 Al7.7 Si16.3 O48 ( H2 O )8 | Analcime | 32 |
| * | 01-085-8594 | 39 | Sodium Chloride | Na Cl | Halite | 27 |
| * | 01-072-1937 | 51 | Calcium Carbonate | Ca ( C O3 ) | Calcite | 12 |
| * | 01-082-8023 | 20 | Sodium Magnesium Silicon Oxide Hydrate | Na2 Mg3 ( Si6 O16 ) ( H2 O )7 | Loughlinite | 5 |
| * | 04-013-9383 | 17 | Potassium Magnesium Aluminum Silicate Fluoride Hydroxide | K Mg3 Al Si3 O10 ( O H ) F | Phlogopite-2M1 | 23 |

Anchor Scan Parameters

Dataset Name	8 ETOSHA 22 CRUST 0-0.1CM S1

File name	C:\aeris_data\XRD data\8 ETOSHA 22 CRUST 0-0.1CM S1.xrdml

Sample Identification	8 ETOSHA 22 CRUST 0-0.1CM S1

Measurement Start Date/Time	8/22/2023 2:10:34 PM

Operator	Instrument

Raw Data Origin	XRD measurement (*.XRDML)

Scan Axis	Gonio

Start Position [°2θ]	5.0064

End Position [°2θ]	84.9874

Step Size [°2θ]	0.0110

Scan Step Time [s]	48.1950

Scan Type	Continuous

PSD Mode	Scanning

PSD Length [°2θ]	5.54

Offset [°2θ]	0.0000

Divergence Slit Type	Fixed

Divergence Slit Size [°]	0.4584

Specimen Length [mm]	10.00

Measurement Temperature [°C]	25.00

Anode Material	Cu

K-α1 [Å]	1.54060

K-α2 [Å]	1.54443

K-β1 [Å]	1.39225

K-A2 / K-A1 Ratio	0.50000

Generator Settings	15 mA, 40 kV

Diffractometer Type	2082464

Diffractometer Number	0

Goniometer Radius [mm]	145.00

Dist. Focus-Diverg. Slit [mm]	95.00

Incident Beam Monochromator	No

Spinning	Yes