CS2

Graphics

Graphics

Graphics

Quantitative Results

Phase Calcium Carbonate

Weight fraction/ %	7.0

Phase Sodium Chloride

Weight fraction/ %	6.0

Phase Sodium Aluminum Silicate Hydrate

Weight fraction/ %	28.0

Phase Potassium Aluminum Silicate Hydroxide

Weight fraction/ %	39.0

Phase Sodium Magnesium Silicon Oxide Hydrate

Weight fraction/ %	2.0

Phase Potassium Sodium Calcium Aluminum Silicate

Weight fraction/ %	18.0

Multiple Quantitative Results

Scans vs Phases Matrix

| Scan name | Calcium Carbonate | Sodium Chloride | Sodium Aluminum Silicate Hydrate | Potassium Aluminum Silicate Hydroxide | Sodium Magnesium Silicon Oxide Hydrate | Potassium Sodium Calcium Aluminum Silicate |
| --- | --- | --- | --- | --- | --- | --- |
| CS2 | 7.0 | 6.0 | 28.0 | 39.0 | 2.0 | 18.0 |

Anchor Scan Data

| Pos. [°2θ] | Iobs [cts] | Icalc [cts] | Iback [cts] |
| --- | --- | --- | --- |
| 6.0000 | 101.0000 | 101.2986 | 101.0000 |
| 6.0200 | 119.0000 | 101.0435 | 100.6777 |
| 6.0400 | 101.0000 | 100.7354 | 100.3553 |
| 6.0600 | 107.0000 | 100.4281 | 100.0330 |
| 6.0800 | 85.0000 | 100.1217 | 99.7106 |
| 6.1000 | 116.0000 | 99.8163 | 99.3883 |
| 6.1200 | 100.0000 | 99.5120 | 99.0659 |
| 6.1400 | 103.0000 | 99.2088 | 98.7436 |
| 6.1600 | 106.0000 | 98.9069 | 98.4212 |
| 6.1800 | 118.0000 | 98.6063 | 98.0989 |
| 6.2000 | 105.0000 | 98.3073 | 97.7765 |
| 6.2200 | 113.0000 | 98.0098 | 97.4542 |
| 6.2400 | 115.0000 | 97.7142 | 97.1318 |
| 6.2600 | 96.0000 | 97.4206 | 96.8095 |
| 6.2800 | 92.0000 | 97.1291 | 96.4871 |
| 6.3000 | 142.0000 | 96.8400 | 96.1648 |
| 6.3200 | 109.0000 | 96.5502 | 95.8424 |
| 6.3400 | 109.0000 | 96.2502 | 95.5003 |
| 6.3600 | 109.0000 | 95.9501 | 95.1581 |
| 6.3800 | 113.0000 | 95.6537 | 94.8160 |
| 6.4000 | 122.0000 | 95.3613 | 94.4738 |
| 6.4200 | 123.0000 | 95.0734 | 94.1317 |
| 6.4400 | 123.0000 | 94.7907 | 93.7895 |
| 6.4600 | 128.0000 | 94.5137 | 93.4474 |
| 6.4800 | 110.0000 | 94.2433 | 93.1052 |
| 6.5000 | 123.0000 | 93.9804 | 92.7631 |
| 6.5200 | 129.0000 | 93.7259 | 92.4209 |
| 6.5400 | 135.0000 | 93.4812 | 92.0788 |
| 6.5600 | 129.0000 | 93.2478 | 91.7366 |
| 6.5800 | 121.0000 | 93.0274 | 91.3944 |
| 6.6000 | 146.0000 | 92.8222 | 91.0523 |
| 6.6200 | 121.0000 | 92.6347 | 90.7101 |
| 6.6400 | 169.0000 | 92.4650 | 90.3680 |
| 6.6600 | 137.0000 | 92.3070 | 90.0060 |
| 6.6800 | 143.0000 | 92.1754 | 89.6441 |
| 6.7000 | 155.0000 | 92.0798 | 89.2821 |
| 6.7200 | 158.0000 | 92.0278 | 88.9202 |
| 6.7400 | 158.0000 | 92.0294 | 88.5582 |
| 6.7600 | 168.0000 | 92.0981 | 88.1962 |
| 6.7800 | 159.0000 | 92.2524 | 87.8343 |
| 6.8000 | 186.0000 | 92.5203 | 87.4723 |
| 6.8200 | 149.0000 | 92.9481 | 87.1104 |
| 6.8400 | 184.0000 | 93.6177 | 86.7484 |
| 6.8600 | 186.0000 | 94.6780 | 86.3864 |
| 6.8800 | 172.0000 | 96.3921 | 86.0245 |
| 6.9000 | 165.0000 | 99.1931 | 85.6625 |
| 6.9200 | 175.0000 | 103.7195 | 85.3006 |
| 6.9400 | 167.0000 | 110.7848 | 84.9386 |
| 6.9600 | 183.0000 | 121.2269 | 84.5766 |
| 6.9800 | 214.0000 | 135.6126 | 84.2147 |
| 7.0000 | 193.0000 | 153.8146 | 83.8527 |
| 7.0200 | 184.0000 | 174.4740 | 83.4908 |
| 7.0400 | 186.0000 | 194.3869 | 83.1288 |
| 7.0600 | 186.0000 | 208.3208 | 82.7668 |
| 7.0800 | 214.0000 | 211.0017 | 82.4049 |
| 7.1000 | 192.0000 | 201.1059 | 82.0429 |
| 7.1200 | 189.0000 | 182.5193 | 81.6810 |
| 7.1400 | 166.0000 | 160.9332 | 81.3190 |
| 7.1600 | 184.0000 | 140.5797 | 80.9571 |
| 7.1800 | 153.0000 | 123.6088 | 80.5951 |
| 7.2000 | 139.0000 | 110.6439 | 80.2331 |
| 7.2200 | 133.0000 | 101.3800 | 79.8712 |
| 7.2400 | 128.0000 | 95.0587 | 79.5092 |
| 7.2600 | 138.0000 | 90.8263 | 79.1473 |
| 7.2800 | 128.0000 | 87.9484 | 78.7853 |
| 7.3000 | 134.0000 | 85.8876 | 78.4035 |
| 7.3200 | 91.0000 | 84.3183 | 78.0218 |
| 7.3400 | 116.0000 | 83.0486 | 77.6400 |
| 7.3600 | 118.0000 | 81.9706 | 77.2582 |
| 7.3800 | 115.0000 | 81.0245 | 76.8765 |
| 7.4000 | 111.0000 | 80.1753 | 76.4947 |
| 7.4200 | 123.0000 | 79.4010 | 76.1130 |
| 7.4400 | 118.0000 | 78.6859 | 75.7312 |
| 7.4600 | 82.0000 | 78.0189 | 75.3494 |
| 7.4800 | 113.0000 | 77.3911 | 74.9677 |
| 7.5000 | 91.0000 | 76.7957 | 74.5859 |
| 7.5200 | 86.0000 | 76.2274 | 74.2041 |
| 7.5400 | 90.0000 | 75.6818 | 73.8224 |
| 7.5600 | 78.0000 | 75.1554 | 73.4406 |
| 7.5800 | 91.0000 | 74.6453 | 73.0588 |
| 7.6000 | 68.0000 | 74.1459 | 72.6771 |
| 7.6200 | 92.0000 | 73.6454 | 72.2755 |
| 7.6400 | 79.0000 | 73.1519 | 71.8739 |
| 7.6600 | 65.0000 | 72.6676 | 71.4724 |
| 7.6800 | 96.0000 | 72.1911 | 71.0708 |
| 7.7000 | 77.0000 | 71.7216 | 70.6692 |
| 7.7200 | 73.0000 | 71.2583 | 70.2677 |
| 7.7400 | 70.0000 | 70.8003 | 69.8661 |
| 7.7600 | 78.0000 | 70.3471 | 69.4645 |
| 7.7800 | 87.0000 | 69.8983 | 69.0629 |
| 7.8000 | 65.0000 | 69.4532 | 68.6614 |
| 7.8200 | 80.0000 | 69.0116 | 68.2598 |
| 7.8400 | 80.0000 | 68.5730 | 67.8582 |
| 7.8600 | 64.0000 | 68.1373 | 67.4567 |
| 7.8800 | 69.0000 | 67.7040 | 67.0551 |
| 7.9000 | 69.0000 | 67.2730 | 66.6535 |
| 7.9200 | 68.0000 | 66.8933 | 66.2520 |
| 7.9400 | 62.0000 | 66.7120 | 66.1454 |
| 7.9600 | 71.0000 | 66.5816 | 66.0388 |
| 7.9800 | 65.0000 | 66.4528 | 65.9322 |
| 8.0000 | 74.0000 | 66.3255 | 65.8256 |
| 8.0200 | 84.0000 | 66.1994 | 65.7190 |
| 8.0400 | 69.0000 | 66.0746 | 65.6124 |
| 8.0600 | 78.0000 | 65.9508 | 65.5059 |
| 8.0800 | 66.0000 | 65.8281 | 65.3993 |
| 8.1000 | 79.0000 | 65.7064 | 65.2927 |
| 8.1200 | 63.0000 | 65.5855 | 65.1861 |
| 8.1400 | 71.0000 | 65.4654 | 65.0795 |
| 8.1600 | 72.0000 | 65.3461 | 64.9729 |
| 8.1800 | 83.0000 | 65.2275 | 64.8664 |
| 8.2000 | 75.0000 | 65.1096 | 64.7598 |
| 8.2200 | 81.0000 | 64.9922 | 64.6532 |
| 8.2400 | 59.0000 | 64.8715 | 64.5466 |
| 8.2600 | 71.0000 | 64.7355 | 64.4164 |
| 8.2800 | 73.0000 | 64.5961 | 64.2861 |
| 8.3000 | 77.0000 | 64.4572 | 64.1559 |
| 8.3200 | 78.0000 | 64.3187 | 64.0257 |
| 8.3400 | 67.0000 | 64.1806 | 63.8955 |
| 8.3600 | 77.0000 | 64.0429 | 63.7652 |
| 8.3800 | 91.0000 | 63.9056 | 63.6350 |
| 8.4000 | 73.0000 | 63.7686 | 63.5048 |
| 8.4200 | 66.0000 | 63.6319 | 63.3745 |
| 8.4400 | 79.0000 | 63.4955 | 63.2443 |
| 8.4600 | 71.0000 | 63.3594 | 63.1141 |
| 8.4800 | 66.0000 | 63.2236 | 62.9839 |
| 8.5000 | 75.0000 | 63.0881 | 62.8536 |
| 8.5200 | 74.0000 | 62.9527 | 62.7234 |
| 8.5400 | 75.0000 | 62.8177 | 62.5932 |
| 8.5600 | 76.0000 | 62.6788 | 62.4629 |
| 8.5800 | 65.0000 | 62.5245 | 62.3091 |
| 8.6000 | 74.0000 | 62.3664 | 62.1552 |
| 8.6200 | 76.0000 | 62.2085 | 62.0013 |
| 8.6400 | 72.0000 | 62.0377 | 61.8475 |
| 8.6600 | 70.0000 | 61.7792 | 61.6936 |
| 8.6800 | 86.0000 | 61.5774 | 61.5397 |
| 8.7000 | 83.0000 | 61.4240 | 61.3859 |
| 8.7200 | 89.0000 | 61.2706 | 61.2320 |
| 8.7400 | 78.0000 | 61.1173 | 61.0781 |
| 8.7600 | 76.0000 | 60.9639 | 60.9242 |
| 8.7800 | 77.0000 | 60.8106 | 60.7704 |
| 8.8000 | 76.0000 | 60.6573 | 60.6165 |
| 8.8200 | 78.0000 | 60.5039 | 60.4626 |
| 8.8400 | 65.0000 | 60.3506 | 60.3088 |
| 8.8600 | 80.0000 | 60.1973 | 60.1549 |
| 8.8800 | 73.0000 | 60.0441 | 60.0010 |
| 8.9000 | 81.0000 | 59.8908 | 59.8471 |
| 8.9200 | 79.0000 | 59.7375 | 59.6933 |
| 8.9400 | 88.0000 | 59.5843 | 59.5394 |
| 8.9600 | 76.0000 | 59.4311 | 59.3855 |
| 8.9800 | 69.0000 | 59.2778 | 59.2317 |
| 9.0000 | 79.0000 | 59.1246 | 59.0778 |
| 9.0200 | 63.0000 | 58.9715 | 58.9239 |
| 9.0400 | 68.0000 | 58.8183 | 58.7701 |
| 9.0600 | 65.0000 | 58.6651 | 58.6162 |
| 9.0800 | 72.0000 | 58.5120 | 58.4623 |
| 9.1000 | 58.0000 | 58.3589 | 58.3084 |
| 9.1200 | 70.0000 | 58.2057 | 58.1546 |
| 9.1400 | 55.0000 | 58.0527 | 58.0007 |
| 9.1600 | 72.0000 | 57.8996 | 57.8468 |
| 9.1800 | 74.0000 | 57.7465 | 57.6930 |
| 9.2000 | 65.0000 | 57.5895 | 57.5391 |
| 9.2200 | 67.0000 | 57.4168 | 57.3616 |
| 9.2400 | 57.0000 | 57.2402 | 57.1841 |
| 9.2600 | 60.0000 | 57.0636 | 57.0066 |
| 9.2800 | 59.0000 | 56.8870 | 56.8290 |
| 9.3000 | 41.0000 | 56.7104 | 56.6515 |
| 9.3200 | 63.0000 | 56.5339 | 56.4740 |
| 9.3400 | 74.0000 | 56.3573 | 56.2965 |
| 9.3600 | 70.0000 | 56.1808 | 56.1190 |
| 9.3800 | 57.0000 | 56.0044 | 55.9415 |
| 9.4000 | 59.0000 | 55.8279 | 55.7640 |
| 9.4200 | 43.0000 | 55.6515 | 55.5865 |
| 9.4400 | 59.0000 | 55.4751 | 55.4089 |
| 9.4600 | 59.0000 | 55.2987 | 55.2314 |
| 9.4800 | 50.0000 | 55.1224 | 55.0539 |
| 9.5000 | 69.0000 | 54.9461 | 54.8764 |
| 9.5200 | 61.0000 | 54.7658 | 54.6989 |
| 9.5400 | 52.0000 | 54.5699 | 54.4977 |
| 9.5600 | 55.0000 | 54.3701 | 54.2966 |
| 9.5800 | 56.0000 | 54.1703 | 54.0954 |
| 9.6000 | 58.0000 | 53.9705 | 53.8943 |
| 9.6200 | 55.0000 | 53.7707 | 53.6931 |
| 9.6400 | 51.0000 | 53.5711 | 53.4920 |
| 9.6600 | 58.0000 | 53.3714 | 53.2908 |
| 9.6800 | 46.0000 | 53.1718 | 53.0897 |
| 9.7000 | 51.0000 | 52.9722 | 52.8885 |
| 9.7200 | 61.0000 | 52.7727 | 52.6874 |
| 9.7400 | 68.0000 | 52.5732 | 52.4862 |
| 9.7600 | 47.0000 | 52.3738 | 52.2851 |
| 9.7800 | 57.0000 | 52.1744 | 52.0839 |
| 9.8000 | 64.0000 | 51.9751 | 51.8828 |
| 9.8200 | 58.0000 | 51.7758 | 51.6816 |
| 9.8400 | 55.0000 | 51.6119 | 51.4805 |
| 9.8600 | 37.0000 | 51.5889 | 51.4907 |
| 9.8800 | 47.0000 | 51.6012 | 51.5010 |
| 9.9000 | 53.0000 | 51.6136 | 51.5112 |
| 9.9200 | 56.0000 | 51.6261 | 51.5215 |
| 9.9400 | 46.0000 | 51.6386 | 51.5317 |
| 9.9600 | 50.0000 | 51.6512 | 51.5420 |
| 9.9800 | 44.0000 | 51.6639 | 51.5522 |

Scan List

| Vis. | Dataset Name | Start pos. [°2θ] | End pos. [°2θ] | Step [°2θ] | Meas.Date/Time |
| --- | --- | --- | --- | --- | --- |
| * | CS2 | 6.0000 | 55.0000 | 0.0200 | 9/25/2019 1:35:00 PM |

Peak List

| Pos. [°2θ] | Height [cts] | FWHM Left [°2θ] | d-spacing [Å] | Rel. Int. [%] |
| --- | --- | --- | --- | --- |
| 7.0688 | 116.81 | 0.1574 | 12.49519 | 12.63 |
| 11.7466 | 11.37 | 0.4723 | 7.52764 | 1.23 |
| 15.9550 | 256.37 | 0.0787 | 5.55033 | 27.71 |
| 18.4110 | 40.03 | 0.2362 | 4.81510 | 4.33 |
| 19.9786 | 161.99 | 0.2755 | 4.44068 | 17.51 |
| 21.6115 | 26.45 | 0.2362 | 4.10870 | 2.86 |
| 23.6549 | 68.94 | 0.1574 | 3.75820 | 7.45 |
| 26.1587 | 559.93 | 0.1574 | 3.40388 | 60.52 |
| 26.8520 | 63.78 | 0.2362 | 3.31755 | 6.89 |
| 27.5727 | 75.99 | 0.3149 | 3.23244 | 8.21 |
| 29.5749 | 405.80 | 0.1574 | 3.01801 | 43.86 |
| 30.7249 | 374.49 | 0.1378 | 2.90762 | 40.48 |
| 31.8580 | 925.22 | 0.1181 | 2.80674 | 100.00 |
| 33.4706 | 96.52 | 0.1968 | 2.67511 | 10.43 |
| 34.9739 | 203.80 | 0.8659 | 2.56349 | 22.03 |
| 36.1068 | 191.44 | 0.1968 | 2.48561 | 20.69 |
| 37.2946 | 109.19 | 0.1968 | 2.40913 | 11.80 |
| 39.5638 | 104.35 | 0.1574 | 2.27602 | 11.28 |
| 40.7491 | 75.48 | 0.1574 | 2.21252 | 8.16 |
| 43.3212 | 66.58 | 0.1968 | 2.08692 | 7.20 |
| 45.5989 | 569.32 | 0.1574 | 1.98783 | 61.53 |
| 47.6740 | 112.42 | 0.1181 | 1.90604 | 12.15 |
| 48.0220 | 121.48 | 0.1574 | 1.89304 | 13.13 |
| 48.6331 | 102.06 | 0.1574 | 1.87067 | 11.03 |
| 52.7151 | 161.48 | 0.2755 | 1.73502 | 17.45 |
| 53.6287 | 61.19 | 0.2362 | 1.70760 | 6.61 |

Pattern List

| Visible | Ref.Code | Score | Compound Name | Chem. Formula | Mineral Name | SemiQuant[%] |
| --- | --- | --- | --- | --- | --- | --- |
| * | 01-085-1108 | 38 | Calcium Carbonate | Ca ( C O3 ) | Calcite | 7 |
| * | 01-071-3741 | 31 | Sodium Chloride | Na Cl | Halite | 6 |
| * | 01-076-6569 | 32 | Sodium Aluminum Silicate Hydrate | Na0.9 ( ( Al0.9 Si2 ) O6 ) ( H2 O ) | Analcime | 28 |
| * | 04-011-5240 | 12 | Potassium Aluminum Silicate Hydroxide | K Al3 Si3 O10 ( O H )2 | Muscovite-2M1 | 39 |
| * | 01-082-8023 | 9 | Sodium Magnesium Silicon Oxide Hydrate | Na2 Mg3 ( Si6 O16 ) ( H2 O )7 | Loughlinite | 2 |
| * | 04-016-1657 | 15 | Potassium Sodium Calcium Aluminum Silicate | K0.42 Na0.58 Ca0.03 Al Si3 O8 | Sanidine | 18 |

Anchor Scan Parameters

Dataset Name	CS2

File name	E:\xrd\XRD\Goldstien\Namibia\CS2.MDI

Comment	CS2, Bulk, lt 2mm, Etosha pan, Namibia, Goldstein

Measurement Start Date/Time	9/25/2019 1:35:00 PM

Raw Data Origin	Jade ASCII (scan) (.MDI)

Scan Axis	Gonio

Start Position [°2θ]	6.0000

End Position [°2θ]	55.0000

Step Size [°2θ]	0.0200

Scan Step Time [s]	1.0000

Scan Type	Pre-set time

Offset [°2θ]	0.0000

Divergence Slit Type	Fixed

Divergence Slit Size [°]	1.0000

Specimen Length [mm]	10.00

Receiving Slit Size [mm]	0.1000

Measurement Temperature [°C]	25.00

Anode Material	Cu

K-α1 [Å]	1.54060

K-α2 [Å]	1.54443

K-β1 [Å]	1.39225

K-A2 / K-A1 Ratio	0.50000

Generator Settings	0 mA, 0 kV

Diffractometer Number	0

Goniometer Radius [mm]	240.00

Dist. Focus-Diverg. Slit [mm]	91.00

Incident Beam Monochromator	No

Spinning	No