1 Etosha 18 RIP 0-2cm heated to 400C

Graphics

Graphics

Graphics

Quantitative Results

Phase Sodium Aluminum Silicate Hydrate

Weight fraction/ %	39.0

Phase Magnesium Silicon Oxide Hydroxide Hydrate

Weight fraction/ %	7.0

Phase Magnesium Aluminum Iron Silicon Oxide Hydroxide Hydrate

Weight fraction/ %	6.0

Phase Potassium Lithium Iron Aluminum Silicate Hydroxide

Weight fraction/ %	24.0

Phase Sodium Magnesium Silicon Oxide Hydrate

Weight fraction/ %	5.0

Phase Magnesium Silicon Oxide Hydroxide

Weight fraction/ %	7.0

Phase Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide

Weight fraction/ %	11.0

Multiple Quantitative Results

Scans vs Phases Matrix

| Scan name | Sodium Aluminum Silicate Hydrate | Magnesium Silicon Oxide Hydroxide Hydrate | Magnesium Aluminum Iron Silicon Oxide Hydroxide Hydrate | Potassium Lithium Iron Aluminum Silicate Hydroxide | Sodium Magnesium Silicon Oxide Hydrate | Magnesium Silicon Oxide Hydroxide | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 1 Etosha18 rip 0-2cm 400C | 39.0 | 7.0 | 6.0 | 24.0 | 5.0 | 7.0 | 11.0 |

Anchor Scan Data

| Pos. [°2θ] | Iobs [cts] | Icalc [cts] | Iback [cts] |
| --- | --- | --- | --- |
| 2.0054 | 3957.0000 | 3955.5392 | 3957.0000 |
| 2.0164 | 3886.3363 | 3935.8413 | 3930.7547 |
| 2.0274 | 3832.7296 | 3909.6871 | 3904.5095 |
| 2.0384 | 3822.5900 | 3883.5359 | 3878.2642 |
| 2.0494 | 3829.7896 | 3857.3880 | 3852.0190 |
| 2.0604 | 3676.0393 | 3831.2434 | 3825.7737 |
| 2.0714 | 3749.8289 | 3805.1025 | 3799.5285 |
| 2.0824 | 3711.1185 | 3778.9653 | 3773.2832 |
| 2.0934 | 3708.1524 | 3752.8321 | 3747.0379 |
| 2.1044 | 3576.0929 | 3726.7030 | 3720.7927 |
| 2.1154 | 3597.8151 | 3700.5784 | 3694.5474 |
| 2.1264 | 3525.4361 | 3674.4585 | 3668.3022 |
| 2.1374 | 3567.1003 | 3648.3435 | 3642.0569 |
| 2.1484 | 3527.4076 | 3622.2336 | 3615.8116 |
| 2.1594 | 3493.1819 | 3596.1292 | 3589.5664 |
| 2.1704 | 3488.6209 | 3570.0306 | 3563.3211 |
| 2.1814 | 3561.7571 | 3543.9380 | 3537.0759 |
| 2.1924 | 3521.0747 | 3518.8882 | 3510.8306 |
| 2.2034 | 3488.7611 | 3495.9834 | 3488.7964 |
| 2.2144 | 3415.6347 | 3474.1221 | 3466.7622 |
| 2.2254 | 3420.2625 | 3452.2682 | 3444.7280 |
| 2.2364 | 3380.8319 | 3430.4222 | 3422.6938 |
| 2.2474 | 3295.3619 | 3408.5844 | 3400.6596 |
| 2.2584 | 3351.3038 | 3386.7553 | 3378.6254 |
| 2.2694 | 3333.7257 | 3364.9354 | 3356.5912 |
| 2.2804 | 3339.7950 | 3343.1249 | 3334.5570 |
| 2.2914 | 3382.4975 | 3321.3245 | 3312.5229 |
| 2.3024 | 3274.4115 | 3299.5346 | 3290.4887 |
| 2.3134 | 3241.4090 | 3277.7558 | 3268.4545 |
| 2.3244 | 3225.3264 | 3255.9885 | 3246.4203 |
| 2.3354 | 3221.9233 | 3234.2333 | 3224.3861 |
| 2.3464 | 3278.8569 | 3212.4907 | 3202.3519 |
| 2.3574 | 3229.4090 | 3190.7613 | 3180.3177 |
| 2.3684 | 3161.2729 | 3169.0457 | 3158.2835 |
| 2.3794 | 3127.6283 | 3149.1507 | 3136.2493 |
| 2.3904 | 3079.4641 | 3132.9977 | 3121.5546 |
| 2.4014 | 3120.7611 | 3118.6666 | 3106.8600 |
| 2.4124 | 3137.8997 | 3104.3517 | 3092.1653 |
| 2.4234 | 3105.1917 | 3090.0538 | 3077.4706 |
| 2.4344 | 3087.7684 | 3075.7733 | 3062.7760 |
| 2.4454 | 3074.1170 | 3061.5110 | 3048.0813 |
| 2.4564 | 3037.2679 | 3047.2675 | 3033.3867 |
| 2.4674 | 3007.4838 | 3033.0436 | 3018.6920 |
| 2.4784 | 3015.4562 | 3018.8398 | 3003.9973 |
| 2.4894 | 2982.9803 | 3004.6569 | 2989.3027 |
| 2.5004 | 2936.2788 | 2990.4955 | 2974.6080 |
| 2.5114 | 2950.8771 | 2976.3562 | 2959.9134 |
| 2.5224 | 2913.3874 | 2962.2397 | 2945.2187 |
| 2.5334 | 2914.4779 | 2948.1467 | 2930.5240 |
| 2.5444 | 2919.9095 | 2934.0778 | 2915.8294 |
| 2.5554 | 2890.4798 | 2920.0336 | 2901.1347 |
| 2.5664 | 2893.2832 | 2907.1484 | 2886.4401 |
| 2.5774 | 2894.2478 | 2896.6279 | 2876.3515 |
| 2.5884 | 2836.9317 | 2887.2675 | 2866.2629 |
| 2.5994 | 2820.6106 | 2877.9342 | 2856.1744 |
| 2.6104 | 2911.5010 | 2868.6283 | 2846.0858 |
| 2.6214 | 2890.0531 | 2859.3504 | 2835.9972 |
| 2.6324 | 2821.3658 | 2850.1010 | 2825.9087 |
| 2.6434 | 2758.3756 | 2840.8804 | 2815.8201 |
| 2.6544 | 2803.8152 | 2831.6890 | 2805.7316 |
| 2.6654 | 2868.5605 | 2822.5272 | 2795.6430 |
| 2.6764 | 2803.5260 | 2813.3951 | 2785.5544 |
| 2.6874 | 2783.0964 | 2804.2931 | 2775.4659 |
| 2.6984 | 2720.7301 | 2795.2213 | 2765.3773 |
| 2.7094 | 2700.4267 | 2786.1798 | 2755.2887 |
| 2.7204 | 2727.1632 | 2777.1686 | 2745.2002 |
| 2.7314 | 2710.4749 | 2768.1878 | 2735.1116 |
| 2.7424 | 2681.9420 | 2759.2372 | 2725.0231 |
| 2.7534 | 2716.2822 | 2751.1590 | 2714.9345 |
| 2.7644 | 2739.2655 | 2744.8485 | 2708.2683 |
| 2.7754 | 2731.6755 | 2739.4098 | 2701.6022 |
| 2.7864 | 2703.8201 | 2734.0002 | 2694.9360 |
| 2.7974 | 2655.7522 | 2728.6192 | 2688.2698 |
| 2.8084 | 2772.0256 | 2723.2663 | 2681.6037 |
| 2.8194 | 2721.4228 | 2717.9408 | 2674.9375 |
| 2.8304 | 2714.0782 | 2712.6418 | 2668.2713 |
| 2.8414 | 2765.3766 | 2707.3685 | 2661.6052 |
| 2.8524 | 2655.4307 | 2702.1199 | 2654.9390 |
| 2.8634 | 2715.1505 | 2696.8949 | 2648.2729 |
| 2.8744 | 2575.2640 | 2691.6922 | 2641.6067 |
| 2.8854 | 2665.3953 | 2686.5104 | 2634.9405 |
| 2.8964 | 2690.8938 | 2681.3480 | 2628.2744 |
| 2.9074 | 2659.3864 | 2676.2034 | 2621.6082 |
| 2.9184 | 2583.5118 | 2671.0747 | 2614.9420 |
| 2.9294 | 2654.3717 | 2665.9601 | 2608.2759 |
| 2.9404 | 2579.9371 | 2660.8278 | 2601.6097 |
| 2.9514 | 2660.4641 | 2655.7006 | 2594.8798 |
| 2.9624 | 2602.9705 | 2650.5509 | 2588.1498 |
| 2.9734 | 2627.5890 | 2645.4058 | 2581.4198 |
| 2.9844 | 2741.1912 | 2640.2625 | 2574.6899 |
| 2.9954 | 2582.1858 | 2635.1179 | 2567.9599 |
| 3.0064 | 2609.9479 | 2629.9689 | 2561.2300 |
| 3.0174 | 2605.6224 | 2624.8121 | 2554.5000 |
| 3.0284 | 2535.2935 | 2619.6439 | 2547.7701 |
| 3.0394 | 2563.5821 | 2614.4605 | 2541.0401 |
| 3.0504 | 2555.8973 | 2609.2581 | 2534.3102 |
| 3.0614 | 2598.1239 | 2604.0323 | 2527.5802 |
| 3.0724 | 2557.6485 | 2598.7790 | 2520.8503 |
| 3.0834 | 2587.7984 | 2593.4936 | 2514.1203 |
| 3.0944 | 2512.3540 | 2588.1715 | 2507.3904 |
| 3.1054 | 2623.6037 | 2582.8079 | 2500.6604 |
| 3.1164 | 2605.5845 | 2577.3979 | 2493.9305 |
| 3.1274 | 2540.8791 | 2571.9368 | 2487.2005 |
| 3.1384 | 2549.4454 | 2566.4194 | 2480.4706 |
| 3.1494 | 2517.6962 | 2560.8407 | 2473.7406 |
| 3.1604 | 2536.5929 | 2555.1960 | 2467.0107 |
| 3.1714 | 2485.4798 | 2549.4804 | 2460.2807 |
| 3.1824 | 2508.7817 | 2543.6891 | 2453.5508 |
| 3.1934 | 2500.3009 | 2537.8177 | 2446.8208 |
| 3.2044 | 2483.6657 | 2531.8619 | 2440.0908 |
| 3.2154 | 2508.4956 | 2525.8179 | 2433.3609 |
| 3.2264 | 2468.7773 | 2519.6820 | 2426.6309 |
| 3.2374 | 2439.7915 | 2513.4511 | 2419.9010 |
| 3.2484 | 2472.7222 | 2507.1224 | 2413.1710 |
| 3.2594 | 2483.7552 | 2500.6938 | 2406.4411 |
| 3.2704 | 2484.1544 | 2494.1636 | 2399.7111 |
| 3.2814 | 2485.0678 | 2487.5306 | 2392.9812 |
| 3.2924 | 2456.8938 | 2480.7944 | 2386.2512 |
| 3.3034 | 2471.9469 | 2473.9548 | 2379.5213 |
| 3.3144 | 2446.6440 | 2466.9830 | 2372.7913 |
| 3.3254 | 2392.1298 | 2459.9052 | 2365.9976 |
| 3.3364 | 2334.6136 | 2452.6980 | 2359.2038 |
| 3.3474 | 2380.4307 | 2445.3934 | 2352.4101 |
| 3.3584 | 2490.9204 | 2437.9942 | 2345.6164 |
| 3.3694 | 2466.1091 | 2430.5035 | 2338.8226 |
| 3.3804 | 2396.1268 | 2422.9250 | 2332.0289 |
| 3.3914 | 2380.0619 | 2415.2627 | 2325.2351 |
| 3.4024 | 2318.7817 | 2407.5208 | 2318.4414 |
| 3.4134 | 2332.4720 | 2399.7038 | 2311.6477 |
| 3.4244 | 2412.3038 | 2391.8165 | 2304.8539 |
| 3.4354 | 2390.7709 | 2383.8636 | 2298.0602 |
| 3.4464 | 2323.6126 | 2375.8502 | 2291.2664 |
| 3.4574 | 2343.3245 | 2367.7811 | 2284.4727 |
| 3.4684 | 2287.1224 | 2359.6614 | 2277.6790 |
| 3.4794 | 2275.5851 | 2351.4959 | 2270.8852 |
| 3.4904 | 2296.9779 | 2343.2896 | 2264.0915 |
| 3.5014 | 2310.7601 | 2335.0105 | 2257.2977 |
| 3.5124 | 2280.7547 | 2326.6943 | 2250.4252 |
| 3.5234 | 2257.0383 | 2318.3145 | 2243.5526 |
| 3.5344 | 2263.2099 | 2309.9118 | 2236.6800 |
| 3.5454 | 2223.7551 | 2301.4906 | 2229.8074 |
| 3.5564 | 2256.1136 | 2293.0547 | 2222.9348 |
| 3.5674 | 2279.2173 | 2284.6078 | 2216.0622 |
| 3.5784 | 2292.3643 | 2276.1535 | 2209.1896 |
| 3.5894 | 2296.7699 | 2267.6953 | 2202.3170 |
| 3.6004 | 2339.2390 | 2259.2361 | 2195.4445 |
| 3.6114 | 2180.9783 | 2250.7791 | 2188.5719 |
| 3.6224 | 2150.7153 | 2242.3269 | 2181.6993 |
| 3.6334 | 2209.6972 | 2233.8823 | 2174.8267 |
| 3.6444 | 2243.6155 | 2225.4476 | 2167.9541 |
| 3.6554 | 2191.4749 | 2217.0251 | 2161.0815 |
| 3.6664 | 2210.1023 | 2208.6168 | 2154.2089 |
| 3.6774 | 2150.7502 | 2200.2247 | 2147.3364 |
| 3.6884 | 2112.8230 | 2192.1584 | 2140.4638 |
| 3.6994 | 2110.7856 | 2184.1585 | 2134.2535 |
| 3.7104 | 2186.1244 | 2176.4874 | 2128.0431 |
| 3.7214 | 2183.9086 | 2168.8388 | 2121.8328 |
| 3.7324 | 2114.2025 | 2161.2139 | 2115.6225 |
| 3.7434 | 2152.3314 | 2153.6138 | 2109.4122 |
| 3.7544 | 2144.5029 | 2146.0395 | 2103.2019 |
| 3.7654 | 2183.6293 | 2138.4918 | 2096.9916 |
| 3.7764 | 2086.1352 | 2130.9717 | 2090.7813 |
| 3.7874 | 2168.2478 | 2123.4796 | 2084.5710 |
| 3.7984 | 2155.6971 | 2116.0163 | 2078.3607 |
| 3.8094 | 2067.8584 | 2108.5821 | 2072.1504 |
| 3.8204 | 2062.8673 | 2101.1775 | 2065.9400 |
| 3.8314 | 2190.8318 | 2093.8028 | 2059.7297 |
| 3.8424 | 2042.4744 | 2086.4582 | 2053.5194 |
| 3.8534 | 2020.1269 | 2079.1439 | 2047.3091 |
| 3.8644 | 2095.0806 | 2071.8599 | 2041.0988 |
| 3.8754 | 2100.4837 | 2064.5653 | 2034.8885 |
| 3.8864 | 2030.8186 | 2057.3136 | 2028.6088 |
| 3.8974 | 2080.2782 | 2050.0510 | 2022.3292 |
| 3.9084 | 2004.4548 | 2042.8185 | 2016.0495 |
| 3.9194 | 2055.4454 | 2035.6158 | 2009.7698 |
| 3.9304 | 2042.0383 | 2028.4425 | 2003.4901 |
| 3.9414 | 1998.2419 | 2021.2984 | 1997.2105 |
| 3.9524 | 2046.7832 | 2014.1831 | 1990.9308 |
| 3.9634 | 1989.9538 | 2007.0962 | 1984.6511 |
| 3.9744 | 2018.3928 | 2000.0373 | 1978.3715 |
| 3.9854 | 1983.5753 | 1993.0057 | 1972.0918 |
| 3.9964 | 2070.1013 | 1986.0012 | 1965.8121 |
| 4.0074 | 2039.7482 | 1979.0230 | 1959.5325 |
| 4.0184 | 1966.7065 | 1972.0707 | 1953.2528 |
| 4.0294 | 1973.8593 | 1965.1436 | 1946.9731 |
| 4.0404 | 1898.5753 | 1958.2411 | 1940.6935 |
| 4.0514 | 1958.4012 | 1951.3627 | 1934.4138 |
| 4.0624 | 1913.1937 | 1944.5077 | 1928.1341 |
| 4.0734 | 1932.1573 | 1937.6754 | 1921.8544 |
| 4.0844 | 1949.2655 | 1930.8651 | 1915.5748 |
| 4.0954 | 1922.0708 | 1924.0763 | 1909.2951 |
| 4.1064 | 1934.1819 | 1917.3083 | 1903.0154 |
| 4.1174 | 1890.7669 | 1910.5603 | 1896.7358 |
| 4.1284 | 1860.4435 | 1903.8318 | 1890.4561 |
| 4.1394 | 1859.9282 | 1897.1220 | 1884.1764 |
| 4.1504 | 1849.3156 | 1890.4303 | 1877.8968 |
| 4.1614 | 1897.3147 | 1883.7561 | 1871.6171 |
| 4.1724 | 1919.9838 | 1877.0987 | 1865.3374 |
| 4.1834 | 1845.3716 | 1870.4574 | 1859.0577 |
| 4.1944 | 1797.6888 | 1863.8316 | 1852.7781 |

Scan List

| Vis. | Dataset Name | Start pos. [°2θ] | End pos. [°2θ] | Step [°2θ] | Meas.Date/Time |
| --- | --- | --- | --- | --- | --- |
| * | 1 Etosha18 rip 0-2cm 400C | 2.0054 | 29.9894 | 0.0110 | 12/5/2023 11:49:40 AM |

Peak List

| Pos. [°2θ] | Height [cts] | FWHM Left [°2θ] | d-spacing [Å] | Rel. Int. [%] |
| --- | --- | --- | --- | --- |
| 3.2835 | 84.35 | 0.8659 | 26.88619 | 7.55 |
| 7.1701 | 1116.64 | 0.2165 | 12.31891 | 100.00 |
| 8.8721 | 796.99 | 0.1948 | 9.95903 | 71.37 |
| 10.6837 | 47.44 | 0.3464 | 8.27405 | 4.25 |
| 15.8993 | 914.61 | 0.0758 | 5.56966 | 81.91 |
| 17.7639 | 73.77 | 0.1732 | 4.98902 | 6.61 |
| 18.3928 | 98.91 | 0.1515 | 4.81982 | 8.86 |
| 19.7097 | 73.18 | 0.3031 | 4.50066 | 6.55 |
| 24.3483 | 46.84 | 0.1732 | 3.65272 | 4.19 |
| 26.0967 | 610.29 | 0.0974 | 3.41182 | 54.65 |
| 26.8576 | 199.02 | 0.1299 | 3.31687 | 17.82 |
| 27.6633 | 81.90 | 0.1948 | 3.22207 | 7.33 |
| 28.0206 | 133.34 | 0.0325 | 3.18179 | 11.94 |

Pattern List

| Visible | Ref.Code | Score | Compound Name | Chem. Formula | Mineral Name | SemiQuant[%] |
| --- | --- | --- | --- | --- | --- | --- |
| * | 01-076-6569 | 64 | Sodium Aluminum Silicate Hydrate | Na0.9 ( ( Al0.9 Si2 ) O6 ) ( H2 O ) | Analcime | 39 |
| * | 01-080-5781 | 21 | Magnesium Silicon Oxide Hydroxide Hydrate | Mg8 ( Si12 O30 ( O H )4 ( H2 O )3.92 ) ( H2 O )7.72 | Sepiolite | 7 |
| * | 04-018-3208 | 18 | Magnesium Aluminum Iron Silicon Oxide Hydroxide Hydrate | Mg1.0 Fe0.08 Al1.0 Si3.99 O10.2 ( O H )0.8 ( H2 O )3.3 | Palygorskite-M | 6 |
| * | 01-089-6879 | 22 | Potassium Lithium Iron Aluminum Silicate Hydroxide | K0.9 ( Li0.20 Fe0.92 Al1.2 ) ( Al0.82 Si3.18 O10 ) ( O H )2 | Muscovite-1M, Fe+3-bearing | 24 |
| * | 01-082-8023 | 21 | Sodium Magnesium Silicon Oxide Hydrate | Na2 Mg3 ( Si6 O16 ) ( H2 O )7 | Loughlinite | 5 |
| * | 01-082-8022 | 14 | Magnesium Silicon Oxide Hydroxide | Mg2 Mg5 ( Si8 O22 ( O H )2 ) | Anthophyllite | 7 |
| * | 04-025-4215 | 2 | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide | Mg10.4 V0.36 Mn33.5 Fe0.14 Al0.69 Si6.77 As6.5 P0.3 O54 ( O H )42 | Carlfrancisite | 11 |

Anchor Scan Parameters

Dataset Name	1 Etosha18 rip 0-2cm 400C

File name	C:\aeris_data\XRD data\Goldstein\Etosha 2023\Etosha Clay Data\Sample 1\1 Etosha18 rip 0-2cm 400C.xrdml

Sample Identification	1 Etosha18 rip 0-2cm 400C

Measurement Start Date/Time	12/5/2023 11:49:40 AM

Operator	Instrument

Raw Data Origin	XRD measurement (*.XRDML)

Scan Axis	Gonio

Start Position [°2θ]	2.0054

End Position [°2θ]	29.9894

Step Size [°2θ]	0.0110

Scan Step Time [s]	48.1950

Scan Type	Continuous

PSD Mode	Scanning

PSD Length [°2θ]	5.54

Offset [°2θ]	0.0000

Divergence Slit Type	Fixed

Divergence Slit Size [°]	0.0603

Specimen Length [mm]	10.00

Measurement Temperature [°C]	25.00

Anode Material	Cu

K-α1 [Å]	1.54060

K-α2 [Å]	1.54443

K-β1 [Å]	1.39225

K-A2 / K-A1 Ratio	0.50000

Generator Settings	15 mA, 40 kV

Diffractometer Type	2082464

Diffractometer Number	0

Goniometer Radius [mm]	145.00

Dist. Focus-Diverg. Slit [mm]	95.00

Incident Beam Monochromator	No

Spinning	Yes