1 Etosha 18 RIP 0-2cm 550C report

Graphics

Graphics

Graphics

Quantitative Results

Phase Potassium Magnesium Manganese Aluminum Iron Silicon Oxide Hydroxide

Weight fraction/ %	51.0

Phase Sodium Aluminum Silicate Hydrate

Weight fraction/ %	13.0

Phase Magnesium Aluminum Iron Silicon Oxide Hydroxide Hydrate

Weight fraction/ %	7.0

Phase Magnesium Silicon Oxide Hydroxide

Weight fraction/ %	12.0

Phase Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide

Weight fraction/ %	16.0

Multiple Quantitative Results

Scans vs Phases Matrix

| Scan name | Potassium Magnesium Manganese Aluminum Iron Silicon Oxide Hydroxide | Sodium Aluminum Silicate Hydrate | Magnesium Aluminum Iron Silicon Oxide Hydroxide Hydrate | Magnesium Silicon Oxide Hydroxide | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide |
| --- | --- | --- | --- | --- | --- |
| 1 Etosha18 RIP 0-2cm 550C | 51.0 | 13.0 | 7.0 | 12.0 | 16.0 |

Anchor Scan Data

| Pos. [°2θ] | Iobs [cts] | Icalc [cts] | Iback [cts] |
| --- | --- | --- | --- |
| 2.0054 | 8805.0000 | 8811.7863 | 8805.0000 |
| 2.0164 | 8736.1932 | 8756.1611 | 8742.0862 |
| 2.0274 | 8593.3353 | 8693.7363 | 8679.1724 |
| 2.0384 | 8679.2153 | 8631.3374 | 8616.2586 |
| 2.0494 | 8494.1337 | 8568.9660 | 8553.3448 |
| 2.0604 | 8355.6431 | 8506.6242 | 8490.4310 |
| 2.0714 | 8560.9764 | 8444.3141 | 8427.5172 |
| 2.0824 | 8508.3736 | 8382.0382 | 8364.6034 |
| 2.0934 | 8353.9833 | 8319.7991 | 8301.6896 |
| 2.1044 | 8337.4469 | 8257.5995 | 8238.7758 |
| 2.1154 | 8149.8220 | 8195.4427 | 8175.8620 |
| 2.1264 | 8265.7783 | 8133.3320 | 8112.9482 |
| 2.1374 | 8193.4100 | 8071.2714 | 8050.0344 |
| 2.1484 | 8202.3033 | 8009.2648 | 7987.1206 |
| 2.1594 | 8224.1534 | 7947.3171 | 7924.2069 |
| 2.1704 | 8006.9381 | 7885.4333 | 7861.2931 |
| 2.1814 | 7969.9961 | 7823.6191 | 7798.3793 |
| 2.1924 | 8038.0143 | 7761.8641 | 7735.4655 |
| 2.2034 | 8047.3894 | 7700.0712 | 7672.3971 |
| 2.2144 | 7831.6706 | 7638.3524 | 7609.3288 |
| 2.2254 | 7881.4150 | 7576.7334 | 7546.2605 |
| 2.2364 | 7897.1770 | 7515.2242 | 7483.1922 |
| 2.2474 | 7695.7847 | 7453.8359 | 7420.1238 |
| 2.2584 | 7841.6499 | 7392.5812 | 7357.0555 |
| 2.2694 | 7781.1121 | 7331.4746 | 7293.9872 |
| 2.2804 | 7677.9272 | 7270.5325 | 7230.9188 |
| 2.2914 | 7671.0000 | 7209.7739 | 7167.8505 |
| 2.3024 | 7571.1106 | 7149.2209 | 7104.7822 |
| 2.3134 | 7453.2842 | 7088.8997 | 7041.7139 |
| 2.3244 | 7585.9798 | 7028.8415 | 6978.6455 |
| 2.3354 | 7541.9499 | 6969.0850 | 6915.5772 |
| 2.3464 | 7465.4611 | 6909.6787 | 6852.5089 |
| 2.3574 | 7348.7325 | 6850.6849 | 6789.4405 |
| 2.3684 | 7363.6711 | 6792.1860 | 6726.3722 |
| 2.3794 | 7324.9262 | 6734.2922 | 6663.3039 |
| 2.3904 | 7314.0905 | 6677.1526 | 6600.2356 |
| 2.4014 | 7276.0885 | 6620.9697 | 6537.1672 |
| 2.4124 | 7268.9489 | 6566.0174 | 6474.0989 |
| 2.4234 | 7258.1091 | 6512.6618 | 6411.0306 |
| 2.4344 | 7163.2817 | 6461.3849 | 6347.9623 |
| 2.4454 | 7158.6018 | 6412.8064 | 6284.8939 |
| 2.4564 | 7059.5123 | 6367.7035 | 6221.8256 |
| 2.4674 | 7047.5575 | 6327.0199 | 6158.7573 |
| 2.4784 | 7120.4258 | 6291.8615 | 6095.6889 |
| 2.4894 | 7050.4405 | 6263.4708 | 6032.6206 |
| 2.5004 | 7061.7080 | 6243.1745 | 5969.5523 |
| 2.5114 | 7001.0029 | 6232.3031 | 5906.4840 |
| 2.5224 | 6886.4464 | 6232.0790 | 5843.4156 |
| 2.5334 | 6829.6224 | 6243.4795 | 5780.3473 |
| 2.5444 | 6832.7380 | 6267.0775 | 5717.2790 |
| 2.5554 | 6737.7768 | 6302.8667 | 5654.2106 |
| 2.5664 | 6741.9823 | 6350.0539 | 5591.1423 |
| 2.5774 | 6679.7079 | 6406.7731 | 5527.9195 |
| 2.5884 | 6676.6283 | 6470.1287 | 5464.6966 |
| 2.5994 | 6671.4956 | 6535.6061 | 5401.4737 |
| 2.6104 | 6669.2242 | 6596.8691 | 5338.2509 |
| 2.6214 | 6556.5477 | 6645.7166 | 5275.0280 |
| 2.6324 | 6446.6534 | 6672.5889 | 5211.8052 |
| 2.6434 | 6460.7827 | 6667.9919 | 5148.5823 |
| 2.6544 | 6326.6145 | 6624.7534 | 5085.3594 |
| 2.6654 | 6251.5634 | 6540.2456 | 5022.1366 |
| 2.6764 | 6197.7655 | 6417.2972 | 4958.9137 |
| 2.6874 | 6085.9823 | 6263.1963 | 4895.6909 |
| 2.6984 | 6007.2168 | 6087.4504 | 4832.4680 |
| 2.7094 | 5872.6460 | 5899.5671 | 4769.2451 |
| 2.7204 | 5637.0747 | 5707.6776 | 4706.0223 |
| 2.7314 | 5572.2094 | 5518.0552 | 4642.7994 |
| 2.7424 | 5452.0629 | 5335.1822 | 4579.5766 |
| 2.7534 | 5386.0462 | 5161.9996 | 4516.3537 |
| 2.7644 | 5108.3097 | 5000.1103 | 4452.9398 |
| 2.7754 | 5042.7925 | 4850.3959 | 4389.5260 |
| 2.7864 | 4949.2429 | 4712.8651 | 4326.1121 |
| 2.7974 | 4837.7699 | 4586.9314 | 4262.6982 |
| 2.8084 | 4625.8112 | 4471.6093 | 4199.2844 |
| 2.8194 | 4488.3982 | 4365.6718 | 4135.8705 |
| 2.8304 | 4341.4911 | 4267.7882 | 4072.4566 |
| 2.8414 | 4206.6961 | 4176.6339 | 4009.0427 |
| 2.8524 | 4182.8574 | 4090.9705 | 3945.6289 |
| 2.8634 | 4048.7404 | 4009.6971 | 3882.2150 |
| 2.8744 | 3978.9144 | 3931.8752 | 3818.8011 |
| 2.8854 | 3829.5074 | 3856.7325 | 3755.3873 |
| 2.8964 | 3965.3850 | 3783.6536 | 3691.9734 |
| 2.9074 | 3645.8348 | 3712.1603 | 3628.5595 |
| 2.9184 | 3622.2586 | 3641.8892 | 3565.1457 |
| 2.9294 | 3485.8200 | 3572.5688 | 3501.7318 |
| 2.9404 | 3392.5211 | 3506.7677 | 3438.3179 |
| 2.9514 | 3423.1180 | 3461.5642 | 3400.4389 |
| 2.9624 | 3383.4734 | 3419.6227 | 3362.5599 |
| 2.9734 | 3269.3265 | 3378.0920 | 3324.6809 |
| 2.9844 | 3263.7974 | 3336.9100 | 3286.8019 |
| 2.9954 | 3180.0974 | 3296.0285 | 3248.9229 |
| 3.0064 | 3208.9002 | 3255.4092 | 3211.0439 |
| 3.0174 | 3094.1917 | 3215.0209 | 3173.1649 |
| 3.0284 | 3014.1209 | 3174.8375 | 3135.2858 |
| 3.0394 | 2947.0610 | 3134.8371 | 3097.4068 |
| 3.0504 | 3053.4203 | 3095.0007 | 3059.5278 |
| 3.0614 | 2986.3599 | 3055.3120 | 3021.6488 |
| 3.0724 | 2996.0738 | 3015.7565 | 2983.7698 |
| 3.0834 | 2999.5260 | 2976.3216 | 2945.8908 |
| 3.0944 | 2884.4690 | 2936.9962 | 2908.0118 |
| 3.1054 | 2887.8358 | 2897.7703 | 2870.1328 |
| 3.1164 | 2833.5845 | 2858.6351 | 2832.2538 |
| 3.1274 | 2759.2389 | 2821.8541 | 2794.3748 |
| 3.1384 | 2774.2886 | 2801.5487 | 2777.4383 |
| 3.1494 | 2773.8594 | 2783.5841 | 2760.5019 |
| 3.1604 | 2629.8230 | 2765.6833 | 2743.5655 |
| 3.1714 | 2603.5939 | 2747.8412 | 2726.6290 |
| 3.1824 | 2658.8786 | 2730.0531 | 2709.6926 |
| 3.1934 | 2696.3009 | 2712.3149 | 2692.7562 |
| 3.2044 | 2712.1809 | 2694.6227 | 2675.8197 |
| 3.2154 | 2667.9843 | 2676.9732 | 2658.8833 |
| 3.2264 | 2640.3835 | 2659.3632 | 2641.9469 |
| 3.2374 | 2592.9597 | 2641.7899 | 2625.0104 |
| 3.2484 | 2620.5556 | 2624.2506 | 2608.0740 |
| 3.2594 | 2612.4012 | 2606.7430 | 2591.1376 |
| 3.2704 | 2547.6716 | 2589.2650 | 2574.2011 |
| 3.2814 | 2469.9017 | 2571.8145 | 2557.2647 |
| 3.2924 | 2517.1593 | 2554.3897 | 2540.3282 |
| 3.3034 | 2538.9400 | 2536.9890 | 2523.3918 |
| 3.3144 | 2504.0319 | 2519.7289 | 2506.4554 |
| 3.3254 | 2486.7493 | 2503.3432 | 2490.6086 |
| 3.3364 | 2498.3338 | 2487.0955 | 2474.7619 |
| 3.3474 | 2482.5221 | 2470.8663 | 2458.9151 |
| 3.3584 | 2503.5030 | 2454.6545 | 2443.0684 |
| 3.3694 | 2450.6637 | 2438.4592 | 2427.2216 |
| 3.3804 | 2361.2453 | 2422.2793 | 2411.3748 |
| 3.3914 | 2376.6549 | 2406.1139 | 2395.5281 |
| 3.4024 | 2420.0482 | 2389.9622 | 2379.6813 |
| 3.4134 | 2417.9233 | 2373.8234 | 2363.8346 |
| 3.4244 | 2402.3422 | 2357.6969 | 2347.9878 |
| 3.4354 | 2343.6185 | 2341.5819 | 2332.1411 |
| 3.4464 | 2268.8328 | 2325.4778 | 2316.2943 |
| 3.4574 | 2306.1298 | 2309.3840 | 2300.4475 |
| 3.4684 | 2361.6760 | 2293.3001 | 2284.6008 |
| 3.4794 | 2278.5378 | 2277.2254 | 2268.7540 |
| 3.4904 | 2258.6460 | 2261.1596 | 2252.9073 |
| 3.5014 | 2227.9892 | 2245.7977 | 2237.0605 |
| 3.5124 | 2217.9936 | 2235.4661 | 2227.6273 |
| 3.5234 | 2217.0383 | 2225.8376 | 2218.1940 |
| 3.5344 | 2182.8279 | 2216.2163 | 2208.7608 |
| 3.5454 | 2224.0561 | 2206.6018 | 2199.3275 |
| 3.5564 | 2239.8687 | 2196.9939 | 2189.8943 |
| 3.5674 | 2166.4484 | 2187.3921 | 2180.4611 |
| 3.5784 | 2173.0624 | 2177.7963 | 2171.0278 |
| 3.5894 | 2116.7876 | 2168.2091 | 2161.5946 |
| 3.6004 | 2189.2999 | 2158.7171 | 2152.1613 |
| 3.6114 | 2122.8387 | 2149.1402 | 2142.7281 |
| 3.6224 | 2111.9086 | 2139.6136 | 2133.2948 |
| 3.6334 | 2169.8781 | 2130.0454 | 2123.8616 |
| 3.6444 | 2140.4316 | 2120.4818 | 2114.4284 |
| 3.6554 | 2105.8466 | 2110.9224 | 2104.9951 |
| 3.6664 | 2147.2213 | 2101.3673 | 2095.5619 |
| 3.6774 | 2082.9361 | 2091.8161 | 2086.1286 |
| 3.6884 | 2080.8053 | 2082.2493 | 2076.6954 |
| 3.6994 | 2073.0718 | 2072.5459 | 2067.0830 |
| 3.7104 | 2106.3943 | 2062.8266 | 2057.4707 |
| 3.7214 | 2066.8820 | 2053.1106 | 2047.8583 |
| 3.7324 | 2043.4764 | 2043.3979 | 2038.2460 |
| 3.7434 | 2042.0000 | 2033.6883 | 2028.6336 |
| 3.7544 | 2076.3540 | 2023.9817 | 2019.0213 |
| 3.7654 | 2056.7355 | 2014.2780 | 2009.4089 |
| 3.7764 | 2093.1967 | 2004.5771 | 1999.7965 |
| 3.7874 | 2042.4602 | 1994.8788 | 1990.1842 |
| 3.7984 | 1979.6765 | 1985.1831 | 1980.5718 |
| 3.8094 | 1888.1554 | 1975.4899 | 1970.9595 |
| 3.8204 | 2021.7109 | 1965.7991 | 1961.3471 |
| 3.8314 | 1978.2094 | 1956.1106 | 1951.7348 |
| 3.8424 | 2005.3166 | 1946.4243 | 1942.1224 |
| 3.8534 | 1966.3687 | 1936.7401 | 1932.5100 |
| 3.8644 | 1851.2626 | 1927.0581 | 1922.8977 |
| 3.8754 | 1959.5841 | 1917.3780 | 1913.2853 |
| 3.8864 | 1927.9779 | 1907.6999 | 1903.6730 |
| 3.8974 | 1866.4562 | 1898.0237 | 1894.0606 |
| 3.9084 | 1876.0649 | 1888.3492 | 1884.4483 |
| 3.9194 | 1901.7787 | 1878.6766 | 1874.8359 |
| 3.9304 | 1811.4145 | 1869.0056 | 1865.2236 |
| 3.9414 | 1869.3471 | 1859.3363 | 1855.6112 |
| 3.9524 | 1870.2124 | 1849.6686 | 1845.9988 |
| 3.9634 | 1892.4415 | 1840.0025 | 1836.3865 |
| 3.9744 | 1883.7905 | 1830.3378 | 1826.7741 |
| 3.9854 | 1787.4601 | 1820.6747 | 1817.1618 |
| 3.9964 | 1726.4587 | 1811.0129 | 1807.5494 |
| 4.0074 | 1783.7729 | 1801.3525 | 1797.9371 |
| 4.0184 | 1821.8068 | 1791.6935 | 1788.3247 |
| 4.0294 | 1757.1996 | 1782.0358 | 1778.7124 |
| 4.0404 | 1735.5354 | 1772.3793 | 1769.1000 |
| 4.0514 | 1729.2861 | 1762.7241 | 1759.4876 |
| 4.0624 | 1756.8584 | 1753.4762 | 1749.8753 |
| 4.0734 | 1784.5781 | 1747.1611 | 1744.0067 |
| 4.0844 | 1732.1637 | 1741.2532 | 1738.1381 |
| 4.0954 | 1781.6352 | 1735.3465 | 1732.2696 |
| 4.1064 | 1759.1819 | 1729.4408 | 1726.4010 |
| 4.1174 | 1754.6342 | 1723.5363 | 1720.5324 |
| 4.1284 | 1756.2261 | 1717.6328 | 1714.6638 |
| 4.1394 | 1718.3029 | 1711.7303 | 1708.7953 |
| 4.1504 | 1728.4779 | 1705.8288 | 1702.9267 |
| 4.1614 | 1708.6824 | 1699.9283 | 1697.0581 |
| 4.1724 | 1712.3761 | 1694.0288 | 1691.1895 |
| 4.1834 | 1695.4778 | 1688.1302 | 1685.3210 |
| 4.1944 | 1685.5521 | 1682.2326 | 1679.4524 |

Scan List

| Vis. | Dataset Name | Start pos. [°2θ] | End pos. [°2θ] | Step [°2θ] | Meas.Date/Time |
| --- | --- | --- | --- | --- | --- |
| * | 1 Etosha18 RIP 0-2cm 550C | 2.0054 | 29.9894 | 0.0110 | 12/7/2023 11:04:49 AM |

Peak List

| Pos. [°2θ] | Height [cts] | FWHM Left [°2θ] | d-spacing [Å] | Rel. Int. [%] |
| --- | --- | --- | --- | --- |
| 2.6521 | 1375.92 | 0.1732 | 33.28618 | 100.00 |
| 5.3315 | 101.94 | 0.1732 | 16.56236 | 7.41 |
| 8.7234 | 980.14 | 0.1732 | 10.12857 | 71.24 |
| 10.6748 | 87.55 | 0.3031 | 8.28097 | 6.36 |
| 15.9715 | 563.84 | 0.2165 | 5.54464 | 40.98 |
| 17.6174 | 61.55 | 0.2165 | 5.03016 | 4.47 |
| 18.4424 | 26.37 | 0.2598 | 4.80695 | 1.92 |
| 19.5911 | 45.10 | 0.2598 | 4.52763 | 3.28 |
| 20.1535 | 47.02 | 0.2598 | 4.40254 | 3.42 |
| 24.5919 | 26.59 | 0.5196 | 3.61709 | 1.93 |
| 26.2503 | 310.86 | 0.1732 | 3.39221 | 22.59 |
| 27.5016 | 88.22 | 0.2598 | 3.24064 | 6.41 |

Pattern List

| Visible | Ref.Code | Score | Compound Name | Chem. Formula | Mineral Name | SemiQuant[%] |
| --- | --- | --- | --- | --- | --- | --- |
| * | 04-016-6884 | 31 | Potassium Magnesium Manganese Aluminum Iron Silicon Oxide Hydroxide | K0.8 Mg2.6 Mn0.1 Fe0.2 Al1.3 Si2.8 O10 ( O H )2 | Muscovite-1M | 51 |
| * | 04-011-6233 | 25 | Sodium Aluminum Silicate Hydrate | Na8 Al8 Si16 O48 ( H2 O )8 | Analcime | 13 |
| * | 04-018-3208 | 14 | Magnesium Aluminum Iron Silicon Oxide Hydroxide Hydrate | Mg1.0 Fe0.08 Al1.0 Si3.99 O10.2 ( O H )0.8 ( H2 O )3.3 | Palygorskite-M | 7 |
| * | 01-082-8022 | Unmatched Strong | Magnesium Silicon Oxide Hydroxide | Mg2 Mg5 ( Si8 O22 ( O H )2 ) | Anthophyllite | 12 |
| * | 04-025-4215 | 15 | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide | Mg10.4 V0.36 Mn33.5 Fe0.14 Al0.69 Si6.77 As6.5 P0.3 O54 ( O H )42 | Carlfrancisite | 16 |

Anchor Scan Parameters

Dataset Name	1 Etosha18 RIP 0-2cm 550C

File name	C:\aeris_data\XRD data\Goldstein\Etosha 2023\Etosha Clay Data\Sample 1\1 Etosha18 RIP 0-2cm 550C.xrdml

Sample Identification	1 Etosha18 RIP 0-2cm 550C

Measurement Start Date/Time	12/7/2023 11:04:49 AM

Operator	Instrument

Raw Data Origin	XRD measurement (*.XRDML)

Scan Axis	Gonio

Start Position [°2θ]	2.0054

End Position [°2θ]	29.9894

Step Size [°2θ]	0.0110

Scan Step Time [s]	48.1950

Scan Type	Continuous

PSD Mode	Scanning

PSD Length [°2θ]	5.54

Offset [°2θ]	0.0000

Divergence Slit Type	Fixed

Divergence Slit Size [°]	0.0603

Specimen Length [mm]	10.00

Measurement Temperature [°C]	25.00

Anode Material	Cu

K-α1 [Å]	1.54060

K-α2 [Å]	1.54443

K-β1 [Å]	1.39225

K-A2 / K-A1 Ratio	0.50000

Generator Settings	15 mA, 40 kV

Diffractometer Type	2082464

Diffractometer Number	0

Goniometer Radius [mm]	145.00

Dist. Focus-Diverg. Slit [mm]	95.00

Incident Beam Monochromator	No

Spinning	Yes