1 Etosha 18 RIP 0-2cm Glycolated report

Graphics

Graphics

Graphics

Quantitative Results

Phase Sodium Magnesium Silicon Oxide Hydrate

Weight fraction/ %	18.0

Phase Sodium Aluminum Silicate Hydrate

Weight fraction/ %	36.0

Phase Potassium Sodium Magnesium Aluminum Iron Silicon Titanium Oxide Fluoride Hydroxide

Weight fraction/ %	34.0

Phase Magnesium Aluminum Iron Silicon Oxide Hydroxide Hydrate

Weight fraction/ %	6.0

Phase Magnesium Silicon Oxide Hydroxide Hydrate

Weight fraction/ %	7.0

Multiple Quantitative Results

Scans vs Phases Matrix

| Scan name | Sodium Magnesium Silicon Oxide Hydrate | Sodium Aluminum Silicate Hydrate | Potassium Sodium Magnesium Aluminum Iron Silicon Titanium Oxide Fluoride Hydroxide | Magnesium Aluminum Iron Silicon Oxide Hydroxide Hydrate | Magnesium Silicon Oxide Hydroxide Hydrate |
| --- | --- | --- | --- | --- | --- |
| 1 Etosha18 RIP 0-2cm GLYCOLATED | 18.0 | 36.0 | 34.0 | 6.0 | 7.0 |

Anchor Scan Data

| Pos. [°2θ] | Iobs [cts] | Icalc [cts] | Iback [cts] |
| --- | --- | --- | --- |
| 2.0054 | 4663.0000 | 4663.1581 | 4663.0000 |
| 2.0164 | 4678.0905 | 4635.3471 | 4632.0375 |
| 2.0274 | 4605.0737 | 4604.4093 | 4601.0750 |
| 2.0384 | 4600.4410 | 4573.4718 | 4570.1126 |
| 2.0494 | 4409.4897 | 4542.5346 | 4539.1501 |
| 2.0604 | 4533.3407 | 4511.5976 | 4508.1876 |
| 2.0714 | 4502.3215 | 4480.6610 | 4477.2251 |
| 2.0824 | 4429.1932 | 4449.7246 | 4446.2626 |
| 2.0934 | 4416.6863 | 4418.7885 | 4415.3002 |
| 2.1044 | 4453.7743 | 4387.8527 | 4384.3377 |
| 2.1154 | 4249.2901 | 4356.9173 | 4353.3752 |
| 2.1264 | 4191.3569 | 4325.9821 | 4322.4127 |
| 2.1374 | 4248.8083 | 4295.0473 | 4291.4502 |
| 2.1484 | 4157.3250 | 4264.1127 | 4260.4878 |
| 2.1594 | 4132.4936 | 4233.1785 | 4229.5253 |
| 2.1704 | 4113.0059 | 4202.2447 | 4198.5628 |
| 2.1814 | 4147.3432 | 4171.3111 | 4167.6003 |
| 2.1924 | 4153.2689 | 4141.1321 | 4136.6378 |
| 2.2034 | 4123.1150 | 4116.9125 | 4113.1427 |
| 2.2144 | 4112.9941 | 4093.4474 | 4089.6476 |
| 2.2254 | 4083.3628 | 4069.9826 | 4066.1525 |
| 2.2364 | 4058.0959 | 4046.5182 | 4042.6574 |
| 2.2474 | 4021.0157 | 4023.0542 | 4019.1624 |
| 2.2584 | 3953.9115 | 3999.5906 | 3995.6673 |
| 2.2694 | 3954.8643 | 3976.1273 | 3972.1722 |
| 2.2804 | 3959.1160 | 3952.6644 | 3948.6771 |
| 2.2914 | 3886.0108 | 3929.2019 | 3925.1820 |
| 2.3024 | 3878.2920 | 3905.7399 | 3901.6869 |
| 2.3134 | 3864.9941 | 3882.2782 | 3878.1918 |
| 2.3244 | 3824.3171 | 3858.8169 | 3854.6967 |
| 2.3354 | 3866.5310 | 3835.3561 | 3831.2016 |
| 2.3464 | 3830.6583 | 3811.8956 | 3807.7065 |
| 2.3574 | 3747.1672 | 3788.4356 | 3784.2114 |
| 2.3684 | 3742.9513 | 3764.9761 | 3760.7163 |
| 2.3794 | 3747.7168 | 3741.7031 | 3737.2212 |
| 2.3904 | 3728.5585 | 3719.9009 | 3715.5686 |
| 2.4014 | 3710.2832 | 3698.2852 | 3693.9160 |
| 2.4124 | 3661.1662 | 3676.6700 | 3672.2635 |
| 2.4234 | 3637.9459 | 3655.0553 | 3650.6109 |
| 2.4344 | 3654.5206 | 3633.4411 | 3628.9583 |
| 2.4454 | 3589.5949 | 3611.8274 | 3607.3058 |
| 2.4564 | 3575.9130 | 3590.2142 | 3585.6532 |
| 2.4674 | 3603.2212 | 3568.6015 | 3564.0006 |
| 2.4784 | 3546.1750 | 3546.9893 | 3542.3481 |
| 2.4894 | 3556.5605 | 3525.3777 | 3520.6955 |
| 2.5004 | 3568.8761 | 3503.7666 | 3499.0429 |
| 2.5114 | 3526.1229 | 3482.1560 | 3477.3904 |
| 2.5224 | 3539.3501 | 3460.5460 | 3455.7378 |
| 2.5334 | 3489.8436 | 3438.9366 | 3434.0852 |
| 2.5444 | 3408.8869 | 3417.3277 | 3412.4327 |
| 2.5554 | 3330.0029 | 3395.7194 | 3390.7801 |
| 2.5664 | 3418.9956 | 3374.8306 | 3369.1275 |
| 2.5774 | 3373.2035 | 3359.6219 | 3354.5921 |
| 2.5884 | 3303.0457 | 3345.1326 | 3340.0567 |
| 2.5994 | 3264.8319 | 3330.6439 | 3325.5213 |
| 2.6104 | 3244.6480 | 3316.1559 | 3310.9859 |
| 2.6214 | 3299.7522 | 3301.6686 | 3296.4504 |
| 2.6324 | 3377.5443 | 3287.1819 | 3281.9150 |
| 2.6434 | 3330.8505 | 3272.6959 | 3267.3796 |
| 2.6544 | 3264.5659 | 3258.2106 | 3252.8442 |
| 2.6654 | 3238.2006 | 3243.7260 | 3238.3088 |
| 2.6764 | 3210.7576 | 3229.2421 | 3223.7734 |
| 2.6874 | 3167.9459 | 3214.7590 | 3209.2379 |
| 2.6984 | 3119.0575 | 3200.2766 | 3194.7025 |
| 2.7094 | 3123.7325 | 3185.7949 | 3180.1671 |
| 2.7204 | 3086.4562 | 3171.3141 | 3165.6317 |
| 2.7314 | 3219.5841 | 3156.8340 | 3151.0963 |
| 2.7424 | 3117.1224 | 3142.3547 | 3136.5609 |
| 2.7534 | 3128.1180 | 3127.8763 | 3122.0254 |
| 2.7644 | 3197.9100 | 3113.3987 | 3107.4900 |
| 2.7754 | 3141.0305 | 3098.9219 | 3092.9546 |
| 2.7864 | 3061.9321 | 3084.4460 | 3078.4192 |
| 2.7974 | 3055.5398 | 3069.9710 | 3063.8838 |
| 2.8084 | 3024.5964 | 3055.4970 | 3049.3484 |
| 2.8194 | 3064.6578 | 3041.0238 | 3034.8129 |
| 2.8304 | 2971.2861 | 3026.5516 | 3020.2775 |
| 2.8414 | 3033.0590 | 3012.0803 | 3005.7421 |
| 2.8524 | 3041.7856 | 2997.6100 | 2991.2067 |
| 2.8634 | 2928.8731 | 2983.1407 | 2976.6713 |
| 2.8744 | 2928.8550 | 2968.6725 | 2962.1359 |
| 2.8854 | 2905.4012 | 2954.2052 | 2947.6005 |
| 2.8964 | 3007.5443 | 2939.7391 | 2933.0650 |
| 2.9074 | 2935.8594 | 2925.2740 | 2918.5296 |
| 2.9184 | 2795.0841 | 2910.8100 | 2903.9942 |
| 2.9294 | 2944.0590 | 2896.3472 | 2889.4588 |
| 2.9404 | 2912.2866 | 2881.8769 | 2874.9234 |
| 2.9514 | 2832.2586 | 2867.3401 | 2860.3031 |
| 2.9624 | 2824.0900 | 2852.7959 | 2845.6828 |
| 2.9734 | 2875.0010 | 2838.2529 | 2831.0624 |
| 2.9844 | 2819.2950 | 2823.7112 | 2816.4421 |
| 2.9954 | 2730.6549 | 2809.1708 | 2801.8218 |
| 3.0064 | 2852.1042 | 2794.6316 | 2787.2015 |
| 3.0174 | 2823.6145 | 2780.0939 | 2772.5812 |
| 3.0284 | 2722.8496 | 2765.5574 | 2757.9609 |
| 3.0394 | 2701.7876 | 2751.0224 | 2743.3406 |
| 3.0504 | 2743.5998 | 2736.4888 | 2728.7203 |
| 3.0614 | 2700.3156 | 2721.9567 | 2714.1000 |
| 3.0724 | 2754.2719 | 2707.4261 | 2699.4797 |
| 3.0834 | 2725.7955 | 2692.8969 | 2684.8594 |
| 3.0944 | 2715.8938 | 2678.3694 | 2670.2391 |
| 3.1054 | 2679.7925 | 2663.8434 | 2655.6187 |
| 3.1164 | 2669.0000 | 2649.3191 | 2640.9984 |
| 3.1274 | 2643.1239 | 2635.1751 | 2626.3781 |
| 3.1384 | 2565.4041 | 2624.0247 | 2615.5070 |
| 3.1494 | 2585.7660 | 2613.2547 | 2604.6359 |
| 3.1604 | 2626.4646 | 2602.4865 | 2593.7648 |
| 3.1714 | 2584.1426 | 2591.7201 | 2582.8937 |
| 3.1824 | 2630.6603 | 2580.9556 | 2572.0226 |
| 3.1934 | 2624.8938 | 2570.1929 | 2561.1514 |
| 3.2044 | 2543.6740 | 2559.4323 | 2550.2803 |
| 3.2154 | 2532.5290 | 2548.6737 | 2539.4092 |
| 3.2264 | 2562.7065 | 2537.9171 | 2528.5381 |
| 3.2374 | 2571.2449 | 2527.1627 | 2517.6670 |
| 3.2484 | 2582.6111 | 2516.4104 | 2506.7959 |
| 3.2594 | 2531.8142 | 2505.6603 | 2495.9247 |
| 3.2704 | 2509.6435 | 2494.9124 | 2485.0536 |
| 3.2814 | 2463.7424 | 2484.1670 | 2474.1825 |
| 3.2924 | 2475.9602 | 2473.4238 | 2463.3114 |
| 3.3034 | 2477.8338 | 2462.6832 | 2452.4403 |
| 3.3144 | 2492.7119 | 2451.9450 | 2441.5692 |
| 3.3254 | 2495.8318 | 2441.2094 | 2430.6981 |
| 3.3364 | 2434.3323 | 2430.4764 | 2419.8269 |
| 3.3474 | 2421.4995 | 2419.7461 | 2408.9558 |
| 3.3584 | 2430.7006 | 2409.0186 | 2398.0847 |
| 3.3694 | 2404.4100 | 2398.2940 | 2387.2136 |
| 3.3804 | 2421.2744 | 2387.5723 | 2376.3425 |
| 3.3914 | 2433.3717 | 2376.8535 | 2365.4714 |
| 3.4024 | 2368.0496 | 2366.1378 | 2354.6002 |
| 3.4134 | 2330.2675 | 2355.4253 | 2343.7291 |
| 3.4244 | 2328.3422 | 2344.7161 | 2332.8580 |
| 3.4354 | 2416.6864 | 2334.0102 | 2321.9869 |
| 3.4464 | 2376.7694 | 2323.3077 | 2311.1158 |
| 3.4574 | 2322.7139 | 2312.6087 | 2300.2447 |
| 3.4684 | 2302.6116 | 2301.9133 | 2289.3736 |
| 3.4794 | 2284.1180 | 2291.2217 | 2278.5024 |
| 3.4904 | 2276.0664 | 2280.5339 | 2267.6313 |
| 3.5014 | 2238.0777 | 2270.2534 | 2256.7602 |
| 3.5124 | 2263.4002 | 2263.1637 | 2249.8825 |
| 3.5234 | 2250.2802 | 2256.4815 | 2243.0047 |
| 3.5344 | 2224.6647 | 2249.8036 | 2236.1270 |
| 3.5454 | 2233.6942 | 2243.1301 | 2229.2493 |
| 3.5564 | 2271.9867 | 2236.4612 | 2222.3715 |
| 3.5674 | 2198.2871 | 2229.7971 | 2215.4938 |
| 3.5784 | 2172.7881 | 2223.1378 | 2208.6161 |
| 3.5894 | 2207.8761 | 2216.4836 | 2201.7383 |
| 3.6004 | 2263.3678 | 2209.8346 | 2194.8606 |
| 3.6114 | 2200.5231 | 2203.1910 | 2187.9829 |
| 3.6224 | 2206.0103 | 2196.5530 | 2181.1052 |
| 3.6334 | 2200.5329 | 2189.9208 | 2174.2274 |
| 3.6444 | 2202.9882 | 2183.2945 | 2167.3497 |
| 3.6554 | 2216.6549 | 2176.6745 | 2160.4720 |
| 3.6664 | 2194.1775 | 2170.0609 | 2153.5942 |
| 3.6774 | 2202.1554 | 2163.4540 | 2146.7165 |
| 3.6884 | 2111.5442 | 2157.0188 | 2139.8388 |
| 3.6994 | 2095.4287 | 2151.8920 | 2134.5916 |
| 3.7104 | 2133.0148 | 2146.9375 | 2129.3445 |
| 3.7214 | 2163.6047 | 2141.9909 | 2124.0973 |
| 3.7324 | 2171.5782 | 2137.0525 | 2118.8502 |
| 3.7434 | 2172.0000 | 2132.1228 | 2113.6031 |
| 3.7544 | 2115.6976 | 2127.2020 | 2108.3559 |
| 3.7654 | 2094.6352 | 2122.2907 | 2103.1088 |
| 3.7764 | 2115.5349 | 2117.3894 | 2097.8616 |
| 3.7874 | 2177.4513 | 2112.4984 | 2092.6145 |
| 3.7984 | 2025.6195 | 2107.6184 | 2087.3674 |
| 3.8094 | 2204.1032 | 2102.7500 | 2082.1202 |
| 3.8204 | 2147.9159 | 2097.8937 | 2076.8731 |
| 3.8314 | 2147.3383 | 2093.0503 | 2071.6259 |
| 3.8424 | 2198.6863 | 2088.2205 | 2066.3788 |
| 3.8534 | 2115.6135 | 2083.4050 | 2061.1317 |
| 3.8644 | 2039.8525 | 2078.6048 | 2055.8845 |
| 3.8754 | 2058.5998 | 2073.8618 | 2050.6374 |
| 3.8864 | 2026.3407 | 2069.4601 | 2045.7965 |
| 3.8974 | 2045.8594 | 2065.1177 | 2040.9557 |
| 3.9084 | 2036.6209 | 2060.7947 | 2036.1148 |
| 3.9194 | 2035.6637 | 2056.4924 | 2031.2739 |
| 3.9304 | 2042.3776 | 2052.2120 | 2026.4331 |
| 3.9414 | 2029.0187 | 2047.9550 | 2021.5922 |
| 3.9524 | 2056.3997 | 2043.7231 | 2016.7513 |
| 3.9634 | 2031.5880 | 2039.5179 | 2011.9105 |
| 3.9744 | 2093.7974 | 2035.3411 | 2007.0696 |
| 3.9854 | 2066.6283 | 2031.1948 | 2002.2288 |
| 3.9964 | 2037.3830 | 2027.0810 | 1997.3879 |
| 4.0074 | 2034.1141 | 2023.0019 | 1992.5470 |
| 4.0184 | 2066.8068 | 2018.9600 | 1987.7062 |
| 4.0294 | 2015.0157 | 2014.9577 | 1982.8653 |
| 4.0404 | 2048.7045 | 2010.9977 | 1978.0244 |
| 4.0514 | 2067.5339 | 2007.0829 | 1973.1836 |
| 4.0624 | 2024.5915 | 2003.2080 | 1968.3427 |
| 4.0734 | 2046.2782 | 1999.3177 | 1963.4180 |
| 4.0844 | 1988.9381 | 1995.4738 | 1958.4933 |
| 4.0954 | 2009.4297 | 1991.6886 | 1953.5685 |
| 4.1064 | 2038.1765 | 1987.9657 | 1948.6438 |
| 4.1174 | 2025.9616 | 1984.3093 | 1943.7191 |
| 4.1284 | 2048.2626 | 1980.7236 | 1938.7943 |
| 4.1394 | 2051.7885 | 1977.2131 | 1933.8696 |
| 4.1504 | 1968.2389 | 1973.7823 | 1928.9449 |
| 4.1614 | 1955.2733 | 1970.4361 | 1924.0202 |
| 4.1724 | 1998.8245 | 1967.1796 | 1919.0954 |
| 4.1834 | 2096.8850 | 1964.0181 | 1914.1707 |
| 4.1944 | 2082.0570 | 1960.9569 | 1909.2460 |

Scan List

| Vis. | Dataset Name | Start pos. [°2θ] | End pos. [°2θ] | Step [°2θ] | Meas.Date/Time |
| --- | --- | --- | --- | --- | --- |
| * | 1 Etosha18 RIP 0-2cm GLYCOLATED | 2.0054 | 29.9894 | 0.0110 | 12/1/2023 9:26:41 AM |

Peak List

| Pos. [°2θ] | Height [cts] | FWHM Left [°2θ] | d-spacing [Å] | Rel. Int. [%] |
| --- | --- | --- | --- | --- |
| 4.9375 | 423.50 | 0.6927 | 17.88278 | 35.28 |
| 6.9664 | 1200.54 | 0.1299 | 12.67860 | 100.00 |
| 8.7328 | 458.90 | 0.1082 | 10.11765 | 38.22 |
| 15.7749 | 664.53 | 0.0866 | 5.61331 | 55.35 |
| 17.6244 | 33.56 | 0.2598 | 5.02820 | 2.80 |
| 18.2465 | 118.89 | 0.0866 | 4.85812 | 9.90 |
| 19.8910 | 54.18 | 0.6061 | 4.46004 | 4.51 |
| 25.9309 | 674.98 | 0.0974 | 3.43327 | 56.22 |
| 26.7676 | 146.33 | 0.3031 | 3.32782 | 12.19 |

Pattern List

| Visible | Ref.Code | Score | Compound Name | Chem. Formula | Mineral Name | SemiQuant[%] |
| --- | --- | --- | --- | --- | --- | --- |
| * | 01-082-8023 | 45 | Sodium Magnesium Silicon Oxide Hydrate | Na2 Mg3 ( Si6 O16 ) ( H2 O )7 | Loughlinite | 18 |
| * | 01-083-1732 | 62 | Sodium Aluminum Silicate Hydrate | Na16.48 Al15.52 Si32.48 O96 ( H2 O )16 | Analcime | 36 |
| * | 04-023-1597 | 42 | Potassium Sodium Magnesium Aluminum Iron Silicon Titanium Oxide Fluoride Hydroxide | K0.865 Na0.135 Mg0.04 Ti0.01 Fe0.09 Al2.84 Si3.045 O10 ( O H )1.945 F0.055 | Muscovite-2M1 | 34 |
| * | 04-018-3208 | 28 | Magnesium Aluminum Iron Silicon Oxide Hydroxide Hydrate | Mg1.0 Fe0.08 Al1.0 Si3.99 O10.2 ( O H )0.8 ( H2 O )3.3 | Palygorskite-M | 6 |
| * | 01-080-5781 | 23 | Magnesium Silicon Oxide Hydroxide Hydrate | Mg8 ( Si12 O30 ( O H )4 ( H2 O )3.92 ) ( H2 O )7.72 | Sepiolite | 7 |

Anchor Scan Parameters

Dataset Name	1 Etosha18 RIP 0-2cm GLYCOLATED

File name	C:\aeris_data\XRD data\Goldstein\Etosha 2023\Etosha Clay Data\Sample 1\1 Etosha18 RIP 0-2cm GLYCOLATED.xrdml

Sample Identification	1 Etosha18 RIP 0-2cm GLYCOLATED

Measurement Start Date/Time	12/1/2023 9:26:41 AM

Operator	Instrument

Raw Data Origin	XRD measurement (*.XRDML)

Scan Axis	Gonio

Start Position [°2θ]	2.0054

End Position [°2θ]	29.9894

Step Size [°2θ]	0.0110

Scan Step Time [s]	48.1950

Scan Type	Continuous

PSD Mode	Scanning

PSD Length [°2θ]	5.54

Offset [°2θ]	0.0000

Divergence Slit Type	Fixed

Divergence Slit Size [°]	0.0603

Specimen Length [mm]	10.00

Measurement Temperature [°C]	25.00

Anode Material	Cu

K-α1 [Å]	1.54060

K-α2 [Å]	1.54443

K-β1 [Å]	1.39225

K-A2 / K-A1 Ratio	0.50000

Generator Settings	15 mA, 40 kV

Diffractometer Type	2082464

Diffractometer Number	0

Goniometer Radius [mm]	145.00

Dist. Focus-Diverg. Slit [mm]	95.00

Incident Beam Monochromator	No

Spinning	Yes