REGULAR

Graphics

Graphics

Graphics

Quantitative Results

Phase Sodium Magnesium Silicon Oxide Hydrate

Weight fraction/ %	9.0

Phase Magnesium Silicon Oxide Hydroxide Hydrate

Weight fraction/ %	18.0

Phase Magnesium Aluminum Iron Silicon Oxide Hydroxide Hydrate

Weight fraction/ %	4.0

Phase Potassium Lithium Iron Aluminum Silicate Hydroxide

Weight fraction/ %	21.0

Phase Sodium Aluminum Silicate Hydrate

Weight fraction/ %	39.0

Phase Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide

Weight fraction/ %	10.0

Multiple Quantitative Results

Scans vs Phases Matrix

| Scan name | Sodium Magnesium Silicon Oxide Hydrate | Magnesium Silicon Oxide Hydroxide Hydrate | Magnesium Aluminum Iron Silicon Oxide Hydroxide Hydrate | Potassium Lithium Iron Aluminum Silicate Hydroxide | Sodium Aluminum Silicate Hydrate | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide |
| --- | --- | --- | --- | --- | --- | --- |
| 1 Etosha18 RIP 0-2cm | 9.0 | 18.0 | 4.0 | 21.0 | 39.0 | 10.0 |

Anchor Scan Data

| Pos. [°2θ] | Iobs [cts] | Icalc [cts] | Iback [cts] |
| --- | --- | --- | --- |
| 2.0054 | 1650.0000 | 1647.7361 | 1650.0000 |
| 2.0164 | 1643.4794 | 1642.5459 | 1642.5459 |
| 2.0274 | 1681.2871 | 1635.0919 | 1635.0919 |
| 2.0384 | 1653.3687 | 1627.6378 | 1627.6378 |
| 2.0494 | 1659.3127 | 1620.1837 | 1620.1837 |
| 2.0604 | 1592.4248 | 1612.7296 | 1612.7296 |
| 2.0714 | 1658.0088 | 1605.2756 | 1605.2756 |
| 2.0824 | 1631.2793 | 1597.8215 | 1597.8215 |
| 2.0934 | 1610.0501 | 1590.3674 | 1590.3674 |
| 2.1044 | 1579.0177 | 1582.9133 | 1582.9133 |
| 2.1154 | 1550.4415 | 1575.4593 | 1575.4593 |
| 2.1264 | 1575.8112 | 1568.0052 | 1568.0052 |
| 2.1374 | 1569.4956 | 1560.5511 | 1560.5511 |
| 2.1484 | 1510.9892 | 1553.0970 | 1553.0970 |
| 2.1594 | 1553.0000 | 1545.6430 | 1545.6430 |
| 2.1704 | 1558.5310 | 1538.1889 | 1538.1889 |
| 2.1814 | 1565.1042 | 1530.7348 | 1530.7348 |
| 2.1924 | 1508.5069 | 1523.2808 | 1523.2808 |
| 2.2034 | 1554.6283 | 1515.8267 | 1515.8267 |
| 2.2144 | 1501.6706 | 1508.3726 | 1508.3726 |
| 2.2254 | 1511.5919 | 1500.9185 | 1500.9185 |
| 2.2364 | 1495.5162 | 1493.4645 | 1493.4645 |
| 2.2474 | 1501.8673 | 1486.0104 | 1486.0104 |
| 2.2584 | 1500.5826 | 1478.5563 | 1478.5563 |
| 2.2694 | 1460.4602 | 1471.1022 | 1471.1022 |
| 2.2804 | 1446.1617 | 1463.6482 | 1463.6482 |
| 2.2914 | 1429.8043 | 1456.1941 | 1456.1941 |
| 2.3024 | 1437.9336 | 1448.7400 | 1448.7400 |
| 2.3134 | 1443.5654 | 1441.2860 | 1441.2860 |
| 2.3244 | 1415.5349 | 1433.8319 | 1433.8319 |
| 2.3354 | 1457.1121 | 1426.3778 | 1426.3778 |
| 2.3464 | 1449.6627 | 1418.9237 | 1418.9237 |
| 2.3574 | 1438.2055 | 1411.4697 | 1411.4697 |
| 2.3684 | 1428.5723 | 1404.0156 | 1404.0156 |
| 2.3794 | 1359.4926 | 1396.6691 | 1396.5615 |
| 2.3904 | 1374.9282 | 1389.4616 | 1389.4616 |
| 2.4014 | 1411.5044 | 1382.3618 | 1382.3618 |
| 2.4124 | 1400.9877 | 1375.2619 | 1375.2619 |
| 2.4234 | 1360.7247 | 1368.1620 | 1368.1620 |
| 2.4344 | 1335.5782 | 1361.0622 | 1361.0622 |
| 2.4454 | 1305.7591 | 1353.9623 | 1353.9623 |
| 2.4564 | 1327.2911 | 1346.8624 | 1346.8624 |
| 2.4674 | 1381.5516 | 1339.7626 | 1339.7626 |
| 2.4784 | 1356.7758 | 1332.6627 | 1332.6627 |
| 2.4894 | 1318.9184 | 1325.5628 | 1325.5628 |
| 2.5004 | 1313.0221 | 1318.4630 | 1318.4630 |
| 2.5114 | 1353.6657 | 1311.3631 | 1311.3631 |
| 2.5224 | 1366.0482 | 1304.2632 | 1304.2632 |
| 2.5334 | 1318.7316 | 1297.1634 | 1297.1634 |
| 2.5444 | 1317.4769 | 1290.0635 | 1290.0635 |
| 2.5554 | 1303.3451 | 1282.9636 | 1282.9636 |
| 2.5664 | 1342.4159 | 1275.8637 | 1275.8637 |
| 2.5774 | 1300.5821 | 1268.7639 | 1268.7639 |
| 2.5884 | 1270.3771 | 1261.6640 | 1261.6640 |
| 2.5994 | 1247.1327 | 1254.5641 | 1254.5641 |
| 2.6104 | 1249.5762 | 1247.4643 | 1247.4643 |
| 2.6214 | 1234.5978 | 1240.3644 | 1240.3644 |
| 2.6324 | 1287.0531 | 1233.2645 | 1233.2645 |
| 2.6434 | 1215.6224 | 1226.1647 | 1226.1647 |
| 2.6544 | 1196.3048 | 1219.0648 | 1219.0648 |
| 2.6654 | 1263.7345 | 1211.9649 | 1211.9649 |
| 2.6764 | 1241.5143 | 1204.8651 | 1204.8651 |
| 2.6874 | 1215.5693 | 1197.7652 | 1197.7652 |
| 2.6984 | 1138.4380 | 1190.6653 | 1190.6653 |
| 2.7094 | 1113.0669 | 1183.5655 | 1183.5655 |
| 2.7204 | 1190.2940 | 1176.4656 | 1176.4656 |
| 2.7314 | 1203.5103 | 1169.3657 | 1169.3657 |
| 2.7424 | 1145.1785 | 1162.2658 | 1162.2658 |
| 2.7534 | 1134.6716 | 1155.7482 | 1155.1660 |
| 2.7644 | 1142.6327 | 1149.9833 | 1149.9833 |
| 2.7754 | 1173.2527 | 1144.8006 | 1144.8006 |
| 2.7864 | 1191.9626 | 1139.6178 | 1139.6178 |
| 2.7974 | 1120.5487 | 1134.4351 | 1134.4351 |
| 2.8084 | 1148.6844 | 1129.2524 | 1129.2524 |
| 2.8194 | 1098.4277 | 1124.0697 | 1124.0697 |
| 2.8304 | 1134.4823 | 1118.8870 | 1118.8870 |
| 2.8414 | 1050.1927 | 1113.7043 | 1113.7043 |
| 2.8524 | 1093.2134 | 1108.5216 | 1108.5216 |
| 2.8634 | 1030.8082 | 1103.3389 | 1103.3389 |
| 2.8744 | 1141.6062 | 1098.1561 | 1098.1561 |
| 2.8854 | 1031.9223 | 1092.9734 | 1092.9734 |
| 2.8964 | 1058.8717 | 1087.7907 | 1087.7907 |
| 2.9074 | 1080.7325 | 1082.6080 | 1082.6080 |
| 2.9184 | 1047.2620 | 1077.4253 | 1077.4253 |
| 2.9294 | 1060.6814 | 1072.2426 | 1072.2426 |
| 2.9404 | 1080.6868 | 1068.1075 | 1067.0599 |
| 2.9514 | 1071.6047 | 1063.8605 | 1063.8605 |
| 2.9624 | 1034.7035 | 1060.6612 | 1060.6612 |
| 2.9734 | 1068.5516 | 1057.4619 | 1057.4619 |
| 2.9844 | 1037.0560 | 1054.2626 | 1054.2626 |
| 2.9954 | 999.4248 | 1051.0632 | 1051.0632 |
| 3.0064 | 1004.7773 | 1047.8639 | 1047.8639 |
| 3.0174 | 1018.6539 | 1044.6646 | 1044.6646 |
| 3.0284 | 1022.1416 | 1041.4653 | 1041.4653 |
| 3.0394 | 1013.4267 | 1038.2659 | 1038.2659 |
| 3.0504 | 1006.5738 | 1035.0666 | 1035.0666 |
| 3.0614 | 1064.8614 | 1031.8673 | 1031.8673 |
| 3.0724 | 1043.5010 | 1028.6680 | 1028.6680 |
| 3.0834 | 1034.6362 | 1025.4686 | 1025.4686 |
| 3.0944 | 1032.3274 | 1022.2693 | 1022.2693 |
| 3.1054 | 998.0216 | 1019.0700 | 1019.0700 |
| 3.1164 | 995.2419 | 1015.8707 | 1015.8707 |
| 3.1274 | 1021.0443 | 1012.6514 | 1012.6713 |
| 3.1384 | 1048.8845 | 1009.4343 | 1009.4343 |
| 3.1494 | 1075.1209 | 1006.1972 | 1006.1972 |
| 3.1604 | 1007.1283 | 1002.9601 | 1002.9601 |
| 3.1714 | 998.6401 | 999.7230 | 999.7230 |
| 3.1824 | 982.7394 | 996.4860 | 996.4860 |
| 3.1934 | 982.9469 | 993.2489 | 993.2489 |
| 3.2044 | 971.3343 | 990.0118 | 990.0118 |
| 3.2154 | 951.4327 | 986.7748 | 986.7748 |
| 3.2264 | 968.8923 | 983.5377 | 983.5377 |
| 3.2374 | 980.1151 | 980.3006 | 980.3006 |
| 3.2484 | 999.7222 | 977.0635 | 977.0635 |
| 3.2594 | 965.2153 | 973.8265 | 973.8265 |
| 3.2704 | 972.1731 | 970.5894 | 970.5894 |
| 3.2814 | 976.9607 | 967.3523 | 967.3523 |
| 3.2924 | 960.4690 | 964.1153 | 964.1153 |
| 3.3034 | 964.1269 | 960.8782 | 960.8782 |
| 3.3144 | 960.2738 | 957.6411 | 957.6411 |
| 3.3254 | 952.5428 | 954.4040 | 954.4040 |
| 3.3364 | 971.3564 | 951.1670 | 951.1670 |
| 3.3474 | 917.0197 | 947.9299 | 947.9299 |
| 3.3584 | 933.3378 | 944.6928 | 944.6928 |
| 3.3694 | 932.3618 | 941.4557 | 941.4557 |
| 3.3804 | 941.3014 | 938.2187 | 938.2187 |
| 3.3914 | 951.7611 | 934.9816 | 934.9816 |
| 3.4024 | 943.3412 | 931.7445 | 931.7445 |
| 3.4134 | 970.1976 | 928.5075 | 928.5075 |
| 3.4244 | 935.5708 | 925.2704 | 925.2704 |
| 3.4354 | 937.2724 | 922.0333 | 922.0333 |
| 3.4464 | 915.2404 | 918.7962 | 918.7962 |
| 3.4574 | 942.6401 | 915.5592 | 915.5592 |
| 3.4684 | 967.4793 | 912.3221 | 912.3221 |
| 3.4794 | 909.5929 | 909.0850 | 909.0850 |
| 3.4904 | 891.5487 | 905.8480 | 905.8480 |
| 3.5014 | 893.6421 | 903.4670 | 902.6109 |
| 3.5124 | 898.8387 | 902.3653 | 900.8280 |
| 3.5234 | 931.2389 | 900.6352 | 899.0451 |
| 3.5344 | 955.3353 | 899.5870 | 897.2621 |
| 3.5454 | 889.3667 | 897.8173 | 895.4792 |
| 3.5564 | 866.3982 | 896.0477 | 893.6963 |
| 3.5674 | 921.6637 | 894.2783 | 891.9134 |
| 3.5784 | 878.6327 | 892.5089 | 890.1305 |
| 3.5894 | 892.1062 | 890.7396 | 888.3476 |
| 3.6004 | 862.8899 | 888.9705 | 886.5647 |
| 3.6114 | 902.8476 | 887.2015 | 884.7818 |
| 3.6224 | 872.4336 | 885.4326 | 882.9988 |
| 3.6334 | 811.2173 | 883.6639 | 881.2159 |
| 3.6444 | 849.8820 | 881.8952 | 879.4330 |
| 3.6554 | 902.1829 | 880.1267 | 877.6501 |
| 3.6664 | 898.0167 | 878.3583 | 875.8672 |
| 3.6774 | 919.4425 | 876.5900 | 874.0843 |
| 3.6884 | 908.0310 | 874.7993 | 872.3014 |
| 3.6994 | 883.6794 | 873.0111 | 870.4756 |
| 3.7104 | 866.5182 | 871.2003 | 868.6498 |
| 3.7214 | 877.8437 | 869.3898 | 866.8241 |
| 3.7324 | 902.2424 | 867.5793 | 864.9983 |
| 3.7434 | 885.1603 | 865.7690 | 863.1726 |
| 3.7544 | 876.3658 | 863.9588 | 861.3468 |
| 3.7654 | 923.3619 | 862.1488 | 859.5210 |
| 3.7764 | 871.1627 | 860.3389 | 857.6953 |
| 3.7874 | 923.5221 | 858.5292 | 855.8695 |
| 3.7984 | 840.2547 | 856.7196 | 854.0438 |
| 3.8094 | 913.0560 | 854.9101 | 852.2180 |
| 3.8204 | 853.9720 | 853.1008 | 850.3922 |
| 3.8314 | 853.3225 | 851.2917 | 848.5665 |
| 3.8424 | 862.5256 | 849.4827 | 846.7407 |
| 3.8534 | 888.5074 | 847.6738 | 844.9150 |
| 3.8644 | 870.8594 | 845.8652 | 843.0892 |
| 3.8754 | 908.6784 | 844.0566 | 841.2634 |
| 3.8864 | 825.0177 | 842.2483 | 839.4377 |
| 3.8974 | 838.7906 | 840.4401 | 837.6119 |
| 3.9084 | 869.6824 | 838.6320 | 835.7862 |
| 3.9194 | 834.5959 | 836.8242 | 833.9604 |
| 3.9304 | 890.4150 | 835.0165 | 832.1346 |
| 3.9414 | 896.4916 | 833.2089 | 830.3089 |
| 3.9524 | 857.1224 | 831.4016 | 828.4831 |
| 3.9634 | 856.0049 | 829.5944 | 826.6574 |
| 3.9744 | 867.1991 | 827.7874 | 824.8316 |
| 3.9854 | 854.4779 | 825.9806 | 823.0058 |
| 3.9964 | 822.7660 | 824.1739 | 821.1801 |
| 4.0074 | 789.9243 | 822.3675 | 819.3543 |
| 4.0184 | 809.7478 | 820.5612 | 817.5286 |
| 4.0294 | 817.2311 | 818.7551 | 815.7028 |
| 4.0404 | 824.6062 | 816.9492 | 813.8770 |
| 4.0514 | 810.7227 | 815.1435 | 812.0513 |
| 4.0624 | 818.4346 | 813.3154 | 810.2255 |
| 4.0734 | 819.4681 | 811.4899 | 808.3569 |
| 4.0844 | 860.1991 | 809.6420 | 806.4883 |
| 4.0954 | 852.5703 | 807.7942 | 804.6197 |
| 4.1064 | 832.1657 | 805.9467 | 802.7511 |
| 4.1174 | 835.2065 | 804.0994 | 800.8825 |
| 4.1284 | 811.1652 | 802.2523 | 799.0139 |
| 4.1394 | 839.9961 | 800.4054 | 797.1452 |
| 4.1504 | 863.1416 | 798.5587 | 795.2766 |
| 4.1614 | 867.4553 | 796.7123 | 793.4080 |
| 4.1724 | 830.6131 | 794.8660 | 791.5394 |
| 4.1834 | 796.0354 | 793.0200 | 789.6708 |
| 4.1944 | 806.2429 | 791.1743 | 787.8022 |

Scan List

| Vis. | Dataset Name | Start pos. [°2θ] | End pos. [°2θ] | Step [°2θ] | Meas.Date/Time |
| --- | --- | --- | --- | --- | --- |
| * | 1 Etosha18 RIP 0-2cm | 2.0054 | 29.9894 | 0.0110 | 11/30/2023 2:44:45 PM |

Peak List

| Pos. [°2θ] | Height [cts] | FWHM Left [°2θ] | d-spacing [Å] | Rel. Int. [%] |
| --- | --- | --- | --- | --- |
| 7.4076 | 1634.85 | 0.3897 | 11.92443 | 100.00 |
| 8.9061 | 459.11 | 0.3031 | 9.92116 | 28.08 |
| 11.8084 | 17.52 | 0.5196 | 7.48841 | 1.07 |
| 13.1688 | 38.94 | 0.3464 | 6.71770 | 2.38 |
| 15.9152 | 630.74 | 0.0433 | 5.56412 | 38.58 |
| 17.8135 | 50.68 | 0.2598 | 4.97522 | 3.10 |
| 18.4131 | 84.93 | 0.1515 | 4.81456 | 5.19 |
| 19.7907 | 72.45 | 0.4330 | 4.48242 | 4.43 |
| 21.2795 | 19.27 | 0.5196 | 4.17205 | 1.18 |
| 23.6191 | 24.68 | 0.6927 | 3.76381 | 1.51 |
| 26.1273 | 567.01 | 0.0649 | 3.40790 | 34.68 |
| 26.8864 | 174.92 | 0.3031 | 3.31339 | 10.70 |
| 27.6766 | 43.46 | 0.2598 | 3.22055 | 2.66 |

Pattern List

| Visible | Ref.Code | Score | Compound Name | Chem. Formula | Mineral Name | SemiQuant[%] |
| --- | --- | --- | --- | --- | --- | --- |
| * | 01-082-8023 | 17 | Sodium Magnesium Silicon Oxide Hydrate | Na2 Mg3 ( Si6 O16 ) ( H2 O )7 | Loughlinite | 9 |
| * | 01-080-5781 | 44 | Magnesium Silicon Oxide Hydroxide Hydrate | Mg8 ( Si12 O30 ( O H )4 ( H2 O )3.92 ) ( H2 O )7.72 | Sepiolite | 18 |
| * | 04-018-3208 | 20 | Magnesium Aluminum Iron Silicon Oxide Hydroxide Hydrate | Mg1.0 Fe0.08 Al1.0 Si3.99 O10.2 ( O H )0.8 ( H2 O )3.3 | Palygorskite-M | 4 |
| * | 01-089-6879 | 26 | Potassium Lithium Iron Aluminum Silicate Hydroxide | K0.9 ( Li0.20 Fe0.92 Al1.2 ) ( Al0.82 Si3.18 O10 ) ( O H )2 | Muscovite-1M, Fe+3-bearing | 21 |
| * | 01-076-6569 | 56 | Sodium Aluminum Silicate Hydrate | Na0.9 ( ( Al0.9 Si2 ) O6 ) ( H2 O ) | Analcime | 39 |
| * | 04-025-4215 | 3 | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide | Mg10.4 V0.36 Mn33.5 Fe0.14 Al0.69 Si6.77 As6.5 P0.3 O54 ( O H )42 | Carlfrancisite | 10 |

Anchor Scan Parameters

Dataset Name	1 Etosha18 RIP 0-2cm

File name	C:\aeris_data\XRD data\Goldstein\Etosha 2023\Etosha Clay Data\Sample 1\1 Etosha18 RIP 0-2cm.xrdml

Sample Identification	1 Etosha18 RIP 0-2cm

Measurement Start Date/Time	11/30/2023 2:44:45 PM

Operator	Instrument

Raw Data Origin	XRD measurement (*.XRDML)

Scan Axis	Gonio

Start Position [°2θ]	2.0054

End Position [°2θ]	29.9894

Step Size [°2θ]	0.0110

Scan Step Time [s]	48.1950

Scan Type	Continuous

PSD Mode	Scanning

PSD Length [°2θ]	5.54

Offset [°2θ]	0.0000

Divergence Slit Type	Fixed

Divergence Slit Size [°]	0.0603

Specimen Length [mm]	10.00

Measurement Temperature [°C]	25.00

Anode Material	Cu

K-α1 [Å]	1.54060

K-α2 [Å]	1.54443

K-β1 [Å]	1.39225

K-A2 / K-A1 Ratio	0.50000

Generator Settings	15 mA, 40 kV

Diffractometer Type	2082464

Diffractometer Number	0

Goniometer Radius [mm]	145.00

Dist. Focus-Diverg. Slit [mm]	95.00

Incident Beam Monochromator	No

Spinning	Yes