10 Etosha 22 CrySub 4-10 cm S1 400 C REPORT

Graphics

Graphics

Graphics

Quantitative Results

Phase Sodium Aluminum Silicate Hydrate

Weight fraction/ %	17.0

Phase Potassium Sodium Magnesium Aluminum Iron Silicon Titanium Oxide Fluoride Hydroxide

Weight fraction/ %	28.0

Phase Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide

Weight fraction/ %	27.0

Phase Magnesium Silicate Hydroxide Hydrate

Weight fraction/ %	8.0

Phase Silicon Oxide

Weight fraction/ %	13.0

Phase Sodium Magnesium Silicon Oxide Hydrate

Weight fraction/ %	8.0

Multiple Quantitative Results

Scans vs Phases Matrix

| Scan name | Sodium Aluminum Silicate Hydrate | Potassium Sodium Magnesium Aluminum Iron Silicon Titanium Oxide Fluoride Hydroxide | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide | Magnesium Silicate Hydroxide Hydrate | Silicon Oxide | Sodium Magnesium Silicon Oxide Hydrate |
| --- | --- | --- | --- | --- | --- | --- |
| 10 Etosha22 Crysub 4-10cm S1 heat400 | 17.0 | 28.0 | 27.0 | 8.0 | 13.0 | 8.0 |

Anchor Scan Data

| Pos. [°2θ] | Iobs [cts] | Icalc [cts] | Iback [cts] |
| --- | --- | --- | --- |
| 2.0054 | 5331.0000 | 5313.0881 | 5331.0000 |
| 2.0164 | 5154.7866 | 5288.0846 | 5287.7569 |
| 2.0274 | 5218.2704 | 5244.8439 | 5244.5138 |
| 2.0384 | 5222.8791 | 5201.6032 | 5201.2707 |
| 2.0494 | 5059.7060 | 5158.3625 | 5158.0276 |
| 2.0604 | 4996.8604 | 5115.1218 | 5114.7845 |
| 2.0714 | 5008.6726 | 5071.8812 | 5071.5414 |
| 2.0824 | 4983.4823 | 5028.6406 | 5028.2983 |
| 2.0934 | 4885.0354 | 4985.4000 | 4985.0552 |
| 2.1044 | 4812.8850 | 4942.1594 | 4941.8121 |
| 2.1154 | 4808.8151 | 4898.9189 | 4898.5690 |
| 2.1264 | 4730.2168 | 4855.6784 | 4855.3259 |
| 2.1374 | 4734.9027 | 4812.4380 | 4812.0828 |
| 2.1484 | 4727.8653 | 4769.1975 | 4768.8397 |
| 2.1594 | 4755.2311 | 4725.9571 | 4725.5966 |
| 2.1704 | 4581.3953 | 4682.7167 | 4682.3535 |
| 2.1814 | 4490.8378 | 4639.4764 | 4639.1104 |
| 2.1924 | 4674.0000 | 4605.1384 | 4595.8673 |
| 2.2034 | 4641.4779 | 4574.1044 | 4573.7328 |
| 2.2144 | 4534.0059 | 4551.9728 | 4551.5984 |
| 2.2254 | 4563.6372 | 4529.8412 | 4529.4639 |
| 2.2364 | 4558.4469 | 4507.7097 | 4507.3294 |
| 2.2474 | 4475.2655 | 4485.5781 | 4485.1950 |
| 2.2584 | 4497.3407 | 4463.4467 | 4463.0605 |
| 2.2694 | 4527.3746 | 4441.3152 | 4440.9260 |
| 2.2804 | 4317.3692 | 4419.1838 | 4418.7916 |
| 2.2914 | 4316.1563 | 4397.0524 | 4396.6571 |
| 2.3024 | 4268.9558 | 4374.9211 | 4374.5226 |
| 2.3134 | 4323.0708 | 4352.7898 | 4352.3881 |
| 2.3244 | 4361.9798 | 4330.6585 | 4330.2537 |
| 2.3354 | 4266.6962 | 4308.5273 | 4308.1192 |
| 2.3464 | 4209.1475 | 4286.3961 | 4285.9847 |
| 2.3574 | 4226.0079 | 4264.2649 | 4263.8503 |
| 2.3684 | 4195.0841 | 4242.1338 | 4241.7158 |
| 2.3794 | 4218.2085 | 4221.5550 | 4219.5813 |
| 2.3904 | 4241.0113 | 4201.5523 | 4201.1274 |
| 2.4014 | 4222.4336 | 4183.1019 | 4182.6736 |
| 2.4124 | 4180.3569 | 4164.6516 | 4164.2197 |
| 2.4234 | 4164.4671 | 4146.2013 | 4145.7658 |
| 2.4344 | 4061.4602 | 4127.7510 | 4127.3119 |
| 2.4454 | 3978.9902 | 4109.3008 | 4108.8580 |
| 2.4564 | 4004.9607 | 4090.8506 | 4090.4041 |
| 2.4674 | 4012.3894 | 4072.4005 | 4071.9502 |
| 2.4784 | 4035.6273 | 4053.9504 | 4053.4964 |
| 2.4894 | 4039.5103 | 4035.5003 | 4035.0425 |
| 2.5004 | 4083.7788 | 4017.0504 | 4016.5886 |
| 2.5114 | 4007.5300 | 3998.6004 | 3998.1347 |
| 2.5224 | 3931.8643 | 3980.1505 | 3979.6808 |
| 2.5334 | 3926.0708 | 3961.7007 | 3961.2269 |
| 2.5444 | 3941.4995 | 3943.2509 | 3942.7731 |
| 2.5554 | 3943.6362 | 3924.8012 | 3924.3192 |
| 2.5664 | 3849.3761 | 3910.2713 | 3905.8653 |
| 2.5774 | 3876.9744 | 3897.1963 | 3896.7058 |
| 2.5884 | 4001.7768 | 3888.0411 | 3887.5463 |
| 2.5994 | 3919.5575 | 3878.8860 | 3878.3868 |
| 2.6104 | 3846.5359 | 3869.7309 | 3869.2273 |
| 2.6214 | 3929.4140 | 3860.5759 | 3860.0678 |
| 2.6324 | 3940.9764 | 3851.4210 | 3850.9083 |
| 2.6434 | 3935.4159 | 3842.2661 | 3841.7488 |
| 2.6544 | 3892.3142 | 3833.1113 | 3832.5893 |
| 2.6654 | 3894.9115 | 3823.9565 | 3823.4298 |
| 2.6764 | 3846.5182 | 3814.8018 | 3814.2703 |
| 2.6874 | 3844.7650 | 3805.6472 | 3805.1108 |
| 2.6984 | 3916.5929 | 3796.4927 | 3795.9513 |
| 2.7094 | 3847.8977 | 3787.3382 | 3786.7918 |
| 2.7204 | 3828.7935 | 3778.1838 | 3777.6322 |
| 2.7314 | 3800.7965 | 3769.0294 | 3768.4727 |
| 2.7424 | 3729.7670 | 3759.8751 | 3759.3132 |
| 2.7534 | 3654.1514 | 3752.2702 | 3750.1537 |
| 2.7644 | 3835.3629 | 3744.6254 | 3744.0529 |
| 2.7754 | 3855.3736 | 3738.5300 | 3737.9520 |
| 2.7864 | 3814.6027 | 3732.4347 | 3731.8511 |
| 2.7974 | 3864.7522 | 3726.3394 | 3725.7503 |
| 2.8084 | 3828.9321 | 3720.2442 | 3719.6494 |
| 2.8194 | 3811.2665 | 3714.1492 | 3713.5485 |
| 2.8304 | 3795.2507 | 3708.0541 | 3707.4477 |
| 2.8414 | 3798.6706 | 3701.9592 | 3701.3468 |
| 2.8524 | 3800.8928 | 3695.8644 | 3695.2459 |
| 2.8634 | 3719.5103 | 3689.7696 | 3689.1450 |
| 2.8744 | 3832.5192 | 3683.6750 | 3683.0442 |
| 2.8854 | 3773.0698 | 3677.5804 | 3676.9433 |
| 2.8964 | 3720.2301 | 3671.4860 | 3670.8424 |
| 2.9074 | 3636.2675 | 3665.3916 | 3664.7416 |
| 2.9184 | 3670.7861 | 3659.2973 | 3658.6407 |
| 2.9294 | 3708.1239 | 3653.2031 | 3652.5398 |
| 2.9404 | 3682.0895 | 3647.0579 | 3646.4390 |
| 2.9514 | 3679.3805 | 3640.9141 | 3640.2370 |
| 2.9624 | 3614.4381 | 3634.7191 | 3634.0351 |
| 2.9734 | 3762.2055 | 3628.5243 | 3627.8332 |
| 2.9844 | 3695.0280 | 3622.3297 | 3621.6313 |
| 2.9954 | 3674.8319 | 3616.1351 | 3615.4293 |
| 3.0064 | 3677.9150 | 3609.9406 | 3609.2274 |
| 3.0174 | 3757.6529 | 3603.7463 | 3603.0255 |
| 3.0284 | 3644.8510 | 3597.5521 | 3596.8236 |
| 3.0394 | 3611.7660 | 3591.3580 | 3590.6216 |
| 3.0504 | 3580.5797 | 3585.1640 | 3584.4197 |
| 3.0614 | 3637.7434 | 3578.9702 | 3578.2178 |
| 3.0724 | 3604.4563 | 3572.7764 | 3572.0159 |
| 3.0834 | 3668.1583 | 3566.5829 | 3565.8139 |
| 3.0944 | 3670.1991 | 3560.3894 | 3559.6120 |
| 3.1054 | 3571.2724 | 3554.1961 | 3553.4101 |
| 3.1164 | 3571.0703 | 3548.0030 | 3547.2082 |
| 3.1274 | 3639.6254 | 3541.7582 | 3541.0062 |
| 3.1384 | 3652.2330 | 3535.5149 | 3534.7021 |
| 3.1494 | 3625.3481 | 3529.2200 | 3528.3979 |
| 3.1604 | 3653.1018 | 3522.9252 | 3522.0937 |
| 3.1714 | 3663.1544 | 3516.6306 | 3515.7896 |
| 3.1824 | 3583.9292 | 3510.3361 | 3509.4854 |
| 3.1934 | 3491.0089 | 3504.0418 | 3503.1812 |
| 3.2044 | 3582.5973 | 3497.7477 | 3496.8771 |
| 3.2154 | 3551.2085 | 3491.4538 | 3490.5729 |
| 3.2264 | 3551.4203 | 3485.1600 | 3484.2687 |
| 3.2374 | 3519.0000 | 3478.8664 | 3477.9646 |
| 3.2484 | 3512.7778 | 3472.5730 | 3471.6604 |
| 3.2594 | 3483.7434 | 3466.2799 | 3465.3562 |
| 3.2704 | 3510.8186 | 3459.9869 | 3459.0521 |
| 3.2814 | 3541.8889 | 3453.6941 | 3452.7479 |
| 3.2924 | 3496.7124 | 3447.4015 | 3446.4437 |
| 3.3034 | 3503.0855 | 3441.1091 | 3440.1396 |
| 3.3144 | 3495.2670 | 3434.7642 | 3433.8354 |
| 3.3254 | 3503.5015 | 3428.4208 | 3427.4270 |
| 3.3364 | 3536.3624 | 3422.0249 | 3421.0186 |
| 3.3474 | 3490.5899 | 3415.6292 | 3414.6101 |
| 3.3584 | 3450.1800 | 3409.2337 | 3408.2017 |
| 3.3694 | 3485.8977 | 3402.8385 | 3401.7933 |
| 3.3804 | 3543.7296 | 3396.4435 | 3395.3849 |
| 3.3914 | 3537.6106 | 3390.0488 | 3388.9764 |
| 3.4024 | 3435.3181 | 3383.6544 | 3382.5680 |
| 3.4134 | 3414.6244 | 3377.2602 | 3376.1596 |
| 3.4244 | 3476.7714 | 3370.8663 | 3369.7512 |
| 3.4354 | 3518.5762 | 3364.4727 | 3363.3428 |
| 3.4464 | 3434.5314 | 3358.0794 | 3356.9343 |
| 3.4574 | 3358.0826 | 3351.6864 | 3350.5259 |
| 3.4684 | 3458.9784 | 3345.2938 | 3344.1175 |
| 3.4794 | 3426.9498 | 3338.9014 | 3337.7091 |
| 3.4904 | 3410.2611 | 3332.5094 | 3331.3007 |
| 3.5014 | 3396.7640 | 3326.0644 | 3324.8922 |
| 3.5124 | 3440.4971 | 3319.6211 | 3318.3786 |
| 3.5234 | 3479.1386 | 3313.1250 | 3311.8650 |
| 3.5344 | 3420.9474 | 3306.6291 | 3305.3514 |
| 3.5454 | 3435.3619 | 3300.1337 | 3298.8378 |
| 3.5564 | 3426.0767 | 3293.6387 | 3292.3242 |
| 3.5674 | 3381.2242 | 3287.1440 | 3285.8105 |
| 3.5784 | 3434.9130 | 3280.6498 | 3279.2969 |
| 3.5894 | 3452.1504 | 3274.1560 | 3272.7833 |
| 3.6004 | 3379.0373 | 3267.6626 | 3266.2697 |
| 3.6114 | 3263.6607 | 3261.1697 | 3259.7561 |
| 3.6224 | 3406.0045 | 3254.6772 | 3253.2425 |
| 3.6334 | 3389.4838 | 3248.1852 | 3246.7288 |
| 3.6444 | 3296.3574 | 3241.6937 | 3240.2152 |
| 3.6554 | 3365.2095 | 3235.2028 | 3233.7016 |
| 3.6664 | 3402.3987 | 3228.7123 | 3227.1880 |
| 3.6774 | 3260.1356 | 3222.2224 | 3220.6744 |
| 3.6884 | 3362.1549 | 3215.6800 | 3214.1608 |
| 3.6994 | 3239.7197 | 3209.1396 | 3207.5426 |
| 3.7104 | 3274.5915 | 3202.5469 | 3200.9244 |
| 3.7214 | 3366.2360 | 3195.9547 | 3194.3063 |
| 3.7324 | 3367.4921 | 3189.3632 | 3187.6881 |
| 3.7434 | 3206.8623 | 3182.7723 | 3181.0699 |
| 3.7544 | 3363.9986 | 3176.1821 | 3174.4518 |
| 3.7654 | 3293.7079 | 3169.5925 | 3167.8336 |
| 3.7764 | 3376.1608 | 3163.0037 | 3161.2154 |
| 3.7874 | 3342.3186 | 3156.4157 | 3154.5973 |
| 3.7984 | 3253.0207 | 3149.8283 | 3147.9791 |
| 3.8094 | 3259.3619 | 3143.2418 | 3141.3609 |
| 3.8204 | 3280.0944 | 3136.6561 | 3134.7428 |
| 3.8314 | 3214.6450 | 3130.0712 | 3128.1246 |
| 3.8424 | 3228.3692 | 3123.4872 | 3121.5064 |
| 3.8534 | 3198.2861 | 3116.9041 | 3114.8883 |
| 3.8644 | 3197.2626 | 3110.3219 | 3108.2701 |
| 3.8754 | 3302.3628 | 3103.6885 | 3101.6519 |
| 3.8864 | 3231.9734 | 3097.0575 | 3094.9307 |
| 3.8974 | 3137.5310 | 3090.3753 | 3088.2095 |
| 3.9084 | 3287.9026 | 3083.6941 | 3081.4883 |
| 3.9194 | 3225.1386 | 3077.0141 | 3074.7670 |
| 3.9304 | 3226.9056 | 3070.3352 | 3068.0458 |
| 3.9414 | 3217.3097 | 3063.6575 | 3061.3246 |
| 3.9524 | 3135.3304 | 3056.9810 | 3054.6034 |
| 3.9634 | 3109.2586 | 3050.3059 | 3047.8821 |
| 3.9744 | 3133.6008 | 3043.6321 | 3041.1609 |
| 3.9854 | 3135.5398 | 3036.9597 | 3034.4397 |
| 3.9964 | 3124.6170 | 3030.2887 | 3027.7184 |
| 4.0074 | 3161.7729 | 3023.6193 | 3020.9972 |
| 4.0184 | 3217.0059 | 3016.9703 | 3014.2760 |
| 4.0294 | 3210.7384 | 3010.4977 | 3007.5548 |
| 4.0404 | 3175.7694 | 3003.9284 | 3000.8335 |
| 4.0514 | 3096.1593 | 2997.2710 | 2994.1123 |
| 4.0624 | 3123.7016 | 2990.5640 | 2987.3911 |
| 4.0734 | 3158.1111 | 2983.8605 | 2980.5683 |
| 4.0844 | 3192.3938 | 2977.1076 | 2973.7455 |
| 4.0954 | 3088.2586 | 2970.3570 | 2966.9227 |
| 4.1064 | 3085.2458 | 2963.6087 | 2960.0999 |
| 4.1174 | 3141.0354 | 2956.8629 | 2953.2771 |
| 4.1284 | 3115.0122 | 2950.1196 | 2946.4543 |
| 4.1394 | 3043.9941 | 2943.3789 | 2939.6315 |
| 4.1504 | 3102.9145 | 2936.6410 | 2932.8087 |
| 4.1614 | 3116.3225 | 2929.9060 | 2925.9859 |
| 4.1724 | 3125.1500 | 2923.1741 | 2919.1632 |
| 4.1834 | 3157.4601 | 2916.4453 | 2912.3404 |
| 4.1944 | 3046.2183 | 2909.7198 | 2905.5176 |

Scan List

| Vis. | Dataset Name | Start pos. [°2θ] | End pos. [°2θ] | Step [°2θ] | Meas.Date/Time |
| --- | --- | --- | --- | --- | --- |
| * | 10 Etosha22 Crysub 4-10cm S1 heat400 | 2.0054 | 29.9894 | 0.0110 | 12/4/2023 12:22:51 PM |

Peak List

| Pos. [°2θ] | Height [cts] | FWHM Left [°2θ] | d-spacing [Å] | Rel. Int. [%] |
| --- | --- | --- | --- | --- |
| 5.0733 | 181.72 | 0.3464 | 17.40464 | 11.49 |
| 5.3198 | 213.39 | 0.1299 | 16.59868 | 13.49 |
| 7.1642 | 1581.54 | 0.0866 | 12.32906 | 100.00 |
| 8.8104 | 1150.77 | 0.1732 | 10.02870 | 72.76 |
| 10.5967 | 60.06 | 0.4330 | 8.34183 | 3.80 |
| 15.8217 | 904.21 | 0.0758 | 5.59680 | 57.17 |
| 17.7027 | 92.78 | 0.2598 | 5.00611 | 5.87 |
| 18.2799 | 131.31 | 0.1082 | 4.84933 | 8.30 |
| 19.6668 | 72.97 | 0.4330 | 4.51036 | 4.61 |
| 24.2884 | 51.52 | 0.1732 | 3.66159 | 3.26 |
| 25.9863 | 669.86 | 0.0433 | 3.42606 | 42.35 |
| 26.7589 | 270.97 | 0.2598 | 3.32888 | 17.13 |

Pattern List

| Visible | Ref.Code | Score | Compound Name | Chem. Formula | Mineral Name | SemiQuant[%] |
| --- | --- | --- | --- | --- | --- | --- |
| * | 01-076-0143 | 75 | Sodium Aluminum Silicate Hydrate | Na Al ( Si2 O6 ) ( H2 O ) | Analcime | 17 |
| * | 04-014-4596 | 34 | Potassium Sodium Magnesium Aluminum Iron Silicon Titanium Oxide Fluoride Hydroxide | K0.922 Na0.064 Mg1.536 Ti0.322 Fe1.104 Al1.169 Si2.895 O10.641 ( O H )1.059 F0.3 | Phlogopite-1M, Fe+2-bearing | 28 |
| * | 04-025-4215 | 4 | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide | Mg10.4 V0.36 Mn33.5 Fe0.14 Al0.69 Si6.77 As6.5 P0.3 O54 ( O H )42 | Carlfrancisite | 27 |
| * | 01-075-8323 | 17 | Magnesium Silicate Hydroxide Hydrate | Mg8 ( Si12 O30 ( O H )4 ) ( H2 O )11.82 | Sepiolite | 8 |
| * | 01-085-9814 | 18 | Silicon Oxide | Si O2 | Zeolite SSZ-70 | 13 |
| * | 01-082-8023 | 13 | Sodium Magnesium Silicon Oxide Hydrate | Na2 Mg3 ( Si6 O16 ) ( H2 O )7 | Loughlinite | 8 |

Anchor Scan Parameters

Dataset Name	10 Etosha22 Crysub 4-10cm S1 heat400

File name	C:\aeris_data\XRD data\Goldstein\Etosha 2023\Etosha Clay Data\Sample 10\10 Etosha22 Crysub 4-10cm S1 heat400.xrdml

Sample Identification	10 Etosha22 Crysub 4-10cm S1 heat400

Measurement Start Date/Time	12/4/2023 12:22:51 PM

Operator	Instrument

Raw Data Origin	XRD measurement (*.XRDML)

Scan Axis	Gonio

Start Position [°2θ]	2.0054

End Position [°2θ]	29.9894

Step Size [°2θ]	0.0110

Scan Step Time [s]	48.1950

Scan Type	Continuous

PSD Mode	Scanning

PSD Length [°2θ]	5.54

Offset [°2θ]	0.0000

Divergence Slit Type	Fixed

Divergence Slit Size [°]	0.0603

Specimen Length [mm]	10.00

Measurement Temperature [°C]	25.00

Anode Material	Cu

K-α1 [Å]	1.54060

K-α2 [Å]	1.54443

K-β1 [Å]	1.39225

K-A2 / K-A1 Ratio	0.50000

Generator Settings	15 mA, 40 kV

Diffractometer Type	2082464

Diffractometer Number	0

Goniometer Radius [mm]	145.00

Dist. Focus-Diverg. Slit [mm]	95.00

Incident Beam Monochromator	No

Spinning	Yes