10 Etosha 22 CrySub 4-10 cm S1 550 C

Graphics

Graphics

Graphics

Quantitative Results

Phase Sodium Aluminum Silicate Hydrate

Weight fraction/ %	31.0

Phase Potassium Magnesium Aluminum Silicate Hydroxide

Weight fraction/ %	51.0

Phase Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide

Weight fraction/ %	18.0

Multiple Quantitative Results

Scans vs Phases Matrix

| Scan name | Sodium Aluminum Silicate Hydrate | Potassium Magnesium Aluminum Silicate Hydroxide | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide |
| --- | --- | --- | --- |
| 10 Etosha22 Crysub 4-10cm S1 heat550 | 31.0 | 51.0 | 18.0 |

Anchor Scan Data

| Pos. [°2θ] | Iobs [cts] | Icalc [cts] | Iback [cts] |
| --- | --- | --- | --- |
| 2.0054 | 5667.0000 | 5648.5189 | 5667.0000 |
| 2.0164 | 5661.2345 | 5628.1779 | 5627.2561 |
| 2.0274 | 5439.7129 | 5588.4411 | 5587.5121 |
| 2.0384 | 5468.1844 | 5548.7044 | 5547.7682 |
| 2.0494 | 5463.7571 | 5508.9677 | 5508.0242 |
| 2.0604 | 5287.0280 | 5469.2311 | 5468.2803 |
| 2.0714 | 5326.3333 | 5429.4947 | 5428.5363 |
| 2.0824 | 5415.8574 | 5389.7583 | 5388.7924 |
| 2.0934 | 5264.0462 | 5350.0220 | 5349.0485 |
| 2.1044 | 5349.2124 | 5310.2857 | 5309.3045 |
| 2.1154 | 5356.3068 | 5270.5496 | 5269.5606 |
| 2.1264 | 5282.2984 | 5230.8136 | 5229.8166 |
| 2.1374 | 5277.2360 | 5191.0777 | 5190.0727 |
| 2.1484 | 5161.0826 | 5151.3418 | 5150.3287 |
| 2.1594 | 5131.8997 | 5111.6061 | 5110.5848 |
| 2.1704 | 5043.5030 | 5071.8704 | 5070.8408 |
| 2.1814 | 5059.1967 | 5032.1349 | 5031.0969 |
| 2.1924 | 5021.3446 | 4998.9114 | 4991.3530 |
| 2.2034 | 4894.4690 | 4966.0076 | 4964.9525 |
| 2.2144 | 4948.2876 | 4939.6159 | 4938.5520 |
| 2.2254 | 4905.8997 | 4913.2242 | 4912.1516 |
| 2.2364 | 4920.1283 | 4886.8327 | 4885.7511 |
| 2.2474 | 4899.5359 | 4860.4413 | 4859.3506 |
| 2.2584 | 4853.9287 | 4834.0500 | 4832.9502 |
| 2.2694 | 4745.1829 | 4807.6588 | 4806.5497 |
| 2.2804 | 4638.6495 | 4781.2677 | 4780.1493 |
| 2.2914 | 4685.7129 | 4754.8768 | 4753.7488 |
| 2.3024 | 4653.9115 | 4728.4860 | 4727.3483 |
| 2.3134 | 4661.3058 | 4702.0953 | 4700.9479 |
| 2.3244 | 4597.5742 | 4675.7047 | 4674.5474 |
| 2.3354 | 4588.3628 | 4649.3142 | 4648.1469 |
| 2.3464 | 4529.7532 | 4622.9239 | 4621.7465 |
| 2.3574 | 4484.8584 | 4596.5337 | 4595.3460 |
| 2.3684 | 4537.2448 | 4570.1436 | 4568.9455 |
| 2.3794 | 4570.4169 | 4544.6424 | 4542.5451 |
| 2.3904 | 4558.3776 | 4519.1850 | 4517.9657 |
| 2.4014 | 4500.6195 | 4494.6164 | 4493.3863 |
| 2.4124 | 4488.0782 | 4470.0480 | 4468.8069 |
| 2.4234 | 4418.7011 | 4445.4797 | 4444.2275 |
| 2.4344 | 4427.2493 | 4420.9115 | 4419.6480 |
| 2.4454 | 4415.1701 | 4396.3435 | 4395.0686 |
| 2.4564 | 4296.1263 | 4371.7757 | 4370.4892 |
| 2.4674 | 4311.9794 | 4347.2080 | 4345.9098 |
| 2.4784 | 4272.1676 | 4322.6405 | 4321.3304 |
| 2.4894 | 4195.8977 | 4298.0731 | 4296.7510 |
| 2.5004 | 4223.1460 | 4273.5059 | 4272.1716 |
| 2.5114 | 4201.9459 | 4248.9389 | 4247.5922 |
| 2.5224 | 4157.6696 | 4224.3720 | 4223.0128 |
| 2.5334 | 4206.9469 | 4199.8053 | 4198.4334 |
| 2.5444 | 4113.8889 | 4175.2388 | 4173.8540 |
| 2.5554 | 4138.9214 | 4150.6725 | 4149.2745 |
| 2.5664 | 4146.4351 | 4129.3064 | 4124.6951 |
| 2.5774 | 4086.2694 | 4108.0976 | 4106.6729 |
| 2.5884 | 4103.3142 | 4090.0891 | 4088.6508 |
| 2.5994 | 4099.0885 | 4072.0807 | 4070.6286 |
| 2.6104 | 4028.1593 | 4054.0726 | 4052.6064 |
| 2.6214 | 3989.3638 | 4036.0646 | 4034.5842 |
| 2.6324 | 4027.7360 | 4018.0569 | 4016.5620 |
| 2.6434 | 3957.6027 | 4000.0494 | 3998.5398 |
| 2.6544 | 4001.0438 | 3982.0421 | 3980.5176 |
| 2.6654 | 3981.5900 | 3964.0350 | 3962.4954 |
| 2.6764 | 3946.7557 | 3946.0281 | 3944.4732 |
| 2.6874 | 3992.8191 | 3928.0215 | 3926.4510 |
| 2.6984 | 3897.4956 | 3910.0151 | 3908.4288 |
| 2.7094 | 3897.2517 | 3892.0089 | 3890.4066 |
| 2.7204 | 3877.2389 | 3874.0030 | 3872.3844 |
| 2.7314 | 3807.5369 | 3855.9973 | 3854.3623 |
| 2.7424 | 3894.2906 | 3837.9919 | 3836.3401 |
| 2.7534 | 3831.5850 | 3821.5311 | 3818.3179 |
| 2.7644 | 3795.4941 | 3805.1464 | 3803.4603 |
| 2.7754 | 3715.4267 | 3790.3064 | 3788.6028 |
| 2.7864 | 3767.5772 | 3775.4667 | 3773.7452 |
| 2.7974 | 3850.4513 | 3760.6272 | 3758.8877 |
| 2.8084 | 3760.4056 | 3745.7881 | 3744.0301 |
| 2.8194 | 3737.1760 | 3730.9492 | 3729.1726 |
| 2.8304 | 3642.8953 | 3716.1106 | 3714.3150 |
| 2.8414 | 3705.0590 | 3701.2723 | 3699.4575 |
| 2.8524 | 3719.4641 | 3686.4343 | 3684.5999 |
| 2.8634 | 3777.5221 | 3671.5967 | 3669.7424 |
| 2.8744 | 3732.4213 | 3656.7594 | 3654.8848 |
| 2.8854 | 3629.7217 | 3641.9223 | 3640.0273 |
| 2.8964 | 3694.7035 | 3627.0857 | 3625.1697 |
| 2.9074 | 3637.5192 | 3612.2494 | 3610.3121 |
| 2.9184 | 3697.9203 | 3597.4134 | 3595.4546 |
| 2.9294 | 3460.7021 | 3582.5778 | 3580.5970 |
| 2.9404 | 3735.6386 | 3568.8963 | 3565.7395 |
| 2.9514 | 3433.1632 | 3555.2718 | 3553.2461 |
| 2.9624 | 3501.1681 | 3542.8014 | 3540.7526 |
| 2.9734 | 3487.6332 | 3530.3314 | 3528.2592 |
| 2.9844 | 3463.8171 | 3517.8618 | 3515.7658 |
| 2.9954 | 3486.4336 | 3505.3926 | 3503.2723 |
| 3.0064 | 3444.9194 | 3492.9239 | 3490.7789 |
| 3.0174 | 3423.4385 | 3480.4555 | 3478.2854 |
| 3.0284 | 3432.4277 | 3467.9877 | 3465.7920 |
| 3.0394 | 3434.7483 | 3455.5202 | 3453.2986 |
| 3.0504 | 3456.1086 | 3443.0532 | 3440.8051 |
| 3.0614 | 3396.7434 | 3430.5867 | 3428.3117 |
| 3.0724 | 3359.0349 | 3418.1207 | 3415.8183 |
| 3.0834 | 3393.9322 | 3405.6551 | 3403.3248 |
| 3.0944 | 3380.6991 | 3393.1901 | 3390.8314 |
| 3.1054 | 3376.2291 | 3380.7256 | 3378.3380 |
| 3.1164 | 3355.0329 | 3368.2616 | 3365.8445 |
| 3.1274 | 3312.1298 | 3356.2424 | 3353.3511 |
| 3.1384 | 3379.1588 | 3344.2455 | 3341.7679 |
| 3.1494 | 3368.4179 | 3332.6935 | 3330.1848 |
| 3.1604 | 3396.1814 | 3321.1420 | 3318.6017 |
| 3.1714 | 3359.0914 | 3309.5911 | 3307.0185 |
| 3.1824 | 3327.0614 | 3298.0409 | 3295.4354 |
| 3.1934 | 3284.5929 | 3286.4912 | 3283.8522 |
| 3.2044 | 3319.7891 | 3274.9423 | 3272.2691 |
| 3.2154 | 3274.7669 | 3263.3939 | 3260.6860 |
| 3.2264 | 3245.1151 | 3251.8463 | 3249.1028 |
| 3.2374 | 3242.3913 | 3240.2993 | 3237.5197 |
| 3.2484 | 3242.0000 | 3228.7531 | 3225.9365 |
| 3.2594 | 3287.9410 | 3217.2075 | 3214.3534 |
| 3.2704 | 3206.3161 | 3205.6627 | 3202.7702 |
| 3.2814 | 3157.6942 | 3194.1187 | 3191.1871 |
| 3.2924 | 3176.1062 | 3182.5755 | 3179.6040 |
| 3.3034 | 3157.9007 | 3171.0331 | 3168.0208 |
| 3.3144 | 3149.2847 | 3161.0594 | 3156.4377 |
| 3.3254 | 3185.0177 | 3151.1636 | 3148.0674 |
| 3.3364 | 3127.8633 | 3142.8366 | 3139.6971 |
| 3.3474 | 3069.9440 | 3134.5105 | 3131.3268 |
| 3.3584 | 3134.6770 | 3126.1853 | 3122.9565 |
| 3.3694 | 3125.7532 | 3117.8611 | 3114.5862 |
| 3.3804 | 3108.3181 | 3109.5379 | 3106.2160 |
| 3.3914 | 3131.7876 | 3101.2157 | 3097.8457 |
| 3.4024 | 3109.8058 | 3092.8945 | 3089.4754 |
| 3.4134 | 3038.1652 | 3084.5743 | 3081.1051 |
| 3.4244 | 3066.7980 | 3076.2553 | 3072.7348 |
| 3.4354 | 3075.9125 | 3067.9374 | 3064.3645 |
| 3.4464 | 3044.6278 | 3059.6207 | 3055.9942 |
| 3.4574 | 3052.3156 | 3051.3052 | 3047.6239 |
| 3.4684 | 3024.8215 | 3042.9910 | 3039.2537 |
| 3.4794 | 3034.4091 | 3034.6780 | 3030.8834 |
| 3.4904 | 3035.1770 | 3026.3663 | 3022.5131 |
| 3.5014 | 3036.4022 | 3018.0561 | 3014.1428 |
| 3.5124 | 3034.8451 | 3009.7472 | 3005.7725 |
| 3.5234 | 2963.0796 | 3001.4399 | 2997.4022 |
| 3.5344 | 3000.3034 | 2993.1340 | 2989.0319 |
| 3.5454 | 3010.7021 | 2984.8298 | 2980.6616 |
| 3.5564 | 2987.1401 | 2976.5272 | 2972.2914 |
| 3.5674 | 3000.3786 | 2968.2263 | 2963.9211 |
| 3.5784 | 2972.9071 | 2959.9271 | 2955.5508 |
| 3.5894 | 3068.2478 | 2951.6298 | 2947.1805 |
| 3.6004 | 2940.4306 | 2943.4004 | 2938.8102 |
| 3.6114 | 2895.2055 | 2935.1958 | 2930.4399 |
| 3.6224 | 2924.8510 | 2926.9398 | 2922.0696 |
| 3.6334 | 2929.5428 | 2918.6975 | 2913.6993 |
| 3.6444 | 2906.5531 | 2910.4138 | 2905.3291 |
| 3.6554 | 2910.4366 | 2902.1325 | 2896.9588 |
| 3.6664 | 2898.3048 | 2893.8538 | 2888.5885 |
| 3.6774 | 2836.9597 | 2885.5779 | 2880.2182 |
| 3.6884 | 2798.0619 | 2878.0872 | 2871.8479 |
| 3.6994 | 2927.9233 | 2870.6381 | 2865.0811 |
| 3.7104 | 2986.5403 | 2863.9745 | 2858.3144 |
| 3.7214 | 2857.9764 | 2857.3144 | 2851.5476 |
| 3.7324 | 2883.1878 | 2850.6577 | 2844.7808 |
| 3.7434 | 2815.3510 | 2844.0047 | 2838.0140 |
| 3.7544 | 2864.4395 | 2837.3556 | 2831.2473 |
| 3.7654 | 2895.9971 | 2830.7107 | 2824.4805 |
| 3.7764 | 2896.0211 | 2824.0702 | 2817.7137 |
| 3.7874 | 2872.2124 | 2817.4344 | 2810.9469 |
| 3.7984 | 2807.1342 | 2810.8035 | 2804.1802 |
| 3.8094 | 2846.0000 | 2804.1780 | 2797.4134 |
| 3.8204 | 2843.3658 | 2797.5580 | 2790.6466 |
| 3.8314 | 2757.2409 | 2790.9440 | 2783.8798 |
| 3.8424 | 2875.0034 | 2784.3365 | 2777.1131 |
| 3.8534 | 2751.7257 | 2777.7357 | 2770.3463 |
| 3.8644 | 2786.8318 | 2771.1422 | 2763.5795 |
| 3.8754 | 2738.5211 | 2764.5368 | 2756.8128 |
| 3.8864 | 2754.7124 | 2757.9387 | 2750.0057 |
| 3.8974 | 2753.0157 | 2751.3298 | 2743.1987 |
| 3.9084 | 2697.5703 | 2744.7303 | 2736.3917 |
| 3.9194 | 2745.7729 | 2738.1410 | 2729.5846 |
| 3.9304 | 2755.6042 | 2731.5623 | 2722.7776 |
| 3.9414 | 2716.7748 | 2724.9952 | 2715.9706 |
| 3.9524 | 2725.0324 | 2718.4404 | 2709.1635 |
| 3.9634 | 2716.1564 | 2711.8986 | 2702.3565 |
| 3.9744 | 2783.9926 | 2705.3708 | 2695.5495 |
| 3.9854 | 2725.0619 | 2698.8579 | 2688.7424 |
| 3.9964 | 2716.4179 | 2692.3608 | 2681.9354 |
| 4.0074 | 2691.2468 | 2685.8806 | 2675.1284 |
| 4.0184 | 2724.8245 | 2679.4184 | 2668.3213 |
| 4.0294 | 2650.5693 | 2672.9752 | 2661.5143 |
| 4.0404 | 2645.4154 | 2666.5523 | 2654.7073 |
| 4.0514 | 2642.0325 | 2660.1510 | 2647.9002 |
| 4.0624 | 2677.9007 | 2653.7724 | 2641.0932 |
| 4.0734 | 2629.5821 | 2647.4180 | 2634.2862 |
| 4.0844 | 2660.4381 | 2641.0891 | 2627.4792 |
| 4.0954 | 2709.8171 | 2634.7872 | 2620.6721 |
| 4.1064 | 2666.4223 | 2628.5138 | 2613.8651 |
| 4.1174 | 2696.6814 | 2622.2703 | 2607.0581 |
| 4.1284 | 2654.3879 | 2616.0584 | 2600.2510 |
| 4.1394 | 2603.6893 | 2609.8797 | 2593.4440 |
| 4.1504 | 2611.6357 | 2603.7358 | 2586.6370 |
| 4.1614 | 2630.7699 | 2597.6283 | 2579.8299 |
| 4.1724 | 2628.8156 | 2591.5590 | 2573.0229 |
| 4.1834 | 2614.8938 | 2585.5296 | 2566.2159 |
| 4.1944 | 2653.6224 | 2579.5416 | 2559.4088 |

Scan List

| Vis. | Dataset Name | Start pos. [°2θ] | End pos. [°2θ] | Step [°2θ] | Meas.Date/Time |
| --- | --- | --- | --- | --- | --- |
| * | 10 Etosha22 Crysub 4-10cm S1 heat550 | 2.0054 | 29.9894 | 0.0110 | 12/4/2023 3:33:30 PM |

Peak List

| Pos. [°2θ] | Height [cts] | FWHM Left [°2θ] | d-spacing [Å] | Rel. Int. [%] |
| --- | --- | --- | --- | --- |
| 4.8328 | 109.78 | 0.6927 | 18.27000 | 8.50 |
| 5.3381 | 163.59 | 0.1732 | 16.54183 | 12.66 |
| 8.7744 | 1291.92 | 0.1732 | 10.06975 | 100.00 |
| 10.6177 | 78.93 | 0.3031 | 8.32535 | 6.11 |
| 15.9751 | 458.89 | 0.1948 | 5.54338 | 35.52 |
| 17.6103 | 86.10 | 0.2598 | 5.03217 | 6.66 |
| 19.6939 | 54.72 | 0.5196 | 4.50422 | 4.24 |
| 26.2656 | 407.76 | 0.1732 | 3.39027 | 31.56 |
| 27.4637 | 211.58 | 0.6927 | 3.24503 | 16.38 |

Pattern List

| Visible | Ref.Code | Score | Compound Name | Chem. Formula | Mineral Name | SemiQuant[%] |
| --- | --- | --- | --- | --- | --- | --- |
| * | 01-076-6569 | 36 | Sodium Aluminum Silicate Hydrate | Na0.9 ( ( Al0.9 Si2 ) O6 ) ( H2 O ) | Analcime | 31 |
| * | 00-042-1339 | 33 | Potassium Magnesium Aluminum Silicate Hydroxide | K Mg3 ( Si3 Al ) O10 ( O H )2 | Phlogopite-2M1 | 51 |
| * | 04-025-4215 | 3 | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide | Mg10.4 V0.36 Mn33.5 Fe0.14 Al0.69 Si6.77 As6.5 P0.3 O54 ( O H )42 | Carlfrancisite | 18 |

Anchor Scan Parameters

Dataset Name	10 Etosha22 Crysub 4-10cm S1 heat550

File name	C:\aeris_data\XRD data\Goldstein\Etosha 2023\Etosha Clay Data\Sample 10\10 Etosha22 Crysub 4-10cm S1 heat550.xrdml

Sample Identification	10 Etosha22 Crysub 4-10cm S1 heat550

Measurement Start Date/Time	12/4/2023 3:33:30 PM

Operator	Instrument

Raw Data Origin	XRD measurement (*.XRDML)

Scan Axis	Gonio

Start Position [°2θ]	2.0054

End Position [°2θ]	29.9894

Step Size [°2θ]	0.0110

Scan Step Time [s]	48.1950

Scan Type	Continuous

PSD Mode	Scanning

PSD Length [°2θ]	5.54

Offset [°2θ]	0.0000

Divergence Slit Type	Fixed

Divergence Slit Size [°]	0.0603

Specimen Length [mm]	10.00

Measurement Temperature [°C]	25.00

Anode Material	Cu

K-α1 [Å]	1.54060

K-α2 [Å]	1.54443

K-β1 [Å]	1.39225

K-A2 / K-A1 Ratio	0.50000

Generator Settings	15 mA, 40 kV

Diffractometer Type	2082464

Diffractometer Number	0

Goniometer Radius [mm]	145.00

Dist. Focus-Diverg. Slit [mm]	95.00

Incident Beam Monochromator	No

Spinning	Yes