10 Etosha 22 CrySub 4-10 cm S1 GLYCOLATED

Graphics

Graphics

Graphics

Quantitative Results

Phase Potassium Iron Magnesium Aluminum Silicate Hydroxide

Weight fraction/ %	10.0

Phase Sodium Aluminum Silicate Hydrate

Weight fraction/ %	25.0

Phase Sodium Magnesium Silicon Oxide Hydrate

Weight fraction/ %	9.0

Phase Magnesium Silicate Hydroxide Hydrate

Weight fraction/ %	9.0

Phase Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide

Weight fraction/ %	46.0

Multiple Quantitative Results

Scans vs Phases Matrix

| Scan name | Potassium Iron Magnesium Aluminum Silicate Hydroxide | Sodium Aluminum Silicate Hydrate | Sodium Magnesium Silicon Oxide Hydrate | Magnesium Silicate Hydroxide Hydrate | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide |
| --- | --- | --- | --- | --- | --- |
| 10 Etosha22 crysub 4-10cm s1 glycola | 10.0 | 25.0 | 9.0 | 9.0 | 46.0 |

Anchor Scan Data

| Pos. [°2θ] | Iobs [cts] | Icalc [cts] | Iback [cts] |
| --- | --- | --- | --- |
| 2.0054 | 4484.0000 | 4484.0000 | 4484.0000 |
| 2.0164 | 4350.4022 | 4451.3882 | 4451.3882 |
| 2.0274 | 4223.2291 | 4418.7763 | 4418.7763 |
| 2.0384 | 4274.0649 | 4386.1645 | 4386.1645 |
| 2.0494 | 4319.3963 | 4353.5526 | 4353.5526 |
| 2.0604 | 4152.5698 | 4320.9408 | 4320.9408 |
| 2.0714 | 4142.2389 | 4288.3289 | 4288.3289 |
| 2.0824 | 4096.0324 | 4255.7171 | 4255.7171 |
| 2.0934 | 4105.0334 | 4223.1052 | 4223.1052 |
| 2.1044 | 4084.7876 | 4190.4934 | 4190.4934 |
| 2.1154 | 4071.0560 | 4157.8815 | 4157.8815 |
| 2.1264 | 4097.8368 | 4125.2697 | 4125.2697 |
| 2.1374 | 4085.6224 | 4092.6579 | 4092.6579 |
| 2.1484 | 4075.6662 | 4060.0460 | 4060.0460 |
| 2.1594 | 3978.6460 | 4027.4342 | 4027.4342 |
| 2.1704 | 4002.6593 | 3994.8223 | 3994.8223 |
| 2.1814 | 3984.4346 | 3962.2105 | 3962.2105 |
| 2.1924 | 3893.3727 | 3929.5986 | 3929.5986 |
| 2.2034 | 3918.1150 | 3909.9595 | 3909.9595 |
| 2.2144 | 3854.0895 | 3890.3204 | 3890.3204 |
| 2.2254 | 3912.5182 | 3870.6813 | 3870.6813 |
| 2.2364 | 3819.2581 | 3851.0422 | 3851.0422 |
| 2.2474 | 3800.5310 | 3831.4031 | 3831.4031 |
| 2.2584 | 3779.0964 | 3811.7639 | 3811.7639 |
| 2.2694 | 3807.2625 | 3792.1248 | 3792.1248 |
| 2.2804 | 3692.7601 | 3772.4857 | 3772.4857 |
| 2.2914 | 3710.2370 | 3752.8466 | 3752.8466 |
| 2.3024 | 3718.9823 | 3733.2075 | 3733.2075 |
| 2.3134 | 3697.7473 | 3713.5684 | 3713.5684 |
| 2.3244 | 3659.4656 | 3693.9293 | 3693.9293 |
| 2.3354 | 3668.8761 | 3674.2901 | 3674.2901 |
| 2.3464 | 3636.3343 | 3654.6510 | 3654.6510 |
| 2.3574 | 3621.0079 | 3635.0119 | 3635.0119 |
| 2.3684 | 3600.2242 | 3615.3728 | 3615.3728 |
| 2.3794 | 3603.1052 | 3595.7337 | 3595.7337 |
| 2.3904 | 3572.2793 | 3582.0204 | 3582.0204 |
| 2.4014 | 3581.5044 | 3568.3072 | 3568.3072 |
| 2.4124 | 3562.3471 | 3554.5939 | 3554.5939 |
| 2.4234 | 3501.9164 | 3540.8807 | 3540.8807 |
| 2.4344 | 3504.8850 | 3527.1674 | 3527.1674 |
| 2.4454 | 3482.3609 | 3513.4541 | 3513.4541 |
| 2.4564 | 3459.7321 | 3499.7409 | 3499.7409 |
| 2.4674 | 3475.0619 | 3486.0276 | 3486.0276 |
| 2.4784 | 3469.3992 | 3472.3144 | 3472.3144 |
| 2.4894 | 3389.4710 | 3458.6011 | 3458.6011 |
| 2.5004 | 3450.9558 | 3444.8879 | 3444.8879 |
| 2.5114 | 3401.6912 | 3431.1746 | 3431.1746 |
| 2.5224 | 3367.8073 | 3417.4613 | 3417.4613 |
| 2.5334 | 3405.4513 | 3403.7481 | 3403.7481 |
| 2.5444 | 3309.9105 | 3390.0348 | 3390.0348 |
| 2.5554 | 3318.6116 | 3376.3216 | 3376.3216 |
| 2.5664 | 3386.7153 | 3362.6083 | 3362.6083 |
| 2.5774 | 3396.6912 | 3355.8451 | 3355.8451 |
| 2.5884 | 3377.0172 | 3349.0818 | 3349.0818 |
| 2.5994 | 3350.4159 | 3342.3186 | 3342.3186 |
| 2.6104 | 3356.5482 | 3335.5554 | 3335.5554 |
| 2.6214 | 3343.3510 | 3328.7921 | 3328.7921 |
| 2.6324 | 3344.5089 | 3322.0289 | 3322.0289 |
| 2.6434 | 3269.8702 | 3315.2657 | 3315.2657 |
| 2.6544 | 3243.8014 | 3308.5024 | 3308.5024 |
| 2.6654 | 3250.4248 | 3301.7392 | 3301.7392 |
| 2.6764 | 3204.0157 | 3294.9759 | 3294.9759 |
| 2.6874 | 3201.7168 | 3288.2127 | 3288.2127 |
| 2.6984 | 3222.2611 | 3281.4495 | 3281.4495 |
| 2.7094 | 3188.4553 | 3274.6862 | 3274.6862 |
| 2.7204 | 3175.6032 | 3267.9230 | 3267.9230 |
| 2.7314 | 3295.8702 | 3261.1598 | 3261.1598 |
| 2.7424 | 3290.2365 | 3254.3965 | 3254.3965 |
| 2.7534 | 3259.5978 | 3247.6287 | 3247.6333 |
| 2.7644 | 3205.8112 | 3240.8313 | 3240.8313 |
| 2.7754 | 3169.4680 | 3234.0292 | 3234.0292 |
| 2.7864 | 3144.0560 | 3227.2272 | 3227.2272 |
| 2.7974 | 3214.4513 | 3220.4252 | 3220.4252 |
| 2.8084 | 3213.2330 | 3213.6232 | 3213.6232 |
| 2.8194 | 3205.6332 | 3206.8211 | 3206.8211 |
| 2.8304 | 3185.6416 | 3200.0191 | 3200.0191 |
| 2.8414 | 3211.0895 | 3193.2171 | 3193.2171 |
| 2.8524 | 3276.4095 | 3186.4151 | 3186.4151 |
| 2.8634 | 3153.4513 | 3179.6130 | 3179.6130 |
| 2.8744 | 3119.8412 | 3172.8110 | 3172.8110 |
| 2.8854 | 3203.5625 | 3166.0090 | 3166.0090 |
| 2.8964 | 3167.1681 | 3159.2070 | 3159.2070 |
| 2.9074 | 3208.3619 | 3152.4049 | 3152.4049 |
| 2.9184 | 3253.5767 | 3145.6029 | 3145.6029 |
| 2.9294 | 3230.3068 | 3138.8009 | 3138.8009 |
| 2.9404 | 3148.1209 | 3131.9691 | 3131.9989 |
| 2.9514 | 3106.1750 | 3125.1155 | 3125.1155 |
| 2.9624 | 3075.1681 | 3118.2322 | 3118.2322 |
| 2.9734 | 3062.8574 | 3111.3488 | 3111.3488 |
| 2.9844 | 3060.1416 | 3104.4655 | 3104.4655 |
| 2.9954 | 3146.3186 | 3097.5821 | 3097.5821 |
| 3.0064 | 3054.6352 | 3090.6988 | 3090.6988 |
| 3.0174 | 3104.1308 | 3083.8155 | 3083.8155 |
| 3.0284 | 3106.8599 | 3076.9321 | 3076.9321 |
| 3.0394 | 3109.1445 | 3070.0488 | 3070.0488 |
| 3.0504 | 3059.6588 | 3063.1654 | 3063.1654 |
| 3.0614 | 3040.4041 | 3056.2821 | 3056.2821 |
| 3.0724 | 3018.5630 | 3049.3988 | 3049.3988 |
| 3.0834 | 3153.6834 | 3042.5154 | 3042.5154 |
| 3.0944 | 3103.4204 | 3035.6321 | 3035.6321 |
| 3.1054 | 3117.9597 | 3028.7487 | 3028.7487 |
| 3.1164 | 3092.5511 | 3021.8654 | 3021.8654 |
| 3.1274 | 3058.3894 | 3014.9821 | 3014.9821 |
| 3.1384 | 3032.0103 | 3008.0987 | 3008.0987 |
| 3.1494 | 3041.3137 | 3001.2154 | 3001.2154 |
| 3.1604 | 3075.1136 | 2994.3320 | 2994.3320 |
| 3.1714 | 3042.3255 | 2987.4487 | 2987.4487 |
| 3.1824 | 3055.9823 | 2980.5654 | 2980.5654 |
| 3.1934 | 3053.3806 | 2973.6820 | 2973.6820 |
| 3.2044 | 3072.0221 | 2966.7987 | 2966.7987 |
| 3.2154 | 3004.7935 | 2959.9153 | 2959.9153 |
| 3.2264 | 3016.7256 | 2953.0320 | 2953.0320 |
| 3.2374 | 2951.5959 | 2946.1487 | 2946.1487 |
| 3.2484 | 2969.1667 | 2939.2653 | 2939.2653 |
| 3.2594 | 2932.7847 | 2932.3820 | 2932.3820 |
| 3.2704 | 2964.2798 | 2925.4986 | 2925.4986 |
| 3.2814 | 2982.1072 | 2918.6153 | 2918.6153 |
| 3.2924 | 2944.5797 | 2911.7320 | 2911.7320 |
| 3.3034 | 2959.7483 | 2904.8486 | 2904.8486 |
| 3.3144 | 2969.0285 | 2897.9355 | 2897.9653 |
| 3.3254 | 2970.1770 | 2891.0006 | 2891.0006 |
| 3.3364 | 2927.2542 | 2884.0360 | 2884.0360 |
| 3.3474 | 2871.5251 | 2877.0713 | 2877.0713 |
| 3.3584 | 2914.5812 | 2870.1066 | 2870.1066 |
| 3.3694 | 2988.9095 | 2863.1420 | 2863.1420 |
| 3.3804 | 2911.1789 | 2856.1773 | 2856.1773 |
| 3.3914 | 2822.1858 | 2849.2127 | 2849.2127 |
| 3.4024 | 2829.6337 | 2842.2480 | 2842.2480 |
| 3.4134 | 2896.5929 | 2835.2834 | 2835.2834 |
| 3.4244 | 2891.0841 | 2828.3187 | 2828.3187 |
| 3.4354 | 2802.0098 | 2821.3541 | 2821.3541 |
| 3.4464 | 2894.1775 | 2814.3894 | 2814.3894 |
| 3.4574 | 2923.2271 | 2807.4247 | 2807.4247 |
| 3.4684 | 2845.5703 | 2800.4601 | 2800.4601 |
| 3.4794 | 2805.1190 | 2793.4954 | 2793.4954 |
| 3.4904 | 2843.8098 | 2786.5308 | 2786.5308 |
| 3.5014 | 2800.1701 | 2780.5551 | 2779.5661 |
| 3.5124 | 2723.2320 | 2775.3072 | 2775.3072 |
| 3.5234 | 2755.9086 | 2771.0483 | 2771.0483 |
| 3.5344 | 2878.1839 | 2766.7894 | 2766.7894 |
| 3.5454 | 2944.9469 | 2762.5305 | 2762.5305 |
| 3.5564 | 2913.9498 | 2758.2716 | 2758.2716 |
| 3.5674 | 2909.4346 | 2754.0127 | 2754.0127 |
| 3.5784 | 2811.4788 | 2749.7538 | 2749.7538 |
| 3.5894 | 2826.7345 | 2745.4949 | 2745.4949 |
| 3.6004 | 2780.7704 | 2741.2360 | 2741.2360 |
| 3.6114 | 2812.4641 | 2736.9771 | 2736.9771 |
| 3.6224 | 2810.4779 | 2732.7181 | 2732.7181 |
| 3.6334 | 2826.6578 | 2728.4592 | 2728.4592 |
| 3.6444 | 2702.1381 | 2724.2003 | 2724.2003 |
| 3.6554 | 2852.3245 | 2719.9414 | 2719.9414 |
| 3.6664 | 2814.8122 | 2715.6825 | 2715.6825 |
| 3.6774 | 2786.5034 | 2711.4236 | 2711.4236 |
| 3.6884 | 2760.2257 | 2707.1334 | 2707.1647 |
| 3.6994 | 2814.1406 | 2702.8202 | 2702.8202 |
| 3.7104 | 2750.4012 | 2698.4756 | 2698.4756 |
| 3.7214 | 2782.4484 | 2694.1311 | 2694.1311 |
| 3.7324 | 2691.1711 | 2689.7866 | 2689.7866 |
| 3.7434 | 2726.3894 | 2685.4420 | 2685.4420 |
| 3.7544 | 2727.0914 | 2681.0975 | 2681.0975 |
| 3.7654 | 2839.1220 | 2676.7530 | 2676.7530 |
| 3.7764 | 2812.6553 | 2672.4084 | 2672.4084 |
| 3.7874 | 2773.3451 | 2668.0639 | 2668.0639 |
| 3.7984 | 2758.9862 | 2663.7194 | 2663.7194 |
| 3.8094 | 2756.0069 | 2659.3748 | 2659.3748 |
| 3.8204 | 2817.0103 | 2655.0303 | 2655.0303 |
| 3.8314 | 2746.9518 | 2650.6858 | 2650.6858 |
| 3.8424 | 2723.0521 | 2646.3412 | 2646.3412 |
| 3.8534 | 2744.9853 | 2641.9967 | 2641.9967 |
| 3.8644 | 2789.5438 | 2637.6522 | 2637.6522 |
| 3.8754 | 2801.7365 | 2633.2761 | 2633.3076 |
| 3.8864 | 2733.8274 | 2628.8768 | 2628.8768 |
| 3.8974 | 2707.8358 | 2624.4460 | 2624.4460 |
| 3.9084 | 2777.4695 | 2620.0152 | 2620.0152 |
| 3.9194 | 2686.2891 | 2615.5845 | 2615.5845 |
| 3.9304 | 2743.0944 | 2611.1537 | 2611.1537 |
| 3.9414 | 2740.7748 | 2606.7229 | 2606.7229 |
| 3.9524 | 2761.1431 | 2602.2921 | 2602.2921 |
| 3.9634 | 2769.7168 | 2597.8613 | 2597.8613 |
| 3.9744 | 2726.6220 | 2593.4305 | 2593.4305 |
| 3.9854 | 2877.3893 | 2588.9997 | 2588.9997 |
| 3.9964 | 2765.1140 | 2584.5689 | 2584.5689 |
| 4.0074 | 2738.8201 | 2580.1381 | 2580.1381 |
| 4.0184 | 2760.5103 | 2575.7073 | 2575.7073 |
| 4.0294 | 2752.0924 | 2571.2765 | 2571.2765 |
| 4.0404 | 2742.1170 | 2567.0000 | 2566.8458 |
| 4.0514 | 2725.7522 | 2563.6218 | 2562.4150 |
| 4.0624 | 2780.1519 | 2559.6590 | 2557.9842 |
| 4.0734 | 2774.0895 | 2555.2083 | 2553.4661 |
| 4.0844 | 2771.3008 | 2550.7206 | 2548.9480 |
| 4.0954 | 2675.9410 | 2546.2338 | 2544.4299 |
| 4.1064 | 2692.4971 | 2541.7478 | 2539.9118 |
| 4.1174 | 2736.8879 | 2537.2626 | 2535.3937 |
| 4.1284 | 2733.0782 | 2532.7784 | 2530.8756 |
| 4.1394 | 2774.7787 | 2528.2950 | 2526.3575 |
| 4.1504 | 2739.9676 | 2523.8127 | 2521.8394 |
| 4.1614 | 2726.7748 | 2519.3313 | 2517.3213 |
| 4.1724 | 2772.3127 | 2514.8509 | 2512.8032 |
| 4.1834 | 2844.8141 | 2510.3717 | 2508.2851 |
| 4.1944 | 2797.2979 | 2505.8935 | 2503.7670 |

Scan List

| Vis. | Dataset Name | Start pos. [°2θ] | End pos. [°2θ] | Step [°2θ] | Meas.Date/Time |
| --- | --- | --- | --- | --- | --- |
| * | 10 Etosha22 crysub 4-10cm s1 glycola | 2.0054 | 29.9894 | 0.0110 | 12/5/2023 9:18:46 AM |

Peak List

| Pos. [°2θ] | Height [cts] | FWHM Left [°2θ] | d-spacing [Å] | Rel. Int. [%] |
| --- | --- | --- | --- | --- |
| 5.3413 | 1185.99 | 0.1299 | 16.53192 | 58.38 |
| 7.1249 | 2031.62 | 0.1082 | 12.39682 | 100.00 |
| 8.8275 | 790.43 | 0.1948 | 10.00927 | 38.91 |
| 13.2809 | 20.19 | 0.5196 | 6.66126 | 0.99 |
| 15.8435 | 909.31 | 0.0866 | 5.58913 | 44.76 |
| 17.6907 | 83.41 | 0.3464 | 5.00950 | 4.11 |
| 18.3040 | 162.16 | 0.1082 | 4.84300 | 7.98 |
| 19.5252 | 79.80 | 0.7793 | 4.54277 | 3.93 |
| 23.4783 | 38.69 | 0.3464 | 3.78606 | 1.90 |
| 26.0179 | 1050.98 | 0.0866 | 3.42198 | 51.73 |
| 26.8050 | 334.24 | 0.2598 | 3.32326 | 16.45 |

Pattern List

| Visible | Ref.Code | Score | Compound Name | Chem. Formula | Mineral Name | SemiQuant[%] |
| --- | --- | --- | --- | --- | --- | --- |
| * | 00-042-1437 | 47 | Potassium Iron Magnesium Aluminum Silicate Hydroxide | K ( Mg , Fe )3 ( Al , Fe ) Si3 O10 ( O H , F )2 | Phlogopite-1M, Fe+2-bearing | 10 |
| * | 01-075-8690 | 69 | Sodium Aluminum Silicate Hydrate | Na1.71 ( ( Al1.806 Si4.194 ) O12 ) ( H2 O )2.16 | Analcime | 25 |
| * | 01-082-8023 | 17 | Sodium Magnesium Silicon Oxide Hydrate | Na2 Mg3 ( Si6 O16 ) ( H2 O )7 | Loughlinite | 9 |
| * | 01-080-5019 | 20 | Magnesium Silicate Hydroxide Hydrate | Mg7.68 ( Si12 O30 ) ( O H )4 ( H2 O )4 ( H2 O )6 | Sepiolite | 9 |
| * | 04-025-4215 | 4 | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide | Mg10.4 V0.36 Mn33.5 Fe0.14 Al0.69 Si6.77 As6.5 P0.3 O54 ( O H )42 | Carlfrancisite | 46 |

Anchor Scan Parameters

Dataset Name	10 Etosha22 crysub 4-10cm s1 glycola

File name	C:\aeris_data\XRD data\Goldstein\Etosha 2023\Etosha Clay Data\Sample 10\10 Etosha22 crysub 4-10cm s1 glycola.xrdml

Sample Identification	10 Etosha22 crysub 4-10cm s1 glycola

Measurement Start Date/Time	12/5/2023 9:18:46 AM

Operator	Instrument

Raw Data Origin	XRD measurement (*.XRDML)

Scan Axis	Gonio

Start Position [°2θ]	2.0054

End Position [°2θ]	29.9894

Step Size [°2θ]	0.0110

Scan Step Time [s]	48.1950

Scan Type	Continuous

PSD Mode	Scanning

PSD Length [°2θ]	5.54

Offset [°2θ]	0.0000

Divergence Slit Type	Fixed

Divergence Slit Size [°]	0.0603

Specimen Length [mm]	10.00

Measurement Temperature [°C]	25.00

Anode Material	Cu

K-α1 [Å]	1.54060

K-α2 [Å]	1.54443

K-β1 [Å]	1.39225

K-A2 / K-A1 Ratio	0.50000

Generator Settings	15 mA, 40 kV

Diffractometer Type	2082464

Diffractometer Number	0

Goniometer Radius [mm]	145.00

Dist. Focus-Diverg. Slit [mm]	95.00

Incident Beam Monochromator	No

Spinning	Yes