10 Etosha 22 CrySub 4-10 cm S1 REGULAR

Graphics

Graphics

Graphics

Quantitative Results

Phase Sodium Aluminum Silicate Hydrate

Weight fraction/ %	20.0

Phase Potassium Iron Magnesium Aluminum Silicate Hydroxide

Weight fraction/ %	9.0

Phase Magnesium Silicate Hydroxide Hydrate

Weight fraction/ %	19.0

Phase Potassium Manganese Silicate Hydroxide Hydrate

Weight fraction/ %	27.0

Phase Sodium Magnesium Silicon Oxide Hydrate

Weight fraction/ %	25.0

Multiple Quantitative Results

Scans vs Phases Matrix

| Scan name | Sodium Aluminum Silicate Hydrate | Potassium Iron Magnesium Aluminum Silicate Hydroxide | Magnesium Silicate Hydroxide Hydrate | Potassium Manganese Silicate Hydroxide Hydrate | Sodium Magnesium Silicon Oxide Hydrate |
| --- | --- | --- | --- | --- | --- |
| 10 Etosha22 CrySub 4-10cm S1 | 20.0 | 9.0 | 19.0 | 27.0 | 25.0 |

Anchor Scan Data

| Pos. [°2θ] | Iobs [cts] | Icalc [cts] | Iback [cts] |
| --- | --- | --- | --- |
| 2.0054 | 4797.0000 | 4797.0000 | 4797.0000 |
| 2.0164 | 4614.8033 | 4762.2329 | 4762.2329 |
| 2.0274 | 4598.3117 | 4727.4659 | 4727.4659 |
| 2.0384 | 4567.9395 | 4692.6988 | 4692.6988 |
| 2.0494 | 4492.2773 | 4657.9318 | 4657.9318 |
| 2.0604 | 4578.5030 | 4623.1647 | 4623.1647 |
| 2.0714 | 4611.6460 | 4588.3977 | 4588.3977 |
| 2.0824 | 4353.5910 | 4553.6306 | 4553.6306 |
| 2.0934 | 4337.1445 | 4518.8636 | 4518.8636 |
| 2.1044 | 4398.7655 | 4484.0965 | 4484.0965 |
| 2.1154 | 4250.4818 | 4449.3295 | 4449.3295 |
| 2.1264 | 4450.2886 | 4414.5624 | 4414.5624 |
| 2.1374 | 4321.8083 | 4379.7953 | 4379.7953 |
| 2.1484 | 4241.0305 | 4345.0283 | 4345.0283 |
| 2.1594 | 4276.6234 | 4310.2612 | 4310.2612 |
| 2.1704 | 4250.2729 | 4275.4942 | 4275.4942 |
| 2.1814 | 4178.3392 | 4240.7271 | 4240.7271 |
| 2.1924 | 4234.9405 | 4205.9601 | 4205.9601 |
| 2.2034 | 4196.2920 | 4183.2778 | 4183.2778 |
| 2.2144 | 4143.1018 | 4160.5956 | 4160.5956 |
| 2.2254 | 4158.1121 | 4137.9133 | 4137.9133 |
| 2.2364 | 4149.7035 | 4115.2311 | 4115.2311 |
| 2.2474 | 4046.4287 | 4092.5488 | 4092.5488 |
| 2.2584 | 4042.3963 | 4069.8666 | 4069.8666 |
| 2.2694 | 4066.8909 | 4047.1843 | 4047.1843 |
| 2.2804 | 4021.6981 | 4024.5020 | 4024.5020 |
| 2.2914 | 4001.1347 | 4001.8198 | 4001.8198 |
| 2.3024 | 3959.4159 | 3979.1375 | 3979.1375 |
| 2.3134 | 3905.1367 | 3956.4553 | 3956.4553 |
| 2.3244 | 3895.0993 | 3933.7730 | 3933.7730 |
| 2.3354 | 3895.9144 | 3911.0908 | 3911.0908 |
| 2.3464 | 3872.0556 | 3888.4085 | 3888.4085 |
| 2.3574 | 3883.3963 | 3865.7263 | 3865.7263 |
| 2.3684 | 3871.2817 | 3843.0440 | 3843.0440 |
| 2.3794 | 3866.0639 | 3820.3618 | 3820.3618 |
| 2.3904 | 3716.2075 | 3806.3767 | 3806.3767 |
| 2.4014 | 3744.7522 | 3792.3916 | 3792.3916 |
| 2.4124 | 3712.8899 | 3778.4066 | 3778.4066 |
| 2.4234 | 3687.0177 | 3764.4215 | 3764.4215 |
| 2.4344 | 3697.0988 | 3750.4365 | 3750.4365 |
| 2.4454 | 3729.1976 | 3736.4514 | 3736.4514 |
| 2.4564 | 3705.4336 | 3722.4664 | 3722.4664 |
| 2.4674 | 3664.9735 | 3708.4813 | 3708.4813 |
| 2.4784 | 3645.3766 | 3694.4963 | 3694.4963 |
| 2.4894 | 3616.6018 | 3680.5112 | 3680.5112 |
| 2.5004 | 3619.5973 | 3666.5261 | 3666.5261 |
| 2.5114 | 3687.1967 | 3652.5411 | 3652.5411 |
| 2.5224 | 3594.8033 | 3638.5560 | 3638.5560 |
| 2.5334 | 3533.3776 | 3624.5710 | 3624.5710 |
| 2.5444 | 3551.3412 | 3610.5859 | 3610.5859 |
| 2.5554 | 3612.2881 | 3596.6009 | 3596.6009 |
| 2.5664 | 3620.6431 | 3582.6158 | 3582.6158 |
| 2.5774 | 3552.3432 | 3576.0109 | 3576.0109 |
| 2.5884 | 3539.6799 | 3569.4060 | 3569.4060 |
| 2.5994 | 3612.0443 | 3562.8011 | 3562.8011 |
| 2.6104 | 3576.7232 | 3556.1962 | 3556.1962 |
| 2.6214 | 3556.3894 | 3549.5913 | 3549.5913 |
| 2.6324 | 3574.6106 | 3542.9864 | 3542.9864 |
| 2.6434 | 3536.5143 | 3536.3815 | 3536.3815 |
| 2.6544 | 3548.0069 | 3529.7766 | 3529.7766 |
| 2.6654 | 3538.3510 | 3523.1717 | 3523.1717 |
| 2.6764 | 3487.5143 | 3516.5668 | 3516.5668 |
| 2.6874 | 3505.0059 | 3509.9619 | 3509.9619 |
| 2.6984 | 3619.5354 | 3503.3571 | 3503.3571 |
| 2.7094 | 3527.2861 | 3496.7522 | 3496.7522 |
| 2.7204 | 3474.8260 | 3490.1473 | 3490.1473 |
| 2.7314 | 3440.7965 | 3483.5424 | 3483.5424 |
| 2.7424 | 3451.2935 | 3476.9375 | 3476.9375 |
| 2.7534 | 3559.4740 | 3470.3326 | 3470.3326 |
| 2.7644 | 3522.3304 | 3463.6549 | 3463.6549 |
| 2.7754 | 3419.0796 | 3456.9773 | 3456.9773 |
| 2.7864 | 3410.1087 | 3450.2997 | 3450.2997 |
| 2.7974 | 3454.3628 | 3443.6221 | 3443.6221 |
| 2.8084 | 3462.6917 | 3436.9444 | 3436.9444 |
| 2.8194 | 3362.9508 | 3430.2668 | 3430.2668 |
| 2.8304 | 3445.1829 | 3423.5892 | 3423.5892 |
| 2.8414 | 3501.5742 | 3416.9116 | 3416.9116 |
| 2.8524 | 3424.5551 | 3410.2339 | 3410.2339 |
| 2.8634 | 3426.7109 | 3403.5563 | 3403.5563 |
| 2.8744 | 3370.6824 | 3396.8787 | 3396.8787 |
| 2.8854 | 3389.6490 | 3390.2010 | 3390.2010 |
| 2.8964 | 3255.5973 | 3383.5234 | 3383.5234 |
| 2.9074 | 3357.6067 | 3376.8458 | 3376.8458 |
| 2.9184 | 3309.5118 | 3370.1682 | 3370.1682 |
| 2.9294 | 3382.0590 | 3363.4905 | 3363.4905 |
| 2.9404 | 3355.5211 | 3356.8129 | 3356.8129 |
| 2.9514 | 3384.4641 | 3350.1353 | 3350.1353 |
| 2.9624 | 3335.1505 | 3343.4577 | 3343.4577 |
| 2.9734 | 3449.7571 | 3336.7800 | 3336.7800 |
| 2.9844 | 3363.2916 | 3330.1024 | 3330.1024 |
| 2.9954 | 3419.4336 | 3323.4248 | 3323.4248 |
| 3.0064 | 3373.1799 | 3316.7471 | 3316.7471 |
| 3.0174 | 3307.4149 | 3310.0695 | 3310.0695 |
| 3.0284 | 3271.7360 | 3303.3919 | 3303.3919 |
| 3.0394 | 3350.9892 | 3296.7143 | 3296.7143 |
| 3.0504 | 3301.1617 | 3290.0366 | 3290.0366 |
| 3.0614 | 3287.1032 | 3283.3590 | 3283.3590 |
| 3.0724 | 3239.5010 | 3276.6814 | 3276.6814 |
| 3.0834 | 3243.5212 | 3270.0037 | 3270.0037 |
| 3.0944 | 3294.1460 | 3263.3261 | 3263.3261 |
| 3.1054 | 3265.4395 | 3256.6485 | 3256.6485 |
| 3.1164 | 3242.4140 | 3249.9709 | 3249.9709 |
| 3.1274 | 3231.7345 | 3243.2932 | 3243.2932 |
| 3.1384 | 3210.1834 | 3238.7113 | 3238.7113 |
| 3.1494 | 3294.5477 | 3234.1293 | 3234.1293 |
| 3.1604 | 3264.1136 | 3229.5474 | 3229.5474 |
| 3.1714 | 3203.7660 | 3224.9654 | 3224.9654 |
| 3.1824 | 3206.9263 | 3220.3835 | 3220.3835 |
| 3.1934 | 3255.2035 | 3215.8015 | 3215.8015 |
| 3.2044 | 3188.5644 | 3211.2195 | 3211.2195 |
| 3.2154 | 3176.9440 | 3206.6376 | 3206.6376 |
| 3.2264 | 3204.8732 | 3202.0556 | 3202.0556 |
| 3.2374 | 3225.7424 | 3197.4737 | 3197.4737 |
| 3.2484 | 3189.5556 | 3192.8917 | 3192.8917 |
| 3.2594 | 3148.6076 | 3188.3098 | 3188.3098 |
| 3.2704 | 3112.1937 | 3183.7278 | 3183.7278 |
| 3.2814 | 3216.8820 | 3179.1459 | 3179.1459 |
| 3.2924 | 3185.3672 | 3174.5639 | 3174.5639 |
| 3.3034 | 3155.4317 | 3169.9819 | 3169.9819 |
| 3.3144 | 3182.8682 | 3165.4000 | 3165.4000 |
| 3.3254 | 3142.7021 | 3160.8404 | 3160.8404 |
| 3.3364 | 3135.7955 | 3156.2808 | 3156.2808 |
| 3.3474 | 3111.0324 | 3151.7212 | 3151.7212 |
| 3.3584 | 3076.9764 | 3147.1616 | 3147.1616 |
| 3.3694 | 3116.8791 | 3142.6020 | 3142.6020 |
| 3.3804 | 3162.0457 | 3138.0424 | 3138.0424 |
| 3.3914 | 3119.6194 | 3133.4828 | 3133.4828 |
| 3.4024 | 3105.9263 | 3128.9232 | 3128.9232 |
| 3.4134 | 3081.7129 | 3124.3636 | 3124.3636 |
| 3.4244 | 3055.6121 | 3119.8040 | 3119.8040 |
| 3.4354 | 3087.3048 | 3115.2444 | 3115.2444 |
| 3.4464 | 3067.7822 | 3110.6848 | 3110.6848 |
| 3.4574 | 3054.5811 | 3106.1252 | 3106.1252 |
| 3.4684 | 3113.6809 | 3101.5656 | 3101.5656 |
| 3.4794 | 3101.9449 | 3097.0060 | 3097.0060 |
| 3.4904 | 3081.6372 | 3092.4464 | 3092.4464 |
| 3.5014 | 3127.9961 | 3087.8868 | 3087.8868 |
| 3.5124 | 3157.5226 | 3083.3272 | 3083.3272 |
| 3.5234 | 3099.7374 | 3078.7676 | 3078.7676 |
| 3.5344 | 3136.7611 | 3074.2080 | 3074.2080 |
| 3.5454 | 3043.3559 | 3069.6484 | 3069.6484 |
| 3.5564 | 3076.9012 | 3065.0888 | 3065.0888 |
| 3.5674 | 3024.7591 | 3060.5292 | 3060.5292 |
| 3.5784 | 2995.4848 | 3055.9696 | 3055.9696 |
| 3.5894 | 2983.4513 | 3051.4100 | 3051.4100 |
| 3.6004 | 3048.8338 | 3046.8504 | 3046.8504 |
| 3.6114 | 2948.8259 | 3042.2908 | 3042.2908 |
| 3.6224 | 2967.2139 | 3037.7312 | 3037.7312 |
| 3.6334 | 3050.2596 | 3033.1716 | 3033.1716 |
| 3.6444 | 2995.3338 | 3028.6120 | 3028.6120 |
| 3.6554 | 3023.1829 | 3024.0524 | 3024.0524 |
| 3.6664 | 3063.5261 | 3019.4928 | 3019.4928 |
| 3.6774 | 3036.0069 | 3014.9332 | 3014.9332 |
| 3.6884 | 2948.2301 | 3010.3736 | 3010.3736 |
| 3.6994 | 3041.4602 | 3007.0760 | 3007.0760 |
| 3.7104 | 2987.0216 | 3003.7784 | 3003.7784 |
| 3.7214 | 3047.8879 | 3000.4808 | 3000.4808 |
| 3.7324 | 3004.7261 | 2997.1832 | 2997.1832 |
| 3.7434 | 3015.1298 | 2993.8857 | 2993.8857 |
| 3.7544 | 2988.3260 | 2990.5881 | 2990.5881 |
| 3.7654 | 3082.6903 | 2987.2905 | 2987.2905 |
| 3.7764 | 2926.4459 | 2983.9929 | 2983.9929 |
| 3.7874 | 2927.9558 | 2980.6953 | 2980.6953 |
| 3.7984 | 3040.6971 | 2977.3977 | 2977.3977 |
| 3.8094 | 2953.4248 | 2974.1002 | 2974.1002 |
| 3.8204 | 2977.7020 | 2970.8026 | 2970.8026 |
| 3.8314 | 2901.0236 | 2967.5050 | 2967.5050 |
| 3.8424 | 2972.8422 | 2964.2074 | 2964.2074 |
| 3.8534 | 2971.6873 | 2960.9098 | 2960.9098 |
| 3.8644 | 2986.5059 | 2957.6122 | 2957.6122 |
| 3.8754 | 2885.7060 | 2954.3147 | 2954.3147 |
| 3.8864 | 3003.6017 | 2950.9742 | 2950.9742 |
| 3.8974 | 2923.1888 | 2947.6337 | 2947.6337 |
| 3.9084 | 3072.7979 | 2944.2933 | 2944.2933 |
| 3.9194 | 3013.7109 | 2940.9528 | 2940.9528 |
| 3.9304 | 2955.5472 | 2937.6124 | 2937.6124 |
| 3.9414 | 2946.7974 | 2934.2719 | 2934.2719 |
| 3.9524 | 2920.0900 | 2930.9315 | 2930.9315 |
| 3.9634 | 2954.8928 | 2927.5910 | 2927.5910 |
| 3.9744 | 2981.1897 | 2924.2505 | 2924.2505 |
| 3.9854 | 2896.7257 | 2920.9101 | 2920.9101 |
| 3.9964 | 2898.9651 | 2917.5696 | 2917.5696 |
| 4.0074 | 2942.6687 | 2914.2292 | 2914.2292 |
| 4.0184 | 2986.3082 | 2910.8887 | 2910.8887 |
| 4.0294 | 2947.9243 | 2907.5483 | 2907.5483 |
| 4.0404 | 2959.6248 | 2904.2078 | 2904.2078 |
| 4.0514 | 2879.2095 | 2900.8673 | 2900.8673 |
| 4.0624 | 2938.2831 | 2897.5533 | 2897.5269 |
| 4.0734 | 2845.8683 | 2894.3308 | 2894.3308 |
| 4.0844 | 2907.7566 | 2891.1347 | 2891.1347 |
| 4.0954 | 2892.4061 | 2887.9386 | 2887.9386 |
| 4.1064 | 2944.8073 | 2884.7425 | 2884.7425 |
| 4.1174 | 2955.6135 | 2881.5464 | 2881.5464 |
| 4.1284 | 2918.8452 | 2878.3503 | 2878.3503 |
| 4.1394 | 2922.5614 | 2875.1542 | 2875.1542 |
| 4.1504 | 2831.7773 | 2871.9581 | 2871.9581 |
| 4.1614 | 2867.0875 | 2868.7620 | 2868.7620 |
| 4.1724 | 2887.9838 | 2865.5659 | 2865.5659 |
| 4.1834 | 2841.5575 | 2862.3698 | 2862.3698 |
| 4.1944 | 2835.5939 | 2859.1737 | 2859.1737 |

Scan List

| Vis. | Dataset Name | Start pos. [°2θ] | End pos. [°2θ] | Step [°2θ] | Meas.Date/Time |
| --- | --- | --- | --- | --- | --- |
| * | 10 Etosha22 CrySub 4-10cm S1 | 2.0054 | 29.9894 | 0.0110 | 12/1/2023 11:38:39 AM |

Peak List

| Pos. [°2θ] | Height [cts] | FWHM Left [°2θ] | d-spacing [Å] | Rel. Int. [%] |
| --- | --- | --- | --- | --- |
| 7.0870 | 3883.32 | 0.1515 | 12.46317 | 100.00 |
| 7.2278 | 3414.46 | 0.1082 | 12.22067 | 87.93 |
| 8.7625 | 723.86 | 0.1948 | 10.08342 | 18.64 |
| 13.0768 | 70.90 | 0.3897 | 6.76479 | 1.83 |
| 15.7739 | 870.30 | 0.0758 | 5.61364 | 22.41 |
| 17.6537 | 95.80 | 0.2598 | 5.01992 | 2.47 |
| 18.2193 | 144.26 | 0.1082 | 4.86532 | 3.71 |
| 19.6082 | 109.20 | 0.5196 | 4.52373 | 2.81 |
| 21.2647 | 30.75 | 0.6061 | 4.17493 | 0.79 |
| 23.4882 | 41.20 | 0.3464 | 3.78449 | 1.06 |
| 25.9232 | 891.80 | 0.1082 | 3.43427 | 22.96 |
| 26.7445 | 265.14 | 0.1299 | 3.33064 | 6.83 |

Pattern List

| Visible | Ref.Code | Score | Compound Name | Chem. Formula | Mineral Name | SemiQuant[%] |
| --- | --- | --- | --- | --- | --- | --- |
| * | 01-072-4625 | 62 | Sodium Aluminum Silicate Hydrate | Na Al ( Si2 O6 ) ( H2 O ) | Analcime | 20 |
| * | 00-042-1437 | 49 | Potassium Iron Magnesium Aluminum Silicate Hydroxide | K ( Mg , Fe )3 ( Al , Fe ) Si3 O10 ( O H , F )2 | Phlogopite-1M, Fe+2-bearing | 9 |
| * | 01-080-5019 | 32 | Magnesium Silicate Hydroxide Hydrate | Mg7.68 ( Si12 O30 ) ( O H )4 ( H2 O )4 ( H2 O )6 | Sepiolite | 19 |
| * | 01-089-6415 | 47 | Potassium Manganese Silicate Hydroxide Hydrate | K3.68 Mn15.904 Si25.472 O64 ( O H )9.376 ( H2 O )7.024 | Ganophyllite | 27 |
| * | 01-082-8023 | 23 | Sodium Magnesium Silicon Oxide Hydrate | Na2 Mg3 ( Si6 O16 ) ( H2 O )7 | Loughlinite | 25 |

Anchor Scan Parameters

Dataset Name	10 Etosha22 CrySub 4-10cm S1

File name	C:\aeris_data\XRD data\Goldstein\Etosha 2023\Etosha Clay Data\Sample 10\10 Etosha22 CrySub 4-10cm S1.xrdml

Sample Identification	10 Etosha22 CrySub 4-10cm S1

Measurement Start Date/Time	12/1/2023 11:38:39 AM

Operator	Instrument

Raw Data Origin	XRD measurement (*.XRDML)

Scan Axis	Gonio

Start Position [°2θ]	2.0054

End Position [°2θ]	29.9894

Step Size [°2θ]	0.0110

Scan Step Time [s]	48.1950

Scan Type	Continuous

PSD Mode	Scanning

PSD Length [°2θ]	5.54

Offset [°2θ]	0.0000

Divergence Slit Type	Fixed

Divergence Slit Size [°]	0.0603

Specimen Length [mm]	10.00

Measurement Temperature [°C]	25.00

Anode Material	Cu

K-α1 [Å]	1.54060

K-α2 [Å]	1.54443

K-β1 [Å]	1.39225

K-A2 / K-A1 Ratio	0.50000

Generator Settings	15 mA, 40 kV

Diffractometer Type	2082464

Diffractometer Number	0

Goniometer Radius [mm]	145.00

Dist. Focus-Diverg. Slit [mm]	95.00

Incident Beam Monochromator	No

Spinning	Yes