11 Etosha 22 Msub 10-15 cm S1 550 C

Graphics

Graphics

Graphics

Quantitative Results

Phase Sodium Aluminum Silicate Hydrate

Weight fraction/ %	29.0

Phase Potassium Sodium Magnesium Aluminum Iron Silicon Titanium Oxide Fluoride Hydroxide

Weight fraction/ %	54.0

Phase Uranyl Aluminum Phosphate Hydroxide Hydrate

Weight fraction/ %	6.0

Phase Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide

Weight fraction/ %	10.0

Multiple Quantitative Results

Scans vs Phases Matrix

| Scan name | Sodium Aluminum Silicate Hydrate | Potassium Sodium Magnesium Aluminum Iron Silicon Titanium Oxide Fluoride Hydroxide | Uranyl Aluminum Phosphate Hydroxide Hydrate | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide |
| --- | --- | --- | --- | --- |
| 11 Etosha22 Msub 10-15cm S1 heat550c | 29.0 | 54.0 | 6.0 | 10.0 |

Anchor Scan Data

| Pos. [°2θ] | Iobs [cts] | Icalc [cts] | Iback [cts] |
| --- | --- | --- | --- |
| 2.0054 | 6101.0000 | 6096.8152 | 6101.0000 |
| 2.0164 | 6260.0949 | 6065.3358 | 6065.0794 |
| 2.0274 | 6107.5408 | 6029.4169 | 6029.1588 |
| 2.0384 | 6128.4100 | 5993.4980 | 5993.2382 |
| 2.0494 | 6101.0039 | 5957.5791 | 5957.3176 |
| 2.0604 | 5871.9499 | 5921.6602 | 5921.3969 |
| 2.0714 | 5918.6224 | 5885.7414 | 5885.4763 |
| 2.0824 | 5933.2355 | 5849.8226 | 5849.5557 |
| 2.0934 | 5858.5290 | 5813.9038 | 5813.6351 |
| 2.1044 | 5724.3805 | 5777.9850 | 5777.7145 |
| 2.1154 | 5645.1455 | 5742.0663 | 5741.7939 |
| 2.1264 | 5688.1888 | 5706.1475 | 5705.8733 |
| 2.1374 | 5679.3127 | 5670.2288 | 5669.9527 |
| 2.1484 | 5661.6750 | 5634.3101 | 5634.0320 |
| 2.1594 | 5664.1367 | 5598.3914 | 5598.1114 |
| 2.1704 | 5575.6254 | 5562.4727 | 5562.1908 |
| 2.1814 | 5525.1042 | 5526.5541 | 5526.2702 |
| 2.1924 | 5454.7163 | 5491.4084 | 5490.3496 |
| 2.2034 | 5470.5310 | 5460.9707 | 5460.6828 |
| 2.2144 | 5471.5511 | 5431.3058 | 5431.0159 |
| 2.2254 | 5424.7660 | 5401.6411 | 5401.3491 |
| 2.2364 | 5467.0000 | 5371.9763 | 5371.6822 |
| 2.2474 | 5411.2969 | 5342.3116 | 5342.0154 |
| 2.2584 | 5260.7173 | 5312.6468 | 5312.3485 |
| 2.2694 | 5284.4838 | 5282.9821 | 5282.6817 |
| 2.2804 | 5325.1780 | 5253.3175 | 5253.0149 |
| 2.2914 | 5310.5654 | 5223.6528 | 5223.3480 |
| 2.3024 | 5317.8761 | 5193.9882 | 5193.6812 |
| 2.3134 | 5194.0914 | 5164.3236 | 5164.0143 |
| 2.3244 | 5163.5944 | 5134.6590 | 5134.3475 |
| 2.3354 | 5210.2124 | 5104.9944 | 5104.6807 |
| 2.3464 | 5162.1809 | 5075.3299 | 5075.0138 |
| 2.3574 | 5083.8997 | 5045.6654 | 5045.3470 |
| 2.3684 | 5066.6357 | 5016.0009 | 5015.6801 |
| 2.3794 | 5010.0305 | 4986.3224 | 4986.0133 |
| 2.3904 | 5011.2414 | 4956.5580 | 4956.2324 |
| 2.4014 | 4943.7876 | 4926.7796 | 4926.4516 |
| 2.4124 | 4773.1613 | 4897.0012 | 4896.6707 |
| 2.4234 | 4740.2812 | 4867.2229 | 4866.8898 |
| 2.4344 | 4780.1327 | 4837.4445 | 4837.1090 |
| 2.4454 | 4757.2606 | 4807.6662 | 4807.3281 |
| 2.4564 | 4722.5905 | 4777.8880 | 4777.5473 |
| 2.4674 | 4703.0265 | 4748.1097 | 4747.7664 |
| 2.4784 | 4687.2129 | 4718.3315 | 4717.9855 |
| 2.4894 | 4701.7040 | 4688.5533 | 4688.2047 |
| 2.5004 | 4644.8186 | 4658.7752 | 4658.4238 |
| 2.5114 | 4524.6303 | 4628.9970 | 4628.6429 |
| 2.5224 | 4611.1092 | 4599.2190 | 4598.8621 |
| 2.5334 | 4566.9174 | 4569.4409 | 4569.0812 |
| 2.5444 | 4538.6804 | 4539.6629 | 4539.3004 |
| 2.5554 | 4597.2183 | 4509.8849 | 4509.5195 |
| 2.5664 | 4509.6003 | 4480.1069 | 4479.7386 |
| 2.5774 | 4436.7434 | 4450.3290 | 4449.9578 |
| 2.5884 | 4334.4975 | 4420.5511 | 4420.1769 |
| 2.5994 | 4411.1062 | 4390.7733 | 4390.3960 |
| 2.6104 | 4405.3712 | 4360.9955 | 4360.6152 |
| 2.6214 | 4303.8584 | 4331.2177 | 4330.8343 |
| 2.6324 | 4278.6047 | 4301.4400 | 4301.0535 |
| 2.6434 | 4272.4454 | 4271.6623 | 4271.2726 |
| 2.6544 | 4318.3117 | 4241.8846 | 4241.4917 |
| 2.6654 | 4273.5782 | 4212.1070 | 4211.7109 |
| 2.6764 | 4233.7557 | 4182.3294 | 4181.9300 |
| 2.6874 | 4186.0875 | 4152.5518 | 4152.1491 |
| 2.6984 | 4135.0575 | 4122.7743 | 4122.3683 |
| 2.7094 | 4143.6657 | 4092.9969 | 4092.5874 |
| 2.7204 | 4035.5536 | 4063.2195 | 4062.8066 |
| 2.7314 | 3992.3982 | 4033.4421 | 4033.0257 |
| 2.7424 | 3995.5880 | 4003.6648 | 4003.2448 |
| 2.7534 | 3994.4926 | 3973.8508 | 3973.4640 |
| 2.7644 | 3945.6593 | 3943.9962 | 3943.5691 |
| 2.7754 | 3944.7434 | 3914.1050 | 3913.6742 |
| 2.7864 | 3906.7301 | 3884.2139 | 3883.7793 |
| 2.7974 | 3854.0973 | 3854.3228 | 3853.8844 |
| 2.8084 | 3768.1450 | 3824.4317 | 3823.9896 |
| 2.8194 | 3710.7945 | 3794.5407 | 3794.0947 |
| 2.8304 | 3865.4764 | 3764.6497 | 3764.1998 |
| 2.8414 | 3823.8869 | 3734.7588 | 3734.3049 |
| 2.8524 | 3737.6622 | 3704.8679 | 3704.4100 |
| 2.8634 | 3629.4602 | 3674.9771 | 3674.5151 |
| 2.8744 | 3758.0261 | 3645.0864 | 3644.6203 |
| 2.8854 | 3514.2124 | 3615.1957 | 3614.7254 |
| 2.8964 | 3534.8894 | 3585.3051 | 3584.8305 |
| 2.9074 | 3478.3383 | 3555.4145 | 3554.9356 |
| 2.9184 | 3521.5846 | 3525.5240 | 3525.0407 |
| 2.9294 | 3546.5929 | 3495.6335 | 3495.1458 |
| 2.9404 | 3444.1052 | 3466.1360 | 3465.2509 |
| 2.9514 | 3420.4375 | 3437.0739 | 3436.5773 |
| 2.9624 | 3347.8422 | 3408.4049 | 3407.9036 |
| 2.9734 | 3371.4729 | 3379.7358 | 3379.2299 |
| 2.9844 | 3212.7891 | 3351.0669 | 3350.5562 |
| 2.9954 | 3255.6018 | 3322.3980 | 3321.8825 |
| 3.0064 | 3234.5831 | 3293.7292 | 3293.2088 |
| 3.0174 | 3286.8151 | 3265.0604 | 3264.5351 |
| 3.0284 | 3245.6947 | 3236.3918 | 3235.8614 |
| 3.0394 | 3169.4179 | 3207.7232 | 3207.1877 |
| 3.0504 | 3196.0472 | 3179.0546 | 3178.5141 |
| 3.0614 | 3224.3038 | 3150.3862 | 3149.8404 |
| 3.0724 | 3161.0039 | 3121.7178 | 3121.1667 |
| 3.0834 | 3115.1141 | 3093.0495 | 3092.4930 |
| 3.0944 | 3080.0531 | 3064.3812 | 3063.8193 |
| 3.1054 | 3021.7463 | 3035.7131 | 3035.1456 |
| 3.1164 | 3030.1008 | 3007.0450 | 3006.4719 |
| 3.1274 | 2930.5339 | 2982.9967 | 2977.7982 |
| 3.1384 | 2989.5959 | 2964.0679 | 2963.4832 |
| 3.1494 | 2960.3294 | 2949.7587 | 2949.1682 |
| 3.1604 | 2927.9160 | 2935.4497 | 2934.8532 |
| 3.1714 | 3008.3952 | 2921.1408 | 2920.5382 |
| 3.1824 | 2896.0300 | 2906.8319 | 2906.2232 |
| 3.1934 | 2891.5133 | 2892.5232 | 2891.9082 |
| 3.2044 | 2839.4548 | 2878.2145 | 2877.5932 |
| 3.2154 | 2851.6480 | 2863.9060 | 2863.2782 |
| 3.2264 | 2843.3496 | 2849.5975 | 2848.9632 |
| 3.2374 | 2866.9066 | 2835.2892 | 2834.6482 |
| 3.2484 | 2860.7222 | 2820.9809 | 2820.3332 |
| 3.2594 | 2757.8083 | 2806.6728 | 2806.0182 |
| 3.2704 | 2794.6642 | 2792.3648 | 2791.7032 |
| 3.2814 | 2754.1445 | 2778.0568 | 2777.3882 |
| 3.2924 | 2677.3009 | 2763.7490 | 2763.0732 |
| 3.3034 | 2777.6372 | 2749.4414 | 2748.7582 |
| 3.3144 | 2766.6794 | 2735.4257 | 2734.4432 |
| 3.3254 | 2713.0207 | 2721.7337 | 2721.0356 |
| 3.3364 | 2687.9700 | 2708.3337 | 2707.6280 |
| 3.3474 | 2660.9685 | 2694.9339 | 2694.2203 |
| 3.3584 | 2712.9602 | 2681.5342 | 2680.8127 |
| 3.3694 | 2713.1327 | 2668.1346 | 2667.4051 |
| 3.3804 | 2665.9626 | 2654.7352 | 2653.9974 |
| 3.3914 | 2649.3274 | 2641.3359 | 2640.5898 |
| 3.4024 | 2613.8058 | 2627.9368 | 2627.1822 |
| 3.4134 | 2561.6558 | 2614.5378 | 2613.7745 |
| 3.4244 | 2576.6918 | 2601.1389 | 2600.3669 |
| 3.4354 | 2598.7935 | 2587.7402 | 2586.9593 |
| 3.4464 | 2564.0024 | 2574.3416 | 2573.5516 |
| 3.4574 | 2571.4985 | 2560.9432 | 2560.1440 |
| 3.4684 | 2591.2694 | 2547.5450 | 2546.7364 |
| 3.4794 | 2595.8820 | 2534.1469 | 2533.3287 |
| 3.4904 | 2553.1681 | 2520.7490 | 2519.9211 |
| 3.5014 | 2511.1957 | 2507.3513 | 2506.5134 |
| 3.5124 | 2502.6839 | 2493.9538 | 2493.1058 |
| 3.5234 | 2468.8879 | 2480.5564 | 2479.6982 |
| 3.5344 | 2399.4488 | 2467.1592 | 2466.2905 |
| 3.5454 | 2464.9312 | 2453.7623 | 2452.8829 |
| 3.5564 | 2399.3067 | 2440.3655 | 2439.4753 |
| 3.5674 | 2384.6146 | 2426.9689 | 2426.0676 |
| 3.5784 | 2357.1494 | 2413.5725 | 2412.6600 |
| 3.5894 | 2336.7611 | 2400.1764 | 2399.2524 |
| 3.6004 | 2323.8314 | 2386.7804 | 2385.8447 |
| 3.6114 | 2373.4366 | 2373.3847 | 2372.4371 |
| 3.6224 | 2367.6372 | 2359.9892 | 2359.0295 |
| 3.6334 | 2331.8751 | 2346.5939 | 2345.6218 |
| 3.6444 | 2361.5801 | 2333.1989 | 2332.2142 |
| 3.6554 | 2349.5959 | 2319.8041 | 2318.8066 |
| 3.6664 | 2334.0167 | 2306.4096 | 2305.3989 |
| 3.6774 | 2309.4258 | 2293.0153 | 2291.9913 |
| 3.6884 | 2246.1239 | 2280.2147 | 2278.5837 |
| 3.6994 | 2279.0698 | 2268.0721 | 2267.0206 |
| 3.7104 | 2259.5619 | 2256.5232 | 2255.4575 |
| 3.7214 | 2312.0443 | 2244.9746 | 2243.8944 |
| 3.7324 | 2295.6170 | 2233.4262 | 2232.3313 |
| 3.7434 | 2351.4612 | 2221.8782 | 2220.7682 |
| 3.7544 | 2249.0752 | 2210.3305 | 2209.2051 |
| 3.7654 | 2195.6716 | 2198.7831 | 2197.6420 |
| 3.7764 | 2205.7463 | 2187.2360 | 2186.0789 |
| 3.7874 | 2184.1947 | 2175.6893 | 2174.5158 |
| 3.7984 | 2134.2685 | 2164.1429 | 2162.9527 |
| 3.8094 | 2210.6155 | 2152.5969 | 2151.3896 |
| 3.8204 | 2126.6062 | 2141.0512 | 2139.8265 |
| 3.8314 | 2211.8800 | 2129.5059 | 2128.2634 |
| 3.8424 | 2093.2616 | 2117.9610 | 2116.7003 |
| 3.8534 | 2147.5870 | 2106.4166 | 2105.1372 |
| 3.8644 | 2083.0737 | 2094.8725 | 2093.5741 |
| 3.8754 | 2071.2842 | 2084.6800 | 2082.0110 |
| 3.8864 | 2066.6460 | 2075.9852 | 2074.6474 |
| 3.8974 | 2096.0452 | 2068.6420 | 2067.2839 |
| 3.9084 | 2136.6824 | 2061.2992 | 2059.9203 |
| 3.9194 | 2091.1976 | 2053.9570 | 2052.5568 |
| 3.9304 | 2086.4902 | 2046.6152 | 2045.1932 |
| 3.9414 | 2110.7581 | 2039.2739 | 2037.8297 |
| 3.9524 | 2047.2979 | 2031.9332 | 2030.4662 |
| 3.9634 | 2050.1977 | 2024.5930 | 2023.1026 |
| 3.9744 | 2082.2026 | 2017.2534 | 2015.7391 |
| 3.9854 | 2105.3363 | 2009.9143 | 2008.3755 |
| 3.9964 | 2100.7438 | 2002.5758 | 2001.0120 |
| 4.0074 | 2045.7581 | 1995.2380 | 1993.6485 |
| 4.0184 | 2016.2493 | 1987.9008 | 1986.2849 |
| 4.0294 | 2024.3235 | 1980.5642 | 1978.9214 |
| 4.0404 | 2026.6524 | 1973.2283 | 1971.5578 |
| 4.0514 | 1976.8555 | 1965.8931 | 1964.1943 |
| 4.0624 | 1972.8063 | 1958.5587 | 1956.8308 |
| 4.0734 | 1981.4966 | 1951.2249 | 1949.4672 |
| 4.0844 | 2001.1858 | 1943.8920 | 1942.1037 |
| 4.0954 | 1934.0108 | 1936.5598 | 1934.7401 |
| 4.1064 | 1856.2832 | 1929.2285 | 1927.3766 |
| 4.1174 | 1929.0354 | 1921.8980 | 1920.0131 |
| 4.1284 | 1936.5078 | 1914.5685 | 1912.6495 |
| 4.1394 | 1912.3825 | 1907.2398 | 1905.2860 |
| 4.1504 | 1930.9189 | 1899.9121 | 1897.9224 |
| 4.1614 | 1893.6420 | 1892.5853 | 1890.5589 |
| 4.1724 | 1837.8029 | 1885.2596 | 1883.1953 |
| 4.1834 | 1855.4602 | 1877.9350 | 1875.8318 |
| 4.1944 | 1872.8766 | 1870.6114 | 1868.4683 |

Scan List

| Vis. | Dataset Name | Start pos. [°2θ] | End pos. [°2θ] | Step [°2θ] | Meas.Date/Time |
| --- | --- | --- | --- | --- | --- |
| * | 11 Etosha22 Msub 10-15cm S1 heat550c | 2.0054 | 29.9894 | 0.0110 | 12/4/2023 3:43:57 PM |

Peak List

| Pos. [°2θ] | Height [cts] | FWHM Left [°2θ] | d-spacing [Å] | Rel. Int. [%] |
| --- | --- | --- | --- | --- |
| 5.3192 | 131.15 | 0.3897 | 16.60042 | 20.57 |
| 8.7258 | 637.46 | 0.1299 | 10.12568 | 100.00 |
| 15.8602 | 271.91 | 0.1299 | 5.58328 | 42.66 |
| 17.5793 | 29.35 | 0.2165 | 5.04099 | 4.60 |
| 18.2717 | 24.79 | 0.2598 | 4.85149 | 3.89 |
| 19.7427 | 19.55 | 0.8659 | 4.49321 | 3.07 |
| 26.0667 | 147.69 | 0.3897 | 3.41569 | 23.17 |
| 27.5172 | 131.25 | 0.1948 | 3.23885 | 20.59 |

Pattern List

| Visible | Ref.Code | Score | Compound Name | Chem. Formula | Mineral Name | SemiQuant[%] |
| --- | --- | --- | --- | --- | --- | --- |
| * | 04-011-6233 | 70 | Sodium Aluminum Silicate Hydrate | Na8 Al8 Si16 O48 ( H2 O )8 | Analcime | 29 |
| * | 04-023-1515 | 49 | Potassium Sodium Magnesium Aluminum Iron Silicon Titanium Oxide Fluoride Hydroxide | K0.93 Na0.05 Mg1.71 Ti0.13 Fe0.97 Al1.44 Si2.75 O10.47 ( O H )1.33 F0.2 | Phlogopite-1M | 54 |
| * | 04-024-3136 | 57 | Uranyl Aluminum Phosphate Hydroxide Hydrate | ( U O2 )4 Al4 ( P O4 )6 ( O H )2 ( H2 O )19.5 | Furongite | 6 |
| * | 04-025-4215 | 3 | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide | Mg10.4 V0.36 Mn33.5 Fe0.14 Al0.69 Si6.77 As6.5 P0.3 O54 ( O H )42 | Carlfrancisite | 10 |

Anchor Scan Parameters

Dataset Name	11 Etosha22 Msub 10-15cm S1 heat550c

File name	C:\aeris_data\XRD data\Goldstein\Etosha 2023\Etosha Clay Data\Sample 11\11 Etosha22 Msub 10-15cm S1 heat550c.xrdml

Sample Identification	11 Etosha22 Msub 10-15cm S1 heat550c

Measurement Start Date/Time	12/4/2023 3:43:57 PM

Operator	Instrument

Raw Data Origin	XRD measurement (*.XRDML)

Scan Axis	Gonio

Start Position [°2θ]	2.0054

End Position [°2θ]	29.9894

Step Size [°2θ]	0.0110

Scan Step Time [s]	48.1950

Scan Type	Continuous

PSD Mode	Scanning

PSD Length [°2θ]	5.54

Offset [°2θ]	0.0000

Divergence Slit Type	Fixed

Divergence Slit Size [°]	0.0603

Specimen Length [mm]	10.00

Measurement Temperature [°C]	25.00

Anode Material	Cu

K-α1 [Å]	1.54060

K-α2 [Å]	1.54443

K-β1 [Å]	1.39225

K-A2 / K-A1 Ratio	0.50000

Generator Settings	15 mA, 40 kV

Diffractometer Type	2082464

Diffractometer Number	0

Goniometer Radius [mm]	145.00

Dist. Focus-Diverg. Slit [mm]	95.00

Incident Beam Monochromator	No

Spinning	Yes