11 Etosha 22 Msub 10-15 cm S1 GLYCOLATED

Graphics

Graphics

Graphics

Quantitative Results

Phase Potassium Sodium Barium Magnesium Manganese Aluminum Iron Silicon Oxide Hydroxide

Weight fraction/ %	37.0

Phase Titanium Oxide

Weight fraction/ %	2.0

Phase Potassium Sodium Calcium Magnesium Aluminum Iron Silicon Oxide Hydroxide

Weight fraction/ %	9.0

Phase Potassium Sodium Calcium Aluminum Silicon Oxide Hydrate

Weight fraction/ %	15.0

Phase Magnesium Silicon Oxide Hydroxide Hydrate

Weight fraction/ %	6.0

Phase Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide

Weight fraction/ %	13.0

Phase Potassium Sodium Calcium Manganese Aluminum Iron Silicon Oxide Hydroxide Hydrate

Weight fraction/ %	16.0

Phase Uranyl Aluminum Phosphate Hydroxide Hydrate

Weight fraction/ %	3.0

Multiple Quantitative Results

Scans vs Phases Matrix

| Scan name | Potassium Sodium Barium Magnesium Manganese Aluminum Iron Silicon Oxide Hydroxide | Titanium Oxide | Potassium Sodium Calcium Magnesium Aluminum Iron Silicon Oxide Hydroxide | Potassium Sodium Calcium Aluminum Silicon Oxide Hydrate | Magnesium Silicon Oxide Hydroxide Hydrate | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide | Potassium Sodium Calcium Manganese Aluminum Iron Silicon Oxide Hydroxide Hydrate | Uranyl Aluminum Phosphate Hydroxide Hydrate |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 11 Etosha22 Moisub 10-15cm s1 glycol | 37.0 | 2.0 | 9.0 | 15.0 | 6.0 | 13.0 | 16.0 | 3.0 |

Anchor Scan Data

| Pos. [°2θ] | Iobs [cts] | Icalc [cts] | Iback [cts] |
| --- | --- | --- | --- |
| 2.0054 | 6196.0000 | 6191.6344 | 6196.0000 |
| 2.0164 | 6207.5374 | 6162.4737 | 6157.1368 |
| 2.0274 | 6088.7955 | 6123.7670 | 6118.2736 |
| 2.0384 | 6040.4100 | 6085.0672 | 6079.4105 |
| 2.0494 | 6015.3638 | 6046.3748 | 6040.5473 |
| 2.0604 | 5828.3240 | 6007.6901 | 6001.6841 |
| 2.0714 | 5825.0796 | 5969.0136 | 5962.8209 |
| 2.0824 | 5903.2453 | 5930.3459 | 5923.9578 |
| 2.0934 | 5792.8348 | 5891.6874 | 5885.0946 |
| 2.1044 | 5818.2655 | 5853.0389 | 5846.2314 |
| 2.1154 | 5751.1849 | 5814.4008 | 5807.3682 |
| 2.1264 | 5833.1632 | 5775.7739 | 5768.5051 |
| 2.1374 | 5822.5162 | 5737.1590 | 5729.6419 |
| 2.1484 | 5693.7827 | 5698.5568 | 5690.7787 |
| 2.1594 | 5760.8279 | 5659.9682 | 5651.9155 |
| 2.1704 | 5728.6578 | 5621.3942 | 5613.0524 |
| 2.1814 | 5571.3176 | 5582.8358 | 5574.1892 |
| 2.1924 | 5510.8800 | 5545.0790 | 5535.3260 |
| 2.2034 | 5511.2655 | 5508.9633 | 5499.6555 |
| 2.2144 | 5359.8496 | 5473.6517 | 5463.9850 |
| 2.2254 | 5533.8260 | 5438.3611 | 5428.3145 |
| 2.2364 | 5452.0280 | 5403.0931 | 5392.6440 |
| 2.2474 | 5355.7148 | 5367.8496 | 5356.9735 |
| 2.2584 | 5330.2562 | 5332.6329 | 5321.3029 |
| 2.2694 | 5409.5782 | 5297.4454 | 5285.6324 |
| 2.2804 | 5240.7925 | 5262.2899 | 5249.9619 |
| 2.2914 | 5234.2763 | 5227.1699 | 5214.2914 |
| 2.3024 | 5243.2655 | 5192.0893 | 5178.6209 |
| 2.3134 | 5137.7984 | 5157.0529 | 5142.9504 |
| 2.3244 | 5200.2183 | 5122.0663 | 5107.2799 |
| 2.3354 | 5248.7257 | 5087.1365 | 5071.6094 |
| 2.3464 | 5179.8963 | 5052.2720 | 5035.9389 |
| 2.3574 | 5097.5270 | 5017.4831 | 5000.2683 |
| 2.3684 | 5080.3215 | 4982.7826 | 4964.5978 |
| 2.3794 | 5095.8201 | 4948.1629 | 4928.9273 |
| 2.3904 | 5064.9022 | 4913.6184 | 4893.1629 |
| 2.4014 | 5042.8319 | 4879.1971 | 4857.3985 |
| 2.4124 | 5033.7748 | 4844.9499 | 4821.6342 |
| 2.4234 | 4929.8682 | 4810.9103 | 4785.8698 |
| 2.4344 | 4950.6947 | 4777.1182 | 4750.1054 |
| 2.4454 | 4945.4346 | 4743.6202 | 4714.3410 |
| 2.4564 | 4853.9926 | 4710.4703 | 4678.5766 |
| 2.4674 | 4853.4956 | 4677.7302 | 4642.8122 |
| 2.4784 | 4857.5059 | 4645.4694 | 4607.0479 |
| 2.4894 | 4732.2871 | 4613.7648 | 4571.2835 |
| 2.5004 | 4715.5664 | 4582.6995 | 4535.5191 |
| 2.5114 | 4686.7188 | 4552.3623 | 4499.7547 |
| 2.5224 | 4693.3456 | 4522.8450 | 4463.9903 |
| 2.5334 | 4681.1327 | 4494.2401 | 4428.2259 |
| 2.5444 | 4633.3638 | 4466.6380 | 4392.4615 |
| 2.5554 | 4637.4474 | 4440.1226 | 4356.6972 |
| 2.5664 | 4598.2404 | 4414.7677 | 4320.9328 |
| 2.5774 | 4540.3215 | 4390.6318 | 4285.1684 |
| 2.5884 | 4541.8913 | 4367.7531 | 4249.4040 |
| 2.5994 | 4521.4690 | 4346.1442 | 4213.6396 |
| 2.6104 | 4503.2960 | 4325.7867 | 4177.8752 |
| 2.6214 | 4421.4690 | 4306.6245 | 4142.1109 |
| 2.6324 | 4448.0531 | 4288.5578 | 4106.3465 |
| 2.6434 | 4407.9892 | 4271.4358 | 4070.5821 |
| 2.6544 | 4359.9700 | 4255.0479 | 4034.8177 |
| 2.6654 | 4239.9056 | 4239.1150 | 3999.0533 |
| 2.6764 | 4294.4690 | 4223.2802 | 3963.2889 |
| 2.6874 | 4187.3077 | 4207.1005 | 3927.5245 |
| 2.6984 | 4099.8628 | 4190.0450 | 3891.7602 |
| 2.7094 | 4215.2203 | 4171.5021 | 3855.9958 |
| 2.7204 | 4178.0973 | 4150.8037 | 3820.2314 |
| 2.7314 | 4031.8289 | 4127.2710 | 3784.4670 |
| 2.7424 | 3984.7065 | 4100.2793 | 3748.7026 |
| 2.7534 | 3996.8800 | 4069.3133 | 3712.9382 |
| 2.7644 | 3937.2419 | 4034.0611 | 3677.0800 |
| 2.7754 | 3956.9735 | 3994.5112 | 3641.2217 |
| 2.7864 | 3852.0442 | 3950.9086 | 3605.3635 |
| 2.7974 | 3775.8230 | 3903.6961 | 3569.5052 |
| 2.8084 | 3691.7340 | 3853.4705 | 3533.6469 |
| 2.8194 | 3703.0098 | 3800.9037 | 3497.7887 |
| 2.8304 | 3629.4100 | 3746.6725 | 3461.9304 |
| 2.8414 | 3574.4258 | 3691.4074 | 3426.0722 |
| 2.8524 | 3500.0192 | 3635.6630 | 3390.2139 |
| 2.8634 | 3429.8495 | 3579.9061 | 3354.3557 |
| 2.8744 | 3448.3619 | 3524.5164 | 3318.4974 |
| 2.8854 | 3423.4346 | 3469.7929 | 3282.6391 |
| 2.8964 | 3274.6593 | 3415.9638 | 3246.7809 |
| 2.9074 | 3208.9528 | 3363.1951 | 3210.9226 |
| 2.9184 | 3200.9036 | 3311.5997 | 3175.0644 |
| 2.9294 | 3099.4218 | 3261.2446 | 3139.2061 |
| 2.9404 | 3109.5841 | 3215.6962 | 3103.3479 |
| 2.9514 | 3062.9046 | 3178.7299 | 3081.8848 |
| 2.9624 | 3138.4543 | 3146.5335 | 3060.4218 |
| 2.9734 | 3067.1013 | 3115.5151 | 3038.9588 |
| 2.9844 | 3096.4597 | 3085.6047 | 3017.4958 |
| 2.9954 | 3035.5664 | 3056.7206 | 2996.0328 |
| 3.0064 | 2973.3555 | 3028.7737 | 2974.5697 |
| 3.0174 | 2962.5300 | 3001.6717 | 2953.1067 |
| 3.0284 | 2868.8510 | 2975.3224 | 2931.6437 |
| 3.0394 | 2848.9715 | 2949.6360 | 2910.1807 |
| 3.0504 | 2863.5939 | 2924.5275 | 2888.7177 |
| 3.0614 | 2805.9587 | 2899.9184 | 2867.2547 |
| 3.0724 | 2808.6214 | 2875.7371 | 2845.7916 |
| 3.0834 | 2750.5447 | 2851.9197 | 2824.3286 |
| 3.0944 | 2774.9159 | 2828.4103 | 2802.8656 |
| 3.1054 | 2765.9597 | 2805.1601 | 2781.4026 |
| 3.1164 | 2742.7237 | 2782.1277 | 2759.9396 |
| 3.1274 | 2723.5074 | 2760.0285 | 2738.4765 |
| 3.1384 | 2731.6495 | 2739.8822 | 2719.9974 |
| 3.1494 | 2736.0865 | 2720.4466 | 2701.5182 |
| 3.1604 | 2661.9366 | 2700.9760 | 2683.0390 |
| 3.1714 | 2609.5821 | 2681.5977 | 2664.5599 |
| 3.1824 | 2672.4312 | 2662.2983 | 2646.0807 |
| 3.1934 | 2581.1150 | 2643.0668 | 2627.6015 |
| 3.2044 | 2559.5561 | 2623.8942 | 2609.1223 |
| 3.2154 | 2565.6057 | 2604.7733 | 2590.6432 |
| 3.2264 | 2498.3230 | 2585.6981 | 2572.1640 |
| 3.2374 | 2531.6893 | 2566.6636 | 2553.6848 |
| 3.2484 | 2501.3889 | 2547.6656 | 2535.2056 |
| 3.2594 | 2455.6961 | 2528.7006 | 2516.7265 |
| 3.2704 | 2427.8083 | 2509.7657 | 2498.2473 |
| 3.2814 | 2469.8122 | 2490.8582 | 2479.7681 |
| 3.2924 | 2452.7168 | 2471.9759 | 2461.2889 |
| 3.3034 | 2487.4523 | 2453.1168 | 2442.8098 |
| 3.3144 | 2488.6509 | 2434.2791 | 2424.3306 |
| 3.3254 | 2426.2449 | 2415.4614 | 2405.8514 |
| 3.3364 | 2420.6121 | 2396.6621 | 2387.3723 |
| 3.3474 | 2360.0157 | 2377.8800 | 2368.8931 |
| 3.3584 | 2317.8982 | 2359.1139 | 2350.4139 |
| 3.3694 | 2273.0846 | 2340.3628 | 2331.9347 |
| 3.3804 | 2280.7463 | 2321.6257 | 2313.4556 |
| 3.3914 | 2302.4513 | 2302.9017 | 2294.9764 |
| 3.4024 | 2282.9272 | 2284.1899 | 2276.4972 |
| 3.4134 | 2257.6814 | 2265.4896 | 2258.0180 |
| 3.4244 | 2262.8820 | 2246.8002 | 2239.5389 |
| 3.4354 | 2278.5762 | 2228.1209 | 2221.0597 |
| 3.4464 | 2248.8328 | 2209.4512 | 2202.5805 |
| 3.4574 | 2198.3687 | 2190.7904 | 2184.1014 |
| 3.4684 | 2184.8083 | 2172.1382 | 2165.6222 |
| 3.4794 | 2176.6480 | 2153.4940 | 2147.1430 |
| 3.4904 | 2126.1681 | 2134.8574 | 2128.6638 |
| 3.5014 | 2100.9852 | 2118.7843 | 2110.1847 |
| 3.5124 | 2084.2709 | 2108.0057 | 2102.1060 |
| 3.5234 | 2102.0620 | 2099.7900 | 2094.0274 |
| 3.5344 | 2122.2099 | 2091.5803 | 2085.9487 |
| 3.5454 | 2064.7365 | 2083.3764 | 2077.8701 |
| 3.5564 | 2095.2449 | 2075.1780 | 2069.7914 |
| 3.5674 | 2111.2734 | 2066.9848 | 2061.7128 |
| 3.5784 | 2066.8156 | 2058.7965 | 2053.6341 |
| 3.5894 | 2026.0531 | 2050.6130 | 2045.5555 |
| 3.6004 | 2017.2178 | 2042.4340 | 2037.4768 |
| 3.6114 | 2054.3412 | 2034.2593 | 2029.3982 |
| 3.6224 | 2045.4439 | 2026.0886 | 2021.3195 |
| 3.6334 | 1959.9115 | 2017.9219 | 2013.2409 |
| 3.6444 | 2015.9917 | 2009.7589 | 2005.1622 |
| 3.6554 | 2008.2212 | 2001.5995 | 1997.0836 |
| 3.6664 | 2018.5511 | 1993.4435 | 1989.0049 |
| 3.6774 | 2017.5270 | 1985.2908 | 1980.9263 |
| 3.6884 | 1982.6593 | 1977.1412 | 1972.8476 |
| 3.6994 | 1963.7148 | 1968.9946 | 1964.7690 |
| 3.7104 | 1866.9631 | 1960.8510 | 1956.6903 |
| 3.7214 | 1956.0797 | 1952.7102 | 1948.6117 |
| 3.7324 | 1852.5068 | 1944.5720 | 1940.5330 |
| 3.7434 | 1920.3009 | 1936.4364 | 1932.4544 |
| 3.7544 | 1902.0973 | 1928.3034 | 1924.3757 |
| 3.7654 | 1909.6991 | 1920.1727 | 1916.2971 |
| 3.7764 | 1899.2325 | 1912.0444 | 1908.2184 |
| 3.7874 | 1875.2124 | 1903.9183 | 1900.1397 |
| 3.7984 | 1812.1205 | 1895.7944 | 1892.0611 |
| 3.8094 | 1846.4965 | 1887.6726 | 1883.9824 |
| 3.8204 | 1814.7758 | 1879.5528 | 1875.9038 |
| 3.8314 | 1808.8545 | 1871.4350 | 1867.8251 |
| 3.8424 | 1853.0526 | 1863.3192 | 1859.7465 |
| 3.8534 | 1856.5310 | 1855.2052 | 1851.6678 |
| 3.8644 | 1887.2881 | 1847.0931 | 1843.5892 |
| 3.8754 | 1821.8633 | 1838.9610 | 1835.5105 |
| 3.8864 | 1847.0310 | 1830.7869 | 1827.3447 |
| 3.8974 | 1815.7640 | 1822.5928 | 1819.1789 |
| 3.9084 | 1837.7979 | 1814.4004 | 1811.0130 |
| 3.9194 | 1771.6401 | 1806.2096 | 1802.8472 |
| 3.9304 | 1683.4332 | 1798.0203 | 1794.6813 |
| 3.9414 | 1767.4877 | 1789.8327 | 1786.5155 |
| 3.9524 | 1806.4366 | 1781.6466 | 1778.3496 |
| 3.9634 | 1779.3658 | 1773.4620 | 1770.1838 |
| 3.9744 | 1750.5978 | 1765.2789 | 1762.0179 |
| 3.9854 | 1747.6549 | 1757.0972 | 1753.8521 |
| 3.9964 | 1788.5192 | 1748.9170 | 1745.6862 |
| 4.0074 | 1745.7915 | 1740.7383 | 1737.5204 |
| 4.0184 | 1762.7360 | 1732.5610 | 1729.3546 |
| 4.0294 | 1755.2910 | 1724.3851 | 1721.1887 |
| 4.0404 | 1686.8800 | 1716.2106 | 1713.0229 |
| 4.0514 | 1673.7227 | 1708.0375 | 1704.8570 |
| 4.0624 | 1699.6387 | 1700.9218 | 1696.6912 |
| 4.0734 | 1722.3392 | 1695.9235 | 1692.7533 |
| 4.0844 | 1702.6327 | 1691.9826 | 1688.8154 |
| 4.0954 | 1687.3589 | 1688.0431 | 1684.8776 |
| 4.1064 | 1691.8289 | 1684.1049 | 1680.9397 |
| 4.1174 | 1676.0826 | 1680.1682 | 1677.0018 |
| 4.1284 | 1659.7670 | 1676.2328 | 1673.0640 |
| 4.1394 | 1677.5300 | 1672.2989 | 1669.1261 |
| 4.1504 | 1698.9071 | 1668.3664 | 1665.1882 |
| 4.1614 | 1682.6814 | 1664.4354 | 1661.2504 |
| 4.1724 | 1695.5841 | 1660.5058 | 1657.3125 |
| 4.1834 | 1668.2743 | 1656.5777 | 1653.3746 |
| 4.1944 | 1622.5674 | 1652.6511 | 1649.4368 |

Scan List

| Vis. | Dataset Name | Start pos. [°2θ] | End pos. [°2θ] | Step [°2θ] | Meas.Date/Time |
| --- | --- | --- | --- | --- | --- |
| * | 11 Etosha22 Moisub 10-15cm s1 glycol | 2.0054 | 29.9894 | 0.0110 | 12/5/2023 9:29:13 AM |

Peak List

| Pos. [°2θ] | Height [cts] | FWHM Left [°2θ] | d-spacing [Å] | Rel. Int. [%] |
| --- | --- | --- | --- | --- |
| 2.7581 | 319.18 | 0.2598 | 32.00657 | 38.08 |
| 5.2982 | 326.92 | 0.2165 | 16.66617 | 39.01 |
| 7.0457 | 838.11 | 0.1732 | 12.53605 | 100.00 |
| 8.7081 | 305.28 | 0.2165 | 10.14625 | 36.42 |
| 15.7247 | 441.99 | 0.0974 | 5.63109 | 52.74 |
| 17.6430 | 24.44 | 0.2598 | 5.02293 | 2.92 |
| 18.1704 | 45.38 | 0.1299 | 4.87830 | 5.41 |
| 19.6349 | 32.03 | 0.3464 | 4.51764 | 3.82 |
| 25.8893 | 405.82 | 0.1299 | 3.43868 | 48.42 |
| 26.6987 | 99.66 | 0.1732 | 3.33625 | 11.89 |
| 27.4997 | 43.66 | 0.1299 | 3.24087 | 5.21 |

Pattern List

| Visible | Ref.Code | Score | Compound Name | Chem. Formula | Mineral Name | SemiQuant[%] |
| --- | --- | --- | --- | --- | --- | --- |
| * | 04-016-5540 | 56 | Potassium Sodium Barium Magnesium Manganese Aluminum Iron Silicon Oxide Hydroxide | K0.84 Na0.18 Ba0.06 Mg1.74 Mn1.13 Fe0.139 Al1.15 Si2.75 O10 ( O H )1.93 | Phlogopite-1M, Mn+2-bearing | 37 |
| * | 04-016-2838 | 21 | Titanium Oxide | Ti O2 | Rutile | 2 |
| * | 04-017-0520 | 27 | Potassium Sodium Calcium Magnesium Aluminum Iron Silicon Oxide Hydroxide | K0.7 Na0.01 Ca0.01 Mg0.15 Fe0.04 Al2.59 Si3.27 O10 ( O H )2 | Illite (NR) | 9 |
| * | 04-024-8347 | 32 | Potassium Sodium Calcium Aluminum Silicon Oxide Hydrate | K0.19 Na7.69 Ca0.06 Al8 Si16 O48 ( H2 O )8 | Analcime | 15 |
| * | 04-014-4556 | 17 | Magnesium Silicon Oxide Hydroxide Hydrate | Mg4 Si6 O15 ( O H )2 ( H2 O )6 | Sepiolite | 6 |
| * | 04-025-4215 | 13 | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide | Mg10.4 V0.36 Mn33.5 Fe0.14 Al0.69 Si6.77 As6.5 P0.3 O54 ( O H )42 | Carlfrancisite | 13 |
| * | 04-016-0693 | 55 | Potassium Sodium Calcium Manganese Aluminum Iron Silicon Oxide Hydroxide Hydrate | K0.3 Na0.4 Ca0.3 Mn3.9 Fe0.1 Al1.4 Si5.3 O16 ( O H )2.7 ( H2 O )3.5 | Ganophyllite | 16 |
| * | 04-024-3136 | 46 | Uranyl Aluminum Phosphate Hydroxide Hydrate | ( U O2 )4 Al4 ( P O4 )6 ( O H )2 ( H2 O )19.5 | Furongite | 3 |

Anchor Scan Parameters

Dataset Name	11 Etosha22 Moisub 10-15cm s1 glycol

File name	C:\aeris_data\XRD data\Goldstein\Etosha 2023\Etosha Clay Data\Sample 11\11 Etosha22 Moisub 10-15cm s1 glycol.xrdml

Sample Identification	11 Etosha22 Moisub 10-15cm s1 glycol

Measurement Start Date/Time	12/5/2023 9:29:13 AM

Operator	Instrument

Raw Data Origin	XRD measurement (*.XRDML)

Scan Axis	Gonio

Start Position [°2θ]	2.0054

End Position [°2θ]	29.9894

Step Size [°2θ]	0.0110

Scan Step Time [s]	48.1950

Scan Type	Continuous

PSD Mode	Scanning

PSD Length [°2θ]	5.54

Offset [°2θ]	0.0000

Divergence Slit Type	Fixed

Divergence Slit Size [°]	0.0603

Specimen Length [mm]	10.00

Measurement Temperature [°C]	25.00

Anode Material	Cu

K-α1 [Å]	1.54060

K-α2 [Å]	1.54443

K-β1 [Å]	1.39225

K-A2 / K-A1 Ratio	0.50000

Generator Settings	15 mA, 40 kV

Diffractometer Type	2082464

Diffractometer Number	0

Goniometer Radius [mm]	145.00

Dist. Focus-Diverg. Slit [mm]	95.00

Incident Beam Monochromator	No

Spinning	Yes