11 Etosha 22 Msub 10-15 cm S1 REGULAR

Graphics

Graphics

Graphics

Quantitative Results

Phase Potassium Sodium Iron Magnesium Aluminum Silicate Fluoride Hydroxide

Weight fraction/ %	29.0

Phase Titanium Oxide

Weight fraction/ %	2.0

Phase Sodium Aluminum Silicon Oxide Hydrate

Weight fraction/ %	10.0

Phase Potassium Sodium Calcium Magnesium Aluminum Iron Aluminum Silicate Hydroxide

Weight fraction/ %	16.0

Phase Sodium Calcium Magnesium Aluminum Iron Titanium Aluminum Silicon Oxide Hydroxide Hydrate

Weight fraction/ %	2.0

Phase Magnesium Silicate Hydroxide Hydrate

Weight fraction/ %	13.0

Phase Uranyl Aluminum Phosphate Hydroxide Hydrate

Weight fraction/ %	2.0

Phase Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide

Weight fraction/ %	13.0

Phase Potassium Manganese Aluminum Silicon Oxide Hydroxide Hydrate

Weight fraction/ %	14.0

Multiple Quantitative Results

Scans vs Phases Matrix

| Scan name | Potassium Sodium Iron Magnesium Aluminum Silicate Fluoride Hydroxide | Titanium Oxide | Sodium Aluminum Silicon Oxide Hydrate | Potassium Sodium Calcium Magnesium Aluminum Iron Aluminum Silicate Hydroxide | Sodium Calcium Magnesium Aluminum Iron Titanium Aluminum Silicon Oxide Hydroxide Hydrate | Magnesium Silicate Hydroxide Hydrate | Uranyl Aluminum Phosphate Hydroxide Hydrate | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide | Potassium Manganese Aluminum Silicon Oxide Hydroxide Hydrate |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 11 Etosha22 MoiSub 10-15cm S1 | 29.0 | 2.0 | 10.0 | 16.0 | 2.0 | 13.0 | 2.0 | 13.0 | 14.0 |

Anchor Scan Data

| Pos. [°2θ] | Iobs [cts] | Icalc [cts] | Iback [cts] |
| --- | --- | --- | --- |
| 2.0054 | 6262.0000 | 6259.6131 | 6262.0000 |
| 2.0164 | 6326.3363 | 6237.7096 | 6224.2243 |
| 2.0274 | 6270.8614 | 6200.3983 | 6186.4486 |
| 2.0384 | 6176.7080 | 6163.1111 | 6148.6729 |
| 2.0494 | 5942.6037 | 6125.8497 | 6110.8972 |
| 2.0604 | 6103.1003 | 6088.6158 | 6073.1215 |
| 2.0714 | 6007.9852 | 6051.4114 | 6035.3458 |
| 2.0824 | 5947.1509 | 6014.2387 | 5997.5702 |
| 2.0934 | 5966.2635 | 5977.1001 | 5959.7945 |
| 2.1044 | 5936.2035 | 5939.9983 | 5922.0188 |
| 2.1154 | 5970.8604 | 5902.9362 | 5884.2431 |
| 2.1264 | 5952.2581 | 5865.9171 | 5846.4674 |
| 2.1374 | 5782.0531 | 5828.9448 | 5808.6917 |
| 2.1484 | 5710.1239 | 5792.0234 | 5770.9160 |
| 2.1594 | 5715.1327 | 5755.1579 | 5733.1403 |
| 2.1704 | 5816.2404 | 5718.3539 | 5695.3646 |
| 2.1814 | 5819.8574 | 5681.6181 | 5657.5889 |
| 2.1924 | 5751.1047 | 5644.9136 | 5619.8132 |
| 2.2034 | 5688.9380 | 5608.2747 | 5581.9279 |
| 2.2144 | 5579.0477 | 5571.6881 | 5544.0425 |
| 2.2254 | 5628.3628 | 5535.2126 | 5506.1572 |
| 2.2364 | 5558.4425 | 5498.8653 | 5468.2718 |
| 2.2474 | 5430.8722 | 5462.6672 | 5430.3865 |
| 2.2584 | 5464.4980 | 5426.6442 | 5392.5011 |
| 2.2694 | 5462.1593 | 5390.8276 | 5354.6158 |
| 2.2804 | 5497.5364 | 5355.2561 | 5316.7304 |
| 2.2914 | 5470.9607 | 5319.9761 | 5278.8451 |
| 2.3024 | 5421.2699 | 5285.0438 | 5240.9597 |
| 2.3134 | 5444.8378 | 5250.5261 | 5203.0744 |
| 2.3244 | 5330.2065 | 5216.5017 | 5165.1890 |
| 2.3354 | 5250.1446 | 5183.0628 | 5127.3037 |
| 2.3464 | 5392.0393 | 5150.3150 | 5089.4183 |
| 2.3574 | 5329.6195 | 5118.3782 | 5051.5330 |
| 2.3684 | 5289.2153 | 5087.3863 | 5013.6476 |
| 2.3794 | 5231.4916 | 5057.4857 | 4975.7623 |
| 2.3904 | 5191.7173 | 5028.8338 | 4937.8769 |
| 2.4014 | 5088.4602 | 5001.5958 | 4899.9916 |
| 2.4124 | 5145.3938 | 4975.9407 | 4862.1062 |
| 2.4234 | 5122.7856 | 4952.0361 | 4824.2209 |
| 2.4344 | 5089.6962 | 4930.0416 | 4786.3355 |
| 2.4454 | 5076.1465 | 4910.1019 | 4748.4502 |
| 2.4564 | 4958.3623 | 4892.3383 | 4710.5648 |
| 2.4674 | 4923.4484 | 4876.8396 | 4672.6795 |
| 2.4784 | 4856.7910 | 4863.6529 | 4634.7941 |
| 2.4894 | 4801.7247 | 4852.7731 | 4596.9088 |
| 2.5004 | 4840.5664 | 4844.1327 | 4559.0234 |
| 2.5114 | 4858.6460 | 4837.5900 | 4521.1381 |
| 2.5224 | 4804.2955 | 4832.9167 | 4483.2527 |
| 2.5334 | 4832.6372 | 4829.7835 | 4445.3674 |
| 2.5444 | 4862.3638 | 4827.7443 | 4407.4820 |
| 2.5554 | 4782.8682 | 4826.2187 | 4369.5966 |
| 2.5664 | 4729.4779 | 4824.4310 | 4331.7113 |
| 2.5774 | 4688.5693 | 4821.5141 | 4293.7163 |
| 2.5884 | 4757.2453 | 4816.3940 | 4255.7213 |
| 2.5994 | 4757.8761 | 4807.9370 | 4217.7263 |
| 2.6104 | 4749.5482 | 4794.8990 | 4179.7313 |
| 2.6214 | 4671.6509 | 4776.0737 | 4141.7362 |
| 2.6324 | 4590.9646 | 4750.4276 | 4103.7412 |
| 2.6434 | 4508.8407 | 4717.2421 | 4065.7462 |
| 2.6544 | 4494.6028 | 4676.2263 | 4027.7512 |
| 2.6654 | 4515.2242 | 4627.5654 | 3989.7562 |
| 2.6764 | 4467.0177 | 4571.8890 | 3951.7612 |
| 2.6874 | 4346.8859 | 4510.1705 | 3913.7662 |
| 2.6984 | 4371.5266 | 4443.5883 | 3875.7712 |
| 2.7094 | 4321.9233 | 4373.3869 | 3837.7762 |
| 2.7204 | 4218.5157 | 4300.7657 | 3799.7811 |
| 2.7314 | 4141.8377 | 4226.8061 | 3761.7861 |
| 2.7424 | 4094.4130 | 4152.4369 | 3723.7911 |
| 2.7534 | 4110.4022 | 4078.3698 | 3685.7961 |
| 2.7644 | 4115.8481 | 4005.2493 | 3647.6656 |
| 2.7754 | 3966.2950 | 3933.5204 | 3609.5350 |
| 2.7864 | 3890.5128 | 3863.5936 | 3571.4044 |
| 2.7974 | 3884.7699 | 3795.7192 | 3533.2739 |
| 2.8084 | 3762.0772 | 3730.0580 | 3495.1433 |
| 2.8194 | 3647.9508 | 3666.6935 | 3457.0128 |
| 2.8304 | 3554.1136 | 3605.6445 | 3418.8822 |
| 2.8414 | 3608.6519 | 3546.8751 | 3380.7517 |
| 2.8524 | 3417.0929 | 3491.2730 | 3342.6211 |
| 2.8634 | 3514.3333 | 3437.4309 | 3304.4905 |
| 2.8744 | 3298.5845 | 3385.3840 | 3266.3600 |
| 2.8854 | 3256.6018 | 3334.9626 | 3228.2294 |
| 2.8964 | 3382.4381 | 3285.8452 | 3190.0989 |
| 2.9074 | 3306.2615 | 3238.1806 | 3151.9683 |
| 2.9184 | 3087.7055 | 3191.8025 | 3113.8378 |
| 2.9294 | 3118.0088 | 3146.5513 | 3075.7072 |
| 2.9404 | 3000.5659 | 3108.7712 | 3037.5766 |
| 2.9514 | 3029.5516 | 3074.7421 | 3015.3429 |
| 2.9624 | 2950.1770 | 3047.9242 | 2993.1092 |
| 2.9734 | 2867.9194 | 3021.7151 | 2970.8755 |
| 2.9844 | 2825.2866 | 2996.0197 | 2948.6418 |
| 2.9954 | 2862.4159 | 2970.7561 | 2926.4081 |
| 3.0064 | 2900.5354 | 2945.8548 | 2904.1744 |
| 3.0174 | 2835.7148 | 2921.2574 | 2881.9407 |
| 3.0284 | 2756.2596 | 2896.9152 | 2859.7070 |
| 3.0394 | 2669.1092 | 2872.7879 | 2837.4733 |
| 3.0504 | 2763.9469 | 2848.8425 | 2815.2396 |
| 3.0614 | 2723.8584 | 2825.0520 | 2793.0059 |
| 3.0724 | 2740.0408 | 2801.3943 | 2770.7722 |
| 3.0834 | 2705.1829 | 2777.8516 | 2748.5385 |
| 3.0944 | 2673.7212 | 2754.4091 | 2726.3047 |
| 3.1054 | 2700.0619 | 2731.0548 | 2704.0710 |
| 3.1164 | 2684.7915 | 2707.7789 | 2681.8373 |
| 3.1274 | 2639.8614 | 2686.5918 | 2659.6036 |
| 3.1384 | 2675.2310 | 2666.3727 | 2642.3125 |
| 3.1494 | 2577.9567 | 2648.2298 | 2625.0215 |
| 3.1604 | 2586.7021 | 2630.1390 | 2607.7304 |
| 3.1714 | 2562.4857 | 2612.0960 | 2590.4393 |
| 3.1824 | 2540.7217 | 2594.0969 | 2573.1482 |
| 3.1934 | 2511.4779 | 2576.1385 | 2555.8572 |
| 3.2044 | 2529.2630 | 2558.2175 | 2538.5661 |
| 3.2154 | 2498.7669 | 2540.3315 | 2521.2750 |
| 3.2264 | 2488.0590 | 2522.4777 | 2503.9839 |
| 3.2374 | 2526.6765 | 2504.6542 | 2486.6928 |
| 3.2484 | 2465.3333 | 2486.8587 | 2469.4018 |
| 3.2594 | 2407.1799 | 2469.0896 | 2452.1107 |
| 3.2704 | 2396.1731 | 2451.3449 | 2434.8196 |
| 3.2814 | 2386.0590 | 2433.6233 | 2417.5285 |
| 3.2924 | 2409.4823 | 2415.9233 | 2400.2374 |
| 3.3034 | 2393.7532 | 2398.2434 | 2382.9464 |
| 3.3144 | 2337.0428 | 2382.8038 | 2365.6553 |
| 3.3254 | 2359.4248 | 2368.3775 | 2353.8020 |
| 3.3364 | 2351.7429 | 2356.1891 | 2341.9488 |
| 3.3474 | 2315.5260 | 2344.0166 | 2330.0955 |
| 3.3584 | 2329.9440 | 2331.8591 | 2318.2423 |
| 3.3694 | 2330.2173 | 2319.7156 | 2306.3890 |
| 3.3804 | 2261.2080 | 2307.5854 | 2294.5357 |
| 3.3914 | 2245.1681 | 2295.4678 | 2282.6825 |
| 3.4024 | 2261.0487 | 2283.3621 | 2270.8292 |
| 3.4134 | 2230.0315 | 2271.2677 | 2258.9760 |
| 3.4244 | 2288.3186 | 2259.1839 | 2247.1227 |
| 3.4354 | 2271.4769 | 2247.1102 | 2235.2695 |
| 3.4464 | 2211.4582 | 2235.0462 | 2223.4162 |
| 3.4574 | 2206.6224 | 2222.9913 | 2211.5630 |
| 3.4684 | 2226.0413 | 2210.9450 | 2199.7097 |
| 3.4794 | 2196.8859 | 2198.9069 | 2187.8564 |
| 3.4904 | 2200.0531 | 2186.8767 | 2176.0032 |
| 3.5014 | 2183.4503 | 2174.8484 | 2164.1499 |
| 3.5124 | 2101.9803 | 2162.8246 | 2152.2829 |
| 3.5234 | 2119.7316 | 2150.8019 | 2140.4158 |
| 3.5344 | 2123.9970 | 2138.7857 | 2128.5487 |
| 3.5454 | 2101.1436 | 2126.7757 | 2116.6816 |
| 3.5564 | 2033.4248 | 2114.7716 | 2104.8145 |
| 3.5674 | 2098.2036 | 2102.7731 | 2092.9475 |
| 3.5784 | 2140.8796 | 2090.7800 | 2081.0804 |
| 3.5894 | 2118.8230 | 2078.7921 | 2069.2133 |
| 3.6004 | 1957.6882 | 2066.8091 | 2057.3462 |
| 3.6114 | 2011.1338 | 2054.8309 | 2045.4791 |
| 3.6224 | 2071.4985 | 2042.8572 | 2033.6120 |
| 3.6334 | 2061.9803 | 2030.8879 | 2021.7450 |
| 3.6444 | 1984.0083 | 2018.9228 | 2009.8779 |
| 3.6554 | 1974.9056 | 2006.9616 | 1998.0108 |
| 3.6664 | 2032.4926 | 1995.0044 | 1986.1437 |
| 3.6774 | 1945.6253 | 1983.0509 | 1974.2766 |
| 3.6884 | 1962.6991 | 1972.3152 | 1962.4096 |
| 3.6994 | 1930.3943 | 1962.1273 | 1953.5154 |
| 3.7104 | 1992.0733 | 1953.1570 | 1944.6212 |
| 3.7214 | 1976.9823 | 1944.1899 | 1935.7270 |
| 3.7324 | 1926.6558 | 1935.2258 | 1926.8328 |
| 3.7434 | 1908.8702 | 1926.2647 | 1917.9386 |
| 3.7544 | 1974.7994 | 1917.3066 | 1909.0444 |
| 3.7654 | 1932.5713 | 1908.3511 | 1900.1502 |
| 3.7764 | 1915.3382 | 1899.3984 | 1891.2560 |
| 3.7874 | 1977.4425 | 1890.4482 | 1882.3618 |
| 3.7984 | 2015.5250 | 1881.5006 | 1873.4676 |
| 3.8094 | 1877.7325 | 1872.5554 | 1864.5734 |
| 3.8204 | 1862.9336 | 1863.6125 | 1855.6792 |
| 3.8314 | 1927.7424 | 1854.6719 | 1846.7849 |
| 3.8424 | 1874.0000 | 1845.7335 | 1837.8907 |
| 3.8534 | 1868.2891 | 1836.7973 | 1828.9965 |
| 3.8644 | 1785.6141 | 1827.8631 | 1820.1023 |
| 3.8754 | 1783.5054 | 1820.4611 | 1811.2081 |
| 3.8864 | 1816.5310 | 1813.7469 | 1806.0600 |
| 3.8974 | 1875.0157 | 1808.5647 | 1800.9119 |
| 3.9084 | 1813.2527 | 1803.3844 | 1795.7638 |
| 3.9194 | 1811.1180 | 1798.2058 | 1790.6157 |
| 3.9304 | 1784.2832 | 1793.0291 | 1785.4676 |
| 3.9414 | 1764.9194 | 1787.8540 | 1780.3195 |
| 3.9524 | 1745.9307 | 1782.6806 | 1775.1713 |
| 3.9634 | 1767.0197 | 1777.5089 | 1770.0232 |
| 3.9744 | 1807.5944 | 1772.3387 | 1764.8751 |
| 3.9854 | 1762.4248 | 1767.1701 | 1759.7270 |
| 3.9964 | 1777.2562 | 1762.0030 | 1754.5789 |
| 4.0074 | 1811.1514 | 1756.8373 | 1749.4308 |
| 4.0184 | 1763.7773 | 1751.6732 | 1744.2827 |
| 4.0294 | 1739.1386 | 1746.5104 | 1739.1345 |
| 4.0404 | 1749.9169 | 1741.3491 | 1733.9864 |
| 4.0514 | 1747.2743 | 1736.1890 | 1728.8383 |
| 4.0624 | 1733.3717 | 1730.9953 | 1723.6902 |
| 4.0734 | 1739.1642 | 1725.7872 | 1718.4563 |
| 4.0844 | 1697.1902 | 1720.5454 | 1713.2224 |
| 4.0954 | 1670.1711 | 1715.3048 | 1707.9885 |
| 4.1064 | 1718.6150 | 1710.0654 | 1702.7546 |
| 4.1174 | 1724.3924 | 1704.8273 | 1697.5207 |
| 4.1284 | 1747.7635 | 1699.5903 | 1692.2868 |
| 4.1394 | 1691.2409 | 1694.3546 | 1687.0529 |
| 4.1504 | 1652.3805 | 1689.1200 | 1681.8190 |
| 4.1614 | 1654.3638 | 1683.8865 | 1676.5851 |
| 4.1724 | 1671.8029 | 1678.6542 | 1671.3512 |
| 4.1834 | 1649.1327 | 1673.4230 | 1666.1173 |
| 4.1944 | 1643.3073 | 1668.1928 | 1660.8835 |

Scan List

| Vis. | Dataset Name | Start pos. [°2θ] | End pos. [°2θ] | Step [°2θ] | Meas.Date/Time |
| --- | --- | --- | --- | --- | --- |
| * | 11 Etosha22 MoiSub 10-15cm S1 | 2.0054 | 29.9894 | 0.0110 | 12/1/2023 11:49:06 AM |

Peak List

| Pos. [°2θ] | Height [cts] | FWHM Left [°2θ] | d-spacing [Å] | Rel. Int. [%] |
| --- | --- | --- | --- | --- |
| 2.6425 | 581.98 | 0.2598 | 33.40660 | 34.13 |
| 7.1819 | 1705.28 | 0.4330 | 12.29869 | 100.00 |
| 8.7396 | 315.58 | 0.1948 | 10.10972 | 18.51 |
| 12.8758 | 30.36 | 0.4330 | 6.86994 | 1.78 |
| 15.7208 | 552.17 | 0.0866 | 5.63251 | 32.38 |
| 17.5883 | 31.78 | 0.3464 | 5.03842 | 1.86 |
| 18.1888 | 69.06 | 0.1299 | 4.87341 | 4.05 |
| 19.5799 | 35.35 | 0.3464 | 4.53020 | 2.07 |
| 25.8854 | 424.32 | 0.0866 | 3.43920 | 24.88 |
| 26.6930 | 179.20 | 0.0649 | 3.33694 | 10.51 |
| 27.4562 | 97.72 | 0.1515 | 3.24589 | 5.73 |

Pattern List

| Visible | Ref.Code | Score | Compound Name | Chem. Formula | Mineral Name | SemiQuant[%] |
| --- | --- | --- | --- | --- | --- | --- |
| * | 01-085-2272 | 53 | Potassium Sodium Iron Magnesium Aluminum Silicate Fluoride Hydroxide | ( K0.93 Na0.04 ) ( Mg2.55 Fe0.21 Al0.24 ) ( Si2.65 Al1.35 O10 ) ( ( O H )1.91 F0.09 ) | Phlogopite-1M | 29 |
| * | 04-007-4874 | 37 | Titanium Oxide | Ti O2 | Rutile | 2 |
| * | 04-009-3254 | 37 | Sodium Aluminum Silicon Oxide Hydrate | Na8 Al8 Si16 O48 ( H2 O )8 | Analcime | 10 |
| * | 01-078-5138 | 43 | Potassium Sodium Calcium Magnesium Aluminum Iron Aluminum Silicate Hydroxide | ( K0.71 Ca0.01 Na0.01 ) ( Al1.86 Mg0.15 Fe0.04 ) ( ( Si3.27 Al0.73 ) O10 ( O H )2 ) | Illite, syn (NR) | 16 |
| * | 01-078-4316 | 20 | Sodium Calcium Magnesium Aluminum Iron Titanium Aluminum Silicon Oxide Hydroxide Hydrate | ( Mg2.46 Al0.3 Fe0.22 Ti0.021 )2 ( Mg0.38 Ca0.03 Na0.02 )2 ( ( Si2.83 Al1.17 ) O10 )2 ( O H )4 ( H2 O )3.4 | Vermiculite | 2 |
| * | 01-080-5019 | 29 | Magnesium Silicate Hydroxide Hydrate | Mg7.68 ( Si12 O30 ) ( O H )4 ( H2 O )4 ( H2 O )6 | Sepiolite | 13 |
| * | 04-024-3136 | 46 | Uranyl Aluminum Phosphate Hydroxide Hydrate | ( U O2 )4 Al4 ( P O4 )6 ( O H )2 ( H2 O )19.5 | Furongite | 2 |
| * | 04-025-4215 | 44 | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide | Mg10.4 V0.36 Mn33.5 Fe0.14 Al0.69 Si6.77 As6.5 P0.3 O54 ( O H )42 | Carlfrancisite | 13 |
| * | 04-017-7286 | 35 | Potassium Manganese Aluminum Silicon Oxide Hydroxide Hydrate | K0.8 Mn4 Al1.08 Si4.92 O16 ( O H )2 ( H2 O )3 | Ganophyllite | 14 |

Anchor Scan Parameters

Dataset Name	11 Etosha22 MoiSub 10-15cm S1

File name	C:\aeris_data\XRD data\Goldstein\Etosha 2023\Etosha Clay Data\Sample 11\11 Etosha22 MoiSub 10-15cm S1.xrdml

Sample Identification	11 Etosha22 MoiSub 10-15cm S1

Measurement Start Date/Time	12/1/2023 11:49:06 AM

Operator	Instrument

Raw Data Origin	XRD measurement (*.XRDML)

Scan Axis	Gonio

Start Position [°2θ]	2.0054

End Position [°2θ]	29.9894

Step Size [°2θ]	0.0110

Scan Step Time [s]	48.1950

Scan Type	Continuous

PSD Mode	Scanning

PSD Length [°2θ]	5.54

Offset [°2θ]	0.0000

Divergence Slit Type	Fixed

Divergence Slit Size [°]	0.0603

Specimen Length [mm]	10.00

Measurement Temperature [°C]	25.00

Anode Material	Cu

K-α1 [Å]	1.54060

K-α2 [Å]	1.54443

K-β1 [Å]	1.39225

K-A2 / K-A1 Ratio	0.50000

Generator Settings	15 mA, 40 kV

Diffractometer Type	2082464

Diffractometer Number	0

Goniometer Radius [mm]	145.00

Dist. Focus-Diverg. Slit [mm]	95.00

Incident Beam Monochromator	No

Spinning	Yes