12 Etosha 22 CRT 0-0.1 cm S2 400 C

Graphics

Graphics

Graphics

Quantitative Results

Phase Potassium Sodium Calcium Manganese Aluminum Iron Silicon Oxide Hydroxide Hydrate

Weight fraction/ %	10.0

Phase Sodium Aluminum Silicate Hydrate

Weight fraction/ %	27.0

Phase Potassium Magnesium Iron Silicate Oxide Hydroxide

Weight fraction/ %	50.0

Phase Magnesium Aluminum Silicon Oxide Hydroxide Hydrate

Weight fraction/ %	12.0

Multiple Quantitative Results

Scans vs Phases Matrix

| Scan name | Potassium Sodium Calcium Manganese Aluminum Iron Silicon Oxide Hydroxide Hydrate | Sodium Aluminum Silicate Hydrate | Potassium Magnesium Iron Silicate Oxide Hydroxide | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide | Magnesium Aluminum Silicon Oxide Hydroxide Hydrate |
| --- | --- | --- | --- | --- | --- |
| 12 Etosha22 Crt 0-0.1cm S2 heat400c | 10.0 | 27.0 | 50.0 | 0.0 | 12.0 |

Anchor Scan Data

| Pos. [°2θ] | Iobs [cts] | Icalc [cts] | Iback [cts] |
| --- | --- | --- | --- |
| 2.0054 | 4817.0000 | 4811.0044 | 4817.0000 |
| 2.0164 | 4830.3609 | 4787.8083 | 4787.8083 |
| 2.0274 | 4781.7778 | 4758.6166 | 4758.6166 |
| 2.0384 | 4881.9336 | 4729.4249 | 4729.4249 |
| 2.0494 | 4620.0816 | 4700.2332 | 4700.2332 |
| 2.0604 | 4637.4356 | 4671.0415 | 4671.0415 |
| 2.0714 | 4597.6755 | 4641.8499 | 4641.8499 |
| 2.0824 | 4752.7473 | 4612.6582 | 4612.6582 |
| 2.0934 | 4454.2911 | 4583.4665 | 4583.4665 |
| 2.1044 | 4559.3673 | 4554.2748 | 4554.2748 |
| 2.1154 | 4503.1622 | 4525.0831 | 4525.0831 |
| 2.1264 | 4524.4518 | 4495.8914 | 4495.8914 |
| 2.1374 | 4439.3068 | 4466.6997 | 4466.6997 |
| 2.1484 | 4502.9857 | 4437.5080 | 4437.5080 |
| 2.1594 | 4410.5713 | 4408.3163 | 4408.3163 |
| 2.1704 | 4436.6755 | 4379.1246 | 4379.1246 |
| 2.1814 | 4384.5103 | 4349.9329 | 4349.9329 |
| 2.1924 | 4330.8368 | 4321.7209 | 4320.7413 |
| 2.2034 | 4229.5487 | 4296.3193 | 4296.3193 |
| 2.2144 | 4245.0418 | 4271.8974 | 4271.8974 |
| 2.2254 | 4281.6873 | 4247.4755 | 4247.4755 |
| 2.2364 | 4291.4513 | 4223.0535 | 4223.0535 |
| 2.2474 | 4232.9194 | 4198.6316 | 4198.6316 |
| 2.2584 | 4109.0502 | 4174.2097 | 4174.2097 |
| 2.2694 | 4130.1917 | 4149.7877 | 4149.7877 |
| 2.2804 | 4063.5929 | 4125.3658 | 4125.3658 |
| 2.2914 | 4054.3432 | 4100.9439 | 4100.9439 |
| 2.3024 | 4024.6903 | 4076.5219 | 4076.5219 |
| 2.3134 | 4142.2861 | 4052.1000 | 4052.1000 |
| 2.3244 | 4052.3063 | 4027.6781 | 4027.6781 |
| 2.3354 | 3952.5133 | 4003.2561 | 4003.2561 |
| 2.3464 | 3985.8206 | 3978.8342 | 3978.8342 |
| 2.3574 | 4043.6686 | 3954.4122 | 3954.4122 |
| 2.3684 | 3916.0752 | 3929.9903 | 3929.9903 |
| 2.3794 | 3852.2675 | 3905.7821 | 3905.5684 |
| 2.3904 | 3909.8943 | 3882.1871 | 3882.1871 |
| 2.4014 | 3862.8230 | 3858.8059 | 3858.8059 |
| 2.4124 | 3824.7458 | 3835.4246 | 3835.4246 |
| 2.4234 | 3821.8928 | 3812.0434 | 3812.0434 |
| 2.4344 | 3763.6445 | 3788.6621 | 3788.6621 |
| 2.4454 | 3735.4179 | 3765.2809 | 3765.2809 |
| 2.4564 | 3724.1101 | 3741.8996 | 3741.8996 |
| 2.4674 | 3730.2566 | 3718.5184 | 3718.5184 |
| 2.4784 | 3696.0457 | 3695.1371 | 3695.1371 |
| 2.4894 | 3711.4789 | 3671.7559 | 3671.7559 |
| 2.5004 | 3660.9292 | 3648.3746 | 3648.3746 |
| 2.5114 | 3586.7807 | 3624.9933 | 3624.9933 |
| 2.5224 | 3512.1008 | 3601.6121 | 3601.6121 |
| 2.5334 | 3484.5988 | 3578.2308 | 3578.2308 |
| 2.5444 | 3547.3741 | 3554.8496 | 3554.8496 |
| 2.5554 | 3566.3235 | 3531.4683 | 3531.4683 |
| 2.5664 | 3506.3451 | 3509.1653 | 3508.0871 |
| 2.5774 | 3452.6303 | 3489.9554 | 3489.9554 |
| 2.5884 | 3471.2684 | 3471.8237 | 3471.8237 |
| 2.5994 | 3484.6814 | 3453.6919 | 3453.6919 |
| 2.6104 | 3467.4518 | 3435.5602 | 3435.5602 |
| 2.6214 | 3442.1042 | 3417.4285 | 3417.4285 |
| 2.6324 | 3386.3599 | 3399.2968 | 3399.2968 |
| 2.6434 | 3465.0905 | 3381.1651 | 3381.1651 |
| 2.6544 | 3455.6883 | 3363.0334 | 3363.0334 |
| 2.6654 | 3406.0265 | 3344.9017 | 3344.9017 |
| 2.6764 | 3386.0029 | 3326.7699 | 3326.7699 |
| 2.6874 | 3369.2832 | 3308.6382 | 3308.6382 |
| 2.6984 | 3363.4513 | 3290.5065 | 3290.5065 |
| 2.7094 | 3218.2605 | 3272.3748 | 3272.3748 |
| 2.7204 | 3291.6475 | 3254.2431 | 3254.2431 |
| 2.7314 | 3216.1652 | 3236.1114 | 3236.1114 |
| 2.7424 | 3244.7040 | 3217.9797 | 3217.9797 |
| 2.7534 | 3225.9115 | 3199.8247 | 3199.8480 |
| 2.7644 | 3147.9130 | 3181.6030 | 3181.6030 |
| 2.7754 | 3185.7621 | 3163.3580 | 3163.3580 |
| 2.7864 | 3147.7488 | 3145.1130 | 3145.1130 |
| 2.7974 | 3115.3363 | 3126.8680 | 3126.8680 |
| 2.8084 | 3095.8496 | 3108.6230 | 3108.6230 |
| 2.8194 | 3021.2370 | 3090.3780 | 3090.3780 |
| 2.8304 | 3067.4661 | 3072.1330 | 3072.1330 |
| 2.8414 | 3111.2330 | 3053.8881 | 3053.8881 |
| 2.8524 | 3128.1962 | 3035.6431 | 3035.6431 |
| 2.8634 | 3042.7168 | 3017.3981 | 3017.3981 |
| 2.8744 | 2900.1480 | 2999.1531 | 2999.1531 |
| 2.8854 | 2979.5792 | 2980.9081 | 2980.9081 |
| 2.8964 | 3037.7478 | 2962.6631 | 2962.6631 |
| 2.9074 | 2956.2360 | 2944.4181 | 2944.4181 |
| 2.9184 | 2985.3146 | 2926.1731 | 2926.1731 |
| 2.9294 | 2948.4631 | 2907.9282 | 2907.9282 |
| 2.9404 | 2844.5211 | 2889.6832 | 2889.6832 |
| 2.9514 | 2879.5093 | 2871.4382 | 2871.4382 |
| 2.9624 | 2913.9292 | 2853.1932 | 2853.1932 |
| 2.9734 | 2818.2655 | 2834.9482 | 2834.9482 |
| 2.9844 | 2800.8913 | 2816.7032 | 2816.7032 |
| 2.9954 | 2717.8850 | 2798.4582 | 2798.4582 |
| 3.0064 | 2752.9572 | 2780.2132 | 2780.2132 |
| 3.0174 | 2710.8771 | 2761.9683 | 2761.9683 |
| 3.0284 | 2721.5590 | 2743.7233 | 2743.7233 |
| 3.0394 | 2670.3786 | 2725.4783 | 2725.4783 |
| 3.0504 | 2679.2385 | 2707.2333 | 2707.2333 |
| 3.0614 | 2713.5486 | 2688.9883 | 2688.9883 |
| 3.0724 | 2605.6873 | 2670.7433 | 2670.7433 |
| 3.0834 | 2645.2969 | 2652.4983 | 2652.4983 |
| 3.0944 | 2621.2699 | 2634.2533 | 2634.2533 |
| 3.1054 | 2699.7365 | 2616.0084 | 2616.0084 |
| 3.1164 | 2608.2414 | 2597.7634 | 2597.7634 |
| 3.1274 | 2606.4631 | 2579.4951 | 2579.5184 |
| 3.1384 | 2571.6042 | 2561.1601 | 2561.1601 |
| 3.1494 | 2502.6785 | 2542.8019 | 2542.8019 |
| 3.1604 | 2495.0118 | 2524.4436 | 2524.4436 |
| 3.1714 | 2471.2508 | 2506.0853 | 2506.0853 |
| 3.1824 | 2505.6317 | 2487.7271 | 2487.7271 |
| 3.1934 | 2388.7611 | 2469.3688 | 2469.3688 |
| 3.2044 | 2376.9808 | 2451.0106 | 2451.0106 |
| 3.2154 | 2371.8319 | 2432.6523 | 2432.6523 |
| 3.2264 | 2379.8437 | 2414.2940 | 2414.2940 |
| 3.2374 | 2376.1317 | 2395.9358 | 2395.9358 |
| 3.2484 | 2347.8889 | 2377.5775 | 2377.5775 |
| 3.2594 | 2336.6843 | 2359.2193 | 2359.2193 |
| 3.2704 | 2316.0394 | 2340.8610 | 2340.8610 |
| 3.2814 | 2375.9607 | 2322.5027 | 2322.5027 |
| 3.2924 | 2310.8451 | 2304.1445 | 2304.1445 |
| 3.3034 | 2242.6696 | 2285.7862 | 2285.7862 |
| 3.3144 | 2297.1318 | 2268.1060 | 2267.4280 |
| 3.3254 | 2266.5339 | 2252.3711 | 2252.3711 |
| 3.3364 | 2204.9489 | 2237.3142 | 2237.3142 |
| 3.3474 | 2257.4504 | 2222.2574 | 2222.2574 |
| 3.3584 | 2277.2920 | 2207.2005 | 2207.2005 |
| 3.3694 | 2238.5664 | 2192.1437 | 2192.1437 |
| 3.3804 | 2224.6362 | 2177.0868 | 2177.0868 |
| 3.3914 | 2161.8407 | 2162.0299 | 2162.0299 |
| 3.4024 | 2151.0236 | 2146.9731 | 2146.9731 |
| 3.4134 | 2119.2350 | 2131.9162 | 2131.9162 |
| 3.4244 | 2063.4602 | 2116.8594 | 2116.8594 |
| 3.4354 | 2104.4248 | 2101.8025 | 2101.8025 |
| 3.4464 | 2129.0683 | 2086.7456 | 2086.7456 |
| 3.4574 | 2082.2979 | 2071.6888 | 2071.6888 |
| 3.4684 | 2008.7620 | 2056.6319 | 2056.6319 |
| 3.4794 | 2026.9371 | 2041.5751 | 2041.5751 |
| 3.4904 | 2070.4602 | 2026.5182 | 2026.5182 |
| 3.5014 | 2061.8672 | 2011.4613 | 2011.4613 |
| 3.5124 | 1991.4513 | 1996.4045 | 1996.4045 |
| 3.5234 | 2014.5162 | 1981.3476 | 1981.3476 |
| 3.5344 | 1975.3643 | 1966.2908 | 1966.2908 |
| 3.5454 | 1903.1514 | 1951.2339 | 1951.2339 |
| 3.5564 | 1920.9189 | 1936.1770 | 1936.1770 |
| 3.5674 | 1911.6401 | 1921.1202 | 1921.1202 |
| 3.5784 | 1960.8216 | 1906.0633 | 1906.0633 |
| 3.5894 | 1888.1504 | 1891.0065 | 1891.0065 |
| 3.6004 | 1850.8314 | 1876.0092 | 1875.9496 |
| 3.6114 | 1939.3668 | 1860.9738 | 1860.8927 |
| 3.6224 | 1872.6401 | 1845.9481 | 1845.8359 |
| 3.6334 | 1855.9145 | 1830.9031 | 1830.7790 |
| 3.6444 | 1773.8633 | 1815.8479 | 1815.7221 |
| 3.6554 | 1826.1800 | 1800.7927 | 1800.6653 |
| 3.6664 | 1786.7871 | 1785.7375 | 1785.6084 |
| 3.6774 | 1784.0777 | 1770.6823 | 1770.5516 |
| 3.6884 | 1664.3672 | 1756.2525 | 1755.4947 |
| 3.6994 | 1802.4583 | 1743.6165 | 1743.4822 |
| 3.7104 | 1776.6494 | 1731.6057 | 1731.4696 |
| 3.7214 | 1773.8348 | 1719.5950 | 1719.4571 |
| 3.7324 | 1681.9601 | 1707.5844 | 1707.4445 |
| 3.7434 | 1693.8397 | 1695.5738 | 1695.4320 |
| 3.7544 | 1671.1431 | 1683.5632 | 1683.4194 |
| 3.7654 | 1660.3343 | 1671.5527 | 1671.4069 |
| 3.7764 | 1671.7463 | 1659.5422 | 1659.3944 |
| 3.7874 | 1633.3451 | 1647.5317 | 1647.3818 |
| 3.7984 | 1670.7109 | 1635.5213 | 1635.3693 |
| 3.8094 | 1587.4720 | 1623.5110 | 1623.3567 |
| 3.8204 | 1615.1224 | 1611.5006 | 1611.3442 |
| 3.8314 | 1550.8869 | 1599.4904 | 1599.3316 |
| 3.8424 | 1570.1062 | 1587.4802 | 1587.3191 |
| 3.8534 | 1533.9882 | 1575.4700 | 1575.3065 |
| 3.8644 | 1512.4101 | 1563.4599 | 1563.2940 |
| 3.8754 | 1601.5369 | 1551.4499 | 1551.2815 |
| 3.8864 | 1595.1947 | 1539.4399 | 1539.2689 |
| 3.8974 | 1493.6234 | 1527.4299 | 1527.2564 |
| 3.9084 | 1507.6824 | 1515.4201 | 1515.2438 |
| 3.9194 | 1465.1091 | 1503.4103 | 1503.2313 |
| 3.9304 | 1474.2640 | 1491.4005 | 1491.2187 |
| 3.9414 | 1486.8368 | 1479.3908 | 1479.2062 |
| 3.9524 | 1488.8083 | 1467.3812 | 1467.1936 |
| 3.9634 | 1485.2851 | 1455.3717 | 1455.1811 |
| 3.9744 | 1405.9965 | 1443.3622 | 1443.1686 |
| 3.9854 | 1404.7611 | 1431.3528 | 1431.1560 |
| 3.9964 | 1504.8987 | 1419.3435 | 1419.1435 |
| 4.0074 | 1496.1514 | 1407.3342 | 1407.1309 |
| 4.0184 | 1455.5074 | 1395.3251 | 1395.1184 |
| 4.0294 | 1420.0137 | 1383.3160 | 1383.1058 |
| 4.0404 | 1348.3938 | 1371.3070 | 1371.0933 |
| 4.0514 | 1371.7198 | 1359.2981 | 1359.0807 |
| 4.0624 | 1364.2881 | 1347.7873 | 1347.0682 |
| 4.0734 | 1328.7286 | 1337.7054 | 1337.4804 |
| 4.0844 | 1322.4646 | 1328.1216 | 1327.8927 |
| 4.0954 | 1319.4946 | 1318.5379 | 1318.3049 |
| 4.1064 | 1359.4012 | 1308.9543 | 1308.7172 |
| 4.1174 | 1303.2094 | 1299.3708 | 1299.1294 |
| 4.1284 | 1260.1878 | 1289.7875 | 1289.5417 |
| 4.1394 | 1273.6155 | 1280.2042 | 1279.9539 |
| 4.1504 | 1279.7448 | 1270.6211 | 1270.3662 |
| 4.1614 | 1298.1809 | 1261.0381 | 1260.7784 |
| 4.1724 | 1301.5732 | 1251.4552 | 1251.1907 |
| 4.1834 | 1282.6283 | 1241.8725 | 1241.6029 |
| 4.1944 | 1280.5806 | 1232.2899 | 1232.0152 |

Scan List

| Vis. | Dataset Name | Start pos. [°2θ] | End pos. [°2θ] | Step [°2θ] | Meas.Date/Time |
| --- | --- | --- | --- | --- | --- |
| * | 12 Etosha22 Crt 0-0.1cm S2 heat400c | 2.0054 | 29.9894 | 0.0110 | 12/4/2023 12:43:46 PM |

Peak List

| Pos. [°2θ] | Height [cts] | FWHM Left [°2θ] | d-spacing [Å] | Rel. Int. [%] |
| --- | --- | --- | --- | --- |
| 5.3346 | 85.42 | 0.1732 | 16.55253 | 38.03 |
| 7.0568 | 224.60 | 0.2598 | 12.51635 | 100.00 |
| 8.7862 | 112.09 | 0.1732 | 10.05628 | 49.91 |
| 15.8597 | 124.08 | 0.1515 | 5.58348 | 55.25 |
| 19.7470 | 9.46 | 0.5196 | 4.49222 | 4.21 |
| 26.0374 | 50.27 | 0.1299 | 3.41947 | 22.38 |

Pattern List

| Visible | Ref.Code | Score | Compound Name | Chem. Formula | Mineral Name | SemiQuant[%] |
| --- | --- | --- | --- | --- | --- | --- |
| * | 04-016-0693 | 65 | Potassium Sodium Calcium Manganese Aluminum Iron Silicon Oxide Hydroxide Hydrate | K0.3 Na0.4 Ca0.3 Mn3.9 Fe0.1 Al1.4 Si5.3 O16 ( O H )2.7 ( H2 O )3.5 | Ganophyllite | 10 |
| * | 01-083-1731 | 51 | Sodium Aluminum Silicate Hydrate | Na14.80 Al14.24 Si33.76 O96 ( H2 O )16 | Analcime | 27 |
| * | 01-082-2701 | 46 | Potassium Magnesium Iron Silicate Oxide Hydroxide | K ( Mg2.41 Fe0.59 ) ( Si2 O5 )2 ( O0.72 ( O H )1.28 ) | Phlogopite-2M1 | 50 |
| * | 04-025-4215 | No Matching Lines | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide | Mg10.4 V0.36 Mn33.5 Fe0.14 Al0.69 Si6.77 As6.5 P0.3 O54 ( O H )42 | Carlfrancisite | - |
| * | 04-017-1305 | 4 | Magnesium Aluminum Silicon Oxide Hydroxide Hydrate | Mg Al Si4 O10 ( O H ) ( H2 O )2 | Palygorskite-M | 12 |

Anchor Scan Parameters

Dataset Name	12 Etosha22 Crt 0-0.1cm S2 heat400c

File name	C:\aeris_data\XRD data\Goldstein\Etosha 2023\Etosha Clay Data\Sample 12\12 Etosha22 Crt 0-0.1cm S2 heat400c.xrdml

Sample Identification	12 Etosha22 Crt 0-0.1cm S2 heat400c

Measurement Start Date/Time	12/4/2023 12:43:46 PM

Operator	Instrument

Raw Data Origin	XRD measurement (*.XRDML)

Scan Axis	Gonio

Start Position [°2θ]	2.0054

End Position [°2θ]	29.9894

Step Size [°2θ]	0.0110

Scan Step Time [s]	48.1950

Scan Type	Continuous

PSD Mode	Scanning

PSD Length [°2θ]	5.54

Offset [°2θ]	0.0000

Divergence Slit Type	Fixed

Divergence Slit Size [°]	0.0603

Specimen Length [mm]	10.00

Measurement Temperature [°C]	25.00

Anode Material	Cu

K-α1 [Å]	1.54060

K-α2 [Å]	1.54443

K-β1 [Å]	1.39225

K-A2 / K-A1 Ratio	0.50000

Generator Settings	15 mA, 40 kV

Diffractometer Type	2082464

Diffractometer Number	0

Goniometer Radius [mm]	145.00

Dist. Focus-Diverg. Slit [mm]	95.00

Incident Beam Monochromator	No

Spinning	Yes