12 Etosha 22 CRT 0-0.1 cm S2 550C

Graphics

Graphics

Graphics

Quantitative Results

Phase Potassium Sodium Barium Magnesium Iron Aluminum Silicon Oxide Fluoride

Weight fraction/ %	90.0

Phase Magnesium Aluminum Silicon Oxide Hydroxide Hydrate

Weight fraction/ %	10.0

Multiple Quantitative Results

Scans vs Phases Matrix

| Scan name | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide | Potassium Sodium Barium Magnesium Iron Aluminum Silicon Oxide Fluoride | Magnesium Aluminum Silicon Oxide Hydroxide Hydrate | Sodium Aluminum Silicate Hydrate |
| --- | --- | --- | --- | --- |
| 12 Etosha22 Crt 0-0.1cm S2 heat550c | 0.0 | 90.0 | 10.0 | 0.0 |

Anchor Scan Data

| Pos. [°2θ] | Iobs [cts] | Icalc [cts] | Iback [cts] |
| --- | --- | --- | --- |
| 2.0054 | 4811.0000 | 4796.7465 | 4811.0000 |
| 2.0164 | 4961.5988 | 4780.6803 | 4780.6803 |
| 2.0274 | 4843.7394 | 4750.3605 | 4750.3605 |
| 2.0384 | 4638.3555 | 4720.0408 | 4720.0408 |
| 2.0494 | 4727.4258 | 4689.7210 | 4689.7210 |
| 2.0604 | 4751.5585 | 4659.4013 | 4659.4013 |
| 2.0714 | 4693.2478 | 4629.0815 | 4629.0815 |
| 2.0824 | 4615.2355 | 4598.7618 | 4598.7618 |
| 2.0934 | 4551.7384 | 4568.4420 | 4568.4420 |
| 2.1044 | 4532.7699 | 4538.1223 | 4538.1223 |
| 2.1154 | 4535.8151 | 4507.8025 | 4507.8025 |
| 2.1264 | 4458.4336 | 4477.4828 | 4477.4828 |
| 2.1374 | 4479.8997 | 4447.1630 | 4447.1630 |
| 2.1484 | 4490.1922 | 4416.8433 | 4416.8433 |
| 2.1594 | 4371.3668 | 4386.5235 | 4386.5235 |
| 2.1704 | 4393.5192 | 4356.2038 | 4356.2038 |
| 2.1814 | 4343.2173 | 4325.8840 | 4325.8840 |
| 2.1924 | 4282.6421 | 4298.1584 | 4295.5643 |
| 2.2034 | 4243.6991 | 4270.7627 | 4270.7627 |
| 2.2144 | 4243.2212 | 4245.9612 | 4245.9612 |
| 2.2254 | 4308.0551 | 4221.1596 | 4221.1596 |
| 2.2364 | 4237.7714 | 4196.3581 | 4196.3581 |
| 2.2474 | 4173.9902 | 4171.5565 | 4171.5565 |
| 2.2584 | 4108.1268 | 4146.7550 | 4146.7550 |
| 2.2694 | 4086.5546 | 4121.9535 | 4121.9535 |
| 2.2804 | 4111.3019 | 4097.2208 | 4097.1519 |
| 2.2914 | 4121.9587 | 4072.4539 | 4072.3504 |
| 2.3024 | 4086.8319 | 4047.6878 | 4047.5488 |
| 2.3134 | 3963.8191 | 4022.9044 | 4022.7473 |
| 2.3244 | 3912.2778 | 3998.1040 | 3997.9458 |
| 2.3354 | 3923.7906 | 3973.3036 | 3973.1442 |
| 2.3464 | 3876.5344 | 3948.5033 | 3948.3427 |
| 2.3574 | 3961.3471 | 3923.7029 | 3923.5411 |
| 2.3684 | 3932.9926 | 3898.9026 | 3898.7396 |
| 2.3794 | 3878.4041 | 3876.4083 | 3873.9381 |
| 2.3904 | 3803.7473 | 3854.2073 | 3854.0419 |
| 2.4014 | 3768.9823 | 3834.3124 | 3834.1457 |
| 2.4124 | 3794.4646 | 3814.4175 | 3814.2495 |
| 2.4234 | 3733.9951 | 3794.5226 | 3794.3534 |
| 2.4344 | 3680.1416 | 3774.6277 | 3774.4572 |
| 2.4454 | 3669.9695 | 3754.7328 | 3754.5610 |
| 2.4564 | 3733.4558 | 3734.8380 | 3734.6648 |
| 2.4674 | 3812.7021 | 3714.9431 | 3714.7687 |
| 2.4784 | 3702.1219 | 3695.0483 | 3694.8725 |
| 2.4894 | 3657.4690 | 3675.1535 | 3674.9763 |
| 2.5004 | 3688.3805 | 3655.2587 | 3655.0801 |
| 2.5114 | 3696.6077 | 3635.3639 | 3635.1840 |
| 2.5224 | 3677.2473 | 3615.4692 | 3615.2878 |
| 2.5334 | 3683.2891 | 3595.5922 | 3595.3916 |
| 2.5444 | 3661.6711 | 3575.7181 | 3575.4955 |
| 2.5554 | 3563.4100 | 3555.8324 | 3555.5993 |
| 2.5664 | 3542.3274 | 3535.9482 | 3535.7031 |
| 2.5774 | 3541.3825 | 3516.0538 | 3515.8069 |
| 2.5884 | 3468.1603 | 3496.1593 | 3495.9108 |
| 2.5994 | 3435.3274 | 3476.2650 | 3476.0146 |
| 2.6104 | 3510.3609 | 3456.3706 | 3456.1184 |
| 2.6214 | 3492.3127 | 3436.4762 | 3436.2222 |
| 2.6324 | 3346.0973 | 3416.5819 | 3416.3261 |
| 2.6434 | 3374.5556 | 3396.6876 | 3396.4299 |
| 2.6544 | 3411.3510 | 3376.7933 | 3376.5337 |
| 2.6654 | 3377.6018 | 3356.8991 | 3356.6376 |
| 2.6764 | 3404.7370 | 3337.0048 | 3336.7414 |
| 2.6874 | 3334.9371 | 3317.1106 | 3316.8452 |
| 2.6984 | 3340.7478 | 3297.2164 | 3296.9490 |
| 2.7094 | 3332.6942 | 3277.3223 | 3277.0529 |
| 2.7204 | 3260.0919 | 3257.4281 | 3257.1567 |
| 2.7314 | 3259.2242 | 3237.5340 | 3237.2605 |
| 2.7424 | 3152.6509 | 3217.6399 | 3217.3643 |
| 2.7534 | 3209.2360 | 3198.6010 | 3197.4682 |
| 2.7644 | 3197.0133 | 3179.3954 | 3179.1156 |
| 2.7754 | 3216.0905 | 3161.0450 | 3160.7630 |
| 2.7864 | 3132.7335 | 3142.6946 | 3142.4104 |
| 2.7974 | 3091.6814 | 3124.3442 | 3124.0579 |
| 2.8084 | 3105.9449 | 3105.9939 | 3105.7053 |
| 2.8194 | 3258.0738 | 3087.6435 | 3087.3527 |
| 2.8304 | 3114.4454 | 3069.2933 | 3069.0001 |
| 2.8414 | 3051.4916 | 3050.9430 | 3050.6475 |
| 2.8524 | 3046.1072 | 3032.5928 | 3032.2950 |
| 2.8634 | 2989.4366 | 3014.2426 | 3013.9424 |
| 2.8744 | 3033.6077 | 2995.8924 | 2995.5898 |
| 2.8854 | 2879.6411 | 2977.5423 | 2977.2372 |
| 2.8964 | 3003.4381 | 2959.1921 | 2958.8847 |
| 2.9074 | 2944.5192 | 2940.8421 | 2940.5321 |
| 2.9184 | 3008.3068 | 2922.4920 | 2922.1795 |
| 2.9294 | 2925.6755 | 2904.1420 | 2903.8269 |
| 2.9404 | 2913.8078 | 2885.7454 | 2885.4743 |
| 2.9514 | 2863.5782 | 2867.3579 | 2867.0376 |
| 2.9624 | 2807.3466 | 2848.9238 | 2848.6008 |
| 2.9734 | 2817.1416 | 2830.4897 | 2830.1640 |
| 2.9844 | 2865.8913 | 2812.0557 | 2811.7273 |
| 2.9954 | 2776.4071 | 2793.6217 | 2793.2905 |
| 3.0064 | 2757.6681 | 2775.1877 | 2774.8537 |
| 3.0174 | 2710.0226 | 2756.7538 | 2756.4169 |
| 3.0284 | 2659.0030 | 2738.3199 | 2737.9802 |
| 3.0394 | 2675.9715 | 2719.8861 | 2719.5434 |
| 3.0504 | 2708.8678 | 2701.4523 | 2701.1066 |
| 3.0614 | 2718.7463 | 2683.0185 | 2682.6698 |
| 3.0724 | 2633.1146 | 2664.5848 | 2664.2331 |
| 3.0834 | 2644.2498 | 2646.1511 | 2645.7963 |
| 3.0944 | 2644.9779 | 2627.7175 | 2627.3595 |
| 3.1054 | 2627.9135 | 2609.2839 | 2608.9228 |
| 3.1164 | 2650.1367 | 2590.8503 | 2590.4860 |
| 3.1274 | 2577.0029 | 2572.4168 | 2572.0492 |
| 3.1384 | 2554.3958 | 2553.9834 | 2553.6124 |
| 3.1494 | 2612.1907 | 2535.5500 | 2535.1757 |
| 3.1604 | 2548.5664 | 2517.1166 | 2516.7389 |
| 3.1714 | 2502.3658 | 2498.6833 | 2498.3021 |
| 3.1824 | 2471.9400 | 2480.2500 | 2479.8653 |
| 3.1934 | 2430.8761 | 2461.8168 | 2461.4286 |
| 3.2044 | 2440.2439 | 2443.3837 | 2442.9918 |
| 3.2154 | 2414.4553 | 2424.9506 | 2424.5550 |
| 3.2264 | 2369.7920 | 2406.5175 | 2406.1183 |
| 3.2374 | 2368.7257 | 2388.0845 | 2387.6815 |
| 3.2484 | 2362.8889 | 2369.6516 | 2369.2447 |
| 3.2594 | 2314.0649 | 2351.2187 | 2350.8079 |
| 3.2704 | 2321.7783 | 2332.7859 | 2332.3712 |
| 3.2814 | 2291.5349 | 2314.3531 | 2313.9344 |
| 3.2924 | 2285.8584 | 2295.9204 | 2295.4976 |
| 3.3034 | 2264.9469 | 2277.4878 | 2277.0608 |
| 3.3144 | 2299.3240 | 2260.8652 | 2258.6241 |
| 3.3254 | 2247.6401 | 2243.8899 | 2243.4545 |
| 3.3364 | 2158.0270 | 2228.7247 | 2228.2850 |
| 3.3474 | 2172.5044 | 2213.5596 | 2213.1154 |
| 3.3584 | 2216.6210 | 2198.3945 | 2197.9458 |
| 3.3694 | 2220.5487 | 2183.2295 | 2182.7763 |
| 3.3804 | 2184.1455 | 2168.0645 | 2167.6067 |
| 3.3914 | 2168.9911 | 2152.8997 | 2152.4372 |
| 3.4024 | 2134.8053 | 2137.7349 | 2137.2676 |
| 3.4134 | 2090.3373 | 2122.5702 | 2122.0981 |
| 3.4244 | 2076.6121 | 2107.4056 | 2106.9285 |
| 3.4354 | 2139.9902 | 2092.2410 | 2091.7590 |
| 3.4464 | 2101.5137 | 2077.0766 | 2076.5894 |
| 3.4574 | 2071.9174 | 2061.9122 | 2061.4198 |
| 3.4684 | 2078.2876 | 2046.7479 | 2046.2503 |
| 3.4794 | 2095.7040 | 2031.5837 | 2031.0807 |
| 3.4904 | 2068.7610 | 2016.4196 | 2015.9112 |
| 3.5014 | 1958.3362 | 2002.7249 | 2000.7416 |
| 3.5124 | 1961.8712 | 1988.7440 | 1988.2244 |
| 3.5234 | 1934.5723 | 1976.2325 | 1975.7071 |
| 3.5344 | 1988.8048 | 1963.7211 | 1963.1899 |
| 3.5454 | 1896.0314 | 1951.2098 | 1950.6726 |
| 3.5564 | 1897.8466 | 1938.6986 | 1938.1554 |
| 3.5674 | 1890.6588 | 1926.1875 | 1925.6381 |
| 3.5784 | 1885.0305 | 1913.6765 | 1913.1209 |
| 3.5894 | 1929.8850 | 1901.1656 | 1900.6036 |
| 3.6004 | 1928.9203 | 1888.6549 | 1888.0864 |
| 3.6114 | 1849.5231 | 1876.1442 | 1875.5691 |
| 3.6224 | 1834.0339 | 1863.6337 | 1863.0519 |
| 3.6334 | 1835.0000 | 1851.1233 | 1850.5346 |
| 3.6444 | 1789.2748 | 1838.6131 | 1838.0174 |
| 3.6554 | 1847.4926 | 1826.1030 | 1825.5001 |
| 3.6664 | 1828.3299 | 1813.5930 | 1812.9829 |
| 3.6774 | 1883.7768 | 1801.0831 | 1800.4656 |
| 3.6884 | 1800.5442 | 1788.5734 | 1787.9484 |
| 3.6994 | 1764.7866 | 1776.0639 | 1775.4311 |
| 3.7104 | 1743.8977 | 1763.5545 | 1762.9139 |
| 3.7214 | 1781.4484 | 1751.0452 | 1750.3966 |
| 3.7324 | 1793.3673 | 1738.5361 | 1737.8794 |
| 3.7434 | 1762.9144 | 1726.0272 | 1725.3621 |
| 3.7544 | 1729.5088 | 1713.5184 | 1712.8449 |
| 3.7654 | 1685.4710 | 1701.0098 | 1700.3276 |
| 3.7764 | 1652.6765 | 1688.5014 | 1687.8104 |
| 3.7874 | 1728.3186 | 1675.9932 | 1675.2932 |
| 3.7984 | 1674.7763 | 1663.4851 | 1662.7759 |
| 3.8094 | 1609.8741 | 1650.9773 | 1650.2587 |
| 3.8204 | 1601.5516 | 1638.4696 | 1637.7414 |
| 3.8314 | 1587.6932 | 1625.9621 | 1625.2242 |
| 3.8424 | 1625.0541 | 1613.4549 | 1612.7069 |
| 3.8534 | 1575.2449 | 1600.9479 | 1600.1897 |
| 3.8644 | 1616.1337 | 1588.4410 | 1587.6724 |
| 3.8754 | 1547.4317 | 1576.7166 | 1575.1552 |
| 3.8864 | 1564.6460 | 1564.8400 | 1564.0498 |
| 3.8974 | 1572.3736 | 1553.7457 | 1552.9443 |
| 3.9084 | 1456.8122 | 1542.6517 | 1541.8389 |
| 3.9194 | 1497.5546 | 1531.5579 | 1530.7335 |
| 3.9304 | 1500.2453 | 1520.4644 | 1519.6281 |
| 3.9414 | 1488.3284 | 1509.3712 | 1508.5227 |
| 3.9524 | 1447.4204 | 1498.2783 | 1497.4173 |
| 3.9634 | 1448.6391 | 1487.1856 | 1486.3119 |
| 3.9744 | 1483.1986 | 1476.0933 | 1475.2065 |
| 3.9854 | 1458.1947 | 1465.0012 | 1464.1011 |
| 3.9964 | 1422.0536 | 1453.9095 | 1452.9957 |
| 4.0074 | 1473.7630 | 1442.8181 | 1441.8903 |
| 4.0184 | 1473.0000 | 1431.7270 | 1430.7848 |
| 4.0294 | 1438.9980 | 1420.6363 | 1419.6794 |
| 4.0404 | 1356.4184 | 1409.5460 | 1408.5740 |
| 4.0514 | 1396.5782 | 1398.4561 | 1397.4686 |
| 4.0624 | 1399.6440 | 1387.4596 | 1386.3632 |
| 4.0734 | 1380.0000 | 1376.4454 | 1375.4259 |
| 4.0844 | 1375.4779 | 1365.5248 | 1364.4886 |
| 4.0954 | 1353.2586 | 1354.6045 | 1353.5513 |
| 4.1064 | 1322.0909 | 1343.6848 | 1342.6140 |
| 4.1174 | 1303.4425 | 1332.7654 | 1331.6767 |
| 4.1284 | 1265.8087 | 1321.8466 | 1320.7393 |
| 4.1394 | 1244.2232 | 1310.9283 | 1309.8020 |
| 4.1504 | 1271.4292 | 1300.0104 | 1298.8647 |
| 4.1614 | 1256.5919 | 1289.0931 | 1287.9274 |
| 4.1724 | 1247.2134 | 1278.1764 | 1276.9901 |
| 4.1834 | 1241.7257 | 1267.2602 | 1266.0528 |
| 4.1944 | 1242.6072 | 1256.3446 | 1255.1155 |

Scan List

| Vis. | Dataset Name | Start pos. [°2θ] | End pos. [°2θ] | Step [°2θ] | Meas.Date/Time |
| --- | --- | --- | --- | --- | --- |
| * | 12 Etosha22 Crt 0-0.1cm S2 heat550c | 2.0054 | 29.9894 | 0.0110 | 12/4/2023 3:54:25 PM |

Peak List

| Pos. [°2θ] | Height [cts] | FWHM Left [°2θ] | d-spacing [Å] | Rel. Int. [%] |
| --- | --- | --- | --- | --- |
| 5.3135 | 109.52 | 0.3031 | 16.61841 | 85.64 |
| 7.7327 | 40.70 | 0.5196 | 11.42378 | 31.82 |
| 8.7496 | 127.89 | 0.3031 | 10.09829 | 100.00 |
| 16.0829 | 50.49 | 0.3031 | 5.50650 | 39.48 |
| 26.3345 | 25.41 | 0.1299 | 3.38155 | 19.87 |

Pattern List

| Visible | Ref.Code | Score | Compound Name | Chem. Formula | Mineral Name | SemiQuant[%] |
| --- | --- | --- | --- | --- | --- | --- |
| * | 04-025-4215 | No Matching Lines | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide | Mg10.4 V0.36 Mn33.5 Fe0.14 Al0.69 Si6.77 As6.5 P0.3 O54 ( O H )42 | Carlfrancisite | - |
| * | 01-076-7144 | 24 | Potassium Sodium Barium Magnesium Iron Aluminum Silicon Oxide Fluoride | ( K0.85 Na0.11 Ba0.03 ) ( Mg2.22 Fe0.78 ) ( ( Si2.75 Al1.25 ) O11.86 F0.14 ) | Phlogopite-1M | 90 |
| * | 04-015-2962 | 8 | Magnesium Aluminum Silicon Oxide Hydroxide Hydrate | Mg Al Si4 O10 ( O H ) ( H2 O )4 | Palygorskite-M | 10 |
| * | 01-083-1731 | No Matching Lines | Sodium Aluminum Silicate Hydrate | Na14.80 Al14.24 Si33.76 O96 ( H2 O )16 | Analcime | - |

Anchor Scan Parameters

Dataset Name	12 Etosha22 Crt 0-0.1cm S2 heat550c

File name	C:\aeris_data\XRD data\Goldstein\Etosha 2023\Etosha Clay Data\Sample 12\12 Etosha22 Crt 0-0.1cm S2 heat550c.xrdml

Sample Identification	12 Etosha22 Crt 0-0.1cm S2 heat550c

Measurement Start Date/Time	12/4/2023 3:54:25 PM

Operator	Instrument

Raw Data Origin	XRD measurement (*.XRDML)

Scan Axis	Gonio

Start Position [°2θ]	2.0054

End Position [°2θ]	29.9894

Step Size [°2θ]	0.0110

Scan Step Time [s]	48.1950

Scan Type	Continuous

PSD Mode	Scanning

PSD Length [°2θ]	5.54

Offset [°2θ]	0.0000

Divergence Slit Type	Fixed

Divergence Slit Size [°]	0.0603

Specimen Length [mm]	10.00

Measurement Temperature [°C]	25.00

Anode Material	Cu

K-α1 [Å]	1.54060

K-α2 [Å]	1.54443

K-β1 [Å]	1.39225

K-A2 / K-A1 Ratio	0.50000

Generator Settings	15 mA, 40 kV

Diffractometer Type	2082464

Diffractometer Number	0

Goniometer Radius [mm]	145.00

Dist. Focus-Diverg. Slit [mm]	95.00

Incident Beam Monochromator	No

Spinning	Yes