12 Etosha 22 CRT 0-0.1 cm S2 GLYCOLATED

Graphics

Graphics

Graphics

Quantitative Results

Phase Potassium Sodium Calcium Manganese Aluminum Iron Silicon Oxide Hydroxide Hydrate

Weight fraction/ %	21.0

Phase Sodium Aluminum Silicon Oxide Hydrate

Weight fraction/ %	23.0

Phase Magnesium Aluminum Iron Silicate Hydroxide Hydrate

Weight fraction/ %	16.0

Phase Potassium Magnesium Iron Silicon Oxide Hydroxide

Weight fraction/ %	40.0

Multiple Quantitative Results

Scans vs Phases Matrix

| Scan name | Potassium Sodium Calcium Manganese Aluminum Iron Silicon Oxide Hydroxide Hydrate | Sodium Aluminum Silicon Oxide Hydrate | Magnesium Aluminum Iron Silicate Hydroxide Hydrate | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide | Potassium Magnesium Iron Silicon Oxide Hydroxide |
| --- | --- | --- | --- | --- | --- |
| 12 Etosha22 crt 0-0.1cm s2 glycolate | 21.0 | 23.0 | 16.0 | 0.0 | 40.0 |

Anchor Scan Data

| Pos. [°2θ] | Iobs [cts] | Icalc [cts] | Iback [cts] |
| --- | --- | --- | --- |
| 2.0054 | 4942.0000 | 4941.2702 | 4942.0000 |
| 2.0164 | 4983.9184 | 4918.2957 | 4918.2957 |
| 2.0274 | 4898.0324 | 4894.5913 | 4894.5913 |
| 2.0384 | 4940.4012 | 4870.8870 | 4870.8870 |
| 2.0494 | 4970.0187 | 4847.1827 | 4847.1827 |
| 2.0604 | 4830.9440 | 4823.4783 | 4823.4783 |
| 2.0714 | 4766.9351 | 4799.7740 | 4799.7740 |
| 2.0824 | 4740.5698 | 4776.0697 | 4776.0697 |
| 2.0934 | 4731.2802 | 4752.3653 | 4752.3653 |
| 2.1044 | 4698.1770 | 4728.6610 | 4728.6610 |
| 2.1154 | 4776.9272 | 4704.9567 | 4704.9567 |
| 2.1264 | 4739.7222 | 4681.2523 | 4681.2523 |
| 2.1374 | 4636.1003 | 4657.5480 | 4657.5480 |
| 2.1484 | 4594.1706 | 4633.8437 | 4633.8437 |
| 2.1594 | 4561.9479 | 4610.1393 | 4610.1393 |
| 2.1704 | 4592.6475 | 4586.4350 | 4586.4350 |
| 2.1814 | 4551.9626 | 4562.7307 | 4562.7307 |
| 2.1924 | 4593.3289 | 4539.0268 | 4539.0263 |
| 2.2034 | 4492.6283 | 4515.3371 | 4515.3371 |
| 2.2144 | 4396.0413 | 4491.6479 | 4491.6479 |
| 2.2254 | 4562.6539 | 4467.9586 | 4467.9586 |
| 2.2364 | 4523.9897 | 4444.2694 | 4444.2694 |
| 2.2474 | 4346.2350 | 4420.5802 | 4420.5802 |
| 2.2584 | 4334.6406 | 4396.8909 | 4396.8909 |
| 2.2694 | 4383.1268 | 4373.2017 | 4373.2017 |
| 2.2804 | 4325.1131 | 4349.5125 | 4349.5125 |
| 2.2914 | 4371.2694 | 4325.8232 | 4325.8232 |
| 2.3024 | 4282.1903 | 4302.1340 | 4302.1340 |
| 2.3134 | 4154.0138 | 4278.4448 | 4278.4448 |
| 2.3244 | 4136.0207 | 4254.7555 | 4254.7555 |
| 2.3354 | 4176.4661 | 4231.0663 | 4231.0663 |
| 2.3464 | 4113.4395 | 4207.3771 | 4207.3771 |
| 2.3574 | 4183.6480 | 4183.6878 | 4183.6878 |
| 2.3684 | 4160.0354 | 4159.9986 | 4159.9986 |
| 2.3794 | 4173.7168 | 4136.3094 | 4136.3094 |
| 2.3904 | 4139.5020 | 4112.6201 | 4112.6201 |
| 2.4014 | 4074.7345 | 4088.9309 | 4088.9309 |
| 2.4124 | 4063.1101 | 4065.2417 | 4065.2417 |
| 2.4234 | 4074.0364 | 4041.5524 | 4041.5524 |
| 2.4344 | 4064.6372 | 4017.8632 | 4017.8632 |
| 2.4454 | 4045.9026 | 3994.1740 | 3994.1740 |
| 2.4564 | 3950.1814 | 3970.4847 | 3970.4847 |
| 2.4674 | 3899.1593 | 3946.7955 | 3946.7955 |
| 2.4784 | 3843.0192 | 3923.1062 | 3923.1062 |
| 2.4894 | 3814.4385 | 3899.4170 | 3899.4170 |
| 2.5004 | 3863.7168 | 3875.7278 | 3875.7278 |
| 2.5114 | 3885.3884 | 3852.0385 | 3852.0385 |
| 2.5224 | 3849.1160 | 3828.3493 | 3828.3493 |
| 2.5334 | 3802.6313 | 3804.6601 | 3804.6601 |
| 2.5444 | 3814.5108 | 3780.9708 | 3780.9708 |
| 2.5554 | 3767.6283 | 3757.2816 | 3757.2816 |
| 2.5664 | 3761.7301 | 3733.5817 | 3733.5924 |
| 2.5774 | 3674.3471 | 3709.8361 | 3709.8361 |
| 2.5884 | 3710.0625 | 3686.0799 | 3686.0799 |
| 2.5994 | 3627.9292 | 3662.3237 | 3662.3237 |
| 2.6104 | 3569.4641 | 3638.5675 | 3638.5675 |
| 2.6214 | 3516.8712 | 3614.8112 | 3614.8112 |
| 2.6324 | 3466.4793 | 3591.0550 | 3591.0550 |
| 2.6434 | 3486.6539 | 3567.2988 | 3567.2988 |
| 2.6544 | 3534.5334 | 3543.5425 | 3543.5425 |
| 2.6654 | 3497.1150 | 3519.7863 | 3519.7863 |
| 2.6764 | 3466.2542 | 3496.0301 | 3496.0301 |
| 2.6874 | 3461.2380 | 3472.2739 | 3472.2739 |
| 2.6984 | 3390.5354 | 3448.5176 | 3448.5176 |
| 2.7094 | 3336.9616 | 3424.7614 | 3424.7614 |
| 2.7204 | 3367.1470 | 3401.0052 | 3401.0052 |
| 2.7314 | 3366.4543 | 3377.2489 | 3377.2489 |
| 2.7424 | 3320.3545 | 3353.4927 | 3353.4927 |
| 2.7534 | 3388.7286 | 3330.0367 | 3329.7365 |
| 2.7644 | 3281.8761 | 3307.0198 | 3307.0198 |
| 2.7754 | 3276.3471 | 3284.3030 | 3284.3030 |
| 2.7864 | 3237.9848 | 3261.5863 | 3261.5863 |
| 2.7974 | 3345.2744 | 3238.8696 | 3238.8696 |
| 2.8084 | 3254.1249 | 3216.1528 | 3216.1528 |
| 2.8194 | 3242.0000 | 3193.4361 | 3193.4361 |
| 2.8304 | 3070.5398 | 3170.7194 | 3170.7194 |
| 2.8414 | 3096.1672 | 3148.0026 | 3148.0026 |
| 2.8524 | 3124.5531 | 3125.2859 | 3125.2859 |
| 2.8634 | 3187.3569 | 3102.5692 | 3102.5692 |
| 2.8744 | 3105.5236 | 3079.8524 | 3079.8524 |
| 2.8854 | 3021.3874 | 3057.1357 | 3057.1357 |
| 2.8964 | 3052.8540 | 3034.4190 | 3034.4190 |
| 2.9074 | 2883.0541 | 3011.7022 | 3011.7022 |
| 2.9184 | 3015.2139 | 2988.9855 | 2988.9855 |
| 2.9294 | 2975.9941 | 2966.2688 | 2966.2688 |
| 2.9404 | 2944.6578 | 2944.9410 | 2943.5520 |
| 2.9514 | 2915.0875 | 2925.6447 | 2925.6447 |
| 2.9624 | 2898.6829 | 2907.7373 | 2907.7373 |
| 2.9734 | 2886.0600 | 2889.8299 | 2889.8299 |
| 2.9844 | 2934.5487 | 2871.9225 | 2871.9225 |
| 2.9954 | 2856.2920 | 2854.0151 | 2854.0151 |
| 3.0064 | 2877.4833 | 2836.1077 | 2836.1077 |
| 3.0174 | 2839.3314 | 2818.2003 | 2818.2003 |
| 3.0284 | 2899.8451 | 2800.2930 | 2800.2930 |
| 3.0394 | 2842.2999 | 2782.3856 | 2782.3856 |
| 3.0504 | 2797.8501 | 2764.4782 | 2764.4782 |
| 3.0614 | 2800.1239 | 2746.5708 | 2746.5708 |
| 3.0724 | 2740.2330 | 2728.6634 | 2728.6634 |
| 3.0834 | 2733.7935 | 2710.7560 | 2710.7560 |
| 3.0944 | 2770.0442 | 2692.8486 | 2692.8486 |
| 3.1054 | 2666.3501 | 2674.9413 | 2674.9413 |
| 3.1164 | 2691.9292 | 2657.0339 | 2657.0339 |
| 3.1274 | 2611.0148 | 2639.8938 | 2639.1265 |
| 3.1384 | 2620.9154 | 2623.8760 | 2623.8760 |
| 3.1494 | 2620.2429 | 2608.9318 | 2608.6255 |
| 3.1604 | 2579.7507 | 2593.8474 | 2593.3750 |
| 3.1714 | 2592.9774 | 2578.6067 | 2578.1245 |
| 3.1824 | 2595.4597 | 2563.3612 | 2562.8739 |
| 3.1934 | 2609.3539 | 2548.1157 | 2547.6234 |
| 3.2044 | 2489.9425 | 2532.8704 | 2532.3729 |
| 3.2154 | 2460.7669 | 2517.6251 | 2517.1224 |
| 3.2264 | 2436.2153 | 2502.3799 | 2501.8719 |
| 3.2374 | 2454.8191 | 2487.1347 | 2486.6214 |
| 3.2484 | 2428.7222 | 2471.8897 | 2471.3709 |
| 3.2594 | 2405.1504 | 2456.6447 | 2456.1204 |
| 3.2704 | 2406.8756 | 2441.3999 | 2440.8699 |
| 3.2814 | 2422.8604 | 2426.1551 | 2425.6194 |
| 3.2924 | 2400.4469 | 2410.9104 | 2410.3689 |
| 3.3034 | 2402.7945 | 2395.6658 | 2395.1183 |
| 3.3144 | 2405.1033 | 2380.4213 | 2379.8678 |
| 3.3254 | 2384.2802 | 2365.1769 | 2364.6173 |
| 3.3364 | 2339.2045 | 2349.9327 | 2349.3668 |
| 3.3474 | 2334.9961 | 2334.6885 | 2334.1163 |
| 3.3584 | 2334.9056 | 2319.4444 | 2318.8658 |
| 3.3694 | 2264.9646 | 2304.2004 | 2303.6153 |
| 3.3804 | 2231.2827 | 2288.9566 | 2288.3648 |
| 3.3914 | 2247.4159 | 2273.7128 | 2273.1143 |
| 3.4024 | 2217.8786 | 2258.4692 | 2257.8638 |
| 3.4134 | 2209.3186 | 2243.2257 | 2242.6132 |
| 3.4244 | 2193.5782 | 2227.9823 | 2227.3627 |
| 3.4354 | 2229.0118 | 2212.7391 | 2212.1122 |
| 3.4464 | 2182.8530 | 2197.4959 | 2196.8617 |
| 3.4574 | 2145.9381 | 2182.2529 | 2181.6112 |
| 3.4684 | 2184.1967 | 2167.0101 | 2166.3607 |
| 3.4794 | 2137.5939 | 2151.7673 | 2151.1102 |
| 3.4904 | 2153.7655 | 2136.5247 | 2135.8597 |
| 3.5014 | 2106.7974 | 2122.2523 | 2120.6092 |
| 3.5124 | 2104.5098 | 2109.0060 | 2108.3247 |
| 3.5234 | 2103.2920 | 2096.7299 | 2096.0402 |
| 3.5344 | 2094.5831 | 2084.4539 | 2083.7557 |
| 3.5454 | 2091.8378 | 2072.1781 | 2071.4712 |
| 3.5564 | 2098.3304 | 2059.9024 | 2059.1867 |
| 3.5674 | 2048.0816 | 2047.6269 | 2046.9022 |
| 3.5784 | 2027.7271 | 2035.3516 | 2034.6177 |
| 3.5894 | 2060.1062 | 2023.0765 | 2022.3332 |
| 3.6004 | 2025.4144 | 2010.8015 | 2010.0487 |
| 3.6114 | 1997.9046 | 1998.5267 | 1997.7642 |
| 3.6224 | 1998.0339 | 1986.2521 | 1985.4797 |
| 3.6334 | 1986.7139 | 1973.9777 | 1973.1952 |
| 3.6444 | 1950.7453 | 1961.7035 | 1960.9107 |
| 3.6554 | 1917.0029 | 1949.4296 | 1948.6262 |
| 3.6664 | 1930.8309 | 1937.1558 | 1936.3417 |
| 3.6774 | 1952.2330 | 1924.8822 | 1924.0572 |
| 3.6884 | 1895.1239 | 1914.3010 | 1911.7727 |
| 3.6994 | 1920.9272 | 1905.5100 | 1904.6625 |
| 3.7104 | 1841.7296 | 1898.4114 | 1897.5522 |
| 3.7214 | 1872.4484 | 1891.3130 | 1890.4420 |
| 3.7324 | 1856.4764 | 1884.2148 | 1883.3318 |
| 3.7434 | 1874.7817 | 1877.1170 | 1876.2215 |
| 3.7544 | 1811.1091 | 1870.0193 | 1869.1113 |
| 3.7654 | 1784.8024 | 1862.9220 | 1862.0011 |
| 3.7764 | 1848.6047 | 1855.8249 | 1854.8908 |
| 3.7874 | 1800.4425 | 1848.7281 | 1847.7806 |
| 3.7984 | 1877.9002 | 1841.6316 | 1840.6703 |
| 3.8094 | 1847.9459 | 1834.5354 | 1833.5601 |
| 3.8204 | 1781.4675 | 1827.4395 | 1826.4499 |
| 3.8314 | 1763.8466 | 1820.3439 | 1819.3396 |
| 3.8424 | 1787.2090 | 1813.2486 | 1812.2294 |
| 3.8534 | 1842.5988 | 1806.1537 | 1805.1192 |
| 3.8644 | 1804.9897 | 1799.0592 | 1798.0089 |
| 3.8754 | 1779.7375 | 1791.9649 | 1790.8987 |
| 3.8864 | 1894.9027 | 1784.8711 | 1783.7885 |
| 3.8974 | 1929.6627 | 1777.7776 | 1776.6782 |
| 3.9084 | 1788.4297 | 1770.6846 | 1769.5680 |
| 3.9194 | 1735.6519 | 1763.5919 | 1762.4577 |
| 3.9304 | 1696.9430 | 1756.4997 | 1755.3475 |
| 3.9414 | 1741.0600 | 1749.4078 | 1748.2373 |
| 3.9524 | 1765.2448 | 1742.3165 | 1741.1270 |
| 3.9634 | 1769.7709 | 1735.2256 | 1734.0168 |
| 3.9744 | 1815.9956 | 1728.1351 | 1726.9066 |
| 3.9854 | 1769.5929 | 1721.0452 | 1719.7963 |
| 3.9964 | 1725.3830 | 1713.9557 | 1712.6861 |
| 4.0074 | 1726.3796 | 1706.8668 | 1705.5758 |
| 4.0184 | 1769.8156 | 1699.7784 | 1698.4656 |
| 4.0294 | 1713.4622 | 1692.6906 | 1691.3554 |
| 4.0404 | 1729.5816 | 1685.6033 | 1684.2451 |
| 4.0514 | 1692.2832 | 1678.5167 | 1677.1349 |
| 4.0624 | 1680.2409 | 1672.0789 | 1670.0247 |
| 4.0734 | 1638.0747 | 1666.3273 | 1664.8965 |
| 4.0844 | 1628.6062 | 1661.2247 | 1659.7683 |
| 4.0954 | 1698.5408 | 1656.1227 | 1654.6402 |
| 4.1064 | 1676.1603 | 1651.0214 | 1649.5120 |
| 4.1174 | 1713.6401 | 1645.9209 | 1644.3838 |
| 4.1284 | 1693.6470 | 1640.8212 | 1639.2556 |
| 4.1394 | 1680.6077 | 1635.7222 | 1634.1275 |
| 4.1504 | 1682.6401 | 1630.6240 | 1628.9993 |
| 4.1614 | 1626.5467 | 1625.5267 | 1623.8711 |
| 4.1724 | 1607.8933 | 1620.4303 | 1618.7430 |
| 4.1834 | 1650.5310 | 1615.3349 | 1613.6148 |
| 4.1944 | 1670.3131 | 1610.2403 | 1608.4866 |

Scan List

| Vis. | Dataset Name | Start pos. [°2θ] | End pos. [°2θ] | Step [°2θ] | Meas.Date/Time |
| --- | --- | --- | --- | --- | --- |
| * | 12 Etosha22 crt 0-0.1cm s2 glycolate | 2.0054 | 29.9894 | 0.0110 | 12/5/2023 9:39:41 AM |

Peak List

| Pos. [°2θ] | Height [cts] | FWHM Left [°2θ] | d-spacing [Å] | Rel. Int. [%] |
| --- | --- | --- | --- | --- |
| 5.3102 | 335.37 | 0.2165 | 16.62869 | 59.67 |
| 6.8484 | 502.24 | 0.1732 | 12.89687 | 89.36 |
| 7.0364 | 562.01 | 0.2165 | 12.55268 | 100.00 |
| 8.7432 | 293.88 | 0.1299 | 10.10564 | 52.29 |
| 15.7438 | 254.10 | 0.1082 | 5.62432 | 45.21 |
| 17.6052 | 27.46 | 0.2598 | 5.03361 | 4.89 |
| 19.6045 | 16.16 | 0.8659 | 4.52457 | 2.88 |
| 25.9035 | 242.60 | 0.1299 | 3.43684 | 43.17 |
| 26.7181 | 74.16 | 0.1732 | 3.33387 | 13.20 |
| 27.5365 | 49.04 | 0.1732 | 3.23662 | 8.73 |

Pattern List

| Visible | Ref.Code | Score | Compound Name | Chem. Formula | Mineral Name | SemiQuant[%] |
| --- | --- | --- | --- | --- | --- | --- |
| * | 04-016-0693 | 56 | Potassium Sodium Calcium Manganese Aluminum Iron Silicon Oxide Hydroxide Hydrate | K0.3 Na0.4 Ca0.3 Mn3.9 Fe0.1 Al1.4 Si5.3 O16 ( O H )2.7 ( H2 O )3.5 | Ganophyllite | 21 |
| * | 04-009-3254 | 38 | Sodium Aluminum Silicon Oxide Hydrate | Na8 Al8 Si16 O48 ( H2 O )8 | Analcime | 23 |
| * | 01-076-7133 | 28 | Magnesium Aluminum Iron Silicate Hydroxide Hydrate | ( Mg2.09 Al1.92 Fe0.11 ) ( ( Si7.8 Al0.2 ) ( H2 O )4 O20 ) ( O H )2 ( H2 O )4.48 | Palygorskite-M | 16 |
| * | 04-025-4215 | No Matching Lines | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide | Mg10.4 V0.36 Mn33.5 Fe0.14 Al0.69 Si6.77 As6.5 P0.3 O54 ( O H )42 | Carlfrancisite | - |
| * | 01-082-3741 | 46 | Potassium Magnesium Iron Silicon Oxide Hydroxide | K ( Mg1.53 Fe1.48 ) ( Si4 O11 ( O H ) ) | Phlogopite-2M1 | 40 |

Anchor Scan Parameters

Dataset Name	12 Etosha22 crt 0-0.1cm s2 glycolate

File name	C:\aeris_data\XRD data\Goldstein\Etosha 2023\Etosha Clay Data\Sample 12\12 Etosha22 crt 0-0.1cm s2 glycolate.xrdml

Sample Identification	12 Etosha22 crt 0-0.1cm s2 glycolate

Measurement Start Date/Time	12/5/2023 9:39:41 AM

Operator	Instrument

Raw Data Origin	XRD measurement (*.XRDML)

Scan Axis	Gonio

Start Position [°2θ]	2.0054

End Position [°2θ]	29.9894

Step Size [°2θ]	0.0110

Scan Step Time [s]	48.1950

Scan Type	Continuous

PSD Mode	Scanning

PSD Length [°2θ]	5.54

Offset [°2θ]	0.0000

Divergence Slit Type	Fixed

Divergence Slit Size [°]	0.0603

Specimen Length [mm]	10.00

Measurement Temperature [°C]	25.00

Anode Material	Cu

K-α1 [Å]	1.54060

K-α2 [Å]	1.54443

K-β1 [Å]	1.39225

K-A2 / K-A1 Ratio	0.50000

Generator Settings	15 mA, 40 kV

Diffractometer Type	2082464

Diffractometer Number	0

Goniometer Radius [mm]	145.00

Dist. Focus-Diverg. Slit [mm]	95.00

Incident Beam Monochromator	No

Spinning	Yes