12 Etosha 22 CRT 0-0.1 cm S2 REGULAR

Graphics

Graphics

Graphics

Quantitative Results

Phase Potassium Manganese Aluminum Silicon Oxide Hydroxide Hydrate

Weight fraction/ %	17.0

Phase Potassium Sodium Magnesium Aluminum Iron Silicon Titanium Oxide Fluoride Hydroxide

Weight fraction/ %	66.0

Phase Sodium Aluminum Silicate Hydrate

Weight fraction/ %	4.0

Phase Magnesium Aluminum Iron Silicon Oxide Hydroxide Hydrate

Weight fraction/ %	13.0

Multiple Quantitative Results

Scans vs Phases Matrix

| Scan name | Potassium Manganese Aluminum Silicon Oxide Hydroxide Hydrate | Potassium Sodium Magnesium Aluminum Iron Silicon Titanium Oxide Fluoride Hydroxide | Sodium Aluminum Silicate Hydrate | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide | Magnesium Aluminum Iron Silicon Oxide Hydroxide Hydrate |
| --- | --- | --- | --- | --- | --- |
| 12 Etosha22 Crt 0-0.1cm S2 | 17.0 | 66.0 | 4.0 | 0.0 | 13.0 |

Anchor Scan Data

| Pos. [°2θ] | Iobs [cts] | Icalc [cts] | Iback [cts] |
| --- | --- | --- | --- |
| 2.0054 | 4679.0000 | 4673.2601 | 4679.0000 |
| 2.0164 | 4705.4267 | 4650.2733 | 4650.2733 |
| 2.0274 | 4578.4346 | 4621.5466 | 4621.5466 |
| 2.0384 | 4554.6726 | 4592.8199 | 4592.8199 |
| 2.0494 | 4516.5093 | 4564.0931 | 4564.0931 |
| 2.0604 | 4446.9105 | 4535.3664 | 4535.3664 |
| 2.0714 | 4419.0560 | 4506.6397 | 4506.6397 |
| 2.0824 | 4471.2045 | 4477.9130 | 4477.9130 |
| 2.0934 | 4466.4975 | 4449.1863 | 4449.1863 |
| 2.1044 | 4322.9248 | 4420.4596 | 4420.4596 |
| 2.1154 | 4435.4012 | 4391.7329 | 4391.7329 |
| 2.1264 | 4273.4897 | 4363.0062 | 4363.0062 |
| 2.1374 | 4291.8437 | 4334.2794 | 4334.2794 |
| 2.1484 | 4199.3840 | 4305.5527 | 4305.5527 |
| 2.1594 | 4393.4258 | 4276.8260 | 4276.8260 |
| 2.1704 | 4282.9499 | 4248.0993 | 4248.0993 |
| 2.1814 | 4267.8781 | 4219.3726 | 4219.3726 |
| 2.1924 | 4146.5226 | 4191.6447 | 4190.6459 |
| 2.2034 | 4133.7257 | 4166.9183 | 4166.9183 |
| 2.2144 | 4136.2340 | 4143.1907 | 4143.1907 |
| 2.2254 | 4039.2360 | 4119.4631 | 4119.4631 |
| 2.2364 | 4126.0634 | 4095.7356 | 4095.7356 |
| 2.2474 | 4089.5310 | 4072.0080 | 4072.0080 |
| 2.2584 | 4028.8019 | 4048.2804 | 4048.2804 |
| 2.2694 | 4020.9794 | 4024.5528 | 4024.5528 |
| 2.2804 | 4055.0728 | 4000.8253 | 4000.8253 |
| 2.2914 | 4058.1652 | 3977.0977 | 3977.0977 |
| 2.3024 | 4038.7168 | 3953.3701 | 3953.3701 |
| 2.3134 | 4006.7080 | 3929.6425 | 3929.6425 |
| 2.3244 | 3987.9307 | 3905.9149 | 3905.9149 |
| 2.3354 | 3948.0206 | 3882.1874 | 3882.1874 |
| 2.3464 | 3849.0890 | 3858.4598 | 3858.4598 |
| 2.3574 | 3795.9666 | 3834.7322 | 3834.7322 |
| 2.3684 | 3802.6504 | 3811.0046 | 3811.0046 |
| 2.3794 | 3823.8800 | 3787.3362 | 3787.2771 |
| 2.3904 | 3790.9361 | 3763.8457 | 3763.8457 |
| 2.4014 | 3684.8142 | 3740.4143 | 3740.4143 |
| 2.4124 | 3685.7483 | 3716.9829 | 3716.9829 |
| 2.4234 | 3680.0187 | 3693.5515 | 3693.5515 |
| 2.4344 | 3670.1254 | 3670.1201 | 3670.1201 |
| 2.4454 | 3725.5752 | 3646.6887 | 3646.6887 |
| 2.4564 | 3699.8348 | 3623.2573 | 3623.2573 |
| 2.4674 | 3651.1239 | 3599.8259 | 3599.8259 |
| 2.4784 | 3639.7984 | 3576.3945 | 3576.3945 |
| 2.4894 | 3644.8879 | 3552.9631 | 3552.9631 |
| 2.5004 | 3616.9823 | 3529.5317 | 3529.5317 |
| 2.5114 | 3558.7266 | 3506.1003 | 3506.1003 |
| 2.5224 | 3583.0349 | 3482.6690 | 3482.6690 |
| 2.5334 | 3495.9764 | 3459.2376 | 3459.2376 |
| 2.5444 | 3444.3402 | 3435.8062 | 3435.8062 |
| 2.5554 | 3386.6499 | 3412.3748 | 3412.3748 |
| 2.5664 | 3413.9823 | 3389.6853 | 3388.9434 |
| 2.5774 | 3356.1819 | 3369.2252 | 3369.2252 |
| 2.5884 | 3345.8569 | 3349.5069 | 3349.5069 |
| 2.5994 | 3399.8761 | 3329.7887 | 3329.7887 |
| 2.6104 | 3275.4184 | 3310.0705 | 3310.0705 |
| 2.6214 | 3245.4798 | 3290.3522 | 3290.3522 |
| 2.6324 | 3285.1195 | 3270.6340 | 3270.6340 |
| 2.6434 | 3280.7424 | 3250.9158 | 3250.9158 |
| 2.6544 | 3280.0762 | 3231.1976 | 3231.1976 |
| 2.6654 | 3298.9617 | 3211.4793 | 3211.4793 |
| 2.6764 | 3212.7802 | 3191.7611 | 3191.7611 |
| 2.6874 | 3140.0875 | 3172.0429 | 3172.0429 |
| 2.6984 | 3162.6195 | 3152.3246 | 3152.3246 |
| 2.7094 | 3180.8663 | 3132.6064 | 3132.6064 |
| 2.7204 | 3185.3968 | 3112.8882 | 3112.8882 |
| 2.7314 | 3134.8938 | 3093.1700 | 3093.1700 |
| 2.7424 | 3109.0005 | 3073.4517 | 3073.4517 |
| 2.7534 | 3078.4189 | 3053.7335 | 3053.7335 |
| 2.7644 | 3063.6711 | 3034.0153 | 3034.0153 |
| 2.7754 | 3002.6342 | 3014.2970 | 3014.2970 |
| 2.7864 | 3102.9558 | 2994.6418 | 2994.5788 |
| 2.7974 | 3008.3805 | 2975.0893 | 2974.8606 |
| 2.8084 | 2993.1028 | 2955.4038 | 2955.1424 |
| 2.8194 | 2992.0905 | 2935.7697 | 2935.4241 |
| 2.8304 | 2984.6254 | 2916.0533 | 2915.7059 |
| 2.8414 | 2948.5034 | 2896.3368 | 2895.9877 |
| 2.8524 | 2875.0192 | 2876.6204 | 2876.2694 |
| 2.8634 | 2842.2389 | 2856.9040 | 2856.5512 |
| 2.8744 | 2888.5787 | 2837.1876 | 2836.8330 |
| 2.8854 | 2913.5988 | 2817.4712 | 2817.1148 |
| 2.8964 | 2858.2478 | 2797.7548 | 2797.3965 |
| 2.9074 | 2677.5340 | 2778.0384 | 2777.6783 |
| 2.9184 | 2868.4803 | 2758.3221 | 2757.9601 |
| 2.9294 | 2744.3451 | 2738.6058 | 2738.2418 |
| 2.9404 | 2694.6421 | 2718.8558 | 2718.5236 |
| 2.9514 | 2693.6156 | 2699.0788 | 2698.7110 |
| 2.9624 | 2796.3451 | 2679.2681 | 2678.8984 |
| 2.9734 | 2705.7758 | 2659.4575 | 2659.0858 |
| 2.9844 | 2689.0890 | 2639.6469 | 2639.2733 |
| 2.9954 | 2645.4956 | 2619.8363 | 2619.4607 |
| 3.0064 | 2525.4268 | 2600.0257 | 2599.6481 |
| 3.0174 | 2593.8456 | 2580.2151 | 2579.8355 |
| 3.0284 | 2527.9926 | 2560.4046 | 2560.0229 |
| 3.0394 | 2507.0108 | 2540.5940 | 2540.2103 |
| 3.0504 | 2564.7178 | 2520.7835 | 2520.3977 |
| 3.0614 | 2586.9469 | 2500.9730 | 2500.5851 |
| 3.0724 | 2496.5747 | 2481.1625 | 2480.7725 |
| 3.0834 | 2499.7522 | 2461.3521 | 2460.9600 |
| 3.0944 | 2416.0133 | 2441.5416 | 2441.1474 |
| 3.1054 | 2385.8574 | 2421.7312 | 2421.3348 |
| 3.1164 | 2359.0010 | 2401.9207 | 2401.5222 |
| 3.1274 | 2412.1328 | 2383.3297 | 2381.7096 |
| 3.1384 | 2397.7733 | 2365.7192 | 2365.3162 |
| 3.1494 | 2330.4710 | 2349.3280 | 2348.9228 |
| 3.1604 | 2419.6194 | 2332.9369 | 2332.5295 |
| 3.1714 | 2339.6686 | 2316.5458 | 2316.1361 |
| 3.1824 | 2319.0791 | 2300.1547 | 2299.7427 |
| 3.1934 | 2298.2035 | 2283.7636 | 2283.3493 |
| 3.2044 | 2315.0383 | 2267.3726 | 2266.9560 |
| 3.2154 | 2307.7355 | 2250.9815 | 2250.5626 |
| 3.2264 | 2293.1932 | 2234.5905 | 2234.1692 |
| 3.2374 | 2282.1573 | 2218.1995 | 2217.7758 |
| 3.2484 | 2211.0000 | 2201.8085 | 2201.3825 |
| 3.2594 | 2174.0531 | 2185.4176 | 2184.9891 |
| 3.2704 | 2210.9233 | 2169.0266 | 2168.5957 |
| 3.2814 | 2210.0983 | 2152.6357 | 2152.2023 |
| 3.2924 | 2163.2787 | 2136.2448 | 2135.8089 |
| 3.3034 | 2141.6096 | 2119.8540 | 2119.4156 |
| 3.3144 | 2170.8791 | 2103.4631 | 2103.0222 |
| 3.3254 | 2146.1563 | 2087.0723 | 2086.6288 |
| 3.3364 | 2111.7188 | 2070.6815 | 2070.2354 |
| 3.3474 | 2081.0413 | 2054.2907 | 2053.8421 |
| 3.3584 | 2047.1888 | 2037.8999 | 2037.4487 |
| 3.3694 | 2045.0423 | 2021.5092 | 2021.0553 |
| 3.3804 | 2022.5905 | 2005.1185 | 2004.6619 |
| 3.3914 | 1988.5044 | 1988.7278 | 1988.2686 |
| 3.4024 | 1976.7316 | 1972.3371 | 1971.8752 |
| 3.4134 | 1943.5919 | 1955.9465 | 1955.4818 |
| 3.4244 | 1935.4941 | 1939.5558 | 1939.0884 |
| 3.4354 | 1906.3579 | 1923.1652 | 1922.6950 |
| 3.4464 | 1895.9140 | 1906.7747 | 1906.3017 |
| 3.4574 | 1900.5310 | 1890.3841 | 1889.9083 |
| 3.4684 | 1883.3058 | 1873.9936 | 1873.5149 |
| 3.4794 | 1853.3550 | 1857.6031 | 1857.1215 |
| 3.4904 | 1830.4513 | 1841.2127 | 1840.7282 |
| 3.5014 | 1802.8377 | 1825.8092 | 1824.3348 |
| 3.5124 | 1832.3486 | 1811.1992 | 1810.7088 |
| 3.5234 | 1824.5457 | 1797.5762 | 1797.0828 |
| 3.5344 | 1822.9184 | 1783.9533 | 1783.4569 |
| 3.5454 | 1806.8191 | 1770.3304 | 1769.8309 |
| 3.5564 | 1771.1445 | 1756.7075 | 1756.2049 |
| 3.5674 | 1801.9931 | 1743.0846 | 1742.5790 |
| 3.5784 | 1744.0260 | 1729.4618 | 1728.9530 |
| 3.5894 | 1698.6726 | 1715.8389 | 1715.3270 |
| 3.6004 | 1735.0212 | 1702.2162 | 1701.7011 |
| 3.6114 | 1671.5231 | 1688.5934 | 1688.0751 |
| 3.6224 | 1703.6342 | 1674.9707 | 1674.4491 |
| 3.6334 | 1688.1514 | 1661.3480 | 1660.8232 |
| 3.6444 | 1680.3373 | 1647.7254 | 1647.1972 |
| 3.6554 | 1602.3835 | 1634.1027 | 1633.5712 |
| 3.6664 | 1670.1711 | 1620.4801 | 1619.9453 |
| 3.6774 | 1614.5408 | 1606.8576 | 1606.3193 |
| 3.6884 | 1530.9159 | 1594.4310 | 1592.6933 |
| 3.6994 | 1586.1760 | 1582.9661 | 1582.4209 |
| 3.7104 | 1643.7812 | 1572.6972 | 1572.1485 |
| 3.7214 | 1625.1475 | 1562.4283 | 1561.8761 |
| 3.7324 | 1566.2886 | 1552.1594 | 1551.6037 |
| 3.7434 | 1523.3786 | 1541.8906 | 1541.3312 |
| 3.7544 | 1568.7139 | 1531.6219 | 1531.0588 |
| 3.7654 | 1559.4012 | 1521.3531 | 1520.7864 |
| 3.7764 | 1557.0423 | 1511.0844 | 1510.5140 |
| 3.7874 | 1550.0619 | 1500.8157 | 1500.2416 |
| 3.7984 | 1455.2031 | 1490.5471 | 1489.9691 |
| 3.8094 | 1513.4651 | 1480.2785 | 1479.6967 |
| 3.8204 | 1480.0841 | 1470.0100 | 1469.4243 |
| 3.8314 | 1483.6047 | 1459.7414 | 1459.1519 |
| 3.8424 | 1492.7394 | 1449.4730 | 1448.8795 |
| 3.8534 | 1400.7257 | 1439.2045 | 1438.6070 |
| 3.8644 | 1438.6106 | 1428.9361 | 1428.3346 |
| 3.8754 | 1419.7630 | 1418.6678 | 1418.0622 |
| 3.8864 | 1400.4602 | 1408.3994 | 1407.7898 |
| 3.8974 | 1428.1485 | 1398.1312 | 1397.5174 |
| 3.9084 | 1400.8196 | 1387.8629 | 1387.2449 |
| 3.9194 | 1360.5634 | 1377.5947 | 1376.9725 |
| 3.9304 | 1345.9804 | 1367.3266 | 1366.7001 |
| 3.9414 | 1406.7581 | 1357.0585 | 1356.4277 |
| 3.9524 | 1337.5059 | 1346.7904 | 1346.1553 |
| 3.9634 | 1303.6195 | 1336.5224 | 1335.8828 |
| 3.9744 | 1291.6013 | 1326.2544 | 1325.6104 |
| 3.9854 | 1303.6991 | 1315.9865 | 1315.3380 |
| 3.9964 | 1308.2026 | 1305.7186 | 1305.0656 |
| 4.0074 | 1291.8102 | 1295.4508 | 1294.7932 |
| 4.0184 | 1262.7389 | 1285.1830 | 1284.5207 |
| 4.0294 | 1268.7689 | 1274.9153 | 1274.2483 |
| 4.0404 | 1238.3908 | 1264.6476 | 1263.9759 |
| 4.0514 | 1200.7198 | 1254.3800 | 1253.7035 |
| 4.0624 | 1242.2301 | 1244.4683 | 1243.4311 |
| 4.0734 | 1295.3176 | 1234.8428 | 1234.1566 |
| 4.0844 | 1233.0487 | 1225.5733 | 1224.8820 |
| 4.0954 | 1205.6529 | 1216.3037 | 1215.6075 |
| 4.1064 | 1204.1283 | 1207.0343 | 1206.3330 |
| 4.1174 | 1203.8820 | 1197.7649 | 1197.0585 |
| 4.1284 | 1183.3235 | 1188.4956 | 1187.7840 |
| 4.1394 | 1165.8466 | 1179.2263 | 1178.5095 |
| 4.1504 | 1153.2876 | 1169.9570 | 1169.2350 |
| 4.1614 | 1155.8161 | 1160.6879 | 1159.9605 |
| 4.1724 | 1166.5678 | 1151.4188 | 1150.6860 |
| 4.1834 | 1145.3009 | 1142.1497 | 1141.4115 |
| 4.1944 | 1137.1898 | 1132.8807 | 1132.1369 |

Scan List

| Vis. | Dataset Name | Start pos. [°2θ] | End pos. [°2θ] | Step [°2θ] | Meas.Date/Time |
| --- | --- | --- | --- | --- | --- |
| * | 12 Etosha22 Crt 0-0.1cm S2 | 2.0054 | 29.9894 | 0.0110 | 12/1/2023 11:59:34 AM |

Peak List

| Pos. [°2θ] | Height [cts] | FWHM Left [°2θ] | d-spacing [Å] | Rel. Int. [%] |
| --- | --- | --- | --- | --- |
| 7.1195 | 242.55 | 0.4330 | 12.40622 | 100.00 |
| 8.7354 | 86.00 | 0.3031 | 10.11461 | 35.46 |
| 15.7388 | 88.26 | 0.1082 | 5.62611 | 36.39 |
| 19.6728 | 13.74 | 0.5196 | 4.50902 | 5.67 |
| 25.9333 | 77.04 | 0.1082 | 3.43295 | 31.76 |
| 26.6357 | 21.61 | 0.2598 | 3.34400 | 8.91 |

Pattern List

| Visible | Ref.Code | Score | Compound Name | Chem. Formula | Mineral Name | SemiQuant[%] |
| --- | --- | --- | --- | --- | --- | --- |
| * | 04-017-7286 | 65 | Potassium Manganese Aluminum Silicon Oxide Hydroxide Hydrate | K0.8 Mn4 Al1.08 Si4.92 O16 ( O H )2 ( H2 O )3 | Ganophyllite | 17 |
| * | 04-023-1515 | 32 | Potassium Sodium Magnesium Aluminum Iron Silicon Titanium Oxide Fluoride Hydroxide | K0.93 Na0.05 Mg1.71 Ti0.13 Fe0.97 Al1.44 Si2.75 O10.47 ( O H )1.33 F0.2 | Phlogopite-1M | 66 |
| * | 04-011-6751 | 26 | Sodium Aluminum Silicate Hydrate | Na8 Al8 Si16 O48 ( H2 O )8 | Analcime | 4 |
| * | 04-025-4215 | No Matching Lines | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide | Mg10.4 V0.36 Mn33.5 Fe0.14 Al0.69 Si6.77 As6.5 P0.3 O54 ( O H )42 | Carlfrancisite | - |
| * | 04-018-3208 | 8 | Magnesium Aluminum Iron Silicon Oxide Hydroxide Hydrate | Mg1.0 Fe0.08 Al1.0 Si3.99 O10.2 ( O H )0.8 ( H2 O )3.3 | Palygorskite-M | 13 |

Anchor Scan Parameters

Dataset Name	12 Etosha22 Crt 0-0.1cm S2

File name	C:\aeris_data\XRD data\Goldstein\Etosha 2023\Etosha Clay Data\Sample 12\12 Etosha22 Crt 0-0.1cm S2.xrdml

Sample Identification	12 Etosha22 Crt 0-0.1cm S2

Measurement Start Date/Time	12/1/2023 11:59:34 AM

Operator	Instrument

Raw Data Origin	XRD measurement (*.XRDML)

Scan Axis	Gonio

Start Position [°2θ]	2.0054

End Position [°2θ]	29.9894

Step Size [°2θ]	0.0110

Scan Step Time [s]	48.1950

Scan Type	Continuous

PSD Mode	Scanning

PSD Length [°2θ]	5.54

Offset [°2θ]	0.0000

Divergence Slit Type	Fixed

Divergence Slit Size [°]	0.0603

Specimen Length [mm]	10.00

Measurement Temperature [°C]	25.00

Anode Material	Cu

K-α1 [Å]	1.54060

K-α2 [Å]	1.54443

K-β1 [Å]	1.39225

K-A2 / K-A1 Ratio	0.50000

Generator Settings	15 mA, 40 kV

Diffractometer Type	2082464

Diffractometer Number	0

Goniometer Radius [mm]	145.00

Dist. Focus-Diverg. Slit [mm]	95.00

Incident Beam Monochromator	No

Spinning	Yes