13 Etosha 22 sub 0.1-10 cm S2 400 C

Graphics

Graphics

Graphics

Quantitative Results

Phase Potassium Sodium Calcium Aluminum Silicon Oxide Hydrate

Weight fraction/ %	19.0

Phase Titanium Oxide

Weight fraction/ %	5.0

Phase Potassium Magnesium Manganese Iron Aluminum Silicate Hydroxide

Weight fraction/ %	20.0

Phase Potassium Sodium Barium Iron Magnesium Manganese Titanium Aluminum Fluoride Silicate Hydroxide

Weight fraction/ %	29.0

Phase Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide

Weight fraction/ %	26.0

Phase Magnesium Silicon Oxide Hydroxide Hydrate

Weight fraction/ %	1.0

Multiple Quantitative Results

Scans vs Phases Matrix

| Scan name | Potassium Sodium Calcium Aluminum Silicon Oxide Hydrate | Titanium Oxide | Potassium Magnesium Manganese Iron Aluminum Silicate Hydroxide | Potassium Sodium Barium Iron Magnesium Manganese Titanium Aluminum Fluoride Silicate Hydroxide | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide | Magnesium Silicon Oxide Hydroxide Hydrate |
| --- | --- | --- | --- | --- | --- | --- |
| 13 Etosha22 sub 0.1-10cm S2 400C | 19.0 | 5.0 | 20.0 | 29.0 | 26.0 | 1.0 |

Anchor Scan Data

| Pos. [°2θ] | Iobs [cts] | Icalc [cts] | Iback [cts] |
| --- | --- | --- | --- |
| 2.0054 | 5201.0000 | 5187.3215 | 5201.0000 |
| 2.0164 | 5191.1888 | 5169.5780 | 5169.2871 |
| 2.0274 | 5123.2714 | 5137.8663 | 5137.5742 |
| 2.0384 | 5017.5442 | 5106.1546 | 5105.8613 |
| 2.0494 | 5088.2773 | 5074.4429 | 5074.1484 |
| 2.0604 | 5172.4749 | 5042.7313 | 5042.4355 |
| 2.0714 | 5181.2832 | 5011.0196 | 5010.7226 |
| 2.0824 | 5006.4189 | 4979.3080 | 4979.0097 |
| 2.0934 | 4972.5103 | 4947.5963 | 4947.2968 |
| 2.1044 | 4913.3319 | 4915.8847 | 4915.5839 |
| 2.1154 | 4894.3677 | 4884.1731 | 4883.8710 |
| 2.1264 | 4764.7419 | 4852.4615 | 4852.1581 |
| 2.1374 | 4895.7139 | 4820.7499 | 4820.4452 |
| 2.1484 | 4733.5261 | 4789.0383 | 4788.7323 |
| 2.1594 | 4725.4867 | 4757.3267 | 4757.0194 |
| 2.1704 | 4779.5354 | 4725.6151 | 4725.3065 |
| 2.1814 | 4663.0413 | 4693.9035 | 4693.5936 |
| 2.1924 | 4581.4469 | 4663.9187 | 4661.8806 |
| 2.2034 | 4678.6460 | 4634.4007 | 4634.0880 |
| 2.2144 | 4678.1858 | 4606.6094 | 4606.2953 |
| 2.2254 | 4580.9646 | 4578.8181 | 4578.5027 |
| 2.2364 | 4457.9366 | 4551.0268 | 4550.7100 |
| 2.2474 | 4474.4592 | 4523.2355 | 4522.9174 |
| 2.2584 | 4481.1981 | 4495.4443 | 4495.1247 |
| 2.2694 | 4506.4248 | 4467.6530 | 4467.3321 |
| 2.2804 | 4497.3343 | 4439.8618 | 4439.5394 |
| 2.2914 | 4476.0089 | 4412.0706 | 4411.7468 |
| 2.3024 | 4496.4602 | 4384.2793 | 4383.9541 |
| 2.3134 | 4405.6175 | 4356.4881 | 4356.1615 |
| 2.3244 | 4370.8717 | 4328.6969 | 4328.3688 |
| 2.3354 | 4363.6342 | 4300.9057 | 4300.5762 |
| 2.3464 | 4268.4774 | 4273.1146 | 4272.7835 |
| 2.3574 | 4256.1878 | 4245.3234 | 4244.9909 |
| 2.3684 | 4223.0280 | 4217.5322 | 4217.1982 |
| 2.3794 | 4182.1209 | 4192.8544 | 4189.4055 |
| 2.3904 | 4149.8225 | 4169.0183 | 4168.6813 |
| 2.4014 | 4176.4956 | 4148.2956 | 4147.9570 |
| 2.4124 | 4175.1883 | 4127.5728 | 4127.2327 |
| 2.4234 | 4127.0128 | 4106.8501 | 4106.5085 |
| 2.4344 | 4089.4720 | 4086.1274 | 4085.7842 |
| 2.4454 | 4099.9764 | 4065.4047 | 4065.0599 |
| 2.4564 | 4069.9921 | 4044.6820 | 4044.3357 |
| 2.4674 | 4011.6991 | 4023.9593 | 4023.6114 |
| 2.4784 | 3952.1863 | 4003.2366 | 4002.8871 |
| 2.4894 | 3984.8564 | 3982.5140 | 3982.1629 |
| 2.5004 | 4000.4071 | 3961.7913 | 3961.4386 |
| 2.5114 | 3965.5152 | 3941.0687 | 3940.7143 |
| 2.5224 | 3854.8382 | 3920.3460 | 3919.9901 |
| 2.5334 | 3818.4484 | 3899.6234 | 3899.2658 |
| 2.5444 | 3860.8746 | 3878.9008 | 3878.5415 |
| 2.5554 | 3904.1131 | 3858.1782 | 3857.8173 |
| 2.5664 | 3938.0443 | 3837.4556 | 3837.0930 |
| 2.5774 | 3745.0334 | 3816.7331 | 3816.3687 |
| 2.5884 | 3732.6224 | 3796.0105 | 3795.6444 |
| 2.5994 | 3743.1947 | 3775.2880 | 3774.9202 |
| 2.6104 | 3769.6726 | 3754.5654 | 3754.1959 |
| 2.6214 | 3760.6499 | 3733.8429 | 3733.4716 |
| 2.6324 | 3669.6357 | 3713.1204 | 3712.7474 |
| 2.6434 | 3617.7522 | 3692.3979 | 3692.0231 |
| 2.6544 | 3617.9769 | 3671.6754 | 3671.2988 |
| 2.6654 | 3608.4631 | 3650.9529 | 3650.5746 |
| 2.6764 | 3656.4828 | 3630.2305 | 3629.8503 |
| 2.6874 | 3510.1603 | 3609.5080 | 3609.1260 |
| 2.6984 | 3489.1991 | 3588.7856 | 3588.4018 |
| 2.7094 | 3449.2291 | 3568.0632 | 3567.6775 |
| 2.7204 | 3474.3481 | 3547.3408 | 3546.9532 |
| 2.7314 | 3515.6372 | 3526.6184 | 3526.2290 |
| 2.7424 | 3476.8840 | 3505.8960 | 3505.5047 |
| 2.7534 | 3538.8781 | 3486.7557 | 3484.7804 |
| 2.7644 | 3467.3436 | 3468.0430 | 3467.6479 |
| 2.7754 | 3375.4267 | 3450.9125 | 3450.5154 |
| 2.7864 | 3413.6146 | 3433.7819 | 3433.3829 |
| 2.7974 | 3489.1416 | 3416.6513 | 3416.2504 |
| 2.8084 | 3457.6239 | 3399.5208 | 3399.1178 |
| 2.8194 | 3370.2320 | 3382.3903 | 3381.9853 |
| 2.8304 | 3409.0133 | 3365.2597 | 3364.8528 |
| 2.8414 | 3330.7974 | 3348.1292 | 3347.7203 |
| 2.8524 | 3354.3387 | 3330.9988 | 3330.5878 |
| 2.8634 | 3393.3894 | 3313.8683 | 3313.4553 |
| 2.8744 | 3345.4793 | 3296.7378 | 3296.3227 |
| 2.8854 | 3199.4572 | 3279.6074 | 3279.1902 |
| 2.8964 | 3339.3673 | 3262.4770 | 3262.0577 |
| 2.9074 | 3249.5664 | 3245.3466 | 3244.9252 |
| 2.9184 | 3318.7020 | 3228.2162 | 3227.7927 |
| 2.9294 | 3205.9941 | 3211.0858 | 3210.6602 |
| 2.9404 | 3176.0447 | 3193.9554 | 3193.5276 |
| 2.9514 | 3178.8250 | 3176.8251 | 3176.3951 |
| 2.9624 | 3207.3363 | 3159.6948 | 3159.2626 |
| 2.9734 | 3180.4297 | 3142.5645 | 3142.1301 |
| 2.9844 | 3133.5074 | 3125.4342 | 3124.9976 |
| 2.9954 | 3171.6903 | 3108.3039 | 3107.8651 |
| 3.0064 | 3117.4026 | 3091.1736 | 3090.7325 |
| 3.0174 | 3041.8151 | 3074.0434 | 3073.6000 |
| 3.0284 | 3025.8746 | 3056.9132 | 3056.4675 |
| 3.0394 | 3104.7680 | 3039.7830 | 3039.3350 |
| 3.0504 | 3131.7438 | 3022.6528 | 3022.2025 |
| 3.0614 | 3033.5074 | 3005.5226 | 3005.0700 |
| 3.0724 | 2966.5630 | 2988.3925 | 2987.9374 |
| 3.0834 | 3092.2753 | 2971.2623 | 2970.8049 |
| 3.0944 | 2996.9646 | 2954.1322 | 2953.6724 |
| 3.1054 | 2972.0246 | 2937.0021 | 2936.5399 |
| 3.1164 | 2934.1731 | 2919.8721 | 2919.4074 |
| 3.1274 | 2920.6342 | 2905.2046 | 2902.2749 |
| 3.1384 | 2819.1401 | 2891.2030 | 2890.7334 |
| 3.1494 | 2900.8093 | 2879.6640 | 2879.1919 |
| 3.1604 | 2944.3850 | 2868.1251 | 2867.6504 |
| 3.1714 | 2898.0236 | 2856.5861 | 2856.1090 |
| 3.1824 | 2824.9086 | 2845.0472 | 2844.5675 |
| 3.1934 | 2837.5133 | 2833.5083 | 2833.0260 |
| 3.2044 | 2799.3835 | 2821.9695 | 2821.4845 |
| 3.2154 | 2842.5202 | 2810.4306 | 2809.9431 |
| 3.2264 | 2840.9852 | 2798.8918 | 2798.4016 |
| 3.2374 | 2827.0000 | 2787.3530 | 2786.8601 |
| 3.2484 | 2813.0000 | 2775.8142 | 2775.3186 |
| 3.2594 | 2810.6578 | 2764.2754 | 2763.7772 |
| 3.2704 | 2804.0280 | 2752.7367 | 2752.2357 |
| 3.2814 | 2773.8624 | 2741.1980 | 2740.6942 |
| 3.2924 | 2813.3894 | 2729.6593 | 2729.1527 |
| 3.3034 | 2739.2822 | 2718.1206 | 2717.6112 |
| 3.3144 | 2675.8756 | 2706.8337 | 2706.0698 |
| 3.3254 | 2695.7050 | 2695.6150 | 2695.1000 |
| 3.3364 | 2641.4857 | 2684.6480 | 2684.1301 |
| 3.3474 | 2600.5211 | 2673.6811 | 2673.1603 |
| 3.3584 | 2612.7788 | 2662.7142 | 2662.1905 |
| 3.3694 | 2656.0059 | 2651.7473 | 2651.2207 |
| 3.3804 | 2632.7443 | 2640.7805 | 2640.2509 |
| 3.3914 | 2583.1504 | 2629.8137 | 2629.2811 |
| 3.4024 | 2602.4627 | 2618.8469 | 2618.3112 |
| 3.4134 | 2602.3373 | 2607.8801 | 2607.3414 |
| 3.4244 | 2566.9469 | 2596.9134 | 2596.3716 |
| 3.4354 | 2583.3048 | 2585.9466 | 2585.4018 |
| 3.4464 | 2574.1544 | 2574.9800 | 2574.4320 |
| 3.4574 | 2580.6519 | 2564.0133 | 2563.4622 |
| 3.4684 | 2539.7802 | 2553.0467 | 2552.4924 |
| 3.4794 | 2533.8800 | 2542.0800 | 2541.5225 |
| 3.4904 | 2574.3717 | 2531.1135 | 2530.5527 |
| 3.5014 | 2532.2586 | 2520.8740 | 2519.5829 |
| 3.5124 | 2474.2257 | 2510.8312 | 2510.2639 |
| 3.5234 | 2457.2153 | 2501.5154 | 2500.9448 |
| 3.5344 | 2419.1603 | 2492.1997 | 2491.6258 |
| 3.5454 | 2424.1809 | 2482.8841 | 2482.3067 |
| 3.5564 | 2429.8009 | 2473.5684 | 2472.9877 |
| 3.5674 | 2438.6893 | 2464.2528 | 2463.6686 |
| 3.5784 | 2414.7257 | 2455.0480 | 2454.3496 |
| 3.5894 | 2405.2301 | 2445.7725 | 2445.0305 |
| 3.6004 | 2399.5246 | 2436.5149 | 2435.7115 |
| 3.6114 | 2384.4936 | 2427.2217 | 2426.3924 |
| 3.6224 | 2443.1224 | 2417.9092 | 2417.0734 |
| 3.6334 | 2427.6942 | 2408.6170 | 2407.7543 |
| 3.6444 | 2386.0826 | 2399.3056 | 2398.4353 |
| 3.6554 | 2457.4602 | 2390.0036 | 2389.1162 |
| 3.6664 | 2401.8122 | 2380.6921 | 2379.7972 |
| 3.6774 | 2380.4494 | 2371.3802 | 2370.4781 |
| 3.6884 | 2423.9071 | 2362.0684 | 2361.1591 |
| 3.6994 | 2342.5034 | 2352.7567 | 2351.8400 |
| 3.7104 | 2411.6500 | 2343.4452 | 2342.5210 |
| 3.7214 | 2385.1386 | 2334.1337 | 2333.2019 |
| 3.7324 | 2332.7261 | 2324.8224 | 2323.8829 |
| 3.7434 | 2311.1023 | 2315.5112 | 2314.5638 |
| 3.7544 | 2240.3377 | 2306.2000 | 2305.2448 |
| 3.7654 | 2246.6657 | 2296.8890 | 2295.9257 |
| 3.7764 | 2326.2876 | 2287.5782 | 2286.6067 |
| 3.7874 | 2221.9469 | 2278.2674 | 2277.2876 |
| 3.7984 | 2294.7247 | 2268.9568 | 2267.9686 |
| 3.8094 | 2216.2744 | 2259.6463 | 2258.6496 |
| 3.8204 | 2295.3835 | 2250.3360 | 2249.3305 |
| 3.8314 | 2271.1376 | 2241.0258 | 2240.0115 |
| 3.8424 | 2205.0516 | 2231.7157 | 2230.6924 |
| 3.8534 | 2239.1445 | 2222.4058 | 2221.3734 |
| 3.8644 | 2196.6878 | 2213.0960 | 2212.0543 |
| 3.8754 | 2184.3107 | 2203.9257 | 2202.7353 |
| 3.8864 | 2217.0841 | 2194.7932 | 2193.7325 |
| 3.8974 | 2214.0187 | 2185.8002 | 2184.7298 |
| 3.9084 | 2247.3141 | 2176.8074 | 2175.7271 |
| 3.9194 | 2209.6637 | 2167.8147 | 2166.7244 |
| 3.9304 | 2213.8117 | 2158.8223 | 2157.7217 |
| 3.9414 | 2177.2045 | 2149.8300 | 2148.7190 |
| 3.9524 | 2162.5590 | 2140.8378 | 2139.7162 |
| 3.9634 | 2144.5123 | 2131.8459 | 2130.7135 |
| 3.9744 | 2174.5988 | 2122.8542 | 2121.7108 |
| 3.9854 | 2173.0708 | 2113.8626 | 2112.7081 |
| 3.9964 | 2180.3072 | 2104.8713 | 2103.7054 |
| 4.0074 | 2112.4268 | 2095.8802 | 2094.7027 |
| 4.0184 | 2127.8038 | 2086.8892 | 2085.6999 |
| 4.0294 | 2068.0305 | 2077.8985 | 2076.6972 |
| 4.0404 | 2058.3815 | 2068.9081 | 2067.6945 |
| 4.0514 | 2068.5693 | 2059.9178 | 2058.6918 |
| 4.0624 | 2054.2566 | 2052.1837 | 2049.6891 |
| 4.0734 | 2038.0108 | 2044.7892 | 2043.5375 |
| 4.0844 | 2043.1416 | 2038.6509 | 2037.3859 |
| 4.0954 | 2023.7355 | 2032.5128 | 2031.2343 |
| 4.1064 | 2041.0909 | 2026.3750 | 2025.0827 |
| 4.1174 | 2058.7906 | 2020.2374 | 2018.9311 |
| 4.1284 | 2053.0575 | 2014.1002 | 2012.7796 |
| 4.1394 | 1956.2311 | 2007.9632 | 2006.6280 |
| 4.1504 | 1972.4572 | 2001.8266 | 2000.4764 |
| 4.1614 | 2009.6352 | 1995.6903 | 1994.3248 |
| 4.1724 | 2021.2080 | 1989.5543 | 1988.1732 |
| 4.1834 | 2025.5398 | 1983.4187 | 1982.0216 |
| 4.1944 | 2007.6775 | 1977.2834 | 1975.8700 |

Scan List

| Vis. | Dataset Name | Start pos. [°2θ] | End pos. [°2θ] | Step [°2θ] | Meas.Date/Time |
| --- | --- | --- | --- | --- | --- |
| * | 13 Etosha22 sub 0.1-10cm S2 400C | 2.0054 | 29.9894 | 0.0110 | 12/7/2023 3:00:43 PM |

Peak List

| Pos. [°2θ] | Height [cts] | FWHM Left [°2θ] | d-spacing [Å] | Rel. Int. [%] |
| --- | --- | --- | --- | --- |
| 5.3127 | 158.96 | 0.1732 | 16.62089 | 9.92 |
| 7.2577 | 154.77 | 0.6061 | 12.17035 | 9.66 |
| 8.7551 | 1601.82 | 0.0974 | 10.09193 | 100.00 |
| 10.5507 | 22.29 | 0.6927 | 8.37806 | 1.39 |
| 15.8233 | 1001.75 | 0.1299 | 5.59623 | 62.54 |
| 17.6357 | 141.50 | 0.1948 | 5.02499 | 8.83 |
| 18.2832 | 126.17 | 0.1299 | 4.84845 | 7.88 |
| 19.6404 | 55.20 | 0.2598 | 4.51637 | 3.45 |
| 22.4132 | 52.71 | 0.1732 | 3.96351 | 3.29 |
| 23.3970 | 37.53 | 0.2598 | 3.79904 | 2.34 |
| 24.2733 | 78.58 | 0.1732 | 3.66383 | 4.91 |
| 25.9545 | 591.43 | 0.0758 | 3.43020 | 36.92 |
| 26.7453 | 468.86 | 0.2165 | 3.33054 | 29.27 |
| 27.5391 | 321.81 | 0.1299 | 3.23631 | 20.09 |

Pattern List

| Visible | Ref.Code | Score | Compound Name | Chem. Formula | Mineral Name | SemiQuant[%] |
| --- | --- | --- | --- | --- | --- | --- |
| * | 04-024-8347 | 71 | Potassium Sodium Calcium Aluminum Silicon Oxide Hydrate | K0.19 Na7.69 Ca0.06 Al8 Si16 O48 ( H2 O )8 | Analcime | 19 |
| * | 04-016-2838 | 50 | Titanium Oxide | Ti O2 | Rutile | 5 |
| * | 04-017-4317 | 41 | Potassium Magnesium Manganese Iron Aluminum Silicate Hydroxide | K Mg0.2 Mn0.1 Fe2.4 Al1.7 Si2.6 O10 ( O H )2 | Biotite-1M | 20 |
| * | 01-076-2507 | 25 | Potassium Sodium Barium Iron Magnesium Manganese Titanium Aluminum Fluoride Silicate Hydroxide | ( Na0.148 K1.793 Ca0.007 Ba0.053 ) ( Al0.034 Fe1.978 Mg3.222 Mn0.019 Ti0.742 ) ( Si5.497 Al2.503 O21.85 ( O H )1.685 F0.465 ) | Phlogopite-1M | 29 |
| * | 04-025-4215 | 7 | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide | Mg10.4 V0.36 Mn33.5 Fe0.14 Al0.69 Si6.77 As6.5 P0.3 O54 ( O H )42 | Carlfrancisite | 26 |
| * | 01-080-5781 | 12 | Magnesium Silicon Oxide Hydroxide Hydrate | Mg8 ( Si12 O30 ( O H )4 ( H2 O )3.92 ) ( H2 O )7.72 | Sepiolite | 1 |

Anchor Scan Parameters

Dataset Name	13 Etosha22 sub 0.1-10cm S2 400C

File name	C:\aeris_data\XRD data\Goldstein\Etosha 2023\Etosha Clay Data\Sample 13\13 Etosha22 sub 0.1-10cm S2 400C.xrdml

Sample Identification	13 Etosha22 sub 0.1-10cm S2 400C

Measurement Start Date/Time	12/7/2023 3:00:43 PM

Operator	Instrument

Raw Data Origin	XRD measurement (*.XRDML)

Scan Axis	Gonio

Start Position [°2θ]	2.0054

End Position [°2θ]	29.9894

Step Size [°2θ]	0.0110

Scan Step Time [s]	48.1950

Scan Type	Continuous

PSD Mode	Scanning

PSD Length [°2θ]	5.54

Offset [°2θ]	0.0000

Divergence Slit Type	Fixed

Divergence Slit Size [°]	0.0603

Specimen Length [mm]	10.00

Measurement Temperature [°C]	25.00

Anode Material	Cu

K-α1 [Å]	1.54060

K-α2 [Å]	1.54443

K-β1 [Å]	1.39225

K-A2 / K-A1 Ratio	0.50000

Generator Settings	15 mA, 40 kV

Diffractometer Type	2082464

Diffractometer Number	0

Goniometer Radius [mm]	145.00

Dist. Focus-Diverg. Slit [mm]	95.00

Incident Beam Monochromator	No

Spinning	Yes