13 Etosha 22 sub 0.1-10 cm S2 550 CM

Graphics

Graphics

Graphics

Quantitative Results

Phase Titanium Oxide

Weight fraction/ %	4.0

Phase Sodium Aluminum Silicate Hydrate

Weight fraction/ %	12.0

Phase Potassium Sodium Barium Iron Magnesium Manganese Titanium Aluminum Fluoride Silicate Hydroxide

Weight fraction/ %	28.0

Phase Potassium Aluminum Silicate

Weight fraction/ %	16.0

Phase Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide

Weight fraction/ %	14.0

Phase Potassium Sodium Magnesium Manganese Aluminum Iron Silicon Titanium Oxide Hydroxide

Weight fraction/ %	25.0

Multiple Quantitative Results

Scans vs Phases Matrix

| Scan name | Titanium Oxide | Sodium Aluminum Silicate Hydrate | Potassium Sodium Barium Iron Magnesium Manganese Titanium Aluminum Fluoride Silicate Hydroxide | Potassium Aluminum Silicate | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide | Potassium Sodium Magnesium Manganese Aluminum Iron Silicon Titanium Oxide Hydroxide |
| --- | --- | --- | --- | --- | --- | --- |
| 13 Etosha22 sub 0.1-10cm s2 550C | 4.0 | 12.0 | 28.0 | 16.0 | 14.0 | 25.0 |

Anchor Scan Data

| Pos. [°2θ] | Iobs [cts] | Icalc [cts] | Iback [cts] |
| --- | --- | --- | --- |
| 2.0054 | 8698.0000 | 8691.0389 | 8698.0000 |
| 2.0164 | 8620.6313 | 8654.8180 | 8635.4301 |
| 2.0274 | 8590.1888 | 8592.8772 | 8572.8601 |
| 2.0384 | 8556.8201 | 8530.9673 | 8510.2902 |
| 2.0494 | 8530.6214 | 8469.0903 | 8447.7203 |
| 2.0604 | 8608.6308 | 8407.2483 | 8385.1504 |
| 2.0714 | 8421.8732 | 8345.4438 | 8322.5804 |
| 2.0824 | 8255.1932 | 8283.6794 | 8260.0105 |
| 2.0934 | 8254.8791 | 8221.9578 | 8197.4406 |
| 2.1044 | 8396.2522 | 8160.2821 | 8134.8706 |
| 2.1154 | 8143.3353 | 8098.6556 | 8072.3007 |
| 2.1264 | 8151.7527 | 8037.0821 | 8009.7308 |
| 2.1374 | 8094.5752 | 7975.5654 | 7947.1608 |
| 2.1484 | 8056.2173 | 7914.1099 | 7884.5909 |
| 2.1594 | 7990.2045 | 7852.7203 | 7822.0210 |
| 2.1704 | 7979.9602 | 7791.4020 | 7759.4511 |
| 2.1814 | 7916.0796 | 7730.1607 | 7696.8811 |
| 2.1924 | 7923.8963 | 7668.9333 | 7634.3112 |
| 2.2034 | 7870.1062 | 7607.7664 | 7571.5724 |
| 2.2144 | 7921.1322 | 7546.6281 | 7508.8336 |
| 2.2254 | 7777.4130 | 7485.5969 | 7446.0948 |
| 2.2364 | 7736.3850 | 7424.6823 | 7383.3560 |
| 2.2474 | 7685.9646 | 7363.8955 | 7320.6172 |
| 2.2584 | 7659.5059 | 7303.2491 | 7257.8784 |
| 2.2694 | 7691.5959 | 7242.7574 | 7195.1396 |
| 2.2804 | 7631.8707 | 7182.4373 | 7132.4008 |
| 2.2914 | 7585.5674 | 7122.3088 | 7069.6620 |
| 2.3024 | 7549.7743 | 7062.3956 | 7006.9232 |
| 2.3134 | 7546.7719 | 7002.7270 | 6944.1844 |
| 2.3244 | 7520.2955 | 6943.3389 | 6881.4456 |
| 2.3354 | 7384.3215 | 6884.2763 | 6818.7068 |
| 2.3464 | 7486.2350 | 6825.5963 | 6755.9680 |
| 2.3574 | 7419.2753 | 6767.3716 | 6693.2292 |
| 2.3684 | 7381.5251 | 6709.6950 | 6630.4904 |
| 2.3794 | 7441.4916 | 6652.6288 | 6567.7516 |
| 2.3904 | 7349.2345 | 6596.3553 | 6504.8762 |
| 2.4014 | 7191.9469 | 6541.0321 | 6442.0008 |
| 2.4124 | 7178.8043 | 6486.9519 | 6379.1253 |
| 2.4234 | 7141.2635 | 6434.4052 | 6316.2499 |
| 2.4344 | 7148.9838 | 6383.7439 | 6253.3745 |
| 2.4454 | 7111.3609 | 6335.3863 | 6190.4991 |
| 2.4564 | 7020.7011 | 6289.8194 | 6127.6237 |
| 2.4674 | 6968.5457 | 6247.5971 | 6064.7483 |
| 2.4784 | 6913.7758 | 6209.3334 | 6001.8728 |
| 2.4894 | 6878.0816 | 6175.6884 | 5938.9974 |
| 2.5004 | 6833.0929 | 6147.3473 | 5876.1220 |
| 2.5114 | 6827.6618 | 6124.9916 | 5813.2466 |
| 2.5224 | 6823.1160 | 6109.2618 | 5750.3712 |
| 2.5334 | 6822.0590 | 6100.7139 | 5687.4957 |
| 2.5444 | 6819.7389 | 6099.7693 | 5624.6203 |
| 2.5554 | 6730.9518 | 6106.6599 | 5561.7449 |
| 2.5664 | 6633.7330 | 6121.3700 | 5498.8695 |
| 2.5774 | 6585.1868 | 6143.5730 | 5435.9941 |
| 2.5884 | 6626.7655 | 6172.5634 | 5373.1186 |
| 2.5994 | 6560.0885 | 6207.1784 | 5310.2432 |
| 2.6104 | 6571.4887 | 6245.7089 | 5247.3678 |
| 2.6214 | 6517.4041 | 6285.8014 | 5184.4924 |
| 2.6324 | 6384.0192 | 6324.3665 | 5121.6170 |
| 2.6434 | 6344.4258 | 6357.5373 | 5058.7416 |
| 2.6544 | 6320.3441 | 6380.7458 | 4995.8661 |
| 2.6654 | 6288.1386 | 6389.0058 | 4932.9907 |
| 2.6764 | 6202.7753 | 6377.4561 | 4870.1153 |
| 2.6874 | 6070.3137 | 6342.1195 | 4807.2399 |
| 2.6984 | 6019.1903 | 6280.6841 | 4744.3645 |
| 2.7094 | 5858.2478 | 6193.0223 | 4681.4890 |
| 2.7204 | 5774.4562 | 6081.2217 | 4618.6136 |
| 2.7314 | 5579.0442 | 5949.1142 | 4555.7382 |
| 2.7424 | 5438.0034 | 5801.5079 | 4492.8628 |
| 2.7534 | 5266.5575 | 5643.3551 | 4429.9874 |
| 2.7644 | 5232.7596 | 5479.3230 | 4366.9753 |
| 2.7754 | 5025.5103 | 5313.3313 | 4303.9633 |
| 2.7864 | 4870.6996 | 5148.6092 | 4240.9513 |
| 2.7974 | 4711.4071 | 4987.5855 | 4177.9392 |
| 2.8084 | 4649.9321 | 4832.0332 | 4114.9272 |
| 2.8194 | 4461.2733 | 4683.1688 | 4051.9151 |
| 2.8304 | 4301.0383 | 4541.7427 | 3988.9031 |
| 2.8414 | 4076.9547 | 4408.1182 | 3925.8911 |
| 2.8524 | 4037.3933 | 4282.3412 | 3862.8790 |
| 2.8634 | 3909.4513 | 4164.2034 | 3799.8670 |
| 2.8744 | 3870.9862 | 4053.3007 | 3736.8550 |
| 2.8854 | 3805.1032 | 3949.0892 | 3673.8429 |
| 2.8964 | 3508.3141 | 3850.9349 | 3610.8309 |
| 2.9074 | 3674.3874 | 3758.1587 | 3547.8188 |
| 2.9184 | 3468.7827 | 3670.0742 | 3484.8068 |
| 2.9294 | 3363.2714 | 3586.0172 | 3421.7948 |
| 2.9404 | 3424.6022 | 3515.8821 | 3358.7827 |
| 2.9514 | 3285.1485 | 3453.1152 | 3321.3204 |
| 2.9624 | 3232.1770 | 3403.2149 | 3283.8580 |
| 2.9734 | 3155.9587 | 3355.2414 | 3246.3957 |
| 2.9844 | 3170.1121 | 3308.8360 | 3208.9334 |
| 2.9954 | 3083.4867 | 3263.7016 | 3171.4710 |
| 3.0064 | 3002.1092 | 3219.5966 | 3134.0087 |
| 3.0174 | 3043.8840 | 3176.3266 | 3096.5463 |
| 3.0284 | 2954.8348 | 3133.7375 | 3059.0840 |
| 3.0394 | 2870.3697 | 3091.7077 | 3021.6217 |
| 3.0504 | 2897.9587 | 3050.1420 | 2984.1593 |
| 3.0614 | 2856.8820 | 3008.9658 | 2946.6970 |
| 3.0724 | 2838.2271 | 2968.1205 | 2909.2346 |
| 3.0834 | 2856.7522 | 2927.5600 | 2871.7723 |
| 3.0944 | 2784.2876 | 2887.2475 | 2834.3099 |
| 3.1054 | 2790.7335 | 2847.1532 | 2796.8476 |
| 3.1164 | 2724.8958 | 2807.2527 | 2759.3853 |
| 3.1274 | 2702.4307 | 2776.2719 | 2721.9229 |
| 3.1384 | 2730.2227 | 2749.2086 | 2705.7139 |
| 3.1494 | 2689.0256 | 2731.0332 | 2689.5048 |
| 3.1604 | 2633.3776 | 2712.9868 | 2673.2957 |
| 3.1714 | 2613.1770 | 2695.0583 | 2657.0867 |
| 3.1824 | 2622.2306 | 2677.2376 | 2640.8776 |
| 3.1934 | 2601.9823 | 2659.5161 | 2624.6685 |
| 3.2044 | 2594.1480 | 2641.8858 | 2608.4595 |
| 3.2154 | 2577.8161 | 2624.3395 | 2592.2504 |
| 3.2264 | 2576.8068 | 2606.8709 | 2576.0414 |
| 3.2374 | 2550.1829 | 2589.4741 | 2559.8323 |
| 3.2484 | 2538.3889 | 2572.1438 | 2543.6232 |
| 3.2594 | 2519.6784 | 2554.8751 | 2527.4142 |
| 3.2704 | 2455.9326 | 2537.6638 | 2511.2051 |
| 3.2814 | 2478.9715 | 2520.5058 | 2494.9960 |
| 3.2924 | 2490.7832 | 2503.3974 | 2478.7870 |
| 3.3034 | 2492.0738 | 2486.3353 | 2462.5779 |
| 3.3144 | 2464.7684 | 2469.3163 | 2446.3689 |
| 3.3254 | 2401.3481 | 2452.3377 | 2430.1598 |
| 3.3364 | 2373.0993 | 2435.3968 | 2413.9507 |
| 3.3474 | 2352.9764 | 2418.4912 | 2397.7417 |
| 3.3584 | 2391.3304 | 2401.6187 | 2381.5326 |
| 3.3694 | 2378.2714 | 2384.7772 | 2365.3235 |
| 3.3804 | 2319.1352 | 2367.9649 | 2349.1145 |
| 3.3914 | 2282.4159 | 2351.1801 | 2332.9054 |
| 3.4024 | 2214.1720 | 2334.4210 | 2316.6964 |
| 3.4134 | 2261.8801 | 2317.6862 | 2300.4873 |
| 3.4244 | 2266.6622 | 2300.9743 | 2284.2782 |
| 3.4354 | 2214.8151 | 2284.2839 | 2268.0692 |
| 3.4464 | 2194.3063 | 2267.6140 | 2251.8601 |
| 3.4574 | 2213.4985 | 2250.9633 | 2235.6510 |
| 3.4684 | 2202.1686 | 2234.3308 | 2219.4420 |
| 3.4794 | 2180.4710 | 2217.7155 | 2203.2329 |
| 3.4904 | 2191.8451 | 2201.1165 | 2187.0239 |
| 3.5014 | 2185.5683 | 2185.9299 | 2170.8148 |
| 3.5124 | 2135.2320 | 2171.3586 | 2158.0002 |
| 3.5234 | 2153.9853 | 2158.1981 | 2145.1857 |
| 3.5344 | 2132.7433 | 2145.0508 | 2132.3711 |
| 3.5454 | 2152.3166 | 2131.9160 | 2119.5566 |
| 3.5564 | 2113.9543 | 2118.8228 | 2106.7420 |
| 3.5674 | 2092.7640 | 2105.8153 | 2093.9274 |
| 3.5784 | 2080.6357 | 2092.7313 | 2081.1129 |
| 3.5894 | 2033.8849 | 2079.6951 | 2068.2983 |
| 3.6004 | 2035.0797 | 2066.6171 | 2055.4838 |
| 3.6114 | 2062.0403 | 2053.5485 | 2042.6692 |
| 3.6224 | 2005.0708 | 2040.4888 | 2029.8547 |
| 3.6334 | 1986.7237 | 2027.4377 | 2017.0401 |
| 3.6444 | 1978.5177 | 2014.3948 | 2004.2255 |
| 3.6554 | 1962.6578 | 2001.3596 | 1991.4110 |
| 3.6664 | 1924.9061 | 1988.3320 | 1978.5964 |
| 3.6774 | 1932.8918 | 1975.3115 | 1965.7819 |
| 3.6884 | 2011.6062 | 1963.1842 | 1952.9673 |
| 3.6994 | 1974.6804 | 1951.4446 | 1942.3066 |
| 3.7104 | 1835.0432 | 1940.5977 | 1931.6459 |
| 3.7214 | 1911.8230 | 1929.7567 | 1920.9851 |
| 3.7324 | 1883.7419 | 1918.9216 | 1910.3244 |
| 3.7434 | 1921.5054 | 1908.0920 | 1899.6637 |
| 3.7544 | 1921.1372 | 1897.2677 | 1889.0030 |
| 3.7654 | 1936.4651 | 1886.4486 | 1878.3422 |
| 3.7764 | 1899.8033 | 1875.6344 | 1867.6815 |
| 3.7874 | 1881.1593 | 1864.8249 | 1857.0208 |
| 3.7984 | 1939.7935 | 1854.0200 | 1846.3601 |
| 3.8094 | 1879.1190 | 1843.2194 | 1835.6994 |
| 3.8204 | 1826.6062 | 1832.4231 | 1825.0386 |
| 3.8314 | 1913.6942 | 1821.6309 | 1814.3779 |
| 3.8424 | 1835.1578 | 1810.8426 | 1803.7172 |
| 3.8534 | 1834.5605 | 1800.0580 | 1793.0565 |
| 3.8644 | 1779.1337 | 1789.2772 | 1782.3957 |
| 3.8754 | 1715.9794 | 1780.0918 | 1771.7350 |
| 3.8864 | 1792.2921 | 1771.5944 | 1764.9428 |
| 3.8974 | 1824.0580 | 1764.6922 | 1758.1506 |
| 3.9084 | 1717.6028 | 1757.7933 | 1751.3584 |
| 3.9194 | 1785.1091 | 1750.8974 | 1744.5662 |
| 3.9304 | 1781.5855 | 1744.0044 | 1737.7740 |
| 3.9414 | 1731.9774 | 1737.1144 | 1730.9818 |
| 3.9524 | 1765.5383 | 1730.2271 | 1724.1896 |
| 3.9634 | 1700.4267 | 1723.3426 | 1717.3974 |
| 3.9744 | 1675.8019 | 1716.4607 | 1710.6052 |
| 3.9854 | 1697.5841 | 1709.5813 | 1703.8130 |
| 3.9964 | 1722.2247 | 1702.7043 | 1697.0208 |
| 4.0074 | 1718.2606 | 1695.8298 | 1690.2285 |
| 4.0184 | 1703.2493 | 1688.9576 | 1683.4363 |
| 4.0294 | 1690.9223 | 1682.0876 | 1676.6441 |
| 4.0404 | 1666.0492 | 1675.2199 | 1669.8519 |
| 4.0514 | 1679.6873 | 1668.3543 | 1663.0597 |
| 4.0624 | 1653.9946 | 1661.4167 | 1656.2675 |
| 4.0734 | 1677.3854 | 1654.4493 | 1649.2953 |
| 4.0844 | 1632.4292 | 1647.4098 | 1642.3232 |
| 4.0954 | 1635.5939 | 1640.3722 | 1635.3510 |
| 4.1064 | 1600.9199 | 1633.3365 | 1628.3788 |
| 4.1174 | 1597.8348 | 1626.3027 | 1621.4066 |
| 4.1284 | 1592.5044 | 1619.2706 | 1614.4345 |
| 4.1394 | 1562.9125 | 1612.2403 | 1607.4623 |
| 4.1504 | 1586.9557 | 1605.2117 | 1600.4901 |
| 4.1614 | 1557.5910 | 1598.1849 | 1593.5179 |
| 4.1724 | 1578.0669 | 1591.1596 | 1586.5458 |
| 4.1834 | 1615.2389 | 1584.1360 | 1579.5736 |
| 4.1944 | 1608.6091 | 1577.1140 | 1572.6014 |

Scan List

| Vis. | Dataset Name | Start pos. [°2θ] | End pos. [°2θ] | Step [°2θ] | Meas.Date/Time |
| --- | --- | --- | --- | --- | --- |
| * | 13 Etosha22 sub 0.1-10cm s2 550C | 2.0054 | 29.9894 | 0.0110 | 12/8/2023 11:53:18 AM |

Peak List

| Pos. [°2θ] | Height [cts] | FWHM Left [°2θ] | d-spacing [Å] | Rel. Int. [%] |
| --- | --- | --- | --- | --- |
| 2.6913 | 1376.28 | 0.2165 | 32.80131 | 72.57 |
| 5.2964 | 141.75 | 0.1732 | 16.67193 | 7.47 |
| 8.7055 | 1896.45 | 0.0541 | 10.14932 | 100.00 |
| 10.5724 | 29.10 | 0.5196 | 8.36093 | 1.53 |
| 13.5261 | 51.87 | 0.1299 | 6.54108 | 2.73 |
| 15.8334 | 582.63 | 0.1732 | 5.59270 | 30.72 |
| 17.6301 | 162.19 | 0.1732 | 5.02658 | 8.55 |
| 18.3200 | 61.37 | 0.3031 | 4.83880 | 3.24 |
| 19.6087 | 57.56 | 0.2165 | 4.52360 | 3.04 |
| 22.4151 | 52.64 | 0.1299 | 3.96318 | 2.78 |
| 23.4151 | 48.43 | 0.1299 | 3.79614 | 2.55 |
| 26.2121 | 336.51 | 0.1299 | 3.39707 | 17.74 |
| 26.6963 | 452.71 | 0.2165 | 3.33654 | 23.87 |
| 27.4996 | 439.40 | 0.1515 | 3.24087 | 23.17 |

Pattern List

| Visible | Ref.Code | Score | Compound Name | Chem. Formula | Mineral Name | SemiQuant[%] |
| --- | --- | --- | --- | --- | --- | --- |
| * | 04-016-2838 | 55 | Titanium Oxide | Ti O2 | Rutile | 4 |
| * | 04-011-6751 | 42 | Sodium Aluminum Silicate Hydrate | Na8 Al8 Si16 O48 ( H2 O )8 | Analcime | 12 |
| * | 01-076-2510 | 28 | Potassium Sodium Barium Iron Magnesium Manganese Titanium Aluminum Fluoride Silicate Hydroxide | ( Na0.22 K1.709 Ba0.071 ) ( Al0.001 Fe1.489 Mg3.4 Mn0.013 Ti0.973 ) ( Si6.505 Al1.495 O22.276 ( O H )1.111 F0.613 ) | Phlogopite-1M | 28 |
| * | 04-007-8600 | 15 | Potassium Aluminum Silicate | K Al Si3 O8 | Microcline | 16 |
| * | 04-025-4215 | 17 | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide | Mg10.4 V0.36 Mn33.5 Fe0.14 Al0.69 Si6.77 As6.5 P0.3 O54 ( O H )42 | Carlfrancisite | 14 |
| * | 04-015-8237 | 27 | Potassium Sodium Magnesium Manganese Aluminum Iron Silicon Titanium Oxide Hydroxide | K0.95 Na0.01 Mg0.71 Ti0.13 Mn0.07 Fe1.52 Al1.58 Si2.78 O10.14 ( O H )1.86 | Biotite-2M1 | 25 |

Anchor Scan Parameters

Dataset Name	13 Etosha22 sub 0.1-10cm s2 550C

File name	C:\aeris_data\XRD data\Goldstein\Etosha 2023\Etosha Clay Data\Sample 13\13 Etosha22 sub 0.1-10cm s2 550C.xrdml

Sample Identification	13 Etosha22 sub 0.1-10cm s2 550C

Measurement Start Date/Time	12/8/2023 11:53:18 AM

Operator	Instrument

Raw Data Origin	XRD measurement (*.XRDML)

Scan Axis	Gonio

Start Position [°2θ]	2.0054

End Position [°2θ]	29.9894

Step Size [°2θ]	0.0110

Scan Step Time [s]	48.1950

Scan Type	Continuous

PSD Mode	Scanning

PSD Length [°2θ]	5.54

Offset [°2θ]	0.0000

Divergence Slit Type	Fixed

Divergence Slit Size [°]	0.0603

Specimen Length [mm]	10.00

Measurement Temperature [°C]	25.00

Anode Material	Cu

K-α1 [Å]	1.54060

K-α2 [Å]	1.54443

K-β1 [Å]	1.39225

K-A2 / K-A1 Ratio	0.50000

Generator Settings	15 mA, 40 kV

Diffractometer Type	2082464

Diffractometer Number	0

Goniometer Radius [mm]	145.00

Dist. Focus-Diverg. Slit [mm]	95.00

Incident Beam Monochromator	No

Spinning	Yes