13 Etosha 22 sub 0.1-10 cm S2 REGULAR

Graphics

Graphics

Graphics

Quantitative Results

Phase Potassium Sodium Magnesium Aluminum Iron Silicon Titanium Oxide Fluoride Hydroxide

Weight fraction/ %	26.0

Phase Potassium Manganese Silicate Hydroxide Hydrate

Weight fraction/ %	7.0

Phase Sodium Aluminum Silicate Hydrate

Weight fraction/ %	4.0

Phase Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide

Weight fraction/ %	25.0

Phase Magnesium Aluminum Silicon Oxide Hydroxide Hydrate

Weight fraction/ %	12.0

Phase Potassium Aluminum Silicon Oxide

Weight fraction/ %	9.0

Phase Magnesium Silicate Hydroxide Hydrate

Weight fraction/ %	4.0

Phase Potassium Sodium Magnesium Manganese Aluminum Iron Titanium Fluoride Aluminum Iron Silicate Hydroxide

Weight fraction/ %	12.0

Multiple Quantitative Results

Scans vs Phases Matrix

| Scan name | Potassium Sodium Magnesium Aluminum Iron Silicon Titanium Oxide Fluoride Hydroxide | Potassium Manganese Silicate Hydroxide Hydrate | Sodium Aluminum Silicate Hydrate | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide | Magnesium Aluminum Silicon Oxide Hydroxide Hydrate | Potassium Aluminum Silicon Oxide | Magnesium Silicate Hydroxide Hydrate | Potassium Sodium Magnesium Manganese Aluminum Iron Titanium Fluoride Aluminum Iron Silicate Hydroxide |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 13 Etosha22 sub 0.1-10cm S2 | 26.0 | 7.0 | 4.0 | 25.0 | 12.0 | 9.0 | 4.0 | 12.0 |

Anchor Scan Data

| Pos. [°2θ] | Iobs [cts] | Icalc [cts] | Iback [cts] |
| --- | --- | --- | --- |
| 2.0054 | 9083.0000 | 9051.1194 | 9083.0000 |
| 2.0164 | 9033.4749 | 9036.6563 | 9014.6884 |
| 2.0274 | 9151.9754 | 8968.9994 | 8946.3767 |
| 2.0384 | 9138.6844 | 8901.3742 | 8878.0651 |
| 2.0494 | 8822.9980 | 8833.7828 | 8809.7535 |
| 2.0604 | 8934.5752 | 8766.2273 | 8741.4419 |
| 2.0714 | 8866.5575 | 8698.7102 | 8673.1302 |
| 2.0824 | 8863.4951 | 8631.2343 | 8604.8186 |
| 2.0934 | 8865.8112 | 8563.8023 | 8536.5070 |
| 2.1044 | 8642.7832 | 8496.4174 | 8468.1954 |
| 2.1154 | 8630.6647 | 8429.0830 | 8399.8837 |
| 2.1264 | 8601.4263 | 8361.8028 | 8331.5721 |
| 2.1374 | 8553.1534 | 8294.5810 | 8263.2605 |
| 2.1484 | 8722.2227 | 8227.4220 | 8194.9489 |
| 2.1594 | 8584.7866 | 8160.3307 | 8126.6372 |
| 2.1704 | 8358.3245 | 8093.3124 | 8058.3256 |
| 2.1814 | 8398.8869 | 8026.3731 | 7990.0140 |
| 2.1924 | 8379.0447 | 7959.3961 | 7921.7024 |
| 2.2034 | 8383.6637 | 7892.6001 | 7853.2326 |
| 2.2144 | 8400.7124 | 7825.7815 | 7784.7628 |
| 2.2254 | 8423.9262 | 7759.0724 | 7716.2930 |
| 2.2364 | 8321.7050 | 7692.4825 | 7647.8232 |
| 2.2474 | 8232.2350 | 7626.0230 | 7579.3534 |
| 2.2584 | 8190.6750 | 7559.7058 | 7510.8836 |
| 2.2694 | 8152.2124 | 7493.5449 | 7442.4139 |
| 2.2804 | 7988.2212 | 7427.5556 | 7373.9441 |
| 2.2914 | 7926.8112 | 7361.7556 | 7305.4743 |
| 2.3024 | 8037.9867 | 7296.1650 | 7237.0045 |
| 2.3134 | 8012.6824 | 7230.8073 | 7168.5347 |
| 2.3244 | 7953.7129 | 7165.7099 | 7100.0649 |
| 2.3354 | 7918.4956 | 7100.9056 | 7031.5951 |
| 2.3464 | 7889.5300 | 7036.4344 | 6963.1254 |
| 2.3574 | 7931.0206 | 6972.3459 | 6894.6556 |
| 2.3684 | 7863.1386 | 6908.7026 | 6826.1858 |
| 2.3794 | 7785.0600 | 6845.5850 | 6757.7160 |
| 2.3904 | 7769.6981 | 6783.0977 | 6689.2462 |
| 2.4014 | 7794.9735 | 6721.3775 | 6620.7764 |
| 2.4124 | 7778.9730 | 6660.6042 | 6552.3066 |
| 2.4234 | 7653.6834 | 6601.0130 | 6483.8369 |
| 2.4344 | 7583.6032 | 6542.9093 | 6415.3671 |
| 2.4454 | 7546.0934 | 6486.6851 | 6346.8973 |
| 2.4564 | 7492.8663 | 6432.8355 | 6278.4275 |
| 2.4674 | 7427.4749 | 6381.9744 | 6209.9577 |
| 2.4784 | 7316.9926 | 6334.8456 | 6141.4879 |
| 2.4894 | 7400.6913 | 6292.3279 | 6073.0182 |
| 2.5004 | 7525.4248 | 6255.4298 | 6004.5484 |
| 2.5114 | 7449.2802 | 6225.2703 | 5936.0786 |
| 2.5224 | 7398.9759 | 6203.0434 | 5867.6088 |
| 2.5334 | 7400.5103 | 6189.9635 | 5799.1390 |
| 2.5444 | 7216.5260 | 6187.1922 | 5730.6692 |
| 2.5554 | 7184.0374 | 6195.7468 | 5662.1994 |
| 2.5664 | 7236.1195 | 6216.2705 | 5593.7297 |
| 2.5774 | 7179.3953 | 6249.3718 | 5525.1017 |
| 2.5884 | 7126.5029 | 6294.7384 | 5456.4738 |
| 2.5994 | 7158.8053 | 6351.7567 | 5387.8458 |
| 2.6104 | 7091.7669 | 6418.8987 | 5319.2179 |
| 2.6214 | 7034.5457 | 6493.6668 | 5250.5899 |
| 2.6324 | 7022.3953 | 6572.3864 | 5181.9620 |
| 2.6434 | 6891.6814 | 6649.9951 | 5113.3340 |
| 2.6544 | 6849.4272 | 6719.9094 | 5044.7061 |
| 2.6654 | 6729.1062 | 6774.1359 | 4976.0781 |
| 2.6764 | 6635.5162 | 6803.8561 | 4907.4502 |
| 2.6874 | 6555.7502 | 6800.6351 | 4838.8222 |
| 2.6984 | 6426.0442 | 6758.1044 | 4770.1943 |
| 2.7094 | 6357.0285 | 6673.5514 | 4701.5664 |
| 2.7204 | 6124.1017 | 6548.6711 | 4632.9384 |
| 2.7314 | 6036.3628 | 6389.0806 | 4564.3105 |
| 2.7424 | 5802.5373 | 6202.8630 | 4495.6825 |
| 2.7534 | 5525.8289 | 5998.7025 | 4427.0546 |
| 2.7644 | 5491.1770 | 5785.1115 | 4358.2311 |
| 2.7754 | 5334.6912 | 5568.7703 | 4289.4077 |
| 2.7864 | 5129.2310 | 5355.2572 | 4220.5842 |
| 2.7974 | 4823.3539 | 5148.5702 | 4151.7608 |
| 2.8084 | 4813.9174 | 4951.4790 | 4082.9374 |
| 2.8194 | 4503.2094 | 4765.7350 | 4014.1139 |
| 2.8304 | 4399.1755 | 4592.2565 | 3945.2905 |
| 2.8414 | 4246.3431 | 4431.2887 | 3876.4670 |
| 2.8524 | 4032.5216 | 4282.5461 | 3807.6436 |
| 2.8634 | 3896.3687 | 4145.3426 | 3738.8202 |
| 2.8744 | 3823.0305 | 4018.7130 | 3669.9967 |
| 2.8854 | 3666.6244 | 3901.5229 | 3601.1733 |
| 2.8964 | 3574.3982 | 3792.5640 | 3532.3498 |
| 2.9074 | 3426.7630 | 3690.6322 | 3463.5264 |
| 2.9184 | 3518.3235 | 3594.5867 | 3394.7029 |
| 2.9294 | 3288.6313 | 3503.3899 | 3325.8795 |
| 2.9404 | 3219.1632 | 3439.5279 | 3257.0561 |
| 2.9514 | 3235.5595 | 3362.0616 | 3218.2630 |
| 2.9624 | 3099.9513 | 3310.5084 | 3179.4699 |
| 2.9734 | 3148.6745 | 3260.9477 | 3140.6768 |
| 2.9844 | 3083.1912 | 3212.9635 | 3101.8837 |
| 2.9954 | 2922.1681 | 3166.2305 | 3063.0906 |
| 3.0064 | 2927.9715 | 3120.4975 | 3024.2975 |
| 3.0174 | 2889.7611 | 3075.5723 | 2985.5044 |
| 3.0284 | 2844.8717 | 3031.3082 | 2946.7113 |
| 3.0394 | 2905.8643 | 2987.5934 | 2907.9182 |
| 3.0504 | 2884.1465 | 2944.3423 | 2869.1251 |
| 3.0614 | 2729.0590 | 2901.4882 | 2830.3320 |
| 3.0724 | 2726.4680 | 2858.9786 | 2791.5389 |
| 3.0834 | 2660.2724 | 2816.7715 | 2752.7459 |
| 3.0944 | 2675.3850 | 2774.8323 | 2713.9528 |
| 3.1054 | 2687.6657 | 2733.1325 | 2675.1597 |
| 3.1164 | 2664.0319 | 2691.6478 | 2636.3666 |
| 3.1274 | 2557.5959 | 2664.2980 | 2597.5735 |
| 3.1384 | 2559.7114 | 2627.1353 | 2576.6734 |
| 3.1494 | 2536.7660 | 2604.0734 | 2555.7733 |
| 3.1604 | 2578.3363 | 2581.1574 | 2534.8732 |
| 3.1714 | 2506.9489 | 2558.3746 | 2513.9731 |
| 3.1824 | 2483.8663 | 2535.7138 | 2493.0730 |
| 3.1934 | 2518.9115 | 2513.1648 | 2472.1729 |
| 3.2044 | 2489.9316 | 2490.7188 | 2451.2727 |
| 3.2154 | 2418.2242 | 2468.3674 | 2430.3726 |
| 3.2264 | 2430.3717 | 2446.1034 | 2409.4725 |
| 3.2374 | 2457.9597 | 2423.9200 | 2388.5724 |
| 3.2484 | 2450.5555 | 2401.8112 | 2367.6723 |
| 3.2594 | 2386.1976 | 2379.7714 | 2346.7722 |
| 3.2704 | 2360.1917 | 2357.7958 | 2325.8721 |
| 3.2814 | 2340.3274 | 2335.8796 | 2304.9720 |
| 3.2924 | 2284.7787 | 2314.0188 | 2284.0719 |
| 3.3034 | 2231.1337 | 2292.2096 | 2263.1718 |
| 3.3144 | 2276.2099 | 2278.2667 | 2242.2717 |
| 3.3254 | 2227.0560 | 2258.7668 | 2231.4064 |
| 3.3364 | 2204.4631 | 2247.1271 | 2220.5412 |
| 3.3474 | 2236.4897 | 2235.5266 | 2209.6759 |
| 3.3584 | 2253.1416 | 2223.9629 | 2198.8106 |
| 3.3694 | 2230.1750 | 2212.4336 | 2187.9453 |
| 3.3804 | 2283.9209 | 2200.9365 | 2177.0801 |
| 3.3914 | 2260.2743 | 2189.4698 | 2166.2148 |
| 3.4024 | 2184.5610 | 2178.0316 | 2155.3495 |
| 3.4134 | 2125.9547 | 2166.6203 | 2144.4843 |
| 3.4244 | 2115.9617 | 2155.2343 | 2133.6190 |
| 3.4354 | 2111.9017 | 2143.8721 | 2122.7537 |
| 3.4464 | 2135.7090 | 2132.5325 | 2111.8884 |
| 3.4574 | 2082.0855 | 2121.2141 | 2101.0232 |
| 3.4684 | 2053.9454 | 2109.9158 | 2090.1579 |
| 3.4794 | 2037.5319 | 2098.6365 | 2079.2926 |
| 3.4904 | 2091.8850 | 2087.3752 | 2068.4274 |
| 3.5014 | 2046.7384 | 2076.7009 | 2057.5621 |
| 3.5124 | 2045.9808 | 2065.6344 | 2047.4282 |
| 3.5234 | 2046.5959 | 2055.1531 | 2037.2943 |
| 3.5344 | 2039.0000 | 2044.6863 | 2027.1603 |
| 3.5454 | 1977.0157 | 2034.2335 | 2017.0264 |
| 3.5564 | 1943.4705 | 2023.7938 | 2006.8925 |
| 3.5674 | 1980.9931 | 2013.3667 | 1996.7586 |
| 3.5784 | 1979.0900 | 2002.9955 | 1986.6247 |
| 3.5894 | 1968.6106 | 1992.6328 | 1976.4907 |
| 3.6004 | 1938.0585 | 1982.2632 | 1966.3568 |
| 3.6114 | 1910.9321 | 1971.9025 | 1956.2229 |
| 3.6224 | 1882.6032 | 1961.5315 | 1946.0890 |
| 3.6334 | 1828.6745 | 1951.1700 | 1935.9551 |
| 3.6444 | 1824.6509 | 1940.8177 | 1925.8211 |
| 3.6554 | 1812.5015 | 1930.4740 | 1915.6872 |
| 3.6664 | 1861.3569 | 1920.1386 | 1905.5533 |
| 3.6774 | 1931.6451 | 1909.8112 | 1895.4194 |
| 3.6884 | 1833.5752 | 1899.9150 | 1885.2855 |
| 3.6994 | 1884.1760 | 1889.7227 | 1875.6953 |
| 3.7104 | 1929.1096 | 1879.9610 | 1866.1050 |
| 3.7214 | 1819.2419 | 1870.2061 | 1856.5148 |
| 3.7324 | 1873.1490 | 1860.4577 | 1846.9246 |
| 3.7434 | 1780.9754 | 1850.7155 | 1837.3344 |
| 3.7544 | 1846.5708 | 1840.9793 | 1827.7442 |
| 3.7654 | 1740.7777 | 1831.2489 | 1818.1540 |
| 3.7764 | 1789.8584 | 1821.5241 | 1808.5638 |
| 3.7874 | 1781.0885 | 1811.8046 | 1798.9736 |
| 3.7984 | 1798.8761 | 1802.0904 | 1789.3834 |
| 3.8094 | 1763.1101 | 1792.3811 | 1779.7932 |
| 3.8204 | 1768.9911 | 1782.6766 | 1770.2030 |
| 3.8314 | 1736.2980 | 1772.9768 | 1760.6128 |
| 3.8424 | 1789.8953 | 1763.2815 | 1751.0226 |
| 3.8534 | 1771.0384 | 1753.5906 | 1741.4324 |
| 3.8644 | 1784.4562 | 1743.9039 | 1731.8422 |
| 3.8754 | 1755.0835 | 1734.2212 | 1722.2520 |
| 3.8864 | 1649.5974 | 1724.5425 | 1712.6618 |
| 3.8974 | 1699.9125 | 1714.8677 | 1703.0716 |
| 3.9084 | 1697.9026 | 1705.1965 | 1693.4814 |
| 3.9194 | 1630.5634 | 1695.5290 | 1683.8912 |
| 3.9304 | 1618.6972 | 1685.8650 | 1674.3009 |
| 3.9414 | 1694.5949 | 1676.2043 | 1664.7107 |
| 3.9524 | 1635.3879 | 1666.5470 | 1655.1205 |
| 3.9634 | 1655.0610 | 1656.8929 | 1645.5303 |
| 3.9744 | 1648.1986 | 1647.2419 | 1635.9401 |
| 3.9854 | 1626.5929 | 1637.5940 | 1626.3499 |
| 3.9964 | 1604.6264 | 1627.9491 | 1616.7597 |
| 4.0074 | 1639.0137 | 1618.3070 | 1607.1695 |
| 4.0184 | 1572.4779 | 1608.6678 | 1597.5793 |
| 4.0294 | 1588.4612 | 1599.0313 | 1587.9891 |
| 4.0404 | 1562.3323 | 1589.3976 | 1578.3989 |
| 4.0514 | 1544.0030 | 1579.7665 | 1568.8087 |
| 4.0624 | 1541.8377 | 1573.1845 | 1559.2185 |
| 4.0734 | 1560.7326 | 1564.4221 | 1553.5385 |
| 4.0844 | 1629.9867 | 1558.7088 | 1547.8585 |
| 4.0954 | 1610.6765 | 1552.9978 | 1542.1784 |
| 4.1064 | 1592.7969 | 1547.2893 | 1536.4984 |
| 4.1174 | 1542.5634 | 1541.5831 | 1530.8184 |
| 4.1284 | 1531.4435 | 1535.8792 | 1525.1384 |
| 4.1394 | 1527.8525 | 1530.1776 | 1519.4584 |
| 4.1504 | 1479.7817 | 1524.4781 | 1513.7784 |
| 4.1614 | 1448.8633 | 1518.7809 | 1508.0984 |
| 4.1724 | 1479.9656 | 1513.0858 | 1502.4183 |
| 4.1834 | 1558.1947 | 1507.3928 | 1496.7383 |
| 4.1944 | 1584.3530 | 1501.7020 | 1491.0583 |

Scan List

| Vis. | Dataset Name | Start pos. [°2θ] | End pos. [°2θ] | Step [°2θ] | Meas.Date/Time |
| --- | --- | --- | --- | --- | --- |
| * | 13 Etosha22 sub 0.1-10cm S2 | 2.0054 | 29.9894 | 0.0110 | 12/7/2023 1:05:01 PM |

Peak List

| Pos. [°2θ] | Height [cts] | FWHM Left [°2θ] | d-spacing [Å] | Rel. Int. [%] |
| --- | --- | --- | --- | --- |
| 2.6976 | 1775.82 | 0.1948 | 32.72510 | 100.00 |
| 5.3151 | 89.84 | 0.1732 | 16.61334 | 5.06 |
| 7.0443 | 1314.77 | 0.5196 | 12.53848 | 74.04 |
| 8.7108 | 1145.28 | 0.2165 | 10.14310 | 64.49 |
| 13.1928 | 12.17 | 0.8659 | 6.70555 | 0.69 |
| 15.7044 | 895.63 | 0.0974 | 5.63832 | 50.43 |
| 17.6221 | 102.46 | 0.2165 | 5.02882 | 5.77 |
| 18.1696 | 142.80 | 0.1082 | 4.87851 | 8.04 |
| 19.6398 | 60.39 | 0.3031 | 4.51652 | 3.40 |
| 20.8453 | 32.90 | 0.2598 | 4.25797 | 1.85 |
| 22.4125 | 59.66 | 0.1299 | 3.96364 | 3.36 |
| 23.3229 | 51.70 | 0.1732 | 3.81094 | 2.91 |
| 24.1650 | 35.95 | 0.1299 | 3.68001 | 2.02 |
| 25.8628 | 876.81 | 0.0541 | 3.44215 | 49.37 |
| 26.6652 | 435.12 | 0.1515 | 3.34036 | 24.50 |
| 27.4857 | 268.11 | 0.1515 | 3.24248 | 15.10 |

Pattern List

| Visible | Ref.Code | Score | Compound Name | Chem. Formula | Mineral Name | SemiQuant[%] |
| --- | --- | --- | --- | --- | --- | --- |
| * | 04-024-2561 | 49 | Potassium Sodium Magnesium Aluminum Iron Silicon Titanium Oxide Fluoride Hydroxide | K0.92 Na0.04 Mg1.74 Ti0.14 Fe1.05 Al1.39 Si2.69 O10.44 ( O H )1.35 F0.21 | Phlogopite-1M | 26 |
| * | 01-089-6415 | 50 | Potassium Manganese Silicate Hydroxide Hydrate | K3.68 Mn15.904 Si25.472 O64 ( O H )9.376 ( H2 O )7.024 | Ganophyllite | 7 |
| * | 04-011-6751 | 17 | Sodium Aluminum Silicate Hydrate | Na8 Al8 Si16 O48 ( H2 O )8 | Analcime | 4 |
| * | 04-025-4215 | 33 | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide | Mg10.4 V0.36 Mn33.5 Fe0.14 Al0.69 Si6.77 As6.5 P0.3 O54 ( O H )42 | Carlfrancisite | 25 |
| * | 04-013-5980 | 25 | Magnesium Aluminum Silicon Oxide Hydroxide Hydrate | Mg Al Si4 O10 ( O H ) ( H2 O )4 | Palygorskite-O | 12 |
| * | 04-007-5003 | 10 | Potassium Aluminum Silicon Oxide | K Al Si3 O8 | Microcline | 9 |
| * | 01-080-5017 | 21 | Magnesium Silicate Hydroxide Hydrate | Mg7.73 ( Si12 O30 ) ( O H )4 ( H2 O )4 ( H2 O )6 | Sepiolite | 4 |
| * | 01-076-8348 | 42 | Potassium Sodium Magnesium Manganese Aluminum Iron Titanium Fluoride Aluminum Iron Silicate Hydroxide | ( K0.96 Na0.02 ) ( Fe0.58 Mg0.23 Mn0.05 ) ( Fe0.46 Al0.315 Mg0.155 Ti0.07 )2 ( ( Si2.77 Al1.18 Fe0.05 ) O10.38 ) ( O H )1.56 F0.06 | Biotite-1M | 12 |

Anchor Scan Parameters

Dataset Name	13 Etosha22 sub 0.1-10cm S2

File name	C:\aeris_data\XRD data\Goldstein\Etosha 2023\Etosha Clay Data\Sample 13\13 Etosha22 sub 0.1-10cm S2.xrdml

Sample Identification	13 Etosha22 sub 0.1-10cm S2

Measurement Start Date/Time	12/7/2023 1:05:01 PM

Operator	Instrument

Raw Data Origin	XRD measurement (*.XRDML)

Scan Axis	Gonio

Start Position [°2θ]	2.0054

End Position [°2θ]	29.9894

Step Size [°2θ]	0.0110

Scan Step Time [s]	48.1950

Scan Type	Continuous

PSD Mode	Scanning

PSD Length [°2θ]	5.54

Offset [°2θ]	0.0000

Divergence Slit Type	Fixed

Divergence Slit Size [°]	0.0603

Specimen Length [mm]	10.00

Measurement Temperature [°C]	25.00

Anode Material	Cu

K-α1 [Å]	1.54060

K-α2 [Å]	1.54443

K-β1 [Å]	1.39225

K-A2 / K-A1 Ratio	0.50000

Generator Settings	15 mA, 40 kV

Diffractometer Type	2082464

Diffractometer Number	0

Goniometer Radius [mm]	145.00

Dist. Focus-Diverg. Slit [mm]	95.00

Incident Beam Monochromator	No

Spinning	Yes