13R Etosha 22 sub 0.1-10 cm S2 400 C

Graphics

Graphics

Graphics

Quantitative Results

Phase Titanium Oxide

Weight fraction/ %	5.0

Phase Potassium Sodium Calcium Aluminum Silicon Oxide Hydrate

Weight fraction/ %	6.0

Phase Potassium Sodium Magnesium Aluminum Iron Silicon Titanium Oxide Fluoride Hydroxide

Weight fraction/ %	19.0

Phase Potassium Magnesium Aluminum Silicate Fluoride Hydroxide

Weight fraction/ %	16.0

Phase Potassium Sodium Aluminum Silicate

Weight fraction/ %	7.0

Phase Potassium Manganese Aluminum Silicon Oxide Hydroxide Hydrate

Weight fraction/ %	1.0

Phase Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide

Weight fraction/ %	18.0

Phase Potassium Aluminum Silicate

Weight fraction/ %	21.0

Phase Magnesium Aluminum Silicon Oxide Hydroxide Hydrate

Weight fraction/ %	7.0

Multiple Quantitative Results

Scans vs Phases Matrix

| Scan name | Titanium Oxide | Potassium Sodium Calcium Aluminum Silicon Oxide Hydrate | Potassium Sodium Magnesium Aluminum Iron Silicon Titanium Oxide Fluoride Hydroxide | Potassium Magnesium Aluminum Silicate Fluoride Hydroxide | Potassium Sodium Aluminum Silicate | Potassium Manganese Aluminum Silicon Oxide Hydroxide Hydrate | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide | Potassium Aluminum Silicate | Magnesium Aluminum Silicon Oxide Hydroxide Hydrate |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 13 400c | 5.0 | 6.0 | 19.0 | 16.0 | 7.0 | 1.0 | 18.0 | 21.0 | 7.0 |

Anchor Scan Data

| Pos. [°2θ] | Iobs [cts] | Icalc [cts] | Iback [cts] |
| --- | --- | --- | --- |
| 2.0054 | 7496.0000 | 7496.5930 | 7496.0000 |
| 2.0164 | 7317.7375 | 7457.1810 | 7440.5905 |
| 2.0274 | 7375.4022 | 7402.2937 | 7385.1809 |
| 2.0384 | 7314.4705 | 7347.4320 | 7329.7714 |
| 2.0494 | 7374.2311 | 7292.5974 | 7274.3618 |
| 2.0604 | 7289.1288 | 7237.7919 | 7218.9523 |
| 2.0714 | 7393.1327 | 7183.0174 | 7163.5427 |
| 2.0824 | 7329.1608 | 7128.2761 | 7108.1332 |
| 2.0934 | 7303.5231 | 7073.5702 | 7052.7236 |
| 2.1044 | 7310.3761 | 7018.9023 | 6997.3141 |
| 2.1154 | 7021.3068 | 6964.2753 | 6941.9045 |
| 2.1264 | 6956.8977 | 6909.6920 | 6886.4950 |
| 2.1374 | 7037.2773 | 6855.1559 | 6831.0854 |
| 2.1484 | 7051.9336 | 6800.6705 | 6775.6759 |
| 2.1594 | 7013.4543 | 6746.2398 | 6720.2663 |
| 2.1704 | 7047.0487 | 6691.8682 | 6664.8568 |
| 2.1814 | 6912.7788 | 6637.5605 | 6609.4472 |
| 2.1924 | 7001.2542 | 6583.2863 | 6554.0377 |
| 2.2034 | 6910.7434 | 6529.0309 | 6498.5006 |
| 2.2144 | 6797.9636 | 6474.8214 | 6442.9636 |
| 2.2254 | 6881.5850 | 6420.7005 | 6387.4265 |
| 2.2364 | 6777.2906 | 6366.6763 | 6331.8895 |
| 2.2474 | 6764.7758 | 6312.7576 | 6276.3524 |
| 2.2584 | 6714.2153 | 6258.9544 | 6220.8154 |
| 2.2694 | 6770.4513 | 6205.2779 | 6165.2783 |
| 2.2804 | 6909.7414 | 6151.7407 | 6109.7413 |
| 2.2914 | 6820.0108 | 6098.3572 | 6054.2042 |
| 2.3024 | 6766.8274 | 6045.1439 | 5998.6672 |
| 2.3134 | 6677.1367 | 5992.1200 | 5943.1301 |
| 2.3244 | 6609.3559 | 5939.3080 | 5887.5931 |
| 2.3354 | 6535.7817 | 5886.7349 | 5832.0560 |
| 2.3464 | 6510.4744 | 5834.4339 | 5776.5189 |
| 2.3574 | 6452.1288 | 5782.4460 | 5720.9819 |
| 2.3684 | 6399.7906 | 5730.8233 | 5665.4448 |
| 2.3794 | 6422.0895 | 5679.6328 | 5609.9078 |
| 2.3904 | 6436.6150 | 5628.9619 | 5554.3707 |
| 2.4014 | 6425.0088 | 5578.9250 | 5498.8337 |
| 2.4124 | 6334.1539 | 5529.6725 | 5443.2966 |
| 2.4234 | 6301.0295 | 5481.4009 | 5387.7596 |
| 2.4344 | 6331.8923 | 5434.3652 | 5332.2225 |
| 2.4454 | 6329.8663 | 5388.8919 | 5276.6855 |
| 2.4564 | 6276.5201 | 5345.3923 | 5221.1484 |
| 2.4674 | 6204.6431 | 5304.3748 | 5165.6114 |
| 2.4784 | 6207.2129 | 5266.4529 | 5110.0743 |
| 2.4894 | 6095.6961 | 5232.3486 | 5054.5373 |
| 2.5004 | 6035.2478 | 5202.8856 | 4999.0002 |
| 2.5114 | 6020.1150 | 5178.9726 | 4943.4632 |
| 2.5224 | 5900.7025 | 5161.5718 | 4887.9261 |
| 2.5334 | 5964.7139 | 5151.6529 | 4832.3891 |
| 2.5444 | 6000.0123 | 5150.1313 | 4776.8520 |
| 2.5554 | 5952.8653 | 5157.7926 | 4721.3150 |
| 2.5664 | 5930.2094 | 5175.1698 | 4665.7779 |
| 2.5774 | 5950.7611 | 5202.4975 | 4610.1134 |
| 2.5884 | 5920.0973 | 5239.6346 | 4554.4488 |
| 2.5994 | 5900.9735 | 5285.9260 | 4498.7843 |
| 2.6104 | 5891.1558 | 5340.0256 | 4443.1197 |
| 2.6214 | 5897.3894 | 5399.7854 | 4387.4551 |
| 2.6324 | 5627.6681 | 5462.0862 | 4331.7906 |
| 2.6434 | 5719.5871 | 5522.6694 | 4276.1260 |
| 2.6544 | 5751.0624 | 5576.0462 | 4220.4615 |
| 2.6654 | 5669.7906 | 5615.6309 | 4164.7969 |
| 2.6764 | 5536.2866 | 5634.2883 | 4109.1324 |
| 2.6874 | 5452.5152 | 5625.3986 | 4053.4678 |
| 2.6984 | 5299.3938 | 5584.2642 | 3997.8033 |
| 2.7094 | 5179.5506 | 5509.3399 | 3942.1387 |
| 2.7204 | 5191.5546 | 5402.6767 | 3886.4741 |
| 2.7314 | 4988.2743 | 5269.3322 | 3830.8096 |
| 2.7424 | 4841.8269 | 5116.0760 | 3775.1450 |
| 2.7534 | 4675.5722 | 4949.9665 | 3719.4805 |
| 2.7644 | 4507.9144 | 4777.4248 | 3663.6583 |
| 2.7754 | 4356.5251 | 4603.7897 | 3607.8362 |
| 2.7864 | 4214.6996 | 4433.1943 | 3552.0140 |
| 2.7974 | 4001.4247 | 4268.6112 | 3496.1919 |
| 2.8084 | 3833.3377 | 4112.0668 | 3440.3697 |
| 2.8194 | 3894.3107 | 3964.8076 | 3384.5475 |
| 2.8304 | 3571.0634 | 3827.4436 | 3328.7254 |
| 2.8414 | 3570.0895 | 3700.0715 | 3272.9032 |
| 2.8524 | 3505.7512 | 3582.3866 | 3217.0811 |
| 2.8634 | 3165.4955 | 3473.7843 | 3161.2589 |
| 2.8744 | 3266.5482 | 3373.4560 | 3105.4368 |
| 2.8854 | 3060.5604 | 3280.4746 | 3049.6146 |
| 2.8964 | 3123.7035 | 3193.8685 | 2993.7924 |
| 2.9074 | 2863.9213 | 3112.6807 | 2937.9703 |
| 2.9184 | 2853.4961 | 3036.0131 | 2882.1481 |
| 2.9294 | 2827.3127 | 2963.0555 | 2826.3260 |
| 2.9404 | 2774.0919 | 2905.6789 | 2770.5038 |
| 2.9514 | 2713.2547 | 2849.2995 | 2738.4291 |
| 2.9624 | 2724.1563 | 2807.4085 | 2706.3545 |
| 2.9734 | 2584.5732 | 2767.0296 | 2674.2798 |
| 2.9844 | 2505.8830 | 2727.8472 | 2642.2051 |
| 2.9954 | 2542.8053 | 2689.6152 | 2610.1305 |
| 3.0064 | 2465.0570 | 2652.1442 | 2578.0558 |
| 3.0174 | 2518.7227 | 2615.2895 | 2545.9811 |
| 3.0284 | 2465.5546 | 2578.9407 | 2513.9065 |
| 3.0394 | 2398.2429 | 2543.0139 | 2481.8318 |
| 3.0504 | 2392.7615 | 2507.4443 | 2449.7571 |
| 3.0614 | 2353.7729 | 2472.1815 | 2417.6825 |
| 3.0724 | 2437.0447 | 2437.1857 | 2385.6078 |
| 3.0834 | 2346.0708 | 2402.4249 | 2353.5331 |
| 3.0944 | 2243.2434 | 2367.8726 | 2321.4585 |
| 3.1054 | 2218.9971 | 2333.5069 | 2289.3838 |
| 3.1164 | 2229.2050 | 2299.3089 | 2257.3091 |
| 3.1274 | 2182.2921 | 2273.0575 | 2225.2345 |
| 3.1384 | 2276.0413 | 2246.0712 | 2207.8773 |
| 3.1494 | 2238.4002 | 2227.0049 | 2190.5202 |
| 3.1604 | 2220.1327 | 2208.0526 | 2173.1630 |
| 3.1714 | 2119.2517 | 2189.2046 | 2155.8059 |
| 3.1824 | 2091.1937 | 2170.4521 | 2138.4487 |
| 3.1934 | 2123.0797 | 2151.7873 | 2121.0916 |
| 3.2044 | 2112.5919 | 2133.2030 | 2103.7344 |
| 3.2154 | 2044.0964 | 2114.6930 | 2086.3773 |
| 3.2264 | 2050.6209 | 2096.2513 | 2069.0202 |
| 3.2374 | 2027.7148 | 2077.8729 | 2051.6630 |
| 3.2484 | 2051.3334 | 2059.5530 | 2034.3059 |
| 3.2594 | 2072.2891 | 2041.2872 | 2016.9487 |
| 3.2704 | 2021.3751 | 2023.0716 | 1999.5916 |
| 3.2814 | 1983.0177 | 2004.9028 | 1982.2344 |
| 3.2924 | 1898.6593 | 1986.7773 | 1964.8773 |
| 3.3034 | 1917.2862 | 1968.6923 | 1947.5201 |
| 3.3144 | 1985.6406 | 1953.4396 | 1930.1630 |
| 3.3254 | 1931.5103 | 1937.9092 | 1918.0823 |
| 3.3364 | 1875.5398 | 1925.2064 | 1906.0016 |
| 3.3474 | 1891.0029 | 1912.5342 | 1893.9209 |
| 3.3584 | 1904.3776 | 1899.8909 | 1881.8401 |
| 3.3694 | 1901.1327 | 1887.2746 | 1869.7594 |
| 3.3804 | 1792.2787 | 1874.6836 | 1857.6787 |
| 3.3914 | 1734.9469 | 1862.1164 | 1845.5980 |
| 3.4024 | 1781.0482 | 1849.5716 | 1833.5173 |
| 3.4134 | 1774.3373 | 1837.0478 | 1821.4366 |
| 3.4244 | 1769.9808 | 1824.5439 | 1809.3558 |
| 3.4354 | 1734.1730 | 1812.0587 | 1797.2751 |
| 3.4464 | 1730.6760 | 1799.5910 | 1785.1944 |
| 3.4574 | 1765.1829 | 1787.1401 | 1773.1137 |
| 3.4684 | 1703.2778 | 1774.7049 | 1761.0330 |
| 3.4794 | 1641.2960 | 1762.2846 | 1748.9523 |
| 3.4904 | 1699.2257 | 1749.8783 | 1736.8716 |
| 3.5014 | 1767.9076 | 1738.0855 | 1724.7908 |
| 3.5124 | 1750.4902 | 1726.2382 | 1713.8431 |
| 3.5234 | 1698.7994 | 1715.0029 | 1702.8953 |
| 3.5344 | 1692.9184 | 1703.7790 | 1691.9475 |
| 3.5454 | 1654.4759 | 1692.5659 | 1680.9997 |
| 3.5564 | 1675.3850 | 1681.3632 | 1670.0519 |
| 3.5674 | 1633.8456 | 1670.1702 | 1659.1042 |
| 3.5784 | 1641.5167 | 1658.9865 | 1648.1564 |
| 3.5894 | 1655.3894 | 1647.8117 | 1637.2086 |
| 3.6004 | 1621.8009 | 1636.6453 | 1626.2608 |
| 3.6114 | 1563.5359 | 1625.4871 | 1615.3130 |
| 3.6224 | 1601.0207 | 1614.3365 | 1604.3653 |
| 3.6334 | 1575.3225 | 1603.1932 | 1593.4175 |
| 3.6444 | 1578.6391 | 1592.0570 | 1582.4697 |
| 3.6554 | 1559.0649 | 1580.9274 | 1571.5219 |
| 3.6664 | 1516.4823 | 1569.8043 | 1560.5741 |
| 3.6774 | 1575.1180 | 1558.6873 | 1549.6264 |
| 3.6884 | 1546.2566 | 1548.5880 | 1538.6786 |
| 3.6994 | 1516.8938 | 1538.3811 | 1529.6412 |
| 3.7104 | 1511.2847 | 1529.1914 | 1520.6039 |
| 3.7214 | 1480.7257 | 1520.0069 | 1511.5665 |
| 3.7324 | 1438.0231 | 1510.8273 | 1502.5291 |
| 3.7434 | 1517.8948 | 1501.6525 | 1493.4918 |
| 3.7544 | 1478.1490 | 1492.4823 | 1484.4544 |
| 3.7654 | 1432.5044 | 1483.3164 | 1475.4171 |
| 3.7764 | 1446.6618 | 1474.1548 | 1466.3797 |
| 3.7874 | 1451.9558 | 1464.9972 | 1457.3423 |
| 3.7984 | 1483.7625 | 1455.8435 | 1448.3050 |
| 3.8094 | 1414.8112 | 1446.6935 | 1439.2676 |
| 3.8204 | 1403.5044 | 1437.5472 | 1430.2303 |
| 3.8314 | 1419.9115 | 1428.4043 | 1421.1929 |
| 3.8424 | 1391.7905 | 1419.2648 | 1412.1555 |
| 3.8534 | 1354.9853 | 1410.1285 | 1403.1182 |
| 3.8644 | 1397.6141 | 1400.9953 | 1394.0808 |
| 3.8754 | 1391.9262 | 1392.6362 | 1385.0435 |
| 3.8864 | 1379.2699 | 1384.1937 | 1377.4619 |
| 3.8974 | 1369.4749 | 1376.5251 | 1369.8804 |
| 3.9084 | 1397.8485 | 1368.8592 | 1362.2988 |
| 3.9194 | 1305.4071 | 1361.1958 | 1354.7173 |
| 3.9304 | 1337.7925 | 1353.5350 | 1347.1358 |
| 3.9414 | 1330.3471 | 1345.8767 | 1339.5542 |
| 3.9524 | 1320.1549 | 1338.2207 | 1331.9727 |
| 3.9634 | 1284.9951 | 1330.5670 | 1324.3911 |
| 3.9744 | 1270.3992 | 1322.9155 | 1316.8096 |
| 3.9854 | 1263.7876 | 1315.2662 | 1309.2280 |
| 3.9964 | 1266.3702 | 1307.6190 | 1301.6465 |
| 4.0074 | 1276.8151 | 1299.9737 | 1294.0650 |
| 4.0184 | 1275.9912 | 1292.3305 | 1286.4834 |
| 4.0294 | 1271.6607 | 1284.6891 | 1278.9019 |
| 4.0404 | 1237.2861 | 1277.0496 | 1271.3203 |
| 4.0514 | 1266.3157 | 1269.4118 | 1263.7388 |
| 4.0624 | 1288.0526 | 1261.7758 | 1256.1572 |
| 4.0734 | 1228.0787 | 1254.1415 | 1248.5757 |
| 4.0844 | 1239.2168 | 1246.5088 | 1240.9941 |
| 4.0954 | 1211.9233 | 1238.8778 | 1233.4126 |
| 4.1064 | 1197.8181 | 1231.2483 | 1225.8311 |
| 4.1174 | 1195.5280 | 1223.6202 | 1218.2495 |
| 4.1284 | 1172.4695 | 1215.9937 | 1210.6680 |
| 4.1394 | 1182.7787 | 1208.3686 | 1203.0864 |
| 4.1504 | 1164.2345 | 1200.7449 | 1195.5049 |
| 4.1614 | 1205.2262 | 1193.1226 | 1187.9233 |
| 4.1724 | 1220.8427 | 1185.5015 | 1180.3418 |
| 4.1834 | 1190.3451 | 1177.8818 | 1172.7603 |
| 4.1944 | 1175.3093 | 1170.2634 | 1165.1787 |

Scan List

| Vis. | Dataset Name | Start pos. [°2θ] | End pos. [°2θ] | Step [°2θ] | Meas.Date/Time |
| --- | --- | --- | --- | --- | --- |
| * | 13 400c | 2.0054 | 29.9894 | 0.0110 | 4/25/2024 1:50:18 PM |

Peak List

| Pos. [°2θ] | Height [cts] | FWHM Left [°2θ] | d-spacing [Å] | Rel. Int. [%] |
| --- | --- | --- | --- | --- |
| 2.6954 | 1416.08 | 0.1948 | 32.75094 | 100.00 |
| 7.0295 | 364.55 | 0.5196 | 12.56491 | 25.74 |
| 8.6899 | 1370.57 | 0.1948 | 10.16747 | 96.79 |
| 13.2585 | 20.18 | 0.5196 | 6.67248 | 1.43 |
| 15.7146 | 1005.59 | 0.0866 | 5.63471 | 71.01 |
| 17.6180 | 159.00 | 0.1299 | 5.02999 | 11.23 |
| 18.2153 | 103.33 | 0.1299 | 4.86638 | 7.30 |
| 19.5575 | 51.06 | 0.2598 | 4.53533 | 3.61 |
| 20.7872 | 25.95 | 0.2598 | 4.26972 | 1.83 |
| 22.3716 | 61.86 | 0.1732 | 3.97080 | 4.37 |
| 23.3285 | 63.16 | 0.1732 | 3.81003 | 4.46 |
| 24.1807 | 52.23 | 0.1299 | 3.67766 | 3.69 |
| 25.8885 | 601.85 | 0.0974 | 3.43880 | 42.50 |
| 26.6416 | 548.72 | 0.1299 | 3.34327 | 38.75 |
| 27.4578 | 569.04 | 0.0758 | 3.24572 | 40.18 |

Pattern List

| Visible | Ref.Code | Score | Compound Name | Chem. Formula | Mineral Name | SemiQuant[%] |
| --- | --- | --- | --- | --- | --- | --- |
| * | 04-008-7810 | 55 | Titanium Oxide | Ti O2 | Rutile | 5 |
| * | 04-024-8347 | 36 | Potassium Sodium Calcium Aluminum Silicon Oxide Hydrate | K0.19 Na7.69 Ca0.06 Al8 Si16 O48 ( H2 O )8 | Analcime | 6 |
| * | 04-015-8232 | 21 | Potassium Sodium Magnesium Aluminum Iron Silicon Titanium Oxide Fluoride Hydroxide | K0.97 Na0.05 Mg0.99 Ti0.14 Fe1.24 Al1.82 Si2.63 O10.18 ( O H )1.75 F0.07 | Biotite-1M | 19 |
| * | 01-073-1660 | 18 | Potassium Magnesium Aluminum Silicate Fluoride Hydroxide | K Mg3 ( Al Si3 O10 ) ( O H ) F | Phlogopite | 16 |
| * | 01-076-2756 | 22 | Potassium Sodium Aluminum Silicate | ( K0.8 Na0.2 ) ( Al Si3 O8 ) | Sanidine | 7 |
| * | 04-017-7286 | 33 | Potassium Manganese Aluminum Silicon Oxide Hydroxide Hydrate | K0.8 Mn4 Al1.08 Si4.92 O16 ( O H )2 ( H2 O )3 | Ganophyllite | 1 |
| * | 04-025-4215 | 21 | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide | Mg10.4 V0.36 Mn33.5 Fe0.14 Al0.69 Si6.77 As6.5 P0.3 O54 ( O H )42 | Carlfrancisite | 18 |
| * | 01-076-1239 | 18 | Potassium Aluminum Silicate | K ( Al Si3 O8 ) | Microcline | 21 |
| * | 01-081-8598 | 15 | Magnesium Aluminum Silicon Oxide Hydroxide Hydrate | ( Mg2 Al2 ) Si8 O20 ( H2 O )4 ( O H )2 ( H2 O )3.84 | Palygorskite-M | 7 |

Anchor Scan Parameters

Dataset Name	13 400c

File name	C:\aeris_data\XRD data\Goldstein\Etosha 2023\Etosha Clay Data\REP 13\13 400c.xrdml

Sample Identification	13 400c

Measurement Start Date/Time	4/25/2024 1:50:18 PM

Operator	Instrument

Raw Data Origin	XRD measurement (*.XRDML)

Scan Axis	Gonio

Start Position [°2θ]	2.0054

End Position [°2θ]	29.9894

Step Size [°2θ]	0.0110

Scan Step Time [s]	48.1950

Scan Type	Continuous

PSD Mode	Scanning

PSD Length [°2θ]	5.54

Offset [°2θ]	0.0000

Divergence Slit Type	Fixed

Divergence Slit Size [°]	0.0603

Specimen Length [mm]	10.00

Measurement Temperature [°C]	25.00

Anode Material	Cu

K-α1 [Å]	1.54060

K-α2 [Å]	1.54443

K-β1 [Å]	1.39225

K-A2 / K-A1 Ratio	0.50000

Generator Settings	15 mA, 40 kV

Diffractometer Type	2082464

Diffractometer Number	0

Goniometer Radius [mm]	145.00

Dist. Focus-Diverg. Slit [mm]	95.00

Incident Beam Monochromator	No

Spinning	Yes