13R Etosha 22 sub 0.1-10 cm S2 550 C REPORT

Graphics

Graphics

Graphics

Quantitative Results

Phase Sodium Aluminum Silicate Hydrate

Weight fraction/ %	7.0

Phase Titanium Antimony Vanadium Oxide

Weight fraction/ %	5.0

Phase Potassium Magnesium Manganese Iron Aluminum Silicate Hydroxide

Weight fraction/ %	16.0

Phase Potassium Magnesium Aluminum Silicate Hydroxide

Weight fraction/ %	21.0

Phase Potassium Aluminum Silicate

Weight fraction/ %	17.0

Phase Potassium Sodium Aluminum Silicate

Weight fraction/ %	4.0

Phase Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide

Weight fraction/ %	19.0

Phase Magnesium Aluminum Silicon Oxide Hydroxide Hydrate

Weight fraction/ %	10.0

Multiple Quantitative Results

Scans vs Phases Matrix

| Scan name | Sodium Aluminum Silicate Hydrate | Titanium Antimony Vanadium Oxide | Potassium Magnesium Manganese Iron Aluminum Silicate Hydroxide | Potassium Magnesium Aluminum Silicate Hydroxide | Potassium Aluminum Silicate | Potassium Sodium Aluminum Silicate | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide | Magnesium Aluminum Silicon Oxide Hydroxide Hydrate |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 13 550c | 7.0 | 5.0 | 16.0 | 21.0 | 17.0 | 4.0 | 19.0 | 10.0 |

Anchor Scan Data

| Pos. [°2θ] | Iobs [cts] | Icalc [cts] | Iback [cts] |
| --- | --- | --- | --- |
| 2.0054 | 7842.0000 | 7830.1592 | 7842.0000 |
| 2.0164 | 7738.5329 | 7793.8714 | 7783.3858 |
| 2.0274 | 7701.5654 | 7735.6037 | 7724.7717 |
| 2.0384 | 7718.9484 | 7677.3535 | 7666.1575 |
| 2.0494 | 7585.9184 | 7619.1217 | 7607.5434 |
| 2.0604 | 7562.9720 | 7560.9099 | 7548.9292 |
| 2.0714 | 7528.0914 | 7502.7192 | 7490.3150 |
| 2.0824 | 7473.8378 | 7444.5514 | 7431.7009 |
| 2.0934 | 7421.8515 | 7386.4079 | 7373.0867 |
| 2.1044 | 7423.7743 | 7328.2905 | 7314.4726 |
| 2.1154 | 7241.9056 | 7270.2014 | 7255.8584 |
| 2.1264 | 7313.8550 | 7212.1426 | 7197.2443 |
| 2.1374 | 7199.3068 | 7154.1164 | 7138.6301 |
| 2.1484 | 7270.1760 | 7096.1255 | 7080.0159 |
| 2.1594 | 7209.5487 | 7038.1728 | 7021.4018 |
| 2.1704 | 7228.7994 | 6980.2614 | 6962.7876 |
| 2.1814 | 7257.4012 | 6922.3947 | 6904.1735 |
| 2.1924 | 7162.0447 | 6864.5089 | 6845.5593 |
| 2.2034 | 7177.9469 | 6806.6309 | 6786.7645 |
| 2.2144 | 7181.4675 | 6748.7428 | 6727.9697 |
| 2.2254 | 7044.9213 | 6690.9177 | 6669.1750 |
| 2.2364 | 7005.4823 | 6633.1614 | 6610.3802 |
| 2.2474 | 7004.2547 | 6575.4806 | 6551.5854 |
| 2.2584 | 7031.6632 | 6517.8826 | 6492.7906 |
| 2.2694 | 6947.6047 | 6460.3759 | 6433.9958 |
| 2.2804 | 6908.1485 | 6402.9698 | 6375.2010 |
| 2.2914 | 6809.7719 | 6345.6750 | 6316.4063 |
| 2.3024 | 6889.8407 | 6288.5034 | 6257.6115 |
| 2.3134 | 6960.2793 | 6231.4689 | 6198.8167 |
| 2.3244 | 6880.3653 | 6174.5870 | 6140.0219 |
| 2.3354 | 6727.9882 | 6117.8757 | 6081.2271 |
| 2.3464 | 6674.2802 | 6061.3555 | 6022.4324 |
| 2.3574 | 6651.9587 | 6005.0505 | 5963.6376 |
| 2.3684 | 6702.9513 | 5948.9886 | 5904.8428 |
| 2.3794 | 6709.3884 | 5893.1480 | 5846.0480 |
| 2.3904 | 6618.1362 | 5837.5869 | 5787.1071 |
| 2.4014 | 6548.1858 | 5782.3357 | 5728.1662 |
| 2.4124 | 6485.8579 | 5727.5108 | 5669.2253 |
| 2.4234 | 6403.0354 | 5673.1925 | 5610.2844 |
| 2.4344 | 6455.7935 | 5619.4886 | 5551.3435 |
| 2.4454 | 6555.8869 | 5566.5475 | 5492.4025 |
| 2.4564 | 6553.2134 | 5514.5779 | 5433.4616 |
| 2.4674 | 6396.6991 | 5463.8753 | 5374.5207 |
| 2.4784 | 6350.3992 | 5414.8569 | 5315.5798 |
| 2.4894 | 6354.8368 | 5368.1043 | 5256.6389 |
| 2.5004 | 6319.8142 | 5324.4114 | 5197.6980 |
| 2.5114 | 6309.3963 | 5284.8297 | 5138.7571 |
| 2.5224 | 6252.1008 | 5250.7040 | 5079.8162 |
| 2.5334 | 6258.8171 | 5223.6809 | 5020.8753 |
| 2.5444 | 6173.1273 | 5205.6772 | 4961.9344 |
| 2.5554 | 6159.4445 | 5198.7903 | 4902.9934 |
| 2.5664 | 6124.0177 | 5205.1417 | 4844.0525 |
| 2.5774 | 6059.1042 | 5226.6496 | 4785.1116 |
| 2.5884 | 6137.5939 | 5264.7383 | 4726.1707 |
| 2.5994 | 6060.2212 | 5319.9985 | 4667.2298 |
| 2.6104 | 6007.1401 | 5391.8076 | 4608.2889 |
| 2.6214 | 5999.6106 | 5477.9018 | 4549.3480 |
| 2.6324 | 5930.9469 | 5573.8723 | 4490.4071 |
| 2.6434 | 5889.0295 | 5672.5762 | 4431.4662 |
| 2.6544 | 5922.1593 | 5763.6140 | 4372.5253 |
| 2.6654 | 5852.9292 | 5833.3894 | 4313.5844 |
| 2.6764 | 5586.8274 | 5866.6443 | 4254.6434 |
| 2.6874 | 5589.5389 | 5850.0356 | 4195.7025 |
| 2.6984 | 5529.8230 | 5776.7073 | 4136.7616 |
| 2.7094 | 5403.5251 | 5649.0978 | 4077.8207 |
| 2.7204 | 5184.2596 | 5477.8725 | 4018.8798 |
| 2.7314 | 5024.8643 | 5277.8440 | 3959.9389 |
| 2.7424 | 4871.3574 | 5063.6975 | 3900.9980 |
| 2.7534 | 4694.3933 | 4847.4212 | 3842.0571 |
| 2.7644 | 4465.7006 | 4637.7546 | 3782.9700 |
| 2.7754 | 4364.6116 | 4440.3872 | 3723.8830 |
| 2.7864 | 4184.7030 | 4258.6506 | 3664.7960 |
| 2.7974 | 4148.4956 | 4093.9377 | 3605.7089 |
| 2.8084 | 4002.5432 | 3946.2192 | 3546.6219 |
| 2.8194 | 3751.3392 | 3814.4460 | 3487.5348 |
| 2.8304 | 3570.3672 | 3696.9100 | 3428.4478 |
| 2.8414 | 3522.4376 | 3591.5612 | 3369.3608 |
| 2.8524 | 3499.1790 | 3496.2679 | 3310.2737 |
| 2.8634 | 3373.3687 | 3409.0093 | 3251.1867 |
| 2.8744 | 3152.4395 | 3327.9972 | 3192.0997 |
| 2.8854 | 3200.0806 | 3251.7352 | 3133.0126 |
| 2.8964 | 3070.5796 | 3179.0279 | 3073.9256 |
| 2.9074 | 2996.5123 | 3108.9576 | 3014.8385 |
| 2.9184 | 2934.3751 | 3040.8419 | 2955.7515 |
| 2.9294 | 2900.9174 | 2974.1865 | 2896.6645 |
| 2.9404 | 2810.3422 | 2918.1353 | 2837.5774 |
| 2.9514 | 2831.6430 | 2869.2559 | 2803.7944 |
| 2.9624 | 2705.2861 | 2830.5558 | 2770.0114 |
| 2.9734 | 2640.1229 | 2792.4126 | 2736.2284 |
| 2.9844 | 2611.2060 | 2754.7337 | 2702.4454 |
| 2.9954 | 2528.9911 | 2717.4487 | 2668.6624 |
| 3.0064 | 2463.3648 | 2680.5030 | 2634.8794 |
| 3.0174 | 2409.2920 | 2643.8525 | 2601.0964 |
| 3.0284 | 2381.2906 | 2607.4611 | 2567.3133 |
| 3.0394 | 2391.0570 | 2571.2983 | 2533.5303 |
| 3.0504 | 2339.8501 | 2535.3384 | 2499.7473 |
| 3.0614 | 2358.6785 | 2499.5590 | 2465.9643 |
| 3.0724 | 2375.0020 | 2463.9410 | 2432.1813 |
| 3.0834 | 2373.6342 | 2428.4676 | 2398.3983 |
| 3.0944 | 2410.1062 | 2393.1242 | 2364.6153 |
| 3.1054 | 2264.8545 | 2357.8979 | 2330.8323 |
| 3.1164 | 2274.0354 | 2322.7775 | 2297.0492 |
| 3.1274 | 2298.0029 | 2293.9860 | 2263.2662 |
| 3.1384 | 2240.5526 | 2269.4251 | 2246.0932 |
| 3.1494 | 2195.2340 | 2251.1765 | 2228.9202 |
| 3.1604 | 2131.0000 | 2232.9999 | 2211.7472 |
| 3.1714 | 2143.7198 | 2214.8893 | 2194.5742 |
| 3.1824 | 2149.0491 | 2196.8388 | 2177.4012 |
| 3.1934 | 2092.4159 | 2178.8436 | 2160.2282 |
| 3.2044 | 2083.3397 | 2160.8992 | 2143.0552 |
| 3.2154 | 2088.9282 | 2143.0014 | 2125.8822 |
| 3.2264 | 2085.2493 | 2125.1466 | 2108.7092 |
| 3.2374 | 2087.1023 | 2107.3315 | 2091.5362 |
| 3.2484 | 2064.0000 | 2089.5531 | 2074.3631 |
| 3.2594 | 2008.7286 | 2071.8086 | 2057.1901 |
| 3.2704 | 2045.8840 | 2054.0956 | 2040.0171 |
| 3.2814 | 2020.0502 | 2036.4118 | 2022.8441 |
| 3.2924 | 2017.9734 | 2018.7552 | 2005.6711 |
| 3.3034 | 1989.1986 | 2001.1239 | 1988.4981 |
| 3.3144 | 1962.9430 | 1984.9951 | 1971.3251 |
| 3.3254 | 1947.8230 | 1969.8715 | 1958.0933 |
| 3.3364 | 1938.1263 | 1956.2474 | 1944.8614 |
| 3.3474 | 1931.9813 | 1942.6424 | 1931.6296 |
| 3.3584 | 1887.0250 | 1929.0555 | 1918.3977 |
| 3.3694 | 1833.3373 | 1915.4854 | 1905.1659 |
| 3.3804 | 1859.3097 | 1901.9311 | 1891.9341 |
| 3.3914 | 1861.1858 | 1888.3916 | 1878.7022 |
| 3.4024 | 1844.5123 | 1874.8660 | 1865.4704 |
| 3.4134 | 1896.6057 | 1861.3535 | 1852.2385 |
| 3.4244 | 1879.4454 | 1847.8534 | 1839.0067 |
| 3.4354 | 1808.1081 | 1834.3650 | 1825.7748 |
| 3.4464 | 1801.4228 | 1820.8874 | 1812.5430 |
| 3.4574 | 1809.3776 | 1807.4203 | 1799.3112 |
| 3.4684 | 1762.0314 | 1793.9629 | 1786.0793 |
| 3.4794 | 1777.7021 | 1780.5148 | 1772.8475 |
| 3.4904 | 1802.9779 | 1767.0755 | 1759.6156 |
| 3.5014 | 1726.0963 | 1754.7481 | 1746.3838 |
| 3.5124 | 1733.8196 | 1743.1622 | 1736.0930 |
| 3.5234 | 1690.9528 | 1732.6875 | 1725.8022 |
| 3.5344 | 1669.3761 | 1722.2199 | 1715.5114 |
| 3.5454 | 1728.2183 | 1711.7589 | 1705.2206 |
| 3.5564 | 1690.6239 | 1701.3043 | 1694.9298 |
| 3.5674 | 1596.7030 | 1690.8558 | 1684.6390 |
| 3.5784 | 1625.0334 | 1680.4131 | 1674.3482 |
| 3.5894 | 1638.9204 | 1669.9759 | 1664.0574 |
| 3.6004 | 1609.8407 | 1659.5438 | 1653.7666 |
| 3.6114 | 1636.1632 | 1649.1168 | 1643.4759 |
| 3.6224 | 1681.3053 | 1638.6945 | 1633.1851 |
| 3.6334 | 1669.5231 | 1628.2768 | 1622.8943 |
| 3.6444 | 1594.3338 | 1617.8634 | 1612.6035 |
| 3.6554 | 1630.6195 | 1607.4541 | 1602.3127 |
| 3.6664 | 1615.1775 | 1597.0488 | 1592.0219 |
| 3.6774 | 1579.7434 | 1586.6472 | 1581.7311 |
| 3.6884 | 1577.6416 | 1576.5462 | 1571.4403 |
| 3.6994 | 1536.0374 | 1566.6461 | 1561.9408 |
| 3.7104 | 1569.0148 | 1557.0462 | 1552.4413 |
| 3.7214 | 1571.1652 | 1547.4495 | 1542.9418 |
| 3.7324 | 1544.9685 | 1537.8559 | 1533.4423 |
| 3.7434 | 1550.5359 | 1528.2652 | 1523.9429 |
| 3.7544 | 1507.1032 | 1518.6772 | 1514.4434 |
| 3.7654 | 1552.3619 | 1509.0920 | 1504.9439 |
| 3.7764 | 1515.8245 | 1499.5093 | 1495.4444 |
| 3.7874 | 1467.4248 | 1489.9291 | 1485.9449 |
| 3.7984 | 1448.0792 | 1480.3513 | 1476.4454 |
| 3.8094 | 1470.2606 | 1470.7757 | 1466.9459 |
| 3.8204 | 1423.3835 | 1461.2024 | 1457.4464 |
| 3.8314 | 1402.2016 | 1451.6311 | 1447.9470 |
| 3.8424 | 1412.0502 | 1442.0619 | 1438.4475 |
| 3.8534 | 1499.3009 | 1432.4947 | 1428.9480 |
| 3.8644 | 1441.3687 | 1422.9293 | 1419.4485 |
| 3.8754 | 1384.0315 | 1414.7107 | 1409.9490 |
| 3.8864 | 1367.9690 | 1407.3879 | 1404.0334 |
| 3.8974 | 1405.2812 | 1401.4117 | 1398.1178 |
| 3.9084 | 1425.4007 | 1395.4371 | 1392.2022 |
| 3.9194 | 1437.5634 | 1389.4641 | 1386.2866 |
| 3.9304 | 1400.6421 | 1383.4926 | 1380.3711 |
| 3.9414 | 1353.2232 | 1377.5226 | 1374.4555 |
| 3.9524 | 1376.4897 | 1371.5539 | 1368.5399 |
| 3.9634 | 1358.4975 | 1365.5867 | 1362.6243 |
| 3.9744 | 1352.4002 | 1359.6207 | 1356.7087 |
| 3.9854 | 1351.0265 | 1353.6560 | 1350.7931 |
| 3.9964 | 1347.4145 | 1347.6926 | 1344.8775 |
| 4.0074 | 1368.9715 | 1341.7303 | 1338.9619 |
| 4.0184 | 1356.9971 | 1335.7692 | 1333.0463 |
| 4.0294 | 1353.4612 | 1329.8092 | 1327.1307 |
| 4.0404 | 1344.5846 | 1323.8503 | 1321.2151 |
| 4.0514 | 1355.1209 | 1317.8924 | 1315.2996 |
| 4.0624 | 1337.9946 | 1311.8736 | 1309.3840 |
| 4.0734 | 1368.5319 | 1305.8146 | 1303.3033 |
| 4.0844 | 1335.8761 | 1299.6945 | 1297.2226 |
| 4.0954 | 1322.5408 | 1293.5754 | 1291.1419 |
| 4.1064 | 1278.6096 | 1287.4572 | 1285.0612 |
| 4.1174 | 1262.6844 | 1281.3398 | 1278.9806 |
| 4.1284 | 1261.7026 | 1275.2233 | 1272.8999 |
| 4.1394 | 1300.3845 | 1269.1075 | 1266.8192 |
| 4.1504 | 1293.0649 | 1262.9926 | 1260.7385 |
| 4.1614 | 1290.4081 | 1256.8784 | 1254.6578 |
| 4.1724 | 1274.0850 | 1250.7650 | 1248.5771 |
| 4.1834 | 1202.6460 | 1244.6523 | 1242.4965 |
| 4.1944 | 1186.6337 | 1238.5403 | 1236.4158 |

Scan List

| Vis. | Dataset Name | Start pos. [°2θ] | End pos. [°2θ] | Step [°2θ] | Meas.Date/Time |
| --- | --- | --- | --- | --- | --- |
| * | 13 550c | 2.0054 | 29.9894 | 0.0110 | 4/25/2024 3:40:31 PM |

Peak List

| Pos. [°2θ] | Height [cts] | FWHM Left [°2θ] | d-spacing [Å] | Rel. Int. [%] |
| --- | --- | --- | --- | --- |
| 2.6880 | 1485.23 | 0.1515 | 32.84180 | 90.48 |
| 8.6819 | 1641.59 | 0.0974 | 10.17679 | 100.00 |
| 10.4824 | 22.09 | 0.5196 | 8.43251 | 1.35 |
| 13.5429 | 50.76 | 0.1299 | 6.53299 | 3.09 |
| 15.7835 | 507.95 | 0.1948 | 5.61024 | 30.94 |
| 17.6127 | 141.12 | 0.2165 | 5.03151 | 8.60 |
| 18.2416 | 46.48 | 0.2598 | 4.85941 | 2.83 |
| 19.6150 | 40.56 | 0.3464 | 4.52217 | 2.47 |
| 22.3987 | 27.38 | 0.2165 | 3.96604 | 1.67 |
| 23.4028 | 35.19 | 0.2598 | 3.79810 | 2.14 |
| 25.9271 | 281.16 | 0.1299 | 3.43376 | 17.13 |
| 26.6867 | 427.93 | 0.1515 | 3.33772 | 26.07 |
| 27.4370 | 496.79 | 0.1948 | 3.24813 | 30.26 |

Pattern List

| Visible | Ref.Code | Score | Compound Name | Chem. Formula | Mineral Name | SemiQuant[%] |
| --- | --- | --- | --- | --- | --- | --- |
| * | 01-072-4625 | 60 | Sodium Aluminum Silicate Hydrate | Na Al ( Si2 O6 ) ( H2 O ) | Analcime | 7 |
| * | 04-015-3139 | 54 | Titanium Antimony Vanadium Oxide | Ti0.917 V0.041 W0.005 Sb0.033 O2 | Rutile | 5 |
| * | 04-017-4317 | 39 | Potassium Magnesium Manganese Iron Aluminum Silicate Hydroxide | K Mg0.2 Mn0.1 Fe2.4 Al1.7 Si2.6 O10 ( O H )2 | Biotite-1M | 16 |
| * | 00-042-1339 | 30 | Potassium Magnesium Aluminum Silicate Hydroxide | K Mg3 ( Si3 Al ) O10 ( O H )2 | Phlogopite-2M1 | 21 |
| * | 01-076-1239 | 20 | Potassium Aluminum Silicate | K ( Al Si3 O8 ) | Microcline | 17 |
| * | 01-076-2756 | 11 | Potassium Sodium Aluminum Silicate | ( K0.8 Na0.2 ) ( Al Si3 O8 ) | Sanidine | 4 |
| * | 04-025-4215 | 25 | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide | Mg10.4 V0.36 Mn33.5 Fe0.14 Al0.69 Si6.77 As6.5 P0.3 O54 ( O H )42 | Carlfrancisite | 19 |
| * | 01-081-8598 | 16 | Magnesium Aluminum Silicon Oxide Hydroxide Hydrate | ( Mg2 Al2 ) Si8 O20 ( H2 O )4 ( O H )2 ( H2 O )3.84 | Palygorskite-M | 10 |

Anchor Scan Parameters

Dataset Name	13 550c

File name	C:\aeris_data\XRD data\Goldstein\Etosha 2023\Etosha Clay Data\REP 13\13 550c.xrdml

Sample Identification	13 550c

Measurement Start Date/Time	4/25/2024 3:40:31 PM

Operator	Instrument

Raw Data Origin	XRD measurement (*.XRDML)

Scan Axis	Gonio

Start Position [°2θ]	2.0054

End Position [°2θ]	29.9894

Step Size [°2θ]	0.0110

Scan Step Time [s]	48.1950

Scan Type	Continuous

PSD Mode	Scanning

PSD Length [°2θ]	5.54

Offset [°2θ]	0.0000

Divergence Slit Type	Fixed

Divergence Slit Size [°]	0.0603

Specimen Length [mm]	10.00

Measurement Temperature [°C]	25.00

Anode Material	Cu

K-α1 [Å]	1.54060

K-α2 [Å]	1.54443

K-β1 [Å]	1.39225

K-A2 / K-A1 Ratio	0.50000

Generator Settings	15 mA, 40 kV

Diffractometer Type	2082464

Diffractometer Number	0

Goniometer Radius [mm]	145.00

Dist. Focus-Diverg. Slit [mm]	95.00

Incident Beam Monochromator	No

Spinning	Yes