13R Etosha 22 sub 0.1-10 cm S2 GLYCOL

Graphics

Graphics

Graphics

Quantitative Results

Phase Titanium Antimony Vanadium Oxide

Weight fraction/ %	4.0

Phase Potassium Magnesium Iron Silicate Oxide Hydroxide

Weight fraction/ %	33.0

Phase Magnesium Aluminum Silicon Oxide Hydroxide Hydrate

Weight fraction/ %	7.0

Phase Potassium Manganese Silicate Hydroxide Hydrate

Weight fraction/ %	3.0

Phase Sodium Aluminum Silicate Hydrate

Weight fraction/ %	11.0

Phase Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide

Weight fraction/ %	30.0

Phase Potassium Sodium Magnesium Aluminum Iron Silicon Titanium Oxide Fluoride Hydroxide

Weight fraction/ %	13.0

Multiple Quantitative Results

Scans vs Phases Matrix

| Scan name | Titanium Antimony Vanadium Oxide | Potassium Magnesium Iron Silicate Oxide Hydroxide | Magnesium Aluminum Silicon Oxide Hydroxide Hydrate | Potassium Manganese Silicate Hydroxide Hydrate | Sodium Aluminum Silicate Hydrate | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide | Potassium Sodium Magnesium Aluminum Iron Silicon Titanium Oxide Fluoride Hydroxide |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 13 glycol | 4.0 | 33.0 | 7.0 | 3.0 | 11.0 | 30.0 | 13.0 |

Anchor Scan Data

| Pos. [°2θ] | Iobs [cts] | Icalc [cts] | Iback [cts] |
| --- | --- | --- | --- |
| 2.0054 | 7067.0000 | 7632.7776 | 7067.0000 |
| 2.0164 | 7353.8658 | 7737.0924 | 7016.4664 |
| 2.0274 | 7101.0413 | 7803.9169 | 6965.9328 |
| 2.0384 | 7064.7330 | 7860.8037 | 6915.3992 |
| 2.0494 | 7118.3579 | 7893.2491 | 6864.8656 |
| 2.0604 | 7271.7035 | 7886.6431 | 6814.3320 |
| 2.0714 | 7130.1032 | 7831.9231 | 6763.7984 |
| 2.0824 | 6938.5261 | 7730.1572 | 6713.2648 |
| 2.0934 | 6890.3117 | 7591.9550 | 6662.7312 |
| 2.1044 | 6885.5487 | 7432.2868 | 6612.1976 |
| 2.1154 | 6909.9223 | 7265.1615 | 6561.6640 |
| 2.1264 | 6975.9366 | 7101.0584 | 6511.1304 |
| 2.1374 | 6865.5044 | 6946.7150 | 6460.5968 |
| 2.1484 | 6914.1042 | 6805.8237 | 6410.0631 |
| 2.1594 | 6797.6303 | 6679.7977 | 6359.5295 |
| 2.1704 | 6690.7375 | 6568.4131 | 6308.9959 |
| 2.1814 | 6712.6824 | 6470.3557 | 6258.4623 |
| 2.1924 | 6763.5084 | 6383.6017 | 6207.9287 |
| 2.2034 | 6596.2035 | 6306.1743 | 6157.2685 |
| 2.2144 | 6396.5084 | 6235.8469 | 6106.6083 |
| 2.2254 | 6532.9430 | 6170.9183 | 6055.9480 |
| 2.2364 | 6485.5221 | 6109.9354 | 6005.2878 |
| 2.2474 | 6601.9843 | 6051.7952 | 5954.6275 |
| 2.2584 | 6588.2379 | 5995.7035 | 5903.9673 |
| 2.2694 | 6404.5546 | 5941.1124 | 5853.3070 |
| 2.2804 | 6450.5039 | 5887.6570 | 5802.6468 |
| 2.2914 | 6508.0000 | 5835.0999 | 5751.9866 |
| 2.3024 | 6501.6947 | 5783.2900 | 5701.3263 |
| 2.3134 | 6425.6765 | 5732.1323 | 5650.6661 |
| 2.3244 | 6342.4263 | 5681.5695 | 5600.0058 |
| 2.3354 | 6327.7728 | 5631.5701 | 5549.3456 |
| 2.3464 | 6229.2935 | 5582.1225 | 5498.6854 |
| 2.3574 | 6304.2930 | 5533.2323 | 5448.0251 |
| 2.3684 | 6271.4115 | 5484.9228 | 5397.3649 |
| 2.3794 | 6173.8967 | 5437.2377 | 5346.7046 |
| 2.3904 | 6153.8225 | 5390.2462 | 5296.0444 |
| 2.4014 | 6162.3540 | 5344.0512 | 5245.3841 |
| 2.4124 | 6122.2714 | 5298.8006 | 5194.7239 |
| 2.4234 | 6065.2881 | 5254.7030 | 5144.0637 |
| 2.4344 | 5992.4956 | 5212.0466 | 5093.4034 |
| 2.4454 | 5968.6922 | 5171.2229 | 5042.7432 |
| 2.4564 | 5995.2989 | 5132.7516 | 4992.0829 |
| 2.4674 | 6018.0295 | 5097.3064 | 4941.4227 |
| 2.4784 | 5978.1027 | 5065.7359 | 4890.7625 |
| 2.4894 | 5953.9184 | 5039.0759 | 4840.1022 |
| 2.5004 | 5953.0000 | 5018.5454 | 4789.4420 |
| 2.5114 | 5891.9380 | 5005.5197 | 4738.7817 |
| 2.5224 | 5784.9213 | 5001.4755 | 4688.1215 |
| 2.5334 | 5726.2507 | 5007.9021 | 4637.4612 |
| 2.5444 | 5727.4430 | 5026.1804 | 4586.8010 |
| 2.5554 | 5705.5015 | 5057.4309 | 4536.1408 |
| 2.5664 | 5695.1490 | 5102.2405 | 4485.4805 |
| 2.5774 | 5745.3786 | 5160.8269 | 4434.6936 |
| 2.5884 | 5736.4744 | 5232.2341 | 4383.9068 |
| 2.5994 | 5690.1239 | 5314.6859 | 4333.1199 |
| 2.6104 | 5665.8599 | 5404.9464 | 4282.3330 |
| 2.6214 | 5581.1573 | 5498.0926 | 4231.5461 |
| 2.6324 | 5617.8614 | 5587.2053 | 4180.7592 |
| 2.6434 | 5589.1180 | 5663.2772 | 4129.9724 |
| 2.6544 | 5577.3279 | 5715.7198 | 4079.1855 |
| 2.6654 | 5521.5280 | 5733.8609 | 4028.3986 |
| 2.6764 | 5426.5241 | 5709.3906 | 3977.6117 |
| 2.6874 | 5264.0698 | 5638.8645 | 3926.8249 |
| 2.6984 | 5170.6681 | 5524.8758 | 3876.0380 |
| 2.7094 | 5112.7355 | 5375.1419 | 3825.2511 |
| 2.7204 | 4914.8520 | 5200.1158 | 3774.4642 |
| 2.7314 | 4739.8289 | 5010.4829 | 3723.6773 |
| 2.7424 | 4648.2375 | 4815.5218 | 3672.8905 |
| 2.7534 | 4610.7620 | 4622.3492 | 3622.1036 |
| 2.7644 | 4351.5752 | 4436.3849 | 3571.1602 |
| 2.7754 | 4176.0836 | 4260.9052 | 3520.2168 |
| 2.7864 | 4019.7370 | 4098.0995 | 3469.2733 |
| 2.7974 | 3796.4601 | 3948.9126 | 3418.3299 |
| 2.8084 | 3860.6219 | 3813.4093 | 3367.3865 |
| 2.8194 | 3639.0678 | 3690.9899 | 3316.4431 |
| 2.8304 | 3565.2994 | 3580.5887 | 3265.4997 |
| 2.8414 | 3362.9665 | 3480.8528 | 3214.5563 |
| 2.8524 | 3316.8220 | 3390.2986 | 3163.6129 |
| 2.8634 | 3156.8141 | 3307.4381 | 3112.6695 |
| 2.8744 | 3034.4518 | 3230.8718 | 3061.7260 |
| 2.8854 | 3115.5625 | 3159.3495 | 3010.7826 |
| 2.8964 | 2920.8717 | 3091.8006 | 2959.8392 |
| 2.9074 | 2929.9213 | 3027.3410 | 2908.8958 |
| 2.9184 | 2917.6013 | 2965.2637 | 2857.9524 |
| 2.9294 | 2799.3127 | 2905.0175 | 2807.0090 |
| 2.9404 | 2747.9710 | 2861.6715 | 2756.0656 |
| 2.9514 | 2719.4415 | 2808.6261 | 2725.3026 |
| 2.9624 | 2608.9203 | 2771.9337 | 2694.5397 |
| 2.9734 | 2577.7355 | 2735.9342 | 2663.7768 |
| 2.9844 | 2539.8732 | 2700.5008 | 2633.0139 |
| 2.9954 | 2520.0796 | 2665.5390 | 2602.2509 |
| 3.0064 | 2439.9051 | 2630.9771 | 2571.4880 |
| 3.0174 | 2411.8083 | 2596.7594 | 2540.7251 |
| 3.0284 | 2470.7050 | 2562.8419 | 2509.9622 |
| 3.0394 | 2423.6785 | 2529.1887 | 2479.1992 |
| 3.0504 | 2379.3707 | 2495.7700 | 2448.4363 |
| 3.0614 | 2382.9292 | 2462.5606 | 2417.6734 |
| 3.0724 | 2264.8038 | 2429.5389 | 2386.9104 |
| 3.0834 | 2292.5015 | 2396.6863 | 2356.1475 |
| 3.0944 | 2242.8186 | 2363.9861 | 2325.3846 |
| 3.1054 | 2250.2507 | 2331.4242 | 2294.6217 |
| 3.1164 | 2236.1721 | 2298.9877 | 2263.8587 |
| 3.1274 | 2217.4484 | 2274.1223 | 2233.0958 |
| 3.1384 | 2222.9587 | 2244.1629 | 2212.0490 |
| 3.1494 | 2263.9390 | 2221.7557 | 2191.0022 |
| 3.1604 | 2244.3776 | 2199.4355 | 2169.9554 |
| 3.1714 | 2201.4631 | 2177.1950 | 2148.9086 |
| 3.1824 | 2160.7517 | 2155.0279 | 2127.8618 |
| 3.1934 | 2101.1239 | 2132.9282 | 2106.8150 |
| 3.2044 | 2014.0575 | 2110.8907 | 2085.7682 |
| 3.2154 | 2029.1524 | 2088.9106 | 2064.7214 |
| 3.2264 | 2048.5501 | 2066.9836 | 2043.6746 |
| 3.2374 | 2060.5320 | 2045.1058 | 2022.6278 |
| 3.2484 | 2034.1111 | 2023.2736 | 2001.5811 |
| 3.2594 | 1971.7965 | 2001.4837 | 1980.5343 |
| 3.2704 | 1998.5295 | 1979.7332 | 1959.4875 |
| 3.2814 | 1985.3540 | 1958.0193 | 1938.4407 |
| 3.2924 | 1913.8761 | 1936.3397 | 1917.3939 |
| 3.3034 | 1897.4366 | 1914.6919 | 1896.3471 |
| 3.3144 | 1867.2099 | 1898.4297 | 1875.3003 |
| 3.3254 | 1862.2242 | 1878.4621 | 1861.2316 |
| 3.3364 | 1852.8963 | 1863.8764 | 1847.1629 |
| 3.3474 | 1820.0167 | 1849.3151 | 1833.0943 |
| 3.3584 | 1817.8422 | 1834.3144 | 1819.0256 |
| 3.3694 | 1843.0059 | 1819.1469 | 1804.9569 |
| 3.3804 | 1809.5531 | 1804.4563 | 1790.8882 |
| 3.3914 | 1790.6549 | 1790.0007 | 1776.8196 |
| 3.4024 | 1748.2207 | 1775.5626 | 1762.7509 |
| 3.4134 | 1805.6126 | 1761.1410 | 1748.6822 |
| 3.4244 | 1757.2787 | 1746.7350 | 1734.6136 |
| 3.4354 | 1658.2389 | 1732.3437 | 1720.5449 |
| 3.4464 | 1683.3368 | 1717.9662 | 1706.4762 |
| 3.4574 | 1699.6431 | 1703.6019 | 1692.4075 |
| 3.4684 | 1688.7488 | 1689.2501 | 1678.3389 |
| 3.4794 | 1662.6490 | 1674.9100 | 1664.2702 |
| 3.4904 | 1653.6372 | 1660.5811 | 1650.2015 |
| 3.5014 | 1630.8230 | 1647.5650 | 1636.1328 |
| 3.5124 | 1629.2581 | 1633.6512 | 1623.7610 |
| 3.5234 | 1606.1534 | 1621.0493 | 1611.3891 |
| 3.5344 | 1587.6239 | 1608.4565 | 1599.0172 |
| 3.5454 | 1596.5320 | 1595.8722 | 1586.6453 |
| 3.5564 | 1603.9322 | 1583.2963 | 1574.2734 |
| 3.5674 | 1590.8387 | 1570.7282 | 1561.9015 |
| 3.5784 | 1602.6677 | 1558.1675 | 1549.5296 |
| 3.5894 | 1551.7964 | 1545.6140 | 1537.1577 |
| 3.6004 | 1507.6229 | 1533.0673 | 1524.7858 |
| 3.6114 | 1482.5211 | 1520.5271 | 1512.4139 |
| 3.6224 | 1523.9867 | 1507.9932 | 1500.0420 |
| 3.6334 | 1480.1219 | 1495.4652 | 1487.6701 |
| 3.6444 | 1468.8314 | 1482.9429 | 1475.2982 |
| 3.6554 | 1479.1239 | 1470.4261 | 1462.9263 |
| 3.6664 | 1467.3048 | 1457.9145 | 1450.5544 |
| 3.6774 | 1437.2163 | 1445.4079 | 1438.1825 |
| 3.6884 | 1448.8496 | 1435.5471 | 1425.8106 |
| 3.6994 | 1389.3953 | 1423.8500 | 1416.8797 |
| 3.7104 | 1373.8540 | 1414.7984 | 1407.9489 |
| 3.7214 | 1363.8260 | 1405.7510 | 1399.0180 |
| 3.7324 | 1362.0703 | 1396.7077 | 1390.0872 |
| 3.7434 | 1340.3343 | 1387.6684 | 1381.1563 |
| 3.7544 | 1389.5767 | 1378.6330 | 1372.2255 |
| 3.7654 | 1389.1003 | 1369.6012 | 1363.2946 |
| 3.7764 | 1361.5919 | 1360.5729 | 1354.3638 |
| 3.7874 | 1353.0708 | 1351.5481 | 1345.4329 |
| 3.7984 | 1385.7143 | 1342.5265 | 1336.5021 |
| 3.8094 | 1302.8584 | 1333.5082 | 1327.5712 |
| 3.8204 | 1294.6726 | 1324.4929 | 1318.6404 |
| 3.8314 | 1316.7906 | 1315.4807 | 1309.7095 |
| 3.8424 | 1290.7881 | 1306.5900 | 1300.7787 |
| 3.8534 | 1338.5339 | 1297.8083 | 1291.8478 |
| 3.8644 | 1297.6740 | 1288.8665 | 1282.9170 |
| 3.8754 | 1238.2055 | 1281.0363 | 1273.9861 |
| 3.8864 | 1276.6239 | 1272.3518 | 1266.4212 |
| 3.8974 | 1239.1406 | 1264.7254 | 1258.8562 |
| 3.9084 | 1246.2311 | 1257.1015 | 1251.2913 |
| 3.9194 | 1231.7817 | 1249.4801 | 1243.7263 |
| 3.9304 | 1218.0000 | 1241.8609 | 1236.1614 |
| 3.9414 | 1212.9400 | 1234.2441 | 1228.5964 |
| 3.9524 | 1187.8776 | 1226.6295 | 1221.0315 |
| 3.9634 | 1190.4975 | 1219.0171 | 1213.4665 |
| 3.9744 | 1183.7999 | 1211.4068 | 1205.9016 |
| 3.9854 | 1170.0442 | 1203.7986 | 1198.3367 |
| 3.9964 | 1123.3481 | 1196.1924 | 1190.7717 |
| 4.0074 | 1121.3648 | 1188.5883 | 1183.2068 |
| 4.0184 | 1116.2021 | 1180.9862 | 1175.6418 |
| 4.0294 | 1184.3550 | 1173.3860 | 1168.0769 |
| 4.0404 | 1206.6863 | 1165.7877 | 1160.5119 |
| 4.0514 | 1135.3068 | 1158.1912 | 1152.9470 |
| 4.0624 | 1165.9267 | 1150.5967 | 1145.3820 |
| 4.0734 | 1148.0964 | 1143.0040 | 1137.8171 |
| 4.0844 | 1119.1725 | 1135.4131 | 1130.2521 |
| 4.0954 | 1107.1239 | 1127.8239 | 1122.6872 |
| 4.1064 | 1121.1927 | 1120.2366 | 1115.1222 |
| 4.1174 | 1070.4395 | 1112.6510 | 1107.5573 |
| 4.1284 | 1072.2557 | 1105.0672 | 1099.9923 |
| 4.1394 | 1068.3087 | 1097.4851 | 1092.4274 |
| 4.1504 | 1050.1136 | 1089.9047 | 1084.8624 |
| 4.1614 | 1037.9990 | 1082.3260 | 1077.2975 |
| 4.1724 | 1068.6962 | 1074.7491 | 1069.7325 |
| 4.1834 | 1057.8761 | 1067.1739 | 1062.1676 |
| 4.1944 | 1013.7837 | 1059.6003 | 1054.6026 |

Scan List

| Vis. | Dataset Name | Start pos. [°2θ] | End pos. [°2θ] | Step [°2θ] | Meas.Date/Time |
| --- | --- | --- | --- | --- | --- |
| * | 13 glycol | 2.0054 | 29.9894 | 0.0110 | 4/24/2024 2:00:12 PM |

Peak List

| Pos. [°2θ] | Height [cts] | FWHM Left [°2θ] | d-spacing [Å] | Rel. Int. [%] |
| --- | --- | --- | --- | --- |
| 2.0632 | 951.61 | 0.1299 | 42.78595 | 61.64 |
| 2.6751 | 1543.86 | 0.1732 | 32.99994 | 100.00 |
| 5.3227 | 53.56 | 0.5196 | 16.58951 | 3.47 |
| 6.8771 | 363.91 | 0.3031 | 12.84308 | 23.57 |
| 8.6276 | 590.92 | 0.2381 | 10.24072 | 38.28 |
| 15.6722 | 598.19 | 0.1082 | 5.64985 | 38.75 |
| 17.5396 | 72.76 | 0.2598 | 5.05230 | 4.71 |
| 18.1781 | 84.93 | 0.1082 | 4.87625 | 5.50 |
| 19.5238 | 33.53 | 0.6927 | 4.54308 | 2.17 |
| 22.3674 | 45.56 | 0.2598 | 3.97154 | 2.95 |
| 24.1036 | 50.13 | 0.1299 | 3.68924 | 3.25 |
| 25.8344 | 473.51 | 0.0758 | 3.44587 | 30.67 |
| 26.6366 | 296.27 | 0.1299 | 3.34389 | 19.19 |
| 27.4579 | 265.56 | 0.1299 | 3.24570 | 17.20 |

Pattern List

| Visible | Ref.Code | Score | Compound Name | Chem. Formula | Mineral Name | SemiQuant[%] |
| --- | --- | --- | --- | --- | --- | --- |
| * | 04-015-3139 | 46 | Titanium Antimony Vanadium Oxide | Ti0.917 V0.041 W0.005 Sb0.033 O2 | Rutile | 4 |
| * | 01-082-2699 | 40 | Potassium Magnesium Iron Silicate Oxide Hydroxide | K ( Mg2.40 Fe0.60 ) ( Si2 O5 )2 ( O0.72 ( O H )1.28 ) | Phlogopite-2M1 | 33 |
| * | 01-081-8598 | 36 | Magnesium Aluminum Silicon Oxide Hydroxide Hydrate | ( Mg2 Al2 ) Si8 O20 ( H2 O )4 ( O H )2 ( H2 O )3.84 | Palygorskite-M | 7 |
| * | 01-089-6415 | 30 | Potassium Manganese Silicate Hydroxide Hydrate | K3.68 Mn15.904 Si25.472 O64 ( O H )9.376 ( H2 O )7.024 | Ganophyllite | 3 |
| * | 04-011-6756 | 16 | Sodium Aluminum Silicate Hydrate | Na8 Al8 Si16 O48 ( H2 O )8 | Analcime | 11 |
| * | 04-025-4215 | 31 | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide | Mg10.4 V0.36 Mn33.5 Fe0.14 Al0.69 Si6.77 As6.5 P0.3 O54 ( O H )42 | Carlfrancisite | 30 |
| * | 04-015-8229 | 37 | Potassium Sodium Magnesium Aluminum Iron Silicon Titanium Oxide Fluoride Hydroxide | K0.81 Na0.04 Mg0.92 Ti0.1 Fe1.41 Al1.77 Si2.7 O10.18 ( O H )1.73 F0.09 | Biotite-1M | 13 |

Anchor Scan Parameters

Dataset Name	13 glycol

File name	C:\aeris_data\XRD data\Goldstein\Etosha 2023\Etosha Clay Data\REP 13\13 glycol.xrdml

Sample Identification	13 glycol

Measurement Start Date/Time	4/24/2024 2:00:12 PM

Operator	Instrument

Raw Data Origin	XRD measurement (*.XRDML)

Scan Axis	Gonio

Start Position [°2θ]	2.0054

End Position [°2θ]	29.9894

Step Size [°2θ]	0.0110

Scan Step Time [s]	48.1950

Scan Type	Continuous

PSD Mode	Scanning

PSD Length [°2θ]	5.54

Offset [°2θ]	0.0000

Divergence Slit Type	Fixed

Divergence Slit Size [°]	0.0603

Specimen Length [mm]	10.00

Measurement Temperature [°C]	25.00

Anode Material	Cu

K-α1 [Å]	1.54060

K-α2 [Å]	1.54443

K-β1 [Å]	1.39225

K-A2 / K-A1 Ratio	0.50000

Generator Settings	15 mA, 40 kV

Diffractometer Type	2082464

Diffractometer Number	0

Goniometer Radius [mm]	145.00

Dist. Focus-Diverg. Slit [mm]	95.00

Incident Beam Monochromator	No

Spinning	Yes