13R Etosha 22 sub 0.1-10 cm S2 regular

Graphics

Graphics

Graphics

Quantitative Results

Phase Titanium Oxide

Weight fraction/ %	4.0

Phase Potassium Calcium Manganese Aluminum Silicate Hydroxide Hydrate

Weight fraction/ %	3.0

Phase Potassium Magnesium Manganese Iron Aluminum Silicate Hydroxide

Weight fraction/ %	7.0

Phase Sodium Aluminum Silicate Hydrate

Weight fraction/ %	4.0

Phase Potassium Magnesium Aluminum Silicate Fluoride Hydroxide

Weight fraction/ %	24.0

Phase Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide

Weight fraction/ %	21.0

Phase Potassium Sodium Aluminum Silicate

Weight fraction/ %	10.0

Phase Potassium Aluminum Silicate

Weight fraction/ %	21.0

Phase Magnesium Aluminum Silicon Oxide Hydroxide Hydrate

Weight fraction/ %	6.0

Multiple Quantitative Results

Scans vs Phases Matrix

| Scan name | Titanium Oxide | Potassium Calcium Manganese Aluminum Silicate Hydroxide Hydrate | Potassium Magnesium Manganese Iron Aluminum Silicate Hydroxide | Sodium Aluminum Silicate Hydrate | Potassium Magnesium Aluminum Silicate Fluoride Hydroxide | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide | Potassium Sodium Aluminum Silicate | Potassium Aluminum Silicate | Magnesium Aluminum Silicon Oxide Hydroxide Hydrate |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 13 reg | 4.0 | 3.0 | 7.0 | 4.0 | 24.0 | 21.0 | 10.0 | 21.0 | 6.0 |

Anchor Scan Data

| Pos. [°2θ] | Iobs [cts] | Icalc [cts] | Iback [cts] |
| --- | --- | --- | --- |
| 2.0054 | 7720.0000 | 8581.1117 | 7720.0000 |
| 2.0164 | 7732.0905 | 8596.3315 | 7664.0820 |
| 2.0274 | 7662.3432 | 8576.0299 | 7608.1640 |
| 2.0384 | 7787.9941 | 8546.2919 | 7552.2460 |
| 2.0494 | 7615.3736 | 8505.6856 | 7496.3280 |
| 2.0604 | 7800.3289 | 8453.3314 | 7440.4100 |
| 2.0714 | 7556.0590 | 8389.0455 | 7384.4920 |
| 2.0824 | 7488.1495 | 8313.3720 | 7328.5740 |
| 2.0934 | 7435.6362 | 8227.4920 | 7272.6560 |
| 2.1044 | 7530.4159 | 8133.0408 | 7216.7380 |
| 2.1154 | 7561.5969 | 8031.8874 | 7160.8200 |
| 2.1264 | 7424.5177 | 7925.9328 | 7104.9020 |
| 2.1374 | 7451.5664 | 7816.9592 | 7048.9840 |
| 2.1484 | 7313.1327 | 7706.5421 | 6993.0660 |
| 2.1594 | 7406.6106 | 7596.0133 | 6937.1480 |
| 2.1704 | 7342.2065 | 7486.4599 | 6881.2300 |
| 2.1814 | 7309.9872 | 7378.7425 | 6825.3120 |
| 2.1924 | 7266.0447 | 7273.4543 | 6769.3940 |
| 2.2034 | 7225.0885 | 7171.1464 | 6713.3426 |
| 2.2144 | 7122.8137 | 7072.0875 | 6657.2911 |
| 2.2254 | 7266.1770 | 6976.5499 | 6601.2397 |
| 2.2364 | 7149.6785 | 6884.6294 | 6545.1882 |
| 2.2474 | 7126.5211 | 6796.3294 | 6489.1367 |
| 2.2584 | 7043.1809 | 6711.5768 | 6433.0853 |
| 2.2694 | 7013.2094 | 6630.2376 | 6377.0338 |
| 2.2804 | 6839.4095 | 6552.1317 | 6320.9824 |
| 2.2914 | 6926.0000 | 6477.0464 | 6264.9309 |
| 2.3024 | 6864.9380 | 6404.7492 | 6208.8795 |
| 2.3134 | 6747.1622 | 6334.9993 | 6152.8280 |
| 2.3244 | 6821.1593 | 6267.5577 | 6096.7766 |
| 2.3354 | 6848.8731 | 6202.1954 | 6040.7251 |
| 2.3464 | 6696.0949 | 6138.7006 | 5984.6736 |
| 2.3574 | 6707.9459 | 6076.8846 | 5928.6222 |
| 2.3684 | 6693.6844 | 6016.5868 | 5872.5707 |
| 2.3794 | 6655.2979 | 5957.6787 | 5816.5193 |
| 2.3904 | 6716.7168 | 5900.0685 | 5760.4678 |
| 2.4014 | 6654.2832 | 5843.7060 | 5704.4164 |
| 2.4124 | 6483.7139 | 5788.5874 | 5648.3649 |
| 2.4234 | 6485.0954 | 5734.7632 | 5592.3134 |
| 2.4344 | 6502.9086 | 5682.3458 | 5536.2620 |
| 2.4454 | 6523.2645 | 5631.5194 | 5480.2105 |
| 2.4564 | 6534.2365 | 5582.5506 | 5424.1591 |
| 2.4674 | 6529.3923 | 5535.7992 | 5368.1076 |
| 2.4784 | 6397.4454 | 5491.7273 | 5312.0562 |
| 2.4894 | 6374.4366 | 5450.9050 | 5256.0047 |
| 2.5004 | 6369.9115 | 5414.0108 | 5199.9533 |
| 2.5114 | 6305.9194 | 5381.8229 | 5143.9018 |
| 2.5224 | 6265.3874 | 5355.1994 | 5087.8503 |
| 2.5334 | 6246.4189 | 5335.0462 | 5031.7989 |
| 2.5444 | 6190.9331 | 5322.2695 | 4975.7474 |
| 2.5554 | 6214.0590 | 5317.7150 | 4919.6960 |
| 2.5664 | 6281.8201 | 5322.0264 | 4863.6445 |
| 2.5774 | 6179.6775 | 5335.7600 | 4807.4596 |
| 2.5884 | 6121.1657 | 5359.0270 | 4751.2747 |
| 2.5994 | 6127.6549 | 5391.6574 | 4695.0898 |
| 2.6104 | 6173.6165 | 5432.8922 | 4638.9049 |
| 2.6214 | 6064.9115 | 5481.3267 | 4582.7200 |
| 2.6324 | 5916.3245 | 5534.7668 | 4526.5350 |
| 2.6434 | 5897.2478 | 5590.0675 | 4470.3501 |
| 2.6544 | 5868.7414 | 5642.9817 | 4414.1652 |
| 2.6654 | 5871.9617 | 5688.1038 | 4357.9803 |
| 2.6764 | 5678.5654 | 5719.0540 | 4301.7954 |
| 2.6874 | 5650.1023 | 5729.0753 | 4245.6105 |
| 2.6984 | 5458.3495 | 5712.1053 | 4189.4256 |
| 2.7094 | 5413.1593 | 5664.1046 | 4133.2406 |
| 2.7204 | 5246.0314 | 5584.1272 | 4077.0557 |
| 2.7314 | 5155.9498 | 5474.5944 | 4020.8708 |
| 2.7424 | 5019.0044 | 5340.6181 | 3964.6859 |
| 2.7534 | 4911.7640 | 5188.6549 | 3908.5010 |
| 2.7644 | 4661.9292 | 5025.4846 | 3852.1511 |
| 2.7754 | 4566.6568 | 4857.0132 | 3795.8012 |
| 2.7864 | 4442.8082 | 4688.2070 | 3739.4514 |
| 2.7974 | 4206.5309 | 4522.7937 | 3683.1015 |
| 2.8084 | 4120.5762 | 4363.4606 | 3626.7516 |
| 2.8194 | 3888.4346 | 4212.0180 | 3570.4017 |
| 2.8304 | 3814.3776 | 4069.5544 | 3514.0519 |
| 2.8414 | 3642.7925 | 3936.5704 | 3457.7020 |
| 2.8524 | 3662.2316 | 3813.0945 | 3401.3521 |
| 2.8634 | 3357.2153 | 3698.7875 | 3345.0022 |
| 2.8744 | 3435.2734 | 3593.0393 | 3288.6524 |
| 2.8854 | 3359.3373 | 3495.0580 | 3232.3025 |
| 2.8964 | 3275.3672 | 3403.9503 | 3175.9526 |
| 2.9074 | 3224.4572 | 3318.7899 | 3119.6027 |
| 2.9184 | 3152.4120 | 3238.6711 | 3063.2529 |
| 2.9294 | 2978.1947 | 3162.7496 | 3006.9030 |
| 2.9404 | 2981.0024 | 3107.1540 | 2950.5531 |
| 2.9514 | 2906.6204 | 3047.2684 | 2920.9056 |
| 2.9624 | 2740.8230 | 3006.4952 | 2891.2582 |
| 2.9734 | 2811.3284 | 2967.4906 | 2861.6107 |
| 2.9844 | 2729.1318 | 2929.8868 | 2831.9632 |
| 2.9954 | 2757.0000 | 2893.3931 | 2802.3158 |
| 3.0064 | 2660.2655 | 2857.7834 | 2772.6683 |
| 3.0174 | 2677.0914 | 2822.8838 | 2743.0209 |
| 3.0284 | 2592.7360 | 2788.5614 | 2713.3734 |
| 3.0394 | 2663.2891 | 2754.7148 | 2683.7259 |
| 3.0504 | 2560.9646 | 2721.2666 | 2654.0785 |
| 3.0614 | 2534.7788 | 2688.1571 | 2624.4310 |
| 3.0724 | 2547.0020 | 2655.3398 | 2594.7835 |
| 3.0834 | 2514.3422 | 2622.7777 | 2565.1361 |
| 3.0944 | 2468.3496 | 2590.4408 | 2535.4886 |
| 3.1054 | 2465.5418 | 2558.3045 | 2505.8411 |
| 3.1164 | 2473.4145 | 2526.3481 | 2476.1937 |
| 3.1274 | 2478.6460 | 2501.1801 | 2446.5462 |
| 3.1384 | 2393.7011 | 2473.3843 | 2427.3765 |
| 3.1494 | 2382.8791 | 2452.3483 | 2408.2067 |
| 3.1604 | 2418.3289 | 2431.4340 | 2389.0370 |
| 3.1714 | 2325.8574 | 2410.6310 | 2369.8672 |
| 3.1824 | 2283.1214 | 2389.9300 | 2350.6975 |
| 3.1934 | 2293.1770 | 2369.3225 | 2331.5278 |
| 3.2044 | 2356.4739 | 2348.8012 | 2312.3580 |
| 3.2154 | 2357.6234 | 2328.3591 | 2293.1883 |
| 3.2264 | 2288.1902 | 2307.9903 | 2274.0185 |
| 3.2374 | 2209.2468 | 2287.6892 | 2254.8488 |
| 3.2484 | 2239.1111 | 2267.4507 | 2235.6791 |
| 3.2594 | 2267.1386 | 2247.2703 | 2216.5093 |
| 3.2704 | 2197.5472 | 2227.1438 | 2197.3396 |
| 3.2814 | 2154.4956 | 2207.0675 | 2178.1698 |
| 3.2924 | 2166.9336 | 2187.0379 | 2159.0001 |
| 3.3034 | 2147.6883 | 2167.0519 | 2139.8304 |
| 3.3144 | 2116.0462 | 2150.2614 | 2120.6606 |
| 3.3254 | 2096.2507 | 2132.1878 | 2106.4797 |
| 3.3364 | 2106.1037 | 2117.3048 | 2092.2988 |
| 3.3474 | 2106.5152 | 2102.4550 | 2078.1178 |
| 3.3584 | 2114.5428 | 2087.6365 | 2063.9369 |
| 3.3694 | 2091.4041 | 2072.8473 | 2049.7560 |
| 3.3804 | 2009.7714 | 2058.0856 | 2035.5750 |
| 3.3914 | 2012.3098 | 2043.3499 | 2021.3941 |
| 3.4024 | 2011.5860 | 2028.6385 | 2007.2132 |
| 3.4134 | 1974.9616 | 2013.9502 | 1993.0322 |
| 3.4244 | 2015.1859 | 1999.2836 | 1978.8513 |
| 3.4354 | 1972.8790 | 1984.6376 | 1964.6704 |
| 3.4464 | 1967.9799 | 1970.0109 | 1950.4894 |
| 3.4574 | 1955.6755 | 1955.4025 | 1936.3085 |
| 3.4684 | 1907.1504 | 1940.8115 | 1922.1276 |
| 3.4794 | 1881.7070 | 1926.2369 | 1907.9467 |
| 3.4904 | 1880.9336 | 1911.6780 | 1893.7657 |
| 3.5014 | 1871.2399 | 1899.6386 | 1879.5848 |
| 3.5124 | 1902.6131 | 1886.5644 | 1869.3646 |
| 3.5234 | 1858.0413 | 1876.0084 | 1859.1443 |
| 3.5344 | 1910.3471 | 1865.4651 | 1848.9241 |
| 3.5454 | 1860.1140 | 1854.9339 | 1838.7039 |
| 3.5564 | 1846.3260 | 1844.4143 | 1828.4837 |
| 3.5674 | 1802.3176 | 1833.9056 | 1818.2634 |
| 3.5784 | 1743.3309 | 1823.4074 | 1808.0432 |
| 3.5894 | 1793.1328 | 1812.9192 | 1797.8230 |
| 3.6004 | 1768.9788 | 1802.4406 | 1787.6027 |
| 3.6114 | 1786.3963 | 1791.9711 | 1777.3825 |
| 3.6224 | 1812.5561 | 1781.5103 | 1767.1623 |
| 3.6334 | 1739.1878 | 1771.0579 | 1756.9421 |
| 3.6444 | 1782.6898 | 1760.6135 | 1746.7218 |
| 3.6554 | 1749.4425 | 1750.1767 | 1736.5016 |
| 3.6664 | 1757.2630 | 1739.7473 | 1726.2814 |
| 3.6774 | 1696.6185 | 1729.3249 | 1716.0611 |
| 3.6884 | 1723.9823 | 1719.1694 | 1705.8409 |
| 3.6994 | 1675.4307 | 1708.9114 | 1696.0319 |
| 3.7104 | 1693.4381 | 1698.9197 | 1686.2228 |
| 3.7214 | 1704.2566 | 1688.9340 | 1676.4138 |
| 3.7324 | 1683.6170 | 1678.9541 | 1666.6048 |
| 3.7434 | 1667.8702 | 1668.9797 | 1656.7958 |
| 3.7544 | 1658.4115 | 1659.0106 | 1646.9867 |
| 3.7654 | 1636.7355 | 1649.0467 | 1637.1777 |
| 3.7764 | 1593.9090 | 1639.0877 | 1627.3687 |
| 3.7874 | 1574.1681 | 1629.1334 | 1617.5596 |
| 3.7984 | 1594.0585 | 1619.1838 | 1607.7506 |
| 3.8094 | 1611.3147 | 1609.2386 | 1597.9416 |
| 3.8204 | 1629.4026 | 1599.2977 | 1588.1325 |
| 3.8314 | 1575.5723 | 1589.3610 | 1578.3235 |
| 3.8424 | 1611.0010 | 1579.4282 | 1568.5145 |
| 3.8534 | 1572.8584 | 1569.4993 | 1558.7054 |
| 3.8644 | 1539.4528 | 1559.5741 | 1548.8964 |
| 3.8754 | 1514.6372 | 1550.8788 | 1539.0874 |
| 3.8864 | 1567.9292 | 1541.6735 | 1531.2173 |
| 3.8974 | 1527.4375 | 1533.6978 | 1523.3473 |
| 3.9084 | 1495.4115 | 1525.7254 | 1515.4773 |
| 3.9194 | 1528.8437 | 1517.7561 | 1507.6072 |
| 3.9304 | 1583.2080 | 1509.7900 | 1499.7372 |
| 3.9414 | 1538.6342 | 1501.8268 | 1491.8671 |
| 3.9524 | 1507.0531 | 1493.8666 | 1483.9971 |
| 3.9634 | 1502.4218 | 1485.9092 | 1476.1271 |
| 3.9744 | 1470.4046 | 1477.9544 | 1468.2570 |
| 3.9854 | 1488.4601 | 1470.0024 | 1460.3870 |
| 3.9964 | 1428.3574 | 1462.0529 | 1452.5169 |
| 4.0074 | 1449.9095 | 1454.1060 | 1444.6469 |
| 4.0184 | 1396.4572 | 1446.1615 | 1436.7769 |
| 4.0294 | 1435.0305 | 1438.2194 | 1428.9068 |
| 4.0404 | 1426.7507 | 1430.2795 | 1421.0368 |
| 4.0514 | 1425.9764 | 1422.3420 | 1413.1667 |
| 4.0624 | 1387.4921 | 1415.9929 | 1405.2967 |
| 4.0734 | 1393.4857 | 1408.9818 | 1399.9350 |
| 4.0844 | 1399.0000 | 1403.5590 | 1394.5733 |
| 4.0954 | 1383.2409 | 1398.1383 | 1389.2117 |
| 4.1064 | 1349.5669 | 1392.7195 | 1383.8500 |
| 4.1174 | 1371.6313 | 1387.3027 | 1378.4883 |
| 4.1284 | 1403.7409 | 1381.8878 | 1373.1266 |
| 4.1394 | 1368.0039 | 1376.4748 | 1367.7649 |
| 4.1504 | 1340.4941 | 1371.0636 | 1362.4033 |
| 4.1614 | 1325.8633 | 1365.6541 | 1357.0416 |
| 4.1724 | 1358.6510 | 1360.2464 | 1351.6799 |
| 4.1834 | 1371.5487 | 1354.8404 | 1346.3182 |
| 4.1944 | 1321.3928 | 1349.4360 | 1340.9566 |

Scan List

| Vis. | Dataset Name | Start pos. [°2θ] | End pos. [°2θ] | Step [°2θ] | Meas.Date/Time |
| --- | --- | --- | --- | --- | --- |
| * | 13 reg | 2.0054 | 29.9894 | 0.0110 | 4/24/2024 1:39:14 PM |

Peak List

| Pos. [°2θ] | Height [cts] | FWHM Left [°2θ] | d-spacing [Å] | Rel. Int. [%] |
| --- | --- | --- | --- | --- |
| 2.0560 | 888.65 | 0.2598 | 42.93555 | 65.80 |
| 2.7047 | 1350.45 | 0.1948 | 32.63883 | 100.00 |
| 7.1178 | 764.25 | 0.5196 | 12.40921 | 56.59 |
| 8.6838 | 809.37 | 0.0866 | 10.17457 | 59.93 |
| 13.2292 | 18.92 | 0.5196 | 6.68720 | 1.40 |
| 15.7208 | 646.30 | 0.1299 | 5.63248 | 47.86 |
| 17.6147 | 76.40 | 0.1299 | 5.03093 | 5.66 |
| 18.1865 | 99.69 | 0.0649 | 4.87402 | 7.38 |
| 19.5517 | 43.60 | 0.6061 | 4.53666 | 3.23 |
| 22.3793 | 62.76 | 0.0866 | 3.96945 | 4.65 |
| 23.3529 | 58.85 | 0.1299 | 3.80611 | 4.36 |
| 24.1769 | 36.05 | 0.1732 | 3.67822 | 2.67 |
| 25.8615 | 656.17 | 0.0758 | 3.44232 | 48.59 |
| 26.6437 | 358.24 | 0.1082 | 3.34301 | 26.53 |
| 27.4579 | 350.47 | 0.1515 | 3.24570 | 25.95 |

Pattern List

| Visible | Ref.Code | Score | Compound Name | Chem. Formula | Mineral Name | SemiQuant[%] |
| --- | --- | --- | --- | --- | --- | --- |
| * | 04-008-7810 | 53 | Titanium Oxide | Ti O2 | Rutile | 4 |
| * | 04-016-6876 | 43 | Potassium Calcium Manganese Aluminum Silicate Hydroxide Hydrate | K0.38 Ca0.12 Mn2 Al0.62 Si2.71 O8 ( O H )1.33 ( H2 O )1.75 | Ganophyllite | 3 |
| * | 04-017-4317 | 41 | Potassium Magnesium Manganese Iron Aluminum Silicate Hydroxide | K Mg0.2 Mn0.1 Fe2.4 Al1.7 Si2.6 O10 ( O H )2 | Biotite-1M | 7 |
| * | 04-011-6751 | 16 | Sodium Aluminum Silicate Hydrate | Na8 Al8 Si16 O48 ( H2 O )8 | Analcime | 4 |
| * | 04-013-9383 | 20 | Potassium Magnesium Aluminum Silicate Fluoride Hydroxide | K Mg3 Al Si3 O10 ( O H ) F | Phlogopite-2M1 | 24 |
| * | 04-025-4215 | 37 | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide | Mg10.4 V0.36 Mn33.5 Fe0.14 Al0.69 Si6.77 As6.5 P0.3 O54 ( O H )42 | Carlfrancisite | 21 |
| * | 01-076-2756 | 36 | Potassium Sodium Aluminum Silicate | ( K0.8 Na0.2 ) ( Al Si3 O8 ) | Sanidine | 10 |
| * | 01-076-1239 | 19 | Potassium Aluminum Silicate | K ( Al Si3 O8 ) | Microcline | 21 |
| * | 01-081-8598 | 27 | Magnesium Aluminum Silicon Oxide Hydroxide Hydrate | ( Mg2 Al2 ) Si8 O20 ( H2 O )4 ( O H )2 ( H2 O )3.84 | Palygorskite-M | 6 |

Anchor Scan Parameters

Dataset Name	13 reg

File name	C:\aeris_data\XRD data\Goldstein\Etosha 2023\Etosha Clay Data\REP 13\13 reg.xrdml

Sample Identification	13 reg

Measurement Start Date/Time	4/24/2024 1:39:14 PM

Operator	Instrument

Raw Data Origin	XRD measurement (*.XRDML)

Scan Axis	Gonio

Start Position [°2θ]	2.0054

End Position [°2θ]	29.9894

Step Size [°2θ]	0.0110

Scan Step Time [s]	48.1950

Scan Type	Continuous

PSD Mode	Scanning

PSD Length [°2θ]	5.54

Offset [°2θ]	0.0000

Divergence Slit Type	Fixed

Divergence Slit Size [°]	0.0603

Specimen Length [mm]	10.00

Measurement Temperature [°C]	25.00

Anode Material	Cu

K-α1 [Å]	1.54060

K-α2 [Å]	1.54443

K-β1 [Å]	1.39225

K-A2 / K-A1 Ratio	0.50000

Generator Settings	15 mA, 40 kV

Diffractometer Type	2082464

Diffractometer Number	0

Goniometer Radius [mm]	145.00

Dist. Focus-Diverg. Slit [mm]	95.00

Incident Beam Monochromator	No

Spinning	Yes