14 Etosha 22 CRT 0-0.1 cm S3  REGULAR report

Graphics

Graphics

Graphics

Quantitative Results

Phase Sodium Aluminum Silicate Hydrate

Weight fraction/ %	5.0

Phase Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide

Weight fraction/ %	47.0

Phase Potassium Sodium Magnesium Iron Silicon Oxide Hydroxide

Weight fraction/ %	11.0

Phase Magnesium Silicon Oxide Hydroxide Hydrate

Weight fraction/ %	7.0

Phase Potassium Calcium Manganese Aluminum Silicate Hydroxide Hydrate

Weight fraction/ %	11.0

Phase Magnesium Aluminum Silicate Hydroxide Hydrate

Weight fraction/ %	1.0

Phase Sodium Magnesium Silicon Oxide Hydrate

Weight fraction/ %	15.0

Phase Magnesium Aluminum Iron Silicon Oxide Hydroxide Hydrate

Weight fraction/ %	4.0

Multiple Quantitative Results

Scans vs Phases Matrix

| Scan name | Sodium Aluminum Silicate Hydrate | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide | Potassium Sodium Magnesium Iron Silicon Oxide Hydroxide | Magnesium Silicon Oxide Hydroxide Hydrate | Potassium Calcium Manganese Aluminum Silicate Hydroxide Hydrate | Magnesium Aluminum Silicate Hydroxide Hydrate | Sodium Magnesium Silicon Oxide Hydrate | Magnesium Aluminum Iron Silicon Oxide Hydroxide Hydrate |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 14 Etosha22 Crt 0-0.1cm S3 | 5.0 | 47.0 | 11.0 | 7.0 | 11.0 | 1.0 | 15.0 | 4.0 |

Anchor Scan Data

| Pos. [°2θ] | Iobs [cts] | Icalc [cts] | Iback [cts] |
| --- | --- | --- | --- |
| 2.0054 | 9691.0000 | 9685.0357 | 9691.0000 |
| 2.0164 | 9766.8402 | 9652.4433 | 9617.7328 |
| 2.0274 | 9745.1996 | 9580.1998 | 9544.4656 |
| 2.0384 | 9403.5590 | 9508.0040 | 9471.1984 |
| 2.0494 | 9586.1032 | 9435.8591 | 9397.9312 |
| 2.0604 | 9304.9444 | 9363.7682 | 9324.6640 |
| 2.0714 | 9406.2802 | 9291.7349 | 9251.3968 |
| 2.0824 | 9335.2989 | 9219.7629 | 9178.1296 |
| 2.0934 | 9230.6657 | 9147.8564 | 9104.8624 |
| 2.1044 | 9393.7434 | 9076.0198 | 9031.5952 |
| 2.1154 | 9234.4739 | 9004.2579 | 8958.3280 |
| 2.1264 | 9087.5944 | 8932.5761 | 8885.0608 |
| 2.1374 | 9079.1003 | 8860.9800 | 8811.7936 |
| 2.1484 | 9041.6445 | 8789.4761 | 8738.5265 |
| 2.1594 | 9048.2625 | 8718.0713 | 8665.2593 |
| 2.1704 | 9137.7139 | 8646.7732 | 8591.9921 |
| 2.1814 | 8990.0580 | 8575.5904 | 8518.7249 |
| 2.1924 | 8877.0747 | 8504.4438 | 8445.4577 |
| 2.2034 | 8858.2566 | 8433.4465 | 8372.0267 |
| 2.2144 | 8831.4671 | 8362.5083 | 8298.5957 |
| 2.2254 | 8769.0865 | 8291.7322 | 8225.1648 |
| 2.2364 | 8611.9749 | 8221.1345 | 8151.7338 |
| 2.2474 | 8679.3835 | 8150.7345 | 8078.3028 |
| 2.2584 | 8607.6234 | 8080.5550 | 8004.8719 |
| 2.2694 | 8726.8702 | 8010.6234 | 7931.4409 |
| 2.2804 | 8683.8142 | 7940.9729 | 7858.0099 |
| 2.2914 | 8609.3196 | 7871.6437 | 7784.5790 |
| 2.3024 | 8589.7566 | 7802.6853 | 7711.1480 |
| 2.3134 | 8586.8564 | 7734.1580 | 7637.7170 |
| 2.3244 | 8575.9493 | 7666.1362 | 7564.2861 |
| 2.3354 | 8377.6962 | 7598.7107 | 7490.8551 |
| 2.3464 | 8291.1898 | 7531.9923 | 7417.4241 |
| 2.3574 | 8313.7119 | 7466.1154 | 7343.9932 |
| 2.3684 | 8355.5664 | 7401.2417 | 7270.5622 |
| 2.3794 | 8284.7188 | 7337.5641 | 7197.1312 |
| 2.3904 | 8190.1396 | 7275.3105 | 7123.7003 |
| 2.4014 | 8161.5664 | 7214.7464 | 7050.2693 |
| 2.4124 | 8231.5969 | 7156.1778 | 6976.8383 |
| 2.4234 | 8237.8997 | 7099.9517 | 6903.4074 |
| 2.4344 | 8078.9911 | 7046.4555 | 6829.9764 |
| 2.4454 | 7964.0295 | 6996.1141 | 6756.5454 |
| 2.4564 | 7968.2591 | 6949.3844 | 6683.1145 |
| 2.4674 | 7981.9203 | 6906.7467 | 6609.6835 |
| 2.4784 | 7801.9395 | 6868.6932 | 6536.2525 |
| 2.4894 | 7807.8860 | 6835.7128 | 6462.8216 |
| 2.5004 | 7825.1814 | 6808.2727 | 6389.3906 |
| 2.5114 | 7814.4041 | 6786.7976 | 6315.9596 |
| 2.5224 | 7838.9125 | 6771.6455 | 6242.5287 |
| 2.5334 | 7826.5103 | 6763.0818 | 6169.0977 |
| 2.5444 | 7705.1612 | 6761.2514 | 6095.6667 |
| 2.5554 | 7685.7680 | 6766.1495 | 6022.2358 |
| 2.5664 | 7755.8496 | 6777.4617 | 5948.8048 |
| 2.5774 | 7609.1858 | 6795.0126 | 5875.2101 |
| 2.5884 | 7514.3486 | 6817.9287 | 5801.6153 |
| 2.5994 | 7538.5575 | 6845.3983 | 5728.0206 |
| 2.6104 | 7540.1839 | 6876.1424 | 5654.4259 |
| 2.6214 | 7546.0128 | 6908.4937 | 5580.8311 |
| 2.6324 | 7347.1283 | 6940.3492 | 5507.2364 |
| 2.6434 | 7271.4061 | 6969.1386 | 5433.6417 |
| 2.6544 | 7225.9631 | 6991.8312 | 5360.0469 |
| 2.6654 | 7178.2389 | 7005.0139 | 5286.4522 |
| 2.6764 | 7021.0482 | 7005.0692 | 5212.8574 |
| 2.6874 | 6885.1268 | 6988.4699 | 5139.2627 |
| 2.6984 | 6822.3805 | 6952.1671 | 5065.6680 |
| 2.7094 | 6540.6135 | 6894.0039 | 4992.0732 |
| 2.7204 | 6426.2552 | 6813.0507 | 4918.4785 |
| 2.7314 | 6317.0324 | 6709.7592 | 4844.8838 |
| 2.7424 | 6141.6524 | 6585.8856 | 4771.2890 |
| 2.7534 | 5915.0963 | 6444.0490 | 4697.6943 |
| 2.7644 | 5743.8510 | 6287.9291 | 4623.8971 |
| 2.7754 | 5498.8839 | 6120.8700 | 4550.1000 |
| 2.7864 | 5281.4857 | 5946.5396 | 4476.3028 |
| 2.7974 | 5174.4690 | 5768.1149 | 4402.5056 |
| 2.8084 | 4875.9837 | 5588.3320 | 4328.7085 |
| 2.8194 | 4832.9951 | 5409.4573 | 4254.9113 |
| 2.8304 | 4575.7315 | 5233.3079 | 4181.1141 |
| 2.8414 | 4392.3972 | 5061.2954 | 4107.3169 |
| 2.8524 | 4139.6652 | 4894.4760 | 4033.5198 |
| 2.8634 | 4105.8673 | 4733.5984 | 3959.7226 |
| 2.8744 | 4006.9297 | 4579.1467 | 3885.9254 |
| 2.8854 | 3812.2596 | 4431.3788 | 3812.1283 |
| 2.8964 | 3930.4602 | 4290.3602 | 3738.3311 |
| 2.9074 | 3576.4494 | 4155.9960 | 3664.5339 |
| 2.9184 | 3508.5320 | 4028.0605 | 3590.7368 |
| 2.9294 | 3577.1593 | 3906.2258 | 3516.9396 |
| 2.9404 | 3404.8343 | 3817.1527 | 3443.1424 |
| 2.9514 | 3434.5899 | 3713.4934 | 3403.6456 |
| 2.9624 | 3274.0782 | 3641.6578 | 3364.1487 |
| 2.9734 | 3204.0826 | 3574.0886 | 3324.6519 |
| 2.9844 | 3150.3279 | 3510.2999 | 3285.1550 |
| 2.9954 | 3057.4248 | 3449.8255 | 3245.6581 |
| 3.0064 | 3055.1942 | 3392.2283 | 3206.1613 |
| 3.0174 | 3015.4002 | 3337.1072 | 3166.6644 |
| 3.0284 | 3044.5811 | 3284.1006 | 3127.1676 |
| 3.0394 | 3070.3284 | 3232.8881 | 3087.6707 |
| 3.0504 | 3001.1972 | 3183.1899 | 3048.1738 |
| 3.0614 | 3000.9085 | 3134.7651 | 3008.6770 |
| 3.0724 | 2910.4504 | 3087.4088 | 2969.1801 |
| 3.0834 | 2983.9823 | 3040.9486 | 2929.6833 |
| 3.0944 | 2808.0354 | 2995.2407 | 2890.1864 |
| 3.1054 | 2802.9626 | 2950.1663 | 2850.6895 |
| 3.1164 | 2774.1052 | 2905.6279 | 2811.1927 |
| 3.1274 | 2820.2743 | 2877.4839 | 2771.6958 |
| 3.1384 | 2732.2453 | 2838.0538 | 2752.3983 |
| 3.1494 | 2728.8427 | 2814.9000 | 2733.1008 |
| 3.1604 | 2659.5472 | 2792.0409 | 2713.8034 |
| 3.1714 | 2657.8171 | 2769.4410 | 2694.5059 |
| 3.1824 | 2639.9400 | 2747.0709 | 2675.2084 |
| 3.1934 | 2608.3717 | 2724.9063 | 2655.9109 |
| 3.2044 | 2632.8274 | 2702.9268 | 2636.6134 |
| 3.2154 | 2588.9508 | 2681.1149 | 2617.3159 |
| 3.2264 | 2540.6357 | 2659.4560 | 2598.0184 |
| 3.2374 | 2505.7296 | 2637.9370 | 2578.7209 |
| 3.2484 | 2468.0556 | 2616.5467 | 2559.4234 |
| 3.2594 | 2525.2803 | 2595.2751 | 2540.1259 |
| 3.2704 | 2546.5669 | 2574.1133 | 2520.8284 |
| 3.2814 | 2511.3363 | 2553.0535 | 2501.5309 |
| 3.2924 | 2478.6593 | 2532.0882 | 2482.2335 |
| 3.3034 | 2428.8338 | 2511.2112 | 2462.9360 |
| 3.3144 | 2455.7404 | 2493.0891 | 2443.6385 |
| 3.3254 | 2470.4572 | 2473.0855 | 2427.7284 |
| 3.3364 | 2354.6873 | 2455.8265 | 2411.8183 |
| 3.3474 | 2352.4356 | 2438.6347 | 2395.9083 |
| 3.3584 | 2384.7330 | 2421.5058 | 2379.9982 |
| 3.3694 | 2310.0246 | 2404.4359 | 2364.0881 |
| 3.3804 | 2262.4179 | 2387.4215 | 2348.1780 |
| 3.3914 | 2280.7876 | 2370.4591 | 2332.2680 |
| 3.4024 | 2303.6829 | 2353.5458 | 2316.3579 |
| 3.4134 | 2266.0187 | 2336.6786 | 2300.4478 |
| 3.4244 | 2205.9661 | 2319.8550 | 2284.5378 |
| 3.4354 | 2223.4572 | 2303.0724 | 2268.6277 |
| 3.4464 | 2239.0177 | 2286.3285 | 2252.7176 |
| 3.4574 | 2190.9203 | 2269.6212 | 2236.8075 |
| 3.4684 | 2258.0330 | 2252.9486 | 2220.8975 |
| 3.4794 | 2246.9469 | 2236.3086 | 2204.9874 |
| 3.4904 | 2167.8274 | 2219.6997 | 2189.0773 |
| 3.5014 | 2174.5497 | 2205.0915 | 2173.1673 |
| 3.5124 | 2137.7094 | 2189.0669 | 2159.7556 |
| 3.5234 | 2155.7699 | 2175.0401 | 2146.3438 |
| 3.5344 | 2114.4897 | 2161.0384 | 2132.9321 |
| 3.5454 | 2075.5850 | 2147.0839 | 2119.5204 |
| 3.5564 | 2099.3215 | 2133.2054 | 2106.1087 |
| 3.5674 | 2048.8830 | 2119.2849 | 2092.6970 |
| 3.5784 | 2080.2758 | 2105.4120 | 2079.2853 |
| 3.5894 | 2112.3982 | 2091.5207 | 2065.8736 |
| 3.6004 | 2077.1077 | 2077.6481 | 2052.4619 |
| 3.6114 | 2001.6460 | 2063.7934 | 2039.0502 |
| 3.6224 | 2014.8510 | 2049.9558 | 2025.6385 |
| 3.6334 | 2023.6382 | 2036.1345 | 2012.2268 |
| 3.6444 | 1969.1298 | 2022.3287 | 1998.8151 |
| 3.6554 | 1984.1534 | 2008.5379 | 1985.4034 |
| 3.6664 | 1947.0585 | 1994.7614 | 1971.9917 |
| 3.6774 | 1975.5978 | 1980.9985 | 1958.5800 |
| 3.6884 | 1933.4513 | 1968.6280 | 1945.1683 |
| 3.6994 | 1951.1062 | 1955.2595 | 1933.5046 |
| 3.7104 | 1906.9341 | 1943.2824 | 1921.8410 |
| 3.7214 | 1893.7434 | 1931.3168 | 1910.1774 |
| 3.7324 | 1881.8437 | 1919.3624 | 1898.5138 |
| 3.7434 | 1946.9391 | 1907.4186 | 1886.8501 |
| 3.7544 | 1912.8289 | 1895.4850 | 1875.1865 |
| 3.7654 | 1874.2704 | 1883.5613 | 1863.5229 |
| 3.7764 | 1900.4081 | 1871.6471 | 1851.8593 |
| 3.7874 | 1806.8407 | 1859.7420 | 1840.1956 |
| 3.7984 | 1858.8658 | 1847.8457 | 1828.5320 |
| 3.8094 | 1820.6922 | 1835.9579 | 1816.8684 |
| 3.8204 | 1864.1962 | 1824.0783 | 1805.2048 |
| 3.8314 | 1870.6372 | 1812.2065 | 1793.5411 |
| 3.8424 | 1861.8948 | 1800.3424 | 1781.8775 |
| 3.8534 | 1854.0295 | 1788.4856 | 1770.2139 |
| 3.8644 | 1763.9090 | 1776.6359 | 1758.5503 |
| 3.8754 | 1714.3736 | 1769.1807 | 1746.8867 |
| 3.8864 | 1714.1062 | 1758.5175 | 1740.7835 |
| 3.8974 | 1768.2281 | 1752.2483 | 1734.6804 |
| 3.9084 | 1755.7222 | 1745.9853 | 1728.5773 |
| 3.9194 | 1677.1033 | 1739.7284 | 1722.4742 |
| 3.9304 | 1806.0752 | 1733.4773 | 1716.3711 |
| 3.9414 | 1808.5968 | 1727.2319 | 1710.2680 |
| 3.9524 | 1713.1269 | 1720.9920 | 1704.1649 |
| 3.9634 | 1763.1367 | 1714.7574 | 1698.0618 |
| 3.9744 | 1783.5949 | 1708.5281 | 1691.9587 |
| 3.9854 | 1729.0442 | 1702.3037 | 1685.8556 |
| 3.9964 | 1698.7498 | 1696.0843 | 1679.7524 |
| 4.0074 | 1739.8574 | 1689.8697 | 1673.6493 |
| 4.0184 | 1692.6977 | 1683.6597 | 1667.5462 |
| 4.0294 | 1737.3687 | 1677.4543 | 1661.4431 |
| 4.0404 | 1708.0708 | 1671.2532 | 1655.3400 |
| 4.0514 | 1682.4100 | 1665.0565 | 1649.2369 |
| 4.0624 | 1655.4764 | 1658.8640 | 1643.1338 |
| 4.0734 | 1652.9498 | 1652.6756 | 1637.0307 |
| 4.0844 | 1625.9381 | 1646.4911 | 1630.9276 |
| 4.0954 | 1610.5526 | 1640.3106 | 1624.8245 |
| 4.1064 | 1589.3796 | 1634.1340 | 1618.7213 |
| 4.1174 | 1620.2006 | 1627.9611 | 1612.6182 |
| 4.1284 | 1614.3948 | 1621.7918 | 1606.5151 |
| 4.1394 | 1602.3107 | 1615.6262 | 1600.4120 |
| 4.1504 | 1574.5265 | 1609.4641 | 1594.3089 |
| 4.1614 | 1587.4051 | 1603.3055 | 1588.2058 |
| 4.1724 | 1618.0904 | 1597.1503 | 1582.1027 |
| 4.1834 | 1573.2566 | 1590.9984 | 1575.9996 |
| 4.1944 | 1556.6755 | 1584.8498 | 1569.8965 |

Scan List

| Vis. | Dataset Name | Start pos. [°2θ] | End pos. [°2θ] | Step [°2θ] | Meas.Date/Time |
| --- | --- | --- | --- | --- | --- |
| * | 14 Etosha22 Crt 0-0.1cm S3 | 2.0054 | 29.9894 | 0.0110 | 12/7/2023 1:15:29 PM |

Peak List

| Pos. [°2θ] | Height [cts] | FWHM Left [°2θ] | d-spacing [Å] | Rel. Int. [%] |
| --- | --- | --- | --- | --- |
| 2.7092 | 1696.75 | 0.2598 | 32.58512 | 100.00 |
| 5.2853 | 105.88 | 0.1732 | 16.70694 | 6.24 |
| 7.0149 | 1537.72 | 0.5196 | 12.59100 | 90.63 |
| 8.7171 | 314.38 | 0.1732 | 10.13586 | 18.53 |
| 12.9404 | 21.91 | 0.5196 | 6.83579 | 1.29 |
| 15.7130 | 373.58 | 0.0541 | 5.63526 | 22.02 |
| 17.5698 | 30.69 | 0.2598 | 5.04369 | 1.81 |
| 18.1530 | 45.25 | 0.1082 | 4.88293 | 2.67 |
| 19.5068 | 27.53 | 0.4330 | 4.54701 | 1.62 |
| 25.8847 | 297.34 | 0.1515 | 3.43929 | 17.52 |
| 26.6782 | 122.46 | 0.1732 | 3.33877 | 7.22 |
| 27.4574 | 113.10 | 0.1299 | 3.24576 | 6.67 |

Pattern List

| Visible | Ref.Code | Score | Compound Name | Chem. Formula | Mineral Name | SemiQuant[%] |
| --- | --- | --- | --- | --- | --- | --- |
| * | 01-070-1575 | 26 | Sodium Aluminum Silicate Hydrate | Na ( Al Si2 O6 ) ( H2 O ) | Analcime | 5 |
| * | 04-025-4215 | 36 | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide | Mg10.4 V0.36 Mn33.5 Fe0.14 Al0.69 Si6.77 As6.5 P0.3 O54 ( O H )42 | Carlfrancisite | 47 |
| * | 01-087-8929 | 48 | Potassium Sodium Magnesium Iron Silicon Oxide Hydroxide | K1.91 Na0.09 ( Mg2.62 Fe4.004 ) ( Si7.376 O20 ) ( O H )4 | Phlogopite-1M, Fe-bearing | 11 |
| * | 04-016-3203 | 24 | Magnesium Silicon Oxide Hydroxide Hydrate | Mg4 Si6 O15 ( O H )2 ( H2 O )6 | Sepiolite | 7 |
| * | 04-016-6876 | 44 | Potassium Calcium Manganese Aluminum Silicate Hydroxide Hydrate | K0.38 Ca0.12 Mn2 Al0.62 Si2.71 O8 ( O H )1.33 ( H2 O )1.75 | Ganophyllite | 11 |
| * | 01-076-6603 | 18 | Magnesium Aluminum Silicate Hydroxide Hydrate | Mg3 ( ( Al Si3 O10 ) ( O H ) ) ( H2 O ) | Vermiculite | 1 |
| * | 01-082-8023 | 33 | Sodium Magnesium Silicon Oxide Hydrate | Na2 Mg3 ( Si6 O16 ) ( H2 O )7 | Loughlinite | 15 |
| * | 04-018-3208 | 27 | Magnesium Aluminum Iron Silicon Oxide Hydroxide Hydrate | Mg1.0 Fe0.08 Al1.0 Si3.99 O10.2 ( O H )0.8 ( H2 O )3.3 | Palygorskite-M | 4 |

Anchor Scan Parameters

Dataset Name	14 Etosha22 Crt 0-0.1cm S3

File name	C:\aeris_data\XRD data\Goldstein\Etosha 2023\Etosha Clay Data\Sample 14\14 Etosha22 Crt 0-0.1cm S3.xrdml

Sample Identification	14 Etosha22 Crt 0-0.1cm S3

Measurement Start Date/Time	12/7/2023 1:15:29 PM

Operator	Instrument

Raw Data Origin	XRD measurement (*.XRDML)

Scan Axis	Gonio

Start Position [°2θ]	2.0054

End Position [°2θ]	29.9894

Step Size [°2θ]	0.0110

Scan Step Time [s]	48.1950

Scan Type	Continuous

PSD Mode	Scanning

PSD Length [°2θ]	5.54

Offset [°2θ]	0.0000

Divergence Slit Type	Fixed

Divergence Slit Size [°]	0.0603

Specimen Length [mm]	10.00

Measurement Temperature [°C]	25.00

Anode Material	Cu

K-α1 [Å]	1.54060

K-α2 [Å]	1.54443

K-β1 [Å]	1.39225

K-A2 / K-A1 Ratio	0.50000

Generator Settings	15 mA, 40 kV

Diffractometer Type	2082464

Diffractometer Number	0

Goniometer Radius [mm]	145.00

Dist. Focus-Diverg. Slit [mm]	95.00

Incident Beam Monochromator	No

Spinning	Yes