14 Etosha 22 crt 0-0.1cm S3 400 C

Graphics

Graphics

Graphics

Quantitative Results

Phase Sodium Aluminum Silicate Hydrate

Weight fraction/ %	17.0

Phase Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide

Weight fraction/ %	18.0

Phase Potassium Magnesium Aluminum Iron Silicon Oxide Hydroxide

Weight fraction/ %	42.0

Phase Potassium Calcium Manganese Aluminum Silicate Hydroxide Hydrate

Weight fraction/ %	4.0

Phase Magnesium Silicate Hydroxide Hydrate

Weight fraction/ %	6.0

Phase Magnesium Aluminum Silicon Oxide Hydroxide Hydrate

Weight fraction/ %	8.0

Phase Sodium Magnesium Silicon Oxide Hydrate

Weight fraction/ %	5.0

Multiple Quantitative Results

Scans vs Phases Matrix

| Scan name | Sodium Aluminum Silicate Hydrate | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide | Potassium Magnesium Aluminum Iron Silicon Oxide Hydroxide | Potassium Calcium Manganese Aluminum Silicate Hydroxide Hydrate | Magnesium Silicate Hydroxide Hydrate | Magnesium Aluminum Silicon Oxide Hydroxide Hydrate | Sodium Magnesium Silicon Oxide Hydrate |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 14 Etosha22 Crt 0-0.1cm S3 400C | 17.0 | 18.0 | 42.0 | 4.0 | 6.0 | 8.0 | 5.0 |

Anchor Scan Data

| Pos. [°2θ] | Iobs [cts] | Icalc [cts] | Iback [cts] |
| --- | --- | --- | --- |
| 2.0054 | 5632.0000 | 5614.2001 | 5632.0000 |
| 2.0164 | 5851.2424 | 5603.0747 | 5603.0747 |
| 2.0274 | 5707.0501 | 5574.1494 | 5574.1494 |
| 2.0384 | 5591.9912 | 5545.2241 | 5545.2241 |
| 2.0494 | 5637.6578 | 5516.2988 | 5516.2988 |
| 2.0604 | 5517.7655 | 5487.3735 | 5487.3735 |
| 2.0714 | 5546.5782 | 5458.4481 | 5458.4481 |
| 2.0824 | 5382.3019 | 5429.5228 | 5429.5228 |
| 2.0934 | 5442.0610 | 5400.5975 | 5400.5975 |
| 2.1044 | 5538.9203 | 5371.6722 | 5371.6722 |
| 2.1154 | 5281.1229 | 5342.7469 | 5342.7469 |
| 2.1264 | 5277.8088 | 5313.8216 | 5313.8216 |
| 2.1374 | 5247.1652 | 5284.8963 | 5284.8963 |
| 2.1484 | 5220.3663 | 5255.9710 | 5255.9710 |
| 2.1594 | 5181.7178 | 5227.0457 | 5227.0457 |
| 2.1704 | 5133.2802 | 5198.1204 | 5198.1204 |
| 2.1814 | 5206.0875 | 5169.1950 | 5169.1950 |
| 2.1924 | 5129.2689 | 5140.6687 | 5140.2697 |
| 2.2034 | 5102.4336 | 5111.9928 | 5111.9928 |
| 2.2144 | 5093.4852 | 5083.7159 | 5083.7159 |
| 2.2254 | 4984.3776 | 5055.4389 | 5055.4389 |
| 2.2364 | 4890.2699 | 5027.1620 | 5027.1620 |
| 2.2474 | 5053.3677 | 4998.8851 | 4998.8851 |
| 2.2584 | 4947.5074 | 4970.6082 | 4970.6082 |
| 2.2694 | 4814.3156 | 4942.3312 | 4942.3312 |
| 2.2804 | 4803.6657 | 4914.0543 | 4914.0543 |
| 2.2914 | 4868.7719 | 4885.7774 | 4885.7774 |
| 2.3024 | 4868.5310 | 4857.5004 | 4857.5004 |
| 2.3134 | 4758.0069 | 4829.2235 | 4829.2235 |
| 2.3244 | 4703.0295 | 4800.9466 | 4800.9466 |
| 2.3354 | 4692.5929 | 4772.6696 | 4772.6696 |
| 2.3464 | 4730.5256 | 4744.3927 | 4744.3927 |
| 2.3574 | 4720.8279 | 4716.1158 | 4716.1158 |
| 2.3684 | 4693.7625 | 4687.8389 | 4687.8389 |
| 2.3794 | 4685.0905 | 4661.5049 | 4659.5619 |
| 2.3904 | 4594.7965 | 4634.4423 | 4634.4423 |
| 2.4014 | 4551.7611 | 4609.3227 | 4609.3227 |
| 2.4124 | 4512.0536 | 4584.2031 | 4584.2031 |
| 2.4234 | 4435.9459 | 4559.0835 | 4559.0835 |
| 2.4344 | 4474.5708 | 4533.9639 | 4533.9639 |
| 2.4454 | 4399.1799 | 4508.8443 | 4508.8443 |
| 2.4564 | 4372.5900 | 4483.7247 | 4483.7247 |
| 2.4674 | 4412.4130 | 4458.6051 | 4458.6051 |
| 2.4784 | 4327.1485 | 4433.4855 | 4433.4855 |
| 2.4894 | 4302.1731 | 4408.3659 | 4408.3659 |
| 2.5004 | 4295.5575 | 4383.2463 | 4383.2463 |
| 2.5114 | 4290.2655 | 4358.1267 | 4358.1267 |
| 2.5224 | 4250.5865 | 4333.0071 | 4333.0071 |
| 2.5334 | 4259.0177 | 4307.8875 | 4307.8875 |
| 2.5444 | 4208.4902 | 4282.7679 | 4282.7679 |
| 2.5554 | 4261.5467 | 4257.6483 | 4257.6483 |
| 2.5664 | 4265.0619 | 4235.4872 | 4232.5287 |
| 2.5774 | 4200.7955 | 4212.2168 | 4212.2168 |
| 2.5884 | 4145.6116 | 4191.9049 | 4191.9049 |
| 2.5994 | 4200.9912 | 4171.5930 | 4171.5930 |
| 2.6104 | 4125.7547 | 4151.2811 | 4151.2811 |
| 2.6214 | 4037.9616 | 4130.9692 | 4130.9692 |
| 2.6324 | 4030.0059 | 4110.6573 | 4110.6573 |
| 2.6434 | 3983.0983 | 4090.3454 | 4090.3454 |
| 2.6544 | 3972.4272 | 4070.0335 | 4070.0335 |
| 2.6654 | 3925.1150 | 4049.7216 | 4049.7216 |
| 2.6764 | 3875.5103 | 4029.4097 | 4029.4097 |
| 2.6874 | 4031.1259 | 4009.0979 | 4009.0979 |
| 2.6984 | 3992.4026 | 3988.7860 | 3988.7860 |
| 2.7094 | 3867.6716 | 3968.4741 | 3968.4741 |
| 2.7204 | 3875.3535 | 3948.1622 | 3948.1622 |
| 2.7314 | 3879.1327 | 3927.8503 | 3927.8503 |
| 2.7424 | 3952.9386 | 3907.5384 | 3907.5384 |
| 2.7534 | 3858.6755 | 3888.4046 | 3887.2265 |
| 2.7644 | 3870.0752 | 3868.8291 | 3868.8291 |
| 2.7754 | 3862.2340 | 3850.4316 | 3850.4316 |
| 2.7864 | 3726.4823 | 3832.0342 | 3832.0342 |
| 2.7974 | 3728.2389 | 3813.6368 | 3813.6368 |
| 2.8084 | 3765.9926 | 3795.2393 | 3795.2393 |
| 2.8194 | 3760.9046 | 3776.8419 | 3776.8419 |
| 2.8304 | 3725.8923 | 3758.4445 | 3758.4445 |
| 2.8414 | 3707.1200 | 3740.0470 | 3740.0470 |
| 2.8524 | 3619.8766 | 3721.6496 | 3721.6496 |
| 2.8634 | 3697.4484 | 3703.2522 | 3703.2522 |
| 2.8744 | 3591.2778 | 3684.8547 | 3684.8547 |
| 2.8854 | 3646.0138 | 3666.4573 | 3666.4573 |
| 2.8964 | 3570.3407 | 3648.0599 | 3648.0599 |
| 2.9074 | 3617.1731 | 3629.6624 | 3629.6624 |
| 2.9184 | 3640.6328 | 3611.2650 | 3611.2650 |
| 2.9294 | 3713.8672 | 3592.8676 | 3592.8676 |
| 2.9404 | 3534.4897 | 3574.4702 | 3574.4702 |
| 2.9514 | 3598.9056 | 3556.0727 | 3556.0727 |
| 2.9624 | 3430.1283 | 3537.6753 | 3537.6753 |
| 2.9734 | 3414.4671 | 3519.2779 | 3519.2779 |
| 2.9844 | 3517.6195 | 3500.8804 | 3500.8804 |
| 2.9954 | 3481.4956 | 3482.4830 | 3482.4830 |
| 3.0064 | 3451.4076 | 3464.0856 | 3464.0856 |
| 3.0174 | 3445.5615 | 3445.6881 | 3445.6881 |
| 3.0284 | 3419.5472 | 3427.2907 | 3427.2907 |
| 3.0394 | 3325.3501 | 3408.8933 | 3408.8933 |
| 3.0504 | 3343.6352 | 3390.4958 | 3390.4958 |
| 3.0614 | 3302.7846 | 3372.0984 | 3372.0984 |
| 3.0724 | 3264.1436 | 3353.7010 | 3353.7010 |
| 3.0834 | 3338.0039 | 3335.3035 | 3335.3035 |
| 3.0944 | 3217.7301 | 3316.9061 | 3316.9061 |
| 3.1054 | 3286.4798 | 3298.5087 | 3298.5087 |
| 3.1164 | 3267.3786 | 3280.1112 | 3280.1112 |
| 3.1274 | 3247.4454 | 3264.5826 | 3261.7138 |
| 3.1384 | 3269.9774 | 3247.9783 | 3247.9783 |
| 3.1494 | 3224.6696 | 3234.2428 | 3234.2428 |
| 3.1604 | 3209.2419 | 3220.5072 | 3220.5072 |
| 3.1714 | 3137.0747 | 3206.7717 | 3206.7717 |
| 3.1824 | 3099.9631 | 3193.0362 | 3193.0362 |
| 3.1934 | 3114.1150 | 3179.3007 | 3179.3007 |
| 3.2044 | 3079.6465 | 3165.5652 | 3165.5652 |
| 3.2154 | 3084.1907 | 3151.8297 | 3151.8297 |
| 3.2264 | 3054.8584 | 3138.0942 | 3138.0942 |
| 3.2374 | 3087.3510 | 3124.3586 | 3124.3586 |
| 3.2484 | 3077.2222 | 3110.7574 | 3110.6231 |
| 3.2594 | 3055.5398 | 3097.3684 | 3096.8876 |
| 3.2704 | 3033.2694 | 3083.7029 | 3083.1521 |
| 3.2814 | 3052.6637 | 3070.1437 | 3069.4166 |
| 3.2924 | 3098.9204 | 3056.4124 | 3055.6811 |
| 3.3034 | 3081.5014 | 3042.6810 | 3041.9456 |
| 3.3144 | 3015.1033 | 3029.5063 | 3028.2100 |
| 3.3254 | 2983.3569 | 3016.1229 | 3015.3790 |
| 3.3364 | 2941.7955 | 3003.2962 | 3002.5480 |
| 3.3474 | 2954.4956 | 2990.4695 | 2989.7170 |
| 3.3584 | 2910.8908 | 2977.6429 | 2976.8860 |
| 3.3694 | 2879.6745 | 2964.8163 | 2964.0550 |
| 3.3804 | 2919.8191 | 2951.9897 | 2951.2241 |
| 3.3914 | 2924.3451 | 2939.1632 | 2938.3931 |
| 3.4024 | 2909.0000 | 2926.3367 | 2925.5621 |
| 3.4134 | 2828.7443 | 2913.5102 | 2912.7311 |
| 3.4244 | 2827.5546 | 2900.6838 | 2899.9001 |
| 3.4354 | 2915.6313 | 2887.8574 | 2887.0691 |
| 3.4464 | 2835.9567 | 2875.0311 | 2874.2381 |
| 3.4574 | 2788.0295 | 2862.2048 | 2861.4071 |
| 3.4684 | 2754.3967 | 2849.3786 | 2848.5761 |
| 3.4794 | 2791.7001 | 2836.5524 | 2835.7451 |
| 3.4904 | 2841.5044 | 2823.7262 | 2822.9141 |
| 3.5014 | 2889.2950 | 2810.8515 | 2810.0831 |
| 3.5124 | 2814.6253 | 2797.9951 | 2797.1731 |
| 3.5234 | 2771.0000 | 2785.0901 | 2784.2632 |
| 3.5344 | 2731.3264 | 2772.1852 | 2771.3533 |
| 3.5454 | 2711.3963 | 2759.2803 | 2758.4433 |
| 3.5564 | 2694.6062 | 2746.3755 | 2745.5334 |
| 3.5674 | 2739.6824 | 2733.5037 | 2732.6234 |
| 3.5784 | 2722.9071 | 2720.7220 | 2719.7135 |
| 3.5894 | 2644.2478 | 2707.8360 | 2706.8036 |
| 3.6004 | 2695.1805 | 2694.9956 | 2693.8936 |
| 3.6114 | 2620.4552 | 2682.0941 | 2680.9837 |
| 3.6224 | 2673.4514 | 2669.1927 | 2668.0738 |
| 3.6334 | 2595.3490 | 2656.2914 | 2655.1638 |
| 3.6444 | 2590.6273 | 2643.3903 | 2642.2539 |
| 3.6554 | 2673.3039 | 2630.4892 | 2629.3440 |
| 3.6664 | 2668.3132 | 2617.5883 | 2616.4340 |
| 3.6774 | 2599.0137 | 2604.6875 | 2603.5241 |
| 3.6884 | 2554.6593 | 2591.7868 | 2590.6142 |
| 3.6994 | 2576.7847 | 2578.8863 | 2577.7042 |
| 3.7104 | 2637.0221 | 2565.9859 | 2564.7943 |
| 3.7214 | 2582.4513 | 2553.0856 | 2551.8844 |
| 3.7324 | 2560.2655 | 2540.1854 | 2538.9744 |
| 3.7434 | 2493.0609 | 2527.2854 | 2526.0645 |
| 3.7544 | 2605.4219 | 2514.3855 | 2513.1546 |
| 3.7654 | 2508.5437 | 2501.4858 | 2500.2446 |
| 3.7764 | 2608.7591 | 2488.5862 | 2487.3347 |
| 3.7874 | 2533.6902 | 2475.6868 | 2474.4248 |
| 3.7984 | 2464.1893 | 2462.7875 | 2461.5148 |
| 3.8094 | 2518.8741 | 2449.8884 | 2448.6049 |
| 3.8204 | 2508.9823 | 2436.9894 | 2435.6950 |
| 3.8314 | 2440.9351 | 2424.0907 | 2422.7850 |
| 3.8424 | 2481.9498 | 2411.1920 | 2409.8751 |
| 3.8534 | 2396.3216 | 2398.2936 | 2396.9652 |
| 3.8644 | 2461.1902 | 2385.3953 | 2384.0552 |
| 3.8754 | 2323.5792 | 2375.0772 | 2371.1453 |
| 3.8864 | 2356.2345 | 2363.7919 | 2362.4279 |
| 3.8974 | 2330.1859 | 2355.0867 | 2353.7106 |
| 3.9084 | 2386.5054 | 2346.3818 | 2344.9932 |
| 3.9194 | 2390.5546 | 2337.6770 | 2336.2758 |
| 3.9304 | 2379.5103 | 2328.9725 | 2327.5585 |
| 3.9414 | 2309.0993 | 2320.2682 | 2318.8411 |
| 3.9524 | 2355.9956 | 2311.5640 | 2310.1237 |
| 3.9634 | 2320.6441 | 2302.8601 | 2301.4064 |
| 3.9744 | 2359.5944 | 2294.1565 | 2292.6890 |
| 3.9854 | 2314.4248 | 2285.4530 | 2283.9716 |
| 3.9964 | 2316.2247 | 2276.7498 | 2275.2543 |
| 4.0074 | 2317.0000 | 2268.0469 | 2266.5369 |
| 4.0184 | 2316.0029 | 2259.3442 | 2257.8195 |
| 4.0294 | 2304.6303 | 2250.6418 | 2249.1022 |
| 4.0404 | 2275.5231 | 2241.9396 | 2240.3848 |
| 4.0514 | 2235.5339 | 2233.2377 | 2231.6674 |
| 4.0624 | 2197.3663 | 2225.4464 | 2222.9501 |
| 4.0734 | 2230.2782 | 2217.3141 | 2215.7121 |
| 4.0844 | 2197.1637 | 2210.0925 | 2208.4741 |
| 4.0954 | 2241.9410 | 2202.8712 | 2201.2361 |
| 4.1064 | 2204.6204 | 2195.6501 | 2193.9981 |
| 4.1174 | 2170.2006 | 2188.4295 | 2186.7601 |
| 4.1284 | 2187.8417 | 2181.2091 | 2179.5221 |
| 4.1394 | 2229.5359 | 2173.9891 | 2172.2841 |
| 4.1504 | 2204.2920 | 2166.7695 | 2165.0461 |
| 4.1614 | 2178.2242 | 2159.5502 | 2157.8082 |
| 4.1724 | 2166.7541 | 2152.3313 | 2150.5702 |
| 4.1834 | 2116.6814 | 2145.1128 | 2143.3322 |
| 4.1944 | 2176.6603 | 2137.8947 | 2136.0942 |

Scan List

| Vis. | Dataset Name | Start pos. [°2θ] | End pos. [°2θ] | Step [°2θ] | Meas.Date/Time |
| --- | --- | --- | --- | --- | --- |
| * | 14 Etosha22 Crt 0-0.1cm S3 400C | 2.0054 | 29.9894 | 0.0110 | 12/7/2023 3:11:11 PM |

Peak List

| Pos. [°2θ] | Height [cts] | FWHM Left [°2θ] | d-spacing [Å] | Rel. Int. [%] |
| --- | --- | --- | --- | --- |
| 5.3075 | 165.57 | 0.1732 | 16.63707 | 29.96 |
| 7.1525 | 510.71 | 0.3897 | 12.34920 | 92.40 |
| 8.7555 | 552.71 | 0.1732 | 10.09145 | 100.00 |
| 13.3139 | 9.73 | 0.6927 | 6.64482 | 1.76 |
| 15.8082 | 376.68 | 0.0866 | 5.60154 | 68.15 |
| 17.6581 | 31.51 | 0.2598 | 5.01866 | 5.70 |
| 18.2513 | 58.21 | 0.1299 | 4.85687 | 10.53 |
| 19.6321 | 29.55 | 0.2598 | 4.51826 | 5.35 |
| 26.0088 | 225.13 | 0.0758 | 3.42316 | 40.73 |
| 26.7203 | 128.89 | 0.2165 | 3.33360 | 23.32 |
| 27.5120 | 127.37 | 0.1082 | 3.23944 | 23.05 |

Pattern List

| Visible | Ref.Code | Score | Compound Name | Chem. Formula | Mineral Name | SemiQuant[%] |
| --- | --- | --- | --- | --- | --- | --- |
| * | 01-083-1732 | 59 | Sodium Aluminum Silicate Hydrate | Na16.48 Al15.52 Si32.48 O96 ( H2 O )16 | Analcime | 17 |
| * | 04-025-4215 | 6 | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide | Mg10.4 V0.36 Mn33.5 Fe0.14 Al0.69 Si6.77 As6.5 P0.3 O54 ( O H )42 | Carlfrancisite | 18 |
| * | 04-017-0517 | 55 | Potassium Magnesium Aluminum Iron Silicon Oxide Hydroxide | K Mg2.24 Fe0.76 Al1.4 Si2.6 O10 ( O H )2 | Phlogopite-1M, Fe+2-bearing | 42 |
| * | 04-016-6876 | 46 | Potassium Calcium Manganese Aluminum Silicate Hydroxide Hydrate | K0.38 Ca0.12 Mn2 Al0.62 Si2.71 O8 ( O H )1.33 ( H2 O )1.75 | Ganophyllite | 4 |
| * | 01-088-9172 | 28 | Magnesium Silicate Hydroxide Hydrate | Mg16 Si24 O60 ( O H )8 ( O H2 )8 ( H2 O )16 | Sepiolite | 6 |
| * | 01-081-8598 | 26 | Magnesium Aluminum Silicon Oxide Hydroxide Hydrate | ( Mg2 Al2 ) Si8 O20 ( H2 O )4 ( O H )2 ( H2 O )3.84 | Palygorskite-M | 8 |
| * | 01-082-8023 | 23 | Sodium Magnesium Silicon Oxide Hydrate | Na2 Mg3 ( Si6 O16 ) ( H2 O )7 | Loughlinite | 5 |

Anchor Scan Parameters

Dataset Name	14 Etosha22 Crt 0-0.1cm S3 400C

File name	C:\aeris_data\XRD data\Goldstein\Etosha 2023\Etosha Clay Data\Sample 14\14 Etosha22 Crt 0-0.1cm S3 400C.xrdml

Sample Identification	14 Etosha22 Crt 0-0.1cm S3 400C

Measurement Start Date/Time	12/7/2023 3:11:11 PM

Operator	Instrument

Raw Data Origin	XRD measurement (*.XRDML)

Scan Axis	Gonio

Start Position [°2θ]	2.0054

End Position [°2θ]	29.9894

Step Size [°2θ]	0.0110

Scan Step Time [s]	48.1950

Scan Type	Continuous

PSD Mode	Scanning

PSD Length [°2θ]	5.54

Offset [°2θ]	0.0000

Divergence Slit Type	Fixed

Divergence Slit Size [°]	0.0603

Specimen Length [mm]	10.00

Measurement Temperature [°C]	25.00

Anode Material	Cu

K-α1 [Å]	1.54060

K-α2 [Å]	1.54443

K-β1 [Å]	1.39225

K-A2 / K-A1 Ratio	0.50000

Generator Settings	15 mA, 40 kV

Diffractometer Type	2082464

Diffractometer Number	0

Goniometer Radius [mm]	145.00

Dist. Focus-Diverg. Slit [mm]	95.00

Incident Beam Monochromator	No

Spinning	Yes