14 Etosha 22 crt 0-0.1cm S3 550 C REPORT

Graphics

Graphics

Graphics

Quantitative Results

Phase Titanium Oxide

Weight fraction/ %	2.0

Phase Potassium Magnesium Manganese Aluminum Iron Silicon Oxide Hydroxide

Weight fraction/ %	34.0

Phase Sodium Aluminum Silicate Hydrate

Weight fraction/ %	6.0

Phase Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide

Weight fraction/ %	27.0

Phase Calcium Magnesium Iron Silicate Hydroxide

Weight fraction/ %	1.0

Phase Sodium Magnesium Silicon Oxide Hydrate

Weight fraction/ %	30.0

Multiple Quantitative Results

Scans vs Phases Matrix

| Scan name | Titanium Oxide | Potassium Magnesium Manganese Aluminum Iron Silicon Oxide Hydroxide | Sodium Aluminum Silicate Hydrate | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide | Calcium Magnesium Iron Silicate Hydroxide | Sodium Magnesium Silicon Oxide Hydrate |
| --- | --- | --- | --- | --- | --- | --- |
| 14 Etosha22 Crt 0-0.1cm S3 550C | 2.0 | 34.0 | 6.0 | 27.0 | 1.0 | 30.0 |

Anchor Scan Data

| Pos. [°2θ] | Iobs [cts] | Icalc [cts] | Iback [cts] |
| --- | --- | --- | --- |
| 2.0054 | 9654.0000 | 9647.1136 | 9654.0000 |
| 2.0164 | 9516.0492 | 9601.6916 | 9582.5753 |
| 2.0274 | 9514.8623 | 9530.8965 | 9511.1506 |
| 2.0384 | 9311.1475 | 9460.1328 | 9439.7259 |
| 2.0494 | 9309.3461 | 9389.4026 | 9368.3011 |
| 2.0604 | 9196.0669 | 9318.7082 | 9296.8764 |
| 2.0714 | 9128.6991 | 9248.0520 | 9225.4517 |
| 2.0824 | 9030.1170 | 9177.4367 | 9154.0270 |
| 2.0934 | 8963.1947 | 9106.8654 | 9082.6023 |
| 2.1044 | 9017.7876 | 9036.3411 | 9011.1776 |
| 2.1154 | 9007.6205 | 8965.8674 | 8939.7528 |
| 2.1264 | 9034.8245 | 8895.4480 | 8868.3281 |
| 2.1374 | 8860.4100 | 8825.0873 | 8796.9034 |
| 2.1484 | 8859.7163 | 8754.7896 | 8725.4787 |
| 2.1594 | 8871.4189 | 8684.5602 | 8654.0540 |
| 2.1704 | 8840.0103 | 8614.4045 | 8582.6293 |
| 2.1814 | 8771.5359 | 8544.3287 | 8511.2045 |
| 2.1924 | 8798.4341 | 8474.2740 | 8439.7798 |
| 2.2034 | 8655.7965 | 8404.2603 | 8368.1711 |
| 2.2144 | 8585.4199 | 8334.2836 | 8296.5625 |
| 2.2254 | 8436.1858 | 8264.4184 | 8224.9538 |
| 2.2364 | 8568.1991 | 8194.6750 | 8153.3451 |
| 2.2474 | 8587.1288 | 8125.0650 | 8081.7365 |
| 2.2584 | 8420.1136 | 8055.6013 | 8010.1278 |
| 2.2694 | 8423.5369 | 7986.2984 | 7938.5191 |
| 2.2804 | 8316.4852 | 7917.1729 | 7866.9104 |
| 2.2914 | 8264.5369 | 7848.2439 | 7795.3018 |
| 2.3024 | 8229.3717 | 7779.5336 | 7723.6931 |
| 2.3134 | 8227.4867 | 7711.0680 | 7652.0844 |
| 2.3244 | 8229.1976 | 7642.8783 | 7580.4758 |
| 2.3354 | 8185.2684 | 7575.0028 | 7508.8671 |
| 2.3464 | 8147.6101 | 7507.4889 | 7437.2584 |
| 2.3574 | 8052.8741 | 7440.3967 | 7365.6497 |
| 2.3684 | 8024.3496 | 7373.8037 | 7294.0411 |
| 2.3794 | 7996.8515 | 7307.7580 | 7222.4324 |
| 2.3904 | 7930.7247 | 7242.4017 | 7150.6749 |
| 2.4014 | 7899.4867 | 7177.8985 | 7078.9174 |
| 2.4124 | 7927.6406 | 7114.5286 | 7007.1599 |
| 2.4234 | 7937.5329 | 7052.5865 | 6935.4024 |
| 2.4344 | 7871.8082 | 6992.4495 | 6863.6449 |
| 2.4454 | 7869.8299 | 6934.5928 | 6791.8874 |
| 2.4564 | 7824.5914 | 6879.6036 | 6720.1299 |
| 2.4674 | 7775.5605 | 6828.1909 | 6648.3725 |
| 2.4784 | 7728.6544 | 6781.1881 | 6576.6150 |
| 2.4894 | 7612.5310 | 6739.5470 | 6504.8575 |
| 2.5004 | 7579.4071 | 6704.3167 | 6433.1000 |
| 2.5114 | 7537.7306 | 6676.6082 | 6361.3425 |
| 2.5224 | 7425.8820 | 6657.5406 | 6289.5850 |
| 2.5334 | 7353.5103 | 6648.1703 | 6217.8275 |
| 2.5444 | 7371.2837 | 6649.4035 | 6146.0700 |
| 2.5554 | 7264.9331 | 6661.8950 | 6074.3125 |
| 2.5664 | 7259.8333 | 6685.9380 | 6002.5550 |
| 2.5774 | 7312.2262 | 6721.3435 | 5930.7975 |
| 2.5884 | 7331.6799 | 6767.3113 | 5859.0400 |
| 2.5994 | 7224.8407 | 6822.2843 | 5787.2825 |
| 2.6104 | 7189.3083 | 6883.7787 | 5715.5250 |
| 2.6214 | 7071.2881 | 6948.1891 | 5643.7675 |
| 2.6324 | 7041.0236 | 7010.5939 | 5572.0100 |
| 2.6434 | 7072.9607 | 7064.6511 | 5500.2526 |
| 2.6544 | 7033.1386 | 7102.7530 | 5428.4951 |
| 2.6654 | 6944.9410 | 7116.6608 | 5356.7376 |
| 2.6764 | 6863.0187 | 7098.7358 | 5284.9801 |
| 2.6874 | 6712.1662 | 7043.5661 | 5213.2226 |
| 2.6984 | 6593.5664 | 6949.3858 | 5141.4651 |
| 2.7094 | 6438.8466 | 6818.5823 | 5069.7076 |
| 2.7204 | 6310.3255 | 6657.0107 | 4997.9501 |
| 2.7314 | 6186.4100 | 6472.4943 | 4926.1926 |
| 2.7424 | 5857.4813 | 6273.2333 | 4854.4351 |
| 2.7534 | 5768.5978 | 6066.6119 | 4782.6776 |
| 2.7644 | 5664.7743 | 5858.7665 | 4710.7713 |
| 2.7754 | 5494.7138 | 5654.3996 | 4638.8650 |
| 2.7864 | 5278.0137 | 5456.9891 | 4566.9587 |
| 2.7974 | 5104.8672 | 5268.8685 | 4495.0523 |
| 2.8084 | 4864.3800 | 5091.4720 | 4423.1460 |
| 2.8194 | 4695.2930 | 4925.5000 | 4351.2397 |
| 2.8304 | 4615.5501 | 4771.0616 | 4279.3334 |
| 2.8414 | 4380.2065 | 4627.8024 | 4207.4271 |
| 2.8524 | 4381.0354 | 4495.0231 | 4135.5208 |
| 2.8634 | 4277.5015 | 4371.7892 | 4063.6144 |
| 2.8744 | 4058.4105 | 4257.0300 | 3991.7081 |
| 2.8854 | 3985.1367 | 4149.6237 | 3919.8018 |
| 2.8964 | 3814.7522 | 4048.4658 | 3847.8955 |
| 2.9074 | 3769.0560 | 3952.5201 | 3775.9892 |
| 2.9184 | 3649.0123 | 3860.8518 | 3704.0829 |
| 2.9294 | 3601.8112 | 3772.6461 | 3632.1765 |
| 2.9404 | 3621.9287 | 3698.7775 | 3560.2702 |
| 2.9514 | 3522.7384 | 3636.4988 | 3520.8808 |
| 2.9624 | 3325.8230 | 3587.5280 | 3481.4913 |
| 2.9734 | 3396.9813 | 3539.9362 | 3442.1019 |
| 2.9844 | 3309.7365 | 3493.4401 | 3402.7124 |
| 2.9954 | 3226.7080 | 3447.8211 | 3363.3230 |
| 3.0064 | 3196.7488 | 3402.9126 | 3323.9335 |
| 3.0174 | 3176.3382 | 3358.5874 | 3284.5440 |
| 3.0284 | 3146.7065 | 3314.7487 | 3245.1546 |
| 3.0394 | 3114.5339 | 3271.3219 | 3205.7651 |
| 3.0504 | 3095.4026 | 3228.2488 | 3166.3757 |
| 3.0614 | 3023.2566 | 3185.4837 | 3126.9862 |
| 3.0724 | 3061.5418 | 3142.9895 | 3087.5968 |
| 3.0834 | 3017.8191 | 3100.7359 | 3048.2073 |
| 3.0944 | 2971.6903 | 3058.6974 | 3008.8178 |
| 3.1054 | 2918.1672 | 3016.8524 | 2969.4284 |
| 3.1164 | 2919.4833 | 2975.1822 | 2930.0389 |
| 3.1274 | 2921.6902 | 2939.5819 | 2890.6495 |
| 3.1384 | 2854.7443 | 2908.9241 | 2867.8811 |
| 3.1494 | 2820.4602 | 2884.3093 | 2845.1126 |
| 3.1604 | 2769.8451 | 2859.8147 | 2822.3442 |
| 3.1714 | 2790.5143 | 2835.4302 | 2799.5758 |
| 3.1824 | 2778.8731 | 2811.1468 | 2776.8074 |
| 3.1934 | 2720.1327 | 2786.9563 | 2754.0390 |
| 3.2044 | 2682.6273 | 2762.8513 | 2731.2706 |
| 3.2154 | 2685.8948 | 2738.8253 | 2708.5021 |
| 3.2264 | 2654.5797 | 2714.8721 | 2685.7337 |
| 3.2374 | 2676.4553 | 2690.9863 | 2662.9653 |
| 3.2484 | 2618.5555 | 2667.1630 | 2640.1969 |
| 3.2594 | 2571.4484 | 2643.3976 | 2617.4285 |
| 3.2704 | 2576.5669 | 2619.6859 | 2594.6601 |
| 3.2814 | 2551.1288 | 2596.0243 | 2571.8917 |
| 3.2924 | 2508.4425 | 2572.4093 | 2549.1232 |
| 3.3034 | 2482.4248 | 2548.8377 | 2526.3548 |
| 3.3144 | 2523.8505 | 2527.0006 | 2503.5864 |
| 3.3254 | 2518.8761 | 2506.5762 | 2485.5807 |
| 3.3364 | 2469.0993 | 2487.8812 | 2467.5751 |
| 3.3474 | 2445.4799 | 2469.2193 | 2449.5694 |
| 3.3584 | 2473.1652 | 2450.5885 | 2431.5637 |
| 3.3694 | 2428.6391 | 2431.9869 | 2413.5580 |
| 3.3804 | 2372.8815 | 2413.4126 | 2395.5523 |
| 3.3914 | 2374.3274 | 2394.8642 | 2377.5467 |
| 3.4024 | 2375.8294 | 2376.3399 | 2359.5410 |
| 3.4134 | 2334.8849 | 2357.8385 | 2341.5353 |
| 3.4244 | 2346.0605 | 2339.3585 | 2323.5296 |
| 3.4354 | 2331.1514 | 2320.8989 | 2305.5239 |
| 3.4464 | 2312.1519 | 2302.4584 | 2287.5183 |
| 3.4574 | 2308.6637 | 2284.0359 | 2269.5126 |
| 3.4684 | 2221.7571 | 2265.6306 | 2251.5069 |
| 3.4794 | 2217.7021 | 2247.2415 | 2233.5012 |
| 3.4904 | 2221.2212 | 2228.8677 | 2215.4955 |
| 3.5014 | 2204.2842 | 2212.3053 | 2197.4899 |
| 3.5124 | 2185.2709 | 2197.2153 | 2184.5364 |
| 3.5234 | 2153.6342 | 2183.9351 | 2171.5830 |
| 3.5344 | 2225.8894 | 2170.6673 | 2158.6295 |
| 3.5454 | 2141.7974 | 2157.4114 | 2145.6761 |
| 3.5564 | 2162.7065 | 2144.2479 | 2132.7227 |
| 3.5674 | 2160.1681 | 2131.0532 | 2119.7692 |
| 3.5784 | 2145.6967 | 2117.8718 | 2106.8158 |
| 3.5894 | 2099.3451 | 2104.6791 | 2093.8623 |
| 3.6004 | 2108.6839 | 2091.4765 | 2080.9089 |
| 3.6114 | 2087.1927 | 2078.2827 | 2067.9555 |
| 3.6224 | 2128.4071 | 2065.0974 | 2055.0020 |
| 3.6334 | 2070.3785 | 2051.9201 | 2042.0486 |
| 3.6444 | 1985.9965 | 2038.7505 | 2029.0951 |
| 3.6554 | 1999.8407 | 2025.5883 | 2016.1417 |
| 3.6664 | 2017.8392 | 2012.4331 | 2003.1883 |
| 3.6774 | 1980.9292 | 1999.2846 | 1990.2348 |
| 3.6884 | 1954.7478 | 1986.2697 | 1977.2814 |
| 3.6994 | 2005.5693 | 1973.3641 | 1964.6852 |
| 3.7104 | 1921.4887 | 1960.5915 | 1952.0890 |
| 3.7214 | 1920.2566 | 1947.8245 | 1939.4928 |
| 3.7324 | 1842.9056 | 1935.0630 | 1926.8966 |
| 3.7434 | 1950.0384 | 1922.3068 | 1914.3004 |
| 3.7544 | 1853.9380 | 1909.5555 | 1901.7042 |
| 3.7654 | 1910.8604 | 1896.8091 | 1889.1080 |
| 3.7764 | 1963.9007 | 1884.0674 | 1876.5118 |
| 3.7874 | 1809.3893 | 1871.3301 | 1863.9156 |
| 3.7984 | 1906.7074 | 1858.5971 | 1851.3195 |
| 3.8094 | 1821.7483 | 1845.8683 | 1838.7233 |
| 3.8204 | 1806.6165 | 1833.1434 | 1826.1271 |
| 3.8314 | 1826.3471 | 1820.4224 | 1813.5309 |
| 3.8424 | 1787.1052 | 1807.7051 | 1800.9347 |
| 3.8534 | 1785.0413 | 1794.9913 | 1788.3385 |
| 3.8644 | 1729.4666 | 1782.2810 | 1775.7423 |
| 3.8754 | 1748.3422 | 1770.9852 | 1763.1461 |
| 3.8864 | 1770.2434 | 1760.8381 | 1754.5177 |
| 3.8974 | 1834.1032 | 1752.1052 | 1745.8893 |
| 3.9084 | 1768.0325 | 1743.3753 | 1737.2609 |
| 3.9194 | 1775.9675 | 1734.6483 | 1728.6325 |
| 3.9304 | 1693.0379 | 1725.9242 | 1720.0041 |
| 3.9414 | 1693.9155 | 1717.2027 | 1711.3757 |
| 3.9524 | 1743.7669 | 1708.4839 | 1702.7473 |
| 3.9634 | 1692.3147 | 1699.7676 | 1694.1189 |
| 3.9744 | 1689.5959 | 1691.0538 | 1685.4904 |
| 3.9854 | 1665.7699 | 1682.3424 | 1676.8620 |
| 3.9964 | 1697.0570 | 1673.6334 | 1668.2336 |
| 4.0074 | 1646.8239 | 1664.9265 | 1659.6052 |
| 4.0184 | 1563.4307 | 1656.2219 | 1650.9768 |
| 4.0294 | 1633.7384 | 1647.5194 | 1642.3484 |
| 4.0404 | 1630.5354 | 1638.8190 | 1633.7200 |
| 4.0514 | 1603.6843 | 1630.1206 | 1625.0916 |
| 4.0624 | 1573.8899 | 1621.7128 | 1616.4632 |
| 4.0734 | 1635.1180 | 1613.5411 | 1608.6462 |
| 4.0844 | 1662.3230 | 1605.6598 | 1600.8292 |
| 4.0954 | 1635.5054 | 1597.7804 | 1593.0122 |
| 4.1064 | 1568.1391 | 1589.9027 | 1585.1952 |
| 4.1174 | 1529.6047 | 1582.0268 | 1577.3782 |
| 4.1284 | 1541.9617 | 1574.1526 | 1569.5612 |
| 4.1394 | 1586.7768 | 1566.2800 | 1561.7442 |
| 4.1504 | 1543.3038 | 1558.4091 | 1553.9272 |
| 4.1614 | 1524.4090 | 1550.5397 | 1546.1102 |
| 4.1724 | 1565.4484 | 1542.6719 | 1538.2932 |
| 4.1834 | 1551.6194 | 1534.8057 | 1530.4762 |
| 4.1944 | 1475.7154 | 1526.9409 | 1522.6592 |

Scan List

| Vis. | Dataset Name | Start pos. [°2θ] | End pos. [°2θ] | Step [°2θ] | Meas.Date/Time |
| --- | --- | --- | --- | --- | --- |
| * | 14 Etosha22 Crt 0-0.1cm S3 550C | 2.0054 | 29.9894 | 0.0110 | 12/8/2023 12:03:46 PM |

Peak List

| Pos. [°2θ] | Height [cts] | FWHM Left [°2θ] | d-spacing [Å] | Rel. Int. [%] |
| --- | --- | --- | --- | --- |
| 2.6844 | 1634.45 | 0.1948 | 32.88565 | 100.00 |
| 5.2914 | 127.19 | 0.1732 | 16.68772 | 7.78 |
| 8.6953 | 616.74 | 0.1082 | 10.16119 | 37.73 |
| 10.6148 | 26.39 | 0.5196 | 8.32764 | 1.61 |
| 15.8440 | 188.45 | 0.1948 | 5.58896 | 11.53 |
| 17.6676 | 35.57 | 0.2598 | 5.01600 | 2.18 |
| 19.4371 | 12.86 | 0.5196 | 4.56315 | 0.79 |
| 26.2134 | 114.92 | 0.0866 | 3.39690 | 7.03 |
| 27.4738 | 124.02 | 0.1082 | 3.24386 | 7.59 |

Pattern List

| Visible | Ref.Code | Score | Compound Name | Chem. Formula | Mineral Name | SemiQuant[%] |
| --- | --- | --- | --- | --- | --- | --- |
| * | 04-008-7810 | 45 | Titanium Oxide | Ti O2 | Rutile | 2 |
| * | 04-016-6884 | 17 | Potassium Magnesium Manganese Aluminum Iron Silicon Oxide Hydroxide | K0.8 Mg2.6 Mn0.1 Fe0.2 Al1.3 Si2.8 O10 ( O H )2 | Muscovite-1M | 34 |
| * | 04-011-6751 | 24 | Sodium Aluminum Silicate Hydrate | Na8 Al8 Si16 O48 ( H2 O )8 | Analcime | 6 |
| * | 04-025-4215 | 14 | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide | Mg10.4 V0.36 Mn33.5 Fe0.14 Al0.69 Si6.77 As6.5 P0.3 O54 ( O H )42 | Carlfrancisite | 27 |
| * | 04-017-1621 | 0 | Calcium Magnesium Iron Silicate Hydroxide | Ca2 Mg2.5 Fe2.5 Si8 O22 ( O H )2 | Actinolite | 1 |
| * | 01-082-8023 | 0 | Sodium Magnesium Silicon Oxide Hydrate | Na2 Mg3 ( Si6 O16 ) ( H2 O )7 | Loughlinite | 30 |

Anchor Scan Parameters

Dataset Name	14 Etosha22 Crt 0-0.1cm S3 550C

File name	C:\aeris_data\XRD data\Goldstein\Etosha 2023\Etosha Clay Data\Sample 14\14 Etosha22 Crt 0-0.1cm S3 550C.xrdml

Sample Identification	14 Etosha22 Crt 0-0.1cm S3 550C

Measurement Start Date/Time	12/8/2023 12:03:46 PM

Operator	Instrument

Raw Data Origin	XRD measurement (*.XRDML)

Scan Axis	Gonio

Start Position [°2θ]	2.0054

End Position [°2θ]	29.9894

Step Size [°2θ]	0.0110

Scan Step Time [s]	48.1950

Scan Type	Continuous

PSD Mode	Scanning

PSD Length [°2θ]	5.54

Offset [°2θ]	0.0000

Divergence Slit Type	Fixed

Divergence Slit Size [°]	0.0603

Specimen Length [mm]	10.00

Measurement Temperature [°C]	25.00

Anode Material	Cu

K-α1 [Å]	1.54060

K-α2 [Å]	1.54443

K-β1 [Å]	1.39225

K-A2 / K-A1 Ratio	0.50000

Generator Settings	15 mA, 40 kV

Diffractometer Type	2082464

Diffractometer Number	0

Goniometer Radius [mm]	145.00

Dist. Focus-Diverg. Slit [mm]	95.00

Incident Beam Monochromator	No

Spinning	Yes