14 Etosha 22 crt 0-0.1cm S3 GLYCOL REPORT

Graphics

Graphics

Graphics

Quantitative Results

Phase Sodium Aluminum Silicon Oxide Hydrate

Weight fraction/ %	5.0

Phase Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide

Weight fraction/ %	49.0

Phase Potassium Sodium Iron Magnesium Aluminum Silicate Fluoride Hydroxide

Weight fraction/ %	29.0

Phase Magnesium Aluminum Iron Silicon Oxide Hydroxide Hydrate

Weight fraction/ %	4.0

Phase Magnesium Silicon Oxide Hydroxide Hydrate

Weight fraction/ %	2.0

Phase Potassium Calcium Manganese Aluminum Silicate Hydroxide Hydrate

Weight fraction/ %	4.0

Phase Sodium Magnesium Silicon Oxide Hydrate

Weight fraction/ %	7.0

Multiple Quantitative Results

Scans vs Phases Matrix

| Scan name | Sodium Aluminum Silicon Oxide Hydrate | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide | Potassium Sodium Iron Magnesium Aluminum Silicate Fluoride Hydroxide | Magnesium Aluminum Iron Silicon Oxide Hydroxide Hydrate | Magnesium Silicon Oxide Hydroxide Hydrate | Potassium Calcium Manganese Aluminum Silicate Hydroxide Hydrate | Sodium Magnesium Silicon Oxide Hydrate |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 14 Etosha22 Crt 0-0.1cm S3 glycol | 5.0 | 49.0 | 29.0 | 4.0 | 2.0 | 4.0 | 7.0 |

Anchor Scan Data

| Pos. [°2θ] | Iobs [cts] | Icalc [cts] | Iback [cts] |
| --- | --- | --- | --- |
| 2.0054 | 9357.0000 | 9329.2495 | 9357.0000 |
| 2.0164 | 9371.1072 | 9296.1470 | 9287.2030 |
| 2.0274 | 9218.4838 | 9226.6630 | 9217.4061 |
| 2.0384 | 9196.6357 | 9157.1959 | 9147.6091 |
| 2.0494 | 9168.1780 | 9087.7468 | 9077.8121 |
| 2.0604 | 9291.0831 | 9018.3171 | 9008.0152 |
| 2.0714 | 9040.1829 | 8948.9082 | 8938.2182 |
| 2.0824 | 8936.2355 | 8879.5218 | 8868.4212 |
| 2.0934 | 8883.9479 | 8810.1597 | 8798.6243 |
| 2.1044 | 8958.6991 | 8740.8237 | 8728.8273 |
| 2.1154 | 8908.8496 | 8671.5161 | 8659.0303 |
| 2.1264 | 8945.5005 | 8602.2393 | 8589.2334 |
| 2.1374 | 8807.5634 | 8532.9959 | 8519.4364 |
| 2.1484 | 8944.3019 | 8463.7888 | 8449.6394 |
| 2.1594 | 8728.9508 | 8394.6213 | 8379.8425 |
| 2.1704 | 8803.2773 | 8325.4970 | 8310.0455 |
| 2.1814 | 8603.3599 | 8256.4201 | 8240.2485 |
| 2.1924 | 8579.1504 | 8187.3164 | 8170.4516 |
| 2.2034 | 8491.4867 | 8118.2762 | 8100.5036 |
| 2.2144 | 8570.9469 | 8049.2201 | 8030.5557 |
| 2.2254 | 8397.1858 | 7980.2335 | 7960.6078 |
| 2.2364 | 8493.8378 | 7911.3237 | 7890.6599 |
| 2.2474 | 8418.9705 | 7842.4992 | 7820.7120 |
| 2.2584 | 8248.8019 | 7773.7698 | 7750.7641 |
| 2.2694 | 8195.8466 | 7705.1465 | 7680.8162 |
| 2.2804 | 8138.3584 | 7636.6421 | 7610.8682 |
| 2.2914 | 8201.4936 | 7568.2715 | 7540.9203 |
| 2.3024 | 8221.4292 | 7500.0517 | 7470.9724 |
| 2.3134 | 8174.9027 | 7432.0028 | 7401.0245 |
| 2.3244 | 8141.5541 | 7364.1484 | 7331.0766 |
| 2.3354 | 8072.0885 | 7296.5161 | 7261.1287 |
| 2.3464 | 8026.5693 | 7229.1387 | 7191.1808 |
| 2.3574 | 8017.8328 | 7162.0554 | 7121.2329 |
| 2.3684 | 8037.4617 | 7095.3133 | 7051.2849 |
| 2.3794 | 7986.7483 | 7028.9692 | 6981.3370 |
| 2.3904 | 7907.0000 | 6963.0924 | 6911.3891 |
| 2.4014 | 7841.0708 | 6897.7678 | 6841.4412 |
| 2.4124 | 7738.4449 | 6833.1008 | 6771.4933 |
| 2.4234 | 7693.0482 | 6769.2233 | 6701.5454 |
| 2.4344 | 7618.1475 | 6706.3028 | 6631.5975 |
| 2.4454 | 7650.0374 | 6644.5562 | 6561.6495 |
| 2.4564 | 7675.5044 | 6584.2756 | 6491.7016 |
| 2.4674 | 7494.7846 | 6525.8784 | 6421.7537 |
| 2.4784 | 7426.8097 | 6470.0142 | 6351.8058 |
| 2.4894 | 7483.9282 | 6417.7852 | 6281.8579 |
| 2.5004 | 7596.7920 | 6371.1649 | 6211.9100 |
| 2.5114 | 7576.0570 | 6333.6877 | 6141.9621 |
| 2.5224 | 7453.7856 | 6311.3755 | 6072.0141 |
| 2.5334 | 7418.2301 | 6313.5995 | 6002.0662 |
| 2.5444 | 7405.5570 | 6353.2038 | 5932.1183 |
| 2.5554 | 7302.7443 | 6444.9676 | 5862.1704 |
| 2.5664 | 7279.9838 | 6601.6210 | 5792.2225 |
| 2.5774 | 7287.9390 | 6827.9476 | 5722.1236 |
| 2.5884 | 7365.3368 | 7112.1684 | 5652.0248 |
| 2.5994 | 7294.1858 | 7416.1811 | 5581.9259 |
| 2.6104 | 7405.3540 | 7666.2627 | 5511.8271 |
| 2.6214 | 7231.6411 | 7767.6713 | 5441.7282 |
| 2.6324 | 7188.1608 | 7665.8825 | 5371.6293 |
| 2.6434 | 7107.0777 | 7399.4922 | 5301.5305 |
| 2.6544 | 6925.6676 | 7070.1667 | 5231.4316 |
| 2.6654 | 6758.9557 | 6775.8534 | 5161.3328 |
| 2.6764 | 6715.0010 | 6578.0686 | 5091.2339 |
| 2.6874 | 6594.3589 | 6499.9192 | 5021.1350 |
| 2.6984 | 6484.9867 | 6529.8332 | 4951.0362 |
| 2.7094 | 6416.0157 | 6621.9966 | 4880.9373 |
| 2.7204 | 6371.0433 | 6696.5400 | 4810.8385 |
| 2.7314 | 6234.8289 | 6660.4981 | 4740.7396 |
| 2.7424 | 6015.5949 | 6465.8893 | 4670.6407 |
| 2.7534 | 5798.6480 | 6145.5732 | 4600.5419 |
| 2.7644 | 5540.9542 | 5773.6606 | 4530.2564 |
| 2.7754 | 5379.6873 | 5411.6638 | 4459.9710 |
| 2.7864 | 5073.7659 | 5093.5818 | 4389.6856 |
| 2.7974 | 5022.2655 | 4831.1896 | 4319.4001 |
| 2.8084 | 4873.8515 | 4622.2055 | 4249.1147 |
| 2.8194 | 4550.4857 | 4456.9388 | 4178.8293 |
| 2.8304 | 4496.0324 | 4323.5113 | 4108.5438 |
| 2.8414 | 4309.0442 | 4211.2683 | 4038.2584 |
| 2.8524 | 4139.8422 | 4112.2613 | 3967.9729 |
| 2.8634 | 4089.7758 | 4021.2929 | 3897.6875 |
| 2.8744 | 3954.9739 | 3935.2716 | 3827.4021 |
| 2.8854 | 3845.7886 | 3852.4558 | 3757.1166 |
| 2.8964 | 3682.7168 | 3771.8695 | 3686.8312 |
| 2.9074 | 3605.1583 | 3692.9392 | 3616.5457 |
| 2.9184 | 3497.6091 | 3615.2982 | 3546.2603 |
| 2.9294 | 3431.7522 | 3538.6913 | 3475.9749 |
| 2.9404 | 3477.8259 | 3482.5312 | 3405.6894 |
| 2.9514 | 3338.8712 | 3419.3304 | 3366.8688 |
| 2.9624 | 3228.2095 | 3376.3150 | 3328.0481 |
| 2.9734 | 3309.7384 | 3333.7910 | 3289.2274 |
| 2.9844 | 3132.4597 | 3291.6835 | 3250.4067 |
| 2.9954 | 3078.4690 | 3249.9320 | 3211.5860 |
| 3.0064 | 3073.7630 | 3208.4861 | 3172.7653 |
| 3.0174 | 3063.1072 | 3167.3045 | 3133.9447 |
| 3.0284 | 2999.9941 | 3126.3525 | 3095.1240 |
| 3.0394 | 2968.2320 | 3085.6009 | 3056.3033 |
| 3.0504 | 2916.7792 | 3045.0252 | 3017.4826 |
| 3.0614 | 2883.9558 | 3004.6045 | 2978.6619 |
| 3.0724 | 2930.6971 | 2964.3207 | 2939.8413 |
| 3.0834 | 2853.0255 | 2924.1587 | 2901.0206 |
| 3.0944 | 2780.1859 | 2884.1051 | 2862.1999 |
| 3.1054 | 2883.6037 | 2844.1485 | 2823.3792 |
| 3.1164 | 2852.3077 | 2804.2788 | 2784.5585 |
| 3.1274 | 2714.4218 | 2774.5282 | 2745.7379 |
| 3.1384 | 2655.1814 | 2740.8839 | 2723.0345 |
| 3.1494 | 2663.3127 | 2717.3443 | 2700.3311 |
| 3.1604 | 2656.5354 | 2693.8625 | 2677.6278 |
| 3.1714 | 2666.1494 | 2670.4335 | 2654.9244 |
| 3.1824 | 2560.0969 | 2647.0523 | 2632.2211 |
| 3.1934 | 2564.0885 | 2623.7150 | 2609.5177 |
| 3.2044 | 2557.3972 | 2600.4178 | 2586.8143 |
| 3.2154 | 2564.7040 | 2577.1574 | 2564.1110 |
| 3.2264 | 2541.9557 | 2553.9307 | 2541.4076 |
| 3.2374 | 2512.4277 | 2530.7350 | 2518.7043 |
| 3.2484 | 2502.2778 | 2507.5681 | 2496.0009 |
| 3.2594 | 2465.6342 | 2484.4275 | 2473.2976 |
| 3.2704 | 2450.3358 | 2461.3115 | 2450.5942 |
| 3.2814 | 2406.1288 | 2438.2181 | 2427.8908 |
| 3.2924 | 2434.8451 | 2415.1457 | 2405.1875 |
| 3.3034 | 2426.5683 | 2392.0929 | 2382.4841 |
| 3.3144 | 2356.1067 | 2374.6132 | 2359.7808 |
| 3.3254 | 2298.8053 | 2354.9573 | 2345.9941 |
| 3.3364 | 2294.6180 | 2340.8721 | 2332.2075 |
| 3.3474 | 2340.9892 | 2326.8016 | 2318.4209 |
| 3.3584 | 2328.9690 | 2312.7450 | 2304.6343 |
| 3.3694 | 2289.1809 | 2298.7012 | 2290.8477 |
| 3.3804 | 2270.8545 | 2284.6695 | 2277.0611 |
| 3.3914 | 2245.4071 | 2270.6492 | 2263.2744 |
| 3.4024 | 2251.8043 | 2256.6395 | 2249.4878 |
| 3.4134 | 2251.9361 | 2242.6399 | 2235.7012 |
| 3.4244 | 2217.0914 | 2228.6496 | 2221.9146 |
| 3.4354 | 2166.5319 | 2214.6682 | 2208.1280 |
| 3.4464 | 2142.6101 | 2200.6952 | 2194.3414 |
| 3.4574 | 2086.3599 | 2186.7301 | 2180.5547 |
| 3.4684 | 2058.3471 | 2172.7724 | 2166.7681 |
| 3.4794 | 2098.8791 | 2158.8217 | 2152.9815 |
| 3.4904 | 2138.1195 | 2143.5726 | 2139.1949 |
| 3.5014 | 2148.6716 | 2128.8508 | 2125.4083 |
| 3.5124 | 2130.5354 | 2114.9357 | 2112.2142 |
| 3.5234 | 2044.0295 | 2101.6667 | 2099.0201 |
| 3.5344 | 2025.5860 | 2088.4009 | 2085.8260 |
| 3.5454 | 2021.1888 | 2075.1378 | 2072.6319 |
| 3.5564 | 1998.6740 | 2061.8776 | 2059.4379 |
| 3.5674 | 2001.6893 | 2048.7512 | 2046.2438 |
| 3.5784 | 1996.6662 | 2035.5665 | 2033.0497 |
| 3.5894 | 1941.6460 | 2022.3825 | 2019.8556 |
| 3.6004 | 2016.7355 | 2007.8584 | 2006.6615 |
| 3.6114 | 1970.4956 | 1993.8533 | 1993.4674 |
| 3.6224 | 2001.2139 | 1980.5906 | 1980.2734 |
| 3.6334 | 1958.1219 | 1967.4006 | 1967.0793 |
| 3.6444 | 1837.9223 | 1954.2108 | 1953.8852 |
| 3.6554 | 1900.3658 | 1941.0211 | 1940.6911 |
| 3.6664 | 1869.7787 | 1927.8314 | 1927.4970 |
| 3.6774 | 1967.0571 | 1914.6419 | 1914.3029 |
| 3.6884 | 1908.1548 | 1901.3970 | 1901.1089 |
| 3.6994 | 1873.0010 | 1888.1741 | 1887.8259 |
| 3.7104 | 1806.6421 | 1874.8960 | 1874.5430 |
| 3.7214 | 1844.0354 | 1861.6180 | 1861.2600 |
| 3.7324 | 1808.9528 | 1848.3400 | 1847.9771 |
| 3.7434 | 1717.4533 | 1835.0622 | 1834.6942 |
| 3.7544 | 1856.0959 | 1821.7845 | 1821.4112 |
| 3.7654 | 1744.1121 | 1808.5069 | 1808.1283 |
| 3.7764 | 1831.0340 | 1795.2294 | 1794.8453 |
| 3.7874 | 1663.5132 | 1781.9520 | 1781.5624 |
| 3.7984 | 1747.8314 | 1768.6747 | 1768.2794 |
| 3.8094 | 1700.5418 | 1755.3976 | 1754.9965 |
| 3.8204 | 1795.9071 | 1742.1206 | 1741.7136 |
| 3.8314 | 1752.3156 | 1728.8437 | 1728.4306 |
| 3.8424 | 1621.3137 | 1715.5670 | 1715.1477 |
| 3.8534 | 1700.1033 | 1702.2904 | 1701.8647 |
| 3.8644 | 1708.1268 | 1689.0139 | 1688.5818 |
| 3.8754 | 1620.2635 | 1679.2479 | 1675.2989 |
| 3.8864 | 1687.7655 | 1668.0961 | 1667.6505 |
| 3.8974 | 1709.9361 | 1660.4547 | 1660.0022 |
| 3.9084 | 1626.2743 | 1652.8135 | 1652.3538 |
| 3.9194 | 1627.8584 | 1645.1724 | 1644.7055 |
| 3.9304 | 1543.3206 | 1637.5315 | 1637.0571 |
| 3.9414 | 1564.1219 | 1629.8908 | 1629.4088 |
| 3.9524 | 1573.7714 | 1622.2503 | 1621.7604 |
| 3.9634 | 1554.2900 | 1614.6100 | 1614.1121 |
| 3.9744 | 1515.2100 | 1606.9698 | 1606.4637 |
| 3.9854 | 1591.5398 | 1599.3299 | 1598.8154 |
| 3.9964 | 1577.6962 | 1591.6902 | 1591.1670 |
| 4.0074 | 1559.5113 | 1584.0507 | 1583.5187 |
| 4.0184 | 1485.9558 | 1576.4114 | 1575.8703 |
| 4.0294 | 1515.0452 | 1568.7724 | 1568.2220 |
| 4.0404 | 1494.0984 | 1561.1336 | 1560.5736 |
| 4.0514 | 1566.0118 | 1553.4951 | 1552.9253 |
| 4.0624 | 1560.3353 | 1547.5023 | 1545.2769 |
| 4.0734 | 1517.4002 | 1540.8601 | 1540.2699 |
| 4.0844 | 1547.6018 | 1535.8637 | 1535.2629 |
| 4.0954 | 1503.1760 | 1530.8676 | 1530.2559 |
| 4.1064 | 1460.4277 | 1525.8718 | 1525.2489 |
| 4.1174 | 1458.0472 | 1520.8763 | 1520.2418 |
| 4.1284 | 1415.2783 | 1515.8811 | 1515.2348 |
| 4.1394 | 1441.6795 | 1510.8863 | 1510.2278 |
| 4.1504 | 1479.7168 | 1505.8918 | 1505.2208 |
| 4.1614 | 1449.4100 | 1500.8976 | 1500.2138 |
| 4.1724 | 1443.7414 | 1495.9038 | 1495.2067 |
| 4.1834 | 1449.9646 | 1490.9105 | 1490.1997 |
| 4.1944 | 1429.5010 | 1485.9175 | 1485.1927 |

Scan List

| Vis. | Dataset Name | Start pos. [°2θ] | End pos. [°2θ] | Step [°2θ] | Meas.Date/Time |
| --- | --- | --- | --- | --- | --- |
| * | 14 Etosha22 Crt 0-0.1cm S3 glycol | 2.0054 | 29.9894 | 0.0110 | 12/8/2023 8:55:00 AM |

Peak List

| Pos. [°2θ] | Height [cts] | FWHM Left [°2θ] | d-spacing [Å] | Rel. Int. [%] |
| --- | --- | --- | --- | --- |
| 2.6214 | 1991.91 | 0.0866 | 33.67578 | 100.00 |
| 2.7291 | 1571.65 | 0.0866 | 32.34666 | 78.90 |
| 5.3026 | 212.95 | 0.1732 | 16.65237 | 10.69 |
| 7.1238 | 481.32 | 0.2381 | 12.39875 | 24.16 |
| 8.7006 | 262.58 | 0.1082 | 10.15504 | 13.18 |
| 15.7068 | 290.98 | 0.0649 | 5.63749 | 14.61 |
| 18.1518 | 28.11 | 0.2598 | 4.88326 | 1.41 |
| 19.7618 | 22.00 | 0.5196 | 4.48891 | 1.10 |
| 25.8775 | 248.72 | 0.1299 | 3.44023 | 12.49 |
| 26.6736 | 88.19 | 0.1732 | 3.33933 | 4.43 |
| 27.4677 | 105.24 | 0.1515 | 3.24456 | 5.28 |

Pattern List

| Visible | Ref.Code | Score | Compound Name | Chem. Formula | Mineral Name | SemiQuant[%] |
| --- | --- | --- | --- | --- | --- | --- |
| * | 04-009-3254 | 18 | Sodium Aluminum Silicon Oxide Hydrate | Na8 Al8 Si16 O48 ( H2 O )8 | Analcime | 5 |
| * | 04-025-4215 | 49 | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide | Mg10.4 V0.36 Mn33.5 Fe0.14 Al0.69 Si6.77 As6.5 P0.3 O54 ( O H )42 | Carlfrancisite | 49 |
| * | 01-085-2272 | 55 | Potassium Sodium Iron Magnesium Aluminum Silicate Fluoride Hydroxide | ( K0.93 Na0.04 ) ( Mg2.55 Fe0.21 Al0.24 ) ( Si2.65 Al1.35 O10 ) ( ( O H )1.91 F0.09 ) | Phlogopite-1M | 29 |
| * | 04-018-3208 | 21 | Magnesium Aluminum Iron Silicon Oxide Hydroxide Hydrate | Mg1.0 Fe0.08 Al1.0 Si3.99 O10.2 ( O H )0.8 ( H2 O )3.3 | Palygorskite-M | 4 |
| * | 04-014-4556 | 12 | Magnesium Silicon Oxide Hydroxide Hydrate | Mg4 Si6 O15 ( O H )2 ( H2 O )6 | Sepiolite | 2 |
| * | 04-016-6876 | 42 | Potassium Calcium Manganese Aluminum Silicate Hydroxide Hydrate | K0.38 Ca0.12 Mn2 Al0.62 Si2.71 O8 ( O H )1.33 ( H2 O )1.75 | Ganophyllite | 4 |
| * | 01-082-8023 | 23 | Sodium Magnesium Silicon Oxide Hydrate | Na2 Mg3 ( Si6 O16 ) ( H2 O )7 | Loughlinite | 7 |

Anchor Scan Parameters

Dataset Name	14 Etosha22 Crt 0-0.1cm S3 glycol

File name	C:\aeris_data\XRD data\Goldstein\Etosha 2023\Etosha Clay Data\Sample 14\14 Etosha22 Crt 0-0.1cm S3 glycol.xrdml

Sample Identification	14 Etosha22 Crt 0-0.1cm S3 glycol

Measurement Start Date/Time	12/8/2023 8:55:00 AM

Operator	Instrument

Raw Data Origin	XRD measurement (*.XRDML)

Scan Axis	Gonio

Start Position [°2θ]	2.0054

End Position [°2θ]	29.9894

Step Size [°2θ]	0.0110

Scan Step Time [s]	48.1950

Scan Type	Continuous

PSD Mode	Scanning

PSD Length [°2θ]	5.54

Offset [°2θ]	0.0000

Divergence Slit Type	Fixed

Divergence Slit Size [°]	0.0603

Specimen Length [mm]	10.00

Measurement Temperature [°C]	25.00

Anode Material	Cu

K-α1 [Å]	1.54060

K-α2 [Å]	1.54443

K-β1 [Å]	1.39225

K-A2 / K-A1 Ratio	0.50000

Generator Settings	15 mA, 40 kV

Diffractometer Type	2082464

Diffractometer Number	0

Goniometer Radius [mm]	145.00

Dist. Focus-Diverg. Slit [mm]	95.00

Incident Beam Monochromator	No

Spinning	Yes