15 Etosha 22 Sub 0.1-3 cm S3 550 C REPORT

Graphics

Graphics

Graphics

Quantitative Results

Phase Sodium Aluminum Silicate Hydrate

Weight fraction/ %	3.0

Phase Potassium Iron Magnesium Aluminum Silicate Hydroxide

Weight fraction/ %	6.0

Phase Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide

Weight fraction/ %	21.0

Phase Potassium Magnesium Manganese Aluminum Iron Silicon Oxide Hydroxide

Weight fraction/ %	45.0

Phase Sodium Magnesium Silicon Oxide Hydrate

Weight fraction/ %	11.0

Phase Magnesium Aluminum Silicon Oxide Hydroxide Hydrate

Weight fraction/ %	9.0

Phase Calcium Magnesium Iron Silicate Hydroxide

Weight fraction/ %	4.0

Multiple Quantitative Results

Scans vs Phases Matrix

| Scan name | Sodium Aluminum Silicate Hydrate | Potassium Iron Magnesium Aluminum Silicate Hydroxide | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide | Potassium Magnesium Manganese Aluminum Iron Silicon Oxide Hydroxide | Sodium Magnesium Silicon Oxide Hydrate | Magnesium Aluminum Silicon Oxide Hydroxide Hydrate | Calcium Magnesium Iron Silicate Hydroxide |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 15 Etosha22 Sub 0.1-3cm S3 550C | 3.0 | 6.0 | 21.0 | 45.0 | 11.0 | 9.0 | 4.0 |

Anchor Scan Data

| Pos. [°2θ] | Iobs [cts] | Icalc [cts] | Iback [cts] |
| --- | --- | --- | --- |
| 2.0054 | 9066.0000 | 9050.4580 | 9066.0000 |
| 2.0164 | 8857.4012 | 9015.2138 | 8998.1298 |
| 2.0274 | 8966.2389 | 8947.8870 | 8930.2597 |
| 2.0384 | 8820.1711 | 8880.5864 | 8862.3895 |
| 2.0494 | 8892.8722 | 8813.3136 | 8794.5193 |
| 2.0604 | 8698.5978 | 8746.0705 | 8726.6491 |
| 2.0714 | 8718.8702 | 8678.8591 | 8658.7790 |
| 2.0824 | 8669.2370 | 8611.6815 | 8590.9088 |
| 2.0934 | 8678.6440 | 8544.5401 | 8523.0386 |
| 2.1044 | 8546.5575 | 8477.4374 | 8455.1684 |
| 2.1154 | 8531.4464 | 8410.3761 | 8387.2983 |
| 2.1264 | 8452.6504 | 8343.3593 | 8319.4281 |
| 2.1374 | 8452.2537 | 8276.3902 | 8251.5579 |
| 2.1484 | 8321.7109 | 8209.4725 | 8183.6877 |
| 2.1594 | 8349.4287 | 8142.6101 | 8115.8176 |
| 2.1704 | 8309.4970 | 8075.8073 | 8047.9474 |
| 2.1814 | 8272.5644 | 8009.0688 | 7980.0772 |
| 2.1924 | 8182.2837 | 7942.3081 | 7912.2070 |
| 2.2034 | 8151.4248 | 7875.6123 | 7844.1430 |
| 2.2144 | 8080.6347 | 7808.9064 | 7776.0789 |
| 2.2254 | 8119.6775 | 7742.2891 | 7708.0149 |
| 2.2364 | 8165.4410 | 7675.7682 | 7639.9508 |
| 2.2474 | 7991.0767 | 7609.3524 | 7571.8867 |
| 2.2584 | 7974.9154 | 7543.0513 | 7503.8227 |
| 2.2694 | 7996.1799 | 7476.8757 | 7435.7586 |
| 2.2804 | 8040.4823 | 7410.8376 | 7367.6946 |
| 2.2914 | 8077.1170 | 7344.9507 | 7299.6305 |
| 2.3024 | 7928.7876 | 7279.2306 | 7231.5664 |
| 2.3134 | 7836.1436 | 7213.6949 | 7163.5024 |
| 2.3244 | 7780.7527 | 7148.3642 | 7095.4383 |
| 2.3354 | 7783.7139 | 7083.2629 | 7027.3743 |
| 2.3464 | 7695.8496 | 7018.4197 | 6959.3102 |
| 2.3574 | 7668.3314 | 6953.8698 | 6891.2461 |
| 2.3684 | 7668.1593 | 6889.6569 | 6823.1821 |
| 2.3794 | 7605.7453 | 6825.7619 | 6755.1180 |
| 2.3904 | 7615.8982 | 6762.3212 | 6686.8971 |
| 2.4014 | 7545.9292 | 6699.3612 | 6618.6762 |
| 2.4124 | 7522.1003 | 6637.0764 | 6550.4553 |
| 2.4234 | 7537.5270 | 6575.6250 | 6482.2344 |
| 2.4344 | 7538.5870 | 6515.2140 | 6414.0134 |
| 2.4454 | 7552.4415 | 6456.1120 | 6345.7925 |
| 2.4564 | 7483.9376 | 6398.6641 | 6277.5716 |
| 2.4674 | 7436.2301 | 6343.3059 | 6209.3507 |
| 2.4784 | 7349.1258 | 6290.5778 | 6141.1298 |
| 2.4894 | 7230.3677 | 6241.1346 | 6072.9088 |
| 2.5004 | 7226.3805 | 6195.7503 | 6004.6879 |
| 2.5114 | 7240.2616 | 6155.3131 | 5936.4670 |
| 2.5224 | 7295.1465 | 6120.8090 | 5868.2461 |
| 2.5334 | 7159.9587 | 6093.2902 | 5800.0252 |
| 2.5444 | 7059.4769 | 6073.8277 | 5731.8043 |
| 2.5554 | 7001.7119 | 6063.4466 | 5663.5833 |
| 2.5664 | 6958.2537 | 6063.0452 | 5595.3624 |
| 2.5774 | 6962.1957 | 6073.3018 | 5527.1415 |
| 2.5884 | 6890.3889 | 6094.5696 | 5458.9206 |
| 2.5994 | 6953.8761 | 6126.7644 | 5390.6997 |
| 2.6104 | 6898.5147 | 6169.2416 | 5322.4788 |
| 2.6214 | 6725.1711 | 6220.6609 | 5254.2578 |
| 2.6324 | 6777.1903 | 6278.8279 | 5186.0369 |
| 2.6434 | 6739.5929 | 6340.5122 | 5117.8160 |
| 2.6544 | 6524.7070 | 6401.2616 | 5049.5951 |
| 2.6654 | 6478.1239 | 6455.2830 | 4981.3742 |
| 2.6764 | 6581.9685 | 6495.5388 | 4913.1532 |
| 2.6874 | 6404.4375 | 6514.2583 | 4844.9323 |
| 2.6984 | 6274.7301 | 6503.9977 | 4776.7114 |
| 2.7094 | 6223.7483 | 6459.1206 | 4708.4905 |
| 2.7204 | 6073.5914 | 6377.2013 | 4640.2696 |
| 2.7314 | 5831.9528 | 6259.6966 | 4572.0487 |
| 2.7424 | 5656.3574 | 6111.5279 | 4503.8277 |
| 2.7534 | 5572.1662 | 5939.7312 | 4435.6068 |
| 2.7644 | 5414.2817 | 5752.1612 | 4367.2290 |
| 2.7754 | 5119.5634 | 5556.0357 | 4298.8513 |
| 2.7864 | 5071.6367 | 5357.5629 | 4230.4735 |
| 2.7974 | 4755.0707 | 5161.5406 | 4162.0957 |
| 2.8084 | 4688.8771 | 4971.5066 | 4093.7179 |
| 2.8194 | 4437.6961 | 4789.9135 | 4025.3402 |
| 2.8304 | 4279.3348 | 4618.3141 | 3956.9624 |
| 2.8414 | 4049.4159 | 4457.5248 | 3888.5846 |
| 2.8524 | 3949.7694 | 4307.7675 | 3820.2068 |
| 2.8634 | 3957.4631 | 4168.7945 | 3751.8291 |
| 2.8744 | 3862.8427 | 4040.0040 | 3683.4513 |
| 2.8854 | 3655.4769 | 3920.5469 | 3615.0735 |
| 2.8964 | 3477.7743 | 3809.4240 | 3546.6957 |
| 2.9074 | 3517.3235 | 3705.5704 | 3478.3180 |
| 2.9184 | 3430.4076 | 3607.9239 | 3409.9402 |
| 2.9294 | 3347.7758 | 3515.4778 | 3341.5624 |
| 2.9404 | 3196.7871 | 3442.1511 | 3273.1846 |
| 2.9514 | 3289.5329 | 3373.9931 | 3236.1657 |
| 2.9624 | 3130.9897 | 3323.4633 | 3199.1467 |
| 2.9734 | 3098.6952 | 3275.1570 | 3162.1278 |
| 2.9844 | 3036.8402 | 3228.6121 | 3125.1088 |
| 2.9954 | 3017.1681 | 3183.4606 | 3088.0898 |
| 3.0064 | 3011.1229 | 3139.4151 | 3051.0709 |
| 3.0174 | 2891.1691 | 3096.2533 | 3014.0519 |
| 3.0284 | 2885.4381 | 3053.8053 | 2977.0330 |
| 3.0394 | 2911.2606 | 3011.9414 | 2940.0140 |
| 3.0504 | 2837.9764 | 2970.5627 | 2902.9950 |
| 3.0614 | 2808.6431 | 2929.5935 | 2865.9761 |
| 3.0724 | 2772.3437 | 2888.9748 | 2828.9571 |
| 3.0834 | 2795.7276 | 2848.6602 | 2791.9382 |
| 3.0944 | 2745.0575 | 2808.6125 | 2754.9192 |
| 3.1054 | 2646.0315 | 2768.8014 | 2717.9002 |
| 3.1164 | 2743.1013 | 2729.2014 | 2680.8813 |
| 3.1274 | 2630.5251 | 2698.4693 | 2643.8623 |
| 3.1384 | 2589.2557 | 2668.8965 | 2625.1878 |
| 3.1494 | 2600.1652 | 2648.1571 | 2606.5133 |
| 3.1604 | 2582.3097 | 2627.5586 | 2587.8388 |
| 3.1714 | 2563.0797 | 2607.0888 | 2569.1643 |
| 3.1824 | 2572.0192 | 2586.7364 | 2550.4898 |
| 3.1934 | 2509.7522 | 2566.4915 | 2531.8153 |
| 3.2044 | 2506.0659 | 2546.3452 | 2513.1408 |
| 3.2154 | 2471.8093 | 2526.2896 | 2494.4662 |
| 3.2264 | 2471.2684 | 2506.3175 | 2475.7917 |
| 3.2374 | 2391.5447 | 2486.4222 | 2457.1172 |
| 3.2484 | 2405.1111 | 2466.5980 | 2438.4427 |
| 3.2594 | 2391.7788 | 2446.8395 | 2419.7682 |
| 3.2704 | 2367.7689 | 2427.1418 | 2401.0937 |
| 3.2814 | 2369.0108 | 2407.5004 | 2382.4192 |
| 3.2924 | 2368.4026 | 2387.9115 | 2363.7447 |
| 3.3034 | 2327.5959 | 2368.3712 | 2345.0702 |
| 3.3144 | 2344.5944 | 2348.8239 | 2326.3957 |
| 3.3254 | 2315.4837 | 2329.3129 | 2307.6106 |
| 3.3364 | 2236.9218 | 2309.7890 | 2288.8255 |
| 3.3474 | 2186.0334 | 2290.3019 | 2270.0404 |
| 3.3584 | 2167.3540 | 2270.8492 | 2251.2553 |
| 3.3694 | 2155.2714 | 2251.4288 | 2232.4702 |
| 3.3804 | 2147.6278 | 2232.0386 | 2213.6851 |
| 3.3914 | 2175.1681 | 2212.6767 | 2194.9000 |
| 3.4024 | 2145.6106 | 2193.3413 | 2176.1149 |
| 3.4134 | 2097.3756 | 2174.0310 | 2157.3298 |
| 3.4244 | 2106.6652 | 2154.7442 | 2138.5448 |
| 3.4354 | 2130.9676 | 2135.4796 | 2119.7597 |
| 3.4464 | 2089.4100 | 2116.2358 | 2100.9746 |
| 3.4574 | 2041.5723 | 2097.0117 | 2082.1895 |
| 3.4684 | 2015.7670 | 2077.8061 | 2063.4044 |
| 3.4794 | 2044.5261 | 2058.6181 | 2044.6193 |
| 3.4904 | 1993.7964 | 2039.4467 | 2025.8342 |
| 3.5014 | 1971.7748 | 2023.7638 | 2007.0491 |
| 3.5124 | 2028.9228 | 2008.4913 | 1995.6051 |
| 3.5234 | 2044.3422 | 1996.7056 | 1984.1611 |
| 3.5344 | 2050.9184 | 1984.9402 | 1972.7171 |
| 3.5454 | 2014.6381 | 1973.2831 | 1961.2731 |
| 3.5564 | 1972.6106 | 1961.5404 | 1949.8291 |
| 3.5674 | 1922.7522 | 1949.8574 | 1938.3851 |
| 3.5784 | 1923.3948 | 1938.1342 | 1926.9411 |
| 3.5894 | 1925.6903 | 1926.4214 | 1915.4971 |
| 3.6004 | 1878.8500 | 1914.7185 | 1904.0531 |
| 3.6114 | 1915.2586 | 1903.0250 | 1892.6091 |
| 3.6224 | 1895.7286 | 1891.3404 | 1881.1651 |
| 3.6334 | 1892.0954 | 1879.6644 | 1869.7211 |
| 3.6444 | 1792.4046 | 1867.9966 | 1858.2771 |
| 3.6554 | 1823.4631 | 1856.3366 | 1846.8331 |
| 3.6664 | 1829.5762 | 1844.6840 | 1835.3890 |
| 3.6774 | 1849.8378 | 1833.0385 | 1823.9450 |
| 3.6884 | 1871.4912 | 1821.3999 | 1812.5010 |
| 3.6994 | 1793.6460 | 1809.7678 | 1801.0570 |
| 3.7104 | 1795.7665 | 1798.1419 | 1789.6130 |
| 3.7214 | 1824.5221 | 1786.5220 | 1778.1690 |
| 3.7324 | 1747.0462 | 1774.9079 | 1766.7250 |
| 3.7434 | 1770.2016 | 1763.2992 | 1755.2810 |
| 3.7544 | 1747.1888 | 1751.6958 | 1743.8370 |
| 3.7654 | 1723.7689 | 1740.0975 | 1732.3930 |
| 3.7764 | 1673.0782 | 1728.5040 | 1720.9490 |
| 3.7874 | 1710.6549 | 1716.9152 | 1709.5050 |
| 3.7984 | 1620.3683 | 1705.3309 | 1698.0610 |
| 3.8094 | 1726.1032 | 1693.7510 | 1686.6170 |
| 3.8204 | 1668.7950 | 1682.1751 | 1675.1730 |
| 3.8314 | 1628.7335 | 1670.6033 | 1663.7290 |
| 3.8424 | 1670.1578 | 1659.0354 | 1652.2850 |
| 3.8534 | 1672.2212 | 1647.4711 | 1640.8410 |
| 3.8644 | 1654.9021 | 1635.9104 | 1629.3970 |
| 3.8754 | 1583.1632 | 1626.4243 | 1617.9529 |
| 3.8864 | 1598.4602 | 1617.1773 | 1610.8869 |
| 3.8974 | 1623.0688 | 1610.0047 | 1603.8209 |
| 3.9084 | 1584.5811 | 1602.8351 | 1596.7549 |
| 3.9194 | 1631.5929 | 1595.6685 | 1589.6889 |
| 3.9304 | 1604.6411 | 1588.5049 | 1582.6229 |
| 3.9414 | 1630.7374 | 1581.3440 | 1575.5569 |
| 3.9524 | 1587.2168 | 1574.1859 | 1568.4909 |
| 3.9634 | 1638.2242 | 1567.0303 | 1561.4249 |
| 3.9744 | 1573.8019 | 1559.8774 | 1554.3588 |
| 3.9854 | 1580.9292 | 1552.7269 | 1547.2928 |
| 3.9964 | 1556.8417 | 1545.5788 | 1540.2268 |
| 4.0074 | 1553.3028 | 1538.4330 | 1533.1608 |
| 4.0184 | 1484.2286 | 1531.2895 | 1526.0948 |
| 4.0294 | 1498.9380 | 1524.1481 | 1519.0288 |
| 4.0404 | 1482.5600 | 1517.0089 | 1511.9628 |
| 4.0514 | 1505.1623 | 1509.8717 | 1504.8968 |
| 4.0624 | 1515.9164 | 1503.1006 | 1497.8308 |
| 4.0734 | 1475.4966 | 1496.3729 | 1491.5343 |
| 4.0844 | 1511.0133 | 1490.0112 | 1485.2378 |
| 4.0954 | 1537.3648 | 1483.6513 | 1478.9413 |
| 4.1064 | 1540.3530 | 1477.2933 | 1472.6449 |
| 4.1174 | 1521.6814 | 1470.9370 | 1466.3484 |
| 4.1284 | 1499.1131 | 1464.5824 | 1460.0519 |
| 4.1394 | 1462.8505 | 1458.2295 | 1453.7555 |
| 4.1504 | 1433.0973 | 1451.8782 | 1447.4590 |
| 4.1614 | 1439.9518 | 1445.5286 | 1441.1625 |
| 4.1724 | 1462.0959 | 1439.1806 | 1434.8660 |
| 4.1834 | 1424.3540 | 1432.8341 | 1428.5696 |
| 4.1944 | 1395.5408 | 1426.4891 | 1422.2731 |

Scan List

| Vis. | Dataset Name | Start pos. [°2θ] | End pos. [°2θ] | Step [°2θ] | Meas.Date/Time |
| --- | --- | --- | --- | --- | --- |
| * | 15 Etosha22 Sub 0.1-3cm S3 550C | 2.0054 | 29.9894 | 0.0110 | 12/8/2023 12:14:13 PM |

Peak List

| Pos. [°2θ] | Height [cts] | FWHM Left [°2θ] | d-spacing [Å] | Rel. Int. [%] |
| --- | --- | --- | --- | --- |
| 2.7087 | 1566.08 | 0.1948 | 32.59107 | 100.00 |
| 5.2762 | 116.41 | 0.1732 | 16.73578 | 7.43 |
| 8.7153 | 1044.89 | 0.1732 | 10.13787 | 66.72 |
| 10.5901 | 38.20 | 0.4330 | 8.34697 | 2.44 |
| 15.7979 | 752.26 | 0.1732 | 5.60518 | 48.03 |
| 17.6011 | 85.11 | 0.1732 | 5.03478 | 5.43 |
| 18.2519 | 66.06 | 0.1732 | 4.85670 | 4.22 |
| 19.5438 | 47.57 | 0.3464 | 4.53848 | 3.04 |
| 25.9854 | 434.14 | 0.1732 | 3.42618 | 27.72 |
| 26.7095 | 233.91 | 0.1299 | 3.33492 | 14.94 |
| 27.4697 | 340.61 | 0.1732 | 3.24434 | 21.75 |

Pattern List

| Visible | Ref.Code | Score | Compound Name | Chem. Formula | Mineral Name | SemiQuant[%] |
| --- | --- | --- | --- | --- | --- | --- |
| * | 00-041-1478 | 62 | Sodium Aluminum Silicate Hydrate | Na ( Si2 Al ) O6 · H2 O | Analcime | 3 |
| * | 00-042-1437 | 36 | Potassium Iron Magnesium Aluminum Silicate Hydroxide | K ( Mg , Fe )3 ( Al , Fe ) Si3 O10 ( O H , F )2 | Phlogopite-1M, Fe+2-bearing | 6 |
| * | 04-025-4215 | 23 | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide | Mg10.4 V0.36 Mn33.5 Fe0.14 Al0.69 Si6.77 As6.5 P0.3 O54 ( O H )42 | Carlfrancisite | 21 |
| * | 04-016-6884 | 11 | Potassium Magnesium Manganese Aluminum Iron Silicon Oxide Hydroxide | K0.8 Mg2.6 Mn0.1 Fe0.2 Al1.3 Si2.8 O10 ( O H )2 | Muscovite-1M | 45 |
| * | 01-082-8023 | 1 | Sodium Magnesium Silicon Oxide Hydrate | Na2 Mg3 ( Si6 O16 ) ( H2 O )7 | Loughlinite | 11 |
| * | 04-013-5979 | 15 | Magnesium Aluminum Silicon Oxide Hydroxide Hydrate | Mg Al Si4 O10 ( O H ) ( H2 O )4 | Palygorskite-M | 9 |
| * | 04-017-1621 | 0 | Calcium Magnesium Iron Silicate Hydroxide | Ca2 Mg2.5 Fe2.5 Si8 O22 ( O H )2 | Actinolite | 4 |

Anchor Scan Parameters

Dataset Name	15 Etosha22 Sub 0.1-3cm S3 550C

File name	C:\aeris_data\XRD data\Goldstein\Etosha 2023\Etosha Clay Data\Sample 15\15 Etosha22 Sub 0.1-3cm S3 550C.xrdml

Sample Identification	15 Etosha22 Sub 0.1-3cm S3 550C

Measurement Start Date/Time	12/8/2023 12:14:13 PM

Operator	Instrument

Raw Data Origin	XRD measurement (*.XRDML)

Scan Axis	Gonio

Start Position [°2θ]	2.0054

End Position [°2θ]	29.9894

Step Size [°2θ]	0.0110

Scan Step Time [s]	48.1950

Scan Type	Continuous

PSD Mode	Scanning

PSD Length [°2θ]	5.54

Offset [°2θ]	0.0000

Divergence Slit Type	Fixed

Divergence Slit Size [°]	0.0603

Specimen Length [mm]	10.00

Measurement Temperature [°C]	25.00

Anode Material	Cu

K-α1 [Å]	1.54060

K-α2 [Å]	1.54443

K-β1 [Å]	1.39225

K-A2 / K-A1 Ratio	0.50000

Generator Settings	15 mA, 40 kV

Diffractometer Type	2082464

Diffractometer Number	0

Goniometer Radius [mm]	145.00

Dist. Focus-Diverg. Slit [mm]	95.00

Incident Beam Monochromator	No

Spinning	Yes