16 Etosha 22 moisub 3-15 cm S3 400 C

Graphics

Graphics

Graphics

Quantitative Results

Phase Sodium Aluminum Silicate Hydrate

Weight fraction/ %	23.0

Phase Potassium Iron Magnesium Aluminum Silicate Hydroxide

Weight fraction/ %	7.0

Phase Titanium Oxide

Weight fraction/ %	5.0

Phase Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide

Weight fraction/ %	30.0

Phase Sodium Magnesium Silicon Oxide Hydrate

Weight fraction/ %	11.0

Phase Magnesium Aluminum Iron Silicate Hydroxide Hydrate

Weight fraction/ %	5.0

Phase Magnesium Silicon Oxide Hydroxide Hydrate

Weight fraction/ %	11.0

Phase Calcium Magnesium Iron Silicate Hydroxide

Weight fraction/ %	7.0

Multiple Quantitative Results

Scans vs Phases Matrix

| Scan name | Sodium Aluminum Silicate Hydrate | Potassium Iron Magnesium Aluminum Silicate Hydroxide | Titanium Oxide | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide | Sodium Magnesium Silicon Oxide Hydrate | Magnesium Aluminum Iron Silicate Hydroxide Hydrate | Magnesium Silicon Oxide Hydroxide Hydrate | Calcium Magnesium Iron Silicate Hydroxide |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 16 Etosha22 moisub 3-15cm S3 400C | 23.0 | 7.0 | 5.0 | 30.0 | 11.0 | 5.0 | 11.0 | 7.0 |

Anchor Scan Data

| Pos. [°2θ] | Iobs [cts] | Icalc [cts] | Iback [cts] |
| --- | --- | --- | --- |
| 2.0054 | 5487.0000 | 5467.8872 | 5487.0000 |
| 2.0164 | 5390.7217 | 5443.1042 | 5443.1042 |
| 2.0274 | 5288.0246 | 5399.2084 | 5399.2084 |
| 2.0384 | 5284.0590 | 5355.3126 | 5355.3126 |
| 2.0494 | 5154.7542 | 5311.4168 | 5311.4168 |
| 2.0604 | 5145.8210 | 5267.5210 | 5267.5210 |
| 2.0714 | 5075.1416 | 5223.6252 | 5223.6252 |
| 2.0824 | 4992.8717 | 5179.7295 | 5179.7295 |
| 2.0934 | 5028.7886 | 5135.8337 | 5135.8337 |
| 2.1044 | 4977.0177 | 5091.9379 | 5091.9379 |
| 2.1154 | 4940.5752 | 5048.0421 | 5048.0421 |
| 2.1264 | 4913.8673 | 5004.1463 | 5004.1463 |
| 2.1374 | 4940.7227 | 4960.2505 | 4960.2505 |
| 2.1484 | 4897.7847 | 4916.3547 | 4916.3547 |
| 2.1594 | 4796.4936 | 4872.4589 | 4872.4589 |
| 2.1704 | 4772.0280 | 4828.5631 | 4828.5631 |
| 2.1814 | 4791.4228 | 4784.6673 | 4784.6673 |
| 2.1924 | 4812.2694 | 4745.9819 | 4740.7715 |
| 2.2034 | 4688.1858 | 4708.8423 | 4708.8423 |
| 2.2144 | 4544.2694 | 4676.9130 | 4676.9130 |
| 2.2254 | 4570.9784 | 4644.9838 | 4644.9838 |
| 2.2364 | 4599.6091 | 4613.0545 | 4613.0545 |
| 2.2474 | 4541.0000 | 4581.1253 | 4581.1253 |
| 2.2584 | 4506.5113 | 4549.1960 | 4549.1960 |
| 2.2694 | 4411.3304 | 4517.2668 | 4517.2668 |
| 2.2804 | 4386.8545 | 4485.3375 | 4485.3375 |
| 2.2914 | 4415.1829 | 4453.4083 | 4453.4083 |
| 2.3024 | 4475.1327 | 4421.4790 | 4421.4790 |
| 2.3134 | 4382.3058 | 4389.5498 | 4389.5498 |
| 2.3244 | 4345.6637 | 4357.6205 | 4357.6205 |
| 2.3354 | 4361.3953 | 4325.6913 | 4325.6913 |
| 2.3464 | 4291.4730 | 4293.7620 | 4293.7620 |
| 2.3574 | 4246.8741 | 4261.8328 | 4261.8328 |
| 2.3684 | 4181.4395 | 4229.9035 | 4229.9035 |
| 2.3794 | 4180.0875 | 4200.5415 | 4197.9743 |
| 2.3904 | 4239.0605 | 4171.9411 | 4171.9411 |
| 2.4014 | 4142.3009 | 4145.9080 | 4145.9080 |
| 2.4124 | 4127.0344 | 4119.8749 | 4119.8749 |
| 2.4234 | 4104.5103 | 4093.8418 | 4093.8418 |
| 2.4344 | 3978.2065 | 4067.8087 | 4067.8087 |
| 2.4454 | 4031.0138 | 4041.7756 | 4041.7756 |
| 2.4564 | 4050.6853 | 4015.7425 | 4015.7425 |
| 2.4674 | 3942.3422 | 3989.7094 | 3989.7094 |
| 2.4784 | 3896.4980 | 3963.6762 | 3963.6762 |
| 2.4894 | 3971.4071 | 3937.6431 | 3937.6431 |
| 2.5004 | 3933.6106 | 3911.6100 | 3911.6100 |
| 2.5114 | 3922.9312 | 3885.5769 | 3885.5769 |
| 2.5224 | 3911.2320 | 3859.5438 | 3859.5438 |
| 2.5334 | 3856.6106 | 3833.5107 | 3833.5107 |
| 2.5444 | 3879.3176 | 3807.4776 | 3807.4776 |
| 2.5554 | 3759.8820 | 3781.4445 | 3781.4445 |
| 2.5664 | 3757.2508 | 3758.1103 | 3755.4114 |
| 2.5774 | 3728.1081 | 3735.5768 | 3735.5768 |
| 2.5884 | 3703.8456 | 3715.7422 | 3715.7422 |
| 2.5994 | 3726.9469 | 3695.9076 | 3695.9076 |
| 2.6104 | 3733.6760 | 3676.0731 | 3676.0731 |
| 2.6214 | 3706.4680 | 3656.2385 | 3656.2385 |
| 2.6324 | 3676.4852 | 3636.4039 | 3636.4039 |
| 2.6434 | 3596.9990 | 3616.5693 | 3616.5693 |
| 2.6544 | 3618.0369 | 3596.7348 | 3596.7348 |
| 2.6654 | 3635.5251 | 3576.9002 | 3576.9002 |
| 2.6764 | 3560.0246 | 3557.0656 | 3557.0656 |
| 2.6874 | 3589.8673 | 3537.2310 | 3537.2310 |
| 2.6984 | 3572.9292 | 3517.3965 | 3517.3965 |
| 2.7094 | 3514.2291 | 3497.5619 | 3497.5619 |
| 2.7204 | 3542.5438 | 3477.7273 | 3477.7273 |
| 2.7314 | 3479.1799 | 3457.8928 | 3457.8928 |
| 2.7424 | 3466.9410 | 3438.0582 | 3438.0582 |
| 2.7534 | 3417.0167 | 3419.5346 | 3418.2236 |
| 2.7644 | 3342.5457 | 3401.4000 | 3401.4000 |
| 2.7754 | 3416.1770 | 3384.5765 | 3384.5765 |
| 2.7864 | 3469.2699 | 3367.7529 | 3367.7529 |
| 2.7974 | 3387.3894 | 3350.9294 | 3350.9294 |
| 2.8084 | 3383.1780 | 3334.1058 | 3334.1058 |
| 2.8194 | 3306.6893 | 3317.2823 | 3317.2823 |
| 2.8304 | 3346.9351 | 3300.4587 | 3300.4587 |
| 2.8414 | 3280.9410 | 3283.6351 | 3283.6351 |
| 2.8524 | 3273.1608 | 3266.8116 | 3266.8116 |
| 2.8634 | 3336.2743 | 3249.9880 | 3249.9880 |
| 2.8744 | 3257.4366 | 3233.1645 | 3233.1645 |
| 2.8854 | 3237.3009 | 3216.3409 | 3216.3409 |
| 2.8964 | 3275.8274 | 3199.5174 | 3199.5174 |
| 2.9074 | 3219.1337 | 3182.6938 | 3182.6938 |
| 2.9184 | 3234.2060 | 3165.8703 | 3165.8703 |
| 2.9294 | 3144.6962 | 3149.0467 | 3149.0467 |
| 2.9404 | 3078.2370 | 3132.2231 | 3132.2231 |
| 2.9514 | 3129.8211 | 3115.3996 | 3115.3996 |
| 2.9624 | 3186.9690 | 3098.5760 | 3098.5760 |
| 2.9734 | 3101.4297 | 3081.7525 | 3081.7525 |
| 2.9844 | 3043.4267 | 3064.9289 | 3064.9289 |
| 2.9954 | 2994.0177 | 3048.1054 | 3048.1054 |
| 3.0064 | 3096.3599 | 3031.2818 | 3031.2818 |
| 3.0174 | 2973.4612 | 3014.4582 | 3014.4582 |
| 3.0284 | 2948.0266 | 2997.6347 | 2997.6347 |
| 3.0394 | 3045.1249 | 2980.8111 | 2980.8111 |
| 3.0504 | 2974.7674 | 2963.9876 | 2963.9876 |
| 3.0614 | 2913.7817 | 2947.1640 | 2947.1640 |
| 3.0724 | 2895.1903 | 2930.3405 | 2930.3405 |
| 3.0834 | 2922.9312 | 2913.5169 | 2913.5169 |
| 3.0944 | 2915.4292 | 2896.6933 | 2896.6933 |
| 3.1054 | 2812.7896 | 2879.8698 | 2879.8698 |
| 3.1164 | 2839.4828 | 2863.0462 | 2863.0462 |
| 3.1274 | 2854.1918 | 2846.1847 | 2846.2227 |
| 3.1384 | 2877.0413 | 2829.3120 | 2829.3120 |
| 3.1494 | 2816.0256 | 2812.4014 | 2812.4014 |
| 3.1604 | 2769.6755 | 2795.4907 | 2795.4907 |
| 3.1714 | 2737.6519 | 2778.5800 | 2778.5800 |
| 3.1824 | 2695.9086 | 2761.6694 | 2761.6694 |
| 3.1934 | 2721.6106 | 2744.7587 | 2744.7587 |
| 3.2044 | 2687.2822 | 2727.8481 | 2727.8481 |
| 3.2154 | 2676.7198 | 2710.9374 | 2710.9374 |
| 3.2264 | 2639.3127 | 2694.0268 | 2694.0268 |
| 3.2374 | 2584.5978 | 2677.1161 | 2677.1161 |
| 3.2484 | 2586.0556 | 2660.2055 | 2660.2055 |
| 3.2594 | 2610.6165 | 2643.2948 | 2643.2948 |
| 3.2704 | 2616.5192 | 2626.3842 | 2626.3842 |
| 3.2814 | 2613.0000 | 2609.4735 | 2609.4735 |
| 3.2924 | 2614.7522 | 2592.5628 | 2592.5628 |
| 3.3034 | 2615.6490 | 2575.6522 | 2575.6522 |
| 3.3144 | 2552.4695 | 2559.9502 | 2558.7415 |
| 3.3254 | 2501.4218 | 2544.6068 | 2544.6068 |
| 3.3364 | 2507.4346 | 2530.4721 | 2530.4721 |
| 3.3474 | 2500.9892 | 2516.3374 | 2516.3374 |
| 3.3584 | 2482.3156 | 2502.2026 | 2502.2026 |
| 3.3694 | 2463.9577 | 2488.0679 | 2488.0679 |
| 3.3804 | 2451.0083 | 2473.9332 | 2473.9332 |
| 3.3914 | 2440.2301 | 2459.7985 | 2459.7985 |
| 3.4024 | 2422.8786 | 2445.6637 | 2445.6637 |
| 3.4134 | 2449.2871 | 2431.5290 | 2431.5290 |
| 3.4244 | 2438.4985 | 2417.3943 | 2417.3943 |
| 3.4354 | 2356.1839 | 2403.2596 | 2403.2596 |
| 3.4464 | 2360.4381 | 2389.1248 | 2389.1248 |
| 3.4574 | 2322.1357 | 2374.9901 | 2374.9901 |
| 3.4684 | 2308.7537 | 2360.8554 | 2360.8554 |
| 3.4794 | 2326.8820 | 2346.7207 | 2346.7207 |
| 3.4904 | 2332.2965 | 2332.5859 | 2332.5859 |
| 3.5014 | 2302.4356 | 2318.8102 | 2318.4512 |
| 3.5124 | 2332.8196 | 2305.1410 | 2305.1410 |
| 3.5234 | 2292.7374 | 2291.8307 | 2291.8307 |
| 3.5344 | 2264.5831 | 2278.5296 | 2278.5205 |
| 3.5454 | 2279.1357 | 2265.3241 | 2265.2102 |
| 3.5564 | 2268.1401 | 2252.0199 | 2251.9000 |
| 3.5674 | 2201.6283 | 2238.7641 | 2238.5897 |
| 3.5784 | 2299.9465 | 2225.4561 | 2225.2795 |
| 3.5894 | 2199.4159 | 2212.1481 | 2211.9692 |
| 3.6004 | 2181.4661 | 2198.8402 | 2198.6590 |
| 3.6114 | 2165.7542 | 2185.5324 | 2185.3487 |
| 3.6224 | 2090.6165 | 2172.2246 | 2172.0385 |
| 3.6334 | 2097.7532 | 2158.9168 | 2158.7282 |
| 3.6444 | 2097.1804 | 2145.6624 | 2145.4180 |
| 3.6554 | 2094.3127 | 2132.3897 | 2132.1078 |
| 3.6664 | 2126.5261 | 2119.0866 | 2118.7975 |
| 3.6774 | 2097.2704 | 2105.7797 | 2105.4873 |
| 3.6884 | 2065.5841 | 2093.2627 | 2092.1770 |
| 3.6994 | 2115.5693 | 2080.9801 | 2080.6809 |
| 3.7104 | 2046.8756 | 2069.4875 | 2069.1848 |
| 3.7214 | 2127.9882 | 2057.9949 | 2057.6887 |
| 3.7324 | 2046.7492 | 2046.5024 | 2046.1926 |
| 3.7434 | 2054.1298 | 2035.0100 | 2034.6965 |
| 3.7544 | 2062.6342 | 2023.5177 | 2023.2004 |
| 3.7654 | 1976.9754 | 2012.0254 | 2011.7043 |
| 3.7764 | 1964.2114 | 2000.5332 | 2000.2082 |
| 3.7874 | 1974.9027 | 1989.0411 | 1988.7121 |
| 3.7984 | 1986.8658 | 1977.5490 | 1977.2160 |
| 3.8094 | 1947.8427 | 1966.0571 | 1965.7199 |
| 3.8204 | 1939.7095 | 1954.5652 | 1954.2238 |
| 3.8314 | 1997.6293 | 1943.0734 | 1942.7277 |
| 3.8424 | 1962.3171 | 1931.5817 | 1931.2316 |
| 3.8534 | 1915.6873 | 1920.0902 | 1919.7355 |
| 3.8644 | 1935.6003 | 1908.5987 | 1908.2394 |
| 3.8754 | 1880.5841 | 1897.1073 | 1896.7433 |
| 3.8864 | 1862.5133 | 1885.6160 | 1885.2472 |
| 3.8974 | 1914.8672 | 1874.1248 | 1873.7511 |
| 3.9084 | 1870.1986 | 1862.6337 | 1862.2550 |
| 3.9194 | 1829.0973 | 1851.1427 | 1850.7589 |
| 3.9304 | 1789.3579 | 1839.6518 | 1839.2628 |
| 3.9414 | 1842.6529 | 1828.1611 | 1827.7667 |
| 3.9524 | 1833.5383 | 1816.6705 | 1816.2706 |
| 3.9634 | 1781.0098 | 1805.1800 | 1804.7744 |
| 3.9744 | 1822.4076 | 1793.6896 | 1793.2783 |
| 3.9854 | 1859.7876 | 1782.1994 | 1781.7822 |
| 3.9964 | 1766.1804 | 1770.7093 | 1770.2861 |
| 4.0074 | 1750.3933 | 1759.2193 | 1758.7900 |
| 4.0184 | 1749.4779 | 1747.7295 | 1747.2939 |
| 4.0294 | 1785.0777 | 1736.2399 | 1735.7978 |
| 4.0404 | 1779.5540 | 1724.7504 | 1724.3017 |
| 4.0514 | 1674.7257 | 1713.2611 | 1712.8056 |
| 4.0624 | 1702.6544 | 1703.5381 | 1701.3095 |
| 4.0734 | 1700.9390 | 1694.3392 | 1693.8697 |
| 4.0844 | 1672.3496 | 1686.9067 | 1686.4299 |
| 4.0954 | 1720.7001 | 1679.4744 | 1678.9901 |
| 4.1064 | 1708.7114 | 1672.0423 | 1671.5502 |
| 4.1174 | 1677.5959 | 1664.6103 | 1664.1104 |
| 4.1284 | 1701.4887 | 1657.1786 | 1656.6706 |
| 4.1394 | 1684.3923 | 1649.7471 | 1649.2308 |
| 4.1504 | 1634.3525 | 1642.3158 | 1641.7909 |
| 4.1614 | 1648.9499 | 1634.8848 | 1634.3511 |
| 4.1724 | 1689.0904 | 1627.4540 | 1626.9113 |
| 4.1834 | 1644.2566 | 1620.0235 | 1619.4715 |
| 4.1944 | 1628.5674 | 1612.5932 | 1612.0317 |

Scan List

| Vis. | Dataset Name | Start pos. [°2θ] | End pos. [°2θ] | Step [°2θ] | Meas.Date/Time |
| --- | --- | --- | --- | --- | --- |
| * | 16 Etosha22 moisub 3-15cm S3 400C | 2.0054 | 29.9894 | 0.0110 | 12/7/2023 3:32:05 PM |

Peak List

| Pos. [°2θ] | Height [cts] | FWHM Left [°2θ] | d-spacing [Å] | Rel. Int. [%] |
| --- | --- | --- | --- | --- |
| 5.2760 | 121.00 | 0.1732 | 16.73638 | 9.69 |
| 7.1020 | 64.99 | 0.3464 | 12.43675 | 5.20 |
| 8.7653 | 682.92 | 0.1948 | 10.08020 | 54.69 |
| 10.5014 | 25.81 | 0.5196 | 8.41733 | 2.07 |
| 15.8024 | 1248.77 | 0.1299 | 5.60358 | 100.00 |
| 17.6700 | 56.27 | 0.2598 | 5.01532 | 4.51 |
| 18.2462 | 132.63 | 0.1515 | 4.85821 | 10.62 |
| 19.6837 | 41.63 | 0.6061 | 4.50654 | 3.33 |
| 23.4293 | 32.63 | 0.1299 | 3.79387 | 2.61 |
| 24.2574 | 55.77 | 0.2165 | 3.66620 | 4.47 |
| 25.9817 | 687.80 | 0.1732 | 3.42667 | 55.08 |
| 26.7132 | 283.64 | 0.1732 | 3.33447 | 22.71 |
| 27.5603 | 294.10 | 0.0758 | 3.23387 | 23.55 |

Pattern List

| Visible | Ref.Code | Score | Compound Name | Chem. Formula | Mineral Name | SemiQuant[%] |
| --- | --- | --- | --- | --- | --- | --- |
| * | 01-072-4625 | 72 | Sodium Aluminum Silicate Hydrate | Na Al ( Si2 O6 ) ( H2 O ) | Analcime | 23 |
| * | 00-042-1437 | 44 | Potassium Iron Magnesium Aluminum Silicate Hydroxide | K ( Mg , Fe )3 ( Al , Fe ) Si3 O10 ( O H , F )2 | Phlogopite-1M, Fe+2-bearing | 7 |
| * | 04-016-0561 | 53 | Titanium Oxide | Ti O2 | Rutile | 5 |
| * | 04-025-4215 | 7 | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide | Mg10.4 V0.36 Mn33.5 Fe0.14 Al0.69 Si6.77 As6.5 P0.3 O54 ( O H )42 | Carlfrancisite | 30 |
| * | 01-082-8023 | 3 | Sodium Magnesium Silicon Oxide Hydrate | Na2 Mg3 ( Si6 O16 ) ( H2 O )7 | Loughlinite | 11 |
| * | 01-076-7133 | 15 | Magnesium Aluminum Iron Silicate Hydroxide Hydrate | ( Mg2.09 Al1.92 Fe0.11 ) ( ( Si7.8 Al0.2 ) ( H2 O )4 O20 ) ( O H )2 ( H2 O )4.48 | Palygorskite-M | 5 |
| * | 04-016-3203 | 3 | Magnesium Silicon Oxide Hydroxide Hydrate | Mg4 Si6 O15 ( O H )2 ( H2 O )6 | Sepiolite | 11 |
| * | 04-017-1621 | 9 | Calcium Magnesium Iron Silicate Hydroxide | Ca2 Mg2.5 Fe2.5 Si8 O22 ( O H )2 | Actinolite | 7 |

Anchor Scan Parameters

Dataset Name	16 Etosha22 moisub 3-15cm S3 400C

File name	C:\aeris_data\XRD data\Goldstein\Etosha 2023\Etosha Clay Data\Sample 16\16 Etosha22 moisub 3-15cm S3 400C.xrdml

Sample Identification	16 Etosha22 moisub 3-15cm S3 400C

Measurement Start Date/Time	12/7/2023 3:32:05 PM

Operator	Instrument

Raw Data Origin	XRD measurement (*.XRDML)

Scan Axis	Gonio

Start Position [°2θ]	2.0054

End Position [°2θ]	29.9894

Step Size [°2θ]	0.0110

Scan Step Time [s]	48.1950

Scan Type	Continuous

PSD Mode	Scanning

PSD Length [°2θ]	5.54

Offset [°2θ]	0.0000

Divergence Slit Type	Fixed

Divergence Slit Size [°]	0.0603

Specimen Length [mm]	10.00

Measurement Temperature [°C]	25.00

Anode Material	Cu

K-α1 [Å]	1.54060

K-α2 [Å]	1.54443

K-β1 [Å]	1.39225

K-A2 / K-A1 Ratio	0.50000

Generator Settings	15 mA, 40 kV

Diffractometer Type	2082464

Diffractometer Number	0

Goniometer Radius [mm]	145.00

Dist. Focus-Diverg. Slit [mm]	95.00

Incident Beam Monochromator	No

Spinning	Yes