16 Etosha 22 moisub 3-15 cm S3 550 C REPORT

Graphics

Graphics

Graphics

Quantitative Results

Phase Sodium Aluminum Silicate Hydrate

Weight fraction/ %	10.0

Phase Potassium Sodium Magnesium Aluminum Iron Silicon Titanium Oxide Fluoride Hydroxide

Weight fraction/ %	27.0

Phase Titanium Antimony Vanadium Oxide

Weight fraction/ %	12.0

Phase Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide

Weight fraction/ %	14.0

Phase Potassium Sodium Aluminum Silicate

Weight fraction/ %	6.0

Phase Potassium Sodium Aluminum Silicate

Weight fraction/ %	30.0

Phase Calcium Magnesium Iron Silicate Hydroxide

Weight fraction/ %	1.0

Multiple Quantitative Results

Scans vs Phases Matrix

| Scan name | Sodium Aluminum Silicate Hydrate | Potassium Sodium Magnesium Aluminum Iron Silicon Titanium Oxide Fluoride Hydroxide | Titanium Antimony Vanadium Oxide | Sodium Magnesium Silicon Oxide Hydrate | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide | Potassium Sodium Aluminum Silicate | Potassium Sodium Aluminum Silicate | Calcium Magnesium Iron Silicate Hydroxide |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 16 Etosha22 moisub 3-15cm S3 550C | 10.0 | 27.0 | 12.0 | 0.0 | 14.0 | 6.0 | 30.0 | 1.0 |

Anchor Scan Data

| Pos. [°2θ] | Iobs [cts] | Icalc [cts] | Iback [cts] |
| --- | --- | --- | --- |
| 2.0054 | 8625.0000 | 8601.9280 | 8625.0000 |
| 2.0164 | 8602.2291 | 8574.2237 | 8561.8689 |
| 2.0274 | 8695.7394 | 8511.4835 | 8498.7379 |
| 2.0384 | 8490.6504 | 8448.7619 | 8435.6068 |
| 2.0494 | 8574.5939 | 8386.0603 | 8372.4758 |
| 2.0604 | 8361.8048 | 8323.3800 | 8309.3447 |
| 2.0714 | 8476.5015 | 8260.7224 | 8246.2137 |
| 2.0824 | 8412.2566 | 8198.0889 | 8183.0826 |
| 2.0934 | 8329.3117 | 8135.4813 | 8119.9516 |
| 2.1044 | 8315.2566 | 8072.9015 | 8056.8205 |
| 2.1154 | 8239.7257 | 8010.3512 | 7993.6895 |
| 2.1264 | 8145.2704 | 7947.8328 | 7930.5584 |
| 2.1374 | 8126.0560 | 7885.3486 | 7867.4274 |
| 2.1484 | 8014.4272 | 7822.9011 | 7804.2963 |
| 2.1594 | 8043.6952 | 7760.4931 | 7741.1652 |
| 2.1704 | 7991.9071 | 7698.1278 | 7678.0342 |
| 2.1814 | 8165.5015 | 7635.8085 | 7614.9031 |
| 2.1924 | 8036.6421 | 7573.4312 | 7551.7721 |
| 2.2034 | 7909.2035 | 7511.1293 | 7488.4471 |
| 2.2144 | 7648.1308 | 7448.7780 | 7425.1221 |
| 2.2254 | 7863.8309 | 7386.4901 | 7361.7971 |
| 2.2364 | 7712.5398 | 7324.2712 | 7298.4722 |
| 2.2474 | 7577.9184 | 7262.1275 | 7235.1472 |
| 2.2584 | 7628.9946 | 7200.0658 | 7171.8222 |
| 2.2694 | 7772.1947 | 7138.0937 | 7108.4972 |
| 2.2804 | 7687.4425 | 7076.2200 | 7045.1722 |
| 2.2914 | 7470.9892 | 7014.4542 | 6981.8472 |
| 2.3024 | 7490.9867 | 6952.8071 | 6918.5223 |
| 2.3134 | 7483.5782 | 6891.2909 | 6855.1973 |
| 2.3244 | 7452.6534 | 6829.9195 | 6791.8723 |
| 2.3354 | 7428.2507 | 6768.7085 | 6728.5473 |
| 2.3464 | 7419.0030 | 6707.6760 | 6665.2223 |
| 2.3574 | 7353.7512 | 6646.8428 | 6601.8974 |
| 2.3684 | 7254.7773 | 6586.2331 | 6538.5724 |
| 2.3794 | 7296.3589 | 6525.7887 | 6475.2474 |
| 2.3904 | 7224.2606 | 6465.6488 | 6411.7655 |
| 2.4014 | 7232.6991 | 6405.7520 | 6348.2836 |
| 2.4124 | 7207.4911 | 6346.2398 | 6284.8018 |
| 2.4234 | 7047.9105 | 6287.1826 | 6221.3199 |
| 2.4344 | 7077.3982 | 6228.6737 | 6157.8380 |
| 2.4454 | 7143.9833 | 6170.8383 | 6094.3562 |
| 2.4564 | 7161.6298 | 6113.8462 | 6030.8743 |
| 2.4674 | 7171.8053 | 6057.9276 | 5967.3924 |
| 2.4784 | 7052.8977 | 6003.3932 | 5903.9105 |
| 2.4894 | 6881.6952 | 5950.6569 | 5840.4287 |
| 2.5004 | 6800.4292 | 5900.2603 | 5776.9468 |
| 2.5114 | 6903.4277 | 5852.8961 | 5713.4649 |
| 2.5224 | 6848.1140 | 5809.4260 | 5649.9830 |
| 2.5334 | 6705.7817 | 5770.8885 | 5586.5012 |
| 2.5444 | 6741.6239 | 5738.4882 | 5523.0193 |
| 2.5554 | 6779.7709 | 5713.5638 | 5459.5374 |
| 2.5664 | 6675.5708 | 5697.5255 | 5396.0556 |
| 2.5774 | 6635.7306 | 5691.7621 | 5332.5737 |
| 2.5884 | 6596.5374 | 5697.5171 | 5269.0918 |
| 2.5994 | 6537.1416 | 5715.7372 | 5205.6099 |
| 2.6104 | 6566.2925 | 5746.8998 | 5142.1281 |
| 2.6214 | 6650.6352 | 5790.8245 | 5078.6462 |
| 2.6324 | 6474.4277 | 5846.4657 | 5015.1643 |
| 2.6434 | 6388.4258 | 5911.6768 | 4951.6824 |
| 2.6544 | 6416.5565 | 5982.9329 | 4888.2006 |
| 2.6654 | 6374.6401 | 6055.0210 | 4824.7187 |
| 2.6764 | 6096.5850 | 6120.7882 | 4761.2368 |
| 2.6874 | 6093.0629 | 6171.1904 | 4697.7550 |
| 2.6984 | 6052.4071 | 6196.0274 | 4634.2731 |
| 2.7094 | 5975.5762 | 6185.6592 | 4570.7912 |
| 2.7204 | 5833.7709 | 6133.4502 | 4507.3093 |
| 2.7314 | 5752.5162 | 6037.8915 | 4443.8275 |
| 2.7424 | 5428.0698 | 5903.1383 | 4380.3456 |
| 2.7534 | 5242.3176 | 5737.5131 | 4316.8637 |
| 2.7644 | 5103.6607 | 5551.3293 | 4253.2250 |
| 2.7754 | 4903.1819 | 5354.2952 | 4189.5862 |
| 2.7864 | 4640.9985 | 5154.6761 | 4125.9474 |
| 2.7974 | 4550.3628 | 4958.6660 | 4062.3087 |
| 2.8084 | 4441.6111 | 4770.6174 | 3998.6699 |
| 2.8194 | 4345.4130 | 4593.3452 | 3935.0311 |
| 2.8304 | 4086.2625 | 4428.4264 | 3871.3924 |
| 2.8414 | 3967.8515 | 4276.4573 | 3807.7536 |
| 2.8524 | 3913.6794 | 4137.2726 | 3744.1148 |
| 2.8634 | 3818.0059 | 4010.1431 | 3680.4761 |
| 2.8744 | 3685.8289 | 3893.9569 | 3616.8373 |
| 2.8854 | 3619.0698 | 3787.3815 | 3553.1985 |
| 2.8964 | 3586.1416 | 3689.0034 | 3489.5598 |
| 2.9074 | 3397.8358 | 3597.4368 | 3425.9210 |
| 2.9184 | 3253.6608 | 3511.4019 | 3362.2823 |
| 2.9294 | 3376.5752 | 3429.7718 | 3298.6435 |
| 2.9404 | 3186.8343 | 3368.0402 | 3235.0047 |
| 2.9514 | 3218.9852 | 3305.7098 | 3200.9856 |
| 2.9624 | 3109.7242 | 3261.8834 | 3166.9666 |
| 2.9734 | 3188.3294 | 3219.6385 | 3132.9475 |
| 2.9844 | 3047.5157 | 3178.6144 | 3098.9284 |
| 2.9954 | 2947.8230 | 3138.5425 | 3064.9093 |
| 3.0064 | 2880.3033 | 3099.2243 | 3030.8902 |
| 3.0174 | 2894.1849 | 3060.5135 | 2996.8712 |
| 3.0284 | 2913.8451 | 3022.3021 | 2962.8521 |
| 3.0394 | 2864.3786 | 2984.5088 | 2928.8330 |
| 3.0504 | 2863.5148 | 2947.0718 | 2894.8139 |
| 3.0614 | 2865.9233 | 2909.9428 | 2860.7948 |
| 3.0724 | 2812.3107 | 2873.0831 | 2826.7757 |
| 3.0834 | 2771.2055 | 2836.4610 | 2792.7567 |
| 3.0944 | 2730.7124 | 2800.0501 | 2758.7376 |
| 3.1054 | 2695.8574 | 2763.8280 | 2724.7185 |
| 3.1164 | 2650.8963 | 2727.7753 | 2690.6994 |
| 3.1274 | 2649.4159 | 2698.8217 | 2656.6803 |
| 3.1384 | 2672.3609 | 2668.6234 | 2635.1720 |
| 3.1494 | 2620.1819 | 2645.4965 | 2613.6637 |
| 3.1604 | 2554.8982 | 2622.4829 | 2592.1553 |
| 3.1714 | 2533.0344 | 2599.5723 | 2570.6470 |
| 3.1824 | 2505.9700 | 2576.7558 | 2549.1387 |
| 3.1934 | 2491.4956 | 2554.0251 | 2527.6303 |
| 3.2044 | 2490.6165 | 2531.3730 | 2506.1220 |
| 3.2154 | 2474.9371 | 2508.7929 | 2484.6137 |
| 3.2264 | 2485.4838 | 2486.2790 | 2463.1053 |
| 3.2374 | 2427.7532 | 2463.8260 | 2441.5970 |
| 3.2484 | 2409.5555 | 2441.4292 | 2420.0887 |
| 3.2594 | 2363.7552 | 2419.0841 | 2398.5803 |
| 3.2704 | 2336.8653 | 2396.7869 | 2377.0720 |
| 3.2814 | 2345.4759 | 2374.5340 | 2355.5637 |
| 3.2924 | 2365.0000 | 2352.3222 | 2334.0554 |
| 3.3034 | 2336.1780 | 2330.1486 | 2312.5470 |
| 3.3144 | 2271.8540 | 2308.3605 | 2291.0387 |
| 3.3254 | 2261.7463 | 2286.5357 | 2270.1608 |
| 3.3364 | 2237.8166 | 2265.0917 | 2249.2830 |
| 3.3474 | 2148.0364 | 2243.6764 | 2228.4051 |
| 3.3584 | 2164.7390 | 2222.2879 | 2207.5272 |
| 3.3694 | 2252.6863 | 2200.9244 | 2186.6494 |
| 3.3804 | 2210.3702 | 2179.5844 | 2165.7715 |
| 3.3914 | 2114.8230 | 2158.2663 | 2144.8936 |
| 3.4024 | 2092.8048 | 2136.9689 | 2124.0158 |
| 3.4134 | 2060.6047 | 2115.6908 | 2103.1379 |
| 3.4244 | 2081.8437 | 2094.4309 | 2082.2601 |
| 3.4354 | 2110.8151 | 2073.1880 | 2061.3822 |
| 3.4464 | 2073.2227 | 2051.9613 | 2040.5043 |
| 3.4574 | 2057.2242 | 2030.7497 | 2019.6265 |
| 3.4684 | 1972.1406 | 2009.5525 | 1998.7486 |
| 3.4794 | 1944.2920 | 1988.3687 | 1977.8707 |
| 3.4904 | 1973.4823 | 1967.1977 | 1956.9929 |
| 3.5014 | 1914.1701 | 1950.2807 | 1936.1150 |
| 3.5124 | 1939.8132 | 1932.5309 | 1922.8768 |
| 3.5234 | 1925.2301 | 1919.0338 | 1909.6385 |
| 3.5344 | 1921.1691 | 1905.5469 | 1896.4003 |
| 3.5454 | 1875.1062 | 1892.0698 | 1883.1620 |
| 3.5564 | 1909.9779 | 1878.6018 | 1869.9238 |
| 3.5674 | 1868.1376 | 1865.1975 | 1856.6855 |
| 3.5784 | 1839.4238 | 1851.7794 | 1843.4473 |
| 3.5894 | 1871.6460 | 1838.3653 | 1830.2090 |
| 3.6004 | 1781.0958 | 1824.9475 | 1816.9708 |
| 3.6114 | 1744.2606 | 1811.5209 | 1803.7325 |
| 3.6224 | 1731.5118 | 1798.1011 | 1790.4943 |
| 3.6334 | 1732.2763 | 1784.6879 | 1777.2560 |
| 3.6444 | 1749.6273 | 1771.2809 | 1764.0178 |
| 3.6554 | 1761.4366 | 1757.8798 | 1750.7795 |
| 3.6664 | 1709.9312 | 1744.4844 | 1737.5413 |
| 3.6774 | 1717.4966 | 1731.0944 | 1724.3030 |
| 3.6884 | 1761.3850 | 1718.2205 | 1711.0648 |
| 3.6994 | 1664.3254 | 1705.2498 | 1698.7466 |
| 3.7104 | 1654.7153 | 1692.7948 | 1686.4285 |
| 3.7214 | 1588.9469 | 1680.3443 | 1674.1103 |
| 3.7324 | 1612.7503 | 1667.8982 | 1661.7921 |
| 3.7434 | 1594.2763 | 1655.4562 | 1649.4739 |
| 3.7544 | 1566.2802 | 1643.0182 | 1637.1558 |
| 3.7654 | 1621.0610 | 1630.5841 | 1624.8376 |
| 3.7764 | 1570.1416 | 1618.1537 | 1612.5194 |
| 3.7874 | 1545.2124 | 1605.7268 | 1600.2012 |
| 3.7984 | 1555.9553 | 1593.3033 | 1587.8831 |
| 3.8094 | 1542.4336 | 1580.8830 | 1575.5649 |
| 3.8204 | 1508.5974 | 1568.4659 | 1563.2467 |
| 3.8314 | 1560.0894 | 1556.0519 | 1550.9285 |
| 3.8424 | 1471.1033 | 1543.6407 | 1538.6104 |
| 3.8534 | 1543.5074 | 1531.2324 | 1526.2922 |
| 3.8644 | 1519.0669 | 1518.8267 | 1513.9740 |
| 3.8754 | 1484.6264 | 1506.3916 | 1501.6558 |
| 3.8864 | 1491.1018 | 1493.9654 | 1489.2799 |
| 3.8974 | 1485.2704 | 1481.5095 | 1476.9039 |
| 3.9084 | 1441.4656 | 1469.0560 | 1464.5279 |
| 3.9194 | 1480.3126 | 1456.6047 | 1452.1520 |
| 3.9304 | 1357.2453 | 1444.1556 | 1439.7760 |
| 3.9414 | 1360.8348 | 1431.7086 | 1427.4000 |
| 3.9524 | 1403.1062 | 1419.2637 | 1415.0241 |
| 3.9634 | 1416.7562 | 1406.8207 | 1402.6481 |
| 3.9744 | 1416.5919 | 1394.3797 | 1390.2721 |
| 3.9854 | 1352.6991 | 1381.9405 | 1377.8961 |
| 3.9964 | 1357.6519 | 1369.5032 | 1365.5202 |
| 4.0074 | 1338.7817 | 1357.0675 | 1353.1442 |
| 4.0184 | 1305.9617 | 1344.6336 | 1340.7682 |
| 4.0294 | 1334.7994 | 1332.2013 | 1328.3923 |
| 4.0404 | 1281.6278 | 1319.7706 | 1316.0163 |
| 4.0514 | 1228.4454 | 1307.3415 | 1303.6403 |
| 4.0624 | 1287.1411 | 1296.8026 | 1291.2644 |
| 4.0734 | 1350.2320 | 1285.8893 | 1282.2900 |
| 4.0844 | 1318.7876 | 1276.8662 | 1273.3157 |
| 4.0954 | 1289.0000 | 1267.8445 | 1264.3414 |
| 4.1064 | 1289.6952 | 1258.8242 | 1255.3671 |
| 4.1174 | 1274.0855 | 1249.8052 | 1246.3928 |
| 4.1284 | 1232.8348 | 1240.7875 | 1237.4185 |
| 4.1394 | 1221.6893 | 1231.7710 | 1228.4442 |
| 4.1504 | 1233.6032 | 1222.7558 | 1219.4699 |
| 4.1614 | 1210.5024 | 1213.7418 | 1210.4955 |
| 4.1724 | 1196.9602 | 1204.7289 | 1201.5212 |
| 4.1834 | 1229.9381 | 1195.7173 | 1192.5469 |
| 4.1944 | 1246.1347 | 1186.7067 | 1183.5726 |

Scan List

| Vis. | Dataset Name | Start pos. [°2θ] | End pos. [°2θ] | Step [°2θ] | Meas.Date/Time |
| --- | --- | --- | --- | --- | --- |
| * | 16 Etosha22 moisub 3-15cm S3 550C | 2.0054 | 29.9894 | 0.0110 | 12/8/2023 12:24:40 PM |

Peak List

| Pos. [°2θ] | Height [cts] | FWHM Left [°2θ] | d-spacing [Å] | Rel. Int. [%] |
| --- | --- | --- | --- | --- |
| 2.7155 | 1455.53 | 0.1732 | 32.50890 | 80.38 |
| 5.3029 | 92.57 | 0.1732 | 16.65151 | 5.11 |
| 8.6954 | 900.34 | 0.1299 | 10.16107 | 49.72 |
| 10.5753 | 18.52 | 0.5196 | 8.35863 | 1.02 |
| 13.2254 | 88.55 | 0.1299 | 6.68911 | 4.89 |
| 13.5443 | 144.32 | 0.1299 | 6.53231 | 7.97 |
| 15.7501 | 1400.87 | 0.0866 | 5.62208 | 77.36 |
| 17.6285 | 121.49 | 0.1082 | 5.02703 | 6.71 |
| 18.2473 | 150.45 | 0.0866 | 4.85792 | 8.31 |
| 19.6019 | 46.44 | 0.4330 | 4.52515 | 2.56 |
| 23.3826 | 55.82 | 0.1732 | 3.80134 | 3.08 |
| 24.1988 | 25.50 | 0.3464 | 3.67495 | 1.41 |
| 25.9425 | 673.48 | 0.1732 | 3.43176 | 37.19 |
| 26.7172 | 838.85 | 0.1948 | 3.33398 | 46.32 |
| 27.4067 | 1674.61 | 0.0660 | 3.25165 | 92.47 |
| 27.5224 | 1810.92 | 0.0866 | 3.23824 | 100.00 |

Pattern List

| Visible | Ref.Code | Score | Compound Name | Chem. Formula | Mineral Name | SemiQuant[%] |
| --- | --- | --- | --- | --- | --- | --- |
| * | 01-072-4625 | 53 | Sodium Aluminum Silicate Hydrate | Na Al ( Si2 O6 ) ( H2 O ) | Analcime | 10 |
| * | 04-017-9632 | 44 | Potassium Sodium Magnesium Aluminum Iron Silicon Titanium Oxide Fluoride Hydroxide | K0.88 Na0.1 Mg2.25 Ti0.13 Fe0.46 Al1.46 Si2.7 O10.28 ( O H )1.61 F0.11 | Phlogopite-1M | 27 |
| * | 04-015-3139 | 50 | Titanium Antimony Vanadium Oxide | Ti0.917 V0.041 W0.005 Sb0.033 O2 | Rutile | 12 |
| * | 01-082-8023 | No Matching Lines | Sodium Magnesium Silicon Oxide Hydrate | Na2 Mg3 ( Si6 O16 ) ( H2 O )7 | Loughlinite | - |
| * | 04-025-4215 | 36 | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide | Mg10.4 V0.36 Mn33.5 Fe0.14 Al0.69 Si6.77 As6.5 P0.3 O54 ( O H )42 | Carlfrancisite | 14 |
| * | 01-076-2756 | 30 | Potassium Sodium Aluminum Silicate | ( K0.8 Na0.2 ) ( Al Si3 O8 ) | Sanidine | 6 |
| * | 04-016-4488 | 27 | Potassium Sodium Aluminum Silicate | K0.5 Na0.5 Al Si3 O8 | Microcline, Na-bearing | 30 |
| * | 04-017-1621 | 7 | Calcium Magnesium Iron Silicate Hydroxide | Ca2 Mg2.5 Fe2.5 Si8 O22 ( O H )2 | Actinolite | 1 |

Anchor Scan Parameters

Dataset Name	16 Etosha22 moisub 3-15cm S3 550C

File name	C:\aeris_data\XRD data\Goldstein\Etosha 2023\Etosha Clay Data\Sample 16\16 Etosha22 moisub 3-15cm S3 550C.xrdml

Sample Identification	16 Etosha22 moisub 3-15cm S3 550C

Measurement Start Date/Time	12/8/2023 12:24:40 PM

Operator	Instrument

Raw Data Origin	XRD measurement (*.XRDML)

Scan Axis	Gonio

Start Position [°2θ]	2.0054

End Position [°2θ]	29.9894

Step Size [°2θ]	0.0110

Scan Step Time [s]	48.1950

Scan Type	Continuous

PSD Mode	Scanning

PSD Length [°2θ]	5.54

Offset [°2θ]	0.0000

Divergence Slit Type	Fixed

Divergence Slit Size [°]	0.0603

Specimen Length [mm]	10.00

Measurement Temperature [°C]	25.00

Anode Material	Cu

K-α1 [Å]	1.54060

K-α2 [Å]	1.54443

K-β1 [Å]	1.39225

K-A2 / K-A1 Ratio	0.50000

Generator Settings	15 mA, 40 kV

Diffractometer Type	2082464

Diffractometer Number	0

Goniometer Radius [mm]	145.00

Dist. Focus-Diverg. Slit [mm]	95.00

Incident Beam Monochromator	No

Spinning	Yes