17 Etosha22 wetsub 15cm S3 400 C

Graphics

Graphics

Graphics

Quantitative Results

Phase Sodium Aluminum Silicate Hydrate

Weight fraction/ %	37.0

Phase Potassium Sodium Magnesium Aluminum Iron Silicon Titanium Oxide Fluoride Hydroxide

Weight fraction/ %	50.0

Phase Magnesium Aluminum Iron Silicon Oxide Hydroxide Hydrate

Weight fraction/ %	1.0

Phase Potassium Calcium Magnesium Aluminum Iron Silicon Oxide Hydroxide Hydrate

Weight fraction/ %	11.0

Phase Titanium Oxide

Weight fraction/ %	1.0

Multiple Quantitative Results

Scans vs Phases Matrix

| Scan name | Sodium Aluminum Silicate Hydrate | Potassium Sodium Magnesium Aluminum Iron Silicon Titanium Oxide Fluoride Hydroxide | Magnesium Aluminum Iron Silicon Oxide Hydroxide Hydrate | Potassium Calcium Magnesium Aluminum Iron Silicon Oxide Hydroxide Hydrate | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide | Titanium Oxide |
| --- | --- | --- | --- | --- | --- | --- |
| 17 Etoshs22 wetsub 15cm S3 400C | 37.0 | 50.0 | 1.0 | 11.0 | 0.0 | 1.0 |

Anchor Scan Data

| Pos. [°2θ] | Iobs [cts] | Icalc [cts] | Iback [cts] |
| --- | --- | --- | --- |
| 2.0054 | 5501.0000 | 5482.4003 | 5501.0000 |
| 2.0164 | 5512.5374 | 5463.6845 | 5463.6845 |
| 2.0274 | 5394.2380 | 5426.3689 | 5426.3689 |
| 2.0384 | 5360.3864 | 5389.0534 | 5389.0534 |
| 2.0494 | 5273.3255 | 5351.7378 | 5351.7378 |
| 2.0604 | 5410.2065 | 5314.4223 | 5314.4223 |
| 2.0714 | 5325.9381 | 5277.1068 | 5277.1068 |
| 2.0824 | 5186.3117 | 5239.7912 | 5239.7912 |
| 2.0934 | 5163.0708 | 5202.4757 | 5202.4757 |
| 2.1044 | 5024.9646 | 5165.1602 | 5165.1602 |
| 2.1154 | 5076.2173 | 5127.8446 | 5127.8446 |
| 2.1264 | 4963.6381 | 5090.5291 | 5090.5291 |
| 2.1374 | 4833.1947 | 5053.2135 | 5053.2135 |
| 2.1484 | 4892.9676 | 5015.8980 | 5015.8980 |
| 2.1594 | 5007.2989 | 4978.5825 | 4978.5825 |
| 2.1704 | 4927.4012 | 4941.2669 | 4941.2669 |
| 2.1814 | 4845.4189 | 4903.9514 | 4903.9514 |
| 2.1924 | 4923.8363 | 4873.5754 | 4866.6358 |
| 2.2034 | 4828.8672 | 4843.2428 | 4843.2428 |
| 2.2144 | 4717.6401 | 4819.8498 | 4819.8498 |
| 2.2254 | 4849.4179 | 4796.4568 | 4796.4568 |
| 2.2364 | 4762.9012 | 4773.0638 | 4773.0638 |
| 2.2474 | 4716.6686 | 4749.6708 | 4749.6708 |
| 2.2584 | 4697.2232 | 4726.2778 | 4726.2778 |
| 2.2694 | 4739.8053 | 4702.8848 | 4702.8848 |
| 2.2804 | 4698.8815 | 4679.4918 | 4679.4918 |
| 2.2914 | 4639.0413 | 4656.0988 | 4656.0988 |
| 2.3024 | 4627.7080 | 4632.7058 | 4632.7058 |
| 2.3134 | 4628.2724 | 4609.3128 | 4609.3128 |
| 2.3244 | 4649.6731 | 4585.9198 | 4585.9198 |
| 2.3354 | 4597.6637 | 4562.5267 | 4562.5267 |
| 2.3464 | 4539.9970 | 4539.1337 | 4539.1337 |
| 2.3574 | 4515.5733 | 4515.7407 | 4515.7407 |
| 2.3684 | 4553.6932 | 4492.3477 | 4492.3477 |
| 2.3794 | 4507.3766 | 4468.9547 | 4468.9547 |
| 2.3904 | 4400.5433 | 4445.5617 | 4445.5617 |
| 2.4014 | 4391.0000 | 4422.1687 | 4422.1687 |
| 2.4124 | 4380.7532 | 4398.7757 | 4398.7757 |
| 2.4234 | 4424.8505 | 4375.3827 | 4375.3827 |
| 2.4344 | 4356.0236 | 4351.9897 | 4351.9897 |
| 2.4454 | 4358.5890 | 4328.5967 | 4328.5967 |
| 2.4564 | 4364.6145 | 4305.2037 | 4305.2037 |
| 2.4674 | 4297.4159 | 4281.8107 | 4281.8107 |
| 2.4784 | 4244.0610 | 4258.4176 | 4258.4176 |
| 2.4894 | 4186.0413 | 4235.0246 | 4235.0246 |
| 2.5004 | 4232.5841 | 4211.6316 | 4211.6316 |
| 2.5114 | 4206.5841 | 4188.2386 | 4188.2386 |
| 2.5224 | 4179.2385 | 4164.8456 | 4164.8456 |
| 2.5334 | 4177.2714 | 4141.4526 | 4141.4526 |
| 2.5444 | 4168.8407 | 4118.0596 | 4118.0596 |
| 2.5554 | 4117.0029 | 4094.6666 | 4094.6666 |
| 2.5664 | 4081.2537 | 4074.1491 | 4071.2736 |
| 2.5774 | 4021.2822 | 4052.8013 | 4052.8013 |
| 2.5884 | 3973.9715 | 4034.3291 | 4034.3291 |
| 2.5994 | 4083.8142 | 4015.8569 | 4015.8569 |
| 2.6104 | 4098.3835 | 3997.3846 | 3997.3846 |
| 2.6214 | 4013.6765 | 3978.9124 | 3978.9124 |
| 2.6324 | 3916.3422 | 3960.4401 | 3960.4401 |
| 2.6434 | 3887.7129 | 3941.9679 | 3941.9679 |
| 2.6544 | 3927.1593 | 3923.4956 | 3923.4956 |
| 2.6654 | 3953.7994 | 3905.0234 | 3905.0234 |
| 2.6764 | 3960.2493 | 3886.5511 | 3886.5511 |
| 2.6874 | 3925.1839 | 3868.0789 | 3868.0789 |
| 2.6984 | 3804.0442 | 3849.6067 | 3849.6067 |
| 2.7094 | 3894.7139 | 3831.1344 | 3831.1344 |
| 2.7204 | 3892.8476 | 3812.6622 | 3812.6622 |
| 2.7314 | 3800.4454 | 3794.1899 | 3794.1899 |
| 2.7424 | 3853.4681 | 3775.7177 | 3775.7177 |
| 2.7534 | 3854.7915 | 3757.1983 | 3757.2454 |
| 2.7644 | 3774.8245 | 3738.7076 | 3738.7076 |
| 2.7754 | 3766.1622 | 3720.1698 | 3720.1698 |
| 2.7864 | 3771.3633 | 3701.6319 | 3701.6319 |
| 2.7974 | 3648.1062 | 3683.0941 | 3683.0941 |
| 2.8084 | 3738.7724 | 3664.5563 | 3664.5563 |
| 2.8194 | 3761.0049 | 3646.0184 | 3646.0184 |
| 2.8304 | 3664.2861 | 3627.4806 | 3627.4806 |
| 2.8414 | 3661.6047 | 3608.9428 | 3608.9428 |
| 2.8524 | 3640.2325 | 3590.4050 | 3590.4050 |
| 2.8634 | 3561.3451 | 3571.8671 | 3571.8671 |
| 2.8744 | 3399.7281 | 3553.3293 | 3553.3293 |
| 2.8854 | 3435.3147 | 3534.7915 | 3534.7915 |
| 2.8964 | 3616.1991 | 3516.2536 | 3516.2536 |
| 2.9074 | 3469.4563 | 3497.7158 | 3497.7158 |
| 2.9184 | 3526.0123 | 3479.1780 | 3479.1780 |
| 2.9294 | 3477.5457 | 3460.6401 | 3460.6401 |
| 2.9404 | 3462.0315 | 3442.1023 | 3442.1023 |
| 2.9514 | 3416.2930 | 3423.5645 | 3423.5645 |
| 2.9624 | 3345.4336 | 3405.0266 | 3405.0266 |
| 2.9734 | 3226.1406 | 3386.4888 | 3386.4888 |
| 2.9844 | 3323.4597 | 3367.9510 | 3367.9510 |
| 2.9954 | 3275.5221 | 3349.4131 | 3349.4131 |
| 3.0064 | 3327.4504 | 3330.8753 | 3330.8753 |
| 3.0174 | 3349.9528 | 3312.3375 | 3312.3375 |
| 3.0284 | 3225.7080 | 3293.7996 | 3293.7996 |
| 3.0394 | 3216.1573 | 3275.2618 | 3275.2618 |
| 3.0504 | 3277.6789 | 3256.7240 | 3256.7240 |
| 3.0614 | 3164.6342 | 3238.1862 | 3238.1862 |
| 3.0724 | 3230.1981 | 3219.6483 | 3219.6483 |
| 3.0834 | 3160.0236 | 3201.1105 | 3201.1105 |
| 3.0944 | 3155.2345 | 3182.5727 | 3182.5727 |
| 3.1054 | 3220.2163 | 3164.0348 | 3164.0348 |
| 3.1164 | 3115.8963 | 3145.4970 | 3145.4970 |
| 3.1274 | 3113.9086 | 3130.0450 | 3126.9592 |
| 3.1384 | 3134.2969 | 3112.7141 | 3112.7141 |
| 3.1494 | 3088.6431 | 3098.4690 | 3098.4690 |
| 3.1604 | 3049.6416 | 3084.2240 | 3084.2240 |
| 3.1714 | 3080.7935 | 3069.9789 | 3069.9789 |
| 3.1824 | 3116.1774 | 3055.7339 | 3055.7339 |
| 3.1934 | 3016.7434 | 3041.4888 | 3041.4888 |
| 3.2044 | 3055.4631 | 3027.2437 | 3027.2437 |
| 3.2154 | 2990.4956 | 3012.9987 | 3012.9987 |
| 3.2264 | 2991.9440 | 2998.7536 | 2998.7536 |
| 3.2374 | 3020.4808 | 2984.5085 | 2984.5085 |
| 3.2484 | 3002.8889 | 2970.2635 | 2970.2635 |
| 3.2594 | 2960.9233 | 2956.0184 | 2956.0184 |
| 3.2704 | 2917.8653 | 2941.7733 | 2941.7733 |
| 3.2814 | 2958.4081 | 2927.5283 | 2927.5283 |
| 3.2924 | 3006.1062 | 2913.2832 | 2913.2832 |
| 3.3034 | 2982.4966 | 2899.0382 | 2899.0382 |
| 3.3144 | 2890.4872 | 2884.7931 | 2884.7931 |
| 3.3254 | 2851.7404 | 2870.5480 | 2870.5480 |
| 3.3364 | 2885.8948 | 2856.3030 | 2856.3030 |
| 3.3474 | 2865.4848 | 2842.0579 | 2842.0579 |
| 3.3584 | 2846.1976 | 2827.8128 | 2827.8128 |
| 3.3694 | 2834.4877 | 2813.5678 | 2813.5678 |
| 3.3804 | 2887.7920 | 2799.3227 | 2799.3227 |
| 3.3914 | 2852.8053 | 2785.0777 | 2785.0777 |
| 3.4024 | 2787.0978 | 2770.8326 | 2770.8326 |
| 3.4134 | 2767.2547 | 2756.5875 | 2756.5875 |
| 3.4244 | 2778.1519 | 2742.3425 | 2742.3425 |
| 3.4354 | 2771.8692 | 2728.0974 | 2728.0974 |
| 3.4464 | 2714.4607 | 2713.8523 | 2713.8523 |
| 3.4574 | 2700.9381 | 2699.6073 | 2699.6073 |
| 3.4684 | 2703.0182 | 2685.3622 | 2685.3622 |
| 3.4794 | 2662.1209 | 2671.1172 | 2671.1172 |
| 3.4904 | 2674.3053 | 2656.8721 | 2656.8721 |
| 3.5014 | 2636.6017 | 2645.3766 | 2642.6270 |
| 3.5124 | 2620.2581 | 2632.2071 | 2632.2071 |
| 3.5234 | 2628.4808 | 2621.7871 | 2621.7871 |
| 3.5344 | 2668.2567 | 2611.3672 | 2611.3672 |
| 3.5454 | 2680.3963 | 2600.9472 | 2600.9472 |
| 3.5564 | 2597.6327 | 2590.5272 | 2590.5272 |
| 3.5674 | 2592.5959 | 2580.1073 | 2580.1073 |
| 3.5784 | 2516.9041 | 2569.6873 | 2569.6873 |
| 3.5894 | 2605.4868 | 2559.2674 | 2559.2674 |
| 3.6004 | 2650.1686 | 2548.8474 | 2548.8474 |
| 3.6114 | 2558.4552 | 2538.4274 | 2538.4274 |
| 3.6224 | 2598.5428 | 2528.0075 | 2528.0075 |
| 3.6334 | 2549.2930 | 2517.5875 | 2517.5875 |
| 3.6444 | 2551.6273 | 2507.1676 | 2507.1676 |
| 3.6554 | 2484.9764 | 2496.7476 | 2496.7476 |
| 3.6664 | 2468.5762 | 2486.3276 | 2486.3276 |
| 3.6774 | 2447.1622 | 2475.9947 | 2475.9077 |
| 3.6884 | 2510.9204 | 2466.3293 | 2465.4877 |
| 3.6994 | 2436.0747 | 2456.1975 | 2455.9411 |
| 3.7104 | 2474.8761 | 2446.6525 | 2446.3945 |
| 3.7214 | 2436.8820 | 2437.1075 | 2436.8478 |
| 3.7324 | 2479.4848 | 2427.5626 | 2427.3012 |
| 3.7434 | 2416.1190 | 2418.0176 | 2417.7546 |
| 3.7544 | 2447.3083 | 2408.4727 | 2408.2079 |
| 3.7654 | 2379.4071 | 2398.9278 | 2398.6613 |
| 3.7764 | 2500.3363 | 2389.3829 | 2389.1146 |
| 3.7874 | 2429.6548 | 2379.8380 | 2379.5680 |
| 3.7984 | 2466.6283 | 2370.2931 | 2370.0214 |
| 3.8094 | 2359.1101 | 2360.7483 | 2360.4747 |
| 3.8204 | 2365.8879 | 2351.2035 | 2350.9281 |
| 3.8314 | 2363.8948 | 2341.6587 | 2341.3815 |
| 3.8424 | 2403.6868 | 2332.1139 | 2331.8348 |
| 3.8534 | 2313.9056 | 2322.5691 | 2322.2882 |
| 3.8644 | 2394.3687 | 2313.0243 | 2312.7416 |
| 3.8754 | 2340.4317 | 2303.4796 | 2303.1949 |
| 3.8864 | 2353.9823 | 2293.9349 | 2293.6483 |
| 3.8974 | 2326.9783 | 2284.3902 | 2284.1016 |
| 3.9084 | 2202.5413 | 2274.8455 | 2274.5550 |
| 3.9194 | 2298.3540 | 2265.3009 | 2265.0084 |
| 3.9304 | 2232.1883 | 2255.7562 | 2255.4617 |
| 3.9414 | 2262.1032 | 2246.2116 | 2245.9151 |
| 3.9524 | 2245.9513 | 2236.6670 | 2236.3685 |
| 3.9634 | 2286.1219 | 2227.1224 | 2226.8218 |
| 3.9744 | 2271.9970 | 2217.5779 | 2217.2752 |
| 3.9854 | 2256.2832 | 2208.1430 | 2207.7286 |
| 3.9964 | 2271.7217 | 2198.6759 | 2198.1819 |
| 4.0074 | 2211.1799 | 2189.1450 | 2188.6353 |
| 4.0184 | 2184.5044 | 2179.6041 | 2179.0886 |
| 4.0294 | 2182.3540 | 2170.0632 | 2169.5420 |
| 4.0404 | 2168.7355 | 2160.5225 | 2159.9954 |
| 4.0514 | 2121.8673 | 2150.9819 | 2150.4487 |
| 4.0624 | 2142.8796 | 2143.6773 | 2140.9021 |
| 4.0734 | 2152.0000 | 2135.0115 | 2134.4659 |
| 4.0844 | 2149.4159 | 2128.5817 | 2128.0297 |
| 4.0954 | 2176.5241 | 2122.1520 | 2121.5935 |
| 4.1064 | 2222.2301 | 2115.7225 | 2115.1573 |
| 4.1174 | 2157.4896 | 2109.2931 | 2108.7211 |
| 4.1284 | 2128.8191 | 2102.8639 | 2102.2849 |
| 4.1394 | 2150.5457 | 2096.4349 | 2095.8487 |
| 4.1504 | 2136.4735 | 2090.0060 | 2089.4125 |
| 4.1614 | 2148.1376 | 2083.5773 | 2082.9762 |
| 4.1724 | 2091.8156 | 2077.1488 | 2076.5400 |
| 4.1834 | 2034.9646 | 2070.7204 | 2070.1038 |
| 4.1944 | 2065.7817 | 2064.2923 | 2063.6676 |

Scan List

| Vis. | Dataset Name | Start pos. [°2θ] | End pos. [°2θ] | Step [°2θ] | Meas.Date/Time |
| --- | --- | --- | --- | --- | --- |
| * | 17 Etoshs22 wetsub 15cm S3 400C | 2.0054 | 29.9894 | 0.0110 | 12/7/2023 3:42:32 PM |

Peak List

| Pos. [°2θ] | Height [cts] | FWHM Left [°2θ] | d-spacing [Å] | Rel. Int. [%] |
| --- | --- | --- | --- | --- |
| 5.2786 | 137.30 | 0.1299 | 16.72801 | 13.00 |
| 7.1389 | 180.01 | 0.3464 | 12.37258 | 17.04 |
| 8.7410 | 1044.94 | 0.1299 | 10.10813 | 98.94 |
| 10.5342 | 51.42 | 0.5196 | 8.39115 | 4.87 |
| 15.8120 | 1056.16 | 0.1407 | 5.60021 | 100.00 |
| 17.6640 | 93.80 | 0.1299 | 5.01699 | 8.88 |
| 18.2430 | 151.41 | 0.1082 | 4.85907 | 14.34 |
| 19.7666 | 25.24 | 0.8659 | 4.48783 | 2.39 |
| 22.4079 | 53.53 | 0.1299 | 3.96444 | 5.07 |
| 23.4455 | 32.83 | 0.2598 | 3.79128 | 3.11 |
| 24.2593 | 92.78 | 0.1732 | 3.66592 | 8.78 |
| 25.9655 | 694.51 | 0.0649 | 3.42877 | 65.76 |
| 26.7129 | 236.77 | 0.1299 | 3.33451 | 22.42 |
| 27.5367 | 127.52 | 0.1732 | 3.23659 | 12.07 |

Pattern List

| Visible | Ref.Code | Score | Compound Name | Chem. Formula | Mineral Name | SemiQuant[%] |
| --- | --- | --- | --- | --- | --- | --- |
| * | 01-083-1732 | 63 | Sodium Aluminum Silicate Hydrate | Na16.48 Al15.52 Si32.48 O96 ( H2 O )16 | Analcime | 37 |
| * | 04-023-1515 | 52 | Potassium Sodium Magnesium Aluminum Iron Silicon Titanium Oxide Fluoride Hydroxide | K0.93 Na0.05 Mg1.71 Ti0.13 Fe0.97 Al1.44 Si2.75 O10.47 ( O H )1.33 F0.2 | Phlogopite-1M | 50 |
| * | 04-017-9668 | 7 | Magnesium Aluminum Iron Silicon Oxide Hydroxide Hydrate | Mg3.84 Ti0.005 Fe0.03 Al0.07 Si6 O15 ( O H )2 ( H2 O )5 | Sepiolite | 1 |
| * | 04-018-3209 | 22 | Potassium Calcium Magnesium Aluminum Iron Silicon Oxide Hydroxide Hydrate | K0.034 Ca0.01 Mg1.005 Fe0.085 Al1.025 Si3.99 O10.215 ( O H )0.93 ( H2 O )3.315 | Palygorskite-O | 11 |
| * | 04-025-4215 | No Matching Lines | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide | Mg10.4 V0.36 Mn33.5 Fe0.14 Al0.69 Si6.77 As6.5 P0.3 O54 ( O H )42 | Carlfrancisite | - |
| * | 04-008-7810 | 31 | Titanium Oxide | Ti O2 | Rutile | 1 |

Anchor Scan Parameters

Dataset Name	17 Etoshs22 wetsub 15cm S3 400C

File name	C:\aeris_data\XRD data\Goldstein\Etosha 2023\Etosha Clay Data\Sample 17\17 Etoshs22 wetsub 15cm S3 400C.xrdml

Sample Identification	17 Etoshs22 wetsub 15cm S3 400C

Measurement Start Date/Time	12/7/2023 3:42:32 PM

Operator	Instrument

Raw Data Origin	XRD measurement (*.XRDML)

Scan Axis	Gonio

Start Position [°2θ]	2.0054

End Position [°2θ]	29.9894

Step Size [°2θ]	0.0110

Scan Step Time [s]	48.1950

Scan Type	Continuous

PSD Mode	Scanning

PSD Length [°2θ]	5.54

Offset [°2θ]	0.0000

Divergence Slit Type	Fixed

Divergence Slit Size [°]	0.0603

Specimen Length [mm]	10.00

Measurement Temperature [°C]	25.00

Anode Material	Cu

K-α1 [Å]	1.54060

K-α2 [Å]	1.54443

K-β1 [Å]	1.39225

K-A2 / K-A1 Ratio	0.50000

Generator Settings	15 mA, 40 kV

Diffractometer Type	2082464

Diffractometer Number	0

Goniometer Radius [mm]	145.00

Dist. Focus-Diverg. Slit [mm]	95.00

Incident Beam Monochromator	No

Spinning	Yes