17 Etosha22 wetsub 15cm S3 550 C

Graphics

Graphics

Graphics

Quantitative Results

Phase Sodium Aluminum Silicate Hydrate

Weight fraction/ %	14.0

Phase Potassium Sodium Magnesium Aluminum Iron Silicon Titanium Oxide Fluoride Hydroxide

Weight fraction/ %	21.0

Phase Titanium Oxide

Weight fraction/ %	3.0

Phase Magnesium Aluminum Silicon Oxide Hydroxide Hydrate

Weight fraction/ %	12.0

Phase Magnesium Silicon Oxide Hydroxide Hydrate

Weight fraction/ %	19.0

Phase Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide

Weight fraction/ %	25.0

Phase Calcium Magnesium Iron Silicate Hydroxide

Weight fraction/ %	6.0

Multiple Quantitative Results

Scans vs Phases Matrix

| Scan name | Sodium Aluminum Silicate Hydrate | Potassium Sodium Magnesium Aluminum Iron Silicon Titanium Oxide Fluoride Hydroxide | Titanium Oxide | Magnesium Aluminum Silicon Oxide Hydroxide Hydrate | Magnesium Silicon Oxide Hydroxide Hydrate | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide | Calcium Magnesium Iron Silicate Hydroxide |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 17 Etosha22 wetsub 15cm S3 550C | 14.0 | 21.0 | 3.0 | 12.0 | 19.0 | 25.0 | 6.0 |

Anchor Scan Data

| Pos. [°2θ] | Iobs [cts] | Icalc [cts] | Iback [cts] |
| --- | --- | --- | --- |
| 2.0054 | 8911.0000 | 8890.7352 | 8911.0000 |
| 2.0164 | 8655.5364 | 8859.9011 | 8845.5433 |
| 2.0274 | 8774.8702 | 8794.9199 | 8780.0867 |
| 2.0384 | 8617.3791 | 8729.9625 | 8714.6300 |
| 2.0494 | 8771.2173 | 8665.0307 | 8649.1733 |
| 2.0604 | 8525.7207 | 8600.1260 | 8583.7167 |
| 2.0714 | 8560.5546 | 8535.2505 | 8518.2600 |
| 2.0824 | 8641.4145 | 8470.4063 | 8452.8033 |
| 2.0934 | 8361.4582 | 8405.5954 | 8387.3467 |
| 2.1044 | 8383.6681 | 8340.8206 | 8321.8900 |
| 2.1154 | 8362.0718 | 8276.0843 | 8256.4333 |
| 2.1264 | 8199.4189 | 8211.3897 | 8190.9767 |
| 2.1374 | 8037.4543 | 8146.7399 | 8125.5200 |
| 2.1484 | 8124.8348 | 8082.1384 | 8060.0634 |
| 2.1594 | 8151.8830 | 8017.5892 | 7994.6067 |
| 2.1704 | 8147.7581 | 7953.0966 | 7929.1500 |
| 2.1814 | 8008.3687 | 7888.6653 | 7863.6934 |
| 2.1924 | 8120.1490 | 7824.2085 | 7798.2367 |
| 2.2034 | 8085.9557 | 7759.8319 | 7732.6035 |
| 2.2144 | 7885.9577 | 7695.4420 | 7666.9702 |
| 2.2254 | 8005.5821 | 7631.1382 | 7601.3370 |
| 2.2364 | 8059.5767 | 7566.9286 | 7535.7038 |
| 2.2474 | 7966.9036 | 7502.8220 | 7470.0706 |
| 2.2584 | 7879.6077 | 7438.8287 | 7404.4374 |
| 2.2694 | 7849.7611 | 7374.9598 | 7338.8041 |
| 2.2804 | 7796.5418 | 7311.2282 | 7273.1709 |
| 2.2914 | 7774.0629 | 7247.6483 | 7207.5377 |
| 2.3024 | 7670.3009 | 7184.2365 | 7141.9045 |
| 2.3134 | 7581.1485 | 7121.0115 | 7076.2712 |
| 2.3244 | 7648.1878 | 7057.9951 | 7010.6380 |
| 2.3354 | 7571.2330 | 6995.2124 | 6945.0048 |
| 2.3464 | 7479.5182 | 6932.6933 | 6879.3716 |
| 2.3574 | 7492.9302 | 6870.4739 | 6813.7384 |
| 2.3684 | 7558.3628 | 6808.5984 | 6748.1051 |
| 2.3794 | 7478.5683 | 6747.0481 | 6682.4719 |
| 2.3904 | 7387.2606 | 6685.9761 | 6616.6959 |
| 2.4014 | 7299.6814 | 6625.3965 | 6550.9198 |
| 2.4124 | 7313.1151 | 6565.5118 | 6485.1437 |
| 2.4234 | 7350.9823 | 6506.4950 | 6419.3677 |
| 2.4344 | 7297.7596 | 6448.5809 | 6353.5916 |
| 2.4454 | 7197.6617 | 6392.0869 | 6287.8156 |
| 2.4564 | 7072.5752 | 6337.4369 | 6222.0395 |
| 2.4674 | 7076.8171 | 6285.1875 | 6156.2634 |
| 2.4784 | 7055.9508 | 6236.0530 | 6090.4874 |
| 2.4894 | 7065.7945 | 6190.9261 | 6024.7113 |
| 2.5004 | 7087.8584 | 6150.8875 | 5958.9353 |
| 2.5114 | 6954.0570 | 6117.1982 | 5893.1592 |
| 2.5224 | 6916.1268 | 6091.2680 | 5827.3831 |
| 2.5334 | 6998.8673 | 6074.5936 | 5761.6071 |
| 2.5444 | 6952.6834 | 6068.6639 | 5695.8310 |
| 2.5554 | 6838.6175 | 6074.8313 | 5630.0550 |
| 2.5664 | 6935.5177 | 6094.1543 | 5564.2789 |
| 2.5774 | 6802.8072 | 6127.2165 | 5498.5028 |
| 2.5884 | 6767.6854 | 6173.9282 | 5432.7268 |
| 2.5994 | 6740.6549 | 6233.3097 | 5366.9507 |
| 2.6104 | 6735.0964 | 6303.2469 | 5301.1747 |
| 2.6214 | 6738.2989 | 6380.2012 | 5235.3986 |
| 2.6324 | 6655.2345 | 6458.8782 | 5169.6226 |
| 2.6434 | 6565.6824 | 6531.9305 | 5103.8465 |
| 2.6544 | 6521.2448 | 6589.9316 | 5038.0704 |
| 2.6654 | 6500.4631 | 6622.0332 | 4972.2944 |
| 2.6764 | 6397.0324 | 6617.6806 | 4906.5183 |
| 2.6874 | 6338.0905 | 6569.2207 | 4840.7423 |
| 2.6984 | 6084.5354 | 6474.3386 | 4774.9662 |
| 2.7094 | 6079.0767 | 6336.8807 | 4709.1901 |
| 2.7204 | 5845.3407 | 6165.5102 | 4643.4141 |
| 2.7314 | 5887.4572 | 5971.0843 | 4577.6380 |
| 2.7424 | 5459.0747 | 5764.2066 | 4511.8620 |
| 2.7534 | 5447.2508 | 5553.7240 | 4446.0859 |
| 2.7644 | 5268.0929 | 5346.5187 | 4380.1670 |
| 2.7754 | 5103.0836 | 5147.3207 | 4314.2481 |
| 2.7864 | 4925.7930 | 4959.3463 | 4248.3292 |
| 2.7974 | 4775.5664 | 4784.3923 | 4182.4103 |
| 2.8084 | 4530.2020 | 4623.1874 | 4116.4914 |
| 2.8194 | 4430.3274 | 4475.6283 | 4050.5725 |
| 2.8304 | 4323.4425 | 4340.9910 | 3984.6536 |
| 2.8414 | 4273.8987 | 4218.1250 | 3918.7347 |
| 2.8524 | 4122.4134 | 4105.6285 | 3852.8158 |
| 2.8634 | 3997.9970 | 4001.9997 | 3786.8969 |
| 2.8744 | 3820.1632 | 3905.7563 | 3720.9780 |
| 2.8854 | 3642.9252 | 3815.5223 | 3655.0591 |
| 2.8964 | 3682.8097 | 3730.0807 | 3589.1402 |
| 2.9074 | 3491.2055 | 3648.3995 | 3523.2213 |
| 2.9184 | 3390.2945 | 3569.6331 | 3457.3024 |
| 2.9294 | 3353.3717 | 3493.1100 | 3391.3836 |
| 2.9404 | 3279.6082 | 3438.0516 | 3325.4647 |
| 2.9514 | 3370.1298 | 3382.6571 | 3297.3630 |
| 2.9624 | 3247.0708 | 3348.0392 | 3269.2613 |
| 2.9734 | 3328.7787 | 3314.2394 | 3241.1597 |
| 2.9844 | 3166.6657 | 3281.0978 | 3213.0580 |
| 2.9954 | 3041.8230 | 3248.4962 | 3184.9563 |
| 3.0064 | 3075.1849 | 3216.3460 | 3156.8547 |
| 3.0174 | 3071.3146 | 3184.5798 | 3128.7530 |
| 3.0284 | 2988.5737 | 3153.1453 | 3100.6514 |
| 3.0394 | 3004.3697 | 3122.0004 | 3072.5497 |
| 3.0504 | 3015.6966 | 3091.1110 | 3044.4480 |
| 3.0614 | 2889.2035 | 3060.4484 | 3016.3464 |
| 3.0724 | 2865.5669 | 3029.9885 | 2988.2447 |
| 3.0834 | 2964.4100 | 2999.7104 | 2960.1431 |
| 3.0944 | 2935.1195 | 2969.5959 | 2932.0414 |
| 3.1054 | 2922.2782 | 2939.6292 | 2903.9397 |
| 3.1164 | 2842.2768 | 2909.7963 | 2875.8381 |
| 3.1274 | 2867.5103 | 2884.9249 | 2847.7364 |
| 3.1384 | 2810.7547 | 2859.7557 | 2828.9065 |
| 3.1494 | 2793.8437 | 2839.5272 | 2810.0765 |
| 3.1604 | 2797.6681 | 2819.3907 | 2791.2466 |
| 3.1714 | 2762.4287 | 2799.3384 | 2772.4166 |
| 3.1824 | 2738.6971 | 2779.3632 | 2753.5867 |
| 3.1934 | 2719.1062 | 2759.4589 | 2734.7567 |
| 3.2044 | 2696.1288 | 2739.6198 | 2715.9268 |
| 3.2154 | 2668.6637 | 2719.8408 | 2697.0968 |
| 3.2264 | 2646.4351 | 2700.1172 | 2678.2669 |
| 3.2374 | 2666.4130 | 2680.4448 | 2659.4369 |
| 3.2484 | 2664.6666 | 2660.8199 | 2640.6070 |
| 3.2594 | 2552.7729 | 2641.2389 | 2621.7770 |
| 3.2704 | 2571.2508 | 2621.6988 | 2602.9471 |
| 3.2814 | 2568.0373 | 2602.1965 | 2584.1171 |
| 3.2924 | 2523.0266 | 2582.7295 | 2565.2872 |
| 3.3034 | 2544.5959 | 2563.2954 | 2546.4572 |
| 3.3144 | 2538.0000 | 2546.2230 | 2527.6273 |
| 3.3254 | 2514.7286 | 2528.9826 | 2513.2627 |
| 3.3364 | 2478.7684 | 2514.0999 | 2498.8981 |
| 3.3474 | 2486.9813 | 2499.2423 | 2484.5336 |
| 3.3584 | 2451.7492 | 2484.4082 | 2470.1690 |
| 3.3694 | 2390.5664 | 2469.5961 | 2455.8044 |
| 3.3804 | 2416.8648 | 2454.8047 | 2441.4399 |
| 3.3914 | 2372.3805 | 2440.0326 | 2427.0753 |
| 3.4024 | 2324.4631 | 2425.2789 | 2412.7108 |
| 3.4134 | 2371.1151 | 2410.5423 | 2398.3462 |
| 3.4244 | 2407.3687 | 2395.8220 | 2383.9816 |
| 3.4354 | 2357.8033 | 2381.1169 | 2369.6171 |
| 3.4464 | 2326.1013 | 2366.4262 | 2355.2525 |
| 3.4574 | 2291.4100 | 2351.7492 | 2340.8879 |
| 3.4684 | 2303.5438 | 2337.0850 | 2326.5234 |
| 3.4794 | 2253.4769 | 2322.4331 | 2312.1588 |
| 3.4904 | 2288.8407 | 2307.7926 | 2297.7942 |
| 3.5014 | 2318.9410 | 2293.6504 | 2283.4297 |
| 3.5124 | 2246.6126 | 2279.4775 | 2269.9987 |
| 3.5234 | 2283.9204 | 2265.8608 | 2256.5678 |
| 3.5344 | 2262.2827 | 2252.2604 | 2243.1368 |
| 3.5454 | 2232.3510 | 2238.6343 | 2229.7058 |
| 3.5564 | 2265.6519 | 2225.0202 | 2216.2749 |
| 3.5674 | 2126.2074 | 2211.3816 | 2202.8439 |
| 3.5784 | 2192.1888 | 2197.7506 | 2189.4130 |
| 3.5894 | 2150.6991 | 2184.1270 | 2175.9820 |
| 3.6004 | 2147.3373 | 2170.5103 | 2162.5510 |
| 3.6114 | 2087.0570 | 2156.9003 | 2149.1201 |
| 3.6224 | 2152.2921 | 2143.2966 | 2135.6891 |
| 3.6334 | 2075.3490 | 2129.6990 | 2122.2582 |
| 3.6444 | 2093.0743 | 2116.1072 | 2108.8272 |
| 3.6554 | 2059.6608 | 2102.5210 | 2095.3962 |
| 3.6664 | 2035.7370 | 2088.9400 | 2081.9653 |
| 3.6774 | 2112.0099 | 2075.3641 | 2068.5343 |
| 3.6884 | 2007.7699 | 2063.5856 | 2055.1034 |
| 3.6994 | 2055.3904 | 2051.6606 | 2045.1063 |
| 3.7104 | 2069.3358 | 2041.5325 | 2035.1092 |
| 3.7214 | 2065.4130 | 2031.4087 | 2025.1120 |
| 3.7324 | 1974.8195 | 2021.2891 | 2015.1149 |
| 3.7434 | 2032.9971 | 2011.1734 | 2005.1178 |
| 3.7544 | 2096.1652 | 2001.0614 | 1995.1207 |
| 3.7654 | 1969.4798 | 1990.9532 | 1985.1236 |
| 3.7764 | 1950.3171 | 1980.8484 | 1975.1265 |
| 3.7874 | 1891.5221 | 1970.7470 | 1965.1294 |
| 3.7984 | 2010.7487 | 1960.6488 | 1955.1323 |
| 3.8094 | 1937.2291 | 1950.5538 | 1945.1352 |
| 3.8204 | 1890.3171 | 1940.4618 | 1935.1381 |
| 3.8314 | 1933.0973 | 1930.3727 | 1925.1410 |
| 3.8424 | 1863.5265 | 1920.2864 | 1915.1439 |
| 3.8534 | 1857.0767 | 1910.2028 | 1905.1468 |
| 3.8644 | 1885.4562 | 1900.1219 | 1895.1496 |
| 3.8754 | 1871.0266 | 1891.5104 | 1885.1525 |
| 3.8864 | 1911.2876 | 1882.7776 | 1877.9656 |
| 3.8974 | 1896.5595 | 1875.5141 | 1870.7786 |
| 3.9084 | 1828.5993 | 1868.2529 | 1863.5917 |
| 3.9194 | 1813.6637 | 1860.9939 | 1856.4047 |
| 3.9304 | 1830.0374 | 1853.7370 | 1849.2178 |
| 3.9414 | 1854.2065 | 1846.4822 | 1842.0308 |
| 3.9524 | 1803.2979 | 1839.2295 | 1834.8439 |
| 3.9634 | 1810.7050 | 1831.9787 | 1827.6569 |
| 3.9744 | 1856.1996 | 1824.7298 | 1820.4700 |
| 3.9854 | 1841.9557 | 1817.4827 | 1813.2830 |
| 3.9964 | 1801.8987 | 1810.2374 | 1806.0961 |
| 4.0074 | 1807.3697 | 1802.9939 | 1798.9091 |
| 4.0184 | 1792.5663 | 1795.7520 | 1791.7222 |
| 4.0294 | 1731.5388 | 1788.5119 | 1784.5352 |
| 4.0404 | 1746.7139 | 1781.2733 | 1777.3483 |
| 4.0514 | 1754.3098 | 1774.0363 | 1770.1613 |
| 4.0624 | 1788.7330 | 1766.9352 | 1762.9744 |
| 4.0734 | 1769.0285 | 1759.8244 | 1756.0449 |
| 4.0844 | 1738.2964 | 1752.8494 | 1749.1155 |
| 4.0954 | 1687.9469 | 1745.8758 | 1742.1860 |
| 4.1064 | 1705.8019 | 1738.9036 | 1735.2566 |
| 4.1174 | 1751.4071 | 1731.9328 | 1728.3271 |
| 4.1284 | 1703.3235 | 1724.9634 | 1721.3977 |
| 4.1394 | 1685.8466 | 1717.9953 | 1714.4682 |
| 4.1504 | 1693.1254 | 1711.0284 | 1707.5388 |
| 4.1614 | 1692.6834 | 1704.0629 | 1700.6093 |
| 4.1724 | 1690.1175 | 1697.0986 | 1693.6799 |
| 4.1834 | 1721.0708 | 1690.1356 | 1686.7504 |
| 4.1944 | 1697.7856 | 1683.1738 | 1679.8210 |

Scan List

| Vis. | Dataset Name | Start pos. [°2θ] | End pos. [°2θ] | Step [°2θ] | Meas.Date/Time |
| --- | --- | --- | --- | --- | --- |
| * | 17 Etosha22 wetsub 15cm S3 550C | 2.0054 | 29.9894 | 0.0110 | 12/8/2023 12:35:07 PM |

Peak List

| Pos. [°2θ] | Height [cts] | FWHM Left [°2θ] | d-spacing [Å] | Rel. Int. [%] |
| --- | --- | --- | --- | --- |
| 2.6838 | 1544.23 | 0.1732 | 32.89290 | 100.00 |
| 5.2607 | 132.27 | 0.1732 | 16.78508 | 8.57 |
| 8.7136 | 1284.89 | 0.0649 | 10.13994 | 83.21 |
| 10.5894 | 66.00 | 0.4330 | 8.34751 | 4.27 |
| 15.8315 | 705.64 | 0.1948 | 5.59336 | 45.70 |
| 17.6142 | 104.19 | 0.1299 | 5.03107 | 6.75 |
| 18.2801 | 73.45 | 0.1299 | 4.84926 | 4.76 |
| 19.5894 | 55.38 | 0.3464 | 4.52802 | 3.59 |
| 22.4701 | 36.22 | 0.3464 | 3.95360 | 2.35 |
| 25.9244 | 352.72 | 0.1732 | 3.43411 | 22.84 |
| 26.6734 | 216.92 | 0.2598 | 3.33935 | 14.05 |
| 27.4806 | 221.59 | 0.1299 | 3.24307 | 14.35 |

Pattern List

| Visible | Ref.Code | Score | Compound Name | Chem. Formula | Mineral Name | SemiQuant[%] |
| --- | --- | --- | --- | --- | --- | --- |
| * | 01-072-4625 | 60 | Sodium Aluminum Silicate Hydrate | Na Al ( Si2 O6 ) ( H2 O ) | Analcime | 14 |
| * | 04-014-4588 | 29 | Potassium Sodium Magnesium Aluminum Iron Silicon Titanium Oxide Fluoride Hydroxide | K0.904 Na0.055 Mg1.362 Ti0.178 Fe1.205 Al1.414 Si2.831 O10.371 ( O H )1.169 F0.46 | Phlogopite-1M, Fe+2-bearing | 21 |
| * | 04-008-7810 | 53 | Titanium Oxide | Ti O2 | Rutile | 3 |
| * | 04-013-5979 | 13 | Magnesium Aluminum Silicon Oxide Hydroxide Hydrate | Mg Al Si4 O10 ( O H ) ( H2 O )4 | Palygorskite-M | 12 |
| * | 04-014-4556 | 1 | Magnesium Silicon Oxide Hydroxide Hydrate | Mg4 Si6 O15 ( O H )2 ( H2 O )6 | Sepiolite | 19 |
| * | 04-025-4215 | 27 | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide | Mg10.4 V0.36 Mn33.5 Fe0.14 Al0.69 Si6.77 As6.5 P0.3 O54 ( O H )42 | Carlfrancisite | 25 |
| * | 04-017-1621 | 5 | Calcium Magnesium Iron Silicate Hydroxide | Ca2 Mg2.5 Fe2.5 Si8 O22 ( O H )2 | Actinolite | 6 |

Anchor Scan Parameters

Dataset Name	17 Etosha22 wetsub 15cm S3 550C

File name	C:\aeris_data\XRD data\Goldstein\Etosha 2023\Etosha Clay Data\Sample 17\17 Etosha22 wetsub 15cm S3 550C.xrdml

Sample Identification	17 Etosha22 wetsub 15cm S3 550C

Measurement Start Date/Time	12/8/2023 12:35:07 PM

Operator	Instrument

Raw Data Origin	XRD measurement (*.XRDML)

Scan Axis	Gonio

Start Position [°2θ]	2.0054

End Position [°2θ]	29.9894

Step Size [°2θ]	0.0110

Scan Step Time [s]	48.1950

Scan Type	Continuous

PSD Mode	Scanning

PSD Length [°2θ]	5.54

Offset [°2θ]	0.0000

Divergence Slit Type	Fixed

Divergence Slit Size [°]	0.0603

Specimen Length [mm]	10.00

Measurement Temperature [°C]	25.00

Anode Material	Cu

K-α1 [Å]	1.54060

K-α2 [Å]	1.54443

K-β1 [Å]	1.39225

K-A2 / K-A1 Ratio	0.50000

Generator Settings	15 mA, 40 kV

Diffractometer Type	2082464

Diffractometer Number	0

Goniometer Radius [mm]	145.00

Dist. Focus-Diverg. Slit [mm]	95.00

Incident Beam Monochromator	No

Spinning	Yes