17 Etosha22 wetsub 15cm S3 GYLCOLATED

Graphics

Graphics

Graphics

Quantitative Results

Phase Potassium Iron Magnesium Aluminum Silicate Hydroxide

Weight fraction/ %	11.0

Phase Sodium Aluminum Silicon Oxide Hydrate

Weight fraction/ %	20.0

Phase Titanium Oxide

Weight fraction/ %	3.0

Phase Magnesium Aluminum Silicon Oxide Hydroxide Hydrate

Weight fraction/ %	11.0

Phase Magnesium Silicon Oxide Hydroxide Hydrate

Weight fraction/ %	3.0

Phase Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide

Weight fraction/ %	47.0

Phase Sodium Calcium Aluminum Silicate

Weight fraction/ %	5.0

Multiple Quantitative Results

Scans vs Phases Matrix

| Scan name | Potassium Iron Magnesium Aluminum Silicate Hydroxide | Sodium Aluminum Silicon Oxide Hydrate | Titanium Oxide | Magnesium Aluminum Silicon Oxide Hydroxide Hydrate | Magnesium Silicon Oxide Hydroxide Hydrate | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide | Sodium Calcium Aluminum Silicate |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 17 Etosha22 wetsub 15cm S3 glycol | 11.0 | 20.0 | 3.0 | 11.0 | 3.0 | 47.0 | 5.0 |

Anchor Scan Data

| Pos. [°2θ] | Iobs [cts] | Icalc [cts] | Iback [cts] |
| --- | --- | --- | --- |
| 2.0054 | 8686.0000 | 8667.2623 | 8686.0000 |
| 2.0164 | 8634.2134 | 8635.0563 | 8622.8074 |
| 2.0274 | 8567.9027 | 8572.2280 | 8559.6148 |
| 2.0384 | 8445.5531 | 8509.4169 | 8496.4223 |
| 2.0494 | 8456.4110 | 8446.6240 | 8433.2297 |
| 2.0604 | 8390.1957 | 8383.8505 | 8370.0371 |
| 2.0714 | 8422.4808 | 8321.0976 | 8306.8445 |
| 2.0824 | 8224.3781 | 8258.3668 | 8243.6519 |
| 2.0934 | 8316.1337 | 8195.6596 | 8180.4594 |
| 2.1044 | 8244.5531 | 8132.9776 | 8117.2668 |
| 2.1154 | 8241.2566 | 8070.3225 | 8054.0742 |
| 2.1264 | 8181.4031 | 8007.6963 | 7990.8816 |
| 2.1374 | 8123.3864 | 7945.1011 | 7927.6890 |
| 2.1484 | 7965.3501 | 7882.5392 | 7864.4965 |
| 2.1594 | 7994.8800 | 7820.0132 | 7801.3039 |
| 2.1704 | 7942.3348 | 7757.5257 | 7738.1113 |
| 2.1814 | 7916.1927 | 7695.0798 | 7674.9187 |
| 2.1924 | 7944.2694 | 7632.5886 | 7611.7261 |
| 2.2034 | 7838.3274 | 7570.1402 | 7548.3471 |
| 2.2144 | 7792.3648 | 7507.6542 | 7484.9681 |
| 2.2254 | 7906.1504 | 7445.2253 | 7421.5891 |
| 2.2364 | 7841.0575 | 7382.8585 | 7358.2101 |
| 2.2474 | 7749.5762 | 7320.5592 | 7294.8311 |
| 2.2584 | 7785.4095 | 7258.3336 | 7231.4521 |
| 2.2694 | 7738.5959 | 7196.1886 | 7168.0731 |
| 2.2804 | 7699.7655 | 7134.1315 | 7104.6941 |
| 2.2914 | 7659.9823 | 7072.1711 | 7041.3151 |
| 2.3024 | 7583.5708 | 7010.3169 | 6977.9361 |
| 2.3134 | 7540.2743 | 6948.5795 | 6914.5571 |
| 2.3244 | 7414.2085 | 6886.9711 | 6851.1781 |
| 2.3354 | 7449.2330 | 6825.5056 | 6787.7991 |
| 2.3464 | 7443.2483 | 6764.1986 | 6724.4201 |
| 2.3574 | 7474.0029 | 6703.0682 | 6661.0411 |
| 2.3684 | 7355.4189 | 6642.1354 | 6597.6621 |
| 2.3794 | 7381.4454 | 6581.3517 | 6534.2831 |
| 2.3904 | 7378.9287 | 6520.8151 | 6470.7532 |
| 2.4014 | 7297.2478 | 6460.4931 | 6407.2234 |
| 2.4124 | 7232.9410 | 6400.5037 | 6343.6936 |
| 2.4234 | 7138.0413 | 6340.9043 | 6280.1638 |
| 2.4344 | 7189.2065 | 6281.7700 | 6216.6340 |
| 2.4454 | 7193.3412 | 6223.2011 | 6153.1041 |
| 2.4564 | 7048.2925 | 6165.3325 | 6089.5743 |
| 2.4674 | 6935.2330 | 6108.3479 | 6026.0445 |
| 2.4784 | 6988.3840 | 6052.4953 | 5962.5147 |
| 2.4894 | 7031.1219 | 5998.1081 | 5898.9848 |
| 2.5004 | 7077.1239 | 5945.6267 | 5835.4550 |
| 2.5114 | 7020.9341 | 5895.6217 | 5771.9252 |
| 2.5224 | 6884.8579 | 5848.8141 | 5708.3954 |
| 2.5334 | 6740.8643 | 5806.0881 | 5644.8655 |
| 2.5444 | 6760.4985 | 5768.4920 | 5581.3357 |
| 2.5554 | 6785.9597 | 5737.2192 | 5517.8059 |
| 2.5664 | 6689.3908 | 5713.5663 | 5454.2761 |
| 2.5774 | 6649.0305 | 5698.8618 | 5390.7462 |
| 2.5884 | 6623.0344 | 5694.3656 | 5327.2164 |
| 2.5994 | 6575.8053 | 5701.1409 | 5263.6866 |
| 2.6104 | 6628.9528 | 5719.9023 | 5200.1568 |
| 2.6214 | 6698.4798 | 5750.8471 | 5136.6269 |
| 2.6324 | 6562.9720 | 5793.4698 | 5073.0971 |
| 2.6434 | 6527.2281 | 5846.3562 | 5009.5673 |
| 2.6544 | 6418.6214 | 5906.9447 | 4946.0375 |
| 2.6654 | 6379.6372 | 5971.2469 | 4882.5076 |
| 2.6764 | 6248.5437 | 6033.5668 | 4818.9778 |
| 2.6874 | 6220.7650 | 6086.3623 | 4755.4480 |
| 2.6984 | 6181.8628 | 6120.5463 | 4691.9182 |
| 2.7094 | 6090.3373 | 6126.5830 | 4628.3884 |
| 2.7204 | 5868.4715 | 6096.4559 | 4564.8585 |
| 2.7314 | 5693.0737 | 6025.9224 | 4501.3287 |
| 2.7424 | 5640.1185 | 5915.9092 | 4437.7989 |
| 2.7534 | 5451.1258 | 5772.1158 | 4374.2691 |
| 2.7644 | 5309.8377 | 5603.3997 | 4310.5884 |
| 2.7754 | 5051.8161 | 5419.2407 | 4246.9078 |
| 2.7864 | 4892.5723 | 5228.3344 | 4183.2271 |
| 2.7974 | 4606.8584 | 5037.5899 | 4119.5465 |
| 2.8084 | 4650.0605 | 4852.0914 | 4055.8658 |
| 2.8194 | 4446.1681 | 4675.3085 | 3992.1852 |
| 2.8304 | 4250.7743 | 4509.3831 | 3928.5045 |
| 2.8414 | 4024.8889 | 4355.3955 | 3864.8239 |
| 2.8524 | 4032.7139 | 4213.5903 | 3801.1433 |
| 2.8634 | 3862.3923 | 4083.5741 | 3737.4626 |
| 2.8744 | 3788.9725 | 3964.4958 | 3673.7820 |
| 2.8854 | 3741.7689 | 3855.2095 | 3610.1013 |
| 2.8964 | 3515.0044 | 3754.4192 | 3546.4207 |
| 2.9074 | 3488.7964 | 3660.7982 | 3482.7400 |
| 2.9184 | 3335.7301 | 3573.0789 | 3419.0594 |
| 2.9294 | 3276.9853 | 3490.1144 | 3355.3788 |
| 2.9404 | 3360.4523 | 3425.8396 | 3291.6981 |
| 2.9514 | 3240.5742 | 3365.4324 | 3258.8070 |
| 2.9624 | 3220.4661 | 3322.2198 | 3225.9159 |
| 2.9734 | 3249.5349 | 3280.7498 | 3193.0248 |
| 2.9844 | 3053.3756 | 3240.6213 | 3160.1337 |
| 2.9954 | 3046.8053 | 3201.5323 | 3127.2426 |
| 3.0064 | 2971.4268 | 3163.2588 | 3094.3515 |
| 3.0174 | 3040.1072 | 3125.6353 | 3061.4604 |
| 3.0284 | 2974.8481 | 3088.5398 | 3028.5692 |
| 3.0394 | 2924.1730 | 3051.8819 | 2995.6781 |
| 3.0504 | 2854.8678 | 3015.5928 | 2962.7870 |
| 3.0614 | 2873.5634 | 2979.6201 | 2929.8959 |
| 3.0724 | 2822.9243 | 2943.9222 | 2897.0048 |
| 3.0834 | 2812.4543 | 2908.4654 | 2864.1137 |
| 3.0944 | 2820.0487 | 2873.2223 | 2831.2226 |
| 3.1054 | 2795.8171 | 2838.1694 | 2798.3315 |
| 3.1164 | 2743.5521 | 2803.2868 | 2765.4404 |
| 3.1274 | 2736.8997 | 2776.7820 | 2732.5493 |
| 3.1384 | 2674.2453 | 2750.9296 | 2716.6218 |
| 3.1494 | 2731.5054 | 2733.4268 | 2700.6943 |
| 3.1604 | 2764.6312 | 2716.0373 | 2684.7668 |
| 3.1714 | 2638.2055 | 2698.7508 | 2668.8394 |
| 3.1824 | 2641.3097 | 2681.5580 | 2652.9119 |
| 3.1934 | 2595.2743 | 2664.4509 | 2636.9844 |
| 3.2044 | 2619.6657 | 2647.4221 | 2621.0569 |
| 3.2154 | 2607.1819 | 2630.4651 | 2605.1295 |
| 3.2264 | 2523.9145 | 2613.5740 | 2589.2020 |
| 3.2374 | 2513.9361 | 2596.7434 | 2573.2745 |
| 3.2484 | 2520.1111 | 2579.9687 | 2557.3470 |
| 3.2594 | 2535.7020 | 2563.2454 | 2541.4195 |
| 3.2704 | 2492.6155 | 2546.5698 | 2525.4921 |
| 3.2814 | 2493.4848 | 2529.9382 | 2509.5646 |
| 3.2924 | 2471.4867 | 2513.3475 | 2493.6371 |
| 3.3034 | 2491.7758 | 2496.7947 | 2477.7096 |
| 3.3144 | 2502.4661 | 2480.6257 | 2461.7822 |
| 3.3254 | 2426.6312 | 2464.5114 | 2446.5737 |
| 3.3364 | 2348.8692 | 2448.7762 | 2431.3652 |
| 3.3474 | 2375.9391 | 2433.0697 | 2416.1568 |
| 3.3584 | 2359.1829 | 2417.3898 | 2400.9483 |
| 3.3694 | 2319.6382 | 2401.7349 | 2385.7399 |
| 3.3804 | 2336.9813 | 2386.1033 | 2370.5314 |
| 3.3914 | 2345.9469 | 2370.4938 | 2355.3229 |
| 3.4024 | 2306.2207 | 2354.9048 | 2340.1145 |
| 3.4134 | 2290.8093 | 2339.3352 | 2324.9060 |
| 3.4244 | 2341.6918 | 2323.7838 | 2309.6976 |
| 3.4354 | 2319.5536 | 2308.2496 | 2294.4891 |
| 3.4464 | 2227.5467 | 2292.7317 | 2279.2806 |
| 3.4574 | 2219.3658 | 2277.2290 | 2264.0722 |
| 3.4684 | 2175.5290 | 2261.7408 | 2248.8637 |
| 3.4794 | 2197.8771 | 2246.2662 | 2233.6553 |
| 3.4904 | 2205.6062 | 2230.8047 | 2218.4468 |
| 3.5014 | 2217.8486 | 2216.5841 | 2203.2383 |
| 3.5124 | 2193.0708 | 2202.4521 | 2190.5642 |
| 3.5234 | 2178.0885 | 2189.5599 | 2177.8901 |
| 3.5344 | 2155.6209 | 2176.6783 | 2165.2160 |
| 3.5454 | 2120.7738 | 2163.8067 | 2152.5419 |
| 3.5564 | 2108.0678 | 2150.9446 | 2139.8677 |
| 3.5674 | 2047.3736 | 2138.0917 | 2127.1936 |
| 3.5784 | 2062.6082 | 2125.2475 | 2114.5195 |
| 3.5894 | 2040.1239 | 2112.4116 | 2101.8454 |
| 3.6004 | 2001.8407 | 2099.5836 | 2089.1713 |
| 3.6114 | 2056.7650 | 2086.7633 | 2076.4972 |
| 3.6224 | 2092.3628 | 2073.9503 | 2063.8230 |
| 3.6334 | 2023.2832 | 2061.1444 | 2051.1489 |
| 3.6444 | 2051.0625 | 2048.3451 | 2038.4748 |
| 3.6554 | 1987.4454 | 2035.5524 | 2025.8007 |
| 3.6664 | 1950.8894 | 2022.7659 | 2013.1266 |
| 3.6774 | 2017.3275 | 2009.9854 | 2000.4524 |
| 3.6884 | 2005.1062 | 1998.9930 | 1987.7783 |
| 3.6994 | 1984.1436 | 1988.1177 | 1978.7802 |
| 3.7104 | 1940.3648 | 1979.0300 | 1969.7822 |
| 3.7214 | 2016.7316 | 1969.9476 | 1960.7841 |
| 3.7324 | 1957.0619 | 1960.8703 | 1951.7860 |
| 3.7434 | 1990.6214 | 1951.7980 | 1942.7879 |
| 3.7544 | 1956.7375 | 1942.7304 | 1933.7898 |
| 3.7654 | 1928.9026 | 1933.6675 | 1924.7918 |
| 3.7764 | 1778.2345 | 1924.6091 | 1915.7937 |
| 3.7874 | 1931.6018 | 1915.5551 | 1906.7956 |
| 3.7984 | 1866.0688 | 1906.5054 | 1897.7975 |
| 3.8094 | 1885.1504 | 1897.4600 | 1888.7994 |
| 3.8204 | 1835.2227 | 1888.4187 | 1879.8014 |
| 3.8314 | 1944.7424 | 1879.3814 | 1870.8033 |
| 3.8424 | 1891.7891 | 1870.3481 | 1861.8052 |
| 3.8534 | 1899.1209 | 1861.3186 | 1852.8071 |
| 3.8644 | 1803.7050 | 1852.2930 | 1843.8090 |
| 3.8754 | 1848.8948 | 1845.1618 | 1834.8110 |
| 3.8864 | 1849.7566 | 1838.1524 | 1829.7122 |
| 3.8974 | 1779.2812 | 1833.0373 | 1824.6135 |
| 3.9084 | 1795.7365 | 1827.9259 | 1819.5148 |
| 3.9194 | 1796.2891 | 1822.8180 | 1814.4160 |
| 3.9304 | 1842.0762 | 1817.7137 | 1809.3173 |
| 3.9414 | 1785.9361 | 1812.6129 | 1804.2185 |
| 3.9524 | 1839.1917 | 1807.5157 | 1799.1198 |
| 3.9634 | 1814.7315 | 1802.4219 | 1794.0211 |
| 3.9744 | 1788.2110 | 1797.3316 | 1788.9223 |
| 3.9854 | 1866.8053 | 1792.2449 | 1783.8236 |
| 3.9964 | 1819.1140 | 1787.1616 | 1778.7249 |
| 4.0074 | 1785.0000 | 1782.0818 | 1773.6261 |
| 4.0184 | 1769.7950 | 1777.0055 | 1768.5274 |
| 4.0294 | 1722.4307 | 1771.9327 | 1763.4287 |
| 4.0404 | 1726.4892 | 1766.8634 | 1758.3299 |
| 4.0514 | 1750.1445 | 1761.7977 | 1753.2312 |
| 4.0624 | 1738.6755 | 1757.3888 | 1748.1325 |
| 4.0734 | 1737.6254 | 1753.0244 | 1744.3810 |
| 4.0844 | 1809.0310 | 1749.3168 | 1740.6296 |
| 4.0954 | 1799.9587 | 1745.6130 | 1736.8781 |
| 4.1064 | 1749.1553 | 1741.9128 | 1733.1267 |
| 4.1174 | 1701.9528 | 1738.2165 | 1729.3753 |
| 4.1284 | 1713.4592 | 1734.5240 | 1725.6238 |
| 4.1394 | 1711.9823 | 1730.8354 | 1721.8724 |
| 4.1504 | 1751.0693 | 1727.1509 | 1718.1209 |
| 4.1614 | 1692.8191 | 1723.4704 | 1714.3695 |
| 4.1724 | 1719.7631 | 1719.7940 | 1710.6181 |
| 4.1834 | 1770.8319 | 1716.1218 | 1706.8666 |
| 4.1944 | 1738.1234 | 1712.4540 | 1703.1152 |

Scan List

| Vis. | Dataset Name | Start pos. [°2θ] | End pos. [°2θ] | Step [°2θ] | Meas.Date/Time |
| --- | --- | --- | --- | --- | --- |
| * | 17 Etosha22 wetsub 15cm S3 glycol | 2.0054 | 29.9894 | 0.0110 | 12/8/2023 9:26:21 AM |

Peak List

| Pos. [°2θ] | Height [cts] | FWHM Left [°2θ] | d-spacing [Å] | Rel. Int. [%] |
| --- | --- | --- | --- | --- |
| 2.7218 | 1372.99 | 0.1732 | 32.43365 | 100.00 |
| 5.3206 | 408.30 | 0.3897 | 16.59629 | 29.74 |
| 6.9997 | 1212.94 | 0.0758 | 12.61837 | 88.34 |
| 8.7216 | 733.70 | 0.1732 | 10.13064 | 53.44 |
| 13.2604 | 19.58 | 0.6927 | 6.67152 | 1.43 |
| 15.7119 | 1305.72 | 0.1191 | 5.63566 | 95.10 |
| 17.6143 | 84.78 | 0.2165 | 5.03104 | 6.18 |
| 18.1681 | 207.95 | 0.0866 | 4.87893 | 15.15 |
| 19.6445 | 74.31 | 0.5196 | 4.51544 | 5.41 |
| 20.8428 | 48.90 | 0.1299 | 4.25847 | 3.56 |
| 22.3668 | 27.51 | 0.2598 | 3.97163 | 2.00 |
| 23.3754 | 54.53 | 0.1732 | 3.80250 | 3.97 |
| 24.1472 | 61.89 | 0.1732 | 3.68268 | 4.51 |
| 25.8572 | 1298.16 | 0.1082 | 3.44288 | 94.55 |
| 26.6635 | 344.15 | 0.1515 | 3.34057 | 25.07 |
| 27.4806 | 132.44 | 0.1515 | 3.24307 | 9.65 |

Pattern List

| Visible | Ref.Code | Score | Compound Name | Chem. Formula | Mineral Name | SemiQuant[%] |
| --- | --- | --- | --- | --- | --- | --- |
| * | 00-042-1437 | 38 | Potassium Iron Magnesium Aluminum Silicate Hydroxide | K ( Mg , Fe )3 ( Al , Fe ) Si3 O10 ( O H , F )2 | Phlogopite-1M, Fe+2-bearing | 11 |
| * | 04-009-3254 | 34 | Sodium Aluminum Silicon Oxide Hydrate | Na8 Al8 Si16 O48 ( H2 O )8 | Analcime | 20 |
| * | 04-008-7810 | 33 | Titanium Oxide | Ti O2 | Rutile | 3 |
| * | 04-015-2963 | 16 | Magnesium Aluminum Silicon Oxide Hydroxide Hydrate | Mg Al Si4 O10 ( O H ) ( H2 O )4 | Palygorskite-M | 11 |
| * | 01-080-5781 | 7 | Magnesium Silicon Oxide Hydroxide Hydrate | Mg8 ( Si12 O30 ( O H )4 ( H2 O )3.92 ) ( H2 O )7.72 | Sepiolite | 3 |
| * | 04-025-4215 | 15 | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide | Mg10.4 V0.36 Mn33.5 Fe0.14 Al0.69 Si6.77 As6.5 P0.3 O54 ( O H )42 | Carlfrancisite | 47 |
| * | 01-078-0432 | 26 | Sodium Calcium Aluminum Silicate | ( Na0.45 Ca0.55 ) ( Al1.55 Si2.45 O8 ) | Anorthite, Na-bearing, syn | 5 |

Anchor Scan Parameters

Dataset Name	17 Etosha22 wetsub 15cm S3 glycol

File name	C:\aeris_data\XRD data\Goldstein\Etosha 2023\Etosha Clay Data\Sample 17\17 Etosha22 wetsub 15cm S3 glycol.xrdml

Sample Identification	17 Etosha22 wetsub 15cm S3 glycol

Measurement Start Date/Time	12/8/2023 9:26:21 AM

Operator	Instrument

Raw Data Origin	XRD measurement (*.XRDML)

Scan Axis	Gonio

Start Position [°2θ]	2.0054

End Position [°2θ]	29.9894

Step Size [°2θ]	0.0110

Scan Step Time [s]	48.1950

Scan Type	Continuous

PSD Mode	Scanning

PSD Length [°2θ]	5.54

Offset [°2θ]	0.0000

Divergence Slit Type	Fixed

Divergence Slit Size [°]	0.0603

Specimen Length [mm]	10.00

Measurement Temperature [°C]	25.00

Anode Material	Cu

K-α1 [Å]	1.54060

K-α2 [Å]	1.54443

K-β1 [Å]	1.39225

K-A2 / K-A1 Ratio	0.50000

Generator Settings	15 mA, 40 kV

Diffractometer Type	2082464

Diffractometer Number	0

Goniometer Radius [mm]	145.00

Dist. Focus-Diverg. Slit [mm]	95.00

Incident Beam Monochromator	No

Spinning	Yes