17 Etosha22 wetsub 15cm S3 regular

Graphics

Graphics

Graphics

Quantitative Results

Phase Sodium Aluminum Silicate Hydrate

Weight fraction/ %	23.0

Phase Potassium Sodium Magnesium Aluminum Iron Titanium Fluoride Silicate Hydroxide

Weight fraction/ %	38.0

Phase Magnesium Silicon Oxide Hydroxide Hydrate

Weight fraction/ %	13.0

Phase Magnesium Aluminum Silicon Oxide Hydroxide Hydrate

Weight fraction/ %	5.0

Phase Potassium Magnesium Aluminum Silicon Titanium Oxide Hydroxide

Weight fraction/ %	17.0

Phase Sodium Calcium Aluminum Silicate

Weight fraction/ %	4.0

Multiple Quantitative Results

Scans vs Phases Matrix

| Scan name | Sodium Aluminum Silicate Hydrate | Potassium Sodium Magnesium Aluminum Iron Titanium Fluoride Silicate Hydroxide | Magnesium Silicon Oxide Hydroxide Hydrate | Magnesium Aluminum Silicon Oxide Hydroxide Hydrate | Potassium Magnesium Aluminum Silicon Titanium Oxide Hydroxide | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide | Titanium Oxide | Sodium Calcium Aluminum Silicate |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 17 Etoshs22 wetsub 15cm S3 | 23.0 | 38.0 | 13.0 | 5.0 | 17.0 | 0.0 | 0.0 | 4.0 |

Anchor Scan Data

| Pos. [°2θ] | Iobs [cts] | Icalc [cts] | Iback [cts] |
| --- | --- | --- | --- |
| 2.0054 | 3700.0000 | 3699.2583 | 3700.0000 |
| 2.0164 | 3675.9587 | 3679.1641 | 3679.1641 |
| 2.0274 | 3750.3206 | 3658.3282 | 3658.3282 |
| 2.0384 | 3644.9218 | 3637.4924 | 3637.4924 |
| 2.0494 | 3666.8368 | 3616.6565 | 3616.6565 |
| 2.0604 | 3628.8717 | 3595.8206 | 3595.8206 |
| 2.0714 | 3670.6696 | 3574.9847 | 3574.9847 |
| 2.0824 | 3465.3033 | 3554.1488 | 3554.1488 |
| 2.0934 | 3591.0836 | 3533.3129 | 3533.3129 |
| 2.1044 | 3545.1150 | 3512.4771 | 3512.4771 |
| 2.1154 | 3537.6313 | 3491.6412 | 3491.6412 |
| 2.1264 | 3527.9695 | 3470.8053 | 3470.8053 |
| 2.1374 | 3481.9676 | 3449.9694 | 3449.9694 |
| 2.1484 | 3454.2694 | 3429.1335 | 3429.1335 |
| 2.1594 | 3345.5064 | 3408.2976 | 3408.2976 |
| 2.1704 | 3376.6091 | 3387.4618 | 3387.4618 |
| 2.1814 | 3393.4602 | 3366.6259 | 3366.6259 |
| 2.1924 | 3346.6131 | 3346.0003 | 3345.7900 |
| 2.2034 | 3262.2743 | 3330.8614 | 3330.8614 |
| 2.2144 | 3404.2394 | 3315.9327 | 3315.9327 |
| 2.2254 | 3413.7424 | 3301.0041 | 3301.0041 |
| 2.2364 | 3354.5133 | 3286.0754 | 3286.0754 |
| 2.2474 | 3307.8368 | 3271.1468 | 3271.1468 |
| 2.2584 | 3301.7173 | 3256.2181 | 3256.2181 |
| 2.2694 | 3285.3658 | 3241.2895 | 3241.2895 |
| 2.2804 | 3254.4528 | 3226.3608 | 3226.3608 |
| 2.2914 | 3258.1347 | 3211.4322 | 3211.4322 |
| 2.3024 | 3225.3761 | 3196.5035 | 3196.5035 |
| 2.3134 | 3225.6165 | 3181.5749 | 3181.5749 |
| 2.3244 | 3221.6529 | 3166.6462 | 3166.6462 |
| 2.3354 | 3145.8938 | 3151.7176 | 3151.7176 |
| 2.3464 | 3161.5270 | 3136.7889 | 3136.7889 |
| 2.3574 | 3187.6401 | 3121.8603 | 3121.8603 |
| 2.3684 | 3129.2434 | 3106.9316 | 3106.9316 |
| 2.3794 | 3055.6863 | 3092.1135 | 3092.0030 |
| 2.3904 | 3058.9774 | 3080.1792 | 3080.1792 |
| 2.4014 | 3064.2743 | 3068.3554 | 3068.3554 |
| 2.4124 | 3049.1662 | 3056.5316 | 3056.5316 |
| 2.4234 | 2991.8505 | 3044.7077 | 3044.7077 |
| 2.4344 | 2958.4956 | 3032.8839 | 3032.8839 |
| 2.4454 | 3007.9469 | 3021.0601 | 3021.0601 |
| 2.4564 | 3022.6145 | 3009.2363 | 3009.2363 |
| 2.4674 | 2972.4513 | 2997.4125 | 2997.4125 |
| 2.4784 | 2954.0875 | 2985.5887 | 2985.5887 |
| 2.4894 | 2968.7444 | 2973.7649 | 2973.7649 |
| 2.5004 | 2923.7566 | 2961.9410 | 2961.9410 |
| 2.5114 | 2822.8997 | 2950.1172 | 2950.1172 |
| 2.5224 | 2853.7001 | 2938.2934 | 2938.2934 |
| 2.5334 | 2894.5103 | 2926.4696 | 2926.4696 |
| 2.5444 | 2858.6824 | 2914.6458 | 2914.6458 |
| 2.5554 | 2892.6952 | 2902.8220 | 2902.8220 |
| 2.5664 | 2860.5546 | 2891.9590 | 2890.9982 |
| 2.5774 | 2878.5221 | 2882.5388 | 2882.5388 |
| 2.5884 | 2975.4912 | 2874.0794 | 2874.0794 |
| 2.5994 | 2887.2124 | 2865.6201 | 2865.6201 |
| 2.6104 | 2837.1681 | 2857.1607 | 2857.1607 |
| 2.6214 | 2783.1180 | 2848.7013 | 2848.7013 |
| 2.6324 | 2791.0295 | 2840.2419 | 2840.2419 |
| 2.6434 | 2734.7119 | 2831.7826 | 2831.7826 |
| 2.6544 | 2795.9214 | 2823.3232 | 2823.3232 |
| 2.6654 | 2862.4484 | 2814.8638 | 2814.8638 |
| 2.6764 | 2816.2689 | 2806.4045 | 2806.4045 |
| 2.6874 | 2797.0000 | 2797.9451 | 2797.9451 |
| 2.6984 | 2749.7655 | 2789.4857 | 2789.4857 |
| 2.7094 | 2774.5447 | 2781.0264 | 2781.0264 |
| 2.7204 | 2785.0000 | 2772.5670 | 2772.5670 |
| 2.7314 | 2710.3687 | 2764.1076 | 2764.1076 |
| 2.7424 | 2776.1736 | 2755.6483 | 2755.6483 |
| 2.7534 | 2759.7325 | 2747.1535 | 2747.1889 |
| 2.7644 | 2721.6209 | 2738.6630 | 2738.6630 |
| 2.7754 | 2778.8073 | 2730.1370 | 2730.1370 |
| 2.7864 | 2816.0526 | 2721.6111 | 2721.6111 |
| 2.7974 | 2755.3982 | 2713.0851 | 2713.0851 |
| 2.8084 | 2692.2679 | 2704.5592 | 2704.5592 |
| 2.8194 | 2669.6283 | 2696.0333 | 2696.0333 |
| 2.8304 | 2656.9381 | 2687.5073 | 2687.5073 |
| 2.8414 | 2645.7247 | 2678.9814 | 2678.9814 |
| 2.8524 | 2669.6067 | 2670.4554 | 2670.4554 |
| 2.8634 | 2699.7611 | 2661.9295 | 2661.9295 |
| 2.8744 | 2687.4061 | 2653.4036 | 2653.4036 |
| 2.8854 | 2711.5821 | 2644.8776 | 2644.8776 |
| 2.8964 | 2757.7965 | 2636.3517 | 2636.3517 |
| 2.9074 | 2667.0865 | 2627.8257 | 2627.8257 |
| 2.9184 | 2677.4154 | 2619.2998 | 2619.2998 |
| 2.9294 | 2649.2596 | 2610.7739 | 2610.7739 |
| 2.9404 | 2654.0919 | 2602.2479 | 2602.2479 |
| 2.9514 | 2595.7640 | 2593.7220 | 2593.7220 |
| 2.9624 | 2650.0973 | 2585.1960 | 2585.1960 |
| 2.9734 | 2546.9381 | 2576.6701 | 2576.6701 |
| 2.9844 | 2586.9489 | 2568.1442 | 2568.1442 |
| 2.9954 | 2642.7433 | 2559.6182 | 2559.6182 |
| 3.0064 | 2551.7915 | 2551.0923 | 2551.0923 |
| 3.0174 | 2593.6008 | 2542.5663 | 2542.5663 |
| 3.0284 | 2665.6873 | 2534.0404 | 2534.0404 |
| 3.0394 | 2556.1554 | 2525.5144 | 2525.5144 |
| 3.0504 | 2552.4734 | 2516.9885 | 2516.9885 |
| 3.0614 | 2527.4808 | 2508.4626 | 2508.4626 |
| 3.0724 | 2509.6563 | 2499.9366 | 2499.9366 |
| 3.0834 | 2496.0895 | 2491.4107 | 2491.4107 |
| 3.0944 | 2534.2080 | 2482.8847 | 2482.8847 |
| 3.1054 | 2492.3530 | 2474.3588 | 2474.3588 |
| 3.1164 | 2496.8613 | 2465.8329 | 2465.8329 |
| 3.1274 | 2485.5487 | 2457.2716 | 2457.3069 |
| 3.1384 | 2534.8289 | 2448.7144 | 2448.7144 |
| 3.1494 | 2475.3382 | 2440.1219 | 2440.1219 |
| 3.1604 | 2423.9543 | 2431.5294 | 2431.5294 |
| 3.1714 | 2497.2625 | 2422.9369 | 2422.9369 |
| 3.1824 | 2483.7409 | 2414.3444 | 2414.3444 |
| 3.1934 | 2393.2124 | 2405.7518 | 2405.7518 |
| 3.2044 | 2445.6794 | 2397.1593 | 2397.1593 |
| 3.2154 | 2452.2802 | 2388.5668 | 2388.5668 |
| 3.2264 | 2450.7065 | 2379.9743 | 2379.9743 |
| 3.2374 | 2422.7148 | 2371.3818 | 2371.3818 |
| 3.2484 | 2421.8333 | 2362.7893 | 2362.7893 |
| 3.2594 | 2420.7375 | 2354.1968 | 2354.1968 |
| 3.2704 | 2413.8083 | 2345.6043 | 2345.6043 |
| 3.2814 | 2442.6136 | 2337.0117 | 2337.0117 |
| 3.2924 | 2391.5088 | 2328.4192 | 2328.4192 |
| 3.3034 | 2329.3441 | 2319.8267 | 2319.8267 |
| 3.3144 | 2320.4626 | 2311.1905 | 2311.2342 |
| 3.3254 | 2329.0738 | 2302.5594 | 2302.5594 |
| 3.3364 | 2338.9744 | 2293.8845 | 2293.8845 |
| 3.3474 | 2315.0246 | 2285.2097 | 2285.2097 |
| 3.3584 | 2282.3230 | 2276.5348 | 2276.5348 |
| 3.3694 | 2302.2527 | 2267.8600 | 2267.8600 |
| 3.3804 | 2343.6278 | 2259.1852 | 2259.1852 |
| 3.3914 | 2316.3009 | 2250.5103 | 2250.5103 |
| 3.4024 | 2234.3181 | 2241.8355 | 2241.8355 |
| 3.4134 | 2244.0069 | 2233.1606 | 2233.1606 |
| 3.4244 | 2298.9086 | 2224.4858 | 2224.4858 |
| 3.4354 | 2292.0757 | 2215.8110 | 2215.8110 |
| 3.4464 | 2256.6455 | 2207.1361 | 2207.1361 |
| 3.4574 | 2196.9410 | 2198.4613 | 2198.4613 |
| 3.4684 | 2207.0826 | 2189.7864 | 2189.7864 |
| 3.4794 | 2208.2960 | 2181.1116 | 2181.1116 |
| 3.4904 | 2220.7345 | 2172.4368 | 2172.4368 |
| 3.5014 | 2138.3067 | 2164.3133 | 2163.7619 |
| 3.5124 | 2126.8776 | 2156.1253 | 2156.1253 |
| 3.5234 | 2164.5811 | 2148.4888 | 2148.4888 |
| 3.5344 | 2130.0757 | 2140.8522 | 2140.8522 |
| 3.5454 | 2157.4071 | 2133.2156 | 2133.2156 |
| 3.5564 | 2204.3215 | 2125.5790 | 2125.5790 |
| 3.5674 | 2102.4552 | 2117.9425 | 2117.9425 |
| 3.5784 | 2097.3353 | 2110.3059 | 2110.3059 |
| 3.5894 | 2121.0885 | 2102.6693 | 2102.6693 |
| 3.6004 | 2078.8500 | 2095.0327 | 2095.0327 |
| 3.6114 | 2131.9430 | 2087.3962 | 2087.3962 |
| 3.6224 | 2148.1932 | 2079.7596 | 2079.7596 |
| 3.6334 | 2135.7139 | 2072.1230 | 2072.1230 |
| 3.6444 | 2048.2006 | 2064.4864 | 2064.4864 |
| 3.6554 | 2063.0590 | 2056.8499 | 2056.8499 |
| 3.6664 | 2039.0418 | 2049.2133 | 2049.2133 |
| 3.6774 | 2049.6283 | 2041.5767 | 2041.5767 |
| 3.6884 | 2029.9867 | 2034.3605 | 2033.9401 |
| 3.6994 | 2014.5005 | 2027.0950 | 2027.0950 |
| 3.7104 | 2070.9273 | 2020.2499 | 2020.2499 |
| 3.7214 | 2038.4690 | 2013.4048 | 2013.4048 |
| 3.7324 | 2026.6327 | 2006.5597 | 2006.5597 |
| 3.7434 | 2112.6628 | 1999.7146 | 1999.7146 |
| 3.7544 | 2041.6578 | 1992.8695 | 1992.8695 |
| 3.7654 | 1971.3068 | 1986.0244 | 1986.0244 |
| 3.7764 | 1995.4292 | 1979.1793 | 1979.1793 |
| 3.7874 | 1991.0442 | 1972.3341 | 1972.3341 |
| 3.7984 | 1976.8623 | 1965.4890 | 1965.4890 |
| 3.8094 | 1937.6765 | 1958.6439 | 1958.6439 |
| 3.8204 | 1977.7861 | 1951.7988 | 1951.7988 |
| 3.8314 | 1901.8466 | 1944.9537 | 1944.9537 |
| 3.8424 | 1920.8427 | 1938.1086 | 1938.1086 |
| 3.8534 | 1900.5841 | 1931.2635 | 1931.2635 |
| 3.8644 | 1905.1406 | 1924.4184 | 1924.4184 |
| 3.8754 | 1875.8221 | 1917.5733 | 1917.5733 |
| 3.8864 | 2036.4159 | 1910.7281 | 1910.7281 |
| 3.8974 | 1942.7719 | 1903.8830 | 1903.8830 |
| 3.9084 | 1929.6283 | 1897.0379 | 1897.0379 |
| 3.9194 | 1856.1298 | 1890.1928 | 1890.1928 |
| 3.9304 | 1882.7173 | 1883.3477 | 1883.3477 |
| 3.9414 | 1854.7955 | 1876.5026 | 1876.5026 |
| 3.9524 | 1865.2286 | 1869.6575 | 1869.6575 |
| 3.9634 | 1861.6096 | 1862.8124 | 1862.8124 |
| 3.9744 | 1822.6008 | 1855.9673 | 1855.9673 |
| 3.9854 | 1816.2566 | 1849.1222 | 1849.1222 |
| 3.9964 | 1782.4808 | 1842.2770 | 1842.2770 |
| 4.0074 | 1828.0521 | 1835.4319 | 1835.4319 |
| 4.0184 | 1812.2876 | 1828.6640 | 1828.5868 |
| 4.0294 | 1776.8771 | 1821.9174 | 1821.7417 |
| 4.0404 | 1768.8431 | 1815.1046 | 1814.8966 |
| 4.0514 | 1776.9322 | 1808.2632 | 1808.0515 |
| 4.0624 | 1868.4872 | 1801.3828 | 1801.2064 |
| 4.0734 | 1785.0000 | 1794.5093 | 1794.2901 |
| 4.0844 | 1777.8938 | 1787.5969 | 1787.3738 |
| 4.0954 | 1781.7768 | 1780.6847 | 1780.4576 |
| 4.1064 | 1810.3102 | 1773.7725 | 1773.5413 |
| 4.1174 | 1765.2094 | 1766.8605 | 1766.6250 |
| 4.1284 | 1740.4243 | 1759.9486 | 1759.7088 |
| 4.1394 | 1772.3127 | 1753.0368 | 1752.7925 |
| 4.1504 | 1763.1092 | 1746.1252 | 1745.8762 |
| 4.1614 | 1810.2694 | 1739.2136 | 1738.9600 |
| 4.1724 | 1856.1067 | 1732.3022 | 1732.0437 |
| 4.1834 | 1796.1238 | 1725.3910 | 1725.1274 |
| 4.1944 | 1754.5787 | 1718.4799 | 1718.2111 |

Scan List

| Vis. | Dataset Name | Start pos. [°2θ] | End pos. [°2θ] | Step [°2θ] | Meas.Date/Time |
| --- | --- | --- | --- | --- | --- |
| * | 17 Etoshs22 wetsub 15cm S3 | 2.0054 | 29.9894 | 0.0110 | 12/7/2023 1:46:49 PM |

Peak List

| Pos. [°2θ] | Height [cts] | FWHM Left [°2θ] | d-spacing [Å] | Rel. Int. [%] |
| --- | --- | --- | --- | --- |
| 5.3146 | 143.02 | 0.1299 | 16.61492 | 6.94 |
| 7.2985 | 2061.03 | 0.1732 | 12.10235 | 100.00 |
| 8.8990 | 667.41 | 0.0758 | 9.92903 | 32.38 |
| 11.7034 | 19.87 | 0.6061 | 7.55534 | 0.96 |
| 12.9288 | 32.45 | 0.5196 | 6.84187 | 1.57 |
| 15.8558 | 1023.23 | 0.0974 | 5.58485 | 49.65 |
| 17.7484 | 82.74 | 0.2165 | 4.99334 | 4.01 |
| 18.3382 | 159.88 | 0.1082 | 4.83404 | 7.76 |
| 19.7146 | 86.09 | 0.4330 | 4.49954 | 4.18 |
| 21.0019 | 40.89 | 0.4330 | 4.22656 | 1.98 |
| 22.5442 | 46.51 | 0.1299 | 3.94078 | 2.26 |
| 23.5487 | 55.43 | 0.1299 | 3.77490 | 2.69 |
| 24.3422 | 48.65 | 0.1299 | 3.65362 | 2.36 |
| 26.0144 | 935.70 | 0.0528 | 3.42243 | 45.40 |
| 26.0700 | 879.86 | 0.0433 | 3.41526 | 42.69 |
| 26.8172 | 278.31 | 0.1299 | 3.32177 | 13.50 |
| 27.6117 | 130.20 | 0.1299 | 3.22797 | 6.32 |

Pattern List

| Visible | Ref.Code | Score | Compound Name | Chem. Formula | Mineral Name | SemiQuant[%] |
| --- | --- | --- | --- | --- | --- | --- |
| * | 01-075-8690 | 61 | Sodium Aluminum Silicate Hydrate | Na1.71 ( ( Al1.806 Si4.194 ) O12 ) ( H2 O )2.16 | Analcime | 23 |
| * | 04-013-1844 | 50 | Potassium Sodium Magnesium Aluminum Iron Titanium Fluoride Silicate Hydroxide | K0.8 Na0.1 Mg1.6 Ti0.3 Fe0.9 Al1.4 Si2.6 O10 ( O H )1.1 F0.9 | Phlogopite-1M | 38 |
| * | 04-014-4556 | 40 | Magnesium Silicon Oxide Hydroxide Hydrate | Mg4 Si6 O15 ( O H )2 ( H2 O )6 | Sepiolite | 13 |
| * | 04-013-5979 | 19 | Magnesium Aluminum Silicon Oxide Hydroxide Hydrate | Mg Al Si4 O10 ( O H ) ( H2 O )4 | Palygorskite-M | 5 |
| * | 04-017-0523 | 18 | Potassium Magnesium Aluminum Silicon Titanium Oxide Hydroxide | K0.78 Mg0.18 Ti0.01 Al2.46 Si3.36 O10 ( O H )2 | Illite (NR) | 17 |
| * | 04-025-4215 | No Matching Lines | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide | Mg10.4 V0.36 Mn33.5 Fe0.14 Al0.69 Si6.77 As6.5 P0.3 O54 ( O H )42 | Carlfrancisite | - |
| * | 04-008-7810 | 9 | Titanium Oxide | Ti O2 | Rutile | - |
| * | 01-078-0432 | 20 | Sodium Calcium Aluminum Silicate | ( Na0.45 Ca0.55 ) ( Al1.55 Si2.45 O8 ) | Anorthite, Na-bearing, syn | 4 |

Anchor Scan Parameters

Dataset Name	17 Etoshs22 wetsub 15cm S3

File name	C:\aeris_data\XRD data\Goldstein\Etosha 2023\Etosha Clay Data\Sample 17\17 Etoshs22 wetsub 15cm S3.xrdml

Sample Identification	17 Etoshs22 wetsub 15cm S3

Measurement Start Date/Time	12/7/2023 1:46:49 PM

Operator	Instrument

Raw Data Origin	XRD measurement (*.XRDML)

Scan Axis	Gonio

Start Position [°2θ]	2.0054

End Position [°2θ]	29.9894

Step Size [°2θ]	0.0110

Scan Step Time [s]	48.1950

Scan Type	Continuous

PSD Mode	Scanning

PSD Length [°2θ]	5.54

Offset [°2θ]	0.0000

Divergence Slit Type	Fixed

Divergence Slit Size [°]	0.0603

Specimen Length [mm]	10.00

Measurement Temperature [°C]	25.00

Anode Material	Cu

K-α1 [Å]	1.54060

K-α2 [Å]	1.54443

K-β1 [Å]	1.39225

K-A2 / K-A1 Ratio	0.50000

Generator Settings	15 mA, 40 kV

Diffractometer Type	2082464

Diffractometer Number	0

Goniometer Radius [mm]	145.00

Dist. Focus-Diverg. Slit [mm]	95.00

Incident Beam Monochromator	No

Spinning	Yes