18 Etosha 22 SSCrt 0-0.5 cm S4 400 C REPORT

Graphics

Graphics

Graphics

Quantitative Results

Phase Sodium Aluminum Silicate Hydrate

Weight fraction/ %	41.0

Phase Potassium Magnesium Manganese Aluminum Iron Silicon Titanium Oxide Fluoride Hydroxide

Weight fraction/ %	28.0

Phase Tin Oxide

Weight fraction/ %	1.0

Phase Potassium Manganese Aluminum Silicon Oxide Hydroxide Hydrate

Weight fraction/ %	2.0

Phase Magnesium Aluminum Iron Silicon Oxide Hydroxide Hydrate

Weight fraction/ %	3.0

Phase Sodium Magnesium Silicon Oxide Hydrate

Weight fraction/ %	3.0

Phase Titanium Oxide

Weight fraction/ %	1.0

Phase Potassium Magnesium Aluminum Fluoride Silicate Hydroxide

Weight fraction/ %	21.0

Multiple Quantitative Results

Scans vs Phases Matrix

| Scan name | Sodium Aluminum Silicate Hydrate | Potassium Magnesium Manganese Aluminum Iron Silicon Titanium Oxide Fluoride Hydroxide | Tin Oxide | Potassium Manganese Aluminum Silicon Oxide Hydroxide Hydrate | Magnesium Aluminum Iron Silicon Oxide Hydroxide Hydrate | Sodium Magnesium Silicon Oxide Hydrate | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide | Magnesium Aluminum Silicate Hydroxide Hydrate | Titanium Oxide | Potassium Magnesium Aluminum Fluoride Silicate Hydroxide |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 18 Etosha22 SSCRT 0-0.5cm S4 400C | 41.0 | 28.0 | 1.0 | 2.0 | 3.0 | 3.0 | 0.0 | 0.0 | 1.0 | 21.0 |

Anchor Scan Data

| Pos. [°2θ] | Iobs [cts] | Icalc [cts] | Iback [cts] |
| --- | --- | --- | --- |
| 2.0054 | 5998.0000 | 5988.0047 | 5998.0000 |
| 2.0164 | 5980.8112 | 5957.6543 | 5957.6543 |
| 2.0274 | 6041.4769 | 5917.3086 | 5917.3086 |
| 2.0384 | 5857.5383 | 5876.9629 | 5876.9629 |
| 2.0494 | 5743.9007 | 5836.6172 | 5836.6172 |
| 2.0604 | 5788.2620 | 5796.2715 | 5796.2715 |
| 2.0714 | 5608.4838 | 5755.9258 | 5755.9258 |
| 2.0824 | 5596.6657 | 5715.5801 | 5715.5801 |
| 2.0934 | 5540.6883 | 5675.2344 | 5675.2344 |
| 2.1044 | 5535.1637 | 5634.8887 | 5634.8887 |
| 2.1154 | 5448.9725 | 5594.5430 | 5594.5430 |
| 2.1264 | 5502.9951 | 5554.1973 | 5554.1973 |
| 2.1374 | 5444.7522 | 5513.8516 | 5513.8516 |
| 2.1484 | 5456.4292 | 5473.5059 | 5473.5059 |
| 2.1594 | 5361.4120 | 5433.1602 | 5433.1602 |
| 2.1704 | 5425.4793 | 5392.8145 | 5392.8145 |
| 2.1814 | 5314.6401 | 5352.4688 | 5352.4688 |
| 2.1924 | 5310.6416 | 5313.3063 | 5312.1231 |
| 2.2034 | 5294.6106 | 5276.5535 | 5276.5535 |
| 2.2144 | 5198.2630 | 5240.9839 | 5240.9839 |
| 2.2254 | 5272.7021 | 5205.4143 | 5205.4143 |
| 2.2364 | 5135.6755 | 5169.8447 | 5169.8447 |
| 2.2474 | 5106.0000 | 5134.2751 | 5134.2751 |
| 2.2584 | 5078.2960 | 5098.7055 | 5098.7055 |
| 2.2694 | 5020.3894 | 5063.1359 | 5063.1359 |
| 2.2804 | 5014.9705 | 5027.5663 | 5027.5663 |
| 2.2914 | 4951.0197 | 4991.9967 | 4991.9967 |
| 2.3024 | 4961.0973 | 4956.4271 | 4956.4271 |
| 2.3134 | 4883.2733 | 4920.8575 | 4920.8575 |
| 2.3244 | 4860.3471 | 4885.2879 | 4885.2879 |
| 2.3354 | 4925.0442 | 4849.7183 | 4849.7183 |
| 2.3464 | 4826.8422 | 4814.1486 | 4814.1486 |
| 2.3574 | 4700.5064 | 4778.5790 | 4778.5790 |
| 2.3684 | 4739.0148 | 4743.0094 | 4743.0094 |
| 2.3794 | 4756.2547 | 4710.2163 | 4707.4398 |
| 2.3904 | 4678.9926 | 4682.4115 | 4682.4115 |
| 2.4014 | 4612.7257 | 4657.3832 | 4657.3832 |
| 2.4124 | 4626.9243 | 4632.3549 | 4632.3549 |
| 2.4234 | 4606.0846 | 4607.5783 | 4607.3266 |
| 2.4344 | 4587.9351 | 4582.8847 | 4582.2983 |
| 2.4454 | 4640.9833 | 4557.9628 | 4557.2699 |
| 2.4564 | 4618.8191 | 4532.9377 | 4532.2416 |
| 2.4674 | 4522.1799 | 4507.9126 | 4507.2133 |
| 2.4784 | 4429.7453 | 4482.8876 | 4482.1850 |
| 2.4894 | 4412.2448 | 4457.8626 | 4457.1567 |
| 2.5004 | 4433.8053 | 4432.8375 | 4432.1283 |
| 2.5114 | 4392.4612 | 4407.8126 | 4407.1000 |
| 2.5224 | 4362.2866 | 4382.7876 | 4382.0717 |
| 2.5334 | 4376.1298 | 4357.7627 | 4357.0434 |
| 2.5444 | 4380.8068 | 4332.7377 | 4332.0151 |
| 2.5554 | 4305.7955 | 4307.7128 | 4306.9867 |
| 2.5664 | 4315.0428 | 4282.6880 | 4281.9584 |
| 2.5774 | 4267.8299 | 4257.6631 | 4256.9301 |
| 2.5884 | 4187.4744 | 4232.6383 | 4231.9018 |
| 2.5994 | 4168.3363 | 4207.6135 | 4206.8735 |
| 2.6104 | 4136.9036 | 4182.5888 | 4181.8452 |
| 2.6214 | 4142.6490 | 4157.5640 | 4156.8168 |
| 2.6324 | 4123.2758 | 4132.5393 | 4131.7885 |
| 2.6434 | 4070.3658 | 4107.5146 | 4106.7602 |
| 2.6544 | 4045.2979 | 4082.4899 | 4081.7319 |
| 2.6654 | 3998.4897 | 4057.4653 | 4056.7036 |
| 2.6764 | 4040.7311 | 4032.4407 | 4031.6752 |
| 2.6874 | 3965.5064 | 4007.4161 | 4006.6469 |
| 2.6984 | 3966.1991 | 3982.3916 | 3981.6186 |
| 2.7094 | 3930.1622 | 3957.3670 | 3956.5903 |
| 2.7204 | 3890.8368 | 3932.3425 | 3931.5620 |
| 2.7314 | 3849.1180 | 3907.3181 | 3906.5336 |
| 2.7424 | 3898.6450 | 3882.2936 | 3881.5053 |
| 2.7534 | 3902.6421 | 3858.4902 | 3856.4770 |
| 2.7644 | 3789.0531 | 3836.8803 | 3836.0842 |
| 2.7754 | 3830.9469 | 3816.4915 | 3815.6914 |
| 2.7864 | 3790.3854 | 3796.1027 | 3795.2986 |
| 2.7974 | 3877.6903 | 3775.7139 | 3774.9058 |
| 2.8084 | 3811.9395 | 3755.3251 | 3754.5130 |
| 2.8194 | 3672.0265 | 3734.9364 | 3734.1202 |
| 2.8304 | 3702.3260 | 3714.5477 | 3713.7274 |
| 2.8414 | 3701.3294 | 3694.1590 | 3693.3346 |
| 2.8524 | 3702.8928 | 3673.7704 | 3672.9417 |
| 2.8634 | 3666.5693 | 3653.3818 | 3652.5489 |
| 2.8744 | 3587.3205 | 3632.9932 | 3632.1561 |
| 2.8854 | 3527.9695 | 3612.6047 | 3611.7633 |
| 2.8964 | 3557.8628 | 3592.2162 | 3591.3705 |
| 2.9074 | 3603.4887 | 3571.8277 | 3570.9777 |
| 2.9184 | 3539.6652 | 3551.4393 | 3550.5849 |
| 2.9294 | 3568.6578 | 3531.0509 | 3530.1921 |
| 2.9404 | 3469.5816 | 3510.6625 | 3509.7993 |
| 2.9514 | 3486.6765 | 3490.2742 | 3489.4065 |
| 2.9624 | 3558.6622 | 3469.8859 | 3469.0137 |
| 2.9734 | 3487.6529 | 3449.4976 | 3448.6209 |
| 2.9844 | 3489.6475 | 3429.1094 | 3428.2281 |
| 2.9954 | 3429.1858 | 3408.7212 | 3407.8353 |
| 3.0064 | 3357.4882 | 3388.3331 | 3387.4424 |
| 3.0174 | 3382.2773 | 3367.9450 | 3367.0496 |
| 3.0284 | 3390.2359 | 3347.5569 | 3346.6568 |
| 3.0394 | 3207.5752 | 3327.1688 | 3326.2640 |
| 3.0504 | 3319.0295 | 3306.7808 | 3305.8712 |
| 3.0614 | 3344.1799 | 3286.3929 | 3285.4784 |
| 3.0724 | 3326.9302 | 3266.0049 | 3265.0856 |
| 3.0834 | 3235.0472 | 3245.6170 | 3244.6928 |
| 3.0944 | 3185.1416 | 3225.2292 | 3224.3000 |
| 3.1054 | 3246.4120 | 3204.8414 | 3203.9072 |
| 3.1164 | 3251.8928 | 3184.4536 | 3183.5144 |
| 3.1274 | 3098.4454 | 3166.9502 | 3163.1216 |
| 3.1384 | 3135.0742 | 3149.5249 | 3148.5755 |
| 3.1494 | 3131.7306 | 3134.9840 | 3134.0295 |
| 3.1604 | 3126.2758 | 3120.4432 | 3119.4834 |
| 3.1714 | 3093.2970 | 3105.9024 | 3104.9374 |
| 3.1824 | 3089.8977 | 3091.3616 | 3090.3913 |
| 3.1934 | 3025.4336 | 3076.8209 | 3075.8452 |
| 3.2044 | 3003.8083 | 3062.2802 | 3061.2992 |
| 3.2154 | 3012.8653 | 3047.7396 | 3046.7531 |
| 3.2264 | 3071.4646 | 3033.1990 | 3032.2071 |
| 3.2374 | 3072.7148 | 3018.6584 | 3017.6610 |
| 3.2484 | 3027.8889 | 3004.1179 | 3003.1150 |
| 3.2594 | 2961.3481 | 2989.5775 | 2988.5689 |
| 3.2704 | 2966.4238 | 2975.0371 | 2974.0229 |
| 3.2814 | 2985.8800 | 2960.4967 | 2959.4768 |
| 3.2924 | 2921.3363 | 2945.9564 | 2944.9307 |
| 3.3034 | 2931.9882 | 2931.4162 | 2930.3847 |
| 3.3144 | 2935.1706 | 2916.8760 | 2915.8386 |
| 3.3254 | 2892.6962 | 2902.3358 | 2901.2926 |
| 3.3364 | 2943.8737 | 2887.7957 | 2886.7465 |
| 3.3474 | 2888.5791 | 2873.2556 | 2872.2005 |
| 3.3584 | 2818.2360 | 2858.7156 | 2857.6544 |
| 3.3694 | 2781.8800 | 2844.1757 | 2843.1084 |
| 3.3804 | 2819.9209 | 2829.6358 | 2828.5623 |
| 3.3914 | 2820.9646 | 2815.0959 | 2814.0163 |
| 3.4024 | 2781.2680 | 2800.5561 | 2799.4702 |
| 3.4134 | 2715.4641 | 2786.0164 | 2784.9241 |
| 3.4244 | 2742.4897 | 2771.4767 | 2770.3781 |
| 3.4354 | 2754.5752 | 2756.9370 | 2755.8320 |
| 3.4464 | 2741.5241 | 2742.3975 | 2741.2860 |
| 3.4574 | 2770.1829 | 2727.8580 | 2726.7399 |
| 3.4684 | 2720.9720 | 2713.3185 | 2712.1939 |
| 3.4794 | 2666.2960 | 2698.7791 | 2697.6478 |
| 3.4904 | 2675.4381 | 2684.2397 | 2683.1018 |
| 3.5014 | 2706.1475 | 2670.9221 | 2668.5557 |
| 3.5124 | 2642.1416 | 2657.6376 | 2656.4860 |
| 3.5234 | 2623.3156 | 2645.5747 | 2644.4162 |
| 3.5344 | 2668.2567 | 2633.5119 | 2632.3465 |
| 3.5454 | 2642.9174 | 2621.4492 | 2620.2768 |
| 3.5564 | 2596.2124 | 2609.3866 | 2608.2070 |
| 3.5674 | 2556.6775 | 2597.3240 | 2596.1373 |
| 3.5784 | 2573.5167 | 2585.2615 | 2584.0676 |
| 3.5894 | 2499.6194 | 2573.1990 | 2571.9978 |
| 3.6004 | 2525.8432 | 2561.1366 | 2559.9281 |
| 3.6114 | 2524.1101 | 2549.0743 | 2547.8584 |
| 3.6224 | 2584.5428 | 2537.0121 | 2535.7886 |
| 3.6334 | 2496.7964 | 2524.9499 | 2523.7189 |
| 3.6444 | 2531.3643 | 2512.8878 | 2511.6492 |
| 3.6554 | 2439.2301 | 2500.8257 | 2499.5794 |
| 3.6664 | 2442.2547 | 2488.7637 | 2487.5097 |
| 3.6774 | 2415.6116 | 2476.7018 | 2475.4400 |
| 3.6884 | 2522.8275 | 2464.5821 | 2463.3702 |
| 3.6994 | 2471.9311 | 2452.4608 | 2451.1831 |
| 3.7104 | 2434.1313 | 2440.2817 | 2438.9959 |
| 3.7214 | 2456.6873 | 2428.1027 | 2426.8087 |
| 3.7324 | 2524.0787 | 2415.9237 | 2414.6215 |
| 3.7434 | 2335.8928 | 2403.7448 | 2402.4344 |
| 3.7544 | 2381.2567 | 2391.5683 | 2390.2472 |
| 3.7654 | 2304.7414 | 2379.5346 | 2378.0600 |
| 3.7764 | 2336.2601 | 2367.4299 | 2365.8728 |
| 3.7874 | 2412.3275 | 2355.2546 | 2353.6857 |
| 3.7984 | 2282.1067 | 2343.0794 | 2341.4985 |
| 3.8094 | 2314.0856 | 2330.9045 | 2329.3113 |
| 3.8204 | 2378.6371 | 2318.7296 | 2317.1241 |
| 3.8314 | 2259.9439 | 2306.5550 | 2304.9369 |
| 3.8424 | 2210.6318 | 2294.3805 | 2292.7498 |
| 3.8534 | 2208.2183 | 2282.2062 | 2280.5626 |
| 3.8644 | 2270.0034 | 2270.0320 | 2268.3754 |
| 3.8754 | 2278.5998 | 2259.3537 | 2256.1882 |
| 3.8864 | 2244.0000 | 2248.7161 | 2247.0329 |
| 3.8974 | 2247.6500 | 2239.5744 | 2237.8775 |
| 3.9084 | 2269.4297 | 2230.4328 | 2228.7221 |
| 3.9194 | 2210.5516 | 2221.2914 | 2219.5668 |
| 3.9304 | 2143.7537 | 2212.1502 | 2210.4114 |
| 3.9414 | 2242.7335 | 2203.0092 | 2201.2560 |
| 3.9524 | 2258.3997 | 2193.8685 | 2192.1007 |
| 3.9634 | 2200.1583 | 2184.7279 | 2182.9453 |
| 3.9744 | 2126.8019 | 2175.5876 | 2173.7899 |
| 3.9854 | 2157.0797 | 2166.4475 | 2164.6346 |
| 3.9964 | 2203.5634 | 2157.3077 | 2155.4792 |
| 4.0074 | 2175.9764 | 2148.1681 | 2146.3238 |
| 4.0184 | 2187.0147 | 2139.0287 | 2137.1685 |
| 4.0294 | 2161.0147 | 2129.8896 | 2128.0131 |
| 4.0404 | 2130.2738 | 2120.7507 | 2118.8577 |
| 4.0514 | 2125.8496 | 2111.6121 | 2109.7024 |
| 4.0624 | 2115.9843 | 2102.4738 | 2100.5470 |
| 4.0734 | 2135.1180 | 2093.3357 | 2091.3916 |
| 4.0844 | 2141.9734 | 2084.1980 | 2082.2362 |
| 4.0954 | 2072.5054 | 2075.0605 | 2073.0809 |
| 4.1064 | 2047.5453 | 2065.9234 | 2063.9255 |
| 4.1174 | 2094.0029 | 2056.7865 | 2054.7701 |
| 4.1284 | 2061.9965 | 2047.6500 | 2045.6148 |
| 4.1394 | 2032.3087 | 2038.5138 | 2036.4594 |
| 4.1504 | 2055.7729 | 2029.3780 | 2027.3040 |
| 4.1614 | 2067.7306 | 2020.2425 | 2018.1487 |
| 4.1724 | 2003.3545 | 2011.1073 | 2008.9933 |
| 4.1834 | 1994.9469 | 2001.9725 | 1999.8379 |
| 4.1944 | 2014.7571 | 1992.8382 | 1990.6826 |

Scan List

| Vis. | Dataset Name | Start pos. [°2θ] | End pos. [°2θ] | Step [°2θ] | Meas.Date/Time |
| --- | --- | --- | --- | --- | --- |
| * | 18 Etosha22 SSCRT 0-0.5cm S4 400C | 2.0054 | 29.9894 | 0.0110 | 12/7/2023 3:53:00 PM |

Peak List

| Pos. [°2θ] | Height [cts] | FWHM Left [°2θ] | d-spacing [Å] | Rel. Int. [%] |
| --- | --- | --- | --- | --- |
| 5.2767 | 154.76 | 0.1515 | 16.73413 | 20.02 |
| 7.1825 | 487.57 | 0.4763 | 12.29765 | 63.07 |
| 8.7598 | 688.61 | 0.1082 | 10.08656 | 89.07 |
| 13.2349 | 11.79 | 0.5196 | 6.68434 | 1.52 |
| 15.7946 | 773.09 | 0.1299 | 5.60635 | 100.00 |
| 17.6109 | 61.34 | 0.1732 | 5.03202 | 7.93 |
| 18.2439 | 99.30 | 0.1082 | 4.85882 | 12.84 |
| 19.6443 | 27.06 | 0.4330 | 4.51548 | 3.50 |
| 24.2575 | 39.42 | 0.1732 | 3.66619 | 5.10 |
| 25.9609 | 406.47 | 0.1732 | 3.42937 | 52.58 |
| 26.7010 | 160.42 | 0.2165 | 3.33597 | 20.75 |
| 27.5208 | 66.65 | 0.2165 | 3.23842 | 8.62 |

Pattern List

| Visible | Ref.Code | Score | Compound Name | Chem. Formula | Mineral Name | SemiQuant[%] |
| --- | --- | --- | --- | --- | --- | --- |
| * | 01-083-1733 | 62 | Sodium Aluminum Silicate Hydrate | Na16.24 Al16.00 Si32.00 O96 ( H2 O )16 | Analcime | 41 |
| * | 04-015-8231 | 56 | Potassium Magnesium Manganese Aluminum Iron Silicon Titanium Oxide Fluoride Hydroxide | K0.87 Mg1.69 Ti0.11 Mn0.03 Fe0.65 Al1.68 Si2.75 O10.14 ( O H )1.74 F0.12 | Biotite-1M | 28 |
| * | 04-015-3277 | 49 | Tin Oxide | Sn O2 | Cassiterite, syn | 1 |
| * | 04-017-7286 | 44 | Potassium Manganese Aluminum Silicon Oxide Hydroxide Hydrate | K0.8 Mn4 Al1.08 Si4.92 O16 ( O H )2 ( H2 O )3 | Ganophyllite | 2 |
| * | 04-017-9668 | 29 | Magnesium Aluminum Iron Silicon Oxide Hydroxide Hydrate | Mg3.84 Ti0.005 Fe0.03 Al0.07 Si6 O15 ( O H )2 ( H2 O )5 | Sepiolite | 3 |
| * | 01-082-8023 | 22 | Sodium Magnesium Silicon Oxide Hydrate | Na2 Mg3 ( Si6 O16 ) ( H2 O )7 | Loughlinite | 3 |
| * | 04-025-4215 | No Matching Lines | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide | Mg10.4 V0.36 Mn33.5 Fe0.14 Al0.69 Si6.77 As6.5 P0.3 O54 ( O H )42 | Carlfrancisite | - |
| * | 04-011-6576 | No Matching Lines | Magnesium Aluminum Silicate Hydroxide Hydrate | Mg3.5 Al Si3 O10 ( O H )2 ( H2 O )4 | Vermiculite | - |
| * | 04-016-2838 | 27 | Titanium Oxide | Ti O2 | Rutile | 1 |
| * | 00-034-0159 | 43 | Potassium Magnesium Aluminum Fluoride Silicate Hydroxide | K Mg3 Si3 Al O10 ( F , O H )2 | Phlogopite-1M | 21 |

Anchor Scan Parameters

Dataset Name	18 Etosha22 SSCRT 0-0.5cm S4 400C

File name	C:\aeris_data\XRD data\Goldstein\Etosha 2023\Etosha Clay Data\Sample 18\18 Etosha22 SSCRT 0-0.5cm S4 400C.xrdml

Sample Identification	18 Etosha22 SSCRT 0-0.5cm S4 400C

Measurement Start Date/Time	12/7/2023 3:53:00 PM

Operator	Instrument

Raw Data Origin	XRD measurement (*.XRDML)

Scan Axis	Gonio

Start Position [°2θ]	2.0054

End Position [°2θ]	29.9894

Step Size [°2θ]	0.0110

Scan Step Time [s]	48.1950

Scan Type	Continuous

PSD Mode	Scanning

PSD Length [°2θ]	5.54

Offset [°2θ]	0.0000

Divergence Slit Type	Fixed

Divergence Slit Size [°]	0.0603

Specimen Length [mm]	10.00

Measurement Temperature [°C]	25.00

Anode Material	Cu

K-α1 [Å]	1.54060

K-α2 [Å]	1.54443

K-β1 [Å]	1.39225

K-A2 / K-A1 Ratio	0.50000

Generator Settings	15 mA, 40 kV

Diffractometer Type	2082464

Diffractometer Number	0

Goniometer Radius [mm]	145.00

Dist. Focus-Diverg. Slit [mm]	95.00

Incident Beam Monochromator	No

Spinning	Yes