18 Etosha 22 SSCrt 0-0.5 cm S4 550C REPORT

Graphics

Graphics

Graphics

Quantitative Results

Phase Sodium Aluminum Silicate Hydrate

Weight fraction/ %	23.0

Phase Tin Oxide

Weight fraction/ %	1.0

Phase Titanium Antimony Vanadium Tungsten Oxide

Weight fraction/ %	2.0

Phase Potassium Magnesium Manganese Iron Aluminum Silicate Hydroxide

Weight fraction/ %	14.0

Phase Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide

Weight fraction/ %	22.0

Phase Calcium Magnesium Iron Silicate Hydroxide

Weight fraction/ %	3.0

Phase Potassium Magnesium Aluminum Fluoride Silicate Hydroxide

Weight fraction/ %	35.0

Multiple Quantitative Results

Scans vs Phases Matrix

| Scan name | Sodium Aluminum Silicate Hydrate | Tin Oxide | Titanium Antimony Vanadium Tungsten Oxide | Potassium Magnesium Manganese Iron Aluminum Silicate Hydroxide | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide | Calcium Magnesium Iron Silicate Hydroxide | Potassium Magnesium Aluminum Fluoride Silicate Hydroxide |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 18 Etosha22 SSCrt 0-0.5cm S4 550C | 23.0 | 1.0 | 2.0 | 14.0 | 22.0 | 3.0 | 35.0 |

Anchor Scan Data

| Pos. [°2θ] | Iobs [cts] | Icalc [cts] | Iback [cts] |
| --- | --- | --- | --- |
| 2.0054 | 9352.0000 | 9351.0382 | 9352.0000 |
| 2.0164 | 9256.3151 | 9295.3922 | 9284.0465 |
| 2.0274 | 9359.1731 | 9227.8206 | 9216.0929 |
| 2.0384 | 9245.2670 | 9160.2685 | 9148.1394 |
| 2.0494 | 9198.6234 | 9092.7372 | 9080.1859 |
| 2.0604 | 9161.4911 | 9025.2284 | 9012.2323 |
| 2.0714 | 8997.3864 | 8957.7434 | 8944.2788 |
| 2.0824 | 8954.5811 | 8890.2841 | 8876.3252 |
| 2.0934 | 8955.6480 | 8822.8524 | 8808.3717 |
| 2.1044 | 8731.0354 | 8755.4503 | 8740.4182 |
| 2.1154 | 8871.9331 | 8688.0801 | 8672.4646 |
| 2.1264 | 8869.0388 | 8620.7443 | 8604.5111 |
| 2.1374 | 8688.1091 | 8553.4457 | 8536.5576 |
| 2.1484 | 8771.9803 | 8486.1872 | 8468.6040 |
| 2.1594 | 8710.3796 | 8418.9723 | 8400.6505 |
| 2.1704 | 8726.7065 | 8351.8045 | 8332.6970 |
| 2.1814 | 8446.6991 | 8284.6880 | 8264.7434 |
| 2.1924 | 8480.7625 | 8217.5979 | 8196.7899 |
| 2.2034 | 8345.9558 | 8150.4605 | 8128.6696 |
| 2.2144 | 8353.9105 | 8083.3602 | 8060.5494 |
| 2.2254 | 8286.3864 | 8016.3326 | 7992.4291 |
| 2.2364 | 8330.3186 | 7949.3845 | 7924.3088 |
| 2.2474 | 8260.9695 | 7882.5239 | 7856.1886 |
| 2.2584 | 8248.2193 | 7815.7596 | 7788.0683 |
| 2.2694 | 8201.1681 | 7749.1016 | 7719.9480 |
| 2.2804 | 8043.3181 | 7682.5610 | 7651.8278 |
| 2.2914 | 8001.0737 | 7616.1507 | 7583.7075 |
| 2.3024 | 7990.8097 | 7549.8852 | 7515.5873 |
| 2.3134 | 8064.2665 | 7483.7810 | 7447.4670 |
| 2.3244 | 7976.9100 | 7417.8572 | 7379.3467 |
| 2.3354 | 7880.6991 | 7352.1357 | 7311.2265 |
| 2.3464 | 7826.4130 | 7286.6419 | 7243.1062 |
| 2.3574 | 7681.1337 | 7221.4055 | 7174.9859 |
| 2.3684 | 7705.0988 | 7156.4617 | 7106.8657 |
| 2.3794 | 7721.6431 | 7091.8530 | 7038.7454 |
| 2.3904 | 7677.4528 | 7027.6316 | 6970.6252 |
| 2.4014 | 7760.3363 | 6963.8637 | 6902.5049 |
| 2.4124 | 7753.4961 | 6900.6356 | 6834.3846 |
| 2.4234 | 7644.6765 | 6838.0638 | 6766.2644 |
| 2.4344 | 7562.6091 | 6776.3092 | 6698.1441 |
| 2.4454 | 7438.8427 | 6715.5982 | 6630.0238 |
| 2.4564 | 7398.8505 | 6656.2518 | 6561.9036 |
| 2.4674 | 7425.9440 | 6598.7227 | 6493.7833 |
| 2.4784 | 7527.6652 | 6543.6412 | 6425.6630 |
| 2.4894 | 7477.7876 | 6491.8651 | 6357.5428 |
| 2.5004 | 7316.8849 | 6444.5270 | 6289.4225 |
| 2.5114 | 7318.6273 | 6403.0693 | 6221.3023 |
| 2.5224 | 7292.6347 | 6369.2488 | 6153.1820 |
| 2.5334 | 7264.9587 | 6345.0981 | 6085.0617 |
| 2.5444 | 7212.5354 | 6332.8238 | 6016.9415 |
| 2.5554 | 7266.7866 | 6334.6338 | 5948.8212 |
| 2.5664 | 7163.2596 | 6352.4620 | 5880.7009 |
| 2.5774 | 7122.8004 | 6387.6370 | 5812.4139 |
| 2.5884 | 7017.2463 | 6440.7295 | 5744.1270 |
| 2.5994 | 7023.9735 | 6510.9434 | 5675.8400 |
| 2.6104 | 6931.8264 | 6595.6836 | 5607.5530 |
| 2.6214 | 6751.6775 | 6690.0473 | 5539.2660 |
| 2.6324 | 6942.8053 | 6786.1996 | 5470.9790 |
| 2.6434 | 6890.1662 | 6872.8465 | 5402.6920 |
| 2.6544 | 6773.3373 | 6935.4039 | 5334.4050 |
| 2.6654 | 6730.1386 | 6957.8365 | 5266.1180 |
| 2.6764 | 6681.5133 | 6926.6702 | 5197.8310 |
| 2.6874 | 6498.8259 | 6835.8112 | 5129.5440 |
| 2.6984 | 6466.1327 | 6689.0945 | 5061.2570 |
| 2.7094 | 6340.6332 | 6498.5986 | 4992.9701 |
| 2.7204 | 6093.2866 | 6280.0944 | 4924.6831 |
| 2.7314 | 5933.7315 | 6048.7046 | 4856.3961 |
| 2.7424 | 5924.6465 | 5816.5695 | 4788.1091 |
| 2.7534 | 5554.4011 | 5592.2995 | 4719.8221 |
| 2.7644 | 5571.7449 | 5381.4253 | 4651.3290 |
| 2.7754 | 5464.9666 | 5187.1327 | 4582.8359 |
| 2.7864 | 5165.7473 | 5010.7027 | 4514.3429 |
| 2.7974 | 5063.0531 | 4851.9396 | 4445.8498 |
| 2.8084 | 4820.8185 | 4709.6338 | 4377.3567 |
| 2.8194 | 4692.1317 | 4581.9335 | 4308.8636 |
| 2.8304 | 4432.1843 | 4466.6693 | 4240.3705 |
| 2.8414 | 4437.1554 | 4361.6176 | 4171.8775 |
| 2.8524 | 4413.4469 | 4264.6924 | 4103.3844 |
| 2.8634 | 4203.0029 | 4174.0630 | 4034.8913 |
| 2.8744 | 3945.4257 | 4088.2079 | 3966.3982 |
| 2.8854 | 4094.3422 | 4005.9192 | 3897.9052 |
| 2.8964 | 3910.8274 | 3926.2740 | 3829.4121 |
| 2.9074 | 3800.1976 | 3848.5891 | 3760.9190 |
| 2.9184 | 3695.4926 | 3772.3711 | 3692.4259 |
| 2.9294 | 3527.0767 | 3697.2691 | 3623.9328 |
| 2.9404 | 3587.9710 | 3631.7388 | 3555.4398 |
| 2.9514 | 3559.7266 | 3585.3425 | 3522.7943 |
| 2.9624 | 3456.4159 | 3548.2160 | 3490.1489 |
| 2.9734 | 3466.2439 | 3511.5630 | 3457.5034 |
| 2.9844 | 3493.0595 | 3475.3127 | 3424.8579 |
| 2.9954 | 3298.1151 | 3439.4098 | 3392.2125 |
| 3.0064 | 3353.6160 | 3403.8096 | 3359.5670 |
| 3.0174 | 3315.6381 | 3368.4752 | 3326.9216 |
| 3.0284 | 3264.1195 | 3333.3757 | 3294.2761 |
| 3.0394 | 3191.9931 | 3298.4845 | 3261.6306 |
| 3.0504 | 3298.0555 | 3263.7791 | 3228.9852 |
| 3.0614 | 3191.7640 | 3229.2395 | 3196.3397 |
| 3.0724 | 3146.1883 | 3194.8488 | 3163.6943 |
| 3.0834 | 3157.9125 | 3160.5918 | 3131.0488 |
| 3.0944 | 3052.1770 | 3126.4554 | 3098.4033 |
| 3.1054 | 3090.2753 | 3092.4280 | 3065.7579 |
| 3.1164 | 3023.8613 | 3058.4992 | 3033.1124 |
| 3.1274 | 2990.9852 | 3026.8656 | 3000.4670 |
| 3.1384 | 2981.0846 | 2999.9865 | 2976.9055 |
| 3.1494 | 2940.5732 | 2975.3872 | 2953.3440 |
| 3.1604 | 2891.3923 | 2950.8559 | 2929.7825 |
| 3.1714 | 2882.4690 | 2926.3867 | 2906.2210 |
| 3.1824 | 2835.7694 | 2901.9744 | 2882.6595 |
| 3.1934 | 2872.7168 | 2877.6146 | 2859.0980 |
| 3.2044 | 2860.8358 | 2853.3029 | 2835.5365 |
| 3.2154 | 2792.2488 | 2829.0356 | 2811.9750 |
| 3.2264 | 2772.9970 | 2804.8093 | 2788.4135 |
| 3.2374 | 2703.5831 | 2780.6208 | 2764.8520 |
| 3.2484 | 2754.2778 | 2756.4675 | 2741.2905 |
| 3.2594 | 2727.2360 | 2732.3467 | 2717.7290 |
| 3.2704 | 2656.8176 | 2708.2561 | 2694.1675 |
| 3.2814 | 2616.2448 | 2684.1935 | 2670.6060 |
| 3.2924 | 2537.8761 | 2660.1571 | 2647.0445 |
| 3.3034 | 2621.4130 | 2636.1451 | 2623.4830 |
| 3.3144 | 2677.1244 | 2613.4756 | 2599.9216 |
| 3.3254 | 2574.6578 | 2593.6238 | 2581.7963 |
| 3.3364 | 2485.3820 | 2575.1118 | 2563.6710 |
| 3.3474 | 2514.9361 | 2556.6183 | 2545.5457 |
| 3.3584 | 2502.7183 | 2538.1423 | 2527.4204 |
| 3.3694 | 2455.7286 | 2519.6826 | 2509.2951 |
| 3.3804 | 2454.2537 | 2501.2382 | 2491.1698 |
| 3.3914 | 2447.3628 | 2482.8083 | 2473.0445 |
| 3.4024 | 2438.6834 | 2464.3919 | 2454.9192 |
| 3.4134 | 2424.2930 | 2445.9884 | 2436.7939 |
| 3.4244 | 2398.4793 | 2427.5968 | 2418.6686 |
| 3.4354 | 2379.0000 | 2409.2167 | 2400.5433 |
| 3.4464 | 2356.4253 | 2390.8472 | 2382.4180 |
| 3.4574 | 2352.5811 | 2372.4879 | 2364.2927 |
| 3.4684 | 2353.9223 | 2354.1382 | 2346.1674 |
| 3.4794 | 2343.8830 | 2335.7975 | 2328.0421 |
| 3.4904 | 2313.6283 | 2317.4654 | 2309.9168 |
| 3.5014 | 2273.8082 | 2300.2920 | 2291.7915 |
| 3.5124 | 2269.2065 | 2285.5642 | 2278.4052 |
| 3.5234 | 2282.7463 | 2271.9943 | 2265.0188 |
| 3.5344 | 2230.3235 | 2258.4313 | 2251.6325 |
| 3.5454 | 2217.8112 | 2244.8750 | 2238.2462 |
| 3.5564 | 2237.3938 | 2231.3249 | 2224.8598 |
| 3.5674 | 2179.6470 | 2217.7808 | 2211.4735 |
| 3.5784 | 2172.3948 | 2204.2424 | 2198.0872 |
| 3.5894 | 2159.2920 | 2190.7094 | 2184.7008 |
| 3.6004 | 2140.7026 | 2177.1816 | 2171.3145 |
| 3.6114 | 2113.1652 | 2163.6587 | 2157.9281 |
| 3.6224 | 2081.9897 | 2150.1405 | 2144.5418 |
| 3.6334 | 2088.2861 | 2136.6268 | 2131.1555 |
| 3.6444 | 2044.4434 | 2123.1174 | 2117.7691 |
| 3.6554 | 2027.4071 | 2109.6121 | 2104.3828 |
| 3.6664 | 2101.3235 | 2096.1107 | 2090.9965 |
| 3.6774 | 2113.1318 | 2082.6131 | 2077.6101 |
| 3.6884 | 2031.9911 | 2069.1190 | 2064.2238 |
| 3.6994 | 2063.8555 | 2055.6284 | 2050.8375 |
| 3.7104 | 2017.4085 | 2042.1411 | 2037.4511 |
| 3.7214 | 1980.8082 | 2028.6569 | 2024.0648 |
| 3.7324 | 1949.1794 | 2015.1757 | 2010.6785 |
| 3.7434 | 1905.5526 | 2001.6975 | 1997.2921 |
| 3.7544 | 1967.8909 | 1988.2220 | 1983.9058 |
| 3.7654 | 1986.4651 | 1974.7492 | 1970.5195 |
| 3.7764 | 1937.0782 | 1961.2790 | 1957.1331 |
| 3.7874 | 1941.9469 | 1947.8113 | 1943.7468 |
| 3.7984 | 1945.7556 | 1934.3459 | 1930.3605 |
| 3.8094 | 1876.9509 | 1920.8828 | 1916.9741 |
| 3.8204 | 1997.2065 | 1907.4219 | 1903.5878 |
| 3.8314 | 1932.8230 | 1893.9631 | 1890.2015 |
| 3.8424 | 1877.8962 | 1880.5063 | 1876.8151 |
| 3.8534 | 1821.6755 | 1867.0515 | 1863.4288 |
| 3.8644 | 1818.9297 | 1853.5986 | 1850.0425 |
| 3.8754 | 1845.2213 | 1840.9670 | 1836.6561 |
| 3.8864 | 1871.9956 | 1830.0609 | 1826.6326 |
| 3.8974 | 1825.3874 | 1819.9760 | 1816.6091 |
| 3.9084 | 1874.4946 | 1809.8928 | 1806.5855 |
| 3.9194 | 1864.6224 | 1799.8111 | 1796.5620 |
| 3.9304 | 1821.6794 | 1789.7310 | 1786.5384 |
| 3.9414 | 1791.9007 | 1779.6523 | 1776.5149 |
| 3.9524 | 1746.0575 | 1769.5750 | 1766.4913 |
| 3.9634 | 1800.6293 | 1759.4991 | 1756.4678 |
| 3.9744 | 1802.3953 | 1749.4245 | 1746.4443 |
| 3.9854 | 1760.1770 | 1739.3512 | 1736.4207 |
| 3.9964 | 1759.0315 | 1729.2791 | 1726.3972 |
| 4.0074 | 1780.7768 | 1719.2083 | 1716.3736 |
| 4.0184 | 1713.9764 | 1709.1474 | 1706.3501 |
| 4.0294 | 1738.7847 | 1699.1970 | 1696.3265 |
| 4.0404 | 1728.6770 | 1689.1883 | 1686.3030 |
| 4.0514 | 1692.5664 | 1679.1251 | 1676.2795 |
| 4.0624 | 1665.1991 | 1670.4516 | 1666.2559 |
| 4.0734 | 1625.0393 | 1664.7005 | 1661.9310 |
| 4.0844 | 1652.7345 | 1660.3391 | 1657.6062 |
| 4.0954 | 1680.9351 | 1655.9788 | 1653.2813 |
| 4.1064 | 1673.9464 | 1651.6194 | 1648.9564 |
| 4.1174 | 1684.0059 | 1647.2610 | 1644.6316 |
| 4.1284 | 1646.4174 | 1642.9036 | 1640.3067 |
| 4.1394 | 1661.2213 | 1638.5471 | 1635.9819 |
| 4.1504 | 1671.8304 | 1634.1915 | 1631.6570 |
| 4.1614 | 1628.5910 | 1629.8367 | 1627.3321 |
| 4.1724 | 1639.3761 | 1625.4829 | 1623.0073 |
| 4.1834 | 1596.8938 | 1621.1299 | 1618.6824 |
| 4.1944 | 1570.4971 | 1615.6619 | 1614.3575 |

Scan List

| Vis. | Dataset Name | Start pos. [°2θ] | End pos. [°2θ] | Step [°2θ] | Meas.Date/Time |
| --- | --- | --- | --- | --- | --- |
| * | 18 Etosha22 SSCrt 0-0.5cm S4 550C | 2.0054 | 29.9894 | 0.0110 | 12/8/2023 12:45:35 PM |

Peak List

| Pos. [°2θ] | Height [cts] | FWHM Left [°2θ] | d-spacing [Å] | Rel. Int. [%] |
| --- | --- | --- | --- | --- |
| 2.6756 | 1549.38 | 0.1515 | 32.99350 | 100.00 |
| 5.3200 | 128.89 | 0.1299 | 16.59795 | 8.32 |
| 8.7036 | 1312.23 | 0.1515 | 10.15149 | 84.69 |
| 10.6602 | 52.31 | 0.3464 | 8.29230 | 3.38 |
| 15.7519 | 561.68 | 0.0866 | 5.62143 | 36.25 |
| 15.8569 | 599.92 | 0.1082 | 5.58446 | 38.72 |
| 17.5457 | 81.91 | 0.1732 | 5.05056 | 5.29 |
| 18.3024 | 45.47 | 0.1732 | 4.84342 | 2.93 |
| 19.5720 | 41.91 | 0.3897 | 4.53201 | 2.71 |
| 26.0445 | 348.76 | 0.3464 | 3.41855 | 22.51 |
| 26.7142 | 229.79 | 0.1299 | 3.33435 | 14.83 |
| 27.4218 | 212.17 | 0.1948 | 3.24989 | 13.69 |

Pattern List

| Visible | Ref.Code | Score | Compound Name | Chem. Formula | Mineral Name | SemiQuant[%] |
| --- | --- | --- | --- | --- | --- | --- |
| * | 04-011-6233 | 63 | Sodium Aluminum Silicate Hydrate | Na8 Al8 Si16 O48 ( H2 O )8 | Analcime | 23 |
| * | 04-015-3277 | 50 | Tin Oxide | Sn O2 | Cassiterite, syn | 1 |
| * | 04-015-3140 | 54 | Titanium Antimony Vanadium Tungsten Oxide | Ti0.894 V0.069 W0.022 Sb0.014 O2 | Rutile | 2 |
| * | 04-017-4317 | 50 | Potassium Magnesium Manganese Iron Aluminum Silicate Hydroxide | K Mg0.2 Mn0.1 Fe2.4 Al1.7 Si2.6 O10 ( O H )2 | Biotite-1M | 14 |
| * | 04-025-4215 | 36 | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide | Mg10.4 V0.36 Mn33.5 Fe0.14 Al0.69 Si6.77 As6.5 P0.3 O54 ( O H )42 | Carlfrancisite | 22 |
| * | 04-017-1621 | 7 | Calcium Magnesium Iron Silicate Hydroxide | Ca2 Mg2.5 Fe2.5 Si8 O22 ( O H )2 | Actinolite | 3 |
| * | 00-034-0159 | 29 | Potassium Magnesium Aluminum Fluoride Silicate Hydroxide | K Mg3 Si3 Al O10 ( F , O H )2 | Phlogopite-1M | 35 |

Anchor Scan Parameters

Dataset Name	18 Etosha22 SSCrt 0-0.5cm S4 550C

File name	C:\aeris_data\XRD data\Goldstein\Etosha 2023\Etosha Clay Data\Sample 18\18 Etosha22 SSCrt 0-0.5cm S4 550C.xrdml

Sample Identification	18 Etosha22 SSCrt 0-0.5cm S4 550C

Measurement Start Date/Time	12/8/2023 12:45:35 PM

Operator	Instrument

Raw Data Origin	XRD measurement (*.XRDML)

Scan Axis	Gonio

Start Position [°2θ]	2.0054

End Position [°2θ]	29.9894

Step Size [°2θ]	0.0110

Scan Step Time [s]	48.1950

Scan Type	Continuous

PSD Mode	Scanning

PSD Length [°2θ]	5.54

Offset [°2θ]	0.0000

Divergence Slit Type	Fixed

Divergence Slit Size [°]	0.0603

Specimen Length [mm]	10.00

Measurement Temperature [°C]	25.00

Anode Material	Cu

K-α1 [Å]	1.54060

K-α2 [Å]	1.54443

K-β1 [Å]	1.39225

K-A2 / K-A1 Ratio	0.50000

Generator Settings	15 mA, 40 kV

Diffractometer Type	2082464

Diffractometer Number	0

Goniometer Radius [mm]	145.00

Dist. Focus-Diverg. Slit [mm]	95.00

Incident Beam Monochromator	No

Spinning	Yes