18 Etosha 22 SSCrt 0-0.5 cm S4  REGULAR REPORT

Graphics

Graphics

Graphics

Quantitative Results

Phase Sodium Aluminum Silicate Hydrate

Weight fraction/ %	6.0

Phase Tin Oxide

Weight fraction/ %	1.0

Phase Potassium Manganese Silicate Hydroxide Hydrate

Weight fraction/ %	14.0

Phase Potassium Magnesium Manganese Iron Aluminum Silicate Hydroxide

Weight fraction/ %	7.0

Phase Magnesium Aluminum Silicate Hydroxide Hydrate

Weight fraction/ %	2.0

Phase Magnesium Silicon Oxide Hydroxide Hydrate

Weight fraction/ %	6.0

Phase Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide

Weight fraction/ %	41.0

Phase Sodium Magnesium Silicon Oxide Hydrate

Weight fraction/ %	15.0

Phase Titanium Oxide

Weight fraction/ %	1.0

Phase Potassium Magnesium Aluminum Fluoride Silicate Hydroxide

Weight fraction/ %	8.0

Multiple Quantitative Results

Scans vs Phases Matrix

| Scan name | Sodium Aluminum Silicate Hydrate | Tin Oxide | Potassium Manganese Silicate Hydroxide Hydrate | Potassium Magnesium Manganese Iron Aluminum Silicate Hydroxide | Magnesium Aluminum Silicate Hydroxide Hydrate | Magnesium Silicon Oxide Hydroxide Hydrate | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide | Sodium Magnesium Silicon Oxide Hydrate | Titanium Oxide | Potassium Magnesium Aluminum Fluoride Silicate Hydroxide |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 18 Etosha22 SSCRT 0-0.5cm S4 | 6.0 | 1.0 | 14.0 | 7.0 | 2.0 | 6.0 | 41.0 | 15.0 | 1.0 | 8.0 |

Anchor Scan Data

| Pos. [°2θ] | Iobs [cts] | Icalc [cts] | Iback [cts] |
| --- | --- | --- | --- |
| 2.0054 | 9437.0000 | 9439.2424 | 9437.0000 |
| 2.0164 | 9346.1185 | 9385.9620 | 9365.3242 |
| 2.0274 | 9433.1731 | 9314.9519 | 9293.6483 |
| 2.0384 | 9321.4425 | 9243.9743 | 9221.9725 |
| 2.0494 | 9327.9852 | 9173.0314 | 9150.2966 |
| 2.0604 | 9225.1003 | 9102.1255 | 9078.6208 |
| 2.0714 | 9134.7788 | 9031.2589 | 9006.9449 |
| 2.0824 | 9130.4513 | 8960.4346 | 8935.2691 |
| 2.0934 | 9111.1485 | 8889.6554 | 8863.5932 |
| 2.1044 | 9073.3850 | 8818.9246 | 8791.9174 |
| 2.1154 | 8965.9882 | 8748.2456 | 8720.2416 |
| 2.1264 | 8845.9902 | 8677.6223 | 8648.5657 |
| 2.1374 | 8750.1534 | 8607.0588 | 8576.8899 |
| 2.1484 | 8920.9803 | 8536.5598 | 8505.2140 |
| 2.1594 | 8832.0197 | 8466.1303 | 8433.5382 |
| 2.1704 | 8758.0044 | 8395.7758 | 8361.8623 |
| 2.1814 | 8636.5103 | 8325.5023 | 8290.1865 |
| 2.1924 | 8624.6264 | 8255.2779 | 8218.5106 |
| 2.2034 | 8701.0177 | 8185.0700 | 8146.6790 |
| 2.2144 | 8766.1259 | 8114.9268 | 8074.8474 |
| 2.2254 | 8670.1367 | 8044.8959 | 8003.0158 |
| 2.2364 | 8449.7714 | 7974.9873 | 7931.1842 |
| 2.2474 | 8438.4484 | 7905.2122 | 7859.3526 |
| 2.2584 | 8470.3092 | 7835.5832 | 7787.5210 |
| 2.2694 | 8329.5900 | 7766.1142 | 7715.6894 |
| 2.2804 | 8299.9651 | 7696.8211 | 7643.8578 |
| 2.2914 | 8278.8938 | 7627.7219 | 7572.0262 |
| 2.3024 | 8316.2965 | 7558.8372 | 7500.1946 |
| 2.3134 | 8248.4209 | 7490.1907 | 7428.3630 |
| 2.3244 | 8302.2861 | 7421.8105 | 7356.5314 |
| 2.3354 | 8154.0383 | 7353.7299 | 7284.6997 |
| 2.3464 | 8117.3795 | 7285.9894 | 7212.8681 |
| 2.3574 | 8094.3805 | 7218.6391 | 7141.0365 |
| 2.3684 | 8119.7773 | 7151.7423 | 7069.2049 |
| 2.3794 | 8042.2586 | 7085.3801 | 6997.3733 |
| 2.3904 | 7848.5698 | 7019.6577 | 6925.5417 |
| 2.4014 | 7871.4513 | 6954.7131 | 6853.7101 |
| 2.4124 | 7845.5182 | 6890.7271 | 6781.8785 |
| 2.4234 | 7770.5929 | 6827.9365 | 6710.0469 |
| 2.4344 | 7781.1327 | 6766.6491 | 6638.2153 |
| 2.4454 | 7810.8663 | 6707.2603 | 6566.3837 |
| 2.4564 | 7796.8269 | 6650.2708 | 6494.5521 |
| 2.4674 | 7644.9115 | 6596.3019 | 6422.7205 |
| 2.4784 | 7593.2925 | 6546.1088 | 6350.8889 |
| 2.4894 | 7676.5506 | 6500.5860 | 6279.0572 |
| 2.5004 | 7597.2080 | 6460.7632 | 6207.2256 |
| 2.5114 | 7617.9430 | 6427.7872 | 6135.3940 |
| 2.5224 | 7625.8338 | 6402.8870 | 6063.5624 |
| 2.5334 | 7522.3127 | 6387.3197 | 5991.7308 |
| 2.5444 | 7392.8540 | 6382.2967 | 5919.8992 |
| 2.5554 | 7406.9754 | 6388.8912 | 5848.0676 |
| 2.5664 | 7332.3923 | 6407.8904 | 5776.2360 |
| 2.5774 | 7389.1052 | 6439.7119 | 5704.2486 |
| 2.5884 | 7316.0806 | 6484.3526 | 5632.2613 |
| 2.5994 | 7291.7611 | 6541.1656 | 5560.2739 |
| 2.6104 | 7339.9562 | 6608.6648 | 5488.2865 |
| 2.6214 | 7276.3520 | 6684.3807 | 5416.2992 |
| 2.6324 | 7210.0723 | 6764.6498 | 5344.3118 |
| 2.6434 | 7024.1956 | 6844.3957 | 5272.3244 |
| 2.6544 | 7112.3624 | 6916.9791 | 5200.3370 |
| 2.6654 | 6907.2507 | 6974.2799 | 5128.3497 |
| 2.6764 | 6774.0128 | 7007.2415 | 5056.3623 |
| 2.6874 | 6741.9489 | 7007.0465 | 4984.3749 |
| 2.6984 | 6615.9779 | 6966.8108 | 4912.3876 |
| 2.7094 | 6648.6500 | 6883.2583 | 4840.4002 |
| 2.7204 | 6372.1991 | 6757.6175 | 4768.4128 |
| 2.7314 | 6099.2537 | 6595.2700 | 4696.4255 |
| 2.7424 | 5956.6504 | 6404.3445 | 4624.4381 |
| 2.7534 | 5687.7699 | 6193.9040 | 4552.4507 |
| 2.7644 | 5559.2802 | 5972.5459 | 4480.2708 |
| 2.7754 | 5394.4346 | 5747.6779 | 4408.0909 |
| 2.7864 | 5246.9543 | 5525.1472 | 4335.9110 |
| 2.7974 | 5080.3274 | 5309.2578 | 4263.7311 |
| 2.8084 | 4951.5359 | 5103.0160 | 4191.5512 |
| 2.8194 | 4717.0727 | 4908.3493 | 4119.3713 |
| 2.8304 | 4398.1710 | 4726.3011 | 4047.1914 |
| 2.8414 | 4391.6824 | 4557.2000 | 3975.0115 |
| 2.8524 | 4176.2718 | 4400.8083 | 3902.8316 |
| 2.8634 | 4076.7581 | 4256.4586 | 3830.6517 |
| 2.8744 | 3863.2655 | 4123.1806 | 3758.4718 |
| 2.8854 | 3855.0334 | 3999.8162 | 3686.2919 |
| 2.8964 | 3687.7433 | 3885.1200 | 3614.1120 |
| 2.9074 | 3709.2301 | 3777.8423 | 3541.9321 |
| 2.9184 | 3483.6013 | 3676.7926 | 3469.7522 |
| 2.9294 | 3364.8908 | 3580.8832 | 3397.5723 |
| 2.9404 | 3301.0157 | 3498.3174 | 3325.3924 |
| 2.9514 | 3279.9430 | 3437.7650 | 3290.1907 |
| 2.9624 | 3272.0678 | 3389.0525 | 3254.9889 |
| 2.9734 | 3173.8584 | 3342.4616 | 3219.7872 |
| 2.9844 | 3109.4267 | 3297.5493 | 3184.5855 |
| 2.9954 | 3052.2655 | 3253.9686 | 3149.3838 |
| 3.0064 | 3091.0187 | 3211.4509 | 3114.1821 |
| 3.0174 | 2983.4690 | 3169.7907 | 3078.9804 |
| 3.0284 | 2951.8451 | 3128.8311 | 3043.7787 |
| 3.0394 | 2908.1268 | 3088.4527 | 3008.5770 |
| 3.0504 | 2920.0732 | 3048.5637 | 2973.3752 |
| 3.0614 | 2850.3569 | 3009.0931 | 2938.1735 |
| 3.0724 | 2882.0428 | 2969.9850 | 2902.9718 |
| 3.0834 | 2816.3658 | 2931.1947 | 2867.7701 |
| 3.0944 | 2747.3717 | 2892.6856 | 2832.5684 |
| 3.1054 | 2770.3343 | 2854.4275 | 2797.3667 |
| 3.1164 | 2754.3791 | 2816.3947 | 2762.1650 |
| 3.1274 | 2743.7611 | 2781.4907 | 2726.9633 |
| 3.1384 | 2711.1568 | 2752.7266 | 2703.5684 |
| 3.1494 | 2630.5831 | 2727.0553 | 2680.1735 |
| 3.1604 | 2667.8038 | 2701.5364 | 2656.7786 |
| 3.1714 | 2643.0403 | 2676.1569 | 2633.3837 |
| 3.1824 | 2595.4911 | 2650.9048 | 2609.9888 |
| 3.1934 | 2607.7788 | 2625.7696 | 2586.5939 |
| 3.2044 | 2605.7728 | 2600.7418 | 2563.1990 |
| 3.2154 | 2496.9528 | 2575.8129 | 2539.8041 |
| 3.2264 | 2531.8215 | 2550.9750 | 2516.4093 |
| 3.2374 | 2489.0550 | 2526.2213 | 2493.0144 |
| 3.2484 | 2416.1111 | 2501.5454 | 2469.6195 |
| 3.2594 | 2405.3540 | 2476.9415 | 2446.2246 |
| 3.2704 | 2396.0580 | 2452.4043 | 2422.8297 |
| 3.2814 | 2391.7316 | 2427.9291 | 2399.4348 |
| 3.2924 | 2379.5885 | 2403.5116 | 2376.0399 |
| 3.3034 | 2338.4483 | 2379.1476 | 2352.6450 |
| 3.3144 | 2307.8152 | 2356.1998 | 2329.2502 |
| 3.3254 | 2332.3805 | 2336.0797 | 2311.3686 |
| 3.3364 | 2305.1804 | 2317.3692 | 2293.4871 |
| 3.3474 | 2303.0147 | 2298.6995 | 2275.6056 |
| 3.3584 | 2278.7876 | 2280.0679 | 2257.7241 |
| 3.3694 | 2270.0000 | 2261.4720 | 2239.8426 |
| 3.3804 | 2230.8441 | 2242.9096 | 2221.9610 |
| 3.3914 | 2225.5310 | 2224.3787 | 2204.0795 |
| 3.4024 | 2223.7566 | 2205.8773 | 2186.1980 |
| 3.4134 | 2187.9489 | 2187.4037 | 2168.3165 |
| 3.4244 | 2178.9277 | 2168.9562 | 2150.4350 |
| 3.4354 | 2170.2389 | 2150.5335 | 2132.5535 |
| 3.4464 | 2112.3594 | 2132.1339 | 2114.6719 |
| 3.4574 | 2092.4484 | 2113.7564 | 2096.7904 |
| 3.4684 | 2044.7802 | 2095.3995 | 2078.9089 |
| 3.4794 | 2049.8791 | 2077.0623 | 2061.0274 |
| 3.4904 | 2068.0221 | 2058.7436 | 2043.1459 |
| 3.5014 | 2028.7197 | 2041.5002 | 2025.2644 |
| 3.5124 | 1999.0580 | 2026.4268 | 2011.6518 |
| 3.5234 | 1969.6342 | 2012.4270 | 1998.0392 |
| 3.5344 | 1997.2567 | 1998.4422 | 1984.4266 |
| 3.5454 | 1966.1514 | 1984.4715 | 1970.8140 |
| 3.5564 | 1980.2537 | 1970.5143 | 1957.2014 |
| 3.5674 | 1928.6470 | 1956.5700 | 1943.5888 |
| 3.5784 | 1919.1219 | 1942.6378 | 1929.9762 |
| 3.5894 | 1926.0796 | 1928.7173 | 1916.3636 |
| 3.6004 | 1934.0398 | 1914.8078 | 1902.7510 |
| 3.6114 | 1945.5339 | 1900.9089 | 1889.1385 |
| 3.6224 | 1886.6843 | 1887.0200 | 1875.5259 |
| 3.6334 | 1931.7925 | 1873.1407 | 1861.9133 |
| 3.6444 | 1900.1062 | 1859.2705 | 1848.3007 |
| 3.6554 | 1835.3186 | 1845.4091 | 1834.6881 |
| 3.6664 | 1778.7787 | 1831.5560 | 1821.0755 |
| 3.6774 | 1806.5978 | 1817.7109 | 1807.4629 |
| 3.6884 | 1797.0310 | 1805.5252 | 1793.8503 |
| 3.6994 | 1811.0708 | 1793.6200 | 1783.8145 |
| 3.7104 | 1765.0290 | 1783.3736 | 1773.7788 |
| 3.7214 | 1792.1092 | 1773.1339 | 1763.7430 |
| 3.7324 | 1791.2812 | 1762.9006 | 1753.7072 |
| 3.7434 | 1731.6548 | 1752.6735 | 1743.6714 |
| 3.7544 | 1731.8171 | 1742.4522 | 1733.6356 |
| 3.7654 | 1764.8633 | 1732.2366 | 1723.5998 |
| 3.7764 | 1800.2601 | 1722.0265 | 1713.5640 |
| 3.7874 | 1703.8672 | 1711.8215 | 1703.5282 |
| 3.7984 | 1694.8382 | 1701.6216 | 1693.4924 |
| 3.8094 | 1647.0875 | 1691.4265 | 1683.4566 |
| 3.8204 | 1593.5871 | 1681.2360 | 1673.4209 |
| 3.8314 | 1718.7257 | 1671.0499 | 1663.3851 |
| 3.8424 | 1728.6878 | 1660.8681 | 1653.3493 |
| 3.8534 | 1601.0885 | 1650.6905 | 1643.3135 |
| 3.8644 | 1657.2212 | 1640.5168 | 1633.2777 |
| 3.8754 | 1623.1947 | 1631.5954 | 1623.2419 |
| 3.8864 | 1612.2522 | 1622.8840 | 1615.9093 |
| 3.8974 | 1592.7906 | 1615.4246 | 1608.5767 |
| 3.9084 | 1630.2527 | 1607.9686 | 1601.2441 |
| 3.9194 | 1631.4454 | 1600.5159 | 1593.9115 |
| 3.9304 | 1614.1140 | 1593.0664 | 1586.5790 |
| 3.9414 | 1538.7748 | 1585.6199 | 1579.2464 |
| 3.9524 | 1560.0207 | 1578.1764 | 1571.9138 |
| 3.9634 | 1596.3805 | 1570.7358 | 1564.5812 |
| 3.9744 | 1617.0030 | 1563.2979 | 1557.2486 |
| 3.9854 | 1626.7699 | 1555.8628 | 1549.9160 |
| 3.9964 | 1571.7532 | 1548.4302 | 1542.5834 |
| 4.0074 | 1555.4690 | 1541.0001 | 1535.2508 |
| 4.0184 | 1522.2670 | 1533.5724 | 1527.9182 |
| 4.0294 | 1499.5074 | 1526.1470 | 1520.5856 |
| 4.0404 | 1473.5939 | 1518.7239 | 1513.2530 |
| 4.0514 | 1458.5900 | 1511.3030 | 1505.9204 |
| 4.0624 | 1500.7434 | 1504.1825 | 1498.5879 |
| 4.0734 | 1533.4572 | 1497.1132 | 1491.9010 |
| 4.0844 | 1531.9115 | 1490.3442 | 1485.2141 |
| 4.0954 | 1486.9587 | 1483.5771 | 1478.5272 |
| 4.1064 | 1463.6150 | 1476.8119 | 1471.8404 |
| 4.1174 | 1454.9971 | 1470.0484 | 1465.1535 |
| 4.1284 | 1481.0487 | 1463.2868 | 1458.4666 |
| 4.1394 | 1477.6234 | 1456.5268 | 1451.7798 |
| 4.1504 | 1438.6519 | 1449.7684 | 1445.0929 |
| 4.1614 | 1451.4976 | 1443.0117 | 1438.4060 |
| 4.1724 | 1471.7812 | 1436.2565 | 1431.7191 |
| 4.1834 | 1478.8496 | 1429.5029 | 1425.0323 |
| 4.1944 | 1454.7060 | 1422.7506 | 1418.3454 |

Scan List

| Vis. | Dataset Name | Start pos. [°2θ] | End pos. [°2θ] | Step [°2θ] | Meas.Date/Time |
| --- | --- | --- | --- | --- | --- |
| * | 18 Etosha22 SSCRT 0-0.5cm S4 | 2.0054 | 29.9894 | 0.0110 | 12/7/2023 1:57:17 PM |

Peak List

| Pos. [°2θ] | Height [cts] | FWHM Left [°2θ] | d-spacing [Å] | Rel. Int. [%] |
| --- | --- | --- | --- | --- |
| 2.6988 | 1839.44 | 0.1948 | 32.71011 | 100.00 |
| 7.0601 | 1383.55 | 0.1732 | 12.51060 | 75.22 |
| 8.6762 | 409.65 | 0.1732 | 10.18346 | 22.27 |
| 12.9011 | 16.34 | 0.6927 | 6.85653 | 0.89 |
| 15.6938 | 640.40 | 0.0866 | 5.64211 | 34.81 |
| 17.6322 | 51.35 | 0.1732 | 5.02599 | 2.79 |
| 18.1669 | 111.42 | 0.0649 | 4.87924 | 6.06 |
| 19.6038 | 36.18 | 0.5196 | 4.52473 | 1.97 |
| 23.3626 | 24.48 | 0.2598 | 3.80456 | 1.33 |
| 25.8366 | 558.46 | 0.1082 | 3.44558 | 30.36 |
| 26.5747 | 123.84 | 0.1732 | 3.35153 | 6.73 |
| 27.4795 | 62.17 | 0.1299 | 3.24320 | 3.38 |

Pattern List

| Visible | Ref.Code | Score | Compound Name | Chem. Formula | Mineral Name | SemiQuant[%] |
| --- | --- | --- | --- | --- | --- | --- |
| * | 01-072-4625 | 25 | Sodium Aluminum Silicate Hydrate | Na Al ( Si2 O6 ) ( H2 O ) | Analcime | 6 |
| * | 01-070-4175 | 46 | Tin Oxide | Sn0.912 O2 | Cassiterite | 1 |
| * | 01-089-6415 | 33 | Potassium Manganese Silicate Hydroxide Hydrate | K3.68 Mn15.904 Si25.472 O64 ( O H )9.376 ( H2 O )7.024 | Ganophyllite | 14 |
| * | 04-017-4317 | 29 | Potassium Magnesium Manganese Iron Aluminum Silicate Hydroxide | K Mg0.2 Mn0.1 Fe2.4 Al1.7 Si2.6 O10 ( O H )2 | Biotite-1M | 7 |
| * | 04-011-6576 | 13 | Magnesium Aluminum Silicate Hydroxide Hydrate | Mg3.5 Al Si3 O10 ( O H )2 ( H2 O )4 | Vermiculite | 2 |
| * | 04-016-3203 | 16 | Magnesium Silicon Oxide Hydroxide Hydrate | Mg4 Si6 O15 ( O H )2 ( H2 O )6 | Sepiolite | 6 |
| * | 04-025-4215 | 17 | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide | Mg10.4 V0.36 Mn33.5 Fe0.14 Al0.69 Si6.77 As6.5 P0.3 O54 ( O H )42 | Carlfrancisite | 41 |
| * | 01-082-8023 | 18 | Sodium Magnesium Silicon Oxide Hydrate | Na2 Mg3 ( Si6 O16 ) ( H2 O )7 | Loughlinite | 15 |
| * | 04-016-2838 | 21 | Titanium Oxide | Ti O2 | Rutile | 1 |
| * | 00-034-0159 | 5 | Potassium Magnesium Aluminum Fluoride Silicate Hydroxide | K Mg3 Si3 Al O10 ( F , O H )2 | Phlogopite-1M | 8 |

Anchor Scan Parameters

Dataset Name	18 Etosha22 SSCRT 0-0.5cm S4

File name	C:\aeris_data\XRD data\Goldstein\Etosha 2023\Etosha Clay Data\Sample 18\18 Etosha22 SSCRT 0-0.5cm S4.xrdml

Sample Identification	18 Etosha22 SSCRT 0-0.5cm S4

Measurement Start Date/Time	12/7/2023 1:57:17 PM

Operator	Instrument

Raw Data Origin	XRD measurement (*.XRDML)

Scan Axis	Gonio

Start Position [°2θ]	2.0054

End Position [°2θ]	29.9894

Step Size [°2θ]	0.0110

Scan Step Time [s]	48.1950

Scan Type	Continuous

PSD Mode	Scanning

PSD Length [°2θ]	5.54

Offset [°2θ]	0.0000

Divergence Slit Type	Fixed

Divergence Slit Size [°]	0.0603

Specimen Length [mm]	10.00

Measurement Temperature [°C]	25.00

Anode Material	Cu

K-α1 [Å]	1.54060

K-α2 [Å]	1.54443

K-β1 [Å]	1.39225

K-A2 / K-A1 Ratio	0.50000

Generator Settings	15 mA, 40 kV

Diffractometer Type	2082464

Diffractometer Number	0

Goniometer Radius [mm]	145.00

Dist. Focus-Diverg. Slit [mm]	95.00

Incident Beam Monochromator	No

Spinning	Yes