19 Etosha 22 Sssub 0.5-5cm S4 400 C REPORT

Graphics

Graphics

Graphics

Quantitative Results

Phase Sodium Aluminum Silicate Hydrate

Weight fraction/ %	17.0

Phase Tin Oxide

Weight fraction/ %	1.0

Phase Potassium Magnesium Manganese Iron Aluminum Silicate Hydroxide

Weight fraction/ %	14.0

Phase Potassium Manganese Silicate Hydrate

Weight fraction/ %	8.0

Phase Magnesium Silicate Hydroxide Hydrate

Weight fraction/ %	9.0

Phase Magnesium Aluminum Silicate Hydroxide Hydrate

Weight fraction/ %	14.0

Phase Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide

Weight fraction/ %	37.0

Multiple Quantitative Results

Scans vs Phases Matrix

| Scan name | Sodium Aluminum Silicate Hydrate | Tin Oxide | Potassium Magnesium Manganese Iron Aluminum Silicate Hydroxide | Potassium Manganese Silicate Hydrate | Magnesium Silicate Hydroxide Hydrate | Magnesium Aluminum Silicate Hydroxide Hydrate | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 19 Etosha22 SSsub 0.5-5cm S4 400C | 17.0 | 1.0 | 14.0 | 8.0 | 9.0 | 14.0 | 37.0 |

Anchor Scan Data

| Pos. [°2θ] | Iobs [cts] | Icalc [cts] | Iback [cts] |
| --- | --- | --- | --- |
| 2.0054 | 8451.0000 | 8428.2299 | 8451.0000 |
| 2.0164 | 8433.2134 | 8410.4472 | 8393.5986 |
| 2.0274 | 8371.8191 | 8353.5817 | 8336.1973 |
| 2.0384 | 8440.9764 | 8296.7440 | 8278.7959 |
| 2.0494 | 8355.2645 | 8239.9362 | 8221.3946 |
| 2.0604 | 8229.9164 | 8183.1603 | 8163.9932 |
| 2.0714 | 8291.5782 | 8126.4188 | 8106.5919 |
| 2.0824 | 8118.9562 | 8069.7141 | 8049.1905 |
| 2.0934 | 8085.7345 | 8013.0492 | 7991.7891 |
| 2.1044 | 8158.9602 | 7956.4269 | 7934.3878 |
| 2.1154 | 8039.8328 | 7899.8508 | 7876.9864 |
| 2.1264 | 8075.1180 | 7843.3244 | 7819.5851 |
| 2.1374 | 7880.7611 | 7786.8520 | 7762.1837 |
| 2.1484 | 8008.0128 | 7730.4379 | 7704.7824 |
| 2.1594 | 7783.0393 | 7674.0873 | 7647.3810 |
| 2.1704 | 7699.3525 | 7617.8055 | 7589.9796 |
| 2.1814 | 7760.6863 | 7561.5987 | 7532.5783 |
| 2.1924 | 7787.5821 | 7505.3608 | 7475.1769 |
| 2.2034 | 7768.7434 | 7449.2724 | 7417.6097 |
| 2.2144 | 7695.6229 | 7393.1689 | 7360.0426 |
| 2.2254 | 7655.7375 | 7337.1728 | 7302.4754 |
| 2.2364 | 7639.4159 | 7281.2948 | 7244.9082 |
| 2.2474 | 7587.3520 | 7225.5468 | 7187.3410 |
| 2.2584 | 7602.5905 | 7169.9424 | 7129.7739 |
| 2.2694 | 7580.6726 | 7114.4971 | 7072.2067 |
| 2.2804 | 7416.5177 | 7059.2284 | 7014.6395 |
| 2.2914 | 7398.7375 | 7004.1567 | 6957.0723 |
| 2.3024 | 7552.0354 | 6949.3055 | 6899.5052 |
| 2.3134 | 7493.6696 | 6894.7027 | 6841.9380 |
| 2.3244 | 7378.4253 | 6840.3815 | 6784.3708 |
| 2.3354 | 7276.9144 | 6786.3828 | 6726.8036 |
| 2.3464 | 7217.6205 | 6732.7578 | 6669.2364 |
| 2.3574 | 7226.0669 | 6679.5722 | 6611.6693 |
| 2.3684 | 7196.0693 | 6626.9124 | 6554.1021 |
| 2.3794 | 7122.1357 | 6574.8023 | 6496.5349 |
| 2.3904 | 7084.7773 | 6523.5381 | 6438.8336 |
| 2.4014 | 7052.1327 | 6473.1914 | 6381.1323 |
| 2.4124 | 7029.8412 | 6424.1404 | 6323.4309 |
| 2.4234 | 7041.1622 | 6376.7686 | 6265.7296 |
| 2.4344 | 6935.3540 | 6331.5821 | 6208.0283 |
| 2.4454 | 6893.6991 | 6289.2336 | 6150.3269 |
| 2.4564 | 6975.4956 | 6250.5442 | 6092.6256 |
| 2.4674 | 6965.2124 | 6216.5152 | 6034.9243 |
| 2.4784 | 6815.6086 | 6188.3257 | 5977.2230 |
| 2.4894 | 6851.1613 | 6167.3083 | 5919.5216 |
| 2.5004 | 6824.6372 | 6154.8963 | 5861.8203 |
| 2.5114 | 6779.3196 | 6152.5407 | 5804.1190 |
| 2.5224 | 6762.5428 | 6161.5937 | 5746.4176 |
| 2.5334 | 6707.2507 | 6183.1633 | 5688.7163 |
| 2.5444 | 6696.3977 | 6217.9429 | 5631.0150 |
| 2.5554 | 6593.9843 | 6266.0234 | 5573.3137 |
| 2.5664 | 6529.3732 | 6326.6879 | 5515.6123 |
| 2.5774 | 6566.0698 | 6398.1810 | 5457.9110 |
| 2.5884 | 6559.6401 | 6477.4397 | 5400.2097 |
| 2.5994 | 6478.6283 | 6559.7801 | 5342.5083 |
| 2.6104 | 6536.9371 | 6638.5952 | 5284.8070 |
| 2.6214 | 6547.9616 | 6705.2513 | 5227.1057 |
| 2.6324 | 6521.0900 | 6749.5423 | 5169.4044 |
| 2.6434 | 6493.1878 | 6761.0848 | 5111.7030 |
| 2.6544 | 6485.4503 | 6731.6620 | 5054.0017 |
| 2.6654 | 6345.8820 | 6657.6633 | 4996.3004 |
| 2.6764 | 6152.0472 | 6541.1725 | 4938.5990 |
| 2.6874 | 6142.8643 | 6389.4258 | 4880.8977 |
| 2.6984 | 6098.4734 | 6212.4860 | 4823.1964 |
| 2.7094 | 5983.6716 | 6020.7499 | 4765.4951 |
| 2.7204 | 5776.4444 | 5823.3274 | 4707.7937 |
| 2.7314 | 5742.3569 | 5627.3701 | 4650.0924 |
| 2.7424 | 5652.7679 | 5438.0581 | 4592.3911 |
| 2.7534 | 5398.1425 | 5258.7755 | 4534.6897 |
| 2.7644 | 5379.1386 | 5091.7491 | 4476.8543 |
| 2.7754 | 5202.4611 | 4937.8172 | 4419.0188 |
| 2.7864 | 4898.1106 | 4797.1811 | 4361.1833 |
| 2.7974 | 4898.7080 | 4669.2935 | 4303.3478 |
| 2.8084 | 4543.3067 | 4553.1429 | 4245.5124 |
| 2.8194 | 4471.0757 | 4447.4294 | 4187.6769 |
| 2.8304 | 4356.4587 | 4350.7174 | 4129.8414 |
| 2.8414 | 4323.6470 | 4261.5601 | 4072.0059 |
| 2.8524 | 4130.8249 | 4178.5921 | 4014.1704 |
| 2.8634 | 4116.1652 | 4100.5898 | 3956.3350 |
| 2.8744 | 3854.8028 | 4026.5028 | 3898.4995 |
| 2.8854 | 3852.8997 | 3955.4620 | 3840.6640 |
| 2.8964 | 3798.2434 | 3886.7704 | 3782.8285 |
| 2.9074 | 3728.8663 | 3819.8845 | 3724.9930 |
| 2.9184 | 3709.1175 | 3754.3895 | 3667.1576 |
| 2.9294 | 3568.7404 | 3689.9746 | 3609.3221 |
| 2.9404 | 3560.5079 | 3642.8301 | 3551.4866 |
| 2.9514 | 3539.0501 | 3587.6253 | 3517.7524 |
| 2.9624 | 3359.5251 | 3549.3957 | 3484.0182 |
| 2.9734 | 3374.7768 | 3511.6271 | 3450.2840 |
| 2.9844 | 3308.5816 | 3474.2488 | 3416.5498 |
| 2.9954 | 3233.8142 | 3437.2061 | 3382.8155 |
| 3.0064 | 3205.4597 | 3400.4555 | 3349.0813 |
| 3.0174 | 3196.7463 | 3363.9619 | 3315.3471 |
| 3.0284 | 3202.9823 | 3327.6961 | 3281.6129 |
| 3.0394 | 3132.5536 | 3291.6334 | 3247.8787 |
| 3.0504 | 3139.9941 | 3255.7527 | 3214.1445 |
| 3.0614 | 3125.6431 | 3220.0358 | 3180.4103 |
| 3.0724 | 3093.1883 | 3184.4666 | 3146.6761 |
| 3.0834 | 3102.0491 | 3149.0312 | 3112.9419 |
| 3.0944 | 2991.0310 | 3113.7170 | 3079.2076 |
| 3.1054 | 3054.3992 | 3078.5130 | 3045.4734 |
| 3.1164 | 2983.2738 | 3043.4096 | 3011.7392 |
| 3.1274 | 2918.6224 | 3019.8903 | 2978.0050 |
| 3.1384 | 3005.1711 | 2990.3379 | 2961.1387 |
| 3.1494 | 3011.7905 | 2972.3549 | 2944.2724 |
| 3.1604 | 2944.0605 | 2954.4424 | 2927.4061 |
| 3.1714 | 2941.3884 | 2936.5949 | 2910.5398 |
| 3.1824 | 2944.7217 | 2918.8072 | 2893.6735 |
| 3.1934 | 2889.2832 | 2901.0747 | 2876.8072 |
| 3.2044 | 2879.7616 | 2883.3932 | 2859.9409 |
| 3.2154 | 2884.2222 | 2865.7589 | 2843.0746 |
| 3.2264 | 2792.4203 | 2848.1683 | 2826.2083 |
| 3.2374 | 2764.5192 | 2830.6183 | 2809.3420 |
| 3.2484 | 2769.6667 | 2813.1060 | 2792.4757 |
| 3.2594 | 2770.4130 | 2795.6288 | 2775.6094 |
| 3.2704 | 2785.2694 | 2778.1844 | 2758.7431 |
| 3.2814 | 2805.9410 | 2760.7704 | 2741.8768 |
| 3.2924 | 2795.6593 | 2743.3850 | 2725.0105 |
| 3.3034 | 2732.3235 | 2726.0262 | 2708.1442 |
| 3.3144 | 2650.6760 | 2711.5621 | 2691.2779 |
| 3.3254 | 2659.6165 | 2695.5939 | 2678.6236 |
| 3.3364 | 2651.3023 | 2682.5174 | 2665.9693 |
| 3.3474 | 2614.4651 | 2669.4614 | 2653.3150 |
| 3.3584 | 2599.3318 | 2656.4249 | 2640.6608 |
| 3.3694 | 2560.9577 | 2643.4065 | 2628.0065 |
| 3.3804 | 2551.7630 | 2630.4053 | 2615.3522 |
| 3.3914 | 2593.0620 | 2617.4203 | 2602.6979 |
| 3.4024 | 2572.1234 | 2604.4506 | 2590.0436 |
| 3.4134 | 2580.9115 | 2591.4952 | 2577.3893 |
| 3.4244 | 2602.4071 | 2578.5535 | 2564.7350 |
| 3.4354 | 2573.0433 | 2565.6247 | 2552.0808 |
| 3.4464 | 2556.4582 | 2552.7081 | 2539.4265 |
| 3.4574 | 2496.2271 | 2539.8031 | 2526.7722 |
| 3.4684 | 2529.6446 | 2526.9091 | 2514.1179 |
| 3.4794 | 2529.8269 | 2514.0254 | 2501.4636 |
| 3.4904 | 2416.0398 | 2501.1517 | 2488.8093 |
| 3.5014 | 2496.9440 | 2488.2873 | 2476.1550 |
| 3.5124 | 2494.3481 | 2475.4319 | 2463.5008 |
| 3.5234 | 2500.8968 | 2462.5850 | 2450.8465 |
| 3.5344 | 2419.9415 | 2449.7463 | 2438.1922 |
| 3.5454 | 2417.4789 | 2436.9152 | 2425.5379 |
| 3.5564 | 2384.3525 | 2424.0916 | 2412.8836 |
| 3.5674 | 2410.9744 | 2411.2750 | 2400.2293 |
| 3.5784 | 2422.9695 | 2398.4651 | 2387.5751 |
| 3.5894 | 2345.7787 | 2385.6616 | 2374.9208 |
| 3.6004 | 2348.0305 | 2372.8643 | 2362.2665 |
| 3.6114 | 2324.8092 | 2360.0730 | 2349.6122 |
| 3.6224 | 2314.5796 | 2347.2872 | 2336.9579 |
| 3.6334 | 2341.0295 | 2334.5069 | 2324.3036 |
| 3.6444 | 2333.6981 | 2321.7317 | 2311.6493 |
| 3.6554 | 2328.4690 | 2308.9615 | 2298.9951 |
| 3.6664 | 2280.9228 | 2296.1962 | 2286.3408 |
| 3.6774 | 2273.8682 | 2283.4354 | 2273.6865 |
| 3.6884 | 2269.5973 | 2273.8563 | 2261.0322 |
| 3.6994 | 2241.3225 | 2262.5903 | 2253.0413 |
| 3.7104 | 2266.0585 | 2254.5057 | 2245.0504 |
| 3.7214 | 2113.0412 | 2246.4250 | 2237.0595 |
| 3.7324 | 2231.9465 | 2238.3481 | 2229.0686 |
| 3.7434 | 2254.2458 | 2230.2749 | 2221.0777 |
| 3.7544 | 2255.9543 | 2222.2052 | 2213.0868 |
| 3.7654 | 2188.3402 | 2214.1390 | 2205.0959 |
| 3.7764 | 2238.8584 | 2206.0761 | 2197.1050 |
| 3.7874 | 2137.9115 | 2198.0164 | 2189.1141 |
| 3.7984 | 2228.0585 | 2189.9597 | 2181.1232 |
| 3.8094 | 2243.8200 | 2181.9061 | 2173.1323 |
| 3.8204 | 2168.6268 | 2173.8554 | 2165.1414 |
| 3.8314 | 2123.0561 | 2165.8075 | 2157.1505 |
| 3.8424 | 2166.0555 | 2157.7623 | 2149.1596 |
| 3.8534 | 2068.6697 | 2149.7198 | 2141.1687 |
| 3.8644 | 2206.8422 | 2141.6799 | 2133.1778 |
| 3.8754 | 2191.5683 | 2133.5636 | 2125.1869 |
| 3.8864 | 2179.4425 | 2125.4918 | 2117.0802 |
| 3.8974 | 2193.0157 | 2117.3434 | 2108.9735 |
| 3.9084 | 2134.0325 | 2109.1974 | 2100.8669 |
| 3.9194 | 2150.1475 | 2101.0536 | 2092.7602 |
| 3.9304 | 2117.5850 | 2092.9121 | 2084.6535 |
| 3.9414 | 2099.9194 | 2084.7727 | 2076.5469 |
| 3.9524 | 2069.5221 | 2076.6354 | 2068.4402 |
| 3.9634 | 2039.8368 | 2068.5002 | 2060.3335 |
| 3.9744 | 2090.3933 | 2060.3669 | 2052.2269 |
| 3.9854 | 2057.6638 | 2052.2357 | 2044.1202 |
| 3.9964 | 2127.6647 | 2044.1064 | 2036.0135 |
| 4.0074 | 2080.3884 | 2035.9791 | 2027.9069 |
| 4.0184 | 2038.0147 | 2027.8535 | 2019.8002 |
| 4.0294 | 2034.7699 | 2019.7299 | 2011.6935 |
| 4.0404 | 2039.5201 | 2011.6080 | 2003.5869 |
| 4.0514 | 1998.6225 | 2003.4879 | 1995.4802 |
| 4.0624 | 2061.7227 | 1995.3696 | 1987.3735 |
| 4.0734 | 2010.4179 | 1987.2530 | 1979.2669 |
| 4.0844 | 2021.5531 | 1979.1382 | 1971.1602 |
| 4.0954 | 2010.2232 | 1971.0250 | 1963.0535 |
| 4.1064 | 1951.7969 | 1962.9135 | 1954.9469 |
| 4.1174 | 1944.0295 | 1954.8036 | 1946.8402 |
| 4.1284 | 1976.8087 | 1946.6955 | 1938.7335 |
| 4.1394 | 1944.0738 | 1938.5889 | 1930.6269 |
| 4.1504 | 1941.1298 | 1930.4840 | 1922.5202 |
| 4.1614 | 1933.7709 | 1922.3806 | 1914.4135 |
| 4.1724 | 1932.7197 | 1914.2789 | 1906.3069 |
| 4.1834 | 1967.8142 | 1906.1788 | 1898.2002 |
| 4.1944 | 2007.7192 | 1898.0803 | 1890.0935 |

Scan List

| Vis. | Dataset Name | Start pos. [°2θ] | End pos. [°2θ] | Step [°2θ] | Meas.Date/Time |
| --- | --- | --- | --- | --- | --- |
| * | 19 Etosha22 SSsub 0.5-5cm S4 400C | 2.0054 | 29.9894 | 0.0110 | 12/12/2023 12:17:22 PM |

Peak List

| Pos. [°2θ] | Height [cts] | FWHM Left [°2θ] | d-spacing [Å] | Rel. Int. [%] |
| --- | --- | --- | --- | --- |
| 2.6537 | 1500.11 | 0.1732 | 33.26536 | 100.00 |
| 5.2524 | 82.40 | 0.2598 | 16.81138 | 5.49 |
| 7.2334 | 965.81 | 0.5628 | 12.21111 | 64.38 |
| 8.6909 | 640.22 | 0.1082 | 10.16626 | 42.68 |
| 13.3124 | 10.40 | 0.8659 | 6.64559 | 0.69 |
| 15.7664 | 667.57 | 0.0974 | 5.61631 | 44.50 |
| 17.6192 | 54.33 | 0.1732 | 5.02965 | 3.62 |
| 18.2142 | 79.27 | 0.1299 | 4.86666 | 5.28 |
| 19.6149 | 76.96 | 0.1299 | 4.52219 | 5.13 |
| 25.9279 | 426.69 | 0.1515 | 3.43366 | 28.44 |
| 26.6841 | 135.70 | 0.2598 | 3.33804 | 9.05 |
| 27.5204 | 57.39 | 0.2598 | 3.23847 | 3.83 |

Pattern List

| Visible | Ref.Code | Score | Compound Name | Chem. Formula | Mineral Name | SemiQuant[%] |
| --- | --- | --- | --- | --- | --- | --- |
| * | 01-072-4625 | 56 | Sodium Aluminum Silicate Hydrate | Na Al ( Si2 O6 ) ( H2 O ) | Analcime | 17 |
| * | 01-070-4177 | 38 | Tin Oxide | Sn O2 | Cassiterite | 1 |
| * | 04-017-4317 | 32 | Potassium Magnesium Manganese Iron Aluminum Silicate Hydroxide | K Mg0.2 Mn0.1 Fe2.4 Al1.7 Si2.6 O10 ( O H )2 | Biotite-1M | 14 |
| * | 01-085-1405 | 21 | Potassium Manganese Silicate Hydrate | K2.16 Mn16 ( Si26.9 O67.8 ) ( O H )8 | Ganophyllite | 8 |
| * | 01-075-8323 | 23 | Magnesium Silicate Hydroxide Hydrate | Mg8 ( Si12 O30 ( O H )4 ) ( H2 O )11.82 | Sepiolite | 9 |
| * | 01-082-1872 | 15 | Magnesium Aluminum Silicate Hydroxide Hydrate | ( Mg0.669 Al0.331 )4 ( Si4 O10 )2 ( O H )2 ( H2 O )8 | Palygorskite-M | 14 |
| * | 04-025-4215 | 25 | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide | Mg10.4 V0.36 Mn33.5 Fe0.14 Al0.69 Si6.77 As6.5 P0.3 O54 ( O H )42 | Carlfrancisite | 37 |

Anchor Scan Parameters

Dataset Name	19 Etosha22 SSsub 0.5-5cm S4 400C

File name	C:\aeris_data\XRD data\Goldstein\Etosha 2023\Etosha Clay Data\Sample 19\19 Etosha22 SSsub 0.5-5cm S4 400C.xrdml

Sample Identification	19 Etosha22 SSsub 0.5-5cm S4 400C

Measurement Start Date/Time	12/12/2023 12:17:22 PM

Operator	Instrument

Raw Data Origin	XRD measurement (*.XRDML)

Scan Axis	Gonio

Start Position [°2θ]	2.0054

End Position [°2θ]	29.9894

Step Size [°2θ]	0.0110

Scan Step Time [s]	48.1950

Scan Type	Continuous

PSD Mode	Scanning

PSD Length [°2θ]	5.54

Offset [°2θ]	0.0000

Divergence Slit Type	Fixed

Divergence Slit Size [°]	0.0603

Specimen Length [mm]	10.00

Measurement Temperature [°C]	25.00

Anode Material	Cu

K-α1 [Å]	1.54060

K-α2 [Å]	1.54443

K-β1 [Å]	1.39225

K-A2 / K-A1 Ratio	0.50000

Generator Settings	15 mA, 40 kV

Diffractometer Type	2082464

Diffractometer Number	0

Goniometer Radius [mm]	145.00

Dist. Focus-Diverg. Slit [mm]	95.00

Incident Beam Monochromator	No

Spinning	Yes