19 Etosha 22 Sssub 0.5-5cm S4 550 C REPORT

Graphics

Graphics

Graphics

Quantitative Results

Phase Titanium Oxide

Weight fraction/ %	3.0

Phase Sodium Aluminum Silicate Hydrate

Weight fraction/ %	25.0

Phase Potassium Magnesium Manganese Iron Aluminum Silicate Hydroxide

Weight fraction/ %	18.0

Phase Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide

Weight fraction/ %	42.0

Phase Magnesium Aluminum Silicon Oxide Hydroxide Hydrate

Weight fraction/ %	12.0

Multiple Quantitative Results

Scans vs Phases Matrix

| Scan name | Titanium Oxide | Sodium Aluminum Silicate Hydrate | Potassium Magnesium Manganese Iron Aluminum Silicate Hydroxide | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide | Magnesium Aluminum Silicon Oxide Hydroxide Hydrate |
| --- | --- | --- | --- | --- | --- |
| 19 Etosha22 SSsub 0.5-5cm S4 550C | 3.0 | 25.0 | 18.0 | 42.0 | 12.0 |

Anchor Scan Data

| Pos. [°2θ] | Iobs [cts] | Icalc [cts] | Iback [cts] |
| --- | --- | --- | --- |
| 2.0054 | 8549.0000 | 9319.1731 | 8549.0000 |
| 2.0164 | 8534.1106 | 9377.0720 | 8489.2919 |
| 2.0274 | 8538.0836 | 9384.3152 | 8429.5837 |
| 2.0384 | 8343.0737 | 9352.0609 | 8369.8756 |
| 2.0494 | 8343.1318 | 9274.3926 | 8310.1675 |
| 2.0604 | 8318.9838 | 9155.4499 | 8250.4593 |
| 2.0714 | 8490.2743 | 9007.0766 | 8190.7512 |
| 2.0824 | 8336.7193 | 8843.3177 | 8131.0431 |
| 2.0934 | 8277.4730 | 8676.1734 | 8071.3349 |
| 2.1044 | 8334.6062 | 8514.1268 | 8011.6268 |
| 2.1154 | 8240.2960 | 8362.3870 | 7951.9187 |
| 2.1264 | 8214.1047 | 8223.6035 | 7892.2106 |
| 2.1374 | 8187.2566 | 8098.5336 | 7832.5024 |
| 2.1484 | 8247.5334 | 7986.5962 | 7772.7943 |
| 2.1594 | 8004.8967 | 7886.3531 | 7713.0862 |
| 2.1704 | 7849.4587 | 7795.9274 | 7653.3780 |
| 2.1814 | 7940.6618 | 7713.3422 | 7593.6699 |
| 2.1924 | 8017.1362 | 7636.7068 | 7533.9618 |
| 2.2034 | 7849.0797 | 7564.4868 | 7474.1208 |
| 2.2144 | 7951.0241 | 7495.4195 | 7414.2799 |
| 2.2254 | 7857.2320 | 7428.6359 | 7354.4390 |
| 2.2364 | 7672.7729 | 7363.4794 | 7294.5981 |
| 2.2474 | 7631.1790 | 7299.5001 | 7234.7571 |
| 2.2584 | 7622.7753 | 7236.3971 | 7174.9162 |
| 2.2694 | 7706.8319 | 7173.9721 | 7115.0753 |
| 2.2804 | 7633.9784 | 7112.0936 | 7055.2344 |
| 2.2914 | 7653.3825 | 7050.6737 | 6995.3934 |
| 2.3024 | 7629.6150 | 6989.6517 | 6935.5525 |
| 2.3134 | 7554.2291 | 6928.9851 | 6875.7116 |
| 2.3244 | 7445.1298 | 6868.6436 | 6815.8707 |
| 2.3354 | 7537.4838 | 6808.6057 | 6756.0297 |
| 2.3464 | 7403.3722 | 6748.8570 | 6696.1888 |
| 2.3574 | 7366.5113 | 6689.3889 | 6636.3479 |
| 2.3684 | 7363.6976 | 6630.1981 | 6576.5070 |
| 2.3794 | 7270.9253 | 6571.2865 | 6516.6660 |
| 2.3904 | 7300.3810 | 6512.6608 | 6456.8251 |
| 2.4014 | 7268.5133 | 6454.3335 | 6396.9842 |
| 2.4124 | 7142.7969 | 6396.3238 | 6337.1433 |
| 2.4234 | 7120.8918 | 6338.6586 | 6277.3023 |
| 2.4344 | 7209.1667 | 6281.3757 | 6217.4614 |
| 2.4454 | 7256.2006 | 6224.5271 | 6157.6205 |
| 2.4564 | 7191.0870 | 6168.1843 | 6097.7795 |
| 2.4674 | 7082.2153 | 6112.4463 | 6037.9386 |
| 2.4784 | 7043.7984 | 6057.4495 | 5978.0977 |
| 2.4894 | 7018.6027 | 6003.3809 | 5918.2568 |
| 2.5004 | 7047.3938 | 5950.4949 | 5858.4158 |
| 2.5114 | 6951.1298 | 5899.1315 | 5798.5749 |
| 2.5224 | 6817.6259 | 5849.7372 | 5738.7340 |
| 2.5334 | 6837.3982 | 5802.8842 | 5678.8931 |
| 2.5444 | 6799.3648 | 5759.2848 | 5619.0521 |
| 2.5554 | 6719.8977 | 5719.7981 | 5559.2112 |
| 2.5664 | 6683.4631 | 5685.3681 | 5499.3703 |
| 2.5774 | 6606.9734 | 5657.1300 | 5439.3966 |
| 2.5884 | 6668.9710 | 5636.2244 | 5379.4229 |
| 2.5994 | 6627.4248 | 5623.8547 | 5319.4491 |
| 2.6104 | 6721.6377 | 5621.0501 | 5259.4754 |
| 2.6214 | 6565.6145 | 5628.5939 | 5199.5017 |
| 2.6324 | 6513.0413 | 5646.8801 | 5139.5280 |
| 2.6434 | 6548.9705 | 5675.7574 | 5079.5543 |
| 2.6544 | 6525.9931 | 5714.3566 | 5019.5805 |
| 2.6654 | 6290.8112 | 5760.8960 | 4959.6068 |
| 2.6764 | 6268.7311 | 5812.4505 | 4899.6331 |
| 2.6874 | 6280.3795 | 5864.6953 | 4839.6594 |
| 2.6984 | 6113.0663 | 5911.6974 | 4779.6857 |
| 2.7094 | 6024.0954 | 5945.9569 | 4719.7119 |
| 2.7204 | 5894.7601 | 5959.0173 | 4659.7382 |
| 2.7314 | 5795.2360 | 5942.8900 | 4599.7645 |
| 2.7424 | 5677.7094 | 5892.0796 | 4539.7908 |
| 2.7534 | 5596.6588 | 5805.2662 | 4479.8171 |
| 2.7644 | 5456.0914 | 5685.9613 | 4419.6792 |
| 2.7754 | 5143.0540 | 5541.0761 | 4359.5413 |
| 2.7864 | 4894.4144 | 5379.1486 | 4299.4035 |
| 2.7974 | 4891.5487 | 5208.3115 | 4239.2656 |
| 2.8084 | 4709.2699 | 5035.3424 | 4179.1278 |
| 2.8194 | 4452.4297 | 4865.3740 | 4118.9899 |
| 2.8304 | 4281.5074 | 4702.0130 | 4058.8520 |
| 2.8414 | 4257.7906 | 4547.5915 | 3998.7142 |
| 2.8524 | 4217.2507 | 4403.4158 | 3938.5763 |
| 2.8634 | 3990.6637 | 4269.9791 | 3878.4384 |
| 2.8744 | 4012.0718 | 4147.1437 | 3818.3006 |
| 2.8854 | 3736.6971 | 4034.3045 | 3758.1627 |
| 2.8964 | 3671.2699 | 3930.5391 | 3698.0249 |
| 2.9074 | 3707.7640 | 3834.7428 | 3637.8870 |
| 2.9184 | 3674.2709 | 3745.7436 | 3577.7491 |
| 2.9294 | 3492.8702 | 3662.3926 | 3517.6113 |
| 2.9404 | 3481.8864 | 3598.1268 | 3457.4734 |
| 2.9514 | 3331.1976 | 3540.0942 | 3428.9119 |
| 2.9624 | 3350.7227 | 3499.4231 | 3400.3503 |
| 2.9734 | 3335.3294 | 3460.9704 | 3371.7887 |
| 2.9844 | 3204.4695 | 3424.2252 | 3343.2272 |
| 2.9954 | 3213.1416 | 3388.7924 | 3314.6656 |
| 3.0064 | 3232.7153 | 3354.3734 | 3286.1041 |
| 3.0174 | 3106.7070 | 3320.7452 | 3257.5425 |
| 3.0284 | 3054.7581 | 3287.7434 | 3228.9810 |
| 3.0394 | 3198.9764 | 3255.2466 | 3200.4194 |
| 3.0504 | 3027.0767 | 3223.1652 | 3171.8579 |
| 3.0614 | 3061.9498 | 3191.4318 | 3143.2963 |
| 3.0724 | 2937.3029 | 3159.9952 | 3114.7347 |
| 3.0834 | 2986.7502 | 3128.8151 | 3086.1732 |
| 3.0944 | 2995.7788 | 3097.8595 | 3057.6116 |
| 3.1054 | 3036.8604 | 3067.1021 | 3029.0501 |
| 3.1164 | 2978.0703 | 3036.5210 | 3000.4885 |
| 3.1274 | 3004.2596 | 3010.8433 | 2971.9270 |
| 3.1384 | 2920.6927 | 2986.1518 | 2953.7020 |
| 3.1494 | 2911.1288 | 2966.3337 | 2935.4770 |
| 3.1604 | 2795.7920 | 2946.6309 | 2917.2521 |
| 3.1714 | 2855.3599 | 2927.0324 | 2899.0271 |
| 3.1824 | 2895.8417 | 2907.5287 | 2880.8021 |
| 3.1934 | 2936.9380 | 2888.1114 | 2862.5771 |
| 3.2044 | 2867.9508 | 2868.7728 | 2844.3522 |
| 3.2154 | 2797.8722 | 2849.5061 | 2826.1272 |
| 3.2264 | 2787.8776 | 2830.3054 | 2807.9022 |
| 3.2374 | 2789.2576 | 2811.1652 | 2789.6773 |
| 3.2484 | 2767.1111 | 2792.0806 | 2771.4523 |
| 3.2594 | 2697.9381 | 2773.0471 | 2753.2273 |
| 3.2704 | 2741.5378 | 2754.0609 | 2735.0024 |
| 3.2814 | 2681.0088 | 2735.1182 | 2716.7774 |
| 3.2924 | 2681.5398 | 2716.2159 | 2698.5524 |
| 3.3034 | 2717.9469 | 2697.3509 | 2680.3275 |
| 3.3144 | 2674.1386 | 2679.5820 | 2662.1025 |
| 3.3254 | 2596.2301 | 2662.0343 | 2646.1895 |
| 3.3364 | 2613.1067 | 2644.9085 | 2630.2764 |
| 3.3474 | 2623.5447 | 2628.0125 | 2614.3634 |
| 3.3584 | 2530.4026 | 2611.5561 | 2598.4504 |
| 3.3694 | 2522.2104 | 2595.1975 | 2582.5373 |
| 3.3804 | 2558.6819 | 2578.8612 | 2566.6243 |
| 3.3914 | 2506.1327 | 2562.5456 | 2550.7113 |
| 3.4024 | 2518.7793 | 2546.2494 | 2534.7982 |
| 3.4134 | 2530.1780 | 2529.9715 | 2518.8852 |
| 3.4244 | 2506.7566 | 2513.7106 | 2502.9722 |
| 3.4354 | 2542.0767 | 2497.4658 | 2487.0591 |
| 3.4464 | 2500.9366 | 2481.2360 | 2471.1461 |
| 3.4574 | 2492.3658 | 2465.0204 | 2455.2331 |
| 3.4684 | 2444.0860 | 2448.8182 | 2439.3200 |
| 3.4794 | 2415.3520 | 2432.6285 | 2423.4070 |
| 3.4904 | 2405.8363 | 2416.4507 | 2407.4940 |
| 3.5014 | 2390.6126 | 2403.1860 | 2391.5810 |
| 3.5124 | 2372.6386 | 2390.4484 | 2381.9883 |
| 3.5234 | 2391.7581 | 2380.6226 | 2372.3955 |
| 3.5344 | 2369.7025 | 2370.8064 | 2362.8028 |
| 3.5454 | 2345.1888 | 2360.9991 | 2353.2101 |
| 3.5564 | 2309.4793 | 2351.2003 | 2343.6174 |
| 3.5674 | 2366.5703 | 2341.4095 | 2334.0247 |
| 3.5784 | 2414.2439 | 2331.6264 | 2324.4320 |
| 3.5894 | 2395.8230 | 2321.8505 | 2314.8393 |
| 3.6004 | 2333.2458 | 2312.0815 | 2305.2466 |
| 3.6114 | 2309.2606 | 2302.3190 | 2295.6539 |
| 3.6224 | 2272.3082 | 2292.5628 | 2286.0612 |
| 3.6334 | 2322.1544 | 2282.8125 | 2276.4685 |
| 3.6444 | 2290.9375 | 2273.0678 | 2266.8758 |
| 3.6554 | 2360.4602 | 2263.3286 | 2257.2831 |
| 3.6664 | 2231.2005 | 2253.5944 | 2247.6904 |
| 3.6774 | 2196.5811 | 2243.8652 | 2238.0977 |
| 3.6884 | 2253.1151 | 2234.7348 | 2228.5050 |
| 3.6994 | 2232.4297 | 2225.7147 | 2220.2066 |
| 3.7104 | 2226.2847 | 2217.2932 | 2211.9082 |
| 3.7214 | 2261.7788 | 2208.8757 | 2203.6098 |
| 3.7324 | 2216.6558 | 2200.4621 | 2195.3114 |
| 3.7434 | 2296.8368 | 2192.0522 | 2187.0130 |
| 3.7544 | 2135.9557 | 2183.6459 | 2178.7146 |
| 3.7654 | 2125.1003 | 2175.2431 | 2170.4162 |
| 3.7764 | 2086.8245 | 2166.8435 | 2162.1178 |
| 3.7874 | 2186.1062 | 2158.4470 | 2153.8194 |
| 3.7984 | 2235.8038 | 2150.0536 | 2145.5210 |
| 3.8094 | 2178.4651 | 2141.6630 | 2137.2226 |
| 3.8204 | 2145.4204 | 2133.2753 | 2128.9242 |
| 3.8314 | 2156.4523 | 2124.8902 | 2120.6257 |
| 3.8424 | 2074.7881 | 2116.5076 | 2112.3273 |
| 3.8534 | 2123.6372 | 2108.1275 | 2104.0289 |
| 3.8644 | 2102.5334 | 2099.7498 | 2095.7305 |
| 3.8754 | 2085.8053 | 2091.3744 | 2087.4321 |
| 3.8864 | 2093.8982 | 2083.0011 | 2079.1337 |
| 3.8974 | 2090.6047 | 2074.6300 | 2070.8353 |
| 3.9084 | 2069.3466 | 2066.2609 | 2062.5369 |
| 3.9194 | 2048.9203 | 2057.8937 | 2054.2385 |
| 3.9304 | 2025.7365 | 2049.5284 | 2045.9401 |
| 3.9414 | 1988.4032 | 2041.1650 | 2037.6417 |
| 3.9524 | 2092.2979 | 2032.8033 | 2029.3433 |
| 3.9634 | 2069.0924 | 2024.4432 | 2021.0449 |
| 3.9744 | 1985.6013 | 2016.0848 | 2012.7465 |
| 3.9854 | 1985.5929 | 2007.7280 | 2004.4481 |
| 3.9964 | 1957.1106 | 1999.3727 | 1996.1497 |
| 4.0074 | 1999.3461 | 1991.0189 | 1987.8513 |
| 4.0184 | 1998.5722 | 1982.7782 | 1979.5529 |
| 4.0294 | 1935.9853 | 1974.4922 | 1971.2545 |
| 4.0404 | 1946.4616 | 1966.1492 | 1962.9561 |
| 4.0514 | 1910.5988 | 1957.8039 | 1954.6577 |
| 4.0624 | 1976.3978 | 1950.2092 | 1946.3593 |
| 4.0734 | 1987.5103 | 1942.7491 | 1939.6926 |
| 4.0844 | 1893.5575 | 1936.0395 | 1933.0260 |
| 4.0954 | 1880.8063 | 1929.3311 | 1926.3593 |
| 4.1064 | 1944.3368 | 1922.6238 | 1919.6927 |
| 4.1174 | 1963.1239 | 1915.9177 | 1913.0260 |
| 4.1284 | 1934.9287 | 1909.2127 | 1906.3594 |
| 4.1394 | 1892.6273 | 1902.5089 | 1899.6928 |
| 4.1504 | 1849.9513 | 1895.8061 | 1893.0261 |
| 4.1614 | 1877.4071 | 1889.1043 | 1886.3595 |
| 4.1724 | 1893.8879 | 1882.4035 | 1879.6928 |
| 4.1834 | 1888.6726 | 1875.7038 | 1873.0262 |
| 4.1944 | 1906.6888 | 1869.0050 | 1866.3595 |

Scan List

| Vis. | Dataset Name | Start pos. [°2θ] | End pos. [°2θ] | Step [°2θ] | Meas.Date/Time |
| --- | --- | --- | --- | --- | --- |
| * | 19 Etosha22 SSsub 0.5-5cm S4 550C | 2.0054 | 29.9894 | 0.0110 | 12/12/2023 2:36:00 PM |

Peak List

| Pos. [°2θ] | Height [cts] | FWHM Left [°2θ] | d-spacing [Å] | Rel. Int. [%] |
| --- | --- | --- | --- | --- |
| 2.0379 | 871.14 | 0.1299 | 43.31675 | 72.19 |
| 2.7375 | 1206.72 | 0.1732 | 32.24808 | 100.00 |
| 5.3105 | 125.37 | 0.1299 | 16.62765 | 10.39 |
| 8.6583 | 640.82 | 0.1515 | 10.20446 | 53.10 |
| 10.5596 | 45.86 | 0.4330 | 8.37107 | 3.80 |
| 15.9413 | 329.49 | 0.1948 | 5.55507 | 27.30 |
| 17.6073 | 39.16 | 0.2598 | 5.03303 | 3.24 |
| 19.6355 | 56.37 | 0.3464 | 4.51748 | 4.67 |
| 26.2876 | 221.49 | 0.1082 | 3.38748 | 18.35 |
| 27.4901 | 104.32 | 0.3464 | 3.24197 | 8.64 |

Pattern List

| Visible | Ref.Code | Score | Compound Name | Chem. Formula | Mineral Name | SemiQuant[%] |
| --- | --- | --- | --- | --- | --- | --- |
| * | 04-003-0648 | 35 | Titanium Oxide | Ti O2 | Rutile | 3 |
| * | 04-011-6233 | 29 | Sodium Aluminum Silicate Hydrate | Na8 Al8 Si16 O48 ( H2 O )8 | Analcime | 25 |
| * | 04-017-4317 | 29 | Potassium Magnesium Manganese Iron Aluminum Silicate Hydroxide | K Mg0.2 Mn0.1 Fe2.4 Al1.7 Si2.6 O10 ( O H )2 | Biotite-1M | 18 |
| * | 04-025-4215 | 12 | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide | Mg10.4 V0.36 Mn33.5 Fe0.14 Al0.69 Si6.77 As6.5 P0.3 O54 ( O H )42 | Carlfrancisite | 42 |
| * | 04-015-2963 | 12 | Magnesium Aluminum Silicon Oxide Hydroxide Hydrate | Mg Al Si4 O10 ( O H ) ( H2 O )4 | Palygorskite-M | 12 |

Anchor Scan Parameters

Dataset Name	19 Etosha22 SSsub 0.5-5cm S4 550C

File name	C:\aeris_data\XRD data\Goldstein\Etosha 2023\Etosha Clay Data\Sample 19\19 Etosha22 SSsub 0.5-5cm S4 550C.xrdml

Sample Identification	19 Etosha22 SSsub 0.5-5cm S4 550C

Measurement Start Date/Time	12/12/2023 2:36:00 PM

Operator	Instrument

Raw Data Origin	XRD measurement (*.XRDML)

Scan Axis	Gonio

Start Position [°2θ]	2.0054

End Position [°2θ]	29.9894

Step Size [°2θ]	0.0110

Scan Step Time [s]	48.1950

Scan Type	Continuous

PSD Mode	Scanning

PSD Length [°2θ]	5.54

Offset [°2θ]	0.0000

Divergence Slit Type	Fixed

Divergence Slit Size [°]	0.0603

Specimen Length [mm]	10.00

Measurement Temperature [°C]	25.00

Anode Material	Cu

K-α1 [Å]	1.54060

K-α2 [Å]	1.54443

K-β1 [Å]	1.39225

K-A2 / K-A1 Ratio	0.50000

Generator Settings	15 mA, 40 kV

Diffractometer Type	2082464

Diffractometer Number	0

Goniometer Radius [mm]	145.00

Dist. Focus-Diverg. Slit [mm]	95.00

Incident Beam Monochromator	No

Spinning	Yes