19 Etosha 22 Sssub 0.5-5cm S4 GLYCOL REPORT

Graphics

Graphics

Graphics

Quantitative Results

Phase Silicon Oxide

Weight fraction/ %	6.0

Phase Potassium Sodium Magnesium Manganese Zinc Aluminum Iron Titanium Fluoride Aluminum Iron Silicate Hydroxide

Weight fraction/ %	21.0

Phase Potassium Sodium Calcium Aluminum Silicon Oxide Hydrate

Weight fraction/ %	19.0

Phase Magnesium Silicate Hydroxide Hydrate

Weight fraction/ %	4.0

Phase Potassium Sodium Calcium Manganese Aluminum Iron Silicon Oxide Hydroxide Hydrate

Weight fraction/ %	13.0

Phase Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide

Weight fraction/ %	37.0

Multiple Quantitative Results

Scans vs Phases Matrix

| Scan name | Silicon Oxide | Potassium Sodium Magnesium Manganese Zinc Aluminum Iron Titanium Fluoride Aluminum Iron Silicate Hydroxide | Potassium Sodium Calcium Aluminum Silicon Oxide Hydrate | Magnesium Silicate Hydroxide Hydrate | Potassium Sodium Calcium Manganese Aluminum Iron Silicon Oxide Hydroxide Hydrate | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide |
| --- | --- | --- | --- | --- | --- | --- |
| 19 Etosha22 SSsub 0.5-5cm glycol | 6.0 | 21.0 | 19.0 | 4.0 | 13.0 | 37.0 |

Anchor Scan Data

| Pos. [°2θ] | Iobs [cts] | Icalc [cts] | Iback [cts] |
| --- | --- | --- | --- |
| 2.0054 | 8190.0000 | 8164.7454 | 8190.0000 |
| 2.0164 | 8046.9174 | 8147.3556 | 8134.9789 |
| 2.0274 | 8198.0501 | 8092.7395 | 8079.9578 |
| 2.0384 | 8085.3510 | 8038.1435 | 8024.9367 |
| 2.0494 | 8194.3294 | 7983.5689 | 7969.9156 |
| 2.0604 | 8099.8825 | 7929.0172 | 7914.8945 |
| 2.0714 | 8031.2478 | 7874.4900 | 7859.8734 |
| 2.0824 | 7950.8264 | 7819.9890 | 7804.8523 |
| 2.0934 | 7866.2616 | 7765.5161 | 7749.8312 |
| 2.1044 | 7879.1460 | 7711.0732 | 7694.8101 |
| 2.1154 | 7808.6254 | 7656.6627 | 7639.7890 |
| 2.1264 | 7752.2144 | 7602.2869 | 7584.7679 |
| 2.1374 | 7756.1711 | 7547.9486 | 7529.7468 |
| 2.1484 | 7887.0433 | 7493.6507 | 7474.7257 |
| 2.1594 | 7690.0914 | 7439.3963 | 7419.7046 |
| 2.1704 | 7558.0059 | 7385.1891 | 7364.6835 |
| 2.1814 | 7606.1091 | 7331.0328 | 7309.6624 |
| 2.1924 | 7644.6578 | 7276.8092 | 7254.6413 |
| 2.2034 | 7541.4867 | 7222.7098 | 7199.4388 |
| 2.2144 | 7574.9823 | 7168.5531 | 7144.2363 |
| 2.2254 | 7515.3412 | 7114.4677 | 7089.0339 |
| 2.2364 | 7507.3481 | 7060.4600 | 7033.8314 |
| 2.2474 | 7393.8879 | 7006.5375 | 6978.6290 |
| 2.2584 | 7348.2537 | 6952.7083 | 6923.4265 |
| 2.2694 | 7295.6696 | 6898.9816 | 6868.2241 |
| 2.2804 | 7291.2616 | 6845.3677 | 6813.0216 |
| 2.2914 | 7299.1200 | 6791.8781 | 6757.8192 |
| 2.3024 | 7394.4690 | 6738.5262 | 6702.6167 |
| 2.3134 | 7260.0403 | 6685.3268 | 6647.4143 |
| 2.3244 | 7134.9012 | 6632.2974 | 6592.2118 |
| 2.3354 | 7167.7434 | 6579.4576 | 6537.0094 |
| 2.3464 | 7225.5797 | 6526.8310 | 6481.8069 |
| 2.3574 | 7220.9105 | 6474.4452 | 6426.6045 |
| 2.3684 | 7149.0502 | 6422.3338 | 6371.4020 |
| 2.3794 | 7173.2851 | 6370.4110 | 6316.1996 |
| 2.3904 | 7031.8456 | 6318.9658 | 6260.8504 |
| 2.4014 | 6964.1681 | 6267.8310 | 6205.5012 |
| 2.4124 | 6983.2591 | 6217.2255 | 6150.1521 |
| 2.4234 | 6944.3953 | 6167.2721 | 6094.8029 |
| 2.4344 | 7007.0266 | 6118.1376 | 6039.4537 |
| 2.4454 | 6955.1563 | 6070.0478 | 5984.1046 |
| 2.4564 | 6870.8658 | 6023.3069 | 5928.7554 |
| 2.4674 | 6874.6696 | 5978.3190 | 5873.4062 |
| 2.4784 | 6803.2891 | 5935.6110 | 5818.0570 |
| 2.4894 | 6804.2035 | 5895.8538 | 5762.7079 |
| 2.5004 | 6794.7080 | 5859.8783 | 5707.3587 |
| 2.5114 | 6728.5536 | 5828.6792 | 5652.0095 |
| 2.5224 | 6690.3348 | 5803.4040 | 5596.6604 |
| 2.5334 | 6610.8436 | 5785.3173 | 5541.3112 |
| 2.5444 | 6635.2827 | 5775.7394 | 5485.9620 |
| 2.5554 | 6565.7768 | 5775.9546 | 5430.6129 |
| 2.5664 | 6527.9838 | 5787.0911 | 5375.2637 |
| 2.5774 | 6512.9302 | 5809.9769 | 5319.9145 |
| 2.5884 | 6503.7257 | 5844.9758 | 5264.5654 |
| 2.5994 | 6423.0531 | 5891.8083 | 5209.2162 |
| 2.6104 | 6503.3855 | 5949.3542 | 5153.8670 |
| 2.6214 | 6408.1327 | 6015.4264 | 5098.5179 |
| 2.6324 | 6349.2094 | 6086.5051 | 5043.1687 |
| 2.6434 | 6420.2979 | 6157.4516 | 4987.8195 |
| 2.6544 | 6331.6976 | 6221.3047 | 4932.4704 |
| 2.6654 | 6241.5398 | 6269.4108 | 4877.1212 |
| 2.6764 | 6060.0541 | 6292.2442 | 4821.7720 |
| 2.6874 | 6072.8220 | 6281.1307 | 4766.4229 |
| 2.6984 | 6022.7611 | 6230.5197 | 4711.0737 |
| 2.7094 | 5962.6686 | 6139.7728 | 4655.7245 |
| 2.7204 | 5879.2984 | 6013.3934 | 4600.3754 |
| 2.7314 | 5754.7315 | 5859.5412 | 4545.0262 |
| 2.7424 | 5451.6568 | 5687.7513 | 4489.6770 |
| 2.7534 | 5330.1514 | 5506.8778 | 4434.3278 |
| 2.7644 | 5252.6976 | 5324.5504 | 4378.8320 |
| 2.7754 | 5126.5703 | 5146.0836 | 4323.3361 |
| 2.7864 | 5057.3854 | 4975.4714 | 4267.8402 |
| 2.7974 | 4858.8495 | 4815.1804 | 4212.3443 |
| 2.8084 | 4795.4184 | 4666.5532 | 4156.8484 |
| 2.8194 | 4542.6961 | 4530.0432 | 4101.3525 |
| 2.8304 | 4444.2537 | 4405.4172 | 4045.8567 |
| 2.8414 | 4421.1858 | 4292.4305 | 3990.3608 |
| 2.8524 | 4061.3102 | 4189.8405 | 3934.8649 |
| 2.8634 | 4068.8024 | 4095.5435 | 3879.3690 |
| 2.8744 | 3897.1632 | 4008.4590 | 3823.8731 |
| 2.8854 | 3823.1701 | 3927.5812 | 3768.3772 |
| 2.8964 | 3798.1062 | 3851.7313 | 3712.8814 |
| 2.9074 | 3732.4258 | 3779.8770 | 3657.3855 |
| 2.9184 | 3657.2384 | 3711.1496 | 3601.8896 |
| 2.9294 | 3524.0384 | 3644.8424 | 3546.3937 |
| 2.9404 | 3548.4680 | 3603.1836 | 3490.8978 |
| 2.9514 | 3403.5821 | 3543.5764 | 3461.5951 |
| 2.9624 | 3308.7316 | 3507.8624 | 3432.2924 |
| 2.9734 | 3233.0216 | 3473.0131 | 3402.9897 |
| 2.9844 | 3182.6342 | 3438.8497 | 3373.6870 |
| 2.9954 | 3229.8849 | 3405.2406 | 3344.3843 |
| 3.0064 | 3174.3840 | 3372.0883 | 3315.0816 |
| 3.0174 | 3217.0698 | 3339.3195 | 3285.7789 |
| 3.0284 | 3273.4130 | 3306.8781 | 3256.4762 |
| 3.0394 | 3203.4749 | 3274.7201 | 3227.1735 |
| 3.0504 | 3143.0201 | 3242.8105 | 3197.8708 |
| 3.0614 | 3034.8348 | 3211.1201 | 3168.5680 |
| 3.0724 | 3088.7379 | 3179.6250 | 3139.2653 |
| 3.0834 | 3038.5880 | 3148.3043 | 3109.9626 |
| 3.0944 | 3124.0044 | 3117.1403 | 3080.6599 |
| 3.1054 | 3035.4021 | 3086.1176 | 3051.3572 |
| 3.1164 | 2957.2070 | 3055.2226 | 3022.0545 |
| 3.1274 | 2969.1180 | 3035.4602 | 2992.7518 |
| 3.1384 | 3011.3525 | 3006.4331 | 2976.1131 |
| 3.1494 | 3033.0600 | 2988.5186 | 2959.4743 |
| 3.1604 | 2966.7168 | 2970.6916 | 2942.8356 |
| 3.1714 | 2976.4916 | 2952.9444 | 2926.1969 |
| 3.1824 | 2940.2306 | 2935.2703 | 2909.5581 |
| 3.1934 | 2877.4159 | 2917.6635 | 2892.9194 |
| 3.2044 | 2842.9587 | 2900.1184 | 2876.2807 |
| 3.2154 | 2883.5654 | 2882.6301 | 2859.6419 |
| 3.2264 | 2800.4086 | 2865.1944 | 2843.0032 |
| 3.2374 | 2854.6745 | 2847.8072 | 2826.3645 |
| 3.2484 | 2834.7222 | 2830.4648 | 2809.7257 |
| 3.2594 | 2849.2242 | 2813.1641 | 2793.0870 |
| 3.2704 | 2872.8633 | 2795.9021 | 2776.4483 |
| 3.2814 | 2757.7729 | 2778.6759 | 2759.8095 |
| 3.2924 | 2778.5044 | 2761.4833 | 2743.1708 |
| 3.3034 | 2728.5083 | 2744.3218 | 2726.5321 |
| 3.3144 | 2680.9681 | 2734.9255 | 2709.8933 |
| 3.3254 | 2706.3245 | 2718.9770 | 2702.1472 |
| 3.3364 | 2725.1037 | 2710.7900 | 2694.4010 |
| 3.3474 | 2729.0118 | 2702.6269 | 2686.6548 |
| 3.3584 | 2711.3702 | 2694.4862 | 2678.9086 |
| 3.3694 | 2738.4936 | 2686.3667 | 2671.1624 |
| 3.3804 | 2670.3785 | 2678.2670 | 2663.4163 |
| 3.3914 | 2585.4513 | 2670.1860 | 2655.6701 |
| 3.4024 | 2640.5354 | 2662.1227 | 2647.9239 |
| 3.4134 | 2657.6303 | 2654.0760 | 2640.1777 |
| 3.4244 | 2610.4793 | 2646.0452 | 2632.4316 |
| 3.4354 | 2647.7945 | 2638.0292 | 2624.6854 |
| 3.4464 | 2732.3697 | 2630.0274 | 2616.9392 |
| 3.4574 | 2664.2802 | 2622.0390 | 2609.1930 |
| 3.4684 | 2589.1322 | 2614.0634 | 2601.4468 |
| 3.4794 | 2572.2360 | 2606.0999 | 2593.7007 |
| 3.4904 | 2622.7213 | 2598.1479 | 2585.9545 |
| 3.5014 | 2639.5831 | 2590.2070 | 2578.2083 |
| 3.5124 | 2586.8127 | 2582.2767 | 2570.4621 |
| 3.5234 | 2635.3127 | 2574.3564 | 2562.7159 |
| 3.5344 | 2574.6091 | 2567.0591 | 2554.9698 |
| 3.5454 | 2495.1966 | 2559.4831 | 2547.2236 |
| 3.5564 | 2594.0871 | 2551.9124 | 2539.4774 |
| 3.5674 | 2601.7148 | 2544.2051 | 2531.7312 |
| 3.5784 | 2538.4818 | 2536.3479 | 2523.9851 |
| 3.5894 | 2564.3451 | 2528.4990 | 2516.2389 |
| 3.6004 | 2494.8687 | 2520.6581 | 2508.4927 |
| 3.6114 | 2478.3560 | 2512.8249 | 2500.7465 |
| 3.6224 | 2525.1800 | 2504.9993 | 2493.0003 |
| 3.6334 | 2558.1151 | 2497.1810 | 2485.2542 |
| 3.6444 | 2547.2040 | 2489.3698 | 2477.5080 |
| 3.6554 | 2448.6666 | 2481.5655 | 2469.7618 |
| 3.6664 | 2424.1524 | 2473.7681 | 2462.0156 |
| 3.6774 | 2442.1013 | 2465.9772 | 2454.2695 |
| 3.6884 | 2442.3584 | 2461.0027 | 2446.5233 |
| 3.6994 | 2492.8909 | 2453.6448 | 2442.0070 |
| 3.7104 | 2428.4012 | 2449.1030 | 2437.4907 |
| 3.7214 | 2449.4395 | 2444.5674 | 2432.9745 |
| 3.7324 | 2460.3673 | 2440.0379 | 2428.4582 |
| 3.7434 | 2404.4808 | 2435.5144 | 2423.9419 |
| 3.7544 | 2497.3820 | 2430.9969 | 2419.4257 |
| 3.7654 | 2423.7079 | 2426.4853 | 2414.9094 |
| 3.7764 | 2520.8437 | 2421.9796 | 2410.3931 |
| 3.7874 | 2494.2566 | 2417.4797 | 2405.8768 |
| 3.7984 | 2451.1755 | 2412.9856 | 2401.3606 |
| 3.8094 | 2501.0403 | 2408.4974 | 2396.8443 |
| 3.8204 | 2441.4204 | 2404.0150 | 2392.3280 |
| 3.8314 | 2454.8309 | 2399.5384 | 2387.8118 |
| 3.8424 | 2426.0005 | 2395.0676 | 2383.2955 |
| 3.8534 | 2412.7375 | 2390.6028 | 2378.7792 |
| 3.8644 | 2473.9759 | 2386.1438 | 2374.2629 |
| 3.8754 | 2380.8731 | 2381.5638 | 2369.7467 |
| 3.8864 | 2302.7567 | 2377.0979 | 2365.0843 |
| 3.8974 | 2432.7719 | 2372.5110 | 2360.4220 |
| 3.9084 | 2422.5344 | 2367.9303 | 2355.7597 |
| 3.9194 | 2374.9528 | 2363.3559 | 2351.0974 |
| 3.9304 | 2449.0374 | 2358.7879 | 2346.4351 |
| 3.9414 | 2477.1239 | 2354.2263 | 2341.7727 |
| 3.9524 | 2448.5796 | 2349.6714 | 2337.1104 |
| 3.9634 | 2451.8682 | 2345.1233 | 2332.4481 |
| 3.9744 | 2439.8029 | 2340.5820 | 2327.7858 |
| 3.9854 | 2473.4071 | 2336.0478 | 2323.1235 |
| 3.9964 | 2498.5192 | 2331.5209 | 2318.4611 |
| 4.0074 | 2443.9430 | 2327.0014 | 2313.7988 |
| 4.0184 | 2439.6859 | 2322.4896 | 2309.1365 |
| 4.0294 | 2486.6912 | 2317.9856 | 2304.4742 |
| 4.0404 | 2454.7168 | 2313.4897 | 2299.8118 |
| 4.0514 | 2504.9970 | 2309.0022 | 2295.1495 |
| 4.0624 | 2499.1047 | 2304.3878 | 2290.4872 |
| 4.0734 | 2474.9390 | 2299.8976 | 2285.6692 |
| 4.0844 | 2448.2876 | 2295.2811 | 2280.8512 |
| 4.0954 | 2504.3884 | 2290.6742 | 2276.0331 |
| 4.1064 | 2479.5511 | 2286.0772 | 2271.2151 |
| 4.1174 | 2389.0029 | 2281.4905 | 2266.3971 |
| 4.1284 | 2436.6417 | 2276.9145 | 2261.5790 |
| 4.1394 | 2535.5418 | 2272.3496 | 2256.7610 |
| 4.1504 | 2507.7168 | 2267.7963 | 2251.9430 |
| 4.1614 | 2476.1829 | 2263.2550 | 2247.1250 |
| 4.1724 | 2443.8825 | 2258.7264 | 2242.3069 |
| 4.1834 | 2422.9027 | 2254.2109 | 2237.4889 |
| 4.1944 | 2446.2827 | 2249.7092 | 2232.6709 |

Scan List

| Vis. | Dataset Name | Start pos. [°2θ] | End pos. [°2θ] | Step [°2θ] | Meas.Date/Time |
| --- | --- | --- | --- | --- | --- |
| * | 19 Etosha22 SSsub 0.5-5cm glycol | 2.0054 | 29.9894 | 0.0110 | 12/13/2023 9:09:00 AM |

Peak List

| Pos. [°2θ] | Height [cts] | FWHM Left [°2θ] | d-spacing [Å] | Rel. Int. [%] |
| --- | --- | --- | --- | --- |
| 2.6920 | 1363.14 | 0.1732 | 32.79311 | 100.00 |
| 5.0081 | 1120.04 | 0.2165 | 17.63107 | 82.17 |
| 5.2696 | 990.26 | 0.1732 | 16.75655 | 72.65 |
| 7.0266 | 1159.49 | 0.2381 | 12.57016 | 85.06 |
| 8.7415 | 513.95 | 0.0649 | 10.10753 | 37.70 |
| 15.7039 | 862.37 | 0.0974 | 5.63852 | 63.26 |
| 17.6253 | 47.44 | 0.2598 | 5.02793 | 3.48 |
| 18.1767 | 157.57 | 0.0866 | 4.87664 | 11.56 |
| 19.6622 | 92.85 | 0.5196 | 4.51141 | 6.81 |
| 21.0362 | 24.56 | 0.5196 | 4.21975 | 1.80 |
| 25.8735 | 979.51 | 0.0758 | 3.44074 | 71.86 |
| 26.6745 | 244.34 | 0.1732 | 3.33922 | 17.92 |
| 27.4933 | 80.83 | 0.1732 | 3.24160 | 5.93 |

Pattern List

| Visible | Ref.Code | Score | Compound Name | Chem. Formula | Mineral Name | SemiQuant[%] |
| --- | --- | --- | --- | --- | --- | --- |
| * | 04-008-2359 | 53 | Silicon Oxide | Si O2 | Quartz | 6 |
| * | 01-076-8347 | 52 | Potassium Sodium Magnesium Manganese Zinc Aluminum Iron Titanium Fluoride Aluminum Iron Silicate Hydroxide | ( K0.98 Na0.01 ) ( Fe0.61 Mg0.16 Mn0.04 Zn0.02 ) ( Fe0.38 Al0.335 Mg0.21 Ti0.075 )2 ( ( Si2.72 Al1.15 Fe0.13 ) O10.32 ) ( O H )1.57 F0.11 | Biotite-1M | 21 |
| * | 04-024-8347 | 33 | Potassium Sodium Calcium Aluminum Silicon Oxide Hydrate | K0.19 Na7.69 Ca0.06 Al8 Si16 O48 ( H2 O )8 | Analcime | 19 |
| * | 01-075-8323 | 18 | Magnesium Silicate Hydroxide Hydrate | Mg8 ( Si12 O30 ( O H )4 ) ( H2 O )11.82 | Sepiolite | 4 |
| * | 04-016-0693 | 51 | Potassium Sodium Calcium Manganese Aluminum Iron Silicon Oxide Hydroxide Hydrate | K0.3 Na0.4 Ca0.3 Mn3.9 Fe0.1 Al1.4 Si5.3 O16 ( O H )2.7 ( H2 O )3.5 | Ganophyllite | 13 |
| * | 04-025-4215 | 33 | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide | Mg10.4 V0.36 Mn33.5 Fe0.14 Al0.69 Si6.77 As6.5 P0.3 O54 ( O H )42 | Carlfrancisite | 37 |

Anchor Scan Parameters

Dataset Name	19 Etosha22 SSsub 0.5-5cm glycol

File name	C:\aeris_data\XRD data\Goldstein\Etosha 2023\Etosha Clay Data\Sample 19\19 Etosha22 SSsub 0.5-5cm glycol.xrdml

Sample Identification	19 Etosha22 SSsub 0.5-5cm S4

Measurement Start Date/Time	12/13/2023 9:09:00 AM

Operator	Instrument

Raw Data Origin	XRD measurement (*.XRDML)

Scan Axis	Gonio

Start Position [°2θ]	2.0054

End Position [°2θ]	29.9894

Step Size [°2θ]	0.0110

Scan Step Time [s]	48.1950

Scan Type	Continuous

PSD Mode	Scanning

PSD Length [°2θ]	5.54

Offset [°2θ]	0.0000

Divergence Slit Type	Fixed

Divergence Slit Size [°]	0.0603

Specimen Length [mm]	10.00

Measurement Temperature [°C]	25.00

Anode Material	Cu

K-α1 [Å]	1.54060

K-α2 [Å]	1.54443

K-β1 [Å]	1.39225

K-A2 / K-A1 Ratio	0.50000

Generator Settings	15 mA, 40 kV

Diffractometer Type	2082464

Diffractometer Number	0

Goniometer Radius [mm]	145.00

Dist. Focus-Diverg. Slit [mm]	95.00

Incident Beam Monochromator	No

Spinning	Yes